Supplementary Information for

Non-template hydrothermal route derived mesoporous Ce0.2Zr0.8O2 nanosized powders with blue-shifted UV absorption and high CO conversion activity

Rui Si,a Ya-Wen Zhang,*a Chao-Xian Xiao,b Shi-Jie Li,b Bing-Xiong Lin,b Yuan Kou,b and Chun-Hua Yan*a

aState Key Lab of Rare Earth Materials Chemistry and Applications & PKU-HKU Joint Lab on Rare Earth Materials and Bioinorganic Chemistry, Peking University, Beijing 100871, China

##### bCollege of Chemistry and Molecular Engineering, Peking University, Beijing 100871, China

Table 1S. Elementary analysis of N, C, H contents and total weight loss (Δm) of the as-prepared CZ samples.

|  | N (wt%) | C (wt%) | H (wt%) | Δm (wt%) |
| --- | --- | --- | --- | --- |
| CZ14 | 0.49 | 1.31 | 2.13 | 21 |
| CZ16 | 0.30 | 1.25 | 1.79 | 12 |

# Text boxes

Fig. 1S	FT-IR spectra of the as-prepared CZ16 powder. ((OH) of water, 3396 cm-1; ((OH) of water and ethanol, 1634 and 1531 cm-1; ((NO) of uncoordinated NO3(, 1365, 1080 and 841 cm-1.

Fig. 2S	TG-DTA curves of the as-prepared CZ16 powder.