Table s1 Comparison of the structural parameters calculated by LDA and vdWs.

|  | Without vdWs interaction | With vdWs interaction |
| --- | --- | --- |
| Lattice parameter a (Å) Lattice parameter c (Å) | 3.194 12.474 | 3.201 12.394 |
| S-Mo bond length (Å) Se-W bond length (Å) | 2.401 2.501 | 2.401 2.501 |
| Bond angle θ (S1-Mo-S2) Bond angle θ (Se1-W-Se2) | 79.645 85.014 | 79.358 84.729 |

Figure s1 Comparison of the band offset calculated by (a) LDA and (b) vdWs.

Figure s2 Comparison of the band structure calculated by (a) LDA and (b) vdWs.

Figure s3 Partial density of state (PDOS) of MoS2/WSe2 superlattice (SL). Black, red, green and blue lines are the PDOS of S, Mo, Se, and W atoms, respectively.

Figure s4 Band structures of (a) MoS2/2WSe2, (b) MoS2/4WSe2, and (c) MoS2/6WSe2 SLs. 2, 4 and 6 mean the number of the WSe2 layers in these SLs, and MoS2 is monolayer. The Fermi energy is set to 0 eV.

Figure s5 The band structure of the SLs whose in-plane lattice parameters was set to the value of the free standing MoS2.

Figure s6 Local density of state (LDOS) of MoS2/WSe2 SLs under mechanical strains. Black and red lines correspond to the LDOS of MoS2 and WSe2 layers, respectively.

Figure s7 Local density of state (LDOS) of MoS2/WSe2 SL. Black and red lines correspond to the PDOS of MoS2 and WSe2 layers, respectively.