## Slide 1
In situ X-ray Spatial Profiling Reveals Uneven Compression of Electrode Assemblies and Steep Lateral Gradients in Lithium-ion Coin Cells
John Okasinski, 1 Ilya A. Shkrob, 2 Andrew Chuang, 1 Marco-Tulio Fonseca Rodrigues, 2 Abhi Raj, 2,3 Dennis W. Dees, 2 and Daniel P. Abraham* 2
1 X-ray Sciences Division, Argonne National Laboratory, Lemont, Illinois 60439, USA
2 Chemical Sciences and Engineering Division, Argonne National Laboratory, Lemont, Illinois, 60439, USA
3 Department of Electrical Engineering, Princeton University, Princeton, New Jersey 08544, USA
* Corresponding author: E-mail: abraham@anl.gov
Supporting Information
To play the movies, press the triangle at the bottom of the panel. To inspect the movie frame by frame, used the slide rule at the bottom.

## Slide 2
Figure S1. The X-ray radiographs and schematic depictions of (a) cell-2 and (b) cell-8 in Table 1. In panel b, an annotated excerpt form the radiograph at the top is shown in more detail. The SS arbor shim at the bottom is 100 mm thick, and the aluminum spacer is 410 mm thick.

## Slide 3
Animated figure S2. Example of the background corrected EDXRD spectra in the d-space domain for scanning of charged cell-8 (Table 1). The y- and z-coordinates are given in the frame; the depth coordinate z=0 approximately corresponds to the midplane of the separator, while the radial coordinate y=0 corresponds to the center of the round cell. The increase in z corresponds to scanning from the graphite anode (at the top of the electrode assembly) towards the oxide cathode (at the bottom of the electrode assembly). The background corrected spectra were divided into several regions of interest that are color coded and annotated in the frames (see Table S3). The red is for the NMC cathode (only the strongest (300) peak was integrated, the (101) peak was used for the lattice indexing only); the green is for a polymer peak in the separator, the magenta is for LiC6, the cyan is for LiC12, and the brown is for copper in the anode current collector. This is the animated version of Figure 2 in the text.
copper
NMC
NMC
LiC6
LiC12
separator

## Slide 4
cathode
anode
top
bottom
separator gap
Animated figure S3. (Transverse z-scans of the oxide cathode (red circles) and the graphite anode (blue circles) in a fully discharged coin cell (cell-1 in Table 1). The cell included a spring loaded stainless steel spacer pressing on the cathode on the top and a stainless steel spacer pressing on the can at the bottom. The lateral position along the diameter is indicated in the top right corner. The solid lines are the gated polynomial fits convoluted with the X-ray beam profile: a function p(z) was given by a polynomial on an interval (z1,z2) and zero outside of this interval. This function was convoluted with the Gaussian z-profile of the X-ray beam in the material. The polynomial coefficients and the hard edges z1 and z2 where optimized for each scan, while the width of the X-ray beam was optimized globally. This is the animated version of Figure 3 in the text.

## Slide 5
graphite anode
oxide cathode
y=
(a)
Animated figure S4. Panel a: Transverse z-scans of integrated X-ray diffraction peaks from charged cell-8 (Table 1) shown schematically in panel b. The z increases from the top to the bottom and y is relative to the center of the cell. In panel a, the red line is for the oxide cathode, the dashed brown line is for the copper collector, the green line is for the ordered polymer lamellae in the separator; the cyan and magenta lines are for the LiC12 and LiC6 phases in the lithiated graphite cathode, respectively. The regions for integration are given in Table S3. The integrals were corrected and scaled as explained in the Experimental. The dashed black line gives the sum of the LiCx contributions. The integral follows both the active material distribution and its lithiation. Cell-8 provided the most uniform compression of the electrode assembly among the cells in Table 1.
separator gap
top
bottom
Cu

## Slide 6
y =
graphite anode
oxide cathode
(a)
electrode lithiation, x
Animated figure S5. Panel a: Transverse z-plots for lithiation in charged coin cell-1 (Table 1) with the standard electrode assembly (the cathode is on top) and the standard set of stainless steel spacers that is shown schematically in panel b. The z increases from the bottom to the top and y is the radial coordinate for a yz-scan across the diameter of this cell; y=0 is at the cell center. The lithiation was estimated from the X-ray peaks as explained in the Experimental. The cyan and magenta plots are for the LiC12 and LiC6 phases, respectively, and red is for the oxide. The dashed gray line is for the material distribution in the oxide. The two LiC6x phases are complementary to each other. The lithiation profiles at the center of the cell are steep, with the LiC6 phase prevalent near the separator, and the LiC12 phase prevalent near the current collector. This is the animated version of Figure 7 in the text.
separator gap
bottom
top

## Slide 7
Figure S6. Examples of lithiation rings on graphite anodes harvested from fast-charged coin cells. The cells were discharged before disassembly, and the anodes were extracted and photographed inside an argon filled glove box. The lithium (which is covered by the solid electrolyte interphase) forms gray deposits on the graphite surface. It is seen that the ring always forms a small distance away from the electrode edge. See Figure 10 panel c, in which our model also predicts the lithiation ring.

## Slide 8
Animated figure S7. (a) The z-average and standard deviation for lithiation in a model semi-infinite periodic cell (a solid solution model with 5-layer particles) plotted vs. the radial coordinate y. The distribution is obtained at the end of 6C charge as the cell voltage reached 4.5 V (at 92% average anode lithiation), assuming variable porosity in the separator ( = 0.4, 0.75). Panel b shows the lithiation maps and panel c shows the plating current in the anode. This is animated version of Figure 10 in the text. The running time is given in panel a. In panel a, observe that for the anode s initially points down near the edge, and only then points up; this explains the difference between Figures 8a and 8b in the text. In panel c, observe that at all times the lithium plating peaks at a radius outside of the flat top region, but not at the edge; i.e. the lithium begins to plate as a ring.
(a)
(b)
(c)
cathode
anode

## Slide 9
(a)
(b)
(c)
cathode
anode
Animated figure S8. Like Figure S7, for the triphasic, semi-infinite periodic model. The model cell was charged at a constant rate of 3C to 2.3 mAh/cm2 at which the cell voltage is 4.33 V. Note the scaling factor in panel b. Panels a and b show the average and the standard deviation for z-profiles for lithium concentration in the NMC oxide electrode, the graphite electrode, and for the three phases. Observe the change in the slope of the standard deviation near the edges during LiC6 to LiC12 phase transition in the electrode. Panel c shows the total lithiation map for the cathode and the anode (all thee phases together). The time is indicted in panel a, and y is the periodic lateral coordinate.

## Slide 10
(a) dilute LiCx
(b) LiC12
(c) LiC6
Animated figure S9. The same system as in Figure S8, with the lithiation of the three phases in the graphite anode shown as a false color map. The charge time is given in the upper right corner of the plot. As the time progresses, the phases succeed and replace each other. The LiC12 to LiC6 phase transition is trailing at the edge relative to the interior, which accounts for the progression of the averages and the standard deviations shown in Figure S7.
anode