Caption : fig. s1 environmental scanning electron microscopy images of the structures formed by to on the surface of a tomato leaf. a) surface of a tomato leaf sprayed with demineralised water and observed under high humidity (98.8%). b) surface of a tomato leaf sprayed with to and observed under high humidity (98.7%). inset: magnification of an epidermal cells showing the presence of a film on the corrugated surface, but absence of fractal objects). c) surface of a leaf sprayed with to and observed under reduced humidity (49.9%). the arrows indicate cracks in the formed film. d) cracks on the surface of a leaf sprayed with to and observed under 0% humidity. inset: film detaching from the leaf surface (arrow). estimated thickness: 100 nm. e) surface of a tomato leaf on which a drop of to was deposited and observed under 100% humidity at t=0. f) surface of a tomato leaf on which a drop of to was deposited and observed under high humidity (95.9%) at t=50 minutes. g) reference surface of a tomato leaf on which no drop was deposited (observation under 98.8% humidity). h) surface of a tomato leaf on which a drop of to was deposited and left to evaporate under greenhouse conditions; the presence of a film with some flakes is observed. inset: detail of the flakes formed on the treated surface. observations under 98.8% humidity. i) film forming on the flat surface of a wax tablet previously chilled at 4 °c, after deposition of to (the white arrow indicates the underlying original surface; observations under 98.7% humidity). j) details of the thin to film showing fractal dendrites on the flat surface of the wax tablet (observations under 99% humidity).