Electronic Supplementary Information

Critical Size of Surface Heat Capacities of Nano-CdS: Theoretical and Experimental Studies

Shengjiang Zhang‡a, Xiuniang Tan‡a, Yan Zhoua, Jinyang Liua, Xiangyao Lianga, Xuehuan Dinga, Guangmiao Lyua, Ying Weia, Junxin Chena, Yidan Maoa, Jinmei Wua, Yushan Huanga, Yusen Huanga, Xuecai Tan*a,b,c, Zaiyin Huang*a,b,c

a School of Chemistry and Chemical Engineering, Guangxi University for Nationalities, Guangxi Colleges and Universities, Nanning 530008, P. R. China

b Key Laboratory of Food Safety and Pharmaceutical Analytical Chemistry, Key Laboratory of Forest Chemistry and Engineering, Nanning 530008, P. R. China

c Key Laboratory of Forest Chemistry and Engineering, Guangxi University for Nationalities, Nanning 530008, PR China

Derivation of Eqns (7) and (8)

When the amount of substance in each phase does not change under constant temperature and pressure, the molar surface Gibbs free energy can be expressed as1:

(1)

For approximately spherical nanoparticles without inner holes, the total surface area can be expressed as:

(2)

In Eqn (2), the superscript s denotes surface phase, the subscript m denotes molar, ,  and  denote the surface tension, radius of nanoparticle, and the number of nanoparticles, respectively.

(1) For a simple physical change process where the particle size of nanoparticles do not change, however, the number of particles change, such as adsorption process of nanoparticles, the partial molar surface Gibbs free energy (surface chemical potential) is equal to the molar surface Gibbs free energy2. The proof is as follows:

(3)

Differentiate Eqn (3), we can get:

(4)

The total amount of matter of nanoparticles can be expressed as:

(5)

Differentiate Eqn (5), we can get:

(6)

Eqn (4) is divided by Eqn (6), the partial molar surface Gibbs free energy of nanoparticles can be obtained as:

(7)

In Eqn (7), the superscript s represents surface phase, the subscript m represents molar, , , , , , , , anddenote Gibbs free energy, volume, molecular weight, density, particle radius, total amount of matter of nanoparticles, absolute temperature and pressure, respectively.

(2) However, for processes where the particle size of nanoparticle changes and the number of particles do not change, such as dissolution, the reaction and phase transition of nanoparticles, the partial molar surface Gibbs free energy is not equal to the molar surface Gibbs free energy3,4. The proof is as follows:

For approximately spherical nanoparticles without inner holes when the particle size changes, the Eqn (3) is differentiated to obtain:

(8)

When the particle size changes the Eqn (5) is differentiated to obtain:

(9)

The partial molar surface Gibbs free energy of nanoparticles can be obtained as Eqn (8) is divided by Eqn (9):

(10)

The proof of Eqns (7) and (8) in the manuscript is completed.

Table S1

Different reaction conditions for preparing supplementary particle sizes of nano-CdS

| No. |  | Temperature /°C | Time /h | Ethylene glycol /mL | PVPK-40 /g | D /nm |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.7:7 | 140 | 8 | 60 | 0.4 | 9.2 |
| 2 | 4:7 | 140 | 8 | 60 | 0.4 | 10.5 |
| 3 | 2:7 | 140 | 8 | 60 | 0.4 | 11.7 |

The reaction temperature and the reaction time for the preparation of nano-CdS were kept at 140 °C and 8 h, respectively. Nano-CdS samples of preparation conditions with supplementary particle sizes are shown in Table S1.

Table S2

Average particle size of nano-CdS

| No. | 2θ /deg | FWHM | /nm | /nm |
| --- | --- | --- | --- | --- |
| 1 | 26.800 | 1.083 | 7.5 | 7.2 |
|  | 43.880 | 0.997 | 8.5 |  |
|  | 51.960 | 1.451 | 6.0 |  |
| 2 | 26.640 | 0.903 | 9.0 | 8.1 |
|  | 43.920 | 0.848 | 9.6 |  |
|  | 51.960 | 1.451 | 5.8 |  |
| 3 | 26.560 | 0.354 | 22.8 | 15.1 |
|  | 43.840 | 0.792 | 10.7 |  |
|  | 52.12 | 0.742 | 11.8 |  |
| 4 | 26.680 | 0.394 | 20.5 | 16.9 |
|  | 43.920 | 0.465 | 18.3 |  |
|  | 52.040 | 0.731 | 11.9 |  |
| 5 | 26.520 | 0.349 | 23.1 | 18.6 |
|  | 43.880 | 0.436 | 18.7 |  |
|  | 52.040 | 0.596 | 14.0 |  |

XRD patterns of CdS with supplementary particle sizes

Fig. S1 XRD patterns of CdS with different particle sizes

TEM images of CdS with supplementary particle sizes

Fig. S2 TEM images of nano-CdS: (a) 9.2 nm, (b) 10.5 nm, (c) 11.7 nm.

Fig. S3 Particle size distribution statistical histogram of nano-CdS: (a) 9.2 nm, (b) 10.5 nm, (c) 11.7 nm.

Table S3

BET specific surface areas data of CdS

|  |  | BET surface area /m2∙g−1 |
| --- | --- | --- |
| 7.2 | 0.13889 | 114.2445 |
| 8.1 | 0.12346 | 83.6113 |
| 15.1 | 0.06623 | 32.0163 |
| 16.9 | 0.05917 | 28.0320 |
| 18.6 | 0.05376 | 24.8024 |
| bulk | →0 | 1.5812 |

Table S4

Conductivities of CdS with different particle sizes and different temperatures

|  |  | /(μS·cm−1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 288.15 K | 298.15 K | 308.15 K | 318.15 K | 328.15 K |
| 7.2 | 0.13889 | 5.60 | 6.30 | 6.90 | 8.31 | 9.67 |
| 8.1 | 0.12346 | 4.94 | 5.61 | 6.36 | 7.55 | 8.97 |
| 9.2 | 0.10870 | 4.65 | 5.20 | 6.07 | 7.18 | 8.54 |
| 10.5 | 0.09524 | 4.21 | 4.92 | 5.87 | 6.74 | 8.29 |
| 11.7 | 0.08547 | 4.03 | 4.39 | 5.27 | 6.05 | 7.58 |
| 15.1 | 0.06623 | 2.76 | 3.26 | 4.01 | 4.71 | 6.15 |
| 16.9 | 0.05917 | 2.38 | 2.93 | 3.53 | 4.15 | 5.62 |
| 18.6 | 0.05376 | 2.16 | 2.64 | 3.24 | 3.81 | 5.10 |
| bulk | →0 | 0.67 | 0.87 | 1.12 | 1.47 | 2.04 |

Table S5

Ionic strength of CdS with different particle sizes and different temperatures

|  |  | /(mol∙kg−1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 288.15 K | 298.15 K | 308.15 K | 318.15 K | 328.15 K |
| 7.2 | 0.13889 | 103.9273 | 116.7947 | 127.9368 | 154.2340 | 179.3955 |
| 8.1 | 0.12346 | 91.6412 | 104.0223 | 118.0405 | 140.1562 | 166.3820 |
| 9.2 | 0.10870 | 86.1801 | 96.4706 | 112.6320 | 133.2420 | 158.4670 |
| 10.5 | 0.09524 | 78.1199 | 91.2553 | 108.9340 | 125.1200 | 153.8560 |
| 11.7 | 0.08547 | 74.7254 | 81.4917 | 97.7477 | 112.2940 | 140.5840 |
| 15.1 | 0.06623 | 51.1956 | 60.4715 | 74.3432 | 87.4199 | 114.1546 |
| 16.9 | 0.05917 | 44.2451 | 54.3833 | 65.541 | 77.0773 | 104.2233 |
| 18.6 | 0.05376 | 39.9901 | 48.9082 | 60.1333 | 70.7246 | 94.7105 |
| bulk | →0 | 12.4959 | 16.0770 | 20.7095 | 27.1831 | 37.8868 |

Effect of surface tension and molar interfacial area

Fig. S4 Relationship between  and  at 288.15 K.

Fig. S4 is based on the nolinear curve fitted equation and substituted the value of reciprocal of particle size, which is via fitting the reciprocal of particle size and the logarithm of the standard dissolution equilibrium constant in Fig. 4 at 288.15 K. The values of particle size used in Fig. S4 are: 1.5, 2.3, 3.7, 5.2, 6.3, 7.2, 8.1, 9.2, 10.5, 11.7, 12.4, 13.6, 14.8, 15.1, 16.9, 18.6, 19.3, 25.0, 42.6, 52.4, 65.5, 72.2, 83.3 and 90.5 nm.

Fig. S4 shows that when the particle size is ≥ 10 nm, the relationship between  and  is linear, and the  of bulk-CdS can be obtained when the linear relationship is extrapolated to  tends to 0. When the particle size is < 10 nm, the curved deviates from the linear relationship because the surface tension is no longer a constant5-7.

The effects of  and  denote the effects of surface tension and molar interfacial area, respectively8-10. The effect of surface tension is defined as the deviation between the physical quantity (or the logarithm of physical quantity) of nanomaterials and the linear part due to the change of surface tension (or temperature coefficient of surface tension). The effect of molar interfacial area is defined as the variation between a physical quantity (or the logarithm of physical quantity) of nanomaterials and the same physical quantity (or the same logarithm of physical quantity) of corresponding bulk materials due to decrease in molar interfacial area.

Error analysis

Table S6

Surface tension obtained by experiments and using Eqn (32)

|  |  | 288.15 K | 298.15 K | 308.15 K | 318.15 K | 328.15 K |
| --- | --- | --- | --- | --- | --- | --- |
| 7.2 | 0.13889 | 0.9145 | 0.8854 | 0.8406 | 0.8270 | 0.7637 |
| 8.1 | 0.12346 | 1.1752 | 1.1390 | 1.0977 | 1.0676 | 0.9927 |
| 15.1 | 0.06623 | 2.1677 | 2.1063 | 2.1022 | 1.9816 | 1.9289 |
| 16.9 | 0.05917 | 2.2185 | 2.2128 | 2.1637 | 2.0184 | 2.0212 |
| 18.6 | 0.05376 | 2.3068 | 2.2831 | 2.2631 | 2.0929 | 2.0673 |

Based on the original experiment, we prepared nano-CdS particles with three different sizes. The values of the reciprocal of particle size in the range 0.065–0.112 nm−1 are 9.2, 10.5 and 11.7 nm. Conductivity data of the novel prepared nano-CdS aqueous solutions at different temperatures are shown in Table S4. Fig. S7 shows the critical size distributions of the molar surface heat capacity and specific surface heat capacity of nano-CdS, which are in the range 0.065–0.112 nm−1.

The critical size numerical diagram of the molar surface heat capacity of nano-CdS after adding three novel particle sizes were derived through calculations. In addition, we have substituted the value of three novel reciprocal of particle size according to the curve fitted equation of specific surface enthalpy and particle size in Fig. 10 (c), which is obtained their specific surface enthalpy data. Finally, the specific surface heat capacity critical size numerical diagram of CdS in the range of 0.065–0.112 nm−1 is calculated by Eqn (35).

Fig. S5 After adding three particle sizes in the range 0.065–0.112 nm−1: (a) Molar surface heat capacity critical size numerical diagram of CdS, (b) specific surface heat capacity critical size numerical diagram of CdS.

Table S7

Values of specific surface enthalpy of nano-CdS

|  |  | /(J∙m−2) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 288.15 K | 298.15 K | 308.15 K | 318.15 K | 328.15 K |
| 7.2 | 0.13889 | 2.5471 | 2.2492 | 1.9608 | 1.6820 | 1.4127 |
| 8.1 | 0.12346 | 3.0729 | 2.7438 | 2.4266 | 2.1213 | 1.8280 |
| 9.2 | 0.10870 | 3.5363 | 3.2099 | 2.8838 | 2.5579 | 2.2321 |
| 10.5 | 0.09524 | 3.9583 | 3.6311 | 3.2931 | 2.9442 | 2.5845 |
| 11.7 | 0.08547 | 4.2572 | 3.9294 | 3.5805 | 3.2104 | 2.8192 |
| 15.1 | 0.06623 | 4.7944 | 4.4827 | 4.1086 | 3.6721 | 3.1732 |
| 16.9 | 0.05917 | 5.0618 | 4.7613 | 4.3232 | 3.9166 | 3.3602 |
| 18.6 | 0.05376 | 5.1619 | 4.8641 | 4.4158 | 4.0010 | 3.4219 |

References

1 W. J. Li, Y. Q. Xue, Z. X. Cui, Size dependence of surface thermodynamic properties of nanoparticles and its determination method by reaction rate constant, Physica B 495 (2016) 98-105.

2 Z. Zhang, Q.S. Fu, Y.Q. Xue, Z.X. Cui, S.S. Wang, Theoretical and experimental researches of size-dependent surface thermodynamic properties of nano-vaterite, J. Phys. Chem. C 120 (2016) 21652-21658.

3 L. Bai, Y. Q. Xue, Z. X. Cui, The size dependence of surface thermodynamic quantities of nano-Cu2(OH)2CO3: Theory and experimental research by thermal decomposition, Thermochim. Acta 658 (2017) 101-109.

4 E.R. Cohen, T. Cvitas, J.G. Frey, B. Holmstrom, K. Kuchitsu, R. Marquardt, I. Mills,F. Pavese, M. Quack, J. Stohner, H. Strauss, M. Takami, A.J. Thor, Chemistry International-Newsmagazine for IUPAC, third ed., 2007.

5 H. J. Duan, Z. X. Cui, Y. Q. Xue, Q. S. Fu, X. H. Chen, R. Zhang, Determination method and size dependence of interfacial tension between nanoparticles and a solution, Langmuir, 2018, 34, 8792-8797.

6 N. Y. Sdobnyakov, V. M. Samsonov, On the size dependence of surface tension in the temperature range from melting point to critical point, Cent. Eur. J. Phys., 2005, 3, 247-257.

7 Z. X. Cui, J. Zhang, Y. Q. Xue, H. J. Duan, Size-dependent thermodynamics and kinetics of adsorption on nanoparticles: a theoretical and experimental study, Langmuir, 2018, 34, 3197-3206.

8 W. J. Li, Y. Q. Xue, Z. X. Cui, Size dependence of surface thermodynamic properties of nanoparticles and its determination method by reaction rate constant, Physica B. 2016, 495, 98-105.

9 H. J. Duan, Z. H. Cheng, Y. Q. Xue, J. Z. Zhao, M. H. Yang, Z. X. Cui, W. M. Gao, S. Y. Wang, Influences of nano-effect on the thermodynamic properties of solid-liquid interfaces: theoretical and experimental researches, Cryst Eng Comm, 2021, 23, 6541-6550.

10 M. Y. Wang, Z. X. Cui, Y. Q. Xue, Determination of interfacial tension of nanomaterials and the effect of particle size on interfacial tension, Langmuir, 2021, 37, 14463-14471.