A Cu(Ⅱ) MOF with laccase-like activity for colorimetric detection of 2,4-dichlorophenol and p-nitrophenol

Baoru Wang, Peng Liu*, Yixiao Hu, Haili Zhao, Liyan Zheng* and Qiue Cao*

School of Chemical Science and Technology, Yunnan University, No. 2 North Cuihu Road, Kunming, 650091, PR China.

* Corresponding author, Email address: pliu@ynu.edu.cn；zhengliyan@ynu.edu.cn; qecao@ynu.edu.cn.

Fig. S1 Synthesis of 5-sulfomethyl isophthalic acid (5-SMIPA).

Compound A (5-methyl isophthalate): H2SO4 (4 mL) was slowly added to solution of 5-methylisophthalic acid (1.08 g, 6 mmol) in CH3OH (20 mL) and resulting mixture stirred at 75 °C for 12 h. When the reaction was end and cooled to room temperature, 10 M NaOH (aq) was added to neutralize the solution. Compound A was extracted by CH2Cl2 (150 mL) and the CH2Cl2 was removed by rotary evaporation to obtain compound A (1.17 g, 94.1%). NMR spectrum was shown in Fig. S2 and Fig. S3.

1H NMR (400 MHz, Chloroform-d) δ 8.48 (s, 1H), 8.04 (s, 2H), 3.94 (s, 6H), 2.45 (s, 3H).

13C NMR (400 MHz, Chloroform-d) δ 166.40, 138.67, 134.39, 130.47, 127.94, 52.27, 21.10.

Compound B (5-bromomethyl isophthalate): Compound A (0.832 g, 4 mmol) and NBS (0.783 g, 4 mmol) were dissolved in anhydrous CH3CN (20 mL), then added the CH3CN solution of BPO (0.09 g, 0.4 mmol). The mixture heated under reflux under N2 and stirred for 6 h. After 6 h quenched BPO with water, and removed solvent. The residue was purified by flash chromatography (EtOAc : petroleum ether, 1:20) to obtain compound B(0.75 g, 65.7%). NMR spectrum was shown in Fig. S4 and Fig. S5.

1H NMR (400 MHz, Chloroform-d) δ 8.60 (s, 1H), 8.26 (s, 2H), 4.55 (s, 2H), 3.96 (s, 6H).

13C NMR (400 MHz, Chloroform-d) δ165.55, 138.83, 134.18, 131.29, 130.51, 52.52, 31.50.

Compound C (5-sulfomethyl isophthalate): Added compound B (0.28 g, 1 mmol), Na2SO3 (0.15 g, 1.2 mmol), TBAB (0.008g, 0.025 mmol) to a mixture of H2O and ethanol and stirred for 12 h. The solvent was evaporated to obtain a mixed solid.

Compound D (5-sulfomethyl isophthalic acid, 5-SMIPA): Added mixed solid, NaOH (0.64 g, 16 mmol) to water and stirred at 85 °C for 3 days. Then added HCl to adjust pH to neutral conditions, the white solid precipitated was compound D (0.16 g). NMR spectrum was shown in Fig. S6 and Fig. S7.

1H NMR (600 MHz, MeOD), 𝛿 (TMS, ppm) 8.50 (1H, s), 8.07 (2H, s), 4,13 (2H, s).

13C NMR (600 MHz, MeOD), 𝛿 (TMS, ppm) δ 173.82, 137.56, 132.76, 132.17, 128.92, 56.94.

Fig. S2. 1H NMR (400 MHz, Chloroform-d) spectrum of 5-methyl isophthalate.

Fig. S3. 13C NMR (400 MHz, Chloroform-d) spectrum of 5-methyl isophthalate.

Fig. S4. 1H NMR (400 MHz, Chloroform-d) spectrum of 5-bromomethyl isophthalate.

Fig. S5. 13C NMR (400 MHz, Chloroform-d) spectrum of 5-bromomethyl isophthalate.

Fig. S6. 1H NMR (600 MHz, MeOD) spectrum of 5-sulfomethyl isophthalic acid (5-SMIPA).

Fig. S7. 13C NMR (600 MHz, MeOD) spectrum of 5-sulfomethyl isophthalic acid (5-SMIPA).

Fig. S8. (A) Crystal packing pattern along the b axis. (B) Crystal packing pattern along the a axis. (C) Specific coordination environment of Cu.

Fig. S9. (A) FTIR spectra of Cu-SM MOF and 5-SMIPA. (B) FTIR spectra of HKUST-1 and 1,3,5-benzenetricarboxylic acid. (C) N2 adsorption isotherm of the Cu-SM MOF after drying to measure the specific surface area. (D) N2 adsorption isotherm of the HKUST-1 after drying to measure the specific surface area.

Fig. S10. (A) XPS spectra of Cu-SM MOF. High-resolution (B) Cu 2p, (C) O 1s, (D) N 1s, (E) S 2p, (F) C 1s.

Fig. S11. (A) XPS spectra of HKUST-1. High-resolution (B) Cu 2p, (C) O 1s, (D) C 1s.

Fig. S12. TGA curves of Cu-SM MOF (red curve) and HKUST-1 (black curve).

Fig. S13. SEM images of (A) Cu-SM MOF and (B) HKUST-1 after grinding.

Fig. S14. PXRD patterns of (A) Cu-SM MOF and (B) HKUST-1 after grinding.

Fig. S15. Catalytic efficiency of (A) Cu-SM MOF and (B) HKUST-1 during the recycling experiment up to the 5th cycle. PXRD patterns of (C) Cu-SM MOF and (D) HKUST-1 during the recycling experiment up to the 5th cycle.

Fig. S16. Plot of absorbance at 510 nm obtained from the time-dependent kinetic data at various concentrations of 2,4-DP, (A) Cu-SM MOF, (B) HKUST-1. Lineweaver-Burk plot of (C) Cu-SM MOF, (D) HKUST-1.

Fig. S17. (A) Structure of a variety of phenolic compounds. (B) Structure of three nitrophenols. (C) Oxidation of three nitrophenols catalyzed by Cu-SM MOF.

Fig. S18. (A) XPS spectra of Cu-SM MOF incubated with 2,4-DP. High-resolution (B) Cu 2p, (C) O 1s, (D) N 1s, (E) S 2p, (F) Cl 2p, (G) C 1s.

Fig. S19. (A) XPS spectra of HKUST-1 incubated with 2,4-DP. High-resolution (B) Cu 2p, (C) O 1s, (D) C 1s, (E) Cl 2p.

Fig. S20. (A) XPS spectra of Cu-SM MOF incubated with p-nitrophenol. High-resolution (B) Cu 2p, (C) O 1s, (D) N 1s, (E) S 2p, (F) C 1s.

Fig. S21. FTIR spectrum of MOFs and that incubated with 2,4-DP. (A) Cu-SM MOF, (B) HKUST-1. PXRD patterns of MOFs and that incubated with 2,4-DP. (C) Cu-SM MOF, (D) HKUST-1.

Fig. S22. (A) FTIR spectrum and (B) PXRD patterns of Cu-SM MOF incubated with p-nitrophenol.

Table S1. Experimental details regarding the LOD calculation for detection of 2,4-DP and p-nitrophenol.

|  | σ | k | LOD=3σ/k |
| --- | --- | --- | --- |
| 2,4-DP | 0.002109 | 0.01203 | 0.53 μM |
| p-nitrophenol | 0.004289 | 0.00796 | 1.62 μM |

σ: standard deviation of blank, k: calibration curve slope from the linear relationships (Fig. 6).

Table S2. Detection of 2,4-DP.

| Sample | Addition (μM) | Found (μM) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| River water | 20 | 20.75 | 103.75 | 1.0 |
|  | 50 | 50.62 | 101.24 | 0.8 |
|  | 80 | 81.82 | 102.27 | 4.4 |
| Lake water | 20 | 21.05 | 105.25 | 0.4 |
|  | 50 | 50.28 | 100.56 | 0.4 |
|  | 80 | 80.33 | 100.41 | 2.0 |
| Tap water | 20 | 20.78 | 103.90 | 0.8 |
|  | 50 | 51.21 | 102.42 | 1.3 |
|  | 80 | 81.64 | 102.05 | 0.3 |

Table S3. Detection of p-nitrophenol.

| Sample | Addition (μM) | Found (μM) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| River water | 50 | 48.93 | 97.86 | 0.8 |
|  | 100 | 99.58 | 99.58 | 1.4 |
|  | 200 | 195.57 | 97.78 | 2.9 |
| Lake water | 50 | 51.29 | 102.58 | 0.8 |
|  | 100 | 100.59 | 100.59 | 0.8 |
|  | 200 | 202.28 | 101.14 | 0.7 |
| Tap water | 50 | 48.98 | 97.96 | 0.9 |
|  | 100 | 100.88 | 100.88 | 0.1 |
|  | 200 | 210.16 | 105.08 | 4.1 |

Table S4. Crystal data and structure refinements for Cu-SM MOF.

| Compound | Cu-SM MOF |
| --- | --- |
| Formula | C11H13CuNO7S |
| M | 366.82 |
| Temperature (K) | 293 (2) |
| Crystal system | trigonal |
| Space group | R-3m |
| a, b, c (Å) | 18.733 (7) 18.733 (7) 28.218 (8) |
| α, β, γ (°) | 90 90 120 |
| V (Å3) | 8576 (7) |
| Z | 18 |
| Dc (g/cm3) | 1.279 |
| μ (mm−1) | 1.279 |
| F (000) | 3366.0 |
| Reflns collected | 24754 |
| Independent reflns | 2428 |
| R (int) | 0.1366 |
| Data / restraints / parameters | 2428/517/220 |
| GOF on F 2 | 1.052 |
| bR1[I>2σ (I )], wR2 | 0.0789, 0.2173 |
| R1[all data], wR2 | 0.1009, 0.2384 |

Table S5. Bond Lengths for Cu-SM MOF.

11-X,-Y,-Z; 21+Y-X,+Y,+Z; 3-Y+X,-Y,-Z; 4-1/3-Y+X,-2/3+X,1/3-Z; 5+X,-1+X-Y,+Z

| Atom | Atom | Length/Å |
| --- | --- | --- |
| Cu1 | Cu11 | 2.6250(17) |
| Cu1 | O12 | 1.955(4) |
| Cu1 | O1 | 1.956(4) |
| Cu1 | O23 | 1.943(4) |
| Cu1 | O21 | 1.943(4) |
| Cu1 | O54 | 2.161(6) |
| S1 | O5 | 1.441(6) |
| S1 | O3 | 1.620(13) |
| S1 | C6 | 1.758(9) |
| S1 | O4 | 1.354(10) |
| O1 | C1 | 1.255(6) |
| O2 | C1 | 1.265(6) |
| C2 | C3 | 1.383(6) |
| C2 | C1 | 1.485(7) |
| C2 | C4 | 1.385(7) |
| C5 | C4 | 1.386(6) |
| C5 | C45 | 1.386(6) |
| C5 | C6 | 1.488(11) |
| C10 | N2 | 1.458(10) |
| C9 | N2 | 1.459(10) |
| N5 | C15 | 1.444(10) |
| N5 | C16 | 1.454(10) |
| C13 | N4 | 1.447(10) |
| N4 | C14 | 1.445(10) |
| C7 | N1 | 1.447(10) |
| N1 | C8 | 1.448(10) |
| C12 | N3 | 1.4848(4) |
| C11 | N3 | 1.455(7) |

Table S6. Bond Angles for Cu-SM MOF.

11+Y-X,+Y,+Z; 21-X,-Y,-Z; 3-1/3-Y+X,-2/3+X,1/3-Z; 4-Y+X,-Y,-Z; 52/3+Y,1/3-X+Y,1/3-Z; 6+X,-1+X-Y,+Z

| Atom | Atom | Atom | Angle/° |  | Atom | Atom | Atom | Angle/° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O11 | Cu1 | Cu12 | 82.15(11) |  | C1 | O1 | Cu1 | 125.2(3) |
| O1 | Cu1 | Cu12 | 82.15(11) |  | C1 | O2 | Cu12 | 120.6(3) |
| O11 | Cu1 | O1 | 89.8(2) |  | S1 | O5 | Cu15 | 137.2(4) |
| O11 | Cu1 | O53 | 95.17(15) |  | C3 | C2 | C1 | 120.2(5) |
| O1 | Cu1 | O53 | 95.17(15) |  | C3 | C2 | C4 | 119.2(5) |
| O24 | Cu1 | Cu12 | 86.49(12) |  | C4 | C2 | C1 | 120.4(5) |
| O22 | Cu1 | Cu12 | 86.49(12) |  | C2 | C3 | C26 | 120.9(7) |
| O24 | Cu1 | O11 | 168.58(16) |  | C46 | C5 | C4 | 119.1(7) |
| O24 | Cu1 | O1 | 89.80(16) |  | C4 | C5 | C6 | 120.4(4) |
| O22 | Cu1 | O1 | 168.58(16) |  | C46 | C5 | C6 | 120.4(4) |
| O22 | Cu1 | O11 | 89.80(16) |  | O1 | C1 | O2 | 125.4(5) |
| O24 | Cu1 | O22 | 88.3(2) |  | O1 | C1 | C2 | 117.0(4) |
| O22 | Cu1 | O53 | 96.23(16) |  | O2 | C1 | C2 | 117.5(4) |
| O24 | Cu1 | O53 | 96.23(16) |  | C2 | C4 | C5 | 120.8(5) |
| O53 | Cu1 | Cu12 | 176.19(16) |  | C5 | C6 | S1 | 115.3(6) |
| O5 | S1 | O3 | 104.5(5) |  | C10 | N2 | C9 | 117.9(12) |
| O5 | S1 | C6 | 106.7(4) |  | C15 | N5 | C16 | 119.7(12) |
| O3 | S1 | C6 | 97.6(5) |  | C14 | N4 | C13 | 120.3(13) |
| O4 | S1 | O5 | 118.7(5) |  | C7 | N1 | C8 | 119.7(13) |
| O4 | S1 | O3 | 115.0(8) |  | C11 | N3 | C12 | 116.4(9) |
| O4 | S1 | C6 | 111.9(5) |  |  |  |  |  |