## Slide 1: Mechanisms and Models for Water Transport in Reverse Osmosis Membranes: History, Critical Assessment, and Recent Developments
Mohammad Heiranian, Hanqing Fan, Li Wang, Xinglin Lu, Menachem Elimelech
Department of Chemical and Environmental Engineering, Yale University
Chemical Society Reviews
Electronic Supplementary Information

## Slide 2: Historical Background
1740s
Discovery of osmosis by Nollet
1953
Reid suggested using RO for desalination (funded by Office of Saline Water of US Department of Interior)
Leob and Sourirajan developed high-permeability asymmetric CA membranes
1958
Sourirajan proposed a pore-based transport model
1959
1963
Kedem and Katchalsky developed a water transport model based on irreversible thermodynamics

## Slide 3: Historical Background
1964
Lonsdale et al suggested a solution-diffusion mechanism based on Fick’s law
1970
Paul and Ebra-Lima incorporated the pressure-induced water concentration gradient into the solution-diffusion framework
No solid proof and no explanation was given as how a water concentration gradient is induced
1969
Rosenbaum and Cotton showed the presence of water concentration gradient in stacked cellulose acetate films
The only experimental evidence in apparent support of a solution-diffusion mechanism
They had to assume an unphysical pressure profile
Biesheuvel, Elimelech, and coworkers suggested a solution-friction mechanism
Consistent with the Kedem-Katchalsky thermodynamic framework
2020

## Slide 4: Pore-Flow and Solution-Diffusion Models
Pore-Flow Model:
Driven by pressure gradient
Described by Darcy’s law:
, flux of water
, permeability coefficient
, feed pressure
, permeate pressure
, length

## Slide 5: Pore-Flow and Solution-Diffusion Models
Pore-Flow Model:
Driven by pressure gradient
Solution-Diffusion Model:
Described by Darcy’s law
, flux of water
, permeability coefficient
, feed pressure
, permeate pressure
, length
Driven by water concentration gradient
Described by Fick’s law of diffusion:
, diffusion coefficient
, feed concentration
, permeate conc.

## Slide 6: Solution-Diffusion Model
How does a pressure difference induce a concentration gradient?
Paul and Ebra-Lima (1970): Assumed a step-like pressure profile (physically questionable!)

## Slide 7: Solution-Diffusion Model
Consequence of the assumption:
decreases exponentially with increasing pressure difference
, partition coefficient
, partial molar volume
, thermal energy
We reach a limiting flux for water as the pressure difference increases
How does a pressure difference induce a concentration gradient?
Paul and Ebra-Lima in 1970: Assume a step-like pressure profile (physically questionable!)
It can be simplified to the final equation

## Slide 8
Is Water Transport in Reverse Osmosis Membranes Governed by the Solution-Diffusion Mechanism?
No in-situ experimental techniques to probe RO membranes at the molecular level under pressure
Hence, we used molecular dynamics simulations

## Slide 9
Synthesis
Resulting structure
MPD
TMC
Initial step
Generated PA membrane
Volume field of PA membrane
Atomistic model of interfacial polymerization between MPD and TMC monomers
A 10 nm-thick membrane is generated with a degree of cross-linking of 78.2%
Creating Atomistic Model for Interfacial Polymerization of Polyamide Membranes
Collaboration with Professor Ying Li,
University of Wisconsin, Madison

## Slide 10: Molecular Dynamics Model for Polyamide has been Validated Against Experimental Data
He, McCutcheon, Li "Effect of different manufacturing methods on polyamide reverse-osmosis membranes for desalination: Insights from molecular dynamics simulations." Desalination 547 (2023): 116204.
He, Yang, McCutcheon, and Li. "Molecular insights into the structure-property relationships of 3D printed polyamide reverse-osmosis membrane for desalination." Journal of Membrane Science 658 (2022): 120731.
Membrane density
Pore size distribution
Atomic composition
Water swelling
Water permeance
Effect of pressure on salt partitioning
Compression of polyamide at ultra high pressures

## Slide 11: Molecular Dynamics Simulations to Elucidate Water Transport Mechanism in RO Membranes
We apply pressures ranging from 30 MPa to 150 MPa
High pressures are applied to collect enough statistics in MD simulations

## Slide 12: Molecular Dynamics Simulations to Elucidate Water Transport Mechanism in RO Membranes
MD simulations show no indication of a water concentration gradient
A pressure gradient is observed inside the membrane
A linear relationship between water flux and applied pressure is observed
Solution-Diffusion
Mechanism

## Slide 13: Water Molecules Travel Through RO Membranes as Clusters
SD model is derived based on a binary system where both polymer and solvent (water) molecules are perfectly mixed
In MD simulations, water molecules are clustered together
Each water molecule is surrounded by ~5 other water molecules
SD model requires water molecules to be dispersed
Solution-Diffusion
Mechanism

## Slide 14: Water Molecules Travel as Clusters Through Transiently Connected Pores
Let us track the trajectory of a group of water molecules as they enter the membrane
Water molecules in the group travel together in clusters along the membrane (not dispersed)!
Feed
Permeate
Solution-Diffusion
Mechanism

## Slide 15: Water Molecules Travel as Clusters Through Transiently Connected Pores

## Slide 16: Apparent Experimental Evidence for the SD Model: Water Concentration Gradient
Four laminated cellulose acetate films (total thickness 500 µm)
Rosenbaum and Cotton, Journal of Polymer Science Part A‐1: Polymer Chemistry,1969

## Slide 17: Water Content Gradient is Attributed to Membrane Compression Under Pressure
Peterlin & Williams, Journal of Applied Polymer Science, 1971
The compacting pressure (Pc) increases along the direction of water flux
Pore (free) volume decreases from feed side to permeate side
Pc

## Slide 18: Poroelastic Model for Solvent Flow and Compaction in RO Membranes
Hedge et al., Science, 2022
x
, solvent volume fraction
, feed side fraction
, elastic modulus
, hydraulic pressure
A poroelastic model treating the solvent
and polymer as distinct phases and the solvent phase as a Newtonian fluid:
, solvent flux
, elastic modulus (feed side)
, parameter related to solvent volume fraction and frictions

## Slide 19: Water Content Gradient is Attributed to Membrane Compression Under Pressure
Hedge et al., Science, 2022
Solvent (water) volume fraction () described by a poroelastic model
Elastic modulus, M, indicates the compressive stiffness
A fully rigid membrane (M ) has a constant water content
Elastic membranes exhibit compaction

## Slide 20: Will We Have Water Flow Here by Diffusion?
Hypothetical Membrane
Realistic Membrane
Of course not!
Perpetual motion machine…Violates thermodynamics!

## Slide 21: Another Apparent Experimental Evidence for the Solution-Diffusion Model is Flawed
Paul and Ebra‐Lima, Journal of Applied Polymer Science, 1970
Hirai et al, Journal of Applied Polymer science, 1989
Notes: , Paul and Ebra-Lima32,34 used organic solvents as penetrants and a highly swollen rubber film to examine the existence of any limiting fluxes. Fig. 10A presents two representative flux-pressure curves for the solvents considered in their study: iso-octane and methyl ethyl ketone. The flux-pressure curves deviate from linearity as the pressure increases. However, compaction is expected to have a significant impact on the highly elastic and swollen rubber film (volume of sorbed solvent in the membrane is > 60%). Fig. 10B shows that compaction induces similar flux suppression of water transport in highly swollen hydrogels.102 Notably, the SD model predicts that we need pressures > 136 bar to cause only ≈5% deviation from linearity for water.103 However, this deviation in Fig. 10 occurs for pressures < 10 bar. Compaction is the only reasonable explanation since no other nonideality effects can explain this order of magnitude difference. In addition to the limiting fluxes, for the rubber film in Fig. 10A we calculated high solvent permeability (>10 𝜇𝑚𝐿/(𝑚^2 ℎ 𝑏𝑎𝑟)), which is typical of ultrafiltration membranes. Therefore, it is questionable to apply these findings for highly porous and swollen rubber films directly to water transport in RO membranes or to consider a diffusion as a possible solvent transport mechanism.

## Slide 22: Nonlinearity in Water Flux vs Pressure is due to Membrane Compression Under Pressure
Linear relationship for rigid membranes (M ) or small pressures
Elastic membranes with larger elasticity show deviation from the linearity
Hedge et al., Science, 2022
The poroelastic model can also explain the nonlinear of solvent fluxv relationship

## Slide 23: Solution-Friction Model
Force balance on solvent cluster:
total pressure exerting on solvent
solvent-membrane friction
gas constant
absolute temperature
solvent-ion friction
ion concentration (inside membrane)
ion velocity
solvent velocity

## Slide 24: Solution-Friction Model
Ion velocity
Substituting into force balance equation
For neutral solutes and assuming no solute-membrane interactions (1)
solvent-ion friction
membrane-ion friction

## Slide 25: Solution-Friction Model
Total pressure
, is the virtual osmotic pressure of the solution that is in equilibrium with the membrane.
Solvent velocity

## Slide 26: Solution-Friction Model
Integrating yields
Let A and
The above equation is identical to the well-known Spiegler-Kedem-Katchalsky equation for water flux.

## Slide 27: Concluding Remarks
The solution-diffusion mechanism for water transport in RO is flawed and based on unphysical assumptions
Water transport in RO is governed by a pressure gradient (“pore flow” mechanism)
Water and solvent transport can be described by the solution-friction model