Supporting Information

Hierarchical Surface-modification of Nano-Cu toward One Pot H-Transfer-Coupling-Cyclization-CO2 Fixation Tandem Reactions

Zhi-Qiang Wang,[ab]# Chenghua Deng,[c]# Bo Li,[b] Hai-Qiang Luo,[b] Peng Hao,[b] Xiao Liu,*[b] Jian-Gong Ma,*[b] Peng Cheng[b].

aCollege of Basic Sciences, Shanxi Agricultural University, Jinzhong, 030800, P. R. China.

bDepartment of Chemistry and Key Laboratory of Advanced Energy Material Chemistry (MOE), College of Chemistry, Nankai University, Tianjin 300071, P. R. China

cDepartment of Chemical Sciences and Bernal Institute, University of Limerick, Limerick V94 T9PX, Ireland

*Correspondence to: mvbasten@nankai.edu.cn; lx@nankai.edu.cn.

Experimental section

General information

Unless otherwise noted, all manipulations were performed under a dry argon or carbon dioxide atmosphere using Schlenk-line techniques. All the reagents employed were commercially available and used without further purification.

Nuclear magnetic resonance (NMR) spectra were recorded on a Bruker Ascend-400 spectrometer (1H NMR, 400 MHz; 13C NMR, 101 MHz). Data were reported in the following order: chemical shift in ppm (multiplicity was indicated by s (singlet), d (doublet), t (triplet), q (quartet), m (multiplet)).

Power X-ray diffraction (PXRD) was tested on an Ultima IV X-ray diffractometer using Cu Kα radiation in the 2θ range of 2.5-80° (λ = 0.154178 nm).

Morphologies of samples were characterized by a scanning electron microscope (SEM, ZEISS, MERLIN Compact) instrument.

X-ray photoelectron spectroscopy (XPS) was tested by a Thermo Scientific K-Alpha instrument.

Transmission electron microscope (TEM) was tested by a JEOL JEM-2800 instrument.

Inductively coupled plasma - optical emission spectrometry (ICP-OMS) was measured by a SpectroBlue, Spectro, instrument.

Gas sorption measurements were conducted by a Micromeritics 3Flex instrument. The 77 K N2 sorption experiments were tested with the sample-loaded tubes soaked in the liquid nitrogen bath.

For Langmuir specific surface area calculation, the Langmuir isotherm model can be expressed by the following equation[1]:

where Q (cm-3 g-1) is the amount adsorbed; Q0 (cm-3 g-1) is the saturated amount adsorbed, p (mmHg) is the equilibrium pressure, and b (mmHg-1) is the adsorption affinity. A line equation for the Langmuir equation can be written as following:

A least-squares fitting is performed on the (pQ, p) designated pairs where pQ is the independent variable and p is the dependent variable. The following are calculated: a) Slope (1Q0, g cm-3, STP); b) Y-intercept (1bQ0, g mmHg cm-3, STP); c) Error of the slope (g cm-3, STP); d) Error of the y-intercept (g mmHg cm-3, STP). Using the results of the above calculations, the Langmuir specific surface area can be calculated as following:

where SLan is the Langmuir specific surface area (m2 g-1); Am is the molecular cross-sectional area (nm2, 1 nm2 = 1 × 10-18 m2) of adsorbate (0.1540 nm2 for N2); Vmol represents the molar volume of a gas at STP (22414 cm3 mol-1), and NA is the Avogadro’s number (6.02 × 1023 molecules/mol).

For BET (Brunauer–Emmett–Teller) specific surface area calculation, the BET isotherm model can be expressed by the following equation4:

where Q (cm-3 g-1) is the amount adsorbed; p and p0 (mmHg) are the equilibrium and the saturation pressure of adsorbates at the temperature of adsorption respectively; vm is the monolayer adsorbed gas quantity and c is the BET constant. The experimental isotherm can be plotted as a straight line with 1/(Q/p0/p-1) on the y-axis and p/p0 on the x-axis. Based on the slope (A) and y-intercept (I) of the line, the value of vm and c could be expressed by the following equations:

The BET specific surface area is given by the following equations:

where St is the total surface area of the sample; NA is the Avogadro’s number (6.02 × 1023 molecules/mol); s is the molecular cross-sectional area (nm2, 1 nm2 = 1 × 10-18 m2) of adsorbate (0.1540 nm2 for N2); V is the molar volume of adsorbed gas (22414 cm3 mol-1 at STP); SBET is the BET specific surface area and a is the mass of the sample.

The sorption isotherms of CO2 were fitted with the Single-site Langmuir Freundlich (SSLF) equation12:

where Q is the gas uptake (mmol g-1), p is the pressure (kPa), Qsat is the saturation uptakes for the binding site (mmol g-1), b is the affinity coefficients of the binding site, and c is the index heterogeneity of the binding site.

The experimental isosteric heat of adsorption (Qst) values for CO2 of Cu@Ag@ZIF-8 was determined by the SSLF fitting parameters of the adsorption isotherms at 298 K, 273 K and 313 K through the Clausius-Clapeyron equation:

where T is the temperature (K), R is the ideal gas constant (8.314 J mol-1 K-1) and p is the pressure (kPa). The partial derivative term represents the slope of the plot of ln P versus  for a number of isotherms at different temperatures at various loadings.

Synthesis of Cu@Ag. In the first step, 0.33 g of Copper (II) acetylacetonate (Cu(acac)2) and 20 mL of oleylamine were added to a 100 mL three-neck flask. The flask was kept under high purity argon and constant stirring at 100 °C for 30 min. Then the flask was heated to 235 °C and held at this temperature for 3 h. In the second step, 0.052 g of AgNO3 and 15 mL of oleylamine were added to the flask, which was then held at 80 °C for 2 h. The Ag shells would form on the surface of the as-synthesized Cu nanoparticles through the galvanic displacement method. Finally, the synthesized Cu@Ag nanoparticles (NPs) were obtained after centrifuging at 10,000 rpm for 30 min and washed three times with hexane. And the powdered nanoparticles were dispersed in ethanol for further use.

Synthesis of Cu@Ag@ZIF-8. The prepared Cu@Ag NPs and 1 g polyvinyl pyrrolidone (PVP) were dispersed in 20 mL methanol solution and sonicated for 5 min. Then, 20 mL methanol solution containing 0.7 g Zn(NO3)2·6H2O and 0.25 g PVP and another equivalent volume of methanol solution of 0.26 g 2-methylimidazole and 0.25 g PVP were successively introduced. Next, the resulting mixture was stirred at 50 °C for 1 h under argon atmosphere. After the reaction, the powder was collected by centrifugation and washed 3 times with methanol. At last, the synthesized sample was dried in vacuum oven at 60 °C for 12 h.

General Experimental Procedures for 2a-i and 2k via 1a-i and 1k. In a 10 mL Schlenk tube, a mixture of 1 (0.2 mmol, 1.0 equiv.), 1,8-Diazabicyclo[5.4.0]undec-7-ene (DBU) (0.3 mmol, 1.5 equiv.), and Cu@Ag@ZIF-8 (20 mg) were added in 1 mL anhydrous CH3CN. Once added, the Schlenk tube was placed at atmospheric pressure of CO2 (1 atm) and stirred for 12 h at 50 °C, then n-C4H9I (0.6 mmol) was added in the system for 6 h. Next, the system was evaporated under the reduced pressure directly. The residue was purified by flash column chromatography with ethyl acetate and petroleum ether as eluents to afford pure product.

Experimental Procedures for 2j via 1a. In a 10 mL Schlenk tube, a mixture of 1a (0.2 mmol, 1.0 equiv.), DBU (0.3 mmol, 1.5 equiv.), and Cu@Ag@ZIF-8 (20 mg) were added in 1 mL anhydrous CH3CN. Once added, the Schlenk tube was placed at atmospheric pressure of CO2 (1 atm) and stirred for 12 h at 50 °C. Then, cooling the reaction system to room temperature and adding 1 M HCl to controlling pH to 2. Then, the system was evaporated under the reduced pressure directly. The residue was purified by flash column chromatography with ethyl acetate and petroleum ether as eluents to afford pure product.

Experimental Procedures for the Recyclability Test of Cu@Ag@ZIF-8. The Cu@Ag@ZIF-8 catalyst was recovered in the solid residue after centrifugation and separation from the organic layer containing the product. The solid residue was washed with methanol, then soaked in methanol for 5 h. The solid residue containing recovered catalyst was directly used as recycled catalyst in the subsequent runs.

DFT Calculations. DFT calculations were then performed to optimize the geometry and calculate the Gibbs free energy of the reaction on the Gaussian 16 program 2 with the B3LYP functional.3 The geometry optimization and transit state search were performed using the def2svp basis set for all atoms. Single point energies were calculated at the B3LYP/def2tzvp level on optimized geometries.4, 5

Figure S1. The PXRD patterns of ZIF-8 and the as-synthesized Cu@Ag NPs and Cu@Ag@ZIF-8.

Figure S2. (a) and (b) are corresponding to the Cu 2p and Ag 3d XPS spectra of the Cu@Ag@ZIF-8 placed in the atmosphere for three months. (c) and (d) are corresponding to the Cu 2p and Ag 3d XPS spectra of the fresh synthesized Cu@Ag@ZIF-8.

Figure S3. The PXRD patterns of Cu@Ag@ZIF-8 after soaking in different solvents systems.

Figure S4. The N2 sorption isotherms of Cu@Ag@ZIF-8 (a) and the pore width distribution (b) calculated by Horvath-Kawazoe method.

Figure S5. The N2 sorption isotherms of ZIF-8 (a) and the pore width distribution (b) calculated by Horvath-Kawazoe method.

Figure S6. The Langmuir surface area analysis of ZIF-8 (a) and Cu@Ag@ZIF-8 (b).

Figure S7. The BET surface area analysis of ZIF-8 (a) and Cu@Ag@ZIF-8 (b).

Figure S8. CO2 sorption studies of ZIF-8 and Cu@Ag@ZIF-8. (a) The 298 K and 273 K CO2 sorption isotherms of ZIF-8. (b) The 298 K and 273 K CO2 sorption isotherms of Cu@Ag@ZIF-8. (c) The SSLF fitting of 298 K CO2 adsorption isotherm of ZIF-8. (d) The SSLF fitting of 273 K CO2 adsorption isotherm of ZIF-8. (e) The SSLF fitting of 298 K CO2 adsorption isotherm of Cu@Ag@ZIF-8. (f) The SSLF fitting of 273 K CO2 adsorption isotherm of Cu@Ag@ZIF-8. (g) The Qst plots of ZIF-8 and Cu@Ag@ZIF-8 for CO2 calculated by Clausius-Clapeyron equation.

Figure S9. The Cu 2p (a) and Ag 3d (b) XPS spectra of Cu@Ag after cycling catalysis.

Figure S10. The Cu 2p (a) and Ag 3d (b) XPS spectra of Cu@Ag@ZIF-8 after cycling catalysis.

Figure S11. XRD patterns of Cu@Ag@ZIF-8 before and after cycling catalysis.

Figure S12. The morphology of separated Cu@Ag (left) and Cu@Ag@ZIF-8 (right) after five cycles.

Table S1. Screening of the optimal reaction conditions.[a]

| Entry | Catalysts (mg) | Base (mmol) | Time (h) | T (°C) | Solvent | Yield (%)[b] |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 mg | 0.3 | 12 | 50 | CH3CN | 0 |
| 2 | 30 mg | 0.3 | 12 | 50 | CH3CN | 90 |
| 3 | 20 mg | 0 | 12 | 50 | CH3CN | 0 |
| 4 | 20 mg | 0.2 | 12 | 50 | CH3CN | 81 |
| 5 | 20 mg | 0.4 | 12 | 50 | CH3CN | 90 |
| 6 | 20 mg | 0.3[c] | 12 | 50 | CH3CN | 80 |
| 7 | 20 mg | 0.3[d] | 12 | 50 | CH3CN | 90 |
| 8 | 20 mg | 0.3 | 12 | 50 | DMSO | 79 |
| 9 | 20 mg | 0.3 | 12 | 50 | DMF | 80 |
| 10 | 20 mg | 0.3 | 12 | 50 | CH3OH | 0 |
| 11 | 20 mg | 0.3 | 12 | 50 | THF | 56 |

[a] Reaction conditions: 1a (0.2 mmol), Cu@Ag@ZIF-8, DBU (0.3 mmol), n-C4H9I (0.6 mmol), solvent (1.0 mL), CO2 (1 atm), in a sealed Schlenk tube, unless otherwise noted. [b] Isolated yield. [c] K2CO3. [d] CsCO3.

NMR data for all products

butyl 2-((Z)-3-((Z)-benzylidene)isobenzofuran-1(3H)-ylidene)acetate (2a)

1H NMR (400 MHz, DMSO-d6)  7.98-8.08 (m, 4H), 7.65-7.69 (t, J = 8 Hz, 1H), 7.54-7.58 (t, J = 8 Hz, 1H), 7.42-7.45 (t, J = 8 Hz, 2H), 7.29-7.33 (t, J = 8 Hz, 1H), 6.74 (s, 1H), 6.02 (s, 1H), 4.18-4.21 (t, J = 8 Hz, 2H), 1.65-1.72 (m, 2H), 1.36-1.45 (m, 2H), 0.90-0.94 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 161.42, 150.32, 134.70, 133.99, 132.17, 131.26, 129.94, 129.23, 129.16, 128.69, 127.57, 122.18, 120.45, 103.46, 88.75, 63.32, 40.14, 39.93, 39.73, 39.52, 39.31, 39.10, 38.89, 30.52, 18.74, 13.65.

butyl 2-((Z)-3-((Z)-4-methylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2b)

1H NMR (400 MHz, DMSO-d6)  8.05-8.07 (d, J = 8 Hz, 1H), 7.96-7.98 (d, J = 8 Hz, 1H), 7.91-7.93 (d, J = 8 Hz, 2H), 7.64-7.68 (t, J = 8 Hz, 1H), 7.53-7.56 (t, J = 8 Hz, 1H), 7.24-7.26 (d, J = 8 Hz, 2H), 6.71 (s, 1H), 6.00 (s, 1H), 4.18-4.21 (t, J = 8 Hz, 2H), 2.34 (s, 3H), 1.66-1.73 (m, 2H), 1.37-1.46 (m, 2H), 0.92-0.95 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.53, 161.45, 149.66, 137.11, 134.77, 132.10, 131.15, 131.10, 129.70, 129.32, 129.19, 122.14, 120.27, 103.55, 88.43, 63.24, 40.15, 39.94, 39.73, 39.52, 39.31, 39.10, 38.89, 30.51, 20.96, 18.71, 13.62.

butyl 2-((Z)-3-((Z)-4-ethylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2c)

1H NMR (400 MHz, DMSO-d6)  8.05-8.07 (d, J = 8 Hz, 1H), 7.97-7.99 (d, J = 8 Hz, 1H), 7.93-7.95 (d, J = 8 Hz, 2H), 7.64-7.68 (t, J = 8 Hz, 1H), 7.52-7.56 (t, J = 8 Hz, 1H), 7.26-7.28 (d, J = 8 Hz, 2H), 6.71 (s, 1H), 6.00 (s, 1H), 4.17-4.21 (t, J = 8 Hz, 2H), 2.61-2.66 (m, 2H), 1.66-1.73 (m, 2H), 1.34-1.46 (m, 2H), 1.18-1.22 (t, J = 8 Hz, 3H), 0.91-0.95 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.60, 161.50, 149.75, 143.45, 134.80, 132.15, 131.45, 131.13, 129.76, 129.72, 129.32, 128.59, 128.14, 127.94, 127.38, 122.17, 120.32, 103.59, 88.45, 63.31, 40.15, 39.94, 39.73, 39.52, 39.31, 39.10, 38.89, 30.56, 28.06, 18.76, 15.45, 15.39, 13.67.

butyl 2-((Z)-3-((Z)-4-ethylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2d)

1H NMR (400 MHz, DMSO-d6)  8.06-8.08 (d, J = 8 Hz, 1H), 7.93-7.99 (dd, J = 8 Hz, 1H), 7.65-7.68 (t, J = 8 Hz, 1H), 7.53-7.56 (t, J = 8 Hz, 1H), 7.24-7.26 (d, J = 8 Hz, 2H), 6.72 (s, 1H), 6.01 (s, 1H), 4.17-4.21 (t, J = 8 Hz, 2H), 2.56-2.60 (t, J = 8 Hz, 2H), 1.57-1.73 (m, 4H), 1.36-1.46 (m, 2H), 0.88-0.95 (m, 6H);

13C NMR (101 MHz, DMSO-d6) δ 164.58, 161.49, 149.74, 141.81, 134.79, 132.15, 131.47, 131.13, 129.76, 129.22, 128.75, 122.19, 120.32, 103.59, 88.46, 63.30, 40.14, 39.94, 39.73, 39.52, 39.31, 39.10, 37.09, 30.55, 23.91, 18.75, 13.67, 13.62.

butyl 2-((Z)-3-((Z)-4-(tert-butyl)benzylidene)isobenzofuran-1(3H)-ylidene)acetate (2e)

1H NMR (400 MHz, DMSO-d6)  8.06-8.08 (d, J = 8 Hz, 1H), 7.95-8.00 (dd, J = 8 Hz, 3H), 7.65-7.69 (t, J = 8 Hz, 1H), 7.53-7.57 (t, J = 8 Hz, 1H), 7.44-7.46 (d, J = 8 Hz, 2H), 6.73 (s, 1H), 6.01 (s, 1H), 4.18-4.21 (t, J = 8 Hz, 2H), 1.67-1.75 (m, 2H), 1.37-1.46 (m, 2H), 1.31 (s, 9H), 0.92-0.96 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.57, 161.48, 150.19, 149.86, 134.77, 132.15, 131.19, 131.14, 129.77, 129.05, 125.48, 122.17, 120.34, 103.42, 88.46, 63.33, 40.15, 39.94, 39.73, 39.52, 39.31, 39.11, 38.90, 34.44, 31.01, 30.56, 18.75, 13.72.

butyl 2-((Z)-3-((Z)-4-methoxybenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2f)

1H NMR (400 MHz, DMSO-d6)  8.04-8.06 (d, J = 8 Hz, 1H), 7.94-8.00 (dd, J = 8 Hz, 3H), 7.63-7.67 (t, J = 8 Hz, 1H), 7.51-7.55 (t, J = 8 Hz, 1H), 6.99-7.02 (d, J = 8 Hz, 2H), 6.71 (s, 1H), 5.99 (s, 1H), 4.17-4.20 (t, J = 8 Hz, 2H), 3.81 (s, 3H), 1.65-1.72 (m, 2H), 1.36-1.45 (m, 2H), 0.91-0.95 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.59, 161.65, 158.80, 148.67, 134.91, 132.09, 130.86, 130.78, 129.44, 126.58, 122.14, 120.06, 114.23, 103.50, 88.03, 63.22, 55.16, 40.15, 39.94, 39.73, 39.52, 39.31, 39.10, 38.89, 30.54, 18.73, 13.67.

butyl 2-((Z)-3-((Z)-4-fluorobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2g)

1H NMR (400 MHz, DMSO-d6)  8.05-8.09 (t, J = 8 Hz, 3H), 7.97-7.99 (d, J = 8 Hz, 1H), 7.67-7.70 (t, J = 8 Hz, 1H), 7.55-7.59 (t, J = 8 Hz, 1H), 7.26-7.30 (t, J = 8 Hz, 2H), 6.78 (s, 1H), 6.05 (s, 1H), 4.17-4.21 (t, J = 8 Hz, 2H), 1.64-1.71 (m, 2H), 1.36-1.45 (m, 2H), 0.91-0.94 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.51, 162.53, 161.45, 160.08, 149.95, 149.93, 134.61, 132.23, 131.20, 131.12, 130.66, 130.62, 129.98, 122.24, 120.40, 115.81, 115.59, 102.33, 88.78, 63.31, 40.14, 39.94, 39.73, 39.52, 39.31, 39.10, 38.89, 30.51, 18.73, 13.66.

butyl 2-((Z)-3-((Z)-4-chlorobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2h)

1H NMR (400 MHz, DMSO-d6)  8.07-8.09 (d, J = 8 Hz, 1H), 7.98-8.03 (dd, J = 8 Hz, 3H), 7.67-7.70 (t, J = 8 Hz, 1H), 7.56-7.60 (t, J = 8 Hz, 1H), 7.47-7.49 (d, J = 8 Hz, 2H), 6.77 (s, 1H), 6.06 (s, 1H), 4.18-4.21 (t, J = 8 Hz, 2H), 1.64-1.71 (m, 2H), 1.36-1.45 (m, 2H), 0.91-0.95 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.47, 161.24, 150.76, 134.45, 132.98, 132.24, 131.83, 131.34, 130.68, 130.17, 128.71, 122.25, 120.54, 102.12, 89.12, 63.37, 40.15, 39.94, 39.73, 39.52, 39.32, 39.11, 38.90, 30.52, 18.72, 13.65.

butyl 2-((Z)-3-((Z)-4-bromobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2i)

1H NMR (400 MHz, DMSO-d6)  7.98-8.11 (m, 3H), 7.94-7.96 (d, J = 8 Hz, 1H), 7.57-7.72 (m, 3H), 7.51-7.53 (d, J = 8 Hz, 1H), 6.81 (s, 1H), 6.08 (s, 1H), 4.20-4.23 (t, J = 8 Hz, 2H), 1.66-1.73 (m, 2H), 1.37-1.46 (m, 2H), 0.92-0.96 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, DMSO-d6) δ 164.49, 161.20, 151.22, 134.71, 134.46, 133.37, 133.30, 132.27, 131.88, 131.73, 131.42, 130.97, 130.27, 129.30, 123.04, 121.56, 120.59, 102.67, 90.88, 89.49, 63.41, 40.15, 39.94, 39.73, 39.52, 39.32, 39.11, 38.90, 30.55, 18.75, 13.67.

2-((Z)-3-((Z)-benzylidene)isobenzofuran-1(3H)-ylidene)acetic acid (2j)

1H NMR (400 MHz, DMSO-d6)   12.08 (s, 1H), 7.98-8.07 (m, 4H), 7.65-7.68 (t, J = 8 Hz, 1H), 7.54-7.58 (t, J = 8 Hz, 1H), 7.39-7.42 (t, J = 8 Hz, 2H), 7.27-7.31 (t, J = 8 Hz, 1H), 6.72 (s, 1H), 5.94 (s, 1H);

13C NMR (101 MHz, DMSO-d6) δ 166.36, 161.54, 150.80, 135.06, 134.56, 132.46, 131.86, 130.37, 129.72, 129.11, 127.90, 122.53, 120.92, 103.53, 90.21, 40.59, 40.37, 40.17, 39.96, 39.75, 39.54, 39.33.

butyl 2-((1Z,3Z)-3-(2-hydroxy-2-phenylpropylidene)isobenzofuran-1(3H)-ylidene)acetate (2k)

1H NMR (400 MHz, CDCl3)  7.79-7.82 (m, 2H), 7.49-7.72 (m, 6H), 7.38-7.42 (m, 1H), 6.04 (s, 1H), 5.74 (s, 1H), 4.53 (s, 1H), 4.35-4.38 (t, J = 8 Hz, 2H), 2.08 (s, 3H), 1.81-1.89 (m, 2H), 1.50-1.62 (m, 2H), 1.09-1.12 (t, J = 8 Hz, 3H);

13C NMR (101 MHz, CDCl3) δ 165.48, 161.02, 149.87, 148.05, 134.37, 131.78, 131.61, 129.73, 128.24, 126.89, 124.85, 121.19, 120.18, 111.20, 88.85, 77.47, 77.16, 76.84, 74.06, 64.14, 31.41, 30.85, 19.22, 14.20, 13.80.

1H NMR and 13C NMR Spectra

butyl 2-((Z)-3-((Z)-benzylidene)isobenzofuran-1(3H)-ylidene)acetate (2a)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-methylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2b)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-ethylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2c)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-ethylbenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2d)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-(tert-butyl)benzylidene)isobenzofuran-1(3H)-ylidene)acetate (2e)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-methoxybenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2f)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-fluorobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2g)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-chlorobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2h)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((Z)-3-((Z)-4-bromobenzylidene)isobenzofuran-1(3H)-ylidene)acetate (2i)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

2-((Z)-3-((Z)-benzylidene)isobenzofuran-1(3H)-ylidene)acetic acid (2j)

1H NMR (400 MHz, DMSO-d6)

13C NMR (101 MHz, DMSO-d6)

butyl 2-((1Z,3Z)-3-(2-hydroxy-2-phenylpropylidene)isobenzofuran-1(3H)-ylidene)acetate (2k)

1H NMR (400 MHz, CDCl3)

13C NMR (101 MHz, CDCl3)

Supplemental References

[1]	a) I. Langmuir, J. Am. Chem. Soc. 1916, 38, 1145–1156. b) I. Langmuir, J. Am. Chem. Soc. 1918, 40, 1361–1403. c) I. Langmuir, Phys. Rev. 1916, 8, 149–176.

[2]	M. J. Frisch, G. W. Trucks, H. B.Schlegel, G. E. M. A. Scuseria, J. R. Robb, Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. V. Marenich, J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian, J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery Jr., J. E. Peralta, F. Ogliaro, M. J. Bearpark, J. J. Heyd, E. N. Brothers, K. N. Kudin, V. N. Staroverov, T. A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. P. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, D. J. Fox. Gaussian 16 Rev. C.01, Wallingford, CT, 2016.

[3]	A. D Becke, Phys. Rev. A. 1988, 38, 3098-3100.

[4]	P. J.Hay, R. W. Wadt, J. Chem. Phys. 1985, 82, 270−283.

[5]	D. Andrae, U. Häußermann, M. Dolg, H. Stoll, H. Preuß, Theor. Chim. Acta. 1990, 77, 123-141.