Supporting Information

Unraveling the Formation of Oxygen Vacancy on the Surface of Transition Metal-Doped Ceria Utilizing Artificial Intelligence

Ning Xu,‡a,c Liangliang Xu,‡b Yue Wang,e Wen Liu,c Wenwu Xu,*a Xiaojuan Hu*c,d and Zhong-Kang Han*c

a Department of Physics, School of Physical Science and Technology, Ningbo University, Ningbo, 315211, China

b Department of Chemical and Biomolecular Engineering, Korea Advanced Institute of Science and Technology (KAIST), 291 Daehak-Ro, Yuseong-Gu, Daejeon 34141, Republic of Korea

c School of Materials Science and Engineering, Zhejiang University, Hangzhou, 310027, China

d Fritz-Haber-Institut der Max-Planck-Gesellschaft, Faradayweg 4-6, 14195 Berlin, Germany

e Department of Electrical Engineering, Hanyang University, Seoul 04763, Republic of Korea

‡ These authors contributed equally to this work.

Contents

Supplementary Methods

Supplemental Figures and Tables

Table S1. The surface energy for CeO2(100), (110), and (111) surfaces.

Table S2. The formation energies of the transition metal doped-CeO2(100) systems.

Table S3. The formation energies of the transition metal doped-CeO2(110) systems.

Table S4. The formation energies of the transition metal doped-CeO2(111) systems.

Figure S1. Calculated spin charges (top and side views) of V-doped CeO2(100) surface (a) (b), and W-doped CeO2(100) surface (c). Nb-doped CeO2(110) surface (d) (e) (f). Os-doped CeO2(111) surface (g), and Ta-doped CeO2(111) surface (h) (i) (j).

Figure S2. Correlation between the formation energies and low-cost features of the 3d-, 4d-, and 5d-block transition metal dopants.

Figure S3. Correlation between the oxygen vacancy formation energies and low-cost features of the 3d-, 4d-, and 5d-block transition metal dopants.

Figure S4. The error distributions for all the lower-dimensional models of the surface Ov formation energies: (a) 1D, (b) 2D, (c) 3D, (d) 4D, and the SISSO selected best 5D model (e).

Table S5. Descriptors components of the SISSO-identified 1D to 5D models for leave-5%-out validation.

Table S6. The selected feature set of the 5D-SISSO model during validation process.

Table S7. The oxygen vacancy formation energy, Fermi level, and Bader charge for different transition metal-doped metal oxide systems.

Supplementary References

Supplementary Methods

Subgroup discovery. The subgroup discovery was performed using RealKD package.1 Each feature was split to 14 subsets using 14-means clustering algorithm.2 The borders between adjacent data clusters (a1, a2, ...) are applied further for construction of inequalities (feature1 < a1), (feature2 ≥ a2), etc.. While final result might depend on the number of considered clusters, in our previous study we found that relatively high numbers of considered clusters provide essentially the same result.3 The candidate subgroups are built as conjunctions of obtained simple inequalities. The main idea of SGD is that the subgroups are unique if the distribution of the data in them is as different as possible from the data distribution in the whole sampling. Here the data distribution is the distribution of a target property (∆EOv). The uniqueness is evaluated with a quality function. In this study we used the following function:

QS=sSsPmedP-medSmedP-minP1-amdSamdP                      (S1)

with S – subgroup, P – whole sampling, s – size, med and min – median and minimal values of a target property, amd – absolute average deviation of the data around the median of target property. With this function the algorithm is searching for subgroups with lower values of target properties. The search was done with an adapted for such purposes Monte-Carlo algorithm,4 in which first a certain number of trial conjunctions (seeds) is generated. Afterwards, for each seed (accompanied with pruning of inequalities) the quality function is calculated. We have tested here several numbers of initial seeds: 10 000, 30 000, 50 000 and 100 000. The subgroups with the overall high quality function value were selected.

SISSO calculation. In SISSO, the feature construction was performed by creating all the possible mathematical combinations, within certain feature complexity, between the primary features using the operators {+, −, ·, /, log, exp, exp−, −1, 2, 3, √, 3√, |−|}. A list of the primary features for model training data sets can be found in the file “Supplementary file1.” The code for SISSO and user guide are available at: https://github.com/rouyang2017/SISSO.

Table S1. The surface energy for CeO2(100), (110), and (111) surfaces.

| Surfaces | Surface energy (J/m2） | Ref. (J/m2） |
| --- | --- | --- |
| CeO2 (100) | 1.72 | 1.71 [Nature Mater., 2017, 16, 328-334] |
| CeO2 (110) | 1.10 | 1.05 [Phys. Rev. B, 2004, 69, 075401] |
| CeO2 (111) | 0.68 | 0.60 [ChemPhysChem, 2007, 8, 849–855] |

Table S2. The formation energies of the transition metal doped-CeO2(100) surfaces.

| Systems | Formation energy (eV) |  |  | Ov formation energy (eV) |
| --- | --- | --- | --- | --- |
| Ce/CeO2(100) |  | / | 1.3248 |  |
| Ag/CeO2(100) | 9.3874 |  |  | -0.7649 |
| Au/CeO2(100) | 9.1957 |  |  | 0.1344 |
| Cd/CeO2(100) | 6.8297 |  |  | -0.3077 |
| Co/CeO2(100) | 6.4028 |  |  | 0.0723 |
| Cr/CeO2(100) | 1.4379 |  |  | 0.3446 |
| Cu/CeO2(100) | 8.3494 |  |  | -0.4801 |
| Fe/CeO2(100) | 5.1223 |  |  | 0.3278 |
| Hf/CeO2(100) | -2.1751 |  |  | 1.1832 |
| Hg/CeO2(100) | 7.7141 |  |  | 0.3417 |
| Ir/CeO2(100) | 6.7473 |  |  | 1.4700 |
| Mn/CeO2(100) | 3.7502 |  |  | 0.5709 |
| Mo/CeO2(100) | -0.2722 |  |  | 1.4765 |
| Nb/CeO2(100) | -1.8859 |  |  | 1.2638 |
| Ni/CeO2(100) | 7.4590 |  |  | 0.1203 |
| Os/CeO2(100) | 4.8905 |  |  | 1.6679 |
| Pd/CeO2(100) | 8.3271 |  |  | 0.0607 |
| Pt/CeO2(100) | 7.9227 |  |  | 0.7017 |
| Re/CeO2(100) | 1.5157 |  |  | 1.7273 |
| Rh/CeO2(100) | 7.3141 |  |  | 0.5603 |
| Ru/CeO2(100) | 5.3904 |  |  | 0.9742 |
| Sc/CeO2(100) | -0.2062 |  |  | 0.1713 |
| Ta/CeO2(100) | -1.6423 |  |  | 0.5735 |
| Tc/CeO2(100) | 2.5507 |  |  | 0.7993 |
| Ti/CeO2(100) | -1.0483 |  |  | 0.1794 |
| V/CeO2(100) | -0.6679 |  |  | 0.6571 |
| W/CeO2(100) | -0.9484 |  |  | 1.4776 |
| Y/CeO2(100) | -0.7122 |  |  | 1.0793 |
| Zn/CeO2(100) | 6.4482 |  |  | -0.6811 |
| Zr/CeO2(100) | -1.9701 |  |  | 1.2418 |
| V/CeO2(100)-a | -0.4041 |  |  | 0.5511 |
| V/CeO2(100)-b | -0.0688 |  |  | 0.8518 |
| W/CeO2(100)-a | -0.8577 |  |  | 1.9251 |

Table S3. The formation energies of the transition metal doped-CeO2(110) surfaces.

| Systems | Formation energy (eV) | Ov formation energy (eV) |
| --- | --- | --- |
| Ce/CeO2(110) | / | 1.3628 |
| Ag/CeO2(110) | 9.4955 | -0.4652 |
| Au/CeO2(110) | 9.3998 | 0.1603 |
| Cd/CeO2(110) | 7.3819 | -0.7864 |
| Co/CeO2(110) | 8.0157 | -1.1726 |
| Cr/CeO2(110) | 4.2819 | -1.7270 |
| Cu/CeO2(110) | 7.9584 | -0.3005 |
| Fe/CeO2(110) | 7.3825 | -1.4013 |
| Hf/CeO2(110) | -1.6930 | 0.3974 |
| Hg/CeO2(110) | 8.9401 | -0.9371 |
| Ir/CeO2(110) | 7.3329 | 0.5169 |
| Mn/CeO2(110) | 4.1687 | 0.7255 |
| Mo/CeO2(110) | 1.0404 | 0.0180 |
| Nb/CeO2(110) | -0.6971 | 0.3260 |
| Ni/CeO2(110) | 7.5697 | -0.6781 |
| Os/CeO2(110) | 5.9154 | 0.1456 |
| Pd/CeO2(110) | 9.2770 | -1.5715 |
| Pt/CeO2(110) | 9.0451 | -1.2349 |
| Re/CeO2(110) | 2.9299 | 0.2676 |
| Rh/CeO2(110) | 8.1762 | 0.0979 |
| Ru/CeO2(110) | 7.6028 | -1.0278 |
| Sc/CeO2(110) | 0.2664 | -0.1570 |
| Ta/CeO2(110) | -1.1535 | 0.1103 |
| Tc/CeO2(110) | 5.0934 | -1.5863 |
| Ti/CeO2(110) | 0.1372 | -0.5202 |
| V/CeO2(110) | 1.4833 | -0.6643 |
| W/CeO2(110) | 0.6735 | -0.0696 |
| Y/CeO2(110) | -0.1730 | 0.3024 |
| Zn/CeO2(110) | 7.2377 | -0.9377 |
| Zr/CeO2(110) | -1.5242 | 0.7530 |
| Nb/CeO2(110)-a | -0.7073 | 0.0056 |
| Nb/CeO2(110)-b | -0.7051 | -0.0201 |
| Nb/CeO2(110)-c | -0.7111 | 0.0222 |

Table S4. The formation energies of the transition metal doped-CeO2(111) surfaces.

| Systems | Formation energy (eV) | Ov formation energy (eV) |
| --- | --- | --- |
| Ce/CeO2(111) | / | 2.1325 |
| Ag/CeO2(111) | 10.5758 | -0.2579 |
| Au/CeO2(111) | 10.2544 | 0.6469 |
| Cd/CeO2(111) | 8.7242 | -0.8739 |
| Co/CeO2(111) | 8.1733 | 0.8430 |
| Cr/CeO2(111) | 4.0750 | 0.1756 |
| Cu/CeO2(111) | 10.7102 | -1.7354 |
| Fe/CeO2(111) | 6.4509 | 0.5071 |
| Hf/CeO2(111) | -1.2509 | 1.2544 |
| Hg/CeO2(111) | 10.2191 | -0.5947 |
| Ir/CeO2(111) | 8.9592 | 1.2674 |
| La/CeO2(111) | 0.1550 | 0.8178 |
| Mn/CeO2(111) | 5.5515 | 1.6282 |
| Mo/CeO2(111) | 3.1552 | -0.3176 |
| Nb/CeO2(111) | -0.1846 | 1.6545 |
| Ni/CeO2(111) | 8.6109 | 0.7988 |
| Os/CeO2(111) | 7.9453 | -0.4504 |
| Pd/CeO2(111) | 9.4139 | 0.8672 |
| Pt/CeO2(111) | 8.9508 | 1.5505 |
| Re/CeO2(111) | 3.3522 | 0.9927 |
| Rh/CeO2(111) | 8.8995 | 1.2897 |
| Ru/CeO2(111) | 8.2315 | 1.2498 |
| Sc/CeO2(111) | 1.3929 | 0.1236 |
| Ta/CeO2(111) | -0.6097 | 1.5726 |
| Tc/CeO2(111) | 4.2860 | 1.0218 |
| Ti/CeO2(111) | 0.6136 | 1.2228 |
| V/CeO2(111) | 2.0367 | 1.1966 |
| W/CeO2(111) | 1.6757 | 1.0265 |
| Y/CeO2(111) | 0.3517 | 0.6026 |
| Zn/CeO2(111) | 8.6148 | -1.0411 |
| Zr/CeO2(111) | -1.1223 | 1.2621 |
| Os/CeO2(111)-a | 6.8930 | 2.2512 |
| Ta/CeO2(111)-a | -0.5837 | 0.8003 |
| Ta/CeO2(111)-b | -0.5436 | 1.0707 |
| Ta/CeO2(111)-c | -0.5860 | 1.0128 |

Figure S1. Calculated spin charges (top and side views) of V-doped CeO2(100) surface (a) (b), and W-doped CeO2(100) surface (c). Nb-doped CeO2(110) surface (d) (e) (f). Os-doped CeO2(111) surface (g), and Ta-doped CeO2(111) surface (h) (i) (j).

Figure S2. Correlation between the formation energies and low-cost features of the 3d-, 4d-, and 5d-block transition metal dopants.

Figure S3. Correlation between the oxygen vacancy formation energies and low-cost features of the 3d-, 4d-, and 5d-block transition metal dopants.

Figure S4. The error distributions for all the lower-dimensional models of the surface Ov formation energies: (a) 1D, (b) 2D, (c) 3D, and (d) 4D, and the SISSO selected best model (e) 5D.

Table S5. Descriptors components of the SISSO-identified 1D to 5D models for leave-5%-out validation.

| Iteration | Dimension | Descriptor |
| --- | --- | --- |
| 01 | 1D | (RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | (RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 4D | (PC*ECm)/((Lm+RDm)+(FL*Ndsm)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 4D | (PC/EIm)/((Lm+RDm)+(FL*Ndsm)) |
|  | 5D | (Rm/PC)/((PC−Rm)−(q*ENm)) |
| 02 | 1D | ((ECm/WF)*(FL−RDm))−(PC*RDm) |
|  | 1D | (FL−(RDm*MdNm))−(WF/(q+PC)) |
|  | 2D | ((FL−MdNm)−PC)/(Rm+(ECm*RDm)) |
|  | 1D | (FL−(RDm*MdNm))−(WF/(q+PC)) |
|  | 2D | ((FL−BDEm)−PC)/(RDm+(Rm/ECm)) |
|  | 3D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 1D | (FL−(RDm*MdNm))−(WF/(q+PC)) |
|  | 2D | (FL/(BDEm−FL))/(WF+(ECm*ENm)) |
|  | 3D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 4D | (DC+MdLm)/((Ndsm/WF)−(Rm+RDm)) |
|  | 1D | (FL−(RDm*MdNm))−(WF/(q+PC)) |
|  | 2D | (FL/(BDEm−FL))/(WF+(ECm*ENm)) |
|  | 3D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 4D | (DC+MdLm)/((Ndsm/WF)−(Rm+RDm)) |
|  | 5D | ((WF/PC)−Hm)/(RDm+(BDEm/Hm)) |
| 03 | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (MdLm/Ndm)/((Ndsm/Hm)−(PC*BDEm)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (RSm/DC)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 4D | (BDEm/(FL+BDEm))/((DC/FL)−PC) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (ENm/Ndm)/((Ndsm/Hm)−(PC*BDEm)) |
|  | 4D | (WF+(EIm/PC))/((DC/FL)−PC) |
|  | 5D | (q−Lm)/((WF+ECm)+(Ndsm/EIm)) |
| 04 | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 1D | (ECm+(ECm/q))+(FL*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (MdNm/Ndm)/((Ndsm/Hm)−(PC*BDEm)) |
|  | 1D | (ECm+(ECm/q))+(FL*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (Lm/Ndm)/((Ndsm/Hm)−(PC*BDEm)) |
|  | 4D | (DC+(FL*BDEm))/((q*WF)−ECm) |
|  | 1D | (ECm+(ECm/q))+(FL*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (MdNm/Ndm)/((Ndsm/Hm)−(PC*BDEm)) |
|  | 4D | (DC+(FL*BDEm))/((q*WF)−ECm) |
|  | 5D | (DC−Lm)/((ENm−MdNm)−(FL/Ndm)) |
| 05 | 1D | (RDm+(FL/q))*((EIm*MdNm)−Ndsm) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 4D | (PC*ECm)/((Lm+RDm)+(FL*Ndsm)) |
|  | 1D | ((FL−ENm)*(RDm*MdLm))−(Ndm/q) |
|  | 2D | (ECm+MdLm)/((Hm+MdLm)−(Lm+WF)) |
|  | 3D | (DC−Hm)/((EIm−BDEm)−(Rm*WF)) |
|  | 4D | (Hm*ECm)/((Lm+RDm)+(FL*Ndsm)) |
|  | 5D | (Hm+BDEm)/((DC+MdLm)−(RSm−PC)) |
| 06 | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (ENm/Lm)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (MdNm/q)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 4D | (BDEm−ENm)/((Hm+PC)−(q*WF)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (MdNm/q)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 4D | (BDEm−ENm)/((Hm+PC)−(q*WF)) |
|  | 5D | (DC*(BDEm−WF))/((PC*Rm)−Hm) |
| 07 | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | ((FL/q)−RSm)*(ECm+(FL*MdLm)) |
|  | 2D | (Rm/(PC+WF))/((ECm−BDEm)−Hm) |
|  | 1D | ((FL/q)−RSm)*(ECm+(FL*MdLm)) |
|  | 2D | (Rm/(PC+WF))/((ECm−BDEm)−Hm) |
|  | 3D | (Ndsm/(FL−PC))/(FL+(RDm/ECm)) |
|  | 1D | ((FL/q)−RSm)*(ECm+(FL*MdLm)) |
|  | 2D | (Rm/(PC+WF))/((ECm−BDEm)−Hm) |
|  | 3D | (Ndm/(FL−PC))/(FL+(RDm/ECm)) |
|  | 4D | (Ndm−WF)/((FL+Hm)+(MdLm−RSm)) |
|  | 1D | ((FL/q)−RSm)*(ECm+(FL*MdLm)) |
|  | 2D | (Rm/(PC+WF))/((ECm−BDEm)−Hm) |
|  | 3D | (Ndm/(FL−PC))/(FL+(RDm/ECm)) |
|  | 4D | (Ndm−WF)/((FL+Hm)+(MdLm−RSm)) |
|  | 5D | (FL+Rm)/((WF/q)+(Rm+RSm)) |
| 08 | 1D | ((RDm−Rm)/q)+(RSm/(WF−FL)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (ECm/DC)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 1D | (q+ECm)+((FL*RSm)*(FL+ENm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (ECm/DC)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 4D | (FL/(FL+MdNm))/((DC/PC)−FL) |
|  | 1D | (q+ECm)+((FL+Rm)*(FL*ENm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | (ECm/RDm)/((Hm*BDEm)−(Ndsm/PC)) |
|  | 4D | ((MdLm−WF)/ECm)/((FL*PC)−DC) |
|  | 5D | (ECm/Rm)/((FL+ECm)+(Lm+EIm)) |
| 09 | 1D | ((FL*BDEm)/(FL−BDEm))−(FL+ECm) |
|  | 1D | (q+ECm)+((FL*ENm)*(FL+RSm)) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 1D | ((FL*BDEm)/(q+FL))−(ECm/Rm) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | ((PC+BDEm)/PC)/(WF+(Lm/BDEm)) |
|  | 1D | ((FL*BDEm)/(q+FL))−(ECm/Rm) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | ((PC+BDEm)/PC)/(WF+(Lm/BDEm)) |
|  | 4D | (MdLm−Ndsm)/((PC−Hm)−(PC/q)) |
|  | 1D | ((FL*BDEm)/(q+FL))−(ECm/Rm) |
|  | 2D | (ECm+MdLm)/((DC/ECm)+(WF−MdLm)) |
|  | 3D | ((PC+BDEm)/PC)/(WF+(Lm/BDEm)) |
|  | 4D | (MdLm−Ndsm)/((PC−Hm)−(PC/q)) |
|  | 5D | (q+Ndm)/((Lm*ENm)+(WF−MdNm)) |
| 10 | 1D | (WF/(DC+ECm))/(PC+(FL*MdNm)) |
|  | 1D | (WF/(q*ENm))/(PC+(FL*MdNm)) |
|  | 2D | (Ndsm/(FL−PC))/(q+(MdLm/MdNm)) |
|  | 1D | (WF/(DC+ECm))/(PC+(FL*MdNm)) |
|  | 2D | ((DC−PC)/ECm)/((DC*MdNm)−ECm) |
|  | 3D | (Lm+BDEm)/((EIm−Ndsm)−(FL*Ndsm)) |
|  | 1D | (WF/(DC+ECm))/(PC+(FL*MdNm)) |
|  | 2D | ((DC−PC)/ECm)/((ECm/MdNm)−DC) |
|  | 3D | (Lm+BDEm)/((EIm−Ndsm)−(FL*Ndsm)) |
|  | 4D | (Ndm/Lm)/((ECm*MdNm)−(Lm−WF)) |
|  | 1D | (WF/(DC+ECm))/(PC+(FL*MdNm)) |
|  | 2D | ((DC−PC)/ECm)/((DC*MdNm)−ECm) |
|  | 3D | (Lm+BDEm)/((EIm−Ndsm)−(FL*Ndsm)) |
|  | 4D | (Ndsm−WF)/((FL*ECm)−(Ndsm/PC)) |
|  | 5D | (Lm−PC)/((DC+FL)−(Ndm/Hm)) |

Table S6. The selected feature set of the 5D-SISSO model during validation process.

| Iteraction | Selected features |
| --- | --- |
| 01 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, Rm, RDm, Ndm, EIm, RSm |
| 02 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, Rm, RDm, Ndm, EIm |
| 03 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, Rm, RDm, EIm |
| 04 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, Rm, RDm, MdNm |
| 05 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, Rm, Ndm, MdNm |
| 06 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, Lm, EIm, Ndm, RSm |
| 07 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, MdNm, Ndm, RSm |
| 08 | WF, ECm, FL, PC, Hm, BDEm, q, DC, Ndsm, ENm, MdLm, MdNm, Rm, RSm |
| 09 | WF, ECm, FL, PC, Hm, BDEm, q, RDm, Rm, Ndm, MdLm, RSm |
| 10 | WF, ECm, FL, PC, Hm, BDEm, DC, Ndsm, Ndm, MdNm, Lm, EIm |

Table S7. The oxygen vacancy formation energy, Fermi level, and Bader charge for different transition metal-doped metal oxide systems.

| Systems | Ov formation energy (eV) | Fermi level (eV) | Bader charge (¦e¦) |
| --- | --- | --- | --- |
| Hf-ZrO2 (111) | 6.1094 | -0.4305 | 2.7476 |
| Zr-ZrO2 (111) | 6.0785 | -0.4296 | 2.6141 |
| Nb-CoO (100) | 6.0722 | 0.5552 | 2.4339 |
| Re-CoO (100) | 5.2981 | 0.7393 | 2.3891 |
| Ti-NiO (100) | 4.6221 | 0.9726 | 2.0987 |
| Mo-NiO (100) | 4.1152 | 1.0041 | 1.7930 |

Supplementary References

1.   	C. Sutton, M. Boley, L. M. Ghiringhelli, M. Rupp, J. Vreeken and M. Scheffler, Nat. Commun., 2020, 11, 4428.

2.    	T. Kanungo, D. M. Mount, N. S. Netanyahu, C. D. Piatko, R. Silverman and A. Y. Wu, IEEE Trans. Pattern Anal. Mach. Intell., 2002, 24, 881–892.

3.	Z.-K. Han, D. Sarker, R. Ouyang, A. Mazheika, Y. Gao and S. V. Levchenko, Nat. Commun., 2021, 12, 1833.

4.	B. R. Goldsmith, M. Boley, J. Vreeken, M. Scheffler and L. M. Ghiringhelli, New J. Phys., 2017, 19, 013031.