Synthesis and photoluminescence properties of 1D polymer chain based on pre-designed heterometallic Al4Ln4 molecular rings

Qian-Ru Sun,#ab Dan Luo,#a Yaokang LV,c  Wei-Hui Fang*a and Jian Zhang*ab

a State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian 350002, China. Email: fwh@fjirsm.ac.cn; zhj@fjirsm.ac.cn

b School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, P. R. China.

c College of Chemical Engineering and Materials Science, Zhejiang University of

Technology, Hangzhou, 310014, China

# These authors contributed equally to this work.

Content

1. Supplementary Notes	S2

2. Synthesis	S3

3. Supplementary Figures	S5

4. Stability of heterometallic one-dimensional chains	S9

5. PXRD spectra of the 1D polymer chain	S10

6. TGA test for 1D polymer chain	S11

7. FT-IR spectra of heterometallic 1D chains	S12

8. The solid-state absorption spectra of heterometallic 1D chains	S13

9. EDS spectra of heterometallic 1D chains	S13

10. Solid-state emission spectrum	S14

11. Structural drawing showing ADPs	S15

12. Supplementary Tables	S16

13. Determination of the valence state of metals	S19

14. Crystallography data	S25

15. Comparison of optical performance data of clusters	S26

16. Lanthanide-oxygen bond length	S26

17. Reference	S29

# 1. Supplementary Notes

## 1.1 Chemicals and Materials

All the reagents and solvents employed are purchased commercially and used as received without further purification. Aluminum isopropoxide (Al(OiPr)3, ≥98%) was acquired from Aladdin Chemical Reagent Shanghai. N, N-dimethylformamide (DMF, ≥99%) and formic acid (HCOOH, ≥98%) were bought from Sinopharm Chemical Reagent Beijing. N-methyldiethanolamine (H2MDEA, ≥99%) and europium nitrate hexahydrate (Eu(NO3)3·6H2O, ≥99.9%) were purchased from Merck.

## 1.2 Energy dispersive spectroscopies (EDS)

The EDS analyses of single crystals were performed on a JEOL JSM6700F field-emission scanning electron microscope equipped with an Oxford INCA system.

## 1.3 Fourier Transform Infrared (FT-IR) Spectroscopies

FT-IR spectra (KBr pellets) were recorded on an ABB Bomem MB102 spectrometer.

## 1.4 UV-vis spectroscopies

The UV-vis diffuse reflection data were recorded at room temperature using powder samples with BaSO4 as a standard (100% reflectance) on a PerkinElmer Lamda-950 UV spectrophotometer and scanned at 200-800 nm. The absorption data are calculated from the Kubelka-Munk function, (F(R) = (1-R)2/2R), where R represents the reflectance.

## 1.5 Powder X-ray diffractions (PXRD)

PXRD data were collected on a Rigaku Mini Flex II diffractometer using Cu-Kα radiation (λ = 1.54056 Å) under ambient conditions.

## 1.6 Thermogravimetric analyses

The thermogravimetric analyses (TGA) were performed on a Mettler Toledo TGA/SDTA 851e analyzer in a nitrogen atmosphere with a heating rate of 10 ℃/min.

## 1.7 Photoluminescence spectroscopies

The photoluminescence (PL) spectra were finished on the UV/V/NIR Fluorescence Spectrometer (Edinburgh, FLS1000).

## 1.8 Crystal photos

Crystal photos were obtained on an LW500LJT infinite high-definition transmission-reflection metallographic microscope with a 20-megapixel color imaging system.

## 1.9 Drawing softwares

The structural diagrams are plotted using Diamond 4.6.5. The channel simulations were realized by using Mercury 2022.3.0.

## 1.10 General methods for X-ray Crystallography

Crystallographic data were collected on a Rigaku Synergy Custom (Liquid MetalJet D2+) diffractometer with Ga-Kα radiation (λ = 1.3405 Å). The structures were solved with direct methods using OLEX2 and refined by full-matrix least-squares on F2 using SHELXTL. All hydrogen atoms were theoretical hydrogenation, riding on the relevant atoms and refined with fixed thermal factors. Non-hydrogen atoms were refined anisotropically. The obtained crystallographic data for AlOC-195 is summarized in Table S2 and Table S13.

# 2. Synthesis

## 2.1 Synthesis of AlOC-195

A mixture of aluminum isopropoxide (204 mg, 1 mmol), europium nitrate hexahydrate (60 mg, 0.13 mmol), N-methyldiethanolamine (2.5 mL), DMF (2.5 mL) and formic acid(100 μL) was sealed in a 20 mL vial and transferred to a preheated oven at 120 °C for 3 days. When cooled to room temperature, colorless bulk crystals were obtained. (yield: 55% based on Eu(NO3)3·6H2O) The crystals are rinsed with DMF and preserved under a sealed and dry environment. FT-IR (KBr, cm-1): 2963(w), 2883(w), 2848(w), 2360(s), 2330(s), 1572(s), 1448(m), 1364(s), 1299(w), 1247(w), 1097(s). Elemental analysis calcd. (%) for Al4Eu4C48N8O32H96 (MW 2013.08): C 28.64, N 5.57, H 4.77; found C 28.73, N 4.89, H 4.17. When the molar ratio of Ln: Al increased from 0.1: 1 to 0.4: 1, we can still obtain the crystals, while continuously increasing to 1:1 the reaction appears white turbidity and a deterioration in the quality of the crystals. Considering the crystal yield, phase purity and the higher cost of rare earth salt, we therefore chose the ratio of 0.1:1.

Among them, europium nitrate hexahydrate can be replaced by samarium nitrate hexahydrate, gadolinium nitrate hexahydrate, terbium nitrate hexahydrate, dysprosium nitrate hexahydrate, erbium nitrate pentahydrate, thulium nitrate pentahydrate and yttrium nitrate hexahydrate to obtain crystals. Basic information about these crystals is summarized in Table S2 (page S16).

## 2.2 Scale-up synthesis of AlOC-195

A mixture of aluminum isopropoxide (2g, 10 mmol), europium nitrate hexahydrate (600 mg, 1.3 mmol), N-methyldiethanolamine (25 mL), DMF (25 mL) and formic acid(1 mL) was sealed in a 100 mL vial and transferred to a preheated oven at 120 ℃ for 3 days. When cooled to room temperature, colorless bulk crystals were washed with DMF over and over. After sufficient drying in an oven at 80 ℃, the precipitate and crystals are sieved by a 200-mesh sieve, and pure phase crystals (~50μm) can be obtained. (312 mg, yield: 46% based on Eu(NO3)3·6H2O).

## 2.3 Synthesis of AlOC-195 contains two lanthanide metals

A mixture of aluminum isopropoxide (204 mg, 1 mmol), europium nitrate hexahydrate (45 mg, 0.10 mmol), terbium nitrate hexahydrate (15 mg, 0.03 mmol), N-methyldiethanolamine (2.5 mL), DMF (2.5 mL) and formic acid(100 μL) was sealed in a 20 mL vial and transferred to a preheated oven at 120 °C for 3 days. When cooled to room temperature, colorless bulk crystals that exhibit orange-light emission were obtained (Fig. S4). When rare earth nitrates were added in the ratios of europium nitrate hexahydrate: terbium nitrate hexahydrate = 1:1 (Fig. S5) and europium nitrate hexahydrate: terbium nitrate hexahydrate = 1:3 (Fig. S6), colorless crystals which exhibit yellow-light and yellowish-light emission could be obtained, respectively. The crystals are rinsed with DMF and preserved under a sealed and dry environment.

§Crystal data for AlOC-195-Eu: C48H96Al4Eu4N8O32, M= 2013.08, monoc-linic, a = 27.7753(5) Å, b = 10.2408(2) Å, c = 29.8910(6) Å, V = 7510.5 (3) Å3, T = 293(2) K, space group C2/c (I2/a), Z = 4, 31456 reflections measured, 30289 indepen-dent reflections (Rint = 0.0525). The final R1 values were 0.0567 (I > 2σ(I)). The final wR(F2) values were 0.1602 (I > 2σ(I)). The final R1 values were 0.0673 (all data). The final wR(F2) value was 0.1602 (all data). The goodness of fit on F2 was 1.159.

# 3. Supplementary Figures

## 3.1 Synthesis

Fig. S1. Plot of reaction time versus yield for the compound AlOC-195-Eu at a reaction temperature of 120°C (the yield based on the lanthanide reagent).

×10 312mg

×1 37.5mg

Fig. S2. Massive production of AlOC-195-Eu.

Fig. S3. The PXRD of the simulated of AlOC-195-Eu and experimental patterns of AlOC-195-EunTb(4-n).

Fig. S4. The EDS spectrum of compound AlOC-195-Ln (Eu: Tb = 3: 1).

Fig. S5. The EDS spectrum of compound AlOC-195-Ln (Eu: Tb = 1: 1).

Fig. S6. The EDS spectrum of compound AlOC-195-Ln (Eu: Tb = 1: 3).

## 3.2 The detailed structure information for the 1D chain structure

Fig. S7. Dimensions of the building block of compound AlOC-195 (a) total diameter; (b) height; (c) central hole.

Fig. S8. One-step strategy of heterometallic compounds. (a) The generalized modeling of heterometallic eight-membered rings bridged by different carboxylic acids and MDEA2- ligands. Ball-and-stick modeling diagram of the compound (b) AlOC-130 and AlOC-131; (c) AlOC-195. Color codes: Al, green; Ln, orange; C, gray; N, blue; O, red; -L, pink.

Fig. S9. Molecular structures of AlOC-130, AlOC-131 and AlOC-195. Ligands, ball-and-stick, space-filling models and stacking diagrams for compounds (a) AlOC-130 (b) AlOC-131 (c) AlOC-195, respectively, from left to right. Color codes: Al, green; Eu, orange; C, gray; N, blue; O, red.

Fig. S10. Molecular structural of compound AlOC-195-Eu (a) Al3+ coordination conformation; (b) Eu3+ coordination conformation; (c) structure of inorganic core; (d) side view.

Fig. S11. Heterobimetallic structures with aminoalcohols (a) Fe10Ln10; (b) Cr8Ln8; (c) Fe18Ln6; (d) Ln18Co7.

Fig. S12. Stacking diagram of AlOC-195-Eu (a) stacking diagram along the b-axis; (b) distance between 1D chains along the c-axis; (c) correspondence of patterns along the a-axis and the b-axis; (d) pattern viewing along the c-axis. Color code: Al, green; Ln: orange; C, grey; O, red; N, blue.

Fig. S13. Perspective view of the void space in AlOC-195 along the crystallographic axis. (a) a-axis; (b) b-axis; (c) c-axis.

The central cavity of the molecular ring has been highlighted by the red box line. The peanut-shaped cavities formed between the one-dimensional chains by hydrogen bonding are also highlighted with blue box lines.

Fig. S14. Structural diagram of compound AlOC-195 (a) hydrogen bonding within the molecular ring; (b) bridging interaction of formic acid; (c) ball-and-stick modeling diagram of the compound.

# 4. Stability of heterometallic one-dimensional chains

Fig. S15. PXRD patterns of AlOC-195-Eu in different organic solvents at room temperature for 24 h.

The crystals of compound AlOC-195-Eu were immersed in organic solvents for 24h and PXRD experiments were performed. As shown in Supplementary Figure S9, the experimentally obtained patterns agree with the simulated ones indicating that the compounds are stable in organic solutions.

Fig. S16. The Temperature-dependent PXRD patterns of AlOC-195-Eu.

The variable temperature PXRD of compounds AlOC-195-Eu showed that they remained thermally stable until 250 °C (Supplementary Figure S10).

# 5. PXRD spectra of the 1D polymer chain

Fig. S17. Simulated single-crystal PXRD patterns (black) and experimental PXRD patterns (red) of AlOC-195-Eu.

Fig. S18. The PXRD of the simulated of AlOC-195-Eu and experimental patterns of AlOC-195-Ln.

# 6. TGA test for 1D polymer chain

Fig. S19. The TGA curve of AlOC-195-Ln (Ln = Eu, Er, Tb, Dy, Gd, Sm, Tm, Yb).

The thermal stability of AlOC-195-Ln was investigated in N2 atmosphere up to 800 °C with a heating rate of 10 K min-1, which is presented in Fig. S12. There are similar structures and compositions in AlOC-195-Eu to AlOC-195-Yb, so only the TG investigation of AlOC-195-Eu was described in detail. It reveals a weight loss (<5%) between 20 and 100 °C corresponds to the release of guests and unresolved solvent molecules. All heterometallic molecular ring compounds show severe weight loss after 350°C indicating a collapse of the ring skeleton.

# 7. FT-IR spectra of heterometallic 1D chains

Fig. S20. FT-IR spectrum of AlOC-195.

The IR spectra of 1D-chains have been recorded in the range of 4000–400 cm–1 from solid samples palletized with KBr, which are presented in Fig. S17. The substitution of different rare earth elements in the compound AlOC-195-Ln does not affect the peak position and intensity of the functional groups. The incorporation of formic acid in the compound is supported by the C=O vibrations at 1572 cm-1 and 1448 cm-1. And the aliphatic C-H stretching-vibrations of the N-methyldiethanolamine molecular occurs at about 2963 cm-1 and 2880 cm-1.

FT-IR (KBr, cm-1) for AlOC-195-Sm: 2960(w), 2879(w), 2849(w), 2361(s), 2341(s), 1568(s), 1452(m), 1362(s), 1296(w), 1252(w), 1095(s)

FT-IR (KBr, cm-1) for AlOC-195-Gd: 2968(w), 2880(w), 2849(w), 2360(s), 2340(s), 1570(s), 1454(m), 1366(s), 1296(w), 1254(w), 1097(s)

FT-IR (KBr, cm-1) for AlOC-195-Tb: 2964(w), 2881(w), 2848(w), 2363(s), 2341(s), 1570(s), 1452(m), 1365(s), 1296(w), 1254(w), 1097(s)

FT-IR (KBr, cm-1) for AlOC-195-Dy: 2968(w), 2881(w), 2849(w), 2359(s), 2334(s), 1572(s), 1452(m), 1365(s), 1296(w), 1254(w), 1099(s)

FT-IR (KBr, cm-1) for AlOC-195-Er: 2970(w), 2883(w), 2849(w), 2361(s), 2341(s), 1568(s), 1452(m), 1367(s), 1296(w), 1254(w), 1099(s)

FT-IR (KBr, cm-1) for AlOC-195-Tm: 2970(w), 2883(w), 2849(w), 2357(s), 2343(s), 1573(s), 1452(m), 1367(s), 1296(w), 1254(w), 1099(s)

FT-IR (KBr, cm-1) for AlOC-195-Yb: 2970(w), 2885(w), 2850(w), 2370(s), 2345(s), 1576(s), 1452(m), 1367(s), 1296(w), 1254(w), 1101(s)

# 8. The solid-state absorption spectra of heterometallic 1D chains

Fig. S21. The solid-state absorption spectra of AlOC-195-Eu.

UV-vis spectra of colorless crystals AlOC-195-Eu display narrow absorptions ranging from 300 to 350 nm, and the calculated adsorption edges are respectively 3.05 eV for AlOC-195-Eu.

# 9. EDS spectra of heterometallic 1D chains

Fig. S22. The EDS spectrum of compound AlOC-195-Eu.

# 10. Solid-state emission spectrum

Fig. S23. Solid-state emission spectrum of AlOC-130.

Fig. S24. Solid-state emission spectrum of AlOC-131.

# 11. Structural drawing showing ADPs

Fig. S25. Structural drawing showing ADPs of AlOC-195-Ln structures. Thermal ellipsoids are set at 40% probability level. All the hydrogen atoms are omitted for clarity. Color codes: Al, pale blue; Ln, green and pink; C, gray; N, blue; O, red.

# 12. Supplementary Tables

Table S1. The representative clusters contain aluminum and lanthanide metals.

| Compound | Molecular formula | Structural diagram | Reference |
| --- | --- | --- | --- |
| —— | [{Yb4(µ4-O)(µ2-OiPr)2(µ2-Me)4} {(µ2-Me)(µ2-OiPr)AlMe2}4] |  | 1 |
| —— | [Cu12Eu6Al6(µ3-OH)18(OH)12(µ4-O)6((µ3-OH2)6(O2CtBu)18] |  | 2 |
| —— | [Al2Ln3L10(OH)6(H2O)2]Et3NH·H2O (Ln = Tb, Dy; HL = pivalic acid, Et3N = triethylamine) |  | 3, 4 |
| —— | [{Al(H2O)6}{Ln(pda)3}].10H2O (Ln = Sm, Eu, Gd, Tb, Dy and Yb; pda = pyridine2,6-dicarboxylic acid) |  | 5 |
| —— | [Ln(H2O)7{Al(OH)6Mo6O18}]·4H2O (Ln = Pr, Nd, Tb, Dy and Ho) |  | 6 |
| —— | [Ln(H2O)7{Al(OH)6Mo6O18}Ln(H2O)7]{Al(OH)6Mo6O18}·16H2O (Ln = Er, Tm and Lu) |  |  |
| AlOC-13-Ln | [LnAl4(L)4(Cat)2(DMF)2(H2O)3]·Hdma (Ln = Sm, Eu, Gd, Tb, Dy, Ho, Er, Yb; H3L = 2,3-dihydroxybenzoic acid, Cat = catechol, DMF = N, N-dimethylformamide, and dma = dimethylamine) |  | 7 |
| Ce@AlM-4 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA-mNH2)8(H2O)2]·3NO3 (BA = 3-aminobenzoic acid) |  | 8 |
| AlOC-129-Ln | Al9Ce7(BA-mNH2)19(NO3)6(C2H3N)2 (μ2-OH)7(μ3-OH)16·2Py·6(C2H3N) (AlOC-129Ce) |  | 9 |
|  | Al9Pr7(BA-mNH2)18(NO3)6(C2H3N)3(H2O)3(μ2-OH)6(μ3-OH)16·2NO3·1.5Py·5.5C2H3N (AlOC-129Pr) |  |  |
|  | Al9Nd7(BA-mNH2)18(NO3)6 (C2H3N)3(H2O)3(μ2-OH)6(μ3-OH)16·2NO3·C2H3N (AlOC129Nd) |  |  |
| Ce@AlM-1 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·3Cl·X (Ce@AlM-1; BA = benzoate, X = solvent guest molecules) |  | 10 |
| Ce@AlM-2 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·6NO3·2Py·5H2O |  |  |
| Ce@AlM-3 | 5[Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·14.25Cl·4Py |  |  |
| AlOC-130 | Al4Eu4(BA)8(mdea)8 (BA = benzoate acid; mdea = N-methyldiethanolamine) |  | 11 |
| AlOC-131 | [Al4Eu4(IN)8(mdea)8(H2O)]·2H2O (IN = isonicotinic acid; mdea = N-methyldiethanolamine) |  |  |

Table S2. Basic information for AlOC-195-Ln (Ln= Sm, Gd, Tb, Dy, Er, Tm, Yb)

| Molecular formula | Crystal color | Molecular weight | Elemental analysis calcd (%) |  |  | Yielda |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | C | N | H |  |
| Al4Sm4C48N8O32H96 | pale yellow | 2006.67 | 28.85 | 4.91 | 4.17 | 45% |
| Al4Gd4C48N8O32H96 | colorless | 2034.23 | 28.73 | 4.89 | 4.17 | 52% |
| Al4Tb4C48N8O32H96 | colorless | 2040.93 | 28.39 | 4.88 | 4.14 | 45% |
| Al4Dy4C48N8O32H96 | colorless | 2055.23 | 28.34 | 4.80 | 4.09 | 50% |
| Al4Er4C48N8O32H96 | pink | 2074.27 | 28.05 | 4.77 | 4.03 | 57% |
| Al4Tm4C48N8O32H96 | colorless | 2080.97 | 27.95 | 4.75 | 4.03 | 43% |
| Al4Yb4C48N8O32H96 | colorless | 2097.39 | 27.73 | 4.69 | 4.02 | 28% |

- Yield based on Ln(NO3)3·6H2O.

Table S3. Stability of representative Al and Al-Ln octanuclear ring.

| Compound | Molecular formula | Structural diagram | Stability | Reference |
| --- | --- | --- | --- | --- |
| AlOC-1 | Al8(OH)4(BA-mF)12- (OButn)8 |  | Slightly soluble in alcohols | 12 |
| AlOC-58NC | Al8(µ2-OH)4(OBun)8(NH2- IN)12 |  |  | 13 |
| AlOC-59NT | Al8(µ2-OH)8(NH2- IN)16 |  |  |  |
| Ce@AlM-1 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·3Cl·X (Ce@AlM-1; BA = benzoate, X = solvent guest molecules) |  |  | 8 |
| Ce@AlM-2 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·6NO3·2Py·5H2O |  |  | 10 |
| Ce@AlM-3 | 5[Al8Ce(μ2-OH)8(μ3-OH)8(BA)8(H2O)2]·14.25Cl·4Py |  |  |  |
| Ce@AlM-4 | [Al8Ce(μ2-OH)8(μ3-OH)8(BA-mNH2)8(H2O)2]·3NO3 (BA = 3-aminobenzoic acid) |  |  |  |
| AlOC-130 | Al4Eu4(BA)8(mdea)8 (BA = benzoate acid; mdea = N-methyldiethanolamine) |  |  | 11 |
| AlOC-131 | [Al4Eu4(IN)8(mdea)8(H2O)]·2H2O (IN = isonicotinic acid; mdea = N-methyldiethanolamine) |  |  |  |

As shown in the table above, the aluminum oxo clusters without aminoalcohol protection have a sustained and significant weight loss up to 300 ℃, whereas AlOC-130 and AlOC-131 with aminoalcohol ligand protection do not have a large weight loss until above 300 ℃, as in this work. This demonstrates that the protection by the aminoalcohol contributes to the thermal stability of the aluminum-oxo wheel clusters.

Table S4. Crystal Data and Refinement Results of AlOC-195-Ln

| Formula a | Space group | a (Å) | b (Å) | c (Å) | Rint b | CCDC Code |
| --- | --- | --- | --- | --- | --- | --- |
| AlOC-195-Eu | I2/a | 27.7753(5) | 10.2408(2) | 29.8910(6) | 0.0473 | 2326475 |
| AlOC-195-Tb | I2/a | 27.9239(5) | 10.1329(2) | 28.9993(8) | 0.0622 | 2335749 |
| AlOC-195-Sm | I2/a | 27.9072(5) | 10.2096(2) | 29.8833(6) | 0.0571 | 2335748 |
| AlOC-195-Gd | I2/a | 27.5463(7) | 10.2945(2) | 29.7052(8) | 0.0776 | 2335746 |
| AlOC-195-Dy | I2/a | 29.190(9) | 10.2991(3) | 27.6382(6) | 0.1070 | 2335744 |
| AlOC-195-Er | I2/a | 28.9871(8) | 10.1594(3) | 27.5988(7) | 0.0739 | 2335745 |
| AlOC-195-Tm | I2/a | 27.5990(6) | 10.1083(3) | 28.8433(8) | 0.0917 | 2335750 |
| AlOC-195-Yb | I2/a | 27.0334(3) | 10.3342(1) | 29.5968(4) | 0.0761 | 2336986 |

[AlOC-195-Ln] = [Al4Eu4(FAchelating)6(FAbridging)2(MDEA)8]. b. The structures were solved with the dual-direct methods using ShelxT and refined with the full-matrix least-squares technique based on F2 using the SHELXL-2014 program through olex2-1.2 software.

# 13. Determination of the valence state of metals

Table S5. ICP analysis for porous materials.

|  |  | AlOC-195-Eu |
| --- | --- | --- |
| Wt% | Exp. | Al:4.18% Eu:18.48% |
|  | Cal. | Al:5.36% Eu:30.18% |
| Al: M | Exp. | 0.226 |
|  | Cal. | 0.178 |
| (M = Eu for AlOC-195) |  |  |

Table S6. BVS analysis for AlOC-195-Sm.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.0529 | Al03- | O005 | 1.872(5) | Al04 3.0950 | Al04- | O0061 | 1.867(6) |
|  | Al03- | O007 | 1.878(6) |  | Al04- | O00A | 1.985(7) |
|  | Al03- | O008 | 1.963(7) |  | Al04- | O00B | 1.858(6) |
|  | Al03- | O00H | 1.863(6) |  | Al04- | O00C | 1.934(6) |
|  | Al03- | O00K1 | 1.875(7) |  | Al04- | O00E | 1.852(6) |
|  | Al03- | O00M | 1.923(7) |  | Al04- | O00F | 1.857(6) |
| Sm01 3.1297 | Sm01- | O007 | 2.387(6) | Sm02 3.1455 | Sm02- | O0051 | 2.409(5) |
|  | Sm01- | O009 | 2.438(6) |  | Sm02- | O0061 | 2.404(6) |
|  | Sm01- | O00B | 2.356(6) |  | Sm02- | O00F | 2.322(5) |
|  | Sm01- | O00D | 2.418(5) |  | Sm02- | O00G | 2.443(6) |
|  | Sm01- | O00E | 2.345(5) |  | Sm02- | O00I2 | 2.352(6) |
|  | Sm01- | O00H | 2.350(5) |  | Sm02- | N00J1 | 2.676(7) |
|  | Sm01- | N00L | 2.658(7) |  | Sm02- | O00K | 2.375(6) |
|  | Sm01- | N00N | 2.720(8) |  | Sm02- | N00O | 2.680(7) |
| System code:13/2-X, +Y, 1-Z; 21/2+X, 1-Y, +Z. |  |  |  |  |  |  |  |

Table S7. BVS analysis for AlOC-195-Eu.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.0732 | Al03- | O0073 | 1.876(7) | Al04 3.0694 | Al04- | O005 | 1.867(7) |
|  | Al03- | O008 | 1.972(9) |  | Al04- | O009 | 1.854(9) |
|  | Al03- | O00A | 1.863(8) |  | Al04- | O00C | 1.867(8) |
|  | Al03- | O00E | 1.863(8) |  | Al04- | O00D | 1.974(9) |
|  | Al03- | O00I3 | 1.858(9) |  | Al04- | O00J | 1.943(9) |
|  | Al03- | O1 | 1.927(1) |  | Al04- | O00K | 1.859(9) |
| Eu01 3.1103 | Eu01- | O006 | 2.423(7) | Eu02 3.0441 | Eu02- | O0052 | 2.393(7) |
|  | Eu01- | O009 | 2.353(7) |  | Eu02- | O0072 | 2.398(7) |
|  | Eu01- | O00A | 2.391(8) |  | Eu02- | O00G | 2.329(8) |
|  | Eu01- | O00B | 2.395(8) |  | Eu02- | O00H2 | 2.432(8) |
|  | Eu01- | O00C | 2.351(8) |  | Eu02- | O00I2 | 2.365(8) |
|  | Eu01- | O00E | 2.320(7) |  | Eu02- | O00K2 | 2.325(7) |
|  | Eu01- | N00L | 2.642(9) |  | Eu02- | N00F2 | 2.668(8) |
|  | Eu01- | N00N | 2.642(9) |  | Eu02- | N00M2 | 2.685(1) |
| System code: 11-X, 1-Y, 1-Z; 21/2+X, 1-Y, +Z; 31/2-X, +Y, 1-Z. |  |  |  |  |  |  |  |

Table S8. BVS analysis for AlOC-195-Gd.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.1267 | Al03- | O006 | 1.868(6) | Al04 3.0940 | Al04- | O0051 | 1.877(6) |
|  | Al03- | O00C | 1.976(7) |  | Al04- | O00A | 1.987(8) |
|  | Al03- | O00D | 1.842(7) |  | Al04- | O00B | 1.868(7) |
|  | Al03- | O00G | 1.854(7) |  | Al04- | O00F | 1.841(7) |
|  | Al03- | O00I | 1.947(7) |  | Al04- | O00L1 | 1.854(8) |
|  | Al03- | O00J | 1.842(7) |  | Al04- | O00N | 1.922(8) |
| Gd01 2.9754 | Gd01- | O005 | 2.381(6) | Gd02 2.9536 | Gd02- | O007 | 2.393(6) |
|  | Gd01- | O006 | 2.374(6) |  | Gd02- | O008 | 2.388(6) |
|  | Gd01- | O0092 | 2.328(7) |  | Gd02- | O00B | 2.374(7) |
|  | Gd01- | O00E | 2.408(6) |  | Gd02- | O00D | 2.335(6) |
|  | Gd01- | O00J | 2.285(7) |  | Gd02- | O00F | 2.312(6) |
|  | Gd01- | O00L | 2.331(7) |  | Gd02- | O00G | 2.320(6) |
|  | Gd01- | N00H | 2.646(7) |  | Gd02- | N00K | 2.640(8) |
|  | Gd01- | N00O | 2.685(9) |  | Gd02- | N00M | 2.690(8) |
| System code: 11/2-X, +Y, 1-Z; 2-1/2+X, 1-Y, +Z. |  |  |  |  |  |  |  |

Table S9. BVS analysis for AlOC-195-Tb.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.1052 | Al03- | O0062 | 1.851(6) | Al04 3.0595 | Al04- | O005 | 1.887(6) |
|  | Al03- | O007 | 1.856(6) |  | Al04- | O0082 | 1.865(6) |
|  | Al03- | O00B | 1.866(6) |  | Al04- | O00A | 1.853(7) |
|  | Al03- | O00C | 1.842(6) |  | Al04- | O00D | 1.846(6) |
|  | Al03- | O00H | 1.971(7) |  | Al04- | O00G | 1.989(7) |
|  | Al03- | O00J | 1.963(7) |  | Al04- | O00K | 1.940(7) |
| Tb01 3.0615 | Tb01- | O005 | 2.341(6) | Tb02 3.0327 | Tb02- | O006 | 2.343(5) |
|  | Tb01- | O0091 | 2.317(5) |  | Tb02- | O0072 | 2.322(6) |
|  | Tb01- | O00A | 2.334(6) |  | Tb02- | O0082 | 2.358(6) |
|  | Tb01- | O00B | 2.400(6) |  | Tb02- | O00D | 2.279(6) |
|  | Tb01- | O00C | 2.266(6) |  | Tb02- | O00E2 | 2.371(6) |
|  | Tb01- | O00F | 2.371(6) |  | Tb02- | O00I | 2.385(6) |
|  | Tb01- | N00L | 2.646(7) |  | Tb02- | N00M | 2.688(8) |
|  | Tb01- | N00N | 2.707(8) |  | Tb02- | N00O2 | 2.652(8) |
| System code: 11-X, 1-Y, 1-Z; 21/2+X, 1-Y, +Z; 31/2-X, +Y, 1-Z. |  |  |  |  |  |  |  |

Table S10. BVS analysis for AlOC-195-Dy.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.0680 | Al03- | O05 | 1.866(6) | Al04 3.0567 | Al04- | O006 | 1.877(7) |
|  | Al03- | O007 | 1.866(7) |  | Al04- | O009 | 1.860(8) |
|  | Al03- | O0082 | 1.860(7) |  | Al04- | O00B2 | 1.874(7) |
|  | Al03- | O00A | 1.846(7) |  | Al04- | O00F | 1.846(7) |
|  | Al03- | O00H | 1.977(8) |  | Al04- | O00G | 1.986(8) |
|  | Al03- | O00I | 1.954(8) |  | Al04- | O00M | 1.932(8) |
| Dy01 3.0111 | Dy01- | O05 | 2.389(6) | Dy02 3.0666 | Dy02- | O0072 | 2.299(6) |
|  | Dy01- | O006 | 2.344(6) |  | Dy02- | O008 | 2.315(6) |
|  | Dy01- | O009 | 2.322(6) |  | Dy02- | O00B2 | 2.342(6) |
|  | Dy01- | O00A | 2.266(6) |  | Dy02- | O00D2 | 2.363(7) |
|  | Dy01- | O00C | 2.373(7) |  | Dy02- | O00F | 2.267(7) |
|  | Dy01- | O00E1 | 2.303(6) |  | Dy02- | O00K | 2.366(7) |
|  | Dy01- | N00J | 2.642(8) |  | Dy02- | N00N | 2.696(9) |
|  | Dy01- | N00L | 2.708(9) |  | Dy02- | N00O2 | 2.641(10) |
| System code: 11/2-X, 3/2-Y, 1/2-Z; 21/2-X, +Y, 1-Z. |  |  |  |  |  |  |  |

Table S11. BVS analysis for AlOC-195-Er.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.0716 | Al03- | O005 | 1.873(6) | Al04 3.0716 | Al04- | O006 | 1.877(7) |
|  | Al03- | O0072 | 1.856(7) |  | Al04- | O008 | 1.852(7) |
|  | Al03- | O00B | 1.859(7) |  | Al04- | O009 | 1.977(7) |
|  | Al03- | O00C | 1.971(8) |  | Al04- | O00A2 | 1.867(7) |
|  | Al03- | O00D | 1.852(7) |  | Al04- | O00G | 1.851(7) |
|  | Al03- | O00I | 1.954(8) |  | Al04- | O00K | 1.940(7) |
| Er01 3.0293 | Er01- | O005 | 2.361(6) | Er02 3.0250 | Er02- | O007 | 2.309(6) |
|  | Er01- | O006 | 2.312(6) |  | Er02- | O008 | 2.252(7) |
|  | Er01- | O00D | 2.238(6) |  | Er02- | O00A2 | 2.329(6) |
|  | Er01- | O00E1 | 2.277(6) |  | Er02- | O00B2 | 2.277(7) |
|  | Er01- | O00G | 2.299(6) |  | Er02- | O00F2 | 2.327(6) |
|  | Er01- | O00H | 2.333(7) |  | Er02- | O00J | 2.334(6) |
|  | Er01- | N00L | 2.632(8) |  | Er02- | N00N | 2.681(9) |
|  | Er01- | N00M | 2.682(9) |  | Er02- | N00O2 | 2.619(9) |
| System code: 13/2-X, 3/2-Y, 3/2-Z; 23/2-X, +Y, 1-Z. |  |  |  |  |  |  |  |

Table S12. BVS analysis for AlOC-195-Tm.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.0964 | Al03- | O006 | 1.864(8) | Al04 3.1093 | Al04- | O008 | 1.985(9) |
|  | Al03- | O007 | 1.853(8) |  | Al04- | O0091 | 1.879(8) |
|  | Al03- | O00A | 1.988(9) |  | Al04- | O00G | 1.880(8) |
|  | Al03- | O00D | 1.942(9) |  | Al04- | O00J1 | 1.843(10) |
|  | Al03- | O00E | 1.854(8) |  | Al04- | O00K | 1.824(8) |
|  | Al03- | O00F | 1.849(8) |  | Al04- | O00L | 1.932(10) |
| Tm01 3.0549 | Tm01- | O005 | 2.310(7) | Tm02 2.9586 | Tm02- | O006 | 2.332(7) |
|  | Tm01- | O007 | 2.279(7) |  | Tm02- | O009 | 2.319(7) |
|  | Tm01- | O00C | 2.318(7) |  | Tm02- | O00B2 | 2.265(8) |
|  | Tm01- | O00E | 2.255(8) |  | Tm02- | O00F | 2.225(8) |
|  | Tm01- | O00G | 2.313(8) |  | Tm02- | O00H | 2.345(8) |
|  | Tm01- | O00K | 2.267(7) |  | Tm02- | O00J | 2.318(8) |
|  | Tm01- | N00M | 2.589(9) |  | Tm02- | N00I | 2.618(8) |
|  | Tm01- | N00N | 2.657(10) |  | Tm02- | N00O | 2.681(11) |
| System code: 11/2-X, +Y, 1-Z; 2-1/2+X, 1-Y, +Z. |  |  |  |  |  |  |  |

Table S13. BVS analysis for AlOC-195-Yb.

| BVS Value | Bond distance |  |  | BVS Value | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al03 3.1134 | Al03- | O006 | 1.857(8) | Al04 3.0707 | Al04- | O0051 | 1.875(8) |
|  | Al03- | O007 | 1.842(9) |  | Al04- | O008 | 1.886(8) |
|  | Al03- | O00D | 1.983(9) |  | Al04- | O00A | 1.984(10) |
|  | Al03- | O00E1 | 1.857(9) |  | Al04- | O00C | 1.841(9) |
|  | Al03- | O00F | 1.860(9) |  | Al04- | O00L | 1.847(11) |
|  | Al03- | O00H | 1.938(10) |  | Al04- | O00M | 1.935(11) |
| Yb01 3.0796 | Yb01- | O007 | 2.272(7) | Yb02 2.9661 | Yb02- | O0051 | 2.310(8) |
|  | Yb01- | O008 | 2.316(8) |  | Yb02- | O0061 | 2.328(8) |
|  | Yb01- | O009 | 2.306(8) |  | Yb02- | O00E | 2.212(8) |
|  | Yb01- | O00B | 2.305(8) |  | Yb02- | O00G2 | 2.259(8) |
|  | Yb01- | O00C | 2.225(8) |  | Yb02- | O00I1 | 2.333(9) |
|  | Yb01- | O00F | 2.238(8) |  | Yb02- | O00L | 2.280(9) |
|  | Yb01- | N00K | 2.585(10) |  | Yb02- | N00J1 | 2.614(9) |
|  | Yb01- | N00O | 2.639(11) |  | Yb02- | N00N | 2.680(11) |
| System code: 11/2-X, +Y, 1-Z; 21-X, 1-Y, 1-Z. |  |  |  |  |  |  |  |

# 14. Crystallography data

Table S14. Experimental single-crystal X-ray data for AlOC-130, AlOC-13114 and AlOC-195-Eu.

|  | AlOC-130 |  |  | AlOC-131 |  | AlOC-195-Eu |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Empirical formula | Al4Eu4C96N8O32H128 |  |  | Al4Eu4C88N16O35H126 |  | Al4Eu4C48N8O32H96 |  |
| Formula weight | 2621.85 |  |  | 2683.81 | 2013.08 |  |
| Temperature / k |  | 100.01(10) |  | 100.01(10) | 99.99(13) |  |
| Crystal system |  | tetragonal |  | monoclinic | monoclinic |  |
| Space group | P-421c |  |  | P21/n | I2/a |  |
| a [Å] | 23.3687(10) |  |  | 18.9563(2) | 27.7753 (5) |  |
| b [Å] | 23.3687(10) |  |  | 21.8313(2) | 10.2408 (2) |  |
| c [Å] | 9.8818(10) |  |  | 27.7034(4) | 29.8910 (6) |  |
| α [◦] | 90 |  |  | 90 | 90 |  |
| β [◦] | 90 |  |  | 93.1440(10) | 117.95(3) |  |
| γ [◦] | 90 |  |  | 90 | 90 |  |
| V [Å 3] | 5396.41(7) |  |  | 11447.5(2) | 7510.5(3) |  |
| Z | 2 |  |  | 2 | 4 |  |
| ρcalcd [g cm-3] | 1.599 |  |  | 1.553 | 1.780 |  |
| μ [mm-1] | 12.916 |  |  | 12.213 | 17.957 |  |
| F (000) | 2592.0 |  |  | 5373.0 | 4000.0 |  |
| Index ranges | -30≤ h ≤ 30 |  |  | -24 ≤ h ≤ 24 | -27 ≤ h ≤ 36 |  |
|  | -30 ≤ k ≤ 29 |  |  | -28 ≤ k ≤ 28 | -12 ≤ k ≤ 13 |  |
|  | -12 ≤ l ≤ 12 |  |  | -34 ≤ l ≤ 36 | -38 ≤ l ≤ 36 |  |
| Reflections collected | 44962 |  |  | 93223 | 29888 |  |
| Independent refs [Rint] |  | 5993 [0.0674] |  | 25769[0.0458] | 8237 [0.0517] |  |
| date/restraints/parameters |  |  | 5993/49/337 | 25769/61/1447 | 8237/80/463 |  |
| Goodness-of-fit on F2 | 1.051 |  |  | 1.110 | 1.039 |  |
| R1, wR2 [I>2σ(I)] | 0.0386, 0.0985 |  |  | 0.0592, 0.1145 | 0.0473, 0.1077 |  |
| R1, wR2 [all data] | 0.0422, 0.1009 |  |  | 0.0719, 0.1184 | 0.0584, 0.1130 |  |

# 15. Comparison of optical performance data of clusters

Table S15. Quantum yields and lifetimes for reported Al-Ln(III) clusters

| Al-Ln(Ⅲ) clusters | QY (%) | Lifetime (ms) | Reference |
| --- | --- | --- | --- |
| Al4Eu4(FAchelating)6(FAbridging)2(MDEA)8 | 30.41 | 0.926 | This work |
| Al4Tb4(FAchelating)6(FAbridging)2(MDEA)8 | 41.44 | 2.050 | This work |
| [Al3(Mq)4(HMq)(μ3-OH)2(μ-OH)3{Eu(hfac)3}2] | 5.2 | 0.0000125 | 14 |
| {[TbAl4(L)4(Cat)2(DMF)2(H2O)3]·Hdma}n | 2.31 | 0.3755 | 7 |

Table S16. Quantum yields and lifetimes for reported Eu(III) clusters

| Eu(Ⅲ) clusters | QY (%) | Lifetime (ms) | Reference |
| --- | --- | --- | --- |
| Al4Eu4(FAchelating)6(FAbridging)2(MDEA)8 | 30.41 | 0.926 | This work |
| Eu4(heda)6(Hheda)2Cl2]Cl4 | 7.27 | 0.23 | 15 |
| [Eu6O(OH)8(NO3)6(H2O)12]·2NO3·2H2O | 7.6(7) | 0.19(2)-0.22(2) | 16 |
| [Eu9(L1)3(HL1)2(μ3-OH)4(OAc)10] | 7.2 | 0.0056 | 17 |
| [{Eu15(μ3-OH)20(PepCO2)10(DBM)10Cl}Cl4] | 16(1) | N/A | 18 |

Table S17. Quantum yields and lifetimes for reported Tb(III) clusters

| Tb(Ⅲ) clusters | QY (%) |  | Lifetime (ms) |  | Reference |  |
| --- | --- | --- | --- | --- | --- | --- |
| Al4Tb4(FAchelating)6(FAbridging)2(MDEA)8 | 41.44 |  | 2.050 |  | This work |  |
| Tb5(H2O)(OH)4(NO3)3(BZA)4L·CH3OH |  | 11.13 |  | N/A |  | 19 |  |
| [Tb6O(OH)8(NO3)6(H2O)12]·2NO3·2H2O |  | 29(3) |  | 0.74(7) |  | 16 |  |
| [Tb6(heda)10(µ-OH)2]Cl6·2H2O |  | 30.09 |  | 1.17 |  | 15 |  |
| [Tb6(μ3-F)8(piv)10(Hpiv)4DMF]·xDMF·yH2O |  | 99.6 |  | 2.03 |  | 20 |  |
| [Tb9(L1)3(HL1)2(μ3-OH)4(OAc)10] |  | 21.3 |  | 0.108 |  | 17 |  |
| [Tb9(methyl 4-methylsalicylate)16(μ-OH)10]+NO3- |  | 57 |  | 0.815 |  | 21 |  |
| [Tb9(methyl 5-methylsalicylate)16(μ-OH)10]+NO3− |  | 16 |  | 0.190 |  |  |  |
| [Tb9(methylsalicylate)16(μ-OH)10]+NO3− |  | 17 |  | 0.264 |  |  |  |
| [{Tb15(μ3-OH)20(PepCO2)10(DBM)10Cl}Cl4] |  | <3 |  | N/A |  | 18 |  |

# 16. Lanthanide-oxygen bond length

Table S18. Sm-O bond length for AlOC-195-Sm.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Sm01- | O007 | 2.387(6) | Sm02- | O0051 | 2.409(5) |
| Sm01- | O009 | 2.438(6) | Sm02- | O0061 | 2.404(6) |
| Sm01- | O00B | 2.356(6) | Sm02- | O00F | 2.322(5) |
| Sm01- | O00D | 2.418(5) | Sm02- | O00G | 2.443(6) |
| Sm01- | O00E | 2.345(5) | Sm02- | O00I2 | 2.352(6) |
| Sm01- | O00H | 2.350(5) | Sm02- | O00K | 2.375(6) |
| Sm01- | N00L | 2.658(7) | Sm02- | N00J1 | 2.676(7) |
| Sm01- | N00N | 2.720(8) | Sm02- | N00O | 2.680(7) |

Table S19. Eu-O bond length for AlOC-195-Eu.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Eu01- | O006 | 2.423(7) | Eu02- | O0052 | 2.393(7) |
| Eu01- | O009 | 2.353(7) | Eu02- | O0072 | 2.398(7) |
| Eu01- | O00A | 2.391(8) | Eu02- | O00G | 2.329(8) |
| Eu01- | O00B | 2.395(8) | Eu02- | O00H2 | 2.432(8) |
| Eu01- | O00C | 2.351(8) | Eu02- | O00I2 | 2.365(8) |
| Eu01- | O00E | 2.320(7) | Eu02- | O00K2 | 2.325(7) |
| Eu01- | N00L | 2.642(9) | Eu02- | N00F2 | 2.668(8) |
| Eu01- | N00N | 2.642(9) | Eu02- | N00M2 | 2.685(1) |

Table S20. Gd-O bond length for AlOC-195-Gd.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Gd01- | O005 | 2.381(6) | Gd02- | O007 | 2.393(6) |
| Gd01- | O006 | 2.374(6) | Gd02- | O008 | 2.388(6) |
| Gd01- | O0092 | 2.328(7) | Gd02- | O00B | 2.374(7) |
| Gd01- | O00E | 2.408(6) | Gd02- | O00D | 2.335(6) |
| Gd01- | O00J | 2.285(7) | Gd02- | O00F | 2.312(6) |
| Gd01- | O00L | 2.331(7) | Gd02- | O00G | 2.320(6) |
| Gd01- | N00H | 2.646(7) | Gd02- | N00K | 2.640(8) |
| Gd01- | N00O | 2.685(9) | Gd02- | N00M | 2.690(8) |

Table S21. Tb-O bond length for AlOC-195-Tb.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Tb01- | O005 | 2.341(6) | Tb02- | O006 | 2.343(5) |
| Tb01- | O0091 | 2.317(5) | Tb02- | O0072 | 2.322(6) |
| Tb01- | O00A | 2.334(6) | Tb02- | O0082 | 2.358(6) |
| Tb01- | O00B | 2.400(6) | Tb02- | O00D | 2.279(6) |
| Tb01- | O00C | 2.266(6) | Tb02- | O00E2 | 2.371(6) |
| Tb01- | O00F | 2.371(6) | Tb02- | O00I | 2.385(6) |
| Tb01- | N00L | 2.646(7) | Tb02- | N00M | 2.688(8) |
| Tb01- | N00N | 2.707(8) | Tb02- | N00O2 | 2.652(8) |

Table S22. Dy-O bond length for AlOC-195-Dy.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Dy01- | O05 | 2.389(6) | Dy02- | O0072 | 2.299(6) |
| Dy01- | O006 | 2.344(6) | Dy02- | O008 | 2.315(6) |
| Dy01- | O009 | 2.322(6) | Dy02- | O00B2 | 2.342(6) |
| Dy01- | O00A | 2.266(6) | Dy02- | O00D2 | 2.363(7) |
| Dy01- | O00C | 2.373(7) | Dy02- | O00F | 2.267(7) |
| Dy01- | O00E1 | 2.303(6) | Dy02- | O00K | 2.366(7) |
| Dy01- | N00J | 2.642(8) | Dy02- | N00N | 2.696(9) |
| Dy01- | N00L | 2.708(9) | Dy02- | N00O2 | 2.641(10) |

Table S23. Er-O bond length for AlOC-195-Er.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Er01- | O005 | 2.361(6) | Er02- | O007 | 2.309(6) |
| Er01- | O006 | 2.312(6) | Er02- | O008 | 2.252(7) |
| Er01- | O00D | 2.238(6) | Er02- | O00A2 | 2.329(6) |
| Er01- | O00E1 | 2.277(6) | Er02- | O00B2 | 2.277(7) |
| Er01- | O00G | 2.299(6) | Er02- | O00F2 | 2.327(6) |
| Er01- | O00H | 2.333(7) | Er02- | O00J | 2.334(6) |
| Er01- | N00L | 2.632(8) | Er02- | N00N | 2.681(9) |
| Er01- | N00M | 2.682(9) | Er02- | N00O2 | 2.619(9) |

Table S24. Tm-O bond length for AlOC-195-Tm.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Tm01- | O005 | 2.310(7) | Tm02- | O006 | 2.332(7) |
| Tm01- | O007 | 2.279(7) | Tm02- | O009 | 2.319(7) |
| Tm01- | O00C | 2.318(7) | Tm02- | O00B2 | 2.265(8) |
| Tm01- | O00E | 2.255(8) | Tm02- | O00F | 2.225(8) |
| Tm01- | O00G | 2.313(8) | Tm02- | O00H | 2.345(8) |
| Tm01- | O00K | 2.267(7) | Tm02- | O00J | 2.318(8) |
| Tm01- | N00M | 2.589(9) | Tm02- | N00I | 2.618(8) |
| Tm01- | N00N | 2.657(10) | Tm02- | N00O | 2.681(11) |

Table S25. Yb-O bond length for AlOC-195-Yb.

| Bond distance |  |  | Bond distance |  |  |
| --- | --- | --- | --- | --- | --- |
| Yb01- | O007 | 2.272(7) | Yb02- | O0051 | 2.310(8) |
| Yb01- | O008 | 2.316(8) | Yb02- | O0061 | 2.328(8) |
| Yb01- | O009 | 2.306(8) | Yb02- | O00E | 2.212(8) |
| Yb01- | O00B | 2.305(8) | Yb02- | O00G2 | 2.259(8) |
| Yb01- | O00C | 2.225(8) | Yb02- | O00I1 | 2.333(9) |
| Yb01- | O00F | 2.238(8) | Yb02- | O00L | 2.280(9) |
| Yb01- | N00K | 2.585(10) | Yb02- | N00J1 | 2.614(9) |
| Yb01- | N00O | 2.639(11) | Yb02- | N00N | 2.680(11) |

# 17. Reference

1.	S. Liu, P. Wei, Y. Wang, E. Santillan-Jimenez, I. I. R. C. Bakus and D. A. Atwood, Main Group Chem., 2005, 4, 3-10.

2.	M. A. Palacios, E. Moreno Pineda, S. Sanz, R. Inglis, M. B. Pitak, S. J. Coles, M. Evangelisti, H. Nojiri, C. Heesing, E. K. Brechin, J. Schnack and R. E. P. Winpenny, ChemPhysChem, 2015, 17, 55-60.

3.	X.-Q. Zhao, S. Xiang, J. Wang, D.-X. Bao and Y.-C. Li, ChemistryOpen, 2018, 7, 192-200.

4.	X.-Q. Zhao, J. Wang, F.-H. Zhang, M.-M. Sun, Y.-C. Li, M.-M. Wang and Y.-F. Tang, Polyhedron, 2020, 179.

5.	D. Kumar, S. Tewari, M. Adnan, S. Ahmad, G. Vijaya Prakash and A. Ramanan, Inorg. Chim. Acta, 2019, 487, 81-91.

6.	S. Tewari, M. Adnan, Balendra, V. Kumar, G. Jangra, G. V. Prakash and A. Ramanan, Front. Chem., 2019, 6.

7.	S.-T. Wang, S.-H. Zhang, W.-H. Fang and J. Zhang, Inorg. Chem., 2020, 59, 13760-13766.

8.	X. Chen, Y.-F. Sun, X. Wu, S. Shi, Z. Wang, J. Zhang, W.-H. Fang and W. Huang, Adv. Mater., 2023, 35, 2306260.

9.	X.-Y. Liu, Y. Yu, Y.-F. Sun, W.-H. Fang and J. Zhang, Polyoxometalates, 2023, 2.

10.	Y.-F. Sun, Y.-J. Liu, S.-T. Wang, X.-Y. Liu, C. Ma, W.-H. Fang and J. Zhang, Sci. China: Chem., 2023, 66, 1384-1393.

11.	D. Luo, C.-H. Liu, Y.-B. Chen, S.-T. Wang, W.-H. Fang and J. Zhang, Adv. Sci., 2024, 11, 2305833.

12.	L. Geng, C.-H. Liu, S.-T. Wang, W.-H. Fang and J. Zhang, Angew. Chem. Int. Ed., 2020, 59, 16735-16740.

13.	D. Luo, H. Xiao, M.-Y. Zhang, S.-D. Li, L. He, H. Lv, C.-S. Li, Q.-P. Lin, W.-H. Fang and J. Zhang, Chem. Sci., 2023, 14, 5396-5404.

14.	H.-B. Xu, X.-M. Chen, Q.-S. Zhang, L.-Y. Zhang and Z.-N. Chen, Chem. Commun., 2009, 7318-7320.

15.	L.-l. Yang, J. Zhou, H.-H. Zou, F. Hu and J.-W. Zhao, Inorg. Chim. Acta, 2020, 499.

16.	F. Le Natur, G. Calvez, J.-P. Guégan, L. Le Pollès, X. Trivelli, K. Bernot, C. Daiguebonne, C. Neaime, K. Costuas, F. Grasset and O. Guillou, Inorg. Chem., 2015, 54, 6043-6054.

17.	G.-R. Fu, B.-N. Li, J.-H. Guo, L. Liu, K.-M. Zhang, W.-X. Feng and X.-Q. Lü, Cryst. Growth Des., 2018, 18, 1020-1029.

18.	D. T. Thielemann, A. T. Wagner, E. Rösch, D. K. Kölmel, J. G. Heck, B. Rudat, M. Neumaier, C. Feldmann, U. Schepers, S. Bräse and P. W. Roesky, J. Am. Chem. Soc., 2013, 135, 7454-7457.

19.	G. Wang, Y. Wei and K. Wu, Dalton Trans., 2016, 45, 12734-12738.

20.	B.-K. Ling, J. Li, Y.-Q. Zhai, H.-K. Hsu, Y.-T. Chan, W.-P. Chen, T. Han and Y.-Z. Zheng, Chem. Commun., 2020, 56, 9130-9133.

21.	S. Omagari, T. Nakanishi, T. Seki, Y. Kitagawa, Y. Takahata, K. Fushimi, H. Ito and Y. Hasegawa, J. Phys. Chem. A, 2015, 119, 1943-1947.