Supplementary Information

Enhanced ferromagnetism, perpendicular magnetic anisotropy and high Curie temperature in the van der Waals semiconductor CrSeBr through strain and doping

Ruilin Han,*a Xiaomin Xue,b and Peng Lia

a  School of Physics and Electronic Engineering, Shanxi University, Taiyuan 030006, China

b  Institute of Theoretical Physics, Shanxi University, Taiyuan, 030006, China

*E-mail: hanruilin0116@sxu.edu.cn.

Table S1. Calculated in-plane lattice constants, bond lengths and bond angles of the CrSeBr monolayer.

| Pristine | a(Å) | b(Å) | θ1() | θ2() | θ3() | d1(Å) | d2(Å) | d3(Å) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CrSeBr | 3.678 | 5.118 | 92.24 | 92.04 | 96.99 | 3.678 | 2.556 | 2.552 |

Figure S1. (a) Total and atomic MAE in which the magnetic moments of the pristine CrSeBr monolayer are aligned along the [100], [010], [011], [101], [111], and [110] directions (with respect to the [001] direction); (b) magnetic (specific) heat capacity as a function of temperature for the pristine CrSeBr monolayer.

Figure S2. Orbital-resolved projected DOSs of (a) the Se-p orbitals and (b) the Br-p orbitals for the pristine monolayer CrSeBr. Orbital-projected contribution to the MAE for the Se atom with spin orientation along the (c) [100] and (d) [010] directions, and for the Br atom with spin orientation along the (e) [100] and (f) [010] directions for the pristine CrSeBr monolayer.

Figure S3. Spin-polarized total DOS, projected DOS of the d orbitals of the Cr atom, projected DOS of the p orbitals of the Se atom, and projected DOS of the p orbitals of the Br atom for the (a) pristine CrSeBr monolayer, (b) strained monolayer, and (c) monolayer doped with carriers.

Figure S4.  The total MAE and Cr, Se, and Br atomic-layer-resolved MAE in some special directions for the CrSeBr monolayer under 8% tensile strain.

Figure S5. (a) d orbital-resolved MAE of the Cr, p orbital-resolved MAE of the (b) Se and (c) Br atoms for the CrSeBr monolayer with a hole doping concentration of 0.7 holes/u.c. when the magnetization is along the [100] direction.