Based on T.E.S.T Toxicity Prediction and Machine Learning to Forecast Toxicity Dynamics in the Photocatalytic Degradation of Tetracycline

Kaihang Liua†, Wenhui Nia†, Qiaoyu Zhanga†, Xu Huangc, Tao Luob,c,d *, Jian Huangb,c,d, Hua Zhangb,c,d, Yong Zhangb,c,d, Fumin Penga, *

a School of Chemistry and Chemical Engineering, Anhui University, Hefei, Anhui 230039, PR China.

b Anhui Institute of Ecological Civilization, Anhui Jianzhu University, Hefei, Anhui 230601, PR China

c Anhui Provincial Key Laboratory of Environmental Pollution Control and Resource Reuse, Anhui Jianzhu University, Hefei, Anhui 230601, PR China.

d Pollution Control and Resource Utilization in Industrial Parks Joint Laboratory of Anhui Province, Anhui Jianzhu University, Hefei, Anhui 230601, PR China.

* Corresponding author E-mail:

luotao_edu@163.com (Tao Luo)

08007@ahu.edu.cn (Fumin Peng)

† These authors contributed equally to this work.

Text. S1. Catalysts characterization

The XRD pattern of the purchased P25 catalyst is displayed in Fig. S1., revealing characteristic peaks (PDF 21-1272) of anatase at 2θ = 25.3° (101), 2θ = 48.0° (200), and others. Similarly, the characteristic peaks of rutile (PDF 21-1276) were observed at 2θ = 27.4° (110), 2θ = 36.1° (101), and so forth. The comparison with the test map shows complete correspondence, with no additional miscellaneous peaks detected. The purchased P25 catalyst was utilized without undergoing any further purification treatment.

Fig. S1 XRD patterns of P25.

Fig. S2 The UV–visible absorption spectrum of TC.

Fig. S3 Mass spectra of intermediates produced during 5 min photocatalytic degradation on P25.

Text. S2. Degradation kinetic equation

To describe the degradation effect, the degradation rate and degradation kinetic equation are introduced, and the degradation rate is calculated by Equation using Langmuir–Hinshelwood model:

r=-dCdt=krkaCt1+kaCt	(1)

In this equation, C0 is the initial TC concentration, and Ct is the actual TC concentration at the selected time. Due to the low TC concentration, a simplified Langmuir–Hinshelwood first-order dynamic model was used for fitting:

r=-dCtdt≈krkaCt=kCt	(2)

lnC0Ct=krkat=kt	(3)

Where k is the rate constant and t is the reaction time. The data obtained by the above calculation method are as follows:

| Table S1 ROS clearance test reaction kinetics related parameters. |  |  |  |
| --- | --- | --- | --- |
| T | C | r | k |
| Blank | 0 | 100% | 0.14187 |
| h+ | 3 mM | 63.6% | 0.02843 |
| •O2− | 4 mM | 36.0% | 0.01025 |
| 1O2 | 3 mM | 46.2% | 0.01230 |
| •OH | 200 mM | 89.2% | 0.06107 |

In the table above, T represents the scavenging radical species; C represents the concentration used to add the corresponding scavenger; r represents the degradation rate of TC; k represents the reaction rate constant of the reaction process.

Fig. S4 Effect of different quenchers on the degradation rate of tetracycline.

Fig. S5 The photocatalytic degradation of TC by P25 with adding different sacrificial agents. (a) LAA; (b) L-His; (c) EDTA -2Na; (d) IPA.

Fig. S6 Random forest feature importance results

Picture. S1 Germination test of mung bean soaked in TC solution with different light reaction times P25 (A: 5 min; B: 10 min; C: 15 min; D: 20 min; E: 25 min; F: 30 min).

Table S2 Change in toxicity during the photodegradation of TC by P25 via T.E.S.T software.

| Type | Fish LC50(mg/L) |  | Daphnid LC50(mg/L) |  |  | Development | Mutagenicity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TC |  | 0.90 |  | 5.44 | 0.86 |  | 0.60 |
| P1 |  | 0.99 |  | 28.43 | 0.87 |  | 0.62 |
| P2 |  | 0.69 |  | 16.53 | 0.86 |  | 0.69 |
| P3 |  | 0.37 |  | 2.67 | 0.90 |  | 0.18 |
| P4 |  | 50.43 |  | 30.71 | 0.69 |  | -0.07 |
| P5 |  | 3.65 |  | 43.45 | 0.84 |  | 0.74 |
| P6 |  | 3.28 |  | 15.32 | 0.72 |  | 0.55 |
| P7 |  | 4.74 |  | 9.23 | 0.75 |  | 0.34 |
| P8 |  | 17.26 |  | 37.77 | 0.68 |  | 0.64 |
| P9 |  | 39.41 |  | 52.92 | 0.46 |  | 0.15 |

Table S3 Explanation of the input parameters and output parameters.

| Parameters | Interpretation |
| --- | --- |
| C (mg/L) | Initial concentration of tetracycline |
| D (mg) | Mass of catalyst P25 |
| m/z | Mass-to-charge ratio of degradation intermediates |
| Area (t = 5 min) | Mass spectral peak area measured by LC-MS at 5 min of photodegradation |
| Area (t = 10 min) | Mass spectral peak area measured by LC-MS at 10 min of photodegradation |
| Area (t = 15 min) | Mass spectral peak area measured by LC-MS at 15 min of photodegradation |
| Area (t = 20 min) | Mass spectral peak area measured by LC-MS at 20 min of photodegradation |
| Area (t = 25 min) | Mass spectral peak area measured by LC-MS at 25 min of photodegradation |
| Area (t = 30 min)) | Mass spectral peak area measured by LC-MS at 30 min of photodegradation |

Table S4 Experimental data of photocatalytic degradation

| C (mg/L) | D (mg) | m/z | Area (t = 5 min) | Area (t = 10 min) | Area (t = 15 min) | Area (t = 20 min) | Area (t = 25 min) | Area (t = 30 min) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 10 | 191 | 326 | 238 | 301 | 384 | 281 | 282 |
| 10 | 10 | 128 | 130 | 137 | 205 | 37 | 257 | 206 |
| 10 | 10 | 459 | 384 | 320 | 346 | 158 | 105 | 40 |
| 10 | 10 | 340 | 602 | 923 | 1588 | 1072 | 1297 | 1123 |
| 10 | 10 | 218 | 1300 | 2523 | 1225 | 1538 | 932 | 1831 |
| 10 | 10 | 274 | 736 | 2357 | 2026 | 2915 | 3525 | 4771 |
| 10 | 10 | 150 | 146 | 156 | 144 | 133 | 198 | 312 |
| 10 | 10 | 246 | 731 | 627 | 958 | 1279 | 1215 | 1155 |
| 10 | 10 | 318 | 96 | 305 | 266 | 534 | 751 | 702 |
| 10 | 20 | 191 | 315 | 360 | 406 | 329 | 327 | 422 |
| 10 | 20 | 128 | 252 | 95 | 109 | 308 | 205 | 236 |
| 10 | 20 | 459 | 547 | 251 | 106 | 31 | 14 | 9 |
| 10 | 20 | 340 | 1077 | 614 | 807 | 907 | 351 | 983 |
| 10 | 20 | 218 | 1897 | 2459 | 2911 | 2680 | 1112 | 1817 |
| 10 | 20 | 274 | 4208 | 9187 | 6163 | 3009 | 3951 | 4233 |
| 10 | 20 | 150 | 274 | 516 | 391 | 155 | 108 | 126 |
| 10 | 20 | 246 | 1383 | 1567 | 1626 | 1134 | 667 | 967 |
| 10 | 20 | 318 | 854 | 1924 | 1090 | 743 | 700 | 678 |
| 10 | 30 | 191 | 532 | 458 | 254 | 473 | 533 | 394 |
| 10 | 30 | 128 | 348 | 197 | 219 | 329 | 178 | 258 |
| 10 | 30 | 459 | 393 | 247 | 45 | 14 | 23 | 38 |
| 10 | 30 | 340 | 1332 | 1045 | 605 | 1062 | 851 | 1214 |
| 10 | 30 | 218 | 3000 | 1902 | 1638 | 3242 | 2515 | 2018 |
| 10 | 30 | 274 | 12396 | 5309 | 1289 | 13739 | 4249 | 4871 |
| 10 | 30 | 150 | 292 | 255 | 356 | 130 | 235 | 67 |
| 10 | 30 | 246 | 3389 | 1242 | 870 | 3157 | 1066 | 1497 |
| 10 | 30 | 318 | 2305 | 705 | 391 | 4345 | 768 | 796 |
| 10 | 40 | 191 | 608 | 491 | 653 | 675 | 530 | 497 |
| 10 | 40 | 128 | 304 | 239 | 268 | 175 | 166 | 197 |
| 10 | 40 | 459 | 403 | 109 | 25 | 24 | 15 | 13 |
| 10 | 40 | 340 | 869 | 859 | 1077 | 955 | 785 | 784 |
| 10 | 40 | 218 | 1735 | 2009 | 1299 | 2160 | 200 | 2257 |
| 10 | 40 | 274 | 3065 | 3888 | 3952 | 4404 | 4005 | 4252 |
| 10 | 40 | 150 | 71 | 240 | 177 | 319 | 258 | 161 |
| 10 | 40 | 246 | 616 | 562 | 592 | 1075 | 1203 | 951 |
| 10 | 40 | 318 | 489 | 641 | 787 | 793 | 672 | 550 |

In the table above, C represents the initial tetracycline concentration; D represents the dosage of P25 administered; m/z represents the charge ratio of intermediate product; Area represents the peak areas detected at different reaction times.

Table S4 Experimental data of photocatalytic degradation (continued)

| C (mg/L) |  | D (mg) |  | m/z |  | Area (t = 5 min) |  | Area (t = 10 min) |  | Area (t = 15 min) |  | Area (t = 20 min) |  | Area (t = 25 min) |  | Area (t = 30 min) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 50 |  | 191 |  | 431 |  | 504 |  | 548 |  | 450 |  | 609 |  | 358 |  |
| 10 | 50 |  | 128 |  | 246 |  | 265 |  | 204 |  | 152 |  | 110 |  | 328 |  |
| 10 | 50 |  | 459 |  | 490 |  | 100 |  | 20 |  | 5 |  | 2 |  | 46 |  |
| 10 | 50 |  | 340 |  | 952 |  | 945 |  | 694 |  | 1198 |  | 952 |  | 930 |  |
| 10 | 50 |  | 218 |  | 1861 |  | 2233 |  | 1999 |  | 1163 |  | 4158 |  | 3149 |  |
| 10 | 50 |  | 274 |  | 6968 |  | 3965 |  | 4782 |  | 4566 |  | 10503 |  | 5831 |  |
| 10 | 50 |  | 150 |  | 252 |  | 249 |  | 489 |  | 311 |  | 158 |  | 176 |  |
| 10 | 50 |  | 246 |  | 1188 |  | 1257 |  | 1021 |  | 675 |  | 2421 |  | 1607 |  |
| 10 | 50 |  | 318 |  | 1360 |  | 725 |  | 825 |  | 907 |  | 2616 |  | 1128 |  |
| 20 | 10 |  | 191 |  | 1555 |  | 2485 |  | 260 |  | 3051 |  | 2782 |  | 3314 |  |
| 20 | 10 |  | 128 |  | 1342 |  | 986 |  | 117 |  | 1367 |  | 1513 |  | 1102 |  |
| 20 | 10 |  | 459 |  | 1057 |  | 1497 |  | 32 |  | 1471 |  | 1291 |  | 697 |  |
| 20 | 10 |  | 340 |  | 1713 |  | 3078 |  | 118 |  | 3457 |  | 3236 |  | 2897 |  |
| 20 | 10 |  | 218 |  | 9580 |  | 6783 |  | 849 |  | 11038 |  | 10060 |  | 10227 |  |
| 20 | 10 |  | 274 |  | 11221 |  | 5178 |  | 370 |  | 8948 |  | 11667 |  | 13299 |  |
| 20 | 10 |  | 150 |  | 116 |  | 358 |  | 164 |  | 294 |  | 185 |  | 250 |  |
| 20 | 10 |  | 246 |  | 5720 |  | 3566 |  | 255 |  | 5419 |  | 5634 |  | 6715 |  |
| 20 | 10 |  | 318 |  | 3703 |  | 947 |  | 91 |  | 2079 |  | 3047 |  | 3368 |  |
| 20 | 20 |  | 191 |  | 3348 |  | 6691 |  | 9895 |  | 7471 |  | 7151 |  | 6596 |  |
| 20 | 20 |  | 128 |  | 833 |  | 1265 |  | 915 |  | 890 |  | 949 |  | 1068 |  |
| 20 | 20 |  | 459 |  | 978 |  | 1405 |  | 321 |  | 100 |  | 20 |  | 10 |  |
| 20 | 20 |  | 340 |  | 716 |  | 3017 |  | 1135 |  | 2077 |  | 2793 |  | 3215 |  |
| 20 | 20 |  | 218 |  | 4206 |  | 8933 |  | 3955 |  | 9110 |  | 8126 |  | 6703 |  |
| 20 | 20 |  | 274 |  | 1644 |  | 9935 |  | 2455 |  | 13099 |  | 11051 |  | 7678 |  |
| 20 | 20 |  | 150 |  | 327 |  | 142 |  | 120 |  | 109 |  | 214 |  | 149 |  |
| 20 | 20 |  | 246 |  | 1148 |  | 5039 |  | 1467 |  | 5483 |  | 4898 |  | 3861 |  |
| 20 | 20 |  | 318 |  | 302 |  | 2474 |  | 546 |  | 23533 |  | 3034 |  | 1630 |  |
| 20 | 30 |  | 191 |  | 3602 |  | 4189 |  | 3574 |  | 3683 |  | 940 |  | 2667 |  |
| 20 | 30 |  | 128 |  | 707 |  | 533 |  | 893 |  | 810 |  | 283 |  | 674 |  |
| 20 | 30 |  | 459 |  | 2147 |  | 2406 |  | 1546 |  | 876 |  | 42 |  | 59 |  |
| 20 | 30 |  | 340 |  | 9112 |  | 2320 |  | 2848 |  | 1746 |  | 796 |  | 1724 |  |
| 20 | 30 |  | 218 |  | 10714 |  | 8006 |  | 7772 |  | 7185 |  | 1804 |  | 5530 |  |
| 20 | 30 |  | 274 |  | 254 |  | 6203 |  | 9989 |  | 4485 |  | 1106 |  | 6988 |  |
| 20 | 30 |  | 150 |  | 16 |  | 270 |  | 206 |  | 259 |  | 229 |  | 94 |  |
| 20 | 30 |  | 246 |  | 5388 |  | 3925 |  | 4683 |  | 2597 |  | 699 |  | 2737 |  |
| 20 | 30 |  | 318 |  | 2351 |  | 1059 |  | 2468 |  | 782 |  | 313 |  | 1559 |  |
| 20 | 40 |  | 191 |  | 4313 |  | 4408 |  | 4103 |  | 4173 |  | 4696 |  | 4447 |  |
| 20 | 40 |  | 128 |  | 934 |  | 884 |  | 852 |  | 1002 |  | 1258 |  | 1007 |  |
| 20 | 40 |  | 459 |  | 1501 |  | 1260 |  | 686 |  | 159 |  | 31 |  | 16 |  |
| 20 | 40 |  | 340 |  | 1190 |  | 1976 |  | 2312 |  | 4087 |  | 2553 |  | 3572 |  |
| 20 | 40 |  | 218 |  | 4265 |  | 9304 |  | 5127 |  | 7267 |  | 6717 |  | 6593 |  |

Table S4 Experimental data of photocatalytic degradation (continued)

| C (mg/L) |  | D (mg) |  | m/z |  | Area (t = 5 min) |  | Area (t = 10 min) |  | Area (t = 15 min) |  | Area (t = 20 min) |  | Area (t = 25 min) |  | Area (t = 30 min) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 | 40 |  | 274 |  | 5431 |  | 14742 |  | 4366 |  | 11054 |  | 13765 |  | 14097 |  |
| 20 | 40 |  | 150 |  | 126 |  | 42 |  | 190 |  | 224 |  | 200 |  | 302 |  |
| 20 | 40 |  | 246 |  | 2508 |  | 6335 |  | 1665 |  | 4669 |  | 4875 |  | 5250 |  |
| 20 | 40 |  | 318 |  | 1552 |  | 4504 |  | 910 |  | 2559 |  | 3650 |  | 3905 |  |
| 20 | 50 |  | 191 |  | 5032 |  | 4525 |  | 5209 |  | 4636 |  | 4548 |  | 4584 |  |
| 20 | 50 |  | 128 |  | 566 |  | 562 |  | 599 |  | 732 |  | 421 |  | 447 |  |
| 20 | 50 |  | 459 |  | 2022 |  | 1314 |  | 615 |  | 137 |  | 27 |  | 11 |  |
| 20 | 50 |  | 340 |  | 2261 |  | 3635 |  | 3534 |  | 2280 |  | 2691 |  | 4185 |  |
| 20 | 50 |  | 218 |  | 6871 |  | 10681 |  | 6759 |  | 9582 |  | 7205 |  | 6983 |  |
| 20 | 50 |  | 274 |  | 6164 |  | 13795 |  | 7035 |  | 16156 |  | 14342 |  | 14722 |  |
| 20 | 50 |  | 150 |  | 153 |  | 199 |  | 172 |  | 134 |  | 181 |  | 123 |  |
| 20 | 50 |  | 246 |  | 3434 |  | 6216 |  | 2969 |  | 7176 |  | 5894 |  | 4757 |  |
| 20 | 50 |  | 318 |  | 1492 |  | 394 |  | 1741 |  | 5305 |  | 4358 |  | 4276 |  |
| 30 | 10 |  | 191 |  | 268 |  | 224 |  | 264 |  | 180 |  | 170 |  | 221 |  |
| 30 | 10 |  | 128 |  | 163 |  | 141 |  | 112 |  | 135 |  | 40 |  | 8 |  |
| 30 | 10 |  | 459 |  | 671 |  | 791 |  | 965 |  | 830 |  | 627 |  | 555 |  |
| 30 | 10 |  | 340 |  | 656 |  | 476 |  | 597 |  | 314 |  | 299 |  | 307 |  |
| 30 | 10 |  | 218 |  | 2318 |  | 1198 |  | 1692 |  | 1231 |  | 1368 |  | 1459 |  |
| 30 | 10 |  | 274 |  | 12496 |  | 5985 |  | 7300 |  | 4768 |  | 3255 |  | 3847 |  |
| 30 | 10 |  | 150 |  | 145 |  | 270 |  | 256 |  | 212 |  | 297 |  | 245 |  |
| 30 | 10 |  | 246 |  | 2049 |  | 1171 |  | 2116 |  | 646 |  | 338 |  | 670 |  |
| 30 | 10 |  | 318 |  | 2368 |  | 1301 |  | 1815 |  | 836 |  | 503 |  | 606 |  |
| 30 | 20 |  | 191 |  | 406 |  | 353 |  | 394 |  | 215 |  | 261 |  | 217 |  |
| 30 | 20 |  | 128 |  | 19 |  | 20 |  | 7 |  | 7 |  | 58 |  | 119 |  |
| 30 | 20 |  | 459 |  | 846 |  | 596 |  | 356 |  | 19 |  | 746 |  | 1045 |  |
| 30 | 20 |  | 340 |  | 427 |  | 357 |  | 253 |  | 270 |  | 399 |  | 1364 |  |
| 30 | 20 |  | 218 |  | 1242 |  | 1203 |  | 1224 |  | 746 |  | 1328 |  | 2767 |  |
| 30 | 20 |  | 274 |  | 5445 |  | 4253 |  | 3742 |  | 2039 |  | 7166 |  | 5264 |  |
| 30 | 20 |  | 150 |  | 472 |  | 536 |  | 281 |  | 247 |  | 185 |  | 13980 |  |
| 30 | 20 |  | 246 |  | 960 |  | 992 |  | 521 |  | 355 |  | 981 |  | 1721 |  |
| 30 | 20 |  | 318 |  | 967 |  | 918 |  | 715 |  | 740 |  | 1015 |  | 921 |  |
| 30 | 30 |  | 191 |  | 564 |  | 387 |  | 327 |  | 572 |  | 270 |  | 562 |  |
| 30 | 30 |  | 128 |  | 19 |  | 15 |  | 11 |  | 34 |  | 27 |  | 29 |  |
| 30 | 30 |  | 459 |  | 905 |  | 1180 |  | 661 |  | 1284 |  | 1371 |  | 1121 |  |
| 30 | 30 |  | 340 |  | 107 |  | 63 |  | 10 |  | 181 |  | 131 |  | 123 |  |
| 30 | 30 |  | 218 |  | 723 |  | 668 |  | 712 |  | 1195 |  | 801 |  | 1265 |  |
| 30 | 30 |  | 274 |  | 916 |  | 293 |  | 788 |  | 1237 |  | 602 |  | 1011 |  |
| 30 | 30 |  | 150 |  | 87 |  | 150 |  | 93 |  | 70 |  | 88 |  | 389 |  |
| 30 | 30 |  | 246 |  | 441 |  | 482 |  | 375 |  | 504 |  | 357 |  | 667 |  |
| 30 | 30 |  | 318 |  | 145 |  | 96 |  | 151 |  | 186 |  | 229 |  | 209 |  |
| 30 | 40 |  | 191 |  | 562 |  | 573 |  | 521 |  | 575 |  | 51 |  | 521 |  |

Table S4 Experimental data of photocatalytic degradation (continued)

| C (mg/L) |  | D (mg) |  | m/z |  | Area (t = 5 min) |  | Area (t = 10 min) |  | Area (t = 15 min) |  | Area (t = 20 min) |  | Area (t = 25 min) |  | Area (t = 30 min) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 40 |  | 128 |  | 43 |  | 33 |  | 15 |  | 24 |  | 39 |  | 19 |  |
| 30 | 40 |  | 459 |  | 2515 |  | 2349 |  | 1753 |  | 1154 |  | 384 |  | 153 |  |
| 30 | 40 |  | 340 |  | 251 |  | 144 |  | 225 |  | 322 |  | 304 |  | 494 |  |
| 30 | 40 |  | 218 |  | 779 |  | 1037 |  | 1171 |  | 1638 |  | 1292 |  | 1190 |  |
| 30 | 40 |  | 274 |  | 3531 |  | 1107 |  | 2789 |  | 3714 |  | 5145 |  | 4899 |  |
| 30 | 40 |  | 150 |  | 113 |  | 144 |  | 252 |  | 788 |  | 162 |  | 209 |  |
| 30 | 40 |  | 246 |  | 818 |  | 445 |  | 647 |  | 1069 |  | 758 |  | 805 |  |
| 30 | 40 |  | 318 |  | 653 |  | 186 |  | 366 |  | 613 |  | 825 |  | 697 |  |
| 30 | 50 |  | 191 |  | 442 |  | 666 |  | 590 |  | 518 |  | 580 |  | 350 |  |
| 30 | 50 |  | 128 |  | 31 |  | 36 |  | 55 |  | 30 |  | 632 |  | 31 |  |
| 30 | 50 |  | 459 |  | 2091 |  | 712 |  | 737 |  | 475 |  | 227 |  | 94 |  |
| 30 | 50 |  | 340 |  | 214 |  | 11 |  | 12 |  | 10 |  | 10 |  | 7 |  |
| 30 | 50 |  | 218 |  | 929 |  | 1489 |  | 954 |  | 878 |  | 872 |  | 1310 |  |
| 30 | 50 |  | 274 |  | 2260 |  | 2945 |  | 1948 |  | 1895 |  | 1514 |  | 4971 |  |
| 30 | 50 |  | 150 |  | 46 |  | 244 |  | 256 |  | 353 |  | 223 |  | 431 |  |
| 30 | 50 |  | 246 |  | 708 |  | 837 |  | 548 |  | 714 |  | 577 |  | 956 |  |
| 30 | 50 |  | 318 |  | 501 |  | 701 |  | 321 |  | 408 |  | 229 |  | 969 |  |
| 40 | 10 |  | 191 |  | 166 |  | 62 |  | 148 |  | 86 |  | 199 |  | 178 |  |
| 40 | 10 |  | 128 |  | 16 |  | 29 |  | 39 |  | 72 |  | 29 |  | 27 |  |
| 40 | 10 |  | 459 |  | 473 |  | 86 |  | 821 |  | 317 |  | 967 |  | 746 |  |
| 40 | 10 |  | 340 |  | 3 |  | 7 |  | 69 |  | 6 |  | 7 |  | 236 |  |
| 40 | 10 |  | 218 |  | 1064 |  | 109 |  | 1850 |  | 370 |  | 1241 |  | 1843 |  |
| 40 | 10 |  | 274 |  | 2631 |  | 176 |  | 5774 |  | 783 |  | 3592 |  | 3833 |  |
| 40 | 10 |  | 150 |  | 407 |  | 177 |  | 142 |  | 225 |  | 79 |  | 333 |  |
| 40 | 10 |  | 246 |  | 451 |  | 46 |  | 1958 |  | 281 |  | 708 |  | 948 |  |
| 40 | 10 |  | 318 |  | 407 |  | 4 |  | 729 |  | 181 |  | 455 |  | 719 |  |
| 40 | 20 |  | 191 |  | 264 |  | 226 |  | 269 |  | 178 |  | 203 |  | 326 |  |
| 40 | 20 |  | 128 |  | 27 |  | 20 |  | 17 |  | 17 |  | 24 |  | 28 |  |
| 40 | 20 |  | 459 |  | 1095 |  | 1308 |  | 1552 |  | 1301 |  | 1112 |  | 918 |  |
| 40 | 20 |  | 340 |  | 280 |  | 538 |  | 254 |  | 548 |  | 201 |  | 249 |  |
| 40 | 30 |  | 459 |  | 1232 |  | 1056 |  | 1016 |  | 860 |  | 197 |  | 500 |  |
| 40 | 30 |  | 340 |  | 249 |  | 236 |  | 169 |  | 194 |  | 46 |  | 154 |  |
| 40 | 30 |  | 218 |  | 1140 |  | 1641 |  | 1233 |  | 1003 |  | 504 |  | 907 |  |
| 40 | 30 |  | 274 |  | 3902 |  | 3725 |  | 3764 |  | 4043 |  | 633 |  | 2968 |  |
| 40 | 30 |  | 150 |  | 186 |  | 238 |  | 65 |  | 21 |  | 212 |  | 186 |  |
| 40 | 30 |  | 246 |  | 489 |  | 760 |  | 544 |  | 805 |  | 133 |  | 881 |  |
| 40 | 30 |  | 318 |  | 532 |  | 650 |  | 562 |  | 380 |  | 90 |  | 507 |  |
| 40 | 40 |  | 191 |  | 366 |  | 269 |  | 322 |  | 264 |  | 433 |  | 294 |  |
| 40 | 40 |  | 128 |  | 17 |  | 11 |  | 33 |  | 26 |  | 27 |  | 24 |  |
| 40 | 40 |  | 459 |  | 943 |  | 1096 |  | 851 |  | 730 |  | 567 |  | 480 |  |
| 40 | 40 |  | 340 |  | 138 |  | 160 |  | 107 |  | 105 |  | 147 |  | 60 |  |

Table S4 Experimental data of photocatalytic degradation (continued)

| C (mg/L) |  | D (mg) |  | m/z |  | Area (t = 5 min) |  | Area (t = 10 min) |  | Area (t = 15 min) |  | Area (t = 20 min) |  | Area (t = 25 min) |  | Area (t = 30 min) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 40 | 40 |  | 218 |  | 760 |  | 1080 |  | 999 |  | 794 |  | 1067 |  | 1074 |  |
| 40 | 40 |  | 274 |  | 4061 |  | 4872 |  | 2668 |  | 3182 |  | 4522 |  | 1993 |  |
| 40 | 40 |  | 150 |  | 85 |  | 123 |  | 136 |  | 168 |  | 132 |  | 57 |  |
| 40 | 40 |  | 246 |  | 794 |  | 817 |  | 645 |  | 622 |  | 767 |  | 327 |  |
| 40 | 40 |  | 318 |  | 606 |  | 626 |  | 633 |  | 628 |  | 685 |  | 209 |  |
| 40 | 50 |  | 191 |  | 351 |  | 392 |  | 298 |  | 377 |  | 406 |  | 356 |  |
| 40 | 50 |  | 128 |  | 22 |  | 16 |  | 33 |  | 54 |  | 17 |  | 45 |  |
| 40 | 50 |  | 459 |  | 1123 |  | 936 |  | 677 |  | 452 |  | 299 |  | 176 |  |
| 40 | 50 |  | 340 |  | 62 |  | 85 |  | 90 |  | 118 |  | 63 |  | 37 |  |
| 40 | 50 |  | 218 |  | 1216 |  | 1415 |  | 1302 |  | 1578 |  | 860 |  | 852 |  |
| 40 | 50 |  | 274 |  | 2777 |  | 3942 |  | 2845 |  | 4258 |  | 2132 |  | 1998 |  |
| 40 | 50 |  | 150 |  | 269 |  | 159 |  | 66 |  | 67 |  | 336 |  | 241 |  |
| 40 | 50 |  | 246 |  | 749 |  | 598 |  | 545 |  | 497 |  | 352 |  | 255 |  |
| 40 | 50 |  | 318 |  | 529 |  | 711 |  | 577 |  | 521 |  | 361 |  | 221 |  |
| 50 | 10 |  | 191 |  | 118 |  | 145 |  | 102 |  | 172 |  | 98 |  | 134 |  |
| 50 | 10 |  | 128 |  | 12 |  | 22 |  | 10 |  | 43 |  | 18 |  | 11 |  |
| 50 | 10 |  | 459 |  | 453 |  | 683 |  | 844 |  | 864 |  | 928 |  | 814 |  |
| 50 | 10 |  | 340 |  | 51 |  | 55 |  | 109 |  | 43 |  | 214 |  | 40 |  |
| 50 | 10 |  | 218 |  | 622 |  | 939 |  | 1384 |  | 1343 |  | 4284 |  | 1557 |  |
| 50 | 10 |  | 274 |  | 2273 |  | 2539 |  | 3447 |  | 3212 |  | 10230 |  | 3764 |  |
| 50 | 10 |  | 150 |  | 133 |  | 126 |  | 186 |  | 477 |  | 61 |  | 231 |  |
| 50 | 10 |  | 246 |  | 668 |  | 418 |  | 1053 |  | 679 |  | 2625 |  | 823 |  |
| 50 | 10 |  | 318 |  | 260 |  | 431 |  | 521 |  | 639 |  | 1917 |  | 567 |  |
| 50 | 20 |  | 191 |  | 205 |  | 99 |  | 188 |  | 252 |  | 174 |  | 222 |  |
| 50 | 20 |  | 128 |  | 11 |  | 14 |  | 15 |  | 186 |  | 697 |  | 11 |  |
| 50 | 20 |  | 459 |  | 249 |  | 570 |  | 1189 |  | 1211 |  | 1264 |  | 1339 |  |
| 50 | 20 |  | 340 |  | 6 |  | 5 |  | 3 |  | 16 |  | 12 |  | 7 |  |
| 50 | 20 |  | 218 |  | 208 |  | 255 |  | 710 |  | 1263 |  | 1057 |  | 935 |  |
| 50 | 20 |  | 274 |  | 1160 |  | 255 |  | 501 |  | 2624 |  | 1382 |  | 1733 |  |
| 50 | 20 |  | 150 |  | 371 |  | 1167 |  | 20180 |  | 18608 |  | 22578 |  | 21321 |  |
| 50 | 20 |  | 246 |  | 1352 |  | 74 |  | 176 |  | 568 |  | 516 |  | 207 |  |
| 50 | 20 |  | 318 |  | 85 |  | 72 |  | 111 |  | 264 |  | 110 |  | 153 |  |
| 50 | 30 |  | 191 |  | 356 |  | 301 |  | 255 |  | 238 |  | 280 |  | 163 |  |
| 50 | 30 |  | 128 |  | 12 |  | 10 |  | 18 |  | 10 |  | 19 |  | 34 |  |
| 50 | 30 |  | 459 |  | 9 |  | 1548 |  | 1683 |  | 1737 |  | 1764 |  | 1609 |  |
| 50 | 30 |  | 340 |  | 4 |  | 4 |  | 2 |  | 3 |  | 7 |  | 6 |  |
| 50 | 30 |  | 218 |  | 568 |  | 964 |  | 932 |  | 1092 |  | 1258 |  | 1270 |  |
| 50 | 30 |  | 274 |  | 2973 |  | 2142 |  | 1712 |  | 2049 |  | 2602 |  | 4424 |  |
| 50 | 30 |  | 150 |  | 22667 |  | 24430 |  | 21695 |  | 23284 |  | 21709 |  | 24303 |  |
| 50 | 30 |  | 246 |  | 436 |  | 323 |  | 251 |  | 390 |  | 248 |  | 741 |  |
| 50 | 30 |  | 318 |  | 475 |  | 313 |  | 287 |  | 235 |  | 356 |  | 474 |  |

Table S4 Experimental data of photocatalytic degradation (continued)

| C (mg/L) |  | D (mg) |  | m/z |  | Area (t = 5 min) |  | Area (t = 10 min) |  | Area (t = 15 min) |  | Area (t = 20 min) |  | Area (t = 25 min) |  | Area (t = 30 min) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 50 | 40 |  | 191 |  | 306 |  | 131 |  | 346 |  | 238 |  | 304 |  | 115 |  |
| 50 | 40 |  | 128 |  | 27 |  | 22 |  | 10 |  | 26 |  | 16 |  | 7 |  |
| 50 | 40 |  | 459 |  | 1268 |  | 443 |  | 1895 |  | 1588 |  | 1453 |  | 277 |  |
| 50 | 40 |  | 340 |  | 19 |  | 9 |  | 25 |  | 37 |  | 2 |  | 9 |  |
| 50 | 40 |  | 218 |  | 673 |  | 221 |  | 1367 |  | 782 |  | 1090 |  | 176 |  |
| 50 | 40 |  | 274 |  | 3280 |  | 892 |  | 1637 |  | 2827 |  | 2455 |  | 839 |  |
| 50 | 40 |  | 150 |  | 22028 |  | 22958 |  | 20528 |  | 21469 |  | 445 |  | 21350 |  |
| 50 | 40 |  | 246 |  | 454 |  | 129 |  | 521 |  | 474 |  | 248 |  | 47 |  |
| 50 | 40 |  | 318 |  | 384 |  | 113 |  | 488 |  | 368 |  | 204 |  | 44 |  |
| 50 | 50 |  | 191 |  | 277 |  | 370 |  | 243 |  | 395 |  | 478 |  | 76 |  |
| 50 | 50 |  | 128 |  | 17 |  | 18 |  | 18 |  | 261 |  | 23 |  | 28 |  |
| 50 | 50 |  | 459 |  | 922 |  | 1438 |  | 901 |  | 1322 |  | 1127 |  | 52 |  |
| 50 | 50 |  | 340 |  | 795 |  | 99 |  | 93 |  | 89 |  | 125 |  | 18 |  |
| 50 | 50 |  | 218 |  | 19180 |  | 1325 |  | 1051 |  | 951 |  | 1072 |  | 5 |  |
| 50 | 50 |  | 274 |  | 4596 |  | 3975 |  | 3208 |  | 2835 |  | 3064 |  | 558 |  |
| 50 | 50 |  | 150 |  | 121 |  | 20637 |  | 18727 |  | 19756 |  | 20575 |  | 21419 |  |
| 50 | 50 |  | 246 |  | 764 |  | 480 |  | 428 |  | 451 |  | 482 |  | 39 |  |
| 50 | 50 |  | 318 |  | 480 |  | 440 |  | 325 |  | 280 |  | 395 |  | 30 |  |