# Supplementary Information for:

Deciphering the structure and the potassium ions transport mechanism of potassium borate glass

Lulu Song a, b, Alex C. Hannon c, Steve Feller d, Ruirui Liu a, Peyton McGuire d, Bo Zhang a, Yongquan Zhou a, Wu Li a, *, Fayan Zhu a, *

a Key Laboratory of Green and High-end Utilization of Salt Lake Resources, Qinghai Institute of Salt Lakes, Chinese Academy of Sciences, Xining 810008, China

b University of Chinese Academy of Science, Beijing 100049, China

c ISIS Facility Rutherford Appleton Laboratory, Chilton, Didcot, Oxon OX11 0QX, UK

d Coe College, Physics Department, 1220 First Ave NE, Cedar Rapids, IA 52402, USA

*Corresponding author

Fayan Zhu: zhufayan@126.com

Table S1. AIMD simulates box parameters

| x | Atom number |  |  | Total atoms | Box length (Å) |
| --- | --- | --- | --- | --- | --- |
|  | K | 11B | O |  |  |
| 0.1 | 20 | 180 | 280 | 480 | 18.1244 |
| 0.2 | 40 | 160 | 260 | 460 | 18.003 |
| 0.3 | 60 | 140 | 240 | 440 | 17.8296 |
| 0.4 | 80 | 120 | 220 | 420 | 17.9773 |

Table S2. Lennard Jones potential parameters

| Atom Type | Lennard Jones Parameters |  |  |  |
| --- | --- | --- | --- | --- |
|  | Epsilon(kJ/mol) | Sigma(Å) | AW (amu) | Charge |
| B | 0.1750 | 0.5000 | 11.0000 | 1.8000 |
| O | 0.1625 | 3.6000 | 16.0000 | -1.2000 |
| K | 0.1750 | 29.0000 | 39.0000 | 0.6000 |

Table S3. EPSR simulates box parameters

| Research system | Atom number |  |  | Total atoms | Box length |
| --- | --- | --- | --- | --- | --- |
|  | K | B | O |  | (Å) |
| 0.10K2O.0.9011B2O3 | 200 | 1800 | 2800 | 4800 | 38.4714 |
| 0.20K2O.0.8011B2O3 | 400 | 1600 | 2600 | 4600 | 37.5618 |
| 0.30K2O.0.7011B2O3 | 600 | 1400 | 2400 | 4400 | 36.5654 |
| 0.40K2O.0.6011B2O3 | 800 | 1200 | 2200 | 4200 | 36.0966 |

Fig. S1 left: Experimental and EPSR diffraction spectra of potassium borate glass F(Q). Right: real space distribution function G(r) simulated by EPSR and experiments on potassium borate glass

Table S4. The interaction distance and coordination number of each atom pair obtained by AIMD, EPSR and difference (DIFF) subtraction

| x | i-j | ri-j/Å | CNi-j/atoms | Method | x | i-j | ri-j/Å | CNi-j/atoms | Method |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.1 | B-O | 1.37 | 3.29 | DIFF | 0.3 | B-O | 1.40 | 3.32 | DIFF |
|  |  | 1.38 | 3.00 | EPSR |  |  | 1.38 | 3.45 | EPSR |
|  |  | 1.38 | 3.09 | AIMD |  |  | 1.39 | 3.27 | AIMD |
|  | O-O | 2.42 | 4.24 | DIFF |  | O-O | 2.41 | 4.45 | DIFF |
|  |  | 2.40 | 5.16 | EPSR |  |  | 2.40 | 6.04 | EPSR |
|  |  | 2.40 | 4.24 | AIMD |  |  | 2.41 | 4.45 | AIMD |
|  | K-O | 2.64 | 9.76 | DIFF |  | K-O | 2.59 | - | DIFF |
|  |  | 2.58 | 8.88 | EPSR |  |  | 2.58 | 11.26 | EPSR |
|  |  | 2.84 | 9.05 | AIMD |  |  | 2.74 | 9.30 | AIMD |
| 0.2 | B-O | 1.39 | 3.29 | DIFF | 0.4 | B-O | 1.41 | 3.38 | DIFF |
|  |  | 1.38 | 3.30 | EPSR |  |  | 1.38 | 3.81 | EPSR |
|  |  | 1.38 | 3.23 | AIMD |  |  | 1.40 | 3.27 | AIMD |
|  | O-O | 2.41 | 4.55 | DIFF |  | O-O | 2.40 | 4.16 | DIFF |
|  |  | 2.40 | 5.42 | EPSR |  |  | 2.40 | 5.88 | EPSR |
|  |  | 2.41 | 4.55 | AIMD |  |  | 2.42 | 4.16 | AIMD |
|  | K-O | 2.58 | - | DIFF |  | K-O | 2.60 | - | DIFF |
|  |  | 2.55 | 8.51 | EPSR |  |  | 2.46 | 8.05 | EPSR |
|  |  | 2.82 | 9.33 | AIMD |  |  | 2.72 | 8.30 | AIMD |

Fig. S2 Coordination number of the first coordination layer of xK2O·(1-x)11B2O3 (0.1≤ x ≤ 0.4) glass and KB5O8, K5B19O31, K2B4O7, K3B3O6 crystals

### Effect of structural change on mass density, atomic density and molar volume

Fig. S3 shows a comparison between the density of potassium borate glass and that of potassium borate glass in SciGlass database[1]. As can be seen from the figure, our experimental density data is relatively close to that in database 1, indicating that we have obtained a good experimental result. With the increase of K2O content, the density of potassium borate glass increases gradually, but its change trend increases rapidly first, and then tends to be flat. The turning point of the change is x = 0.3. With the increase of K2O content, the void occupancy gradually decreases, so the void occupancy is inversely proportional to the density of the glass. This conclusion is consistent with the conclusions of studies on the correlation between void space and density in arsenate glass systems [2-4], indicating that this may be a common phenomenon in glass systems. As can be seen from the Fig. S4, NBO content in glass increases with the increase of K2O content, so the change of NBO content is proportional to the change of density. This conclusion is consistent with the findings of Singh et al. [5] In addition, when x = 0.3, N4 is the largest [6]. when 0.1 ≤ x ≤ 0.3, the number of rings gradually increases, indicating that the three-dimensional network connectivity of the system is enhanced; when 0.3 ≤ x ≤ 0.4, the number of rings gradually decreases, indicating that the system begins to disperse, so the density of potassium borate glass first increases rapidly, and then changes gently.

With the increase of K2O content, the atomic density first increases and then decreases, the molar volume first decreases and then increases, and the turning point of both changes is x = 0.3. Therefore, the atomic density and molar volume are related to the ring structure and N4.

Fig. S3 Density data of xK2O·(1-x)11B2O3 (x=0.10, 0.20, 0.30, 0.40) glass and comparison with literature values, atomic number density and molar volume curves

Table S5. The data of interaction distance, relative content and half-peak width of each atom pair obtained by atom labeling method

| Pair i-j | x | ri-j | Proportion | FWHM |
| --- | --- | --- | --- | --- |
| 3B-BO | 0.1 | 1.38 | 0.88 | 0.19 |
|  | 0.2 | 1.39 | 0.75 | 0.19 |
|  | 0.3 | 1.39 | 0.59 | 0.20 |
|  | 0.4 | 1.40 | 0.57 | 0.21 |
| 3B-NBO | 0.1 | 1.37 | 0.04 | 0.18 |
|  | 0.2 | 1.36 | 0.04 | 0.21 |
|  | 0.3 | 1.36 | 0.12 | 0.20 |
|  | 0.4 | 1.35 | 0.17 | 0.20 |
| 4B-BO | 0.1 | 1.48 | 0.09 | 0.20 |
|  | 0.2 | 1.48 | 0.19 | 0.20 |
|  | 0.3 | 1.48 | 0.28 | 0.20 |
|  | 0.4 | 1.49 | 0.23 | 0.20 |
| 4B-NBO | 0.1 |  |  |  |
|  | 0.2 | 1.49 | 0.01 | 0.23 |
|  | 0.3 | 1.49 | 0.02 | 0.19 |
|  | 0.4 | 1.49 | 0.03 | 0.20 |
| K-BO | 0.1 | 2.87 | 0.81 | 0.61 |
|  | 0.2 | 2.86 | 0.79 | 0.69 |
|  | 0.3 | 2.77 | 0.62 | 0.65 |
|  | 0.4 | 2.81 | 0.51 | 0.74 |
| K-NBO | 0.1 | 2.96 | 0.19 | 0.68 |
|  | 0.2 | 2.96 | 0.21 | 0.88 |
|  | 0.3 | 2.78 | 0.38 | 0.76 |
|  | 0.4 | 2.71 | 0.49 | 0.55 |
| BO-BO | 0.1 | 2.40 | 0.94 | 0.22 |
|  | 0.2 | 2.41 | 0.87 | 0.22 |
|  | 0.3 | 2.41 | 0.74 | 0.23 |
|  | 0.4 | 2.42 | 0.64 | 0.23 |
| BO-NBO | 0.1 | 2.40 | 0.06 | 0.23 |
|  | 0.2 | 2.42 | 0.12 | 0.22 |
|  | 0.3 | 2.42 | 0.21 | 0.21 |
|  | 0.4 | 2.42 | 0.30 | 0.21 |
| NBO-NBO | 0.1 | 2.40 | 0.00 | 0.23 |
|  | 0.2 | 2.42 | 0.01 | 0.19 |
|  | 0.3 | 2.42 | 0.05 | 0.23 |
|  | 0.4 | 2.42 | 0.05 | 0.20 |

Fig. S4 Variation curve of BO and NBO content of xK2O·(1-x)11B2O3 (x=0.10, 0.20, 0.30, 0.40) glasses

Fig. S5 O-B-O angle distribution functions for xK2O·(1-x)11B2O3 (x = 0.10, 0.20, 0.30, 0.40) glasses

Fig. S6 Ring and chain structure units, the tri-coordinated boron containing three BOs in the ring structure is abbreviated, and the BO in the periphery of the ring structure is omitted.

Fig. S7 Schematic diagram of transformation mechanism between structural units

Fig. S8 Transport GIFs of K+ ions in0.40K2O·0.6011B2O3 glass

Fig. S9 (a) Time trajectory diagram of K+ at frame 600; (b) K-O coordination map at frame 600; (c) Distribution of structural units around K+ at frame 600

Fig. S10 The change of the mean square displacement (MSD) with the simulation time

## References

[1] SciGlass Professional 7.3., ITC Inc., 2008.

[2] M. Kassem, T. Bounazef, D. Fontanari, A. Sokolov, M. Bokova, A.C. Hannon, E. Bychkov, Chemical and Structural Variety in Sodium Thioarsenate Glasses Studied by Neutron Diffraction and Supported by First-Principles Simulations, Inorganic Chemistry. 59 (2020) 16410-16420.

[3] J. Akola, P. Jóvári, I. Kaban, I. Voleská, J. Kolář, T. Wágner, R.O. Jones, Structure, electronic, and vibrational properties of amorphous AsS2 and AgAsS2: Experimentally constrained density functional study, Physical Review B. 89 (2014) 064202.

[4] J. Akola, B. Beuneu, R.O. Jones, P. Jóvári, I. Kaban, J. Kolář, I. Voleská, T. Wágner, Structure of amorphous Ag/Ge/S alloys: experimentally constrained density functional study, Journal of Physics: Condensed Matter. 27 (2015) 485304.

[5] V. Dua, S.K. Arya, K. Singh, Review on transition metals containing lithium borate glasses properties, applications and perspectives, 58 (2023) 8678-8699.

[6] O.N. Koroleva, M.V. Shtenberg, The structure of glasses M2O-B2O3 (М – Li, Na, K): Estimation of thermodynamic characteristics of alkali borates and physicochemical modeling, Journal of Non-Crystalline Solids. 601 (2023) 122053.