Supplementary Information

An innovative CuxAg50-x/UiO66-NH2 photocatalyst prepared by dual ship bottling strategy for photocatalytic CO2 reduction: the controlled product selectivity and pathways

Lipeng Jianga, Dengqian Chena, Zhengkai Haoa, Dongxue Caoa, Runqiao Liua, Jingyu Chenga, Limei Chena, Xin Liub, Boyin Jiac and Dongdong Liua,*

a College of Engineering and Technology, Jilin Agricultural University, Changchun, 130118, P. R. China

b Key Laboratory of Engineering Dielectric and Applications (Ministry of Education), School of Electrical and Electronic Engineering, Harbin University of Science and Technology, Harbin 150080, P. R. China

c College of animal medicine, Jilin Agricultural University, Changchun, 130118, P. R. China

*: Corresponding author.

E-mail address: liudongdong@jlau.edu.cn

Experimental section

Text S1. Chemicals

Silver nitrate (AgNO3), copper(II) acetate monohydrate (Cu(OAc)2·H2O), ethylene glycol (EG), ethanol, isopropanol (IPA), Acetic acid, Isopropyl alcohol, Ethanol absolute, potassium bicarbonate (KHCO3), sulfuric acid (H2SO4, 98%), hydrogen peroxide (H2O2, 30%), Fumaric acid, sodium hydroxide (NaOH), chloroauric acid (HAuCl4), sodium thiosulfate (Na2S2O3·5H2O), ammonium chloride (NH4Cl), sodium sulfite (Na2SO3), ZrCl4 anhydrous, ammonium fluoride (NH4F, 40%), 2-Aminoterephthalic acid (BDC-NH2), Copper Nitrate hemipentahydrate Isopropyl alcohol, hydrofluoric acid (HF, 40%) were purchased from Sinopharm Chemical Reagent Co., Ltd. Polyvinyl pyrrolidone (PVP) 58000 and 1H-Pyrazole-3,5-dicarboxylic acid (PDA) were purchased from Shanghai Aladdin Biochemical Technology Co., Ltd. Nafion solution (D-520 dispersion, 5 wt.%) was purchased from Alfa Aesar Chemical Co., Ltd. CO2 (≥ 99.999%) was provided by Shanxi Kuaite Gas and Equipment Co., Ltd. All materials were used as received without further purification. Deionized water with a resistivity of 18.25 M·cm-1 was used for all experiments.

Text S2. Synthesis of CuxAg50-x/UiO66-NH2

(1) Synthesis of Zr6-oxo clusters: 1.2 g ZrCl4 was added into a mixture of 15 mL of glacial acetic acid and 25 mL of isopropanol under stirring at 600 rpm and heated at 120 °C for 60 min. The product was collected sequentially through centrifugation at 10000 rpm and suction filtration. The collected white solid was subsequently washed with acetone twice and dried under vacuum at room temperature.

(2) Synthesis of UiO66-NH2: Firstly, 300 mg of Zr6-oxo clusters were dissolved in 1.5 mL of acetic acid and 6 mL of H2O. Then, 100 mg of 2-aminoterephthalic acid and 5 mL of ethanol were added. The reaction was stirred vigorously at room temperature for 24 h. Finally, the product was collected by centrifugation, and then the product was washed three times with MeOH and dried overnight in vacuum at 60 °C.

(3) Synthesis of CuxAg50-x: AgNO3 and Cu(OAc)2·H2O with different concentrations (the feed amounts were shown in Table S1) and 1.06 g of PVP were dissolved in 50 mL of ethylene glycol. The 50 mL of ethylene glycol was poured into the round bottom flask. The N2-flowing gas pipe was put into the mixed solution for degassing at 20 min and then stopped. The glass plug was quickly covered on the round-bottomed flask and the sealing film was wrapped around the bottle mouth to prevent leakage. The round-bottomed flask was moved into an oil bath pot preheated to 180 °C and fixed. After heating for 15 min, the mixed solution was stopped and quickly transferred to cold water bath for rapid cooling. The products were collected by centrifugation at 8000 rpm and washed twice with anhydrous ethanol. The obtained product was transferred to a vacuum oven at 60 °C overnight. The obtained trace powder was redispersed with 25 mL of pure water and labeled as CuxAg50-x aqueous solution.

(4) Synthesis of Ag and Cu references: Ag and Cu references were prepared using the same methods as CuxAg50-x, where the feed amounts and reaction times of AgNO3 and Cu(OAc)2·H2O were shown in Table S2.

Text S3. Characterization

Transmission electron microscopy (TEM, FEI Talos F200x G2) were used to analyze the microstructure of the materials. High-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) images and corresponding energy dispersive spectroscopy (EDS) mapping images were obtained on a Talos F200X equipped with a Super-X EDX operating at 200 kV. The X-ray absorption find structure spectra (Cu K-edge and Ag K-edge) were collected at 1W1B station in Beijing Synchrotron Radiation Facility (BSRF)1. The storage rings of BSRF were operated at 2.5 GeV with a maximum current of 250 mA. Using Si(111) double-crystal monochromator, the data collection was carried out in transmission mode using ionization chamber2. The solid 13C Nuclear Magnetic Resonance (NMR) is conducted on an AVANCE III WB 400MHz equipment (Bruker)3. The absorption coefficient data in the XANES region were obtained by applying consistent procedures for pre-edge line fitting, post-edge curve fitting, and edge-step normalization across all the data. The XANES and EXAFS data processing and analysis were carried out using the IINFFIT package4. X-ray powder diffraction (XRD) measurements were performed on the D8 Advanced X-ray diffractometer (Burker-AXS D8 Advance, 2014) with Cu Kα radiation. X-ray photoelectron spectroscopy (XPS) and Auger electron spectroscopy (AES) measurements were conducted using the Kratos Axis Ultra DLD instrument with Al Kα X-ray (1486.6 eV) radiation. FT-IR spectra of powder samples were recorded on a Nicolet 6700 spectrometer (Thermo Fisher Nicolet, USA) using KBr pellets. Raman spectra were obtained using a Raman spectrometer from Thermo Scientific with a 532 nm laser source. UV-Vis-NIR diffused reflectance spectra (DRS) were collected on a spectrophotometer (UV-3100, Shimadzu, Japan) with BaSO4 as the background holder. Fluorescence spectrometers (FS5, Edinburgh Instruments, Britain) were used to record fluorescence spectra (PL) and time-resolved fluorescence spectra (TRPL) to analyze the steady-state optical properties and fluorescence carrier dynamics of samples. The photoelectrochemical measurements were carried out on a CHI 760E electrochemical workstation (Chenhua, Shanghai). CO2 temperature-programmed desorption (TPD) measurements were performed using a Quantachrome Autosorb-iQC chemisorption analyzer with a thermal conductivity detector. N2 and CO2 adsorption isotherms were obtained using an ASAP2020M apparatus. The samples were degassed in vacuum at 120 °C for 6 h and then measured at -196 °C for N2 adsorption and at 25 °C for CO2 adsorption. Photocatalytic experiments were conducted with a 300 W Xe lamp (Perfect Light, Beijing) as the light source coupled with a UVCUT-420 nm filter. The gases produced from the CO2 photoreduction system were analyzed and quantified using an online gas chromatography (GC) system (GC-2014, Shimadzu) equipped with a thermal conductivity detector (TCD) and two flame-ionized detectors (FIDs). The origin of photocatalytic CO2 reduction products was determined using isotope-labeled 13CO2 (99%), H218O (99%), D2O (99%) and analyzed by gas chromatography-mass spectrometry (GC-MS) (Trace 1310 GC-ISQ quadrupole MS, Thermo-Fisher, USA). Liquid products obtained at the end of photocatalysis were analyzed by 1H nuclear magnetic resonance (NMR) using an AVANCE III HD 600 MHz instrument.

Text S4. Photocatalytic CO2 reduction experiment

(1) Standard testing.

In quantification of reaction products by GC, note that trace products including HCOOH and C2H6 were ignored in the quantification analysis, and O2 was not quantified due to manual injection in which it was impossible to avoid exposure to air. The main liquid product of ethanol was quantified according to the obtained relative mole correction factors of DMF. The gas product (CO, CH4, C2H4) rate (μmol·g-1·h-1), and product selectivity were calculated using equations presented in the following eqn.(S1) and eqn.(S2):

Gasi = Ci*(PVRT)W*t*106                            (S1)

Sel. = mole Product*number of electronsmCO*2+mCH4*8+mCH3OH*6+mC2H4*12+mC2H5OH*12*100%          (S2)

Where Ci (ppm) is the mole concentration obtained by GC, P (Pa) is the pressure in the reaction, V (m3) is the volume of reactor (m3), R the gas constant, T (K) is the temperature generated by light irradiation, W (g) is the mass of catalyst, t (h) is the reaction time, represents the area of product obtained by GC, f represents the mole relative correction factor, ρ (g cm-3) is the density of DMF , M is the molecular weight and m (mol) is the mole number of the product.

For stability tests, 10 mg of catalysts and 10 mL of distilled water were added to a Pyrex glass reaction cell, which was then filled with CO2. The photocatalytic CO2RR was performed under Xe lamp light source. After 240 min, 1 μL aliquots was extracted for the analysis. Then the reaction suspension was filtered and washed for several times by using ethanol and H2O. After thoroughly dried of the catalyst, the identical reaction system was conducted for the next 4 h illumination and further for the next subsequent 5 recycling runs.

(2) Calculation method of apparent quantum yield (AQY %).

The apparent quantum yield (AQY) was measured in a 20 mL home-made quartz bottle with a 3 W monochromatic LED light as the light source. The number of incident photons was measured by using a radiant power energy meter (Beijing Zhong jiao Jin yuan Technology Co., Ltd.). AQY was calculated by the following eqn.(S3)5:

AQY= number of reacted eletronsnumber of incident electrons×100%                      (S3)

(3) In-situ diffuse reflectance infrared Fourier-transform spectra (DRIFTS).

In situ DRIFTS spectra were recorded to detect the intermediates during the CO2 reduction process. The measurements were performed using a Thermo-Fisher IS50 spectrometer equipped with Harrick accessories. The reaction chamber was purged with Ar gas and then filled with CO2. The spectra were collected periodically under visible light irradiation. Each spectrum was recorded by averaging 20 scans at a 4 cm-1 spectral resolution.

(4) In situ Raman tests.

The ink used for in situ Raman analysis contained 10 mg of photocatalysts, 500 μL H2O, 460 μL isopropanol, and 40 μL Nafion. The ink was coated on a sample cell (type-K004, Tianjin Aida) equipped with a 3 mm thick quartz window and a 5 mm × 5 mm gold plate. The sample cell was purged with Ar gas and then filled with CO2. In situ Raman spectra were recorded using a LabRAM HR Evolution (Horiba) instrument with a 633 nm laser. The irradiation device employed an optical fiber.

(5) Labelled H218O, D2O and 13CO2 experiments.

To confirm the oxygen source of O2, the labelled H218O experiment was performed as follows: 50 mg of photocatalysts and 1 mL of H218O were introduced into the reactor. Then, the reactor was evacuated, and this filled-pump cycle was repeated for 5 times by CO2. After the final evacuation, the reactor was filled with 0.6 MPa CO2 and then sealed. The temperature was controlled at 80 ℃. Then, the photocatalytic reaction experiment was conducted as before by irradiating the mixture for 4 h. The gas samples from the reactor were collected and analyzed by mass spectroscopy.

Labelled D2O experiments were similar as the labelled H218O experiment, except that D2O was used, which was performed to confirm the hydrogen source of product.

To confirm the carbon source of product in this work, the labelled 13CO2 experiment was performed as follows: 50 mg of photocatalysts and 1 mL of H2O were introduced into the reactor. Then, the reactor was evacuated, and this filled-pump cycle was repeated for 5 times by 13CO2. After the final evacuation, the reactor was filled with 0.6 MPa 13CO2 and then sealed. The temperature was controlled at 80 ℃. Next, the photocatalytic reaction experiment was conducted as before by irradiating the mixture for 4 h. The gas samples from the reactor were collected and analyzed by mass spectroscopy.

Text S5. Photoelectrochemical measurements

The Mott-Schottky, transient photocurrent test, and electrochemical impedance spectroscopy (EIS) analysis were performed on the electrochemistry workstation (Zennium pro, Zahner, Germany). The determination process was detected by traditional three electrode cell system which use Pt sheet as counter electrode, Ag/AgCl electrode as reference electrode and the treated ITO glasses (1 cm × 2 cm) acted as working electrodes. In the photocurrent experiments, Na2SO4 solution (0.1 M) was used as electrolyte while the light was controlled on/off every 50 s. In addition, 0.5 M KCl solution and 5.0 mM K3[Fe(CN)6]/K4[Fe(CN)6] were used as electrolyte in the electrochemical impedance spectroscopy (EIS) measurements with frequency from 1 Hz to 100 kHz. Besides, Na2SO4 solution (0.2 M) was used as electrolyte for measurement of Mott-Schottky plots, under the potential ranged from -1.5 V to 1.5 V (vs. Ag/AgCl) with different frequencies of 0.5, 1.0 and 1.5 kHz, respectively6. Femtosecond transient absorption spectroscopy (fs-TA): the transient absorption (TA) spectra were measured by optical femtosecond pump-probe spectroscopy. The output of a mode-locked Ti-sapphire amplified laser system (Spitfire Ace, Spectra-Physics) with wavelength 800 nm, pulse-width 35 fs, repetition rate 1 kHz, average power 4 W was split into two beams (10:1). The strong radiation was converted into UV-VIS-IR in the range of 240~2400 nm by use of Optical Parametric Amplifier (TOPAS, Light Conversion) with 420 nm excitation and used as a pump beam. The weaker beam after passing a variable delay line (up to 6 ns) was focused in a 3 mm thickness rotated CaF2 plate to produce a white light continuum (WLC), which was used as a probe beam. Home-built pump-probe setup was used for obtaining transient absorption spectra and kinetics. The relative polarizations between pump and probe beam were set to the magic angle (54.7°) to avoid rotational depolarization effects. The entire setup was controlled by a PC with the help of LabView software (National Instruments). All measurements were performed at room temperature under aerated conditions. The 0.1 mg·mL-1 ethanol dispersion of UiO66-NH2, Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were transferred to 1 mm path length cuvettes. The experimental data were fitted to a multiexponential decay function convoluted with the instrument response function. Overall time resolution was about 2~2000 fs7.

Text S6. Method of DFT calculations

All spin-polarized density functional theory (DFT) calculations were performed using the Vienna Ab initio Simulation Package (VASP) software8. The projector augmented plane wave (PAW) pseudopotential and the Perdew–Burke–Ernzerhof generalized gradient approximation (PBE-GGA) exchange correlation functional were used to describe the ionic cores. The van der Waals correction of Grimme’s DFT-D3 model was also adopted9. The energy cutoff was set to be 520 eV. The Brillouin-zone integration was sampled with a Γ-centered Monkhorst-Pack mesh of 1 × 1 × 110. The structures were fully relaxed until the maximum force on each atom was less than 0.01 eV/Å, and the energy convergent standard was 10-5 eV. The structure was fully relaxed and reached the minimum energy principle during the structure optimization process. The slab model included a vacuum layer of 15 Å to separate the slabs along the perpendicular Z-direction.

The adsorption energy was calculated as eqn.(S4):

ΔEabs (ΔEabs = E(slab-abs) − E(slab) − E(abs))                      (S4)

The Gibbs free-energies (ΔG) of the adsorbed state were determined by eqn.(S5):

ΔG = ΔE + ΔZPE - TΔS + ΔGU + ΔGpH                     (S5)

where ΔE is the total energy difference between the reactant and product species adsorbed on catalyst surface obtained directly from DFT calculations, ΔZPE is the change in zero-point energies, T is the temperature (298.15 K), and ΔS is the difference vibrational entropy. The zero-point energy and entropy corrections of the intermediate adsorbed species are obtained from the vibrational frequency calculations and presented in Table S13~16. The e and U are the number of electrons transferred and electrode potential applied (1.23 V); ΔGpH is the free energy correction of pH, which could be calculated by eqn.(S6):

ΔGpH = -kBT × ln10 × pH                        (S6)

The pH is set to 0, therefore the ΔGpH =0.

Fig. S1 (a) TEM image, (b) HRTEM image and (c) HAADF-STEM image of Cu39Ag11 and corresponding EDS mapping for (d1) total, (d2) C, (d3) Cu, (d4) Ag and (d5) O.

Fig. S2 (a) TEM image, (b) HRTEM image and (c) HAADF-STEM image of Cu27Ag23 and corresponding EDS mapping for (d1) total, (d2) C, (d3) Cu, (d4) Ag and (d5) O.

Fig. S3 (a) TEM image, (b) HRTEM image and (c) HAADF-STEM image of Cu12Ag38 and corresponding EDS mapping for (d1) total, (d2) C, (d3) Cu, (d4) Ag and (d5) O.

Fig. S4 (a) TEM image, (b) HRTEM image and (c) HAADF-STEM image of UiO66-NH2 and corresponding EDS mapping for (d1) N, (d2) O, (d3) Zr and (d4) C.

Fig. S5. Size distribution of (a) Cu39Ag11, (b) Cu27Ag23 and (c) Cu12Ag38.

Fig. S6 UV-vis DRS spectra of UiO66-NH2, CuxAg50-x/UiO66-NH2.

Fig. S7 XRD patterns of the prepared CuxAg50-x alloys.

As shown in Fig. S7, the bulk phase separation of metallic Ag0 and Cu0 in CuxAg50-x could be confirmed by XRD patterns, which reveals no distinctive XRD peak shifts induced by the alloying of metallic Ag and Cu phases.

Fig. S8 (a) The XPS total spectra of Cu39Ag11, Cu27Ag23 and Cu12Ag38. High-resolution XPS spectra on (b) Cu, (c) Ag of Cu39Ag11, Cu27Ag23 and Cu12Ag38.

As shown in Fig. S8(a), C1s standard peak was observed at 287 eV for all samples to correct the peak position. The characteristic peaks of Cu 2p, Ag 3d and O 1s of CuxAg50-x catalyst were mainly at 364 eV, 912 eV and 532 eV (Fig. S8(b~c)). With the reduced Cu: Ag molar ratios, the Cu 2p and Ag 3d peaks were gradually shifted to higher and lower binding energy, respectively, which indicates the transfer of electrons from metallic Ag to Cu in CuxAg50-x11,12.

Fig. S9 High-resolution XPS spectra of (a, d, g) Zr 3d, (b, e, h) Cu 2p and (c, f, i) Ag 3d for Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2.

To verify the examine the direction of charge transfer in CuxAg50-x/UiO66-NH2, XPS and SI-XPS techniques were adopted, by which electron density change of various metal atoms in the excited state can be probed13. In the absence of light irradiation, the Zr 3d XPS signal of CuxAg50-x/UiO66-NH2 exhibited a shift to a higher binding energy than that of UiO66-NH2 (Fig. S9(a, d, g)), possibly due to the transfer of electrons from the MOF to CuxAg50-x14,15. Under light irradiation, the Zr 3d binding energy of CuxAg50-x/UiO66-NH2 manifested a positive shift (Fig. S9(a, d, g)), suggesting decreased electron density of the MOF. Meanwhile, the Cu 2p and Ag 3d binding energy of CuxAg50-x/UiO66-NH2 had a negative shift (Fig. S9(b, c, e, f, h, i)), indicating increased electron density of the CuxAg50-x16, 17. Upon light off, the binding energy of Cu 2p, Ag 3d and Zr 3d in CuxAg50-x/UiO66-NH2 returned to their original position, supporting the reversibility of light-induced electron transfer in the composites (Fig. S9). The changed binding energy provided direct evidence on the migration pathways of charge carriers, specifically, from the MOF to CuxAg50-x at the CuxAg50-x/UiO66-NH2 interface under light irradiation.

Fig. S10 Reaction device diagram of photocatalytic CO2 reduction.

Fig. S11 Reaction device for the photocatalytic CO2 reduction.

Fig. S12 The quantitative standard curves of (a) C2H4, (b) CH4, (c) CO, (d) O2, (e) H2, (f) CH3OH and (g) CH3CH2OH.

Fig. S13 The gas chromatography (GC) of standard (a) C2H4, (b) CH4, (c) CO, (d) O2, (e) H2 and the ion chromatography (IC) of standard (f) CH3OH, (g) CH3CH2OH with the reaction over UiO66-NH2, CuxAg50-x/UiO66-NH2.

Fig. S14 Yields of (a) UiO66-NH2, (b) Cu39Ag11/UiO66-NH2, (c) Cu27Ag23/UiO66-NH2 and (d) Cu12Ag38/UiO66-NH2 under different conditions.

To further explore the generation pathways of reduced product in the UiO66-NH2 and CuxAg50-x/UiO66-NH2 photocatalytic system, the six controlled experiments were conducted under different conditions. As shown in Fig. S14, the reduced product yields in the UiO66-NH2 and CuxAg50-x/UiO66-NH2 system were very low (<8 μmol·g-1·h-1) under dark conditions, indicating that UiO66-NH2 and CuxAg50-x/UiO66-NH2 had almost no catalytic ability without illumination. The reduced product yields in the system were also extremely low (<3 μmol·g-1·h-1) with illumination but without a catalyst. The above results confirmed that the light source and photocatalyst played the decisive role in photocatalytic CO2 reduction. Under N2 or Ar atmosphere, the reduced product yield in the UiO66-NH2 and CuxAg50-x/UiO66-NH2 photocatalytic system was zero, implying that the generation of reduced product originated from the CO2 reduction reaction (CO2RR). Finally, the reduced product yields in the UiO66-NH2 and CuxAg50-x/UiO66-NH2 system under the extra addition of sacrificial agent (triethanolamine, TEOA) were slightly higher than those under standard conditions, which might be related to self-decomposition of TEOA for the generation of small amounts of gas8. This indicated that the UiO66-NH2 and CuxAg50-x/UiO66-NH2 could achieve excellent separation of charge carriers without the addition of traditional sacrificial agents, maintaining high photocatalytic activity.

Fig. S15 Photocatalytic CO2RR properties of CuxAg50-x/UiO66-NH2.

As shown in Fig.S15, the CO formation rate of Cu12Ag38 photocatalytic system was 67.2 μmol·g-1·h-1. Cu27Ag23 alloys was beneficial for the conversion of CO2 to CH3OH (43.87 μmol·g-1·h-1) and CH4 (54.32 μmol·g-1·h-1), while Cu39Ag11 alloys was beneficial for the conversion of CO2 into CH3CH2OH (8.77 μmol·g-1·h-1) and C2H4 (15.21 μmol·g-1·h-1), respectively. The selectivity of reduced carbon products for Cu12Ag38, Cu27Ag23 and Cu39Ag11 were C1-(CO) (72.43%), C1-(CH4, CH3OH) (89.88%) and C2-(C2H4, C2H5OH) (83.4%), respectively.

Fig. S16 XRD images of CuxAg50-x/UiO66-NH2 after 5 reactions.

Fig. S17 TEM and HAADF images of (a, b) Cu39Ag11/UiO66-NH2, (c, d) Cu27Ag23/UiO66-NH2 and (e, f) Cu12Ag38/UiO66-NH2 after 5 reactions.

Fig. S18 Comparison of yield under visible light and sunlight.

Fig. S19 Tauc plots of (a) UiO66-NH2. Mott-Schottky curves of (b) UiO66-NH2.

As shown in Fig. S19(a), the bandgap (Eg) values of UiO66-NH2 were calculated to be 2.87 eV, respectively. Next, the flat band potential (Efb) of the semiconductors could be determined through Mott-Schottky (M-S) plots. The longest straight part of the M-S plots served as the tangent (X-axis intercept). As shown in Fig. S19(b), the Efb value of UiO66-NH2 was -0.81 V (vs. Ag/AgCl, pH=7). The potential relative to Ag/AgCl could be converted into the potential relative to the standard hydrogen electrode (NHE) through Nernst equation (eqn.(S7)).

ECB = E(NHE) = E(Ag/AgCl) + 0.197                                              (S7)

In the M-S plots, UiO66-NH2 presented the positive slope, indicating N-type semiconductors. Usually, the Efb value of N-type semiconductors was lower (0.1~0.3 V) than the ECB value13. Finally, the ECB values of UiO66-NH2 was calculated to be -0.61 V (vs. NHE, pH = 0), and the EVB values of UiO66-NH2 was calculated to be 2.26 V (vs. NHE, pH = 0), respectively.

Fig. S20 Tauc plots and Mott-Schottky curves of (a, b) Cu39Ag11/UiO66-NH2, (c, d) Cu27Ag23/UiO66-NH2 and (e, f) Cu12Ag38/UiO66-NH2.

As shown in Fig. S20(a, c, e), the bandgap (Eg) values of Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were calculated to be 1.57 eV, 1.63 eV and 1.69 eV, respectively. As shown in Fig. S20(b, d, f), the Efb values of Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were -0.83 V, -0.92 V and -0.99 V, (vs. Ag/AgCl, pH=7). In the M-S plots, Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 both presented the positive slope, indicating N-type semiconductors. Usually, the Efb value of N-type semiconductors was lower (0.1~0.3 V) than the ECB value13. Finally, the ECB values of Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were calculated to be -0.63 V, -0.72 V and -0.79 V (vs. NHE, pH = 0), and the EVB values of Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were calculated to be 0.94 V, 0.91 V and 0.90 V (vs. NHE, pH = 0), respectively.

Fig. S21 Band structure of UiO66-NH2, Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2.

Fig. S22 The corresponding pore size distributions.

Fig. S23 N2 adsorption-desorption isotherms of (a) Cu39Ag11, (b) Cu27Ag23 and (c) Cu12Ag38. The corresponding pore size distributions of (d) Cu39Ag11, (e) Cu27Ag23 and (f) Cu12Ag38.

The N2 adsorption-desorption isotherms of CuxAg50-x exhibited a significant H3 hysteresis loop, displaying typical IV type curve characteristics. The pore size was mostly distributed between 5-10 nm, indicating that the material belonged to mesoporous materials. The maximum specific surface area of Cu39Ag11 was 35.77 m2·g-1, which was higher than the specific surface areas of Cu27Ag23 (16.83 m2·g-1) and Cu12Ag38 (12.13 m2·g-1).

Fig. S24 (a) In-situ Raman spectra and (b) In-situ DRIFTS spectra for reaction intermediates on UiO66-NH2 at different irradiation times.

Fig. S25 Peak areas of H2O and *CO2 integrated based on the in-situ DRIFTS spectra of (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2.

Fig. S26 Peak areas of *COOH integrated based on the in-situ DRIFTS spectra of (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2.

Fig. S27 Peak areas of C≡O, C=C, C-O-H and C-OH integrated based on the in-situ DRIFTS spectra of (a) Cu39Ag11/UiO66-NH2 and (b) Cu27Ag23/UiO66-NH2.

Fig. S28 Peak areas of CO signal at different applied potentials, which are integrated based on the in-situ DRIFTS spectra of Cu12Ag38/UiO66-NH2.

Fig. S29 Charge density differences of (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2. Plane average charge density difference of (d) Cu39Ag11/UiO66-NH2, (e) Cu27Ag23/UiO66-NH2 and (f) Cu12Ag38/UiO66-NH2. Two-dimensional sectional differential charge density of (g) Cu39Ag11/UiO66-NH2, (h) Cu27Ag23/UiO66-NH2 and (i) Cu12Ag38/UiO66-NH2.

Fig. S30 Work functions and electrostatic potentials of (a) Cu12Ag38, (b) Cu27Ag23, (c) Cu39Ag11 and (d) UiO66-NH2 calculated by DFT (illustrated as a structural optimization model).

The work function was an important parameter in the process of semiconductor photocatalytic reactions, which was used to determine the direction of electron transfer in photocatalysts18. It was defined as the energy of stationary electrons in vacuum (EVAC) minus the Fermi level (EF) of the metal (eqn.(S8)).

Φ= EVAC-EF                                                              (S8)

As shown in Fig. S30(a~d), the functional values of UiO66-NH2, Cu39Ag11, Cu27Ag23 and Cu12Ag38 were calculated to 4.67 eV, 5.06 eV, 4.95 eV and 4.74 eV through DFT. Materials with a lower work function more easily lost electrons19, thus the ability of the three materials to lose electrons was as followed: UiO66-NH2> Cu12Ag38> Cu27Ag23> Cu39Ag11.

Fig. S31 Plane average charge density difference of CO2 on (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2. Two-dimensional sectional differential charge density of CO2 on (d) Cu39Ag11/UiO66-NH2, (e) Cu27Ag23/UiO66-NH2 and (f) Cu12Ag38/UiO66-NH2.

Fig. S32 PDOS of (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2. (d) Schematic illustration of the interactions between the d-band states and the adsorbate states (EF: Fermi energy level).

As shown in Fig. S32(a)~(c), the Ed of Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 were calculated to be −0.87624, −0.91346 and −1.27183 eV, respectively. Ed downshifts depending linearly on the increasing Ag compositions. As the d-band center theory suggests20, the binding strengths of adsorbates on the metal surface depend, to a large extent, on the coupling between the adsorbate states and the metal d-band states, which would create two states, i.e., bonding and antibonding states, as illustrated in Fig. S32(d). The bonding states are usually fully filled by electrons, due to their much lower energy levels than the Fermi energy level (EF). However, the filling of the antibonding states would be dependent on both metal d-band and adsorbate states, which heavily determines the adsorbate-metal binding strength. The downshifted Ed of metal would lower the antibonding states, enabling the antibonding states to be filled with more electrons and thus weakening the adsobate-metal binding strength.

Fig. S33 LDOS of (a) Cu39Ag11/UiO66-NH2, (b) Cu27Ag23/UiO66-NH2 and (c) Cu12Ag38/UiO66-NH2.

Fig. S34 The adsorption configurations of reaction intermediates (CO2, *CO2, *COOH, *CO, *CO-CO, *CO-COH, *CO-CHO, *CHO-CHO, *CHO-COH, *CH2O-CO, *CH2O-CHO, *CH2O-CHOH, *CH2O-CH2OH, *CH2O-CH, *CH2O-CH3, *CH2O-CH2, C2H5OH and C2H4) on the optimized Cu39Ag11/UiO66-NH2.

Fig. S35 The adsorption configurations of reaction intermediates (CO2, *CO2, *COOH, *CO, CO, *CHO, *CH2O, *CH2OH, *CH2, *CH3 and *CH4) on the optimized Cu27Ag23/UiO66-NH2.

Fig. S36 The adsorption configurations of reaction intermediates (CO2, *CO2, *COOH, *CO, CO, and *CHO) on the optimized Cu12Ag38/UiO66-NH2.

Fig. S37 Gibbs free energy and adsorption energy of UiO66-NH2, Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2 for HER.

As shown in Fig. S37, the reaction energy barrier of H2O photolysis in CuxAg50-x/UiO66-NH2 under alkaline conditions had been investigated. The construction of the reaction pathway of alkaline HER included the early stages of hydrolysis to generate H* (Volmer step) and H2 generation (Tafel step or Heyrovsky step). The results indicated that the strong negative H* adsorption energy barrier of CuxAg50-x/UiO66-NH2 could hinder the evolution of H2, leading to slower HER kinetics, which was consistent with the experimental results (Fig.3(a)).

Fig. S38 The photocatalytic CO2RR pathway of CuxAg50-x/UiO66-NH2.

Based on the results of in-situ characterization and DFT calculation, the photocatalytic CO2RR pathway of CuxAg50-x/UiO66-NH2 was proposed (Fig. S38). Firstly, CO2 was adsorbed on CuxAg50-x/UiO66-NH2 to generate *CO2. This generated *CO2 was protonated to produce *COOH intermediate, which was then transformed into *CO intermediate through proton coupled electron transfer (PCET) steps. Importantly, the subsequent reaction of *CO intermediate followed three different pathways. (1) pathway P1: the *COCO intermediate formed by the coupled reaction of two *CO intermediates on Cu39Ag11/UiO66-NH2 was further hydrogenated to generate *COCHO intermediate. Next, *CH2OCHOH and *CH2OCH2O intermediates were generated through the PCET step of *COCHO intermediate. On the one hand, the *CH2OCH intermediate formed by the dehydroxylation reaction of CH2OCHOH intermediate, which was then hydrogenated to form *CH2OCH2 intermediate. The formed *CH2OCH2 was finally deoxygenated to form C2H4. On the other hand, CH2OCH2OH intermediate formed by hydrogenation reaction of *CH2OCH2O intermediate, which was then deoxygenated to form CH2OCH3. Finally, the formed CH2OCH3 was hydrogenated to form C2H5OH. (2) pathway P2: *CHO intermediate generated by electron transfer of *CO intermediate on Cu27Ag23/UiO66-NH2 under proton assistance was protonated to form *CH2O intermediate. The CH2O intermediate was reduced to *CH2OH by hydrogenation. The formed *CH2OH intermediate was subiected to hydrogenation and dihydroxylation reactions to generate CH3OH and *CH2 intermediate. Whereas the *CH2 intermediate was further generated into the *CH3 intermediate through the PCET reaction. Finally, the CH3 intermediate was hydrogenated to generate CH4. (3) pathway P3: *CO intermediate on Cu12Ag38/UiO66-NH2 could be desorbed from the Ag site to generate CO.

Table S1. The feeding amounts of AgNO3 and Cu(OAc)2·H2O for the preparation of CuxAg50-x surface alloys.

| Sample | Ag(NO)3 (mg) | Cu(OAc)2·H2O (mg) |
| --- | --- | --- |
| Cu39Ag11 | 33.74 | 119.65 |
| Cu27Ag23 | 78.24 | 75.16 |
| Cu12Ag38 | 116.58 | 36.81 |

Table S2. The feeding amounts of AgNO3 and Cu(OAc)2·H2O and the reaction times for the preparation of Cu and Ag references.

| Sample | Ag(NO)3 (mg) | Cu(OAc)2·H2O (mg) | Reaction time (min) |
| --- | --- | --- | --- |
| Cu | 0 | 139.82 | 60 |
| Ag | 119.37 | 0 | 90 |

Table S3. The zeta potential of the different samples.

| Entry | Sample | Zeta potential (mV) |
| --- | --- | --- |
| 1 | UiO66-NH2 | +43.71 |
| 2 | Cu39Ag11 | -36.21 |
| 3 | Cu27Ag23 | -40.25 |
| 4 | Cu12Ag38 | -42.87 |

Table S4. The summary of ICP data for samples.

| Entry | Sample | Cu content (wt.%) | Ag content (wt.%) |
| --- | --- | --- | --- |
| 1 | Cu39Ag11/UiO66-NH2 | 28.57 | 8.06 |
| 2 | Cu27Ag23/UiO66-NH2 | 19.78 | 16.85 |
| 3 | Cu12Ag38/UiO66-NH2 | 8.79 | 27.84 |

Table S5. EXAFS fitting parameters at the Cu K-edge for the samples.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Cu-foil | Cu-Cu | 12* | 2.622±0.019 | 0.0057±0.0021 | 5.7±2.8 | 0.0065 |
|  | Cu-Cu | 8* | 2.402±0.024 | 0.0048±0.0024 | 3.6±4.1 |  |
| CuO | Cu-O | 4.3±0.5 | 1.472±0.001 | 0.0133±0.0015 | -1.8±0.4 | 0.0024 |
|  | Cu-Cu | 1.4±0.5 | 2.252±0.001 | 0.0080±0.0008 | 3.7±0.3 |  |
|  | Cu-Cu | 7.8±0.2 | 2.659±0.001 | 0.0006±0.0001 | -5.1±0.6 |  |
| Cu39Ag11/UiO66-NH2 | Cu-O | 1.3±0.1 | 1.543±0.001 | 0.0045±0.0008 | 1.2±0.4 | 0.0023 |
|  | Cu-Cu | 1.9±0.5 | 2.363±0.001 | 0.0105±0.0007 | 2.4±0.5 |  |
|  | Cu-Cu | 2.8±0.5 | 2.674±0.001 | 0.0044±0.0008 | -12.9±0.5 |  |
|  | Cu-Ag | 1.2±0.1 | 3.052±0.001 | 0.0019±0.0008 | -2.5±0.1 |  |
| Cu27Ag23/UiO66-NH2 | Cu-O | 1.6±0.1 | 1.673±0.001 | 0.0045±0.0006 | -1.3±0.3 | 0.0017 |
|  | Cu-Cu | 2.1±0.5 | 2.213±0.001 | 0.0105±0.0006 | 2.2±0.2 |  |
|  | Cu-Cu | 3.1±0.5 | 2.714±0.001 | 0.0044±0.0009 | -12.0±0.1 |  |
|  | Cu-Ag | 1.1±0.1 | 3.087±0.001 | 0.0012±0.0009 | -2.7±0.4 |  |
| Cu12Ag38/UiO66-NH2 | Cu-O | 1.7±0.4 | 1.517±0.001 | 0.0041±0.0012 | 2.1±0.5 | 0.0006 |
|  | Cu-Cu | 2.4±0.6 | 2.142±0.001 | 0.0024±0.0011 | -13.4±0.3 |  |
|  | Cu-Cu | 3.2±0.5 | 2.582±0.001 | 0.0024±0.0012 | -12.1±0.3 |  |
|  | Cu-Ag | 1.0±0.1 | 3.104±0.001 | 0.0008±0.0010 | -2.9±0.6 |  |

aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.705, according to the experimental EXAFS fit of Fe foil by fixing CN as the known crystallographic value. * This value was fixed during EXAFS fitting, based on the known structure of Cu. Fitting range: 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Ag foil); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Ag2O); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Cu39Ag11/UiO66-NH2); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Cu27Ag23/UiO66-NH2) ; 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Cu12Ag38/UiO66-NH2). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 15 eV; R factor < 0.02.

Table S6. EXAFS fitting parameters at the Ag K-edge for the samples.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Ag-foil | Ag-Ag | 12* | 2.642±0.019 | 0.0051±0.0020 | 5.1±2.8 | 0.0057 |
| Ag2O | Ag-O | 1.5±0.5 | 1.752±0.001 | 0.0133±0.0012 | -1.9±0.4 | 0.0023 |
|  | Ag-Ag | 2.9±0.2 | 2.879±0.001 | 0.0006±0.0001 | -9.9±0.6 |  |
| Cu39Ag11/UiO66-NH2 | Ag-Ag | 2.6±0.2 | 2.814±0.001 | 0.0043±0.0007 | -12.8±0.1 | 0.0008 |
|  | Cu-Ag | 0.9±0.1 | 3.052±0.001 | 0.0017±0.0012 | -2.4±0.3 |  |
| Cu27Ag23/UiO66-NH2 | Ag-Ag | 2.7±0.2 | 2.734±0.001 | 0.0045±0.0008 | -12.8±0.1 | 0.0019 |
|  | Cu-Ag | 0.9±0.1 | 3.087±0.001 | 0.0015±0.0009 | -2.6±0.1 |  |
| Cu12Ag38/UiO66-NH2 | Ag-Ag | 2.9±0.2 | 2.692±0.001 | 0.0024±0.0011 | -11.4±0.5 | 0.0023 |
|  | Cu-Ag | 0.9±0.1 | 3.104±0.001 | 0.0013±0.0008 | -2.8±0.6 |  |

aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.705, according to the experimental EXAFS fit of Fe foil by fixing CN as the known crystallographic value. * This value was fixed during EXAFS fitting, based on the known structure of Ag. Fitting range: 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Ag foil); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.5 (Ag2O); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.5 (Cu39Ag11/UiO66-NH2); 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.5 (Cu27Ag23/UiO66-NH2) ; 1.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.5 (Cu12Ag38/UiO66-NH2). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 15 eV; R factor < 0.02.

Table S7. Intensity of different monochromatic light.

| Wavelength (nm) | Light intensity (mW·cm-2) |
| --- | --- |
| 400 | 26.37 |
| 450 | 22.41 |
| 500 | 19.86 |
| 550 | 16.53 |
| 600 | 13.72 |

Table S8. Comparison of photocatalytic activity of different samples.

| Photocatalysts | Light source | Products | Yield (μmol·g-1·h-1) | Selectivity (%) | Reference | AQY (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Cu39Ag11/UiO66-NH2 | 300W Xe lamp | C2H4/C2H5OH | 64.72/38.64 | 91.67% | This work | 10.1% (385 nm) |
| Cu27Ag23/UiO66-NH2 | 300W Xe lamp | CH4/CH3OH | 132.44/108.25 | 96.25% | This work | 8.4% (385 nm) |
| Cu12Ag38/UiO66-NH2 | 300W Xe lamp | CO | 162.47 | 93.01% | This work | 7.6% (385 nm) |
| UiO-66-NH2 | 500W Xe lamp | CO | 26.4 | N/A | [21] | N/A |
| Pt/MIL-125(Ti)-NH2 | 300W Xe lamp | CO | 32.4 | N/A | [22] | N/A |
| Au/MIL-125(Ti)-NH2 | 300W Xe lamp | CO | 16.3 | N/A | [23] | N/A |
| Cu NCs@MOF-801 | 300W Xe lamp | HCOOH | 94 | N/A | [24] | N/A |
| Cu NCs@UiO-66-NH2 | 300W Xe lamp | HCOOH | 128 | N/A | [25] | N/A |
| UiO-66-NH2 (Zr/Ti) | 300W Xe lamp | CO | 4.66 | N/A | [26] | N/A |
| Co-ZIF-9/TiO2 | 200≤λ≤900nm | CH4/CO | 2/17.6 | N/A | [27] | N/A |
| MCOF-Ti6Cu3 | 300W Xe lamp | HCOOH | 77.3 | N/A | [28] | N/A |
| Au-NC@UiO-68-NHC | 300W Xe lamp | CO | 145.3 | 90% | [29] | N/A |
| Pd@PCN-222(Co) | 300W Xe lamp | CO | 23.4 | 68.8% | [30] | N/A |
| Pt@NH2 -UiO-68 | 300W Xe lamp | CO | 66.7 | N/A | [31] | N/A |
| MAPbI3@PCN-221(Fe) | 300W Xe lamp | CH4/CO | 12.9/6.6 | N/A | [32] | N/A |
| CsPbBr3@ZIF-8 | 100W Xe lamp | CH4/CO | 1.81/0.51 | N/A | [33] | N/A |
| Au/PPF-3 | Visible-light | CO | 42.7 | N/A | [34] | N/A |
| (Zr-PMOF)/ultrathin g-C3N4 | λ> 420 nm | CO | 5.5 | N/A | [35] | N/A |

Table S9. Fluorescence decay time (τi) and fitting data (Ai) of sample.

| Sample | τ1 (ns) | τ2 (ns) | A1 (%) | A2 (%) | τavg (ns) |
| --- | --- | --- | --- | --- | --- |
| UiO66-NH2 | 0.5737 | 3.2764 | 774.218 | 34.034 | 3.206 |
| Cu39Ag11/UiO66-NH2 | 0.4764 | 3.9257 | 859.997 | 7.622 | 2.098 |
| Cu27Ag23/UiO66-NH2 | 0.5382 | 3.4625 | 813.276 | 29.172 | 2.871 |
| Cu12Ag38/UiO66-NH2 | 0.5578 | 3.3903 | 796.606 | 32.391 | 3.063 |

Table S10. Pore structure parameters of the samples.

| Sample | SBET(m2∙g-1) | Pore volume (mL∙g-1) | Pore size (nm) |
| --- | --- | --- | --- |
| Cu39Ag11/UiO66-NH2 | 773.81 | 0.48 | 1.54 |
| Cu27Ag23/UiO66-NH2 | 751.12 | 0.44 | 1.36 |
| Cu12Ag38/UiO66-NH2 | 742.37 | 0.42 | 3.02 |

Table S11. The results of CuxAg50-x/UiO66-NH2 Bader charge calculation.

| Type | CHARGE in hetero (e-) | CHARGE TRANSFER (e-) |
| --- | --- | --- |
| UiO66-NH2 | 237.986516 | -1.375614 |
| Cu39Ag11 | 534.665474 | 1.175321 |
| UiO66-NH2 | 246.844169 | -0.914612 |
| Cu27Ag23 | 518.986615 | 0.828158 |
| UiO66-NH2 | 255.671549 | -0.734648 |
| Cu12Ag38 | 499.778114 | 0.671879 |

Table S12. The results of CuxAg50-x/UiO66-NH2 and CO2 Bader charge calculation.

| Type | CHARGE in hetero (e-) | CHARGE TRANSFER (e-) |
| --- | --- | --- |
| Cu39Ag11/UiO66-NH2 | 257.154376 | -0.692542 |
| CO2 | 485.922154 | 0.559135 |
| Cu27Ag23/UiO66-NH2 | 262.642582 | -0.588267 |
| CO2 | 474.349751 | 0.460661 |
| Cu12Ag38/UiO66-NH2 | 273.379458 | -0.449265 |
| CO2 | 458.823467 | 0.372156 |

Table S13. The calculated zero-point energy and entropy of different adsorbed species on the Cu12Ag38/UiO66-NH2.

| Adsorption species | EZPE (eV) | TS (eV) |
| --- | --- | --- |
| *CO2 | 0.47 | 0.75 |
| *COOH | 0.09 | 1.36 |
| *CO | 0.56 | 0.73 |
| *CHO | 0.72 | 0.85 |
| CO | 0.38 | 0.19 |

* represented the adsorption site.

Table S14. The calculated zero-point energy and entropy of different adsorbed species on the Cu27Ag23/UiO66-NH2.

| Adsorption species | EZPE (eV) | TS (eV) |
| --- | --- | --- |
| *CO2 | 0.47 | 0.75 |
| *COOH | 0.09 | 1.36 |
| *CO | 0.56 | 0.73 |
| *CHO | 0.36 | 0.27 |
| *CH2O | 0.47 | 0.54 |
| *CH2OH | 1.11 | 1.44 |
| CH3OH | 0.87 | 0.91 |
| *CH2 | 2.36 | 0.83 |
| *CH3 | 1.87 | 1.39 |
| CH4 | 0.49 | 0.63 |
| CO | 0.98 | 1.15 |

* represented the adsorption site.

Table S15. The calculated zero-point energy and entropy of different adsorbed species on the Cu39Ag11/UiO66-NH2.

| Adsorption species | EZPE (eV) | TS (eV) |
| --- | --- | --- |
| *CO2 | 0.47 | 0.75 |
| *COOH | 0.09 | 1.36 |
| *CO | 0.56 | 0.73 |
| *CO-CO | 0.19 | 0.23 |
| *COH-CO | 0.53 | 0.55 |
| *CHO-CO | 0.73 | 0.58 |
| *CHO-COH | 2.51 | 2.23 |
| *CH2O-CO | 1.62 | 1.21 |
| *CHO-CHO | 0.51 | 0.81 |
| *CH2O-CHO | 0.47 | 0.53 |
| *CH2O-CHOH | 1.74 | 1.89 |
| *CH2OH-CH2O | 1.47 | 1.21 |
| *CH2O-CH | 0.49 | 1.47 |
| *CH2O-CH3 | 0.74 | 0.89 |
| *CH2O-CH2 | 0.11 | 0.19 |
| CH3CH2OH | 0.13 | 0.24 |
| C2H4 | 0.32 | 0.22 |

* represented the adsorption site.

Table S16. The calculated zero-point energy and entropy of *H species on UiO66-NH2, Cu39Ag11/UiO66-NH2, Cu27Ag23/UiO66-NH2 and Cu12Ag38/UiO66-NH2.

| Photocatalysts | Adsorption species | ΔG (eV) |
| --- | --- | --- |
| UiO66-NH2 | *H | -0.43 |
| Cu39Ag11/UiO66-NH2 | *H | 0.74 |
| Cu27Ag23/UiO66-NH2 | *H | 1.18 |
| Cu12Ag38/UiO66-NH2 | *H | 1.63 |

* represented the adsorption site

References for Supporting Information

- B. Ravel, M. Newville and A. ATHENA, Journal of Synchrotron Radiation. 2005, 12, 537-541.

- S. Zabinsky, J. Rehr, A. Ankudinov, R. Albers and M. Eller, Phys. Rev. B., 1995, 52, 2995−3009.

- G. Kresse and D. Joubert, Physical Review B., 1999, 59, 1758-177.

- J. Perdew, K. Burke and M. Ernzerhof, Physical Review Letters., 1996, 77, 3865-3868.

- J. Jin, J. Luo, L. Zan and T. Peng, ChemPhysChem., 2017, 18, 3230-3239.

- T. Le, T. Nguyen, Z. Yacouba, L. Zoungrana, F. Avril, D. Nguyen, E. Petit, J. Mendret and V. Bonniol, Chemosphere., 2017, 172, 1-9.

- Q. Mei, J. Sun, D. Han, B. Wei, Z. An, X. Wang, J. Xie, J. Zhan and M. He, Chem. Eng. J., 2019, 373, 668-676.

- L. Collado, A. Reynal, J. Coronado, D. Serrano, J. Durrant and V. De la Peña O'Shea, Applied Catalysis B: Environmental., 2015, 178, 177-185.

- M. Xing, Y. Zhou, C. Dong, L. Cai, L. Zeng, B. Shen and Y. Yin, Nano letters., 2018, 18, 3384-3390.

- W. He, Y. Wei, J. Xiong, Z. Tang, W. Song, J. Liu and Z. Zhao, Chem. Eur. J., 2022, 433, 133540.

- D. Liu, L. Jiang, D. Chen, Z. Hao, B. Deng, Y. Sun, X. Liu, B. Jia, L. Chen, H. Liu, ACS Catalysis., 2024, 14, 5326-5343.

- J. Jiao, R. Lin, S. Liu, W. Cheong, C. Zhang, Z. Chen, Y. Pan, J. Tang, K. Wu, S. Hung, H. Chen, L. Zheng, Q. Lu, X. Yang, B. Xu, H. Xiao, J. Li, D. Wang, Q. Peng, C. Chen, Y. Li, Nat. Chem., 2019, 11, 222–228.

- W. Ren, X. Tan, J. Qu, S. Li, J. Li, X. Liu, S. Ringer, J. Cairney, K. Wang, S. Smith, C. Zhao, Nat. Commun., 2021, 12, 1449.

- S. Dai, T. Huang, W. Liu, C. Hsu, S. Lee, T. Chen, Y. Wang, J. Wang, K. Wang, Nano Lett., 2021, 21, 9293–9300.

- H. Liu, J. Xia, N. Zhang, H. Cheng, W. Bi, X. Zu, W. Chu, H. Wu, C. Wu, Y. Xie, Nat. Catal., 2021, 4, 202–211.

- X. Cao, A. J. Huang, C. Liang, H. C. Chen, T. Han, R. Lin, Q. Peng, Z. W. Zhuang, R. G. Shen, H. M. Chen, Y. Yu, C. Chen and Y. D. Li, J. Am. Chem. Soc., 2022, 144, 3386–3397.

- Y. Duan, Y. Wang, W. Zhang, J. Zhang, C. Ban, D. Yu, K. Zhou, J. Tang, X. Zhang, X. Han, L. Gan, X. Tao and X. Zhou, Adv. Funct. Mater., 2023, 33, 2301729.

- S. Yu, X. Cheng, Y. Wang, B. Xiao, Y. Xing, J. Ren, Y. Lu, H. Li, C. Zhuang and G. Chen, Nat. Commun., 2022, 13, 4737.

- A. Chen, X. Yu, Y. Zhou, S. Miao, Y. Li, S. Kuld, J. Sehested, J. Liu, T. Aoki, S. Hong, M. Camellone, S. Fabris, J. Ning, C. Jin, C. Yang, A. Nefedov, C. Wo¨ll, Y. Wang and W. Shen, Nat. Catal., 2019, 2, 334–341.

- Y. Feng, C. Wang, P. Cui, C. Li, B. Zhang, L. Gan, S. Zhang, X. Zhang, X. Zhou, Z. Sun, K. Wang, Y. Duan, H. Li, K. Zhou, H. Huang, A. Li, C. Zhuang, L. Wang, Z. Zhang and X. Han, Adv. Mater., 2022, 34, e2109074.

- D. Sun, Y. Fu, W. Liu, L. Ye, D. Wang, L. Yang, X. Fu and Z. Li, Chem. Eur. J., 2013, 19 (42), 14279-14285.

- D. Sun, W. Liu, Y. Fu, Z. Fang, F. Sun, X. Fu, Y. Zhang and Z. Li, Chem. Eur. J., 2014, 20 (16), 4780-4788.

- Y. Fu, D. Sun, Y. Chen, R. Huang, Z. Ding, X. Fu and Z. Li, Angew. Chem., Int. Ed., 2012, 51 (14), 3364-3367.

- S. Dai, T. Kajiwara, M. Ikeda, I. Romero‐Muñiz, G. Patriarche, A. Platero‐Prats and A. Vimont, Angew. Chem., Int. Ed., 2022, 61(43): e202211848.

- S. Dai, C. Simms, I. Dovgaliuk, G. Patriarche, A. Tissot, T. Parac-Vogt and C. Serre, Chem. Mater., 2021, 33 (17), 7057-7066.

- Y. Lee, S. Kim, J. Kang and S. Cohen, Chem. Commun., 2015, 51 (26), 5735-5738.

- S. Yan, S. Ouyang, H. Xu, M. Zhao, X. Zhang, and J. Ye, J. Mater. Chem. A., 2016, 4, 15126-15133.

- J. Zhou, J. Li, L. Kan, L. Zhang, Q. Huang, Y. Yan, Y. Chen, J. Liu, S. Li and Y. Lan, Nat. Commun., 2022, 13(1): 4681.

- Y. Jiang, Y. Yu, X. Zhang, M. Weinert, X. Song, J. Ai, L. Han and H. Fei, Angew. Chem. Int. Ed., 2021, 60, 17388 –17393.

- S. Fu, S. Yao, S. Guo, G. Guo, W. Yuan, T. Lu and Z. Zhang, J. Am. Chem. Soc., 2021, 143, 20792−20801.

- F. Guo, Y. Wei, S. Wang, X. Zhang, F. Wang and W. Sun, J. Mater. Chem. A., 2019, 7, 26490-26495.

- L. Wu, Y. Mu, X. Guo, W. Zhang, Z. Zhang, M. Zhang and T. Lu, Angew. Chem. Int. Ed., 2019, 58, 9491-9495.

- Z. Kong, J. Liao, Y. Dong, Y. Xu, H. Chen, D. Kuang and C. Su, ACS Energy Lett., 2018, 3, 2656-2662.

- L. Chen, Y. Wang, F. Yu, X. Shen and C. Duan, J. Mater. Chem. A., 2019, 7, 11355-11361.

- Y. Wang, W. Zhen, Y. Zeng, S. Wan, H. Guo, S. Zhang and Q. Zhong, J. Mater. Chem. A., 2020, 8, 6034-6040.