SUPPLEMENTARY INFORMATION

Effect of the catechol structure on the functionalization and magnetic properties of barium hexaferrite nanoplatelets

Katja Drobež, ab Nina Popov a* and Darja Lisjak a

aDepartment for Material Synthesis, Jožef Stefan Institute, 1000 Ljubljana, Slovenia

bJožef Stefan International Postgraduate School, 1000 Ljubljana, Slovenia

- * now with the Ruđer Boskovic Institute, Bijenicka cesta 54, 10 000 Zagreb, Croatia

Fig. S1 XRD pattern of the BHF NPLs.

Fig. S2 Thermal analysis data: On the top are the TGA curves for the ligands (CAFA - left and DA -right), the core, and functionalized NPLs. The left y-axis depicts the total mass loss of the NPLs and the right y-axis depicts the mass loss of the ligand. At the bottom are MS spectra of the functionalized NPLs. In the MS spectra of BHF@CAFA10, the fragments with m/z = 17 correspond to OH, m/z = 18 to H2O, m/z = 28 to CO and C2H4, m/z = 30 to NO, m/z = 43 to C3H7, m/z = 44 to CO2, and m/z = 46 to NO2 and CH2O2. In the MS spectra of BHF@DA10, the fragments with m/z = 17 correspond to OH and NH3, m/z = 18 to H2O, m/z = 28 to CO and C2H4, m/z = 30 to NO, m/z = 43 to C3H7, m/z = 44 to CO2, and m/z = 46 to NO2 and CH2O2.

Fig. S3 Zeta potential behavior of the NPLs functionalized using the US and heating (labeled with 80) method with 2 and 10 molecules/nm2 of: a) CAT, b) CAFA, and c) DA.

Fig. S4 The core BHFb NPLs: a) TEM image with the corresponding SAED (in the inset), and b) diameter distribution.

Fig. S5 Thermal analyses results of the core and functionalized BHFb NPLs samples prepared by the US method: a) TGA (also with data for CAT) and b, c) mass spectra. On the graph a), the left y-axis depicts the total mass loss of the NPLs and the right y-axis depicts the mass loss of the ligand. The fragments in panels b and c with m/z = 17 correspond to OH, m/z = 18 to H2O, m/z = 28 to CO and C2H4, m/z = 30 to NO, m/z = 43 to C3H7, m/z = 44 to CO2, and m/z = 46 to C2H6O and CH2O2, m/z = 53 to C6H5, m/z = 56 to CnH2n-1, and m/z = 57 to CnH2n+1.

Fig. S6 Zeta potential behavior of the functionalized BHFb NPLs with a nominal surface density of 10 CAT molecules/nm2 using the US method. For comparison, the zeta-potential behavior of the core BHFb NPLs is also shown. Error bars denote the standard deviation of a measured point.

Fig. S7 Zeta potential behaviors of the fresh, 7 days (t = 7 d), and a month-old (t = 1 m) DA-functionalized NPLs with 2 molecules of DA/nm2 prepared with the heating method: a) unwashed functionalized NPLs and b) washed samples. Error bars denote the standard deviation of a measured point.

Fig. S8 Magnetization hysteresis loops of the NPLs functionalized using the US method with 2 and 10 molecules/nm2: a) CAT, b) CAFA, and c) DA. For comparison, the hysteresis loop of the core BHF NPLs is added.