Supporting Information

Photoinduced solid-to-liquid transition of an N-benzylideneaniline derivative towards smart glass

Jing Huab and Haifeng Yu*b

a. School of Mechanical Engineering, Shenyang University, Shenyang, 110044, Liaoning, China

b. School of Materials Science and Engineering, Key Laboratory of Polymer Chemistry and Physics of Ministry of Education, Peking University, Beijing, 100871, China.

*Email: yuhaifeng@pku.edu.cn

Content

1. Supplementary Figures

2. Supplementary Movie

1. Supplementary Figures

Fig. S1 1H NMR (500 MHz, CDCl3): δ 8.36 (s, 1H, CH), 7.74 (s, 1H; Ar H), 7.60 (d, J = 8.2 Hz, 1H; Ar H), 7.18 (d, J = 8.8 Hz, 2H, Ar H), 6.90 (d, J = 8.8 Hz, 1H; Ar H), 6.85 (d, J = 8.4 Hz, 2H; Ar H), 3.95–4.03 (m, 4H, CH2), 2.27 (s, 3H, CH3), 1.75–1.84 (m, 4H, CH2), 1.42-1.51 (m, 4H, CH2), 1.27 (m, 32H), 0.88 (m, 6H, CH3).

Fig. S2 13C NMR (500 MHz, CDCl3): δ 158.3, 157.5, 130.3, 128.7, 127.4, 122.0, 115.0, 110.6, 68.3, 31.9, 29.6, 29.4, 29.3, 26.1, 22.7, 16.2, 14.1.

Fig. S3 Fabrication schematic of smart glass. (a) MCN and 5CB were dissolved in THF and fully stirred. Then, the solution was dropped on the glass. The glass was kept on 60°C hot stage to make sure the THF was fully vapored. (b) and (c) Another piece of glass was covered on top of the mixture. The two piece of glass was glued by commercial adhesive. The sample thickness can be adjusted by altering the spacer. (b) Thick sample with LDPE spacer (25 m). (c) Thin sample without spacer (5 m).

Fig. S4 (a) 365 nm UV irradiated DSC sample at cool atmosphere of liquid nitrogen. (b) Before UV irradiation. (c) After UV irradiation.

Fig. S5 A series of MCN-5CB samples denoted by MCN molar ratio. (a) Thin sample-3%. (b) Thick sample-33%. (c) Thick sample-48%. (d) Thick sample-58%.

Fig. S6 POM images of MCN-5CB samples. (a) Pure-MCN. (b) 97%-MCN. (c)33%-MCN. (d)3%-MCN. (e) Pure 5CB.

Fig. S7 Sample microstructure diagram of MCN-5CB doping system. (a) to (f) shows the plausible microphase separation with different MCN molar ratio (lower right corner).

Fig. S8 The plausible phase diagram of MCN-5CB according to Figure S3-S5.

Fig. S9 POM video screenshots of 3%-MCN sample. The thickness of sample central area was 5 m. The time in the upper left corner was recorded continuously from UV ON.

Fig. S10 POM video screenshots of 3%-MCN sample. The thickness of sample edge region was 3 m. The time in the upper left corner was recorded continuously from UV ON.

Fig. S11 Plausible RTPT mechanism schematic of 3%-MCN sample.

2. Supplementary Movie

Movie S1. RTPT and photo-switchable transmittance of smart glass samples. (1) RTPT of 3%-MCN sample (center), Figure S7. (2) RTPT of 3%-MCN sample (edge), Figure S8. (3) RTPT of 33%-MCN sample, Figure 6. (4) Photo-switchable transmittance, Figure 10.