SUPPORTING INFORMATION

Lattice Engineering for Enhancing Stability of CsPbI3/CsxFA1–xPbI3 Quantum Dots Synthesized via Direct Arrangement

Paundra Rizky Pratama,a Azzah Dyah Pramata,a* Yuki Suenari,b Jonas Karl Christopher N. Agutaya,c Yu Nagata,b Takeshi Shinkai,b Yusuke Inomata,d Mas Irfan Purbawanto Hidayat,a Biplap Manna,e Yuji Akaishi,f* Tetsuya Kidac, d, f*

- Department of Materials Engineering, Faculty of Industrial Technology and Systems Engineering, Institut Teknologi Sepuluh Nopember, Surabaya 60111, Indonesia

- Graduate School of Science and Technology (GSST), Kumamoto University, Kumamoto 860-8555, Japan

- International Research Organization for Advanced Science and Technology (IROAST), Kumamoto University, Kumamoto 860-8555, Japan

- Faculty of Advanced Science and Technology, Kumamoto University, Kumamoto 860-8555, Japan

- National Institute for Materials Science (NIMS), Tsukuba, Ibaraki 305-0044, Japan.

- Institute of Industrial Nanomaterials (IINa), Kumamoto University, Kumamoto 860–8555, Japan

*Corresponding authors: azzah@its.ac.id (A. D. Pramata); akaishi@kumamoto-u.ac.jp (Y. Akaishi); tetsuya@kumamoto-u.ac.jp (T. Kida)

Figure S1. FTIR Spectra of Cs-Oleate, FA-Oleate, and CsxFA1-x-Oleate.

Figure S2. Lattice parameters for the 2×2×1 orthorhombic supercell of CsPbI3.

Table S1. Effect of the kinetic energy cutoff (Ecut,wfc) on the computed lattice parameters a, b, and c (as indicated in Figure S2), and total energy of the system E. The calculations were performed with a kinetic energy cutoff for the charge density set to 10 times the Ecut,wfc (Ecut,rho = 10Ecut,wfc) and the number of k-points set to 4×4×8.

| Ecut,wfc, Ry | a = b, Å | %diff | c, Å | %diff | E, Ry | %diff |
| --- | --- | --- | --- | --- | --- | --- |
| 25 | 10.9699 |  | 5.4850 |  | –9685.0222 |  |
| 50 | 12.6317 | 15.15 | 6.3158 | 15.15 | –9694.0245 | 0.09 |
| 75 | 12.6295 | 0.02 | 6.3148 | 0.02 | –9694.0588 | < 0.01 |

Table S2. Effect of the factor n in Ecut,rho = nEcut,wfc on the computed lattice parameters a, b, and c (as indicated in Figure S2), and total energy of the system E. The calculations were performed with Ecut,rho = 50 Ry and the number of k-points set to 4×4×8.

| n | a = b, Å | %diff | c, Å | %diff | E, Ry | %diff |
| --- | --- | --- | --- | --- | --- | --- |
| 8 | 12.6316 |  | 6.3158 |  | –9694.0245 |  |
| 10 | 12.6317 | < 0.01 | 6.3158 | < 0.01 | –9694.0245 | < 0.01 |
| 12 | 12.6316 | < 0.01 | 6.3158 | < 0.01 | –9694.0245 | < 0.01 |

Table S3. Effect of the number of k-points on the computed lattice parameters a, b, and c (as indicated in Figure S2), and total energy of the system E. The calculations were performed with Ecut,wfc = 50 Ry and Ecut,rho = 500 Ry (10Ecut,wfc).

| No. of k-points | a = b, Å | %diff | c, Å | %diff | E, Ry | %diff |
| --- | --- | --- | --- | --- | --- | --- |
| 2×2×4 | 12.6559 |  | 6.3279 |  | –9694.0122 |  |
| 4×4×8 | 12.6317 | 0.19 | 6.3158 | 0.19 | –9694.0245 | < 0.01 |
| 8×8×16 | 12.6310 | < 0.01 | 6.3155 | < 0.01 | –9694.0247 | < 0.01 |

The difference (%diff) in Tables S1–S3 was computed using the following formula:

%diff=Mj-MiMi×100%

where Mi (a, b, c, or E) is the property at the parameter (Ecut,wfc, n, or no. of k-points) immediately lower than j.

Table S4. Peak list of simulated XRD for Cubic CsPbI3 (mp-1069538)

| h | k | L | d (Å) | 2θ | I | M |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 6.2894 | 14.06997 | 37.33092 | 6 |
| 1 | 1 | 0 | 4.447277 | 19.94858 | 36.46261 | 12 |
| 1 | 1 | 1 | 3.631187 | 24.49482 | 39.3404 | 8 |
| 2 | 0 | 0 | 3.1447 | 28.35784 | 100 | 6 |
| 2 | 1 | 0 | 2.812705 | 31.78856 | 21.89382 | 24 |
| 2 | 1 | 1 | 2.567637 | 34.91546 | 18.50887 | 24 |
| 2 | 2 | 0 | 2.223639 | 40.5361 | 76.20443 | 12 |
| 2 | 2 | 1 | 2.096467 | 43.11392 | 9.65725 | 24 |
| 3 | 0 | 0 | 2.096467 | 43.11392 | 2.41431 | 6 |
| 3 | 1 | 0 | 1.988883 | 45.57333 | 8.86268 | 24 |
| 3 | 1 | 1 | 1.896325 | 47.93329 | 18.10158 | 24 |
| 2 | 2 | 2 | 1.815593 | 50.20856 | 27.27831 | 8 |
| 3 | 2 | 0 | 1.744366 | 52.41089 | 5.5112 | 24 |
| 3 | 2 | 1 | 1.680913 | 54.54987 | 10.46145 | 48 |
| 4 | 0 | 0 | 1.57235 | 58.6682 | 12.83201 | 6 |
| 4 | 1 | 0 | 1.525404 | 60.65989 | 3.57242 | 24 |
| 3 | 2 | 2 | 1.525404 | 60.65989 | 3.57242 | 24 |
| 3 | 3 | 0 | 1.482426 | 62.61338 | 1.73512 | 12 |
| 4 | 1 | 1 | 1.482426 | 62.61338 | 3.47024 | 24 |
| 3 | 3 | 1 | 1.442887 | 64.53295 | 7.36021 | 24 |
| 4 | 2 | 0 | 1.406353 | 66.42235 | 35.46169 | 24 |
| 4 | 2 | 1 | 1.37246 | 68.28493 | 5.0421 | 48 |
| 3 | 3 | 2 | 1.340905 | 70.12369 | 2.50065 | 24 |
| 4 | 2 | 2 | 1.283818 | 73.7404 | 26.35742 | 24 |
| 4 | 3 | 0 | 1.25788 | 75.52311 | 1.90468 | 24 |
| 5 | 0 | 0 | 1.25788 | 75.52311 | 0.47617 | 6 |
| 4 | 3 | 1 | 1.233453 | 77.29161 | 3.85641 | 48 |
| 5 | 1 | 0 | 1.233453 | 77.29161 | 1.92821 | 24 |
| 3 | 3 | 3 | 1.210396 | 79.04788 | 1.39111 | 8 |
| 5 | 1 | 1 | 1.210396 | 79.04788 | 4.17334 | 24 |
| 4 | 3 | 2 | 1.167912 | 82.53111 | 3.05984 | 48 |
| 5 | 2 | 0 | 1.167912 | 82.53111 | 1.52992 | 24 |
| 5 | 2 | 1 | 1.148282 | 84.26156 | 3.16036 | 48 |
| 4 | 4 | 0 | 1.111819 | 87.70833 | 8.75754 | 12 |
| 4 | 4 | 1 | 1.094844 | 89.42783 | 1.30241 | 24 |
| 5 | 2 | 2 | 1.094844 | 89.42783 | 1.30241 | 24 |
| 4 | 3 | 3 | 1.078623 | 91.14681 | 1.37142 | 24 |
| 5 | 3 | 0 | 1.078623 | 91.14681 | 1.37142 | 24 |
| 5 | 3 | 1 | 1.063103 | 92.86683 | 6.01461 | 48 |
| 4 | 4 | 2 | 1.048233 | 94.58944 | 15.55006 | 24 |
| 6 | 0 | 0 | 1.048233 | 94.58944 | 3.88751 | 6 |
| 6 | 1 | 0 | 1.033971 | 96.31621 | 1.17239 | 24 |
| 6 | 1 | 1 | 1.020275 | 98.04877 | 1.25708 | 24 |
| 5 | 3 | 2 | 1.020275 | 98.04877 | 2.51415 | 48 |
| 6 | 2 | 0 | 0.994441 | 101.5379 | 14.56486 | 24 |
| 6 | 2 | 1 | 0.982239 | 103.2981 | 2.22617 | 48 |
| 4 | 4 | 3 | 0.982239 | 103.2981 | 1.11309 | 24 |
| 5 | 4 | 0 | 0.982239 | 103.2981 | 1.11309 | 24 |
| 5 | 4 | 1 | 0.970476 | 105.0711 | 2.42696 | 48 |
| 5 | 3 | 3 | 0.959125 | 106.859 | 2.69027 | 24 |
| 6 | 2 | 2 | 0.948163 | 108.664 | 14.35406 | 24 |
| 5 | 4 | 2 | 0.937568 | 110.4885 | 2.22318 | 48 |
| 6 | 3 | 0 | 0.937568 | 110.4885 | 1.11159 | 24 |
| 6 | 3 | 1 | 0.927321 | 112.3349 | 2.46075 | 48 |
| 4 | 4 | 4 | 0.907797 | 116.1052 | 4.95215 | 8 |
| 6 | 3 | 2 | 0.898486 | 118.0356 | 2.33177 | 48 |
| 7 | 0 | 0 | 0.898486 | 118.0356 | 0.29147 | 6 |
| 5 | 4 | 3 | 0.889455 | 120.0014 | 2.61839 | 48 |
| 5 | 5 | 0 | 0.889455 | 120.0014 | 0.6546 | 12 |
| 7 | 1 | 0 | 0.889455 | 120.0014 | 1.30919 | 24 |
| 5 | 5 | 1 | 0.880692 | 122.0069 | 2.94087 | 24 |
| 7 | 1 | 1 | 0.880692 | 122.0069 | 2.94087 | 24 |
| 6 | 4 | 0 | 0.872183 | 124.0573 | 16.16672 | 24 |
| 6 | 4 | 1 | 0.863916 | 126.1586 | 2.57464 | 48 |
| 7 | 2 | 0 | 0.863916 | 126.1586 | 1.28732 | 24 |
| 6 | 3 | 3 | 0.855879 | 128.3178 | 1.46799 | 24 |
| 5 | 5 | 2 | 0.855879 | 128.3178 | 1.46799 | 24 |
| 7 | 2 | 1 | 0.855879 | 128.3178 | 2.93598 | 48 |

Table S5. The reference information of the XRD pattern for Orthorhombic CsPbI31

| Chemical formula | Pb4.00Cs4.00I12.00 |
| --- | --- |
| Ref. code | 96-412-7360 |
| Crystal system | Orthorhombic |
| Space group | Pnma |
| Space group number | 62 |
| a | 8.864 |
| b | 12.484 |
| c | 8.578 |
| Alpha | 90 |
| Beta | 90 |
| Gamma | 90 |
| Calculated density | 5.04 |
| Volume of cell | 949.23 |
| RIR | 3.83 |

Table S6. Peak list of XRD data for Orthorhombic CsPbI3

| h | k | l | d [A] | 2Theta[deg] | I [%] |
| --- | --- | --- | --- | --- | --- |
| 0 | 1 | 1 | 7.06989 | 12.51 | 0.7 |
| 0 | 2 | 0 | 6.242 | 14.177 | 30.9 |
| 1 | 0 | 1 | 6.16419 | 14.357 | 56.4 |
| 1 | 1 | 1 | 5.52713 | 16.022 | 3.8 |
| 2 | 0 | 0 | 4.432 | 20.018 | 20.4 |
| 1 | 2 | 1 | 4.38599 | 20.23 | 55.5 |
| 0 | 0 | 2 | 4.289 | 20.693 | 18.6 |
| 2 | 1 | 0 | 4.17661 | 21.256 | 2.3 |
| 2 | 0 | 1 | 3.9375 | 22.563 | 11.5 |
| 1 | 0 | 2 | 3.86079 | 23.018 | 13.5 |
| 2 | 1 | 1 | 3.75515 | 23.674 | 7.8 |
| 0 | 3 | 1 | 3.74403 | 23.746 | 18.2 |
| 1 | 1 | 2 | 3.68843 | 24.109 | 19.1 |
| 2 | 2 | 0 | 3.61373 | 24.615 | 22.4 |
| 0 | 2 | 2 | 3.53494 | 25.173 | 18.3 |
| 1 | 3 | 1 | 3.44898 | 25.811 | 8.7 |
| 2 | 2 | 1 | 3.33027 | 26.748 | 19.6 |
| 1 | 2 | 2 | 3.28347 | 27.136 | 19 |
| 0 | 4 | 0 | 3.121 | 28.578 | 73.5 |
| 2 | 0 | 2 | 3.0821 | 28.946 | 100 |
| 2 | 3 | 0 | 3.03368 | 29.419 | 9.5 |
| 2 | 1 | 2 | 2.99225 | 29.835 | 7 |
| 2 | 3 | 1 | 2.86009 | 31.248 | 2.8 |
| 1 | 3 | 2 | 2.83028 | 31.586 | 4 |
| 3 | 0 | 1 | 2.79359 | 32.012 | 29.9 |
| 0 | 1 | 3 | 2.78716 | 32.088 | 2.2 |
| 1 | 4 | 1 | 2.78444 | 32.12 | 19 |
| 2 | 2 | 2 | 2.76357 | 32.369 | 17.7 |
| 3 | 1 | 1 | 2.72617 | 32.826 | 7.2 |
| 1 | 0 | 3 | 2.72125 | 32.887 | 11.1 |
| 1 | 1 | 3 | 2.65882 | 33.682 | 2.8 |
| 2 | 4 | 0 | 2.55178 | 35.14 | 16.7 |
| 3 | 2 | 1 | 2.54987 | 35.167 | 18.6 |
| 0 | 4 | 2 | 2.52358 | 35.545 | 15.4 |
| 1 | 2 | 3 | 2.49451 | 35.974 | 40.2 |
| 2 | 3 | 2 | 2.47675 | 36.241 | 0.1 |
| 2 | 4 | 1 | 2.44585 | 36.715 | 2 |
| 3 | 0 | 2 | 2.43318 | 36.913 | 1.7 |
| 1 | 4 | 2 | 2.42713 | 37.008 | 2.5 |
| 2 | 0 | 3 | 2.40269 | 37.398 | 1.9 |
| 0 | 5 | 1 | 2.39731 | 37.485 | 3.6 |
| 3 | 1 | 2 | 2.38825 | 37.633 | 0.9 |
| 2 | 1 | 3 | 2.35939 | 38.111 | 0.9 |
| 0 | 3 | 3 | 2.35663 | 38.157 | 0 |
| 3 | 3 | 1 | 2.31941 | 38.794 | 2.1 |
| 1 | 5 | 1 | 2.31417 | 38.885 | 0.1 |
| 1 | 3 | 3 | 2.27751 | 39.537 | 1.6 |
| 3 | 2 | 2 | 2.26703 | 39.727 | 0.7 |
| 2 | 2 | 3 | 2.24231 | 40.184 | 0.1 |
| 4 | 0 | 0 | 2.216 | 40.682 | 9.1 |
| 2 | 4 | 2 | 2.193 | 41.128 | 52.6 |
| 4 | 1 | 0 | 2.18189 | 41.347 | 2.6 |
| 2 | 5 | 0 | 2.17535 | 41.477 | 0.2 |
| 4 | 0 | 1 | 2.14556 | 42.08 | 6.7 |
| 0 | 0 | 4 | 2.1445 | 42.102 | 6.4 |
| 4 | 1 | 1 | 2.11456 | 42.727 | 0.2 |
| 2 | 5 | 1 | 2.10861 | 42.854 | 7.6 |
| 3 | 3 | 2 | 2.10047 | 43.028 | 5 |
| 1 | 5 | 2 | 2.09657 | 43.112 | 5.2 |
| 4 | 2 | 0 | 2.0883 | 43.291 | 2.7 |
| 1 | 0 | 4 | 2.08437 | 43.377 | 6.2 |
| 3 | 4 | 1 | 2.08153 | 43.439 | 20 |
| 2 | 3 | 3 | 2.08076 | 43.456 | 3.9 |
| 1 | 1 | 4 | 2.05591 | 44.009 | 3.2 |
| 3 | 0 | 3 | 2.05473 | 44.035 | 0 |
| 1 | 4 | 3 | 2.05108 | 44.118 | 7.3 |
| 4 | 2 | 1 | 2.02904 | 44.622 | 6 |
| 0 | 2 | 4 | 2.02814 | 44.643 | 2.4 |
| 3 | 1 | 3 | 2.02745 | 44.659 | 0.6 |
| 1 | 2 | 4 | 1.97705 | 45.862 | 5.5 |
| 1 | 6 | 1 | 1.97139 | 46.001 | 5.4 |
| 4 | 0 | 2 | 1.96875 | 46.066 | 3.7 |
| 4 | 3 | 0 | 1.95595 | 46.385 | 0.1 |
| 3 | 2 | 3 | 1.95171 | 46.492 | 0.4 |
| 4 | 1 | 2 | 1.94471 | 46.669 | 0.6 |
| 2 | 5 | 2 | 1.94008 | 46.787 | 3.8 |
| 2 | 0 | 4 | 1.93039 | 47.036 | 3.4 |
| 3 | 4 | 2 | 1.91893 | 47.334 | 0.7 |
| 2 | 1 | 4 | 1.90772 | 47.629 | 0.6 |
| 4 | 3 | 1 | 1.90701 | 47.648 | 1.1 |
| 2 | 4 | 3 | 1.90387 | 47.732 | 0.9 |
| 2 | 6 | 0 | 1.88344 | 48.282 | 0.2 |
| 0 | 5 | 3 | 1.8807 | 48.357 | 2 |
| 4 | 2 | 2 | 1.87757 | 48.443 | 0.8 |
| 0 | 6 | 2 | 1.87202 | 48.596 | 0.1 |
| 1 | 3 | 4 | 1.86365 | 48.828 | 4.5 |
| 3 | 5 | 1 | 1.86162 | 48.885 | 2.4 |
| 2 | 2 | 4 | 1.84422 | 49.377 | 1.2 |
| 3 | 3 | 3 | 1.84238 | 49.43 | 2.5 |
| 1 | 5 | 3 | 1.83975 | 49.505 | 4.3 |
| 1 | 6 | 2 | 1.83161 | 49.74 | 0.3 |
| 4 | 4 | 0 | 1.80686 | 50.468 | 7.4 |
| 4 | 3 | 2 | 1.77963 | 51.296 | 4.3 |
| 4 | 4 | 1 | 1.76807 | 51.656 | 2.8 |
| 0 | 4 | 4 | 1.76747 | 51.675 | 5.3 |
| 4 | 0 | 3 | 1.75155 | 52.18 | 0.2 |
| 2 | 3 | 4 | 1.75115 | 52.193 | 0.5 |
| 0 | 7 | 1 | 1.74609 | 52.355 | 2.7 |
| 3 | 5 | 2 | 1.74258 | 52.469 | 0 |
| 5 | 0 | 1 | 1.73611 | 52.679 | 2.9 |
| 3 | 0 | 4 | 1.73555 | 52.698 | 0.4 |
| 4 | 1 | 3 | 1.73457 | 52.73 | 1.2 |
| 1 | 4 | 4 | 1.73335 | 52.77 | 2.6 |
| 2 | 5 | 3 | 1.73127 | 52.838 | 0 |
| 2 | 6 | 2 | 1.72449 | 53.062 | 0.9 |
| 5 | 1 | 1 | 1.71956 | 53.226 | 0.9 |
| 3 | 1 | 4 | 1.71902 | 53.244 | 1.7 |
| 3 | 4 | 3 | 1.71619 | 53.339 | 0.7 |
| 1 | 7 | 1 | 1.71317 | 53.441 | 1 |
| 0 | 1 | 5 | 1.69963 | 53.901 | 0 |
| 4 | 2 | 3 | 1.68642 | 54.357 | 1.9 |
| 1 | 0 | 5 | 1.68434 | 54.43 | 0 |
| 5 | 2 | 1 | 1.67262 | 54.843 | 0.1 |
| 3 | 2 | 4 | 1.67212 | 54.861 | 2.1 |
| 1 | 1 | 5 | 1.66922 | 54.964 | 0.1 |
| 3 | 6 | 1 | 1.66869 | 54.983 | 2.3 |
| 4 | 4 | 2 | 1.66514 | 55.111 | 5 |
| 4 | 5 | 0 | 1.65737 | 55.391 | 3 |
| 2 | 7 | 0 | 1.6545 | 55.495 | 1.5 |
| 1 | 6 | 3 | 1.65288 | 55.554 | 6.3 |
| 2 | 4 | 4 | 1.64174 | 55.965 | 4.3 |
| 5 | 0 | 2 | 1.63836 | 56.09 | 0 |
| 4 | 5 | 1 | 1.62728 | 56.506 | 0 |
| 1 | 2 | 5 | 1.62618 | 56.548 | 4.5 |
| 2 | 7 | 1 | 1.62456 | 56.609 | 0.9 |
| 1 | 7 | 2 | 1.61904 | 56.82 | 0.4 |
| 4 | 3 | 3 | 1.61438 | 56.999 | 0.2 |
| 5 | 3 | 1 | 1.60226 | 57.47 | 0.5 |
| 3 | 3 | 4 | 1.60182 | 57.487 | 0 |
| 1 | 5 | 4 | 1.60009 | 57.555 | 0.5 |
| 2 | 0 | 5 | 1.59992 | 57.562 | 0.2 |
| 2 | 1 | 5 | 1.58694 | 58.077 | 0.1 |
| 3 | 5 | 3 | 1.58656 | 58.092 | 0 |
| 0 | 3 | 5 | 1.58609 | 58.111 | 0 |
| 5 | 2 | 2 | 1.58468 | 58.168 | 0 |
| 3 | 6 | 2 | 1.58134 | 58.303 | 0 |
| 2 | 6 | 3 | 1.57288 | 58.647 | 0 |
| 1 | 3 | 5 | 1.5613 | 59.125 | 1.3 |
| 0 | 8 | 0 | 1.5605 | 59.158 | 3.2 |
| 2 | 2 | 5 | 1.54982 | 59.607 | 0 |
| 4 | 5 | 2 | 1.54596 | 59.771 | 0.1 |
| 2 | 7 | 2 | 1.54363 | 59.87 | 0 |
| 4 | 0 | 4 | 1.54105 | 59.981 | 2.1 |
| 4 | 1 | 4 | 1.52944 | 60.483 | 0.5 |
| 4 | 4 | 3 | 1.52745 | 60.57 | 0 |
| 2 | 5 | 4 | 1.52718 | 60.582 | 0.1 |
| 5 | 3 | 2 | 1.52446 | 60.702 | 0.1 |
| 5 | 4 | 1 | 1.51718 | 61.024 | 4.2 |
| 4 | 6 | 0 | 1.51684 | 61.039 | 0.4 |
| 0 | 7 | 3 | 1.51321 | 61.201 | 0 |
| 1 | 8 | 1 | 1.51278 | 61.221 | 3.3 |
| 5 | 0 | 3 | 1.5067 | 61.494 | 5.8 |
| 3 | 7 | 1 | 1.50322 | 61.652 | 0.2 |
| 4 | 2 | 4 | 1.49613 | 61.977 | 3.3 |
| 5 | 1 | 3 | 1.49585 | 61.989 | 0.2 |
| 4 | 6 | 1 | 1.49367 | 62.09 | 0.1 |
| 0 | 6 | 4 | 1.49331 | 62.106 | 0.5 |
| 1 | 7 | 3 | 1.49163 | 62.184 | 0.8 |
| 3 | 0 | 5 | 1.48363 | 62.557 | 2.7 |
| 1 | 4 | 5 | 1.48226 | 62.622 | 0.2 |
| 6 | 0 | 0 | 1.47733 | 62.854 | 1.2 |
| 3 | 1 | 5 | 1.47327 | 63.047 | 0.3 |
| 1 | 6 | 4 | 1.47256 | 63.081 | 0.1 |
| 2 | 8 | 0 | 1.47193 | 63.112 | 4.6 |
| 6 | 1 | 0 | 1.4671 | 63.343 | 0 |
| 0 | 8 | 2 | 1.46645 | 63.374 | 4.1 |
| 5 | 2 | 3 | 1.46464 | 63.462 | 5.6 |
| 3 | 6 | 3 | 1.462 | 63.59 | 1.2 |
| 6 | 0 | 1 | 1.4559 | 63.888 | 0.9 |
| 5 | 4 | 2 | 1.45063 | 64.147 | 0 |
| 1 | 8 | 2 | 1.44679 | 64.338 | 0 |
| 6 | 1 | 1 | 1.4461 | 64.373 | 0 |
| 4 | 3 | 4 | 1.44514 | 64.421 | 0.2 |
| 3 | 2 | 5 | 1.44342 | 64.506 | 8.7 |
| 3 | 7 | 2 | 1.43842 | 64.758 | 1.6 |
| 6 | 2 | 0 | 1.43762 | 64.799 | 1.6 |
| 4 | 5 | 3 | 1.43391 | 64.987 | 0.9 |
| 2 | 7 | 3 | 1.43204 | 65.082 | 1.3 |
| 4 | 6 | 2 | 1.43004 | 65.184 | 0.7 |
| 0 | 0 | 6 | 1.42967 | 65.204 | 1 |
| 5 | 5 | 1 | 1.4254 | 65.423 | 0.4 |
| 3 | 5 | 4 | 1.42508 | 65.439 | 2.6 |
| 2 | 4 | 5 | 1.42374 | 65.509 | 0.2 |
| 6 | 2 | 1 | 1.41784 | 65.816 | 1.6 |
| 5 | 3 | 3 | 1.4167 | 65.876 | 0.2 |
| 2 | 6 | 4 | 1.41514 | 65.957 | 0.9 |
| 0 | 5 | 5 | 1.41398 | 66.019 | 0.1 |
| 1 | 0 | 6 | 1.41143 | 66.153 | 0.5 |
| 1 | 1 | 6 | 1.40249 | 66.629 | 0.4 |
| 3 | 3 | 5 | 1.39747 | 66.9 | 0 |
| 6 | 0 | 2 | 1.39679 | 66.937 | 0.5 |
| 1 | 5 | 5 | 1.39632 | 66.962 | 0.9 |
| 0 | 2 | 6 | 1.39358 | 67.112 | 1.7 |
| 2 | 8 | 2 | 1.39222 | 67.186 | 4.8 |
| 4 | 7 | 0 | 1.38937 | 67.342 | 0.2 |
| 6 | 1 | 2 | 1.38813 | 67.41 | 0.3 |
| 4 | 4 | 4 | 1.38178 | 67.762 | 2.2 |
| 1 | 2 | 6 | 1.37667 | 68.048 | 1.4 |
| 6 | 3 | 1 | 1.37422 | 68.186 | 0.2 |
| 4 | 7 | 1 | 1.37149 | 68.34 | 0.4 |
| 5 | 5 | 2 | 1.36979 | 68.437 | 0.9 |
| 0 | 9 | 1 | 1.36932 | 68.463 | 0.2 |
| 5 | 0 | 4 | 1.36637 | 68.632 | 0 |

Table S7. XRD analysis data for each composition and peak

| Composition (X) | Peak | Faced | FWHM | Crystallite Size (nm) | Dislocation Density (nm-2) | Lattice Strain (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.25 | 14.28 | {001} | 0.63 | 12.9 | 0.006009254 | 2.199 |
|  | 28.72 | {002} | 0.945 | 8.8 | 0.012913223 | 1.611 |
| 0.75 | 12.60 | PbI2 | 0.315 | 26 | 0.00147929 | 1.238 |
|  | 14.24 | {001} | 0.394 | 20.7 | 0.002333777 | 1.38 |
|  | 28.66 | {002} | 0.394 | 21.2 | 0.002224991 | 0.677 |
| 1 | 14.16 | {001} | 0.472 | 20.7 | 0.00233777 | 1.387 |
|  | 28.64 | {002} | 0.709 | 30.7 | 0.00106100 | 0.474 |

Figure S3. Peak shift coordinate (A) and compressive force (B) illustration.

Figure S4. Pseudocolor mapping of HR-TEM for x=0.25  based on the lattice length. The red, yellow, and green colors represent the lattice fringe values of 0.57-0.55 nm, less than 0.55 nm, and 0.60-0.76 respectively.

Figure S5. Optimized structures of (A, B) two configurations of Cs0.5FA0.5PbI3 (x = 0.5) and (C) FAPbI3 (x = 0). (D) Supercell volume and band gap as a function of the composition x. The red boxes in (A), (B), and (C) represent the supercell used in the simulations. The optimized structures for x = 1, 0.75, and 0 are in the main text.

Figure S6. Fast fourier transformation images of shell region (A) and core region (D); Simulated electron diffraction of orthorhombic (B) and cubic (E) phase; and representative crystal model of orthorhombic (C) and cubic (F) phase.

Figure S7. TEM image raw data of x = 1 (A), x = 0.75 (B), x = 0.25 (C). The black scale bar size is 200 nm for (A) and 100 nm for (B) and (C).

Figure S8. Raw data of captured TEM (A) and HAADF (B) images for x =0.25

Figure S9. Particle distribution (A) (x = 1), (B) (x = 0.75), (C) (x = 0.25), (D-E) representative HAADF images with different magnification, and elemental mapping of (F) Pb, (G) I, (H) Cs, and N (I) inside CsPbI3/CsxFA1-xPbI3 sample.

Figure S10. Photoluminescence excitation spectra of the sample (λem = 603 nm).

Figure S11. The spectra of (A) Photoluminescence, (B) absorbance, and (C) physical appearances of CsxFA1-xPbI3 (from left to right; x = 1, x = 0.75, x = 0.25, x = 0) prepared with cation exchange method.

Figure S12. Matched PL emission and excitation of CsPbI3/CsxFA1-xPbI3 QDs (x = 0.25).

Figure S13. Side view (A) of superlattice crystal model of CsxFA1–xPbI3 QDs with (x = 1) (B), (x = 0.75) (C), (x = 0.25) (D).

Figure S14. The physical appearance of the sample with FA addition before and after storage for one year under ambient conditions.

Figure S15. PL emission spectra of (A) x =1, (B) x = 0.75, (C) x = 0.25 the as-synthesized quantum dots and after storage for one year under ambient conditions (λex=365 nm).

Figure S16. The absorbance of CsPbI3@CsxFA1-xPbI3 QDs (x = 1 (A), x = 0.75 (B), x = 0.25 (C)) before and after UV irradiation.

Figure S17. Particle morphology of (A) degraded pristine CsPbI3, and (B) CsPbI3/CsxFA1-xPbI3 (x = 0.25).

Figure S18. Photoluminescence spectra of CsPbI3@CsxFA1-xPbI3 QDs in polar solvent.

Figure S19. Representative X-ray diffraction diffractogram of CsPbI3@CsxFA1-xPbI3 after stability measurement in different solvents.

Figure S20. Polar stability of (A) Cs0.75FA0.25PbI3, and (B) Cs0.25FA0.75PbI3 prepared using the cation exchange method.

Figure S21. Photoluminescence spectra of CsPbI3@CsxFA1-xPbI3 QDs at various temperatures for 60 min (A) and at 100 °C with time-lapse (B).

Figure S22. Schematic illustrating the internal structural stabilization strategy by a previous work2 and this present study.

Table S8. Comparison of previously reported red-emitting quantum dots.

| Materials | Emission Wavelength (nm) | PLQY (%) | FWHM (nm) | Stability |
| --- | --- | --- | --- | --- |
| CdSe/ZnS3 | ~600 | 50 | 40 | N/A |
| CuInS2/ZnS4 | 626 | 60 | 45 | 60 min in ambient condition |
| Carbon dots5 | ~630 | 43.3 | ~53 | N/A |
| CdSe/ZnS6 | ~615 | ~60 | ~42 | N/A |
| ZnCdSe/ZnSeS7 | 647 | 92 | ~42 | 167 h under UV illumination |
| CsPbI3/APTES8 | ~660 | 84 | N/A | 50% PLQY after 28 days, 2 h in water |
| CsPbI3/TiO29 | 705 | 85 | 50 | 40 h in ambient condition |
| CsPbI3/HPAI/ TBSI10 | 637 | 87 | 42 | 1 day in ambient condition |
| Entropy driven-CsPbI311 | 632 | 100 | 32 | N/A |
| GAI-CsPbI312 | 668 | 46 | 46 | 150 hours in ambient condition |
| Our work | 603 | 87 | 38 | PLQY ~70%, retain the emission after 1 year in ambient condition, 30 min in ethanol mix solvent, and sustain its emissions in high temperature up to 150oC |

References:

1	D. B. Straus, S. Guo and R. J. Cava, J. Am. Chem. Soc., 2019, 141, 11435–11439.

2	E. A. Erazo, H. E. Sánchez-Godoy, A. F. Gualdrón-Reyes, S. Masi and I. Mora-Seró, Nanomaterials, 2020, 10, 1–14.

3	B. O. Dabbousi, J. Rodriguez-Viejo, F. V. Mikulec, J. R. Heine, H. Mattoussi, R. Ober, K. F. Jensen and M. G. Bawendi, J. Phys. Chem. B, 1997, 101, 9463–9475.

4	L. Li, T. J. Daou, I. Texier, T. T. K. Chi, N. Q. Liem and P. Reiss, Chem. Mater., 2009, 21, 2422–2429.

5	H. Zhang, G. Wang, Z. Zhang, J. H. Lei, T. M. Liu, G. Xing, C. X. Deng, Z. Tang and S. Qu, Light Sci. Appl., 2022, 11, 113.

6	J. Li, H. Zheng, Z. Zheng, H. Rong, Z. Zeng and H. Zeng, Nanomaterials, 2022, 12, 2969.

7	X. Liu, L. Wang, Y. Gao, Y. Zeng, F. Liu, H. Shen, L. Manna and H. Li, Nano Lett., 2023, 23, 6689–6697.

8	K. He, C. Shen, Y. Zhu, X. Chen, Z. Bi, T. Marimuthu, G. Xu and X. Xu, Langmuir, 2020, 36, 10210–10217.

9	A. D. Pramata, Y. Akaishi, N. Kodama, Y. Mokuge, S. Kawashima, M. Shimoyoshi, C. Sairot, P. Nuket, P. Vas-Umnuay and T. Kida, ACS Appl. Nano Mater., 2021, 4, 4103–4113.

10	Y. F. Lan, J. S. Yao, J. N. Yang, Y. H. Song, X. C. Ru, Q. Zhang, L. Z. Feng, T. Chen, K. H. Song and H. Bin Yao, Nano Lett., 2021, 21, 8756–8763.

11	J. Guo, Y. Fu, W. Zheng, M. Xie, Y. Huang, Z. Miao, C. Han, W. Yin, J. Zhang, X. Yang, J. Tian and X. Zhang, Nano Lett., 2023, 24, 417–423.

12	H. Ebe, R. Suzuki, S. Sumikoshi, M. Uwano, R. Moriyama, D. Yokota, M. Otaki, K. Enomoto, T. Oto, T. Chiba and J. Kido, Chem. Eng. J., 2023, 471, 144578.