Supporting information

Casein-based film enriched with lignin as a biodegradable substrate for enzyme immobilization

Elena Dembech,a Giovanna Sotgiu,b,c Anna Donnadio,d Sara Buoso,b,c Giovanni Dolci,e Mary Jo Floriana Antonia Nichilo,e and Valentina Sinisi*a

a Institute of Materials for Electronics and Magnetism, National Research Council (CNR-IMEM), Parco Area delle Scienze, 37/A, 43124 Parma, Italy. Email: valentina.sinisi@cnr.it

b Institute for Organic Synthesis and Photoreactivity, National Research Council (CNR-ISOF), via P. Gobetti, 101, 40129 Bologna, Italy

c Kerline srl Via P. Gobetti 101 40129 Bologna

d Department of Pharmaceuticals Sciences, University of Perugia, Via del Liceo 1, 06123 Perugia, Italy

e Politecnico di Milano, Department of Civil and Environmental Engineering, Environmental section, Piazza Leonardo da Vinci 32, 20133 Milano, Italy

Table 1-SI Inventory data for the Life Cycle Assessment of different samples.

| Input |  |  |  |  |  |  |  |  |  |  |  |  | Output |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Casein | Phosphate buffer |  | Electricity | Glycerol | Lignin |  | Sodium hydroxide | Water | TGM | Electricity | Electricity | Film |  | Evaporated water (g) |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Sample | Mass (g) |  |
| Ecoinvent dataset | Table 2-SI | Sodium phosphate {RER}¦ market for | Water, deionised {Europe without Switzerland}¦ water production, deionised | Electricity, low voltage {IT}¦ market for | Glycerine {RER}¦ market for | Table 14-SI |  | Sodium hydroxide, without water, in 50% solution state {RER}¦ market for | Water, deionised {Europe without Switzerland}¦ water production, deionised | Enzymes {GLO} ¦ market for | Electricity, low voltage {IT}¦ market for | Electricity, low voltage {IT}¦ market for |  |  |  |
| Amount | 4 | 0.137 | 15 | 0.108 | 0.50 | 50 | 100 | 0.01 | 0.70 | 250 | 3 |  |  |  |  |
| Unit of measure | g | g | mL | kWh | g | mg | mg | g | mL | mg | kWh |  |  |  |  |
| Data source |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Notes | An amount of 4 g has been chosen for the LCA to ensure a conservative approach | Casein is solubilized in a phosphate buffer. In the paper the buffer is indicated as KH₂PO₄/K₂HPO₄ buffer, but potassium phosphate is not available as ecoinvent dataset: a sodium phosphate has been there modelled here, since also sodium phosphate could be used for the purpose |  | Stirring on a heated magnetic plate (target temperature: 80°C). Time: 2h. Measured power consumption: 0.009 kWh/10min |  | The modelling is the same for both lignin Sigma and lignin UPM |  |  |  |  | The synthetized film base is left to dry overnight in a Teflon mold, placed under a chemical extractor hood. Time: ~20h. Nominal power: 0.15 kW (from technical data sheet, available at https://www.bicasa.it/prodotti/cappe-chimiche/) | Stove (70°C). Time: 3h. Measured power consumption: 0.096 kWh/20min |  | Output film mass range: 2.5-3 g. The base formulation sample (C) mass is set to half the range, i.e. 2.75 g. Other film masses are calculated as the difference between input mass and output mass, once set the value of evaporated water (see “Evaporated water”) | Evaporated water is assumed equal for all samples and set equal to that calculated for the base formulation sample (C), which in turn as the difference between input mass and output mass, once set the output sample mass) |
|  | x | x | x | x | x |  |  | x | x |  | x |  | C | 2.75 | 17.6 |
|  | x | x | x | x | x |  |  |  |  | x | x |  | CT | 2.29 | 17.6 |
|  | x | x | x | x | x | x |  |  | x |  | x |  | CS50 | 2.79 | 17.6 |
|  | x | x | x | x | x |  | x |  | x |  | x |  | CS100 | 2.84 | 17.6 |
|  | x | x | x | x | x | x |  | x | x |  | x |  | CU50 | 2.80 | 17.6 |
|  | x | x | x | x | x |  | x | x | x |  | x |  | CU100 | 2.85 | 17.6 |
|  | x | x | x | x | x | x |  |  | x | x | x |  | CS50T | 3.04 | 17.6 |
|  | x | x | x | x | x |  | x |  | x | x | x |  | CS100T | 3.09 | 17.6 |
|  | x | x | x | x | x | x |  | x | x | x | x |  | CU50T | 3.05 | 17.6 |
|  | x | x | x | x | x |  | x | x | x | x | x |  | CU100T | 3.10 | 17.6 |

Table 2-SI Inventory data for the Life Cycle Assessment of casein production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | UHT skimmed milk | Table 3-SI | 0.50 | L | Primary data |  |
|  |  |  | 513 | g |  | Milk density: 1.026 kg/L |
|  | White wine vinegar | Table 10-SI | 50 | mL |  |  |
|  |  |  | 54.9 | g |  | Vinegar density: 1.097 g/mL |
|  | Electricity | Electricity, low voltage {IT}¦ market for | 0.138 | kWh |  | Stirring on a heated magnetic plate (target temperature: 52°C). Time: 1h. Measured electricity consumption: 0.023 kWh/10 min. |
|  | Electricity | Electricity, low voltage {IT}¦ market for | negligible | kWh |  | Magnetic stirring only (adding vinegar). Time: 5 min |
|  | Deionised water | Water, deionised {Europe without Switzerland} ¦ water production, deionised | 200 | mL |  | Water used for washing the precipitate |
|  | Electricity | Electricity, low voltage {IT}¦ market for | 3 | kWh |  | Casein is left to dry overnight under a chemical extractor hood. Time: ~20h. Nominal power: 0.15 kW (from technical data sheet, available at https://www.bicasa.it/prodotti/cappe-chimiche/) N.B. The considered impact is valid if the hood is used only for the drying of 40 g of casein |
|  | Electricity | Electricity, low voltage {IT}¦ market for | 0.288 | kWh |  | Oven (90°C) to evaluate the residual humidity. Time: 2 h. |
|  | Electricity | Electricity, low voltage {IT}¦ market for | 0.124 | kWh |  | Refrigerator time: ~ 4 weeks. Annual electricity consumption: 81 kWh/y. Number of items in the refrigerator: ~50 items. N.B. Storage is not necessary: casein is stored if not immediately used for the films production |
| Output | Casein |  | 40 | g |  | Number of produced films: ~ 10 films |
|  | Liquid derived from washing the precipitate | Wastewater, average {IT}, treatment of | 200 | mL |  | The dataset Wastewater, average {Europe without Switzerland}, treatment of wastewater, average has been regionalized |
|  | Milk whey discarded in the sink |  | 528 | g |  |  |
|  |  | Wastewater, average {IT}, treatment of | 515 | mL |  | The dataset Wastewater, average {Europe without Switzerland}, treatment of wastewater, average has been regionalized. Milk whey density: 1.025 kg/L |

Table 3-SI Inventory data for the Life Cycle Assessment of UHT skimmed milk production.

|  |  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Input | Skimmed milk production |  | Skimmed milk, from cow milk {IT}¦ market for (modified dataset) | 1 | L | Ecoinvent | The dataset Skimmed milk, from cow milk {GLO}¦ market for has been regionalized |
|  | Pumping product | Electricity | Electricity, medium voltage {IT}¦ market for | 1.77E-04 | kWh | Valsasina et al. (2016) | The 90% reduced electricity values ​​were used because large-scale UHTH plants ensure up to 90% energy recovery (Valsasina et al., 2016) |
|  | Pre-heating | Electricity | Electricity, medium voltage {IT}¦ market for | 8.15E-03 | kWh |  |  |
|  | UHT homogenization | Electricity | Electricity, medium voltage {IT}¦ market for | 6.81E-04 | kWh |  |  |
|  |  | Compressed air at 2 bar | Table 4-SI | 2.60E-02 | m3 |  |  |
|  | UHT sterilization | Electricity | Electricity, medium voltage {IT}¦ market for | 1.87E-02 | kWh |  |  |
|  |  | Compressed air at 2 bar | Table 5-SI | 3.12E-02 | m3 |  |  |
|  |  | Water | Tap water {Europe without Switzerland} ¦ market for | 1.41E-01 | L |  |  |
|  | Cooling | Electricity | Electricity, medium voltage {IT}¦ market for | 1.75E-03 | kWh |  |  |
|  | Cleaning | Electricity | Electricity, medium voltage {IT}¦ market for | 1.34E-04 | kWh |  |  |
|  |  | Compressed air at 2 bar | Table 4-SI | 4.67E-03 | m3 |  |  |
|  |  | Water | Tap water {Europe without Switzerland} ¦ market for | 1.91E-01 | L |  |  |
|  |  | BTS 3000 | Table 6-SI | 1.05E-03 | kg |  |  |
|  |  | Biomelk solution | Table 8-SI | 1.69E-04 | kg |  |  |
|  |  | Heating Biomelk solution | Electricity, medium voltage {IT}¦ market for | 7.90E-04 | kWh |  |  |
|  |  |  | Wastewater, average {IT}¦ treatment of wastewater (modified dataset) | 1.91E-04 | m3 |  | The dataset Wastewater, average {Europe without Switzerland} ¦ treatment of wastewater has been regionalized by modifying the electricity consumption process and setting the Italian one |
|  |  | BTS 4000 | Table 9-SI | 5.00E-05 | kg |  |  |
|  | Packaging |  | Beverage carton, 1 L, for UHT milk (ambient) {RER}¦ market for | 1 | L | Ecoinvent |  |
| Output |  | UHT skimmed milk |  | 1 | L |  |  |

Table 4-SI Inventory data for the Life Cycle Assessment of compressed air, 33.33% 600 kPa production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Steel, low-alloyed, hot rolled {GLO}¦ market for | 9.79E-05 | kg | Valsasina et al. (2016) |
|  | Lubricating oil {RER}¦ market for | 2.45E-06 | kg |  |
|  | Section bar rolling, steel {GLO}¦ market for | 9.79E-05 | kg |  |
|  | Air compressor, screw-type compressor, 300kW {GLO}¦ market for | 9.00E-08 | p |  |
|  | Electricity, low voltage {SK}¦ market for | 3.56E-04 | kWh |  |
|  | Electricity, low voltage {BA}¦ market for | 1.17E-04 | kWh |  |
|  | Electricity, low voltage {PL}¦ market for | 1.79E-03 | kWh |  |
|  | Electricity, low voltage {IE}¦ market for | 3.64E-04 | kWh |  |
|  | Electricity, low voltage {AT}¦ market for | 8.43E-04 | kWh |  |
|  | Electricity, low voltage {DE}¦ market for | 7.47E-03 | kWh |  |
|  | Electricity, low voltage {BG}¦ market for | 4.28E-04 | kWh |  |
|  | Electricity, low voltage {SE}¦ market for | 1.84E-03 | kWh |  |
|  | Electricity, low voltage {ES}¦ market for | 3.76E-03 | kWh |  |
|  | Electricity, low voltage {NO}¦ market for | 1.61E-03 | kWh |  |
|  | Electricity, low voltage {FR}¦ market for | 6.42E-03 | kWh |  |
|  | Electricity, low voltage {RO}¦ market for | 6.96E-04 | kWh |  |
|  | Electricity, low voltage {HU}¦ market for | 5.26E-04 | kWh |  |
|  | Electricity, low voltage {MK}¦ market for | 1.03E-04 | kWh |  |
|  | Electricity, low voltage {SI}¦ market for | 1.80E-04 | kWh |  |
|  | Electricity, low voltage {FI}¦ market for | 1.15E-03 | kWh |  |
|  | Electricity, low voltage {GR}¦ market for | 8.20E-04 | kWh |  |
|  | Electricity, low voltage {PT}¦ market for | 6.88E-04 | kWh |  |
|  | Electricity, low voltage {HR}¦ market for | 2.32E-04 | kWh |  |
|  | Electricity, low voltage {UA}¦ market for | 2.12E-03 | kWh |  |
|  | Electricity, low voltage {RS}¦ market for | 4.09E-04 | kWh |  |
|  | Electricity, low voltage {LU}¦ market for | 9.02E-05 | kWh |  |
|  | Electricity, low voltage {IT}¦ market for | 4.43E-03 | kWh |  |
|  | Electricity, low voltage {BE}¦ market for | 1.18E-03 | kWh |  |
|  | Electricity, low voltage {CH}¦ market for | 8.02E-04 | kWh |  |
|  | Electricity, low voltage {CZ}¦ market for | 8.41E-04 | kWh |  |
|  | Electricity, low voltage {NL}¦ market for | 1.57E-03 | kWh |  |
|  | Electricity, low voltage {GB}¦ market for | 4.89E-03 | kWh |  |
|  | Electricity, low voltage {DK}¦ market for | 4.76E-04 | kWh |  |
| Output | Waste mineral oil {Europe without Switzerland}¦ market for | 2.45E-06 | kg |  |
|  | Compressed air, 33.33% 600 kPa {RER} >30 kW | 1 | m3 |  |

Table 5-SI Inventory data for the Life Cycle Assessment of compressed air, 60% 600 kPa production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Steel, low-alloyed, hot rolled {GLO}¦ market for | 9.79E-05 | kg | Valsasina et al. (2016) |
|  | Lubricating oil {RER}¦ market for | 2.45E-06 | kg |  |
|  | Section bar rolling, steel {GLO}¦ market for | 9.79E-05 | kg |  |
|  | Air compressor, screw-type compressor, 300kW {GLO}¦ market for | 9.00E-08 | p |  |
|  | Electricity, low voltage {SK}¦ market for | 6.46E-04 | kWh |  |
|  | Electricity, low voltage {BA}¦ market for | 2.13E-04 | kWh |  |
|  | Electricity, low voltage {PL}¦ market for | 3.26E-03 | kWh |  |
|  | Electricity, low voltage {IE}¦ market for | 6.62E-04 | kWh |  |
|  | Electricity, low voltage {AT}¦ market for | 1.53E-03 | kWh |  |
|  | Electricity, low voltage {DE}¦ market for | 1.36E-02 | kWh |  |
|  | Electricity, low voltage {BG}¦ market for | 7.79E-04 | kWh |  |
|  | Electricity, low voltage {SE}¦ market for | 3.34E-03 | kWh |  |
|  | Electricity, low voltage {ES}¦ market for | 6.83E-03 | kWh |  |
|  | Electricity, low voltage {NO}¦ market for | 2.93E-03 | kWh |  |
|  | Electricity, low voltage {FR}¦ market for | 1.17E-02 | kWh |  |
|  | Electricity, low voltage {RO}¦ market for | 1.26E-03 | kWh |  |
|  | Electricity, low voltage {HU}¦ market for | 9.56E-04 | kWh |  |
|  | Electricity, low voltage {MK}¦ market for | 1.88E-04 | kWh |  |
|  | Electricity, low voltage {SI}¦ market for | 3.27E-04 | kWh |  |
|  | Electricity, low voltage {FI}¦ market for | 2.09E-03 | kWh |  |
|  | Electricity, low voltage {GR}¦ market for | 1.49E-03 | kWh |  |
|  | Electricity, low voltage {PT}¦ market for | 1.25E-03 | kWh |  |
|  | Electricity, low voltage {HR}¦ market for | 4.22E-04 | kWh |  |
|  | Electricity, low voltage {UA}¦ market for | 3.85E-03 | kWh |  |
|  | Electricity, low voltage {RS}¦ market for | 7.43E-04 | kWh |  |
|  | Electricity, low voltage {LU}¦ market for | 1.64E-04 | kWh |  |
|  | Electricity, low voltage {IT}¦ market for | 8.05E-03 | kWh |  |
|  | Electricity, low voltage {BE}¦ market for | 2.15E-03 | kWh |  |
|  | Electricity, low voltage {CH}¦ market for | 1.46E-03 | kWh |  |
|  | Electricity, low voltage {CZ}¦ market for | 1.53E-03 | kWh |  |
|  | Electricity, low voltage {NL}¦ market for | 2.86E-03 | kWh |  |
|  | Electricity, low voltage {GB}¦ market for | 8.88E-03 | kWh |  |
|  | Electricity, low voltage {DK}¦ market for | 8.66E-04 | kWh |  |
| Output | Waste mineral oil {GLO}¦ market for | 2.45E-06 | kg |  |
|  | Compressed air, 60% 600 kPa {RER} >30 kW | 1 | m3 |  |

Table 6-SI Inventory data for the Life Cycle Assessment of BTS 3000 production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Table 7-SI | 0.100 | kg | Valsasina et al. (2016) |
|  | Potassium hydroxide {GLO}¦ market for | 0.030 | kg |  |
|  | Chlorine, liquid {RER}¦ market for | 0.032 | kg |  |
|  | Ethoxylated alcohol (AE7) {RER}¦ market for | 0.030 | kg |  |
| Output | BTS 3000 | 1 | kg |  |

Table 7-SI Inventory data for the Life Cycle Assessment of sodium hydroxide in 10% solution state production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Transport, freight, sea, transoceanic ship {GLO}¦ market for | 3 | tkm | Valsasina et al. (2016) |
|  | Transport, freight, inland waterways, barge {GLO}¦ market for | 0.123 | tkm |  |
|  | Sodium hydroxide, without water, in 50% solution state {RER} market for | 1 | kg |  |
|  | Transport, freight, lorry, unspecified {GLO}¦ market for | 1.040 | tkm |  |
|  | Transport, freight train {Europe without Switzerland}¦ market for | 0.101 | tkm |  |
|  | Transport, freight train {CN}¦ market for | 0.341 | tkm |  |
|  | Transport, freight train {CH}¦ market for | 0.002 | tkm |  |
|  | Transport, freight train {US}¦ market for | 0.479 | tkm |  |
|  | Transport, freight train {RoW}¦ market for | 0.623 | tkm |  |
| Output | Sodium hydroxide, without water, in 10% solution state {GLO}¦ market for | 1 | kg |  |

Table 8-SI Inventory data for the Life Cycle Assessment of Biomelk solution production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Chlorine, liquid {RER}¦ market for | 0.5 | kg | Valsasina et al. (2016) |
| Output | Biomelk solution | 1 | kg |  |

Table 9-SI Inventory data for the Life Cycle Assessment of BTS 4000 production.

|  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- |
| Input | Chlorine, liquid {RER}¦ market for | 0.008 | kg | Valsasina et al. (2016) |
| Output | BTS 4000 | 1 | kg |  |

Table 10-SI Inventory data for the Life Cycle Assessment of vinegar production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Wine | Table 13-SI | 1 | L | Hidalgo et al. (2010) |  |
|  | Vinegar mother | Table 11-SI | 0.15 | kg |  |  |
|  | Water | Tap water {Europe without Switzerland}¦market for | 0.38 | kg |  |  |
|  | Electricity | Electricity, low voltage {IT}¦ market for | 0.82 | MJ |  | The same electricity consumption required per litre of wine production is assumed: 0.4 MJ/0.75 L = 0.53 MJ/L |
| Output |  | Vinegar | 1.538 | kg |  |  |

Table 11-SI Inventory data for the Life Cycle Assessment of vinegar mother production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source |
| --- | --- | --- | --- | --- | --- |
| Input | Vinegar | Table 10-SI | 0.038 | kg | Hidalgo et al. (2010) |
|  | Wine | Table 13-SI | 0.075 | kg |  |
|  | Water | Tap water {Europe without Switzerland}¦market for | 0.038 | kg |  |
| Output | Vinegar mother |  | 0.15 | kg |  |

Table 12-SI Inventory data for the Life Cycle Assessment of grapes production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Diesel | Diesel {RER} ¦ market group for | 292 | L | Bartocci et al. (2016) |  |
|  | Urea | Urea {RER} ¦ market for | 100 | kg |  |  |
|  | Galigan | Pesticide, unspecified {GLO} ¦ market for | 1 | kg |  | Proxy process for Herbicides |
|  | Silglif | Pesticide, unspecified {GLO} ¦ market for | 1 | kg |  |  |
|  | Water | Tap water {Europe without Switzerland}¦market for | 0.800 | t |  | Water that herbicides are mixed with |
|  | Antifoam | Chemical, inorganic {GLO} ¦ market for | 0.030 | kg |  | Proxy process for antifoam that herbicides are mixed with |
|  | Acrobat | Pesticide, unspecified {GLO} ¦ market for | 5.700 | kg |  | Phytosanitary products |
|  | Topas | Pesticide, unspecified {GLO} ¦ market for | 6.850 | kg |  |  |
|  | Antifoam | Pesticide, unspecified {GLO} ¦ market for | 0.045 | kg |  |  |
|  | Siaram | Pesticide, unspecified {GLO} ¦ market for | 6 | kg |  |  |
|  | Switch | Pesticide, unspecified {GLO} ¦ market for | 0.80 | kg |  |  |
|  | Water | Tap water {Europe without Switzerland}¦market for | 0.60 | t |  | Water that phytosanitary products are mixed with |
| Output | Grapes |  | 9 | t | Bartocci et al. (2016) |  |

Table 13-SI Inventory data for the Life Cycle Assessment of wine production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Grapes | Table 12-SI | 1.071 | kg | Fusi et al. (2014) |  |
|  | Liquid sulphur dioxide | Sulphur dioxide, liquid {RER}¦ market for | 64.3 | mg |  |  |
|  | Liquid nitrogen | Nitrogen, liquid {RER} ¦ market for | 0.37 | g |  |  |
|  | Bentonite | Bentonite {GLO} ¦ market for | 0.35 | g |  |  |
|  | Liquefied petroleum gas (LPG) | Liquefied petroleum gas {Europe without Switzerland}¦ market for | 0.64 | g |  |  |
|  | Water | Tap water {Europe without Switzerland}¦ market for | 5.34 | kg |  |  |
|  | Electricity | Electricity, medium {IT} ¦ market for | 0.40 | MJ |  |  |
| Output | Air emissions (A) | Ethanol (A) | 0.165 | g |  |  |
|  |  | Carbon dioxide (A) | 1.87 | g |  |  |
|  |  | Dinitrogen monoxide (A) | 0.003 | mg |  |  |
|  |  | Methane (A) | 0.03 | mg |  |  |
|  | Wastewater | Wastewater, average {IT} ¦ treatment of |  |  |  | The dataset Wastewater, average {Europe without Switzerland}, treatment of wastewater, average has been regionalized |
|  | Wine |  | 0.75 | L |  | Impacts economic allocation (source: Fusi et al., 2013): wine 99.95%, marc and lees 0.05%, stalks 0% |
|  | Marc and lees |  | 0.27 | kg |  |  |
|  | Stalks |  | 0.05 | kg |  |  |

Table 14-SI Inventory data for the Life Cycle Assessment of lignin production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Paper pulp production | Table 15-SI | 2.04 | kg | Secondary data depending on the input | For 1 t of pulp, 7 t of black liquor is produced (Morya et al., 2022). For 1 t of black liquor, 0.07 t of lignin is produced (Secchi et al., 2019) |
|  | Lignin precipitation | Table 16-SI | 1 | kg |  |  |
| Output | Lignin |  | 1 | kg |  | Impacts economic allocation (source: Culbertson et al., 2016): lignin: 0.3 €/kg; pulp: 0.77 €/kg, i.e. impacts allocation: 16% lignin, 84% pulp. The impacts allocation is performed by considering pulp production and lignin precipitation as a one single process, since in pulp production it is not possible to separate the processes that are exclusive to pulp production from those that are exclusive to lignin production. |
|  | Paper pulp |  | 2.04 | kg |  |  |

Table 15-SI Inventory data for the Life Cycle Assessment of pulp production.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Water | Water, unspecified natural origin, RER | 0.027 | m3 | Secchi et al. (2019) |  |
|  | Hardwood | Pulpwood, hardwood, measured as solid wood under bark {Europe without Switzerland} ¦ market for | 0.003 | m3 |  |  |
|  | Chlorine dioxide | Chlorine dioxide {RER}¦ market for | 0.010 | kg |  |  |
|  | Hydrogen peroxide | Hydrogen peroxide, without water, in 50% solution state {RER}¦ market for | 0.012 | kg |  |  |
|  | Sulphuric acid | Sulfuric acid {RER}¦ market for | 0.030 | kg |  |  |
|  | Sodium chlorate | Sodium chlorate, powder {RER}¦ market for | 0.021 | kg |  |  |
|  | Sodium hydroxide | Sodium hydroxide, without water, in 50% solution state {RER}¦ market for | 0.038 | kg |  |  |
|  | Oxygen | Oxygen, liquid {RER}¦ market for | 0.020 | kg |  |  |
|  | Natural gas | Natural gas, high pressure {IT}¦ market for | 0.018 | m3 |  | The energy deriving from biomass combustion (black liquor, bark, etc.) is replaced with energy deriving from natural gas combustion (it is therefore assumed that there is no energy recovery from internal biomass combustion, but that the fuel is supplied from outside). Energy input from Secchi et al (2019): 0.630 MJ. Natural gas calorific value: 36 MJ/m3. |
|  | Heavy fuel oil | Heavy fuel oil {RER}¦ market group for | 0.006 | kg |  | Energy input from Secchi et al (2019): 0.238 MJ. Heavy fuel oil calorific: 41.2 MJ/kg (source: ecoinvent). |
| Output | Emissions in air (A) | Carbon dioxide, fossil (A) | 2.65E-02 | kg |  | CO2 emissions from natural gas combustion. Natural gas is assumed 100% CH4. CH4 density = 0.657 kg/m3; CO2 molar mass: 44 g/mol; CH4 molar mass: 16 g/mol. |
|  |  | Nitrogen oxides (A) | 1.00E-04 | kg |  |  |
|  |  | Sulphur dioxide (A) | 1.86E-05 | kg |  |  |
|  |  | Particulates (A) | 1.00E-04 | kg |  |  |
|  | Emissions in water (W) | AOX, Adsorbable Organic Halogen (W) | 4.80E-05 | kg |  |  |
|  |  | BOD5 (Biological Oxygen Demand) (W) | 2.00E-04 | kg |  |  |
|  |  | COD (Chemical Oxygen Demand) (W) | 6.00E-03 | kg |  |  |
|  |  | Sulphate (W) | 3.90E-02 | kg |  |  |
|  |  | Nitrogen (W) | 1.00E-04 | kg |  |  |
|  |  | Phosphorus (W) | 4.20E-06 | kg |  |  |
|  |  | Water, RER (W) | 2.70E-02 | m3 |  | Water output has been added to balance water input |
|  | Waste to incineration | Waste plastic, mixture {GLO}¦ treatment of waste plastic, mixture, municipal incineration | 8.00E-03 | kg |  |  |
|  |  | Waste graphical paper {GLO}¦ treatment of waste graphical paper, municipal incineration | 2.00E-03 | kg |  |  |
|  |  | Waste textile, soiled {GLO}¦ treatment of waste textile, soiled, municipal incineration | 8.00E-04 | kg |  |  |
|  |  | Waste wood, untreated {GLO}¦ treatment of waste wood, untreated, municipal incineration | 4.00E-04 | kg |  |  |
|  |  | Scrap steel {Europe without Switzerland}¦ treatment of scrap steel, municipal incineration | 8.00E-04 | kg |  |  |
|  | Waste to landfill | Wood ash mixture, pure {Europe without Switzerland}¦ treatment of wood ash mixture, pure, sanitary landfill | 7.30E-02 | kg |  |  |
|  |  | Green liquor dregs {RER}¦ treatment of green liquor dregs, residual material landfill | 6.00E-03 | kg |  |  |
|  |  | Municipal solid waste {RoW}¦ treatment of municipal solid waste, sanitary landfill | 6.00E-03 | kg |  |  |
|  |  | Sludge from pulp and paper production {Europe without Switzerland}¦ treatment of sludge from pulp and paper production, sanitary landfill | 1.70E-02 | kg |  |  |
|  |  | Ash from paper production sludge {Europe without Switzerland}¦ treatment of ash from paper production sludge, residual material landfill | 5.00E-03 | kg |  |  |
|  | Paper pulp |  | 1 | kg |  |  |

Table 16-SI Inventory data for the Life Cycle Assessment of lignin precipitation.

|  |  | Ecoinvent dataset | Amount | Unit of measure | Data source | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Input | Carbon dioxide | Carbon dioxide, liquid {RER}¦ market for | 0.34 | kg | Secchi et al. (2019) | Chemicals for lignin precipitation through LignoBoost technology |
|  | Sulfuric acid | Sulfuric acid {RER}¦ market for | 0.062 | kg |  |  |
| Output | Lignin |  | 1 | kg |  |  |

Fig. 1-SI UV-Vis spectrum of isolated casein solubilized in phosphate buffer, image limited to the range of interest (250-400 nm).

Table 17-SI DLS of casein, summary data.

| Measurement | Eff. Diam. (nm) | Polydispersity | Baseline Index | Mean Diam. By Intensity (nm) | Count Rate (kcps) |
| --- | --- | --- | --- | --- | --- |
| I | 880,77 | 0,399 | 9,4 | 1.015,32 | 372,7 |
| II | 972,91 | 0,456 | 8,4 | 1.188,87 | 351,3 |
| III | 973,19 | 0,466 | 9,7 | 1.594,85 | 338,4 |
| IV | 1.149,59 | 0,356 | 8,0 | 2.440,19 | 323,2 |
| Mean: | 994,11 | 0,419 | 8,9 | 1.559,81 | 346,4 |
| Std Err: | 56,20 | 0,026 | 0,4 | 317,59 | 10,5 |
| Std Dev: | 112,41 | 0,051 | 0,8 | 635,18 | 21,0 |

Fig. 2-SI DLS of casein, correlation curve.

Table 18-SI Z-potential data of casein.

| Measurement | Zeta Potential (mV) |
| --- | --- |
| I | -18,28 |
| II | -20,23 |
| III | -18,94 |
| IV | -19,42 |
| V | -18,84 |

Fig. 3-SI 1H NMR of casein solubilized in DMSO-d6.

Table 19-SI Films’ average thickness.

| Sample | Average thickness (µm) | Standard deviation (µm) |
| --- | --- | --- |
| C | 178 | 13 |
| CT | 201 | 20 |
| CS50 | 222 | 40 |
| CS100 | 203 | 42 |
| CU50 | 231 | 25 |
| CU100 | 244 | 29 |
| CS50T | 207 | 17 |
| CS100T | 258 | 15 |
| CU50T | 220 | 14 |
| CU100T | 269 | 18 |
| CT-GOx | 253 | 79 |
| CST-GOx | 260 | 39 |

Table 20-SI Evaluation of film solubility (in the brackets the short acronyms as in Fig. 4-SI).

| Sample | Condition | Initial weight (g) | Final weight (g) | Solubility (%) |
| --- | --- | --- | --- | --- |
| (A) C | Water | 0.0288 | 0.0070 | 76 |
|  | PBS | 0.0230 | / | / |
|  | Water after soaking in CA | 0.0189 | 0.0079 | 58 |
| (B) CT | Water | 0.0228 | 0.0138 | 39 |
|  | PBS | 0.0164 | 0.0104 | 37 |
|  | Water after soaking in CA | 0.0207 | 0.0122 | 41 |
| (C) CS50 | Water | 0.0161 | / | / |
|  | PBS | 0.0174 | 0.0056 | 68 |
|  | Water after soaking in CA | 0.0204 | 0.0107 | 48 |
| (D) CS100 | Water | 0.0143 | 0.0026 | 82 |
|  | PBS | 0.0211 | / | / |
|  | Water after soaking in CA | 0.0187 | 0.0082 | 56 |
| (E) CU50 | Water | 0.0307 | 0.0083 | 73 |
|  | PBS | 0.0216 | 0.0073 | 66 |
|  | Water after soaking in CA | 0.0168 | 0.0088 | 48 |
| (F) CU100 | Water | 0.0243 | 0.0072 | 70 |
|  | PBS | 0.0278 | / | / |
|  | Water after soaking in CA | 0.0177 | 0.0096 | 46 |
| (G) CS50T | Water | 0.0240 | 0.0144 | 40 |
|  | PBS | 0.0226 | 0.0142 | 37 |
|  | Water after soaking in CA | 0.0167 | 0.0094 | 44 |
| (H) CS100T | Water | 0.0224 | 0.0126 | 44 |
|  | PBS | 0.0239 | 0.0139 | 42 |
|  | Water after soaking in CA | 0.0200 | 0.0100 | 50 |
| (I) CU50T | Water | 0.0222 | 0.0140 | 37 |
|  | PBS | 0.0221 | 0.0152 | 31 |
|  | Water after soaking in CA | 0.0207 | 0.0123 | 41 |
| (L) CU100T | Water | 0.0183 | 0.0100 | 45 |
|  | PBS | 0.0189 | 0.0109 | 42 |
|  | Water after soaking in CA | 0.0135 | 0.0071 | 47 |
| (CG) CT-GOx | Water | 0.0200 | 0.0100 | 50 |
|  | PBS | 0.0259 | 0.0152 | 41 |
|  | Water after soaking in CA | 0.0141 | 0.0070 | 50 |
| (CLG) CST-GOx | Water | 0.0222 | 0.0081 | 64 |
|  | PBS | 0.0187 | 0.0089 | 52 |
|  | Water after soaking in CA | 0.0153 | 0.0078 | 49 |

Fig. 4-SI Film residues (see Table 20-SI for nomenclature, “Sample” column) after the overnight immersion in water (samples 1), PBS (samples 2), or acid citric followed by immersion in water (samples 3).

Table 21-SI Biodegradability data: weight loss % during time.

| Sample | 1h | 3h | 6h | 8h | 12h |
| --- | --- | --- | --- | --- | --- |
| C | 95.34 | 100.0 |  |  |  |
| CT | 27.23 | 47.34 | 55.23 | 94.46 | 93.85 |
| CS50 | 32.69 | 42.54 | 53.87 | 93.72 | 92.77 |
| CS100 | 26.86 | 43.07 | 54.16 | 90.1 | 98.11 |
| CU50 | 26.51 | 42.91 | 53.72 | 87.12 | 93.31 |
| CU100 | 26.16 | 40.18 | 55.61 | 84.11 | 98.83 |
| CS50T | 33.77 | 47.48 | 53.71 | 84.87 | 96.58 |
| CS100T | 33.16 | 43.58 | 55.19 | 89.24 | 92.48 |
| CU50T | 29.45 | 46.79 | 56.32 | 82.81 | 96.32 |
| CU100T | 28.3 | 46.22 | 52.29 | 88.61 | 96.39 |

Fig. 5-SI Graph of the weight loss % during time.

Fig. 6-SI Films biodegradability measurements: pictures at time 0 (A) and after 12 hours (B). See Table 20-SI for nomenclature, “Sample” column.

Fig. 7-SI XRD analyses, overlapping of all the acquired diffractograms.

Fig. 8-SI Matching between the XRD diffractogram of CU50 and the KH2PO4 reference signals (ICSD card 84-0328).

Fig. 9-SI Film images taken with Nikon Microphot-FXA optical microscope at 20x MAG.

C                                                                                            CT

CS100                                                                                CS100T

CU100                                                                               CU100T

Fig. 10-SI SEM images with SE2 detector of the samples C, CS100, and CU100.

20 µm

20 µm

C (Mag 512 X)                                                                          CS100 (Mag 2.59K X)

CU100 (Mag 512 X)                                                                      CU100 (Mag 4.84K X)

Table 22-SI Mechanical properties data.

| Sample | E (MPa) | Yield strength point (MPa) | Stress at break (MPa) | Elongation at break (%) |
| --- | --- | --- | --- | --- |
| CT | 336.54±18.42 | 13.03±0.18 | 12.08±0.59 | 74.84±5.80 |
| CS50T | 282.73±23.03 | 10.11±0.10 | 9.05±0.13 | 63.25±8.43 |
| CS100T | 141.86±6.84 | 4.58±0.11 | 5.90±0.10 | 131.10±2.75 |
| CU50T | 395.01±1.11 | 14.02±0.06 | 12.05±0.30 | 47.36±4.39 |
| CU100T | 82.28± 6.66 | 2.93±0.13 | 3.95±0.19 | 137.64±12.96 |

Fig. 11-SI Mechanical properties plot.

Table 23-SI Results of the comparative LCA. The percentage variation is calculated as the ratio between the difference between the final value and the initial value, and the initial value itself.

| Impact category | Unit of measure | C | Percentage variation with respect to sample C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CT | CS50 | CS100 | CU50 | CU100 | CS50T | CS100T | CU50T | CU100T |
| Acidification | mol H+ eq | 7.07E-03 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Climate change | kg CO2 eq | 1.59E+00 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Ecotoxicity, freshwater | CTUe | 6.84E+00 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |
| Particulate matter | disease inc. | 3.68E-08 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |
| Eutrophication, marine | kg N eq | 1.22E-03 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |
| Eutrophication, freshwater | kg P eq | 3.53E-04 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Eutrophication, terrestrial | mol N eq | 1.30E-02 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |
| Human toxicity, cancer | CTUh | 8.22E-10 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Human toxicity, non-cancer | CTUh | 1.97E-08 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |
| Ionising radiation | kBq U-235 eq | 1.85E-01 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Land use | Pt | 3.35E+01 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Ozone depletion | kg CFC11 eq | 3.65E-08 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Photochemical ozone formation | kg NMVOC eq | 4.65E-03 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Resource use, fossils | MJ | 2.50E+01 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Resource use, minerals and metals | kg Sb eq | 1.95E-05 | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% | <1% |
| Water use | m3 depriv. | 1.17E+00 | 1% | <1% | <1% | <1% | <1% | 1% | 1% | 1% | 1% |

Table 24-SI Normalization and weighting factors according to the Environmental Footprint 3.1 method (Andreasi Bassi et al., 2023).

| Impact category | Normalization factors |  | Weighting factos |
| --- | --- | --- | --- |
|  | Unit of measure | Value |  |
| Acidification | mol H+ eq | 5.56E+01 | 6.20% |
| Climate change | kg CO2 eq | 7.55E+03 | 21.06% |
| Ecotoxicity, freshwater | CTUe | 5.67E+04 | 1.92% |
| Particulate matter | disease inc. | 5.95E-04 | 8.96% |
| Eutrophication, marine | kg N eq | 1.95E+01 | 2.96% |
| Eutrophication, freshwater | kg P eq | 1.61E+00 | 2.80% |
| Eutrophication, terrestrial | mol N eq | 1.77E+02 | 3.71% |
| Human toxicity, cancer | CTUh | 1.73E-05 | 2.13% |
| Human toxicity, non-cancer | CTUh | 1.29E-04 | 1.84% |
| Ionising radiation | kBq U-235 eq | 4.22E+03 | 5.01% |
| Land use | Pt | 8.19E+05 | 7.94% |
| Ozone depletion | kg CFC11 eq | 5.23E-02 | 6.31% |
| Photochemical ozone formation | kg NMVOC eq | 4.09E+01 | 4.78% |
| Resource use, fossils | MJ | 6.50E+04 | 8.32% |
| Resource use, minerals and metals | kg Sb eq | 6.36E-02 | 7.55% |
| Water use | m3 depriv. | 1.15E+04 | 8.51% |

Table 25-SI Results of the comparative LCA after normalization and weighting stages.

| Impact category | C | CT | CS50 | CS100 | CU50 | CU100 | CS50T | CS100T | CU50T | CU100T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Acidification | 7.88 | 7.92 | 7.88 | 7.88 | 7.88 | 7.88 | 7.92 | 7.92 | 7.92 | 7.92 |
| Climate change | 44.4 | 44.5 | 44.4 | 44.4 | 44.4 | 44.4 | 44.5 | 44.5 | 44.5 | 44.5 |
| Ecotoxicity, freshwater | 2.31 | 2.34 | 2.31 | 2.31 | 2.31 | 2.31 | 2.34 | 2.34 | 2.34 | 2.34 |
| Particulate matter | 5.53 | 5.57 | 5.53 | 5.53 | 5.53 | 5.53 | 5.57 | 5.57 | 5.57 | 5.57 |
| Eutrophication, marine | 1.85 | 1.87 | 1.85 | 1.85 | 1.85 | 1.85 | 1.87 | 1.87 | 1.87 | 1.87 |
| Eutrophication, freshwater | 6.15 | 6.18 | 6.15 | 6.15 | 6.15 | 6.15 | 6.18 | 6.18 | 6.18 | 6.18 |
| Eutrophication, terrestrial | 2.72 | 2.75 | 2.72 | 2.72 | 2.72 | 2.72 | 2.75 | 2.75 | 2.75 | 2.75 |
| Human toxicity, cancer | 1.01 | 1.02 | 1.01 | 1.01 | 1.01 | 1.01 | 1.02 | 1.02 | 1.02 | 1.02 |
| Human toxicity, non-cancer | 2.82 | 2.83 | 2.82 | 2.82 | 2.82 | 2.82 | 2.83 | 2.83 | 2.83 | 2.83 |
| Ionising radiation | 2.19 | 2.20 | 2.19 | 2.19 | 2.19 | 2.19 | 2.20 | 2.20 | 2.20 | 2.20 |
| Land use | 3.24 | 3.25 | 3.24 | 3.24 | 3.24 | 3.24 | 3.25 | 3.25 | 3.25 | 3.25 |
| Ozone depletion | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 |
| Photochemical ozone formation | 5.44 | 5.46 | 5.44 | 5.44 | 5.44 | 5.44 | 5.46 | 5.46 | 5.46 | 5.46 |
| Resource use, fossils | 31.9 | 32.0 | 31.9 | 31.9 | 31.9 | 31.9 | 32.0 | 32.0 | 32.0 | 32.0 |
| Resource use, minerals and metals | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 | 23.1 |
| Water use | 8.65 | 8.71 | 8.65 | 8.65 | 8.65 | 8.65 | 8.71 | 8.71 | 8.71 | 8.71 |
| Single score | 149.3 | 149.7 | 149.3 | 149.3 | 149.3 | 149.3 | 149.7 | 149.7 | 149.7 | 149.7 |

Table 26-SI Results of the comparative LCA after normalization and weighting stages in the case of use of expired milk.

| Impact category | C | CT | CS50 | CS100 | CU50 | CU100 | CS50T | CS100T | CU50T | CU100T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Acidification | 7.22 | 7.26 | 7.22 | 7.22 | 7.22 | 7.22 | 7.26 | 7.26 | 7.26 | 7.26 |
| Climate change | 42.9 | 43.0 | 42.9 | 42.9 | 42.9 | 42.9 | 43.0 | 43.0 | 43.0 | 43.0 |
| Ecotoxicity, freshwater | 1.39 | 1.41 | 1.39 | 1.39 | 1.39 | 1.39 | 1.41 | 1.41 | 1.41 | 1.41 |
| Particulate matter | 4.82 | 4.85 | 4.82 | 4.82 | 4.82 | 4.82 | 4.85 | 4.85 | 4.85 | 4.85 |
| Eutrophication, marine | 1.48 | 1.51 | 1.48 | 1.48 | 1.48 | 1.48 | 1.51 | 1.51 | 1.51 | 1.51 |
| Eutrophication, freshwater | 5.97 | 5.99 | 5.97 | 5.97 | 5.97 | 5.97 | 5.99 | 5.99 | 5.99 | 5.99 |
| Eutrophication, terrestrial | 2.22 | 2.25 | 2.22 | 2.22 | 2.22 | 2.22 | 2.25 | 2.25 | 2.25 | 2.25 |
| Human toxicity, cancer | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 | 0.98 |
| Human toxicity, non-cancer | 2.74 | 2.75 | 2.74 | 2.74 | 2.74 | 2.74 | 2.75 | 2.75 | 2.75 | 2.75 |
| Ionising radiation | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 | 2.17 |
| Land use | 0.88 | 0.89 | 0.88 | 0.88 | 0.88 | 0.88 | 0.89 | 0.89 | 0.89 | 0.89 |
| Ozone depletion | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 |
| Photochemical ozone formation | 5.27 | 5.29 | 5.27 | 5.27 | 5.27 | 5.27 | 5.29 | 5.29 | 5.29 | 5.29 |
| Resource use, fossils | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 | 31.5 |
| Resource use, minerals and metals | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 | 22.8 |
| Water use | 8.24 | 8.30 | 8.24 | 8.24 | 8.24 | 8.24 | 8.30 | 8.30 | 8.30 | 8.30 |
| Single score | 140.6 | 141.0 | 140.6 | 140.6 | 140.6 | 140.6 | 141.0 | 141.0 | 141.0 | 141.0 |

Table 27-SI Results of the comparative LCA after normalization and weighting stages in the best-case scenario (use of expired milk and 50% reduction of laboratory energy consumptions).

| Impact category | C | CT | CS50 | CS100 | CU50 | CU100 | CS50T | CS100T | CU50T | CU100T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Acidification | 3.63 | 3.67 | 3.63 | 3.63 | 3.63 | 3.63 | 3.67 | 3.67 | 3.67 | 3.67 |
| Climate change | 21.5 | 21.6 | 21.5 | 21.5 | 21.5 | 21.5 | 21.6 | 21.6 | 21.6 | 21.6 |
| Ecotoxicity, freshwater | 0.70 | 0.73 | 0.70 | 0.70 | 0.70 | 0.70 | 0.73 | 0.73 | 0.73 | 0.73 |
| Particulate matter | 2.42 | 2.46 | 2.42 | 2.42 | 2.42 | 2.42 | 2.46 | 2.46 | 2.46 | 2.46 |
| Eutrophication, marine | 0.75 | 0.78 | 0.75 | 0.75 | 0.75 | 0.75 | 0.78 | 0.78 | 0.78 | 0.78 |
| Eutrophication, freshwater | 2.99 | 3.02 | 2.99 | 2.99 | 2.99 | 2.99 | 3.02 | 3.02 | 3.02 | 3.02 |
| Eutrophication, terrestrial | 1.12 | 1.14 | 1.12 | 1.12 | 1.12 | 1.12 | 1.14 | 1.15 | 1.15 | 1.15 |
| Human toxicity, cancer | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 | 0.49 |
| Human toxicity, non-cancer | 1.37 | 1.39 | 1.37 | 1.37 | 1.37 | 1.37 | 1.39 | 1.39 | 1.39 | 1.39 |
| Ionising radiation | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 |
| Land use | 0.44 | 0.45 | 0.44 | 0.44 | 0.44 | 0.44 | 0.45 | 0.45 | 0.45 | 0.45 |
| Ozone depletion | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 |
| Photochemical ozone formation | 2.64 | 2.66 | 2.64 | 2.64 | 2.64 | 2.64 | 2.66 | 2.66 | 2.66 | 2.66 |
| Resource use, fossils | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 | 15.8 |
| Resource use, minerals and metals | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 | 11.4 |
| Water use | 4.12 | 4.18 | 4.12 | 4.12 | 4.12 | 4.12 | 4.18 | 4.18 | 4.18 | 4.18 |
| Single score | 70.5 | 70.9 | 70.5 | 70.5 | 70.5 | 70.5 | 70.9 | 70.9 | 70.9 | 70.9 |

Fig. 12-SI Results of the hotspot analysis for sample C.

Fig. 13-SI Results of the hotspot analysis for sample CT.

Fig. 14-SI Results of the hotspot analysis for sample CS50.

Fig. 15-SI Results of the hotspot analysis for sample CS100.

Fig. 16-SI Results of the hotspot analysis for sample CU50.

Fig. 17-SI Results of the hotspot analysis for sample CU100.

Fig. 18-SI Results of the hotspot analysis for sample CS50T.

Fig. 19-SI Results of the hotspot analysis for sample CS100T.

Fig. 20-SI Results of the hotspot analysis for sample CU50T.

Fig. 21-SI Results of the hotspot analysis for sample CU100T.

Fig. 22-SI FT-IR spectra of samples CT-GOx and CST-Gox.

CT-GOx

CT-GOx

CT-GOx

CT-GOx

CST-GOx

CST-GOx

Fig. 23-SI SEM images of samples CT-GOx and CST-GOx.

CT-GOx (Mag 503 X)                                                                CT-GOx (Mag 3.01K X)

CST-GOx (Mag 2.70K X)                                                         CST-GOx (Mag 5.71K X)

Fig. 24-SI GOx maximum activity (expressed as vmax) in absence of casein and lignin in solution (no C/L), in the presence of casein (C), in the presence of lignin (L), and in the presence of casein and lignin (C/L).

Fig. 25-SI GOx maximum activity (expressed as vmax) evaluated during time after film preparation for CT-GOx and CST-GOx films.

## References (LCA)

S. Andreasi Bassi, F. Biganzoli, N. Ferrara, A. Amadei, A. Valente, S. Sala, F. Ardente, Updated characterisation and normalisation factors for the Environmental Footprint 3.1 method, 2023, Publications Office of the European Union. DOI:10.2760/798894

P. Bartocci, P. Fantozzi, F. Fantozzi, Environmental impact of Sagrantino and Grechetto grapes cultivation for wine and vinegar production in central Italy. Journal of Cleaner Production, 2017, 140, 569-580. DOI: 10.1016/j.jclepro.2016.04.090

C. Culbertson, T. Treasure, R. Venditti, H. Jameel, R. Gonzalez, Life Cycle Assessment of lignin extraction in a softwood kraft pulp mill. Nordic Pulp & Paper Research Journal, 2016, 31(1), 30-40. DOI:  10.3183/NPPRJ-2016-31-01-p030-040

A. Fusi, R. Guidetti, G. Benedetto, Delving into the environmental aspect of a Sardinian white wine: From partial to total life cycle assessment. Science of the Total Environment, 2014, 472, 989-1000. DOI: 10.1016/j.scitotenv.2013.11.148

C. Hidalgo, C. Vegas, E. Mateo, W. Tesfaye, A. B. Cerezo, R. M. Callejón, M.J. Torija, Effect of barrel design and the inoculation of Acetobacter pasteurianus in wine vinegar production. International Journal of Food Microbiology, 2010, 141(1-2), 56-62. DOI: 10.1016/j.ijfoodmicro.2010.04.018

R. Morya, M. Kumar, I. Tyagi, A.K. Pandey, J. Park, T. Raj, R. Siroh, V. Kumar, S.H. Kim, Recent advances in black liquor valorization. Bioresource technology, 2022, 350, 126916. DOI: 10.1016/j.biortech.2022.126916

M. Secchi, V. Castellani, M. Orlandi, E. Collina, Use of lignin side-streams from biorefineries as fuel or co-product? Life cycle analysis of bio-ethanol and pulp production processes. BioResources, 2019, 14(2), 4832-4865. DOI: 10.15376/biores.14.2.4832-4865

L. Valsasina, M. Pizzol, S. Smetana, E. Georget, A. Mathys, V. Heinz, Life cycle assessment of emerging technologies: The case of milk ultra-high pressure homogenisation. Journal of Cleaner Production, 2017, 142, 2209-2217. DOI: 10.1016/j.jclepro.2016.11.059