Supplementary materials

Dendrite suppression by scalable acid treatment of zinc metal anodes for aqueous zinc-ion batteries

Huanlin Lyua, Suihan Cuia,b, Chao Huanga, Qingdong Ruana, Xiaolin Zhanga, Junmin Xua,d, Fangyu Xiong*c, Dan Li*a, Paul K. Chu*a

a Department of Physics, Department of Materials Science and Engineering, and Department of Biomedical Engineering, City University of Hong Kong, Tat Chee Avenue, Kowloon, Hong Kong, China

b School of Advanced Materials, Peking University, Shenzhen Graduate School, Shenzhen, 518055 P. R. China

c College of Materials Science and Engineering, Chongqing University, Chongqing 400030, China

d Key Laboratory of Materials Physics, Ministry of Education, School of Physics, Zhengzhou University, Zhengzhou 450001, China

* Corresponding authors: xfy@cqu.edu.cn (F. Xiong); dan.li@my.cityu.edu.hk (D. Li); paul.chu@cityu.edu.hk (P.K. Chu)

Fig. S1. Electrochemical plating/stripping cycles of symmetrical coin cells with the three Zn foil electrodes (pristine Zn, HCl-5 Zn, and HCl-30 Zn) and Zn(CF3SO3)2 electrolyte at a current density of ±1 mA cm-2 for 1 h at room temperature.

Fig. S2. (a) Electrochemical plating/stripping cycles of symmetrical coin cells with the two Zn foil electrodes (pristine Zn and one treated with HCl for 5 s) and hydrogel electrolyte at a current density of ± 1 mA cm-2 for 1 h at room temperature; (b) Rate performance of the symmetric coin cells (pristine Zn and one treated with HCl for 5 s) at 0.5, 1, 2, and 4 mA cm-2.

Fig. S3. XRD patterns of K0.5V2O5@CC.

Fig. S4. Photographs of (a) Raw CC (left) and KVO@CC (right); (b) SEM images and (c) EDS maps of KVO.

Fig. S5. Charging/discharging profiles of full cells with (a) Pristine and (b) HCl-30 Zn anodes at 0.5, 1.0, 2.0, 5.0, 10.0 A g−1; Charging/Discharging profiles of full cells with (c) Pristine and (d) HCl-30 Zn anodes for the 1st, 100th, and 300th cycles.

Fig. S6. Cycling characteristics of full cells with three different Zn anodes versus the KVO@CC cathode; Galvanostatic charging/discharging at a current density of 2.0 A g-1.

Fig. S7. (a) Cycling characteristics of the flexible full battery with the HCl-5 Zn anode and hydrogel electrolyte and galvanostatic charging/discharging curves acquired at a current density of 0.5 A g-1; (b) Charging/discharging profiles of the flexible full battery with the HCl-5 Zn anode in the 1st, 50th, 100th, 150th, and 200th cycles.

Fig. S8. Contact angle on the HCl-30 Zn foil.

Fig. S9. (a)  Nyquist plots of the pristine and HCl-5 Zn symmetric cells based on electrochemical impedance spectroscopy (EIS); (b) Linear sweep voltammetry (LSV) curves of the pristine and HCl-5 Zn symmetric cells at a sweeping rate of 1 mV s−1.

Fig. S10. SEM images (left) and AFM images (right) of the HCl-30 Zn foil electrode after plating for (a, d) 1 min, (b, e) 1 h, and (c, f) After stripping for 1 h.

Fig. S11. SEM images of (a) Pristine, (b) HCl-5, and (c) HCl-30 Zn electrodes after plating for 1 min.

Fig. S12. SEM images: (a, c) Pristine and (b, d) HCl-5 Zn foil electrodes after stripping for (a and b) 1 min and (c and d) 1 h.

Table S1. Comparison of cycling characteristics of Zn electrodes with different treatments.

| Treatment | Concentration | Etching time | Separator | Current density (mA cm-2) | Fixed capacity (mAh cm-2) | Cycling time (h) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HCl | 6% | 5 min | GF | 1 | 0.5 | 200 | [1] |
| HCl | 6 M | 10 s | GF | 5 | 2.5 | 112.5 | [2] |
| H3PO4 | 85% | 10 min | GF/D | 10 | 2 | 1200 | [3] |
| Citric acid | 10 % | 2 min | GF | 1 | 1 | 225 | [4] |
| Oxalic acid | 10 % | 2 min | GF | 1 | 1 | 140 | [4] |
| NaOH | 2 M | 36 h | GF/D | 1 | 1 | 1600 | [5] |
| HCl | 5% HCl | 5 s | GF/A | 1 | 1 | 300 | This work |
| HCl | 5% HCl | 5 s | Gelatin | 1 | 1 | 1000 | This work |

References

[1] J. Wang, Z. Cai, R. Xiao, Y. Ou, R. Zhan, Z. Yuan, Y. Sun, A chemically polished zinc metal electrode with a ridge-like structure for cycle-stable aqueous batteries, ACS applied materials & interfaces 12 (2020) 23028-23034.

[2] P. Kulkarni, S.-S. Kim, H.Y. Jung, Chemical surface tuning of zinc metal anode toward stable, dendrite-less aqueous zinc-ion batteries, Journal of Energy Chemistry 86 (2023) 1-8.

[3] T.T. Su, K. Wang, B.Y. Chi, W.F. Ren, R.C. Sun, Stripy zinc array with preferential crystal plane for the ultra‐long lifespan of zinc metal anodes for zinc ion batteries, EcoMat 4 (2022) e12219.

[4] X. Wang, J. Meng, X. Lin, Y. Yang, S. Zhou, Y. Wang, A. Pan, Stable zinc metal anodes with textured crystal faces and functional zinc compound coatings, Advanced Functional Materials 31 (2021) 2106114.

[5] R. Guo, X. Liu, F. Xia, Y. Jiang, H. Zhang, M. Huang, C. Niu, J. Wu, Y. Zhao, X. Wang, Large‐Scale Integration of a Zinc Metasilicate Interface Layer Guiding Well‐Regulated Zn Deposition, Advanced Materials 34 (2022) 2202188.