## Slide 2
Bovine Serum Albumin
(BSA)
750-800 C
Dissolve in
75 mM NaCl
In pH-2
8 Hour
D-Gel
L-Gel
D-C-Dot
L-C-Dot
D-C-Dot-doped BSA-Gel
L-C-Dot-doped BSA-Gel

## Slide 3
Figure-1
PL Intensity

## Slide 4
10 µm
10 µm
10 µm
Figure-2

## Slide 5
Figure-3

## Slide 6
Figure-4
20
40
50
60
30
10 mM
50
60
10 mM
20
30
40

## Slide 7
Figure-5

## Slide 8
0 mM
60 mM
0 mM
60 mM
50 mM
0 mM
50 mM
0 mM
Figure-6

## Slide 9
Supporting Data

## Slide 10
Bovine Serum Albumin
(BSA)
BSA Solution
750-800 C
For 8 Hour
BSA-Hydrogel
Dissolve in
75 mM
NaCl
pH-2
S1

## Slide 11
S2

## Slide 12
S3

## Slide 13
S4

## Slide 14
S5

## Slide 15
S6

## Slide 16
S7

## Slide 17
S8

## Slide 18
S9

## Slide 19
S10

## Slide 20
S11

## Slide 21
S12

## Slide 22
S13

## Slide 23
0 mM
60 mM
0 mM
60 mM
0 mM
50 mM
0 mM
50 mM
L L-UV
L D-UV
L D-PL
L L-PL
S14

## Slide 24
D
50 mM
0 mM
50 mM
0 mM
50 mM
0 mM
50 mM
0 mM
D-Gel-system
D Leu
D PA
L PA
L Leu
S15

## Slide 25
L Gel
50 mM
0 mM
50 mM
0 mM
50 mM
0 mM
50 mM
0 mM
D Leu
L Leu
L PA
D PA
S16

## Slide 26
S17

## Slide 27
System | t₁ (ns) | B₁ (%) | c2
D-C-Dot | 11.0592 | 100 | 2.1
L-C-Dot | 11.0759 | 100 | 2
A-C-Dot | 10.9626 | 100 | 1.8
Singal exponential fitting time of time-resolved fluorescence lifetime measurement for all C-Dot.

## Slide 28
Fitting time of time-resolved fluorescence lifetime measurement for all C-Dot-Gel
System | t₁ (ns) | B₁ (%) | t₂ (ns) | B₂ (%) | t3 (ns) | B3 (%) | c2 | <t> (ns)
D-Gel | 0.151 | 27.1 | 2.88 | 24.01 | 9.49 | 48.89 | 1 | 5.37
L-Gel | 0.180 | 30.24 | 2.93 | 22.3 | 9.63 | 47.47 | 1 | 5.28
A-Gel | 0.155 | 27.12 | 2.93 | 24.64 | 9.48 | 48.24 | 1.1 | 5.34

## Slide 29
System | L (mm) | R (Ohm) | W (cm) | T (mm) | Conductivity (S.cm-1)
B-Gel | 0.5 | 1413403 | 1 | 0.04 | 0.89×10-5
D-Gel | 0.5 | 419492 | 1 | 0.04 | 2.97×10-5
L-Gel | 0.5 | 369041 | 1 | 0.04 | 3.38×10-5
A-Gel | 0.5 | 1229436 | 1 | 0.04 | 1.01×10-5
Conductivity of B-Gel and chiral C-Dots-B-Gel Composite system