Supporting Information

CsMgGa5S9: a diamond-like network formed by mixed tetrahedral units for excellent nonlinear optical properties

Yi-Bing Huang,a,b,d Bin-Wen Liu,a,c,* and Guo-Cong Guoa,c,*

a State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian 350002, P. R. China.

b College of Chemistry, Fuzhou University, Fuzhou, Fujian 350116, P. R. China.

c Fujian Science & Technology Innovation Laboratory for Optoelectronic Information of China, Fuzhou, Fujian 350108, P. R. China.

d Fujian College, University of Chinese Academy of Sciences, Fuzhou, Fujian 350002, P. R. China.

Experimental Section

The raw materials, including Ga (33.3 mg, Alfa, 99.99%), Mg (133.3 mg, Aladdin, 99%), S (266.7 mg, Aladdin, 99.9%), and CsI (66.6 mg, Aladdin, 99.9%), were accurately weighed. The mixtures were placed into a quartz tube inside an argon-filled glove box. The quartz tube was sealed with a hydrogen-oxygen flame at a pressure of 10⁻2 Torr and then placed in a programmable muffle furnace. The temperature was gradually increased from room temperature to 740 °C over 25 hours, maintained at this temperature for 96 hours, and then slowly decreased to 300°C at a rate of 3 °C/h. Finally, the furnace was turned off to cool naturally to room temperature. The water-soluble nature of CsI allowed its efficient removal through successive deionized water washes. The yield of CsMgGa5S9 was ~30%. Elemental composition was determined by micro-probe analysis using a Hitachi S-3500 scanning electron microscope (SEM) equipped with energy-dispersive X-ray spectroscopy (EDS). Single-crystal X-ray Diffraction (XRD) data for CsMgGa5S9 was obtained using a Rigaku FR-X Microfocus diffractometer, employing Mo-Kα radiation (λ = 0.71073 Å) and a graphite monochromator. The collected data was processed and integrated using the CrysAlisPro software.1 The intensity data were recorded via the ω-scan technique, followed by refinement using the Siemens SHELXTL software.2 Structural analysis, confirming the absence of higher symmetries, was carried out with the PLATON program.3 Detailed crystallographic parameters, including atomic coordinates, isotropic displacement factors, bond lengths, angles, and refinement results, are provided in Tables S1-3. For powder XRD measurements, a Rigaku MiniFlex 600 diffractometer with Cu-Kα radiation (λ = 1.54057 Å) was used in reflection mode at room temperature. The optical diffuse reflectance spectrum of CsMgGa5S9 was recorded using a PerkinElmer Lambda 950 UV/Vis/NIR spectrophotometer with a BaSO4 plate serving as the reference for full reflectance, covering a wide wavelength range from 200 to 2500 nm. The acquired reflectance data was then transformed into absorption spectra using the Kubelka-Munk function. The second-harmonic generation (SHG) response of CsMgGa5S9 was measured using a modified Kurtz-Perry NLO setup with a 1910 nm laser. The samples and commercial AgGaS2 were ground into different size fractions, categorized into ranges of 30–50, 50–75, 75–100, 100–150, and 150–200 μm. These fractions were then compacted into cylindrical containers with a thickness of 1 mm and a diameter of 8 mm for SHG testing. Additionally, the preliminary laser-induced damage thresholds (LIDTs) of single-crystal CsMgGa5S9 and AgGaS2 were determined under high-power 1064 nm laser irradiation. A pulse width (τp) of 10 ns and a repetition rate of 1 Hz were employed, and the single-pulse technique was utilized. During the experiment, the laser power was gradually increased until a damaged spot was observed under microscopic inspection. The LIDT was calculated using the formula I(threshold) = E/(πr²τp), where E represents the laser energy per pulse, r is the spot radius, and τp is the pulse width. To gain deeper insights into the relationship between the structure of CsMgGa5S9 and its linear and nonlinear optical properties, a series of density functional theory (DFT) calculations were performed using the ABINIT software package. The generalized gradient approximation (GGA), as parameterized by Perdew, Burke, and Ernzerhof (PBE), was employed for the calculations. Valence electron configurations for the constituent elements—Mg-2s22p6, S-3s23p4, Ga-4s23d104p1, and Cs-5s26s15p6—were included through projector-augmented wave (PAW) pseudopotentials. The plane wave energy cutoff was set to 18 Hartree. For K-point sampling, the Brillouin zone integration was performed using the tetrahedron method, with a Monkhorst-Pack mesh of 4×4×2 tailored for CsMgGa5S9. The optical properties were derived from the complex dielectric function, and the second-order NLO susceptibility tensor, χijk(2ω, ω, ω), was calculated using density functional perturbation theory combined with the "sum over states" method. The total SHG susceptibility was decomposed into three main contributions: the pure interband transition term χinter(2ω,ω,ω), the intraband transition term χintra(2ω,ω,ω), and the modulation term χmod. The angle-averaged effective NLO coefficient squared <deff2> was used to determine the effective SHG coefficient deff for polycrystalline materials：

deff2=19105idiii2+13105i≠jdiiidijj+44105i≠jdiij2+13105ijk,cyclicdiijdjkk+57dijk2dijk=12χijk

Figures and Tables

Fig S1.. EDS of CsMgGa5S9.

Table S1. Crystallographic data and structure refinement results of CsMgGa5S9.

| Empirical formula | CsMgGa₅S₉ |
| --- | --- |
| CCDC | 2415340 |
| Fw | 794.36 |
| Temperature (K) | 293(2) |
| Space group | P1 |
| a (Å) | 8.9771(3) |
| b (Å) | 9.6445(3) |
| c (Å) | 9.7174(2) |
| V (Å3) | 750.06(4) |
| (Å3) | 95.806(2) |
| (Å3) | 115.504(3) |
| (Å3) | 93.640(2) |
| Z | 2 |
| Dcalcd (g·cm−3) | 3.517 |
| μ(mm−1) | 12.514 |
| GOF on F2 | 1.047 |
| R1a (I > 2σ(I)) | 0.0388 |
| wR2b (I > 2σ(I)) | 0.0966 |
| R1a (all data) | 0.0408 |
| wR2b (all data) | 0.0978 |
| Δρmax/Δρmin (e Å−3) | 1.73/-1.40 |
| Flack | 0.082(15) |
| aR = Σ¦¦Fo¦−¦Fc¦¦/Σ¦Fo¦, bwR = (Σ(w(Fo2−Fc2)2)/Σ(w(Fo2)2))1/2. |  |

Table S2 Coordinates (×104) and equivalent isotropic displacement parameters (Å2×103) of all crystallographically independent atoms in CsMgGa5S9.

| Atom | x | y | z | U(eq) |
| --- | --- | --- | --- | --- |
| Cs(1) | -3756.5(11) | 9583.9(9) | 11023.9(10) | 22.6(3) |
| Cs(2) | 2331.0(12) | 3823.4(9) | 6528.9(10) | 24.4(3) |
| Mg(1) | -1352(6) | 5356(5) | 8310(5) | 11.8(12) |
| Mg(2) | -1203(4) | 7098(3) | 4946(3) | 8.9(8) |
| Mg(3) | 842(3) | 7433(2) | 12207(2) | 11.2(5) |
| Ga(1) | -1203(4) | 7098(3) | 4946(3) | 8.9(8) |
| Ga(2) | 795(2) | 9144.9(17) | 8717.7(18) | 12.6(4) |
| Ga(3) | 2981(2) | 4485.0(15) | 11226.8(17) | 13.0(4) |
| Ga(4) | -3184(2) | 10258.4(15) | 5917.9(17) | 13.7(4) |
| Ga(5) | 842(3) | 7433(2) | 12207(2) | 11.2(5) |
| Ga(6) | 6707(2) | 3413.9(17) | 14241.8(18) | 11.9 (4) |
| Ga(7) | 6876(2) | 4938.8(16) | 10960.7(18) | 13.0(4) |
| Ga(8) | 2664(2) | 11069.9(16) | 12814.1(18) | 12.4(4) |
| Ga(9) | -928(2) | 12222.2(15) | 10035.9(17) | 13.0(4) |
| Ga(10) | 2789(2) | 9239.3(17) | 6240.0(17) | 12.2(4) |
| Ga(11) | 4850(2) | 6624.7(15) | 15156.5(18) | 13.1(4) |
| S(1) | 4316(5) | 7510(4) | 7080(4) | 12.5(8) |
| S(2) | 310(5) | 11893(4) | 12500(4) | 14.5(9) |
| S(3) | -1622(5) | 4800(4) | 3564(4) | 14.4(8) |
| S(4) | 2400(5) | 10543(4) | 8084(4) | 15.3(9) |
| S(5) | -1767(5) | 6692(4) | 10309(4) | 14.1(8) |
| S(6) | 540(5) | 3586(3) | 9172(4) | 11.1(8) |
| S(7) | 2370(4) | 5587(3) | 13130(4) | 8.9(8) |
| S(8) | 2320(5) | 8937(3) | 11344(4) | 13.2(8) |
| S(9) | -3706(5) | 8120(3) | 4374(4) | 12.2(8) |
| S(10) | 4458(5) | 5835(4) | 10446(4) | 15.0(8) |
| S(11) | 6562(5) | 2932(4) | 9440(4) | 22.1(10) |
| S(12) | 6061(5) | 4653(4) | 15987(4) | 13.8(8) |
| S(13) | -5795(5) | 10903(4) | 5432(4) | 12.5(8) |
| S(14) | 306(5) | 8647(4) | 4089(4) | 14.7(9) |
| S(15) | -1770(5) | 11679(3) | 5112(4) | 12.1(8) |
| S(16) | -1674(4) | 9986(3) | 8485(3) | 9.2(8) |
| S(17) | 332(5) | 6905(4) | 7569(4) | 16.2(9) |
| S(18) | 4289(5) | 12525(4) | 12082(4) | 11.1(8) |

Table S3. Selected bond lengths (Å) of CsMgGa5S9.

| bond | length/Å | bond | length/Å | bond | length/Å |
| --- | --- | --- | --- | --- | --- |
| Cs(1)−S(1) | 3.739(3) | Mg(1)−S(5) | 2.398(6) | Ga(6)−S(3) | 2.290(4) |
| Cs(1)−S(2) | 3.763(4) | Mg(1)−S(6) | 2.436(6) | Ga(6)−S(12) | 2.273(5) |
| Cs(1)−S(4) | 3.657(4) | Mg(1)−S(12) | 2.434(7) | Ga(6)−S(15) | 2.228(4) |
| Cs(1)−S(5) | 3.572(4) | Mg(1)−S(17) | 2.430(7) | Ga(6)−S(18) | 2.308(4) |
| Cs(1)−S(8) | 3.687(4) | Mg/Ga(2)−S(3) | 2.391(5) | Ga(7)−S(3) | 2.322(4) |
| Cs(1)−S(9) | 3.661(3) | Mg/Ga(2)−S(9) | 2.376(5) | Ga(7)−S(5) | 2.316(4) |
| Cs(1)−S(10) | 3.746(4) | Mg/Ga(2)−S(14) | 2.393(5) | Ga(7)−S(10) | 2.258(4) |
| Cs(1)−S(11) | 3.761(4) | Mg/Ga(2)−S(17) | 2.353(4) | Ga(7)−S(11) | 2.237(4) |
| Cs(1)−S(14) | 3.820(4) | Mg/Ga(3)−S(5) | 2.280(4) | Ga(8)−S(2) | 2.213(4) |
| Cs(1)−S(15) | 3.855(4) | Mg/Ga(3)−S(7) | 2.330(4) | Ga(8)−S(8) | 2.305(4) |
| Cs(1)−S(16) | 3.715(3) | Mg/Ga(3)−S(8) | 2.351(4) | Ga(8)−S(13) | 2.344(4) |
| Cs(1)−S(18) | 3.712(4) | Mg/Ga(3)−S(14) | 2.311(4) | Ga(8)−S(18) | 2.332(4) |
| Cs(2)−S(1) | 3.754(4) | Ga(2)−S(4) | 2.226(4) | Ga(9)−S(2) | 2.230(4) |
| Cs(2)−S(2) | 3.750(3) | Ga(2)−S(8) | 2.357(4) | Ga(9)−S(6) | 2.264(4) |
| Cs(2)−S(3) | 3.735(4) | Ga(2)−S(16) | 2.336(4) | Ga(9)−S(11) | 2.244(5) |
| Cs(2)−S(4) | 3.634(4) | Ga(2)−S(17) | 2.255(4) | Ga(9)−S(16) | 2.379(3) |
| Cs(2)−S(6) | 3.587(4) | Ga(3)−S(6) | 2.276(4) | Ga(10)−S(1) | 2.220(4) |
| Cs(2)−S(7) | 3.877(3) | Ga(3)−S(7) | 2.324(4) | Ga(10)−S(4) | 2.248(4) |
| Cs(2)−S(10) | 3.698(4) | Ga(3)−S(10) | 2.209(4) | Ga(10)−S(13) | 2.380(4) |
| Cs(2)−S(11) | 3.850(4) | Ga(3)−S(18) | 2.324(4) | Ga(10)−S(14) | 2.291(4) |
| Cs(2)−S(12) | 3.660(4) | Ga(4)−S(9) | 2.317(4) | Ga(11)−S(1) | 2.226(4) |
| Cs(2)−S(13) | 3.666(4) | Ga(4)−S(13) | 2.322(5) | Ga(11)−S(7) | 2.319(4) |
| Cs(2)−S(15) | 3.717(4) | Ga(4)−S(15) | 2.226(4) | Ga(11)−S(9) | 2.274(4) |
| Cs(2)−S(17) | 3.835(4) | Ga(4)−S(16) | 2.323(4) | Ga(11)−S(12) | 2.295(4) |

Table S4. The LIDTs of CsMgGa5S9 and the reference AgGaS2.

| Compounds | Damage energy (mJ) | Spot area (cm2) | Damage threshold (MW/cm2) | Relative values (times) |
| --- | --- | --- | --- | --- |
| CsMgGa5S9 | 11.95 | 0.015 | 77.6 | 8.0 |
| AgGaS2 | 1.50 | 0.015 | 9.74 | 1.0 |

References

1.	Rigaku, O. D., CrysAlisPro Software System. Version 2018, 1 (38.41), l.

2.	Sheldrick, G., SHELXS-9L ProgramforX-ray Crystal Structure Solution. University ofG6ttingen, Germany 1997, 13.

3.	Spek, A., Single-crystal structure validation with the program PLATON. J. Appl. Crystallogr. 2003, 36 (1), 7-13.