Supplementary material

Temperature-dependent structural stability, mechanical strength, and thermodynamics of pyrite-type silicon pernitride

Haiyan Yana,*, Lei Chena,b,*, Yun Zhanga,b, Xuanyu Caoa,b, Meiguang Zhanga,b,, Qun Weic,

a College of Chemistry and Materials Engineering, Collaborative Innovation Center of Rare-Earth Functional Materials and Devices Development, Baoji University of Arts and Sciences, Baoji 721013, China

b College of Physics and Optoelectronic Technology, Baoji University of Arts and Sciences, Baoji 721013, China

c School of Physics, Xidian University, Xi'an 710071, China

Table S1 AIMD tests of elastic constants Cij, the Hill bulk modulus B, shear modulus G, and Young's modulus E using different supercells for diamond and p-SiN2 (all in GPa).

|  | T | Supercell | K-mesh | Source | C11 | C12 | C44 | B | G | E |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Diamond | 1000 K | 2×2×2 | 4×4×4 | This work | 1006 | 120 | 520 | 417 | 488 | 1052 |
|  |  | 3×3×3 | 2×2×2 | This work | 997 | 113 | 531 | 408 | 493 | 1054 |
|  |  | 2×2×2 | 2×2×2 | Theory1 | 944 | 143 | 510 | 408 | 467 |  |
|  |  |  |  | Exp.2 | 1054.1 | 124.3 | 556.6 | 434.2 | 517.9 | 1111.7 |
| p-SiN2 | 1200 K | 2×2×2 | 4×4×4 | This work | 609 | 119 | 341 | 282 | 299 | 662 |
|  |  | 3×3×3 | 2×2×2 | This work | 606 | 121 | 342 | 283 | 298 | 661 |

Fig. S1 AIMD NVT tests of extended system energy vs. time at different temperatures (using the Nosé-Hoover thermostat with 1 fs time step).

Fig. S2 AIMD NPT tests of average stress–strain curves of p-SiN2 under ideal tensile strains along [001] direction at 900 K using two different supercells.

Fig. S3 AIMD NPT simulations at 300, 600, 2000, and 3000 K for p-SiN2 under ambient conditions. Insets are the equilibrium structures after 30 ps.

Fig. S4 High-temperature renormalized phonon spectra of p-SiN2 (a) and diamond (b).

Fig. S5 Calculated N–N bond length versus ICOHP at various indentation shear strains alongdirection.

References

1  L. B. Wen, H. Wu, H. Sun and C. F. Chen, Carbon, 2019, 155, 361−368.

2  E. S. Zouboulis, M. Grimsditch, A. K. Ramdas and S. Rodriguez, Phys. Rev. B, 1998, 57,2889.

*These authors contributed equally to this work.

zhmgbj@126.com (Meiguang Zhang)

weiaqun@163.com (Qun Wei)