Supporting Information

Ultrafast Charging of Ionic liquid-Ti2CT2 MXene Supercapacitor: A First-Principles Study

Mengmeng Gea, Kun Jiangb* Chunlei Weic*,

a College of Materials Science and Engineering, Qingdao University, Qingdao 266071, Shandong, China

b School of Chemistry and Chemical Engineering, Wuhan Textile University, Wuhan 430079, Hubei, China

c. Institute of Zhejiang University-Quzhou, Quzhou, 324000, Zhejiang, China

*Corresponding author: jiangkun90@126.com; weichunlei2018@163.com;

Table of Content

Figure S1. Test of the influence of K-point density on DOS

Figure S2. Test of the influence of smearing method on DOS.

Figure S3. Test of the influence of smearing value on DOS.

Figure S4. Energy profiles and geometrical structures of Ti2CO2-[Emim][BF4], Ti2CF2-[Emim][BF4], and Ti2C(OH)2-[Emim][BF4] after an AIMD simulation, respectively.

Figure S5. The side view of (a) [Emim][Cl], (b)[Emim][BF4]; (c)[Emim][PF6] (d)[Emim][OAc] on the Ti2CO2 surface.

Figure S6. The (a) side and (b) top view of [Emim]+ structure; (c-d) The different side view of [Emim]+ on the Ti2CO2 surface.

Figure S7. (a-c) Three different migration paths of [Emim]+ on Ti2CO2; (d-f) Three different migration paths of [Emim]+ on Ti2CF2 Take the center of imidazolium ring as the migration center.

Figure S8. The schematic diagram defining the atomic numbers on the imidazolium ring, as well as the definition of atomic height.

Figure S9. The convergence standard test of [Emim]+ on the Ti2CO2 via C-C′ path.

Figure S10. The energy profile of Ti2CT2-[Emim]+ via AIMD simulation.

Figure S11. The snapshots of (a) Ti2CF2-[Emim]+ and (b) Ti2CO2-[Emim]+via AIMD simulation.

Figure S12. The MSD curve of [Emim]+ on Ti2CT2 after AIMD simulation.

Figure S13. The different coverage (a) 0.08, (b) 0.12, (c) 0.16, (d) 0.20 ML of [Emim]+ on Ti2CO2 with the flat model.

Figure S14. The different coverage (a) 0.24, (b) 0.28, (c) 0.32, (d) 0.36 ML of [Emim]+ on Ti2CO2 with the stand model.

Figure S15. The 0.40 ML coverage of [Emim]+ on Ti2CO2 in the stand model, the local magnification diagram represents the crowded form of the molecular structure.

Table S1. The test for different dispersion correction choices.

Table S2. Convergence tests using different K-point densities for different supercells, taking Ti2CO2 as example.

Table S3. Convergence tests using different thickness of the vacuum layer crystal cells, taking Ti2CO2 as example.

Table S4. Convergence test of the adsorption energies of [Emim]+ cations by supercells with different lateral dimensions, taking Ti2CO2 as example.

Table S5. Comparison of adsorption energy and diffusion barrier of adsorbate on MXenes.

Table S6. Sensitivity test of the adsorption energies of Ti2CO2-[Emim]+ with or without background.

Table S7. The variations in the height of the NEB process snapshot.

Table S8. The convergence standard test of [Emim]+ on the Ti2CO2 via C-C′ path.

Table S9. The diffusion coefficient of [Emim]+ on Ti2CT2.

Table S10. Charge transfer between [Emim]+ cation and Ti2CT2 monolayer.

Computational Method.

In this work, Ab initio MD simulations were conducted via CP2K code (2025.2)1. The Perdew-Burke-Ernzerhof (PBE) generalized-gradient approximations for the exchange and correlation terms were used2-3, together with the Grimme’s-D3 dispersion correction, to provide a more accurate description of the structure. The Goedecker-Teter-Hutter (GTH) pseudopotentials were used to describe the core-valence interactions. All atomic species were represented using a double-zeta valence polarized (DZVP) basis set. The plane wave kinetic energy cut off was set to 400 Ry. The tolerance for the wave function optimization was set to 10−6 a.u. that allows for a 1 fs time steps with reasonable energy conservation. AIMD simulations were carried out in the NVT ensemble using a Nosé–Hoover chain thermostat to maintain the average temperature at 298.15 K. Periodic boundary conditions were applied throughout.

Figure S1. Test of the influence of K-point density on DOS

Figure S2. Test of the influence of smearing method on DOS

Figure S3. Test of the influence of smearing value on DOS

Figure S4. The (a) side and (b) top view of [Emim]+ structure; (c-d) The different side view of [Emim]+ on the Ti2CO2 surface.

Figure S5. The side view of (a) [Emim][Cl], (b)[Emim][BF4]; (c)[Emim][PF6] (d)[Emim][OAc] on the Ti2C(OH)2 surface.

Figure S6. (a-c) Energy profiles and (d-f) geometrical structures of Ti2CO2-[Emim][BF4], Ti2CF2-[Emim][BF4], and Ti2C(OH)2-[Emim][BF4] after an AIMD simulation, respectively.

(a) The diffusion path of Ti2CO2-[Emim]+ via C-C path

(b) The diffusion path of Ti2CO2-[Emim]+ via C-Ti1-C path

(c) The diffusion path of Ti2CO2-[Emim]+ via C-Ti2-C path

(d) The diffusion path of Ti2CF2-[Emim]+ via C-C path

(e) The diffusion path of Ti2CF2-[Emim]+ via C-Ti1-C path

(f) The diffusion path of Ti2CF2-[Emim]+ via C-Ti2-C path

Figure S7. (a-c) Three different migration paths of [Emim]+ on Ti2CO2; (d-f) Three different migration paths of [Emim]+ on Ti2CF2 Take the center of imidazolium ring as the migration center.

Figure S8. The schematic diagram defining the atomic numbers on the imidazolium ring, as well as the definition of atomic height (relative to the substrate plane)

Figure S9. Taking [Emim]+ on the Ti2CO2 via C-C′ path as example, the different convergence standard test was performed.

Figure S10. The energy profile of Ti2CT2-[Emim]+ via AIMD simulation.

Figure S11. The snapshots of (a) Ti2CF2-[Emim]+ and (b) Ti2CO2-[Emim]+via AIMD simulation.

Figure S12. The MSD curve of [Emim]+ on Ti2CT2 after AIMD simulation.

Figure S13. The different coverage (a) 0.08, (b) 0.12, (c) 0.16, (d) 0.20 ML of [Emim]+ on Ti2CO2 with the flat model.

Figure S14. The different coverage (a) 0.24, (b) 0.28, (c) 0.32, (d) 0.36 ML of [Emim]+ on Ti2CO2 with the stand model.

Figure S15. The 0.40 ML coverage of [Emim]+ on Ti2CO2 in the stand model, the local magnification diagram represents the crowded form of the molecular structure.

Table S1. The test for different dispersion correction choices.

| System | Dispersion correction choice | [Emim][BF4] (eV) | Ti2CO2 (eV) | Ti2CO2-[Emim][BF4] (eV) | Eads (eV) |
| --- | --- | --- | --- | --- | --- |
| Ti2CO2-[Emim][BF4] | DFT-D2 | −141.249 | −413.576 | −555.455 | −0.630 |
|  | DFT-D3 | −141.040 | −411.652 | −553.573 | −0.881 |
|  | DFT-D3(BJ) | −141.284 | −415.834 | −557.947 | −0.829 |

Table S2. Convergence tests using different K-point densities for different supercells, taking Ti2CO2 as example.

| Supercell | K-point density | Total Energy (eV) | CPU time (Sec) |
| --- | --- | --- | --- |
| 3×3 ×1 | 3×3 ×1 | −411.590 | 149.724 |
|  | 6×6 ×1 | −411.622 | 595.084 |
|  | 9×9 ×1 | −411.623 | 1185.677 |
| 5×5 ×1 | 2×2×1 | −1143.346 | 2317.362 |
|  | 4×4 ×1 | −1143.399 | 6124.747 |
|  | 6×6 ×1 | −1143.399 | 11899.952 |

Table S3. Convergence tests using different thickness of the vacuum layer crystal cells, taking Ti2CO2 as example.

| Supercell | Thickness of vacuum layer | Energy of slab (eV) | Total Energy (with [Emim]+) (eV) | [Emim]+ (eV) | Eads (eV) | CPU time (Sec) |
| --- | --- | --- | --- | --- | --- | --- |
| 3×3×1 | 15 Å | −411.590 | −524.172 | −106.146 | −6.437 | 1524.009 |
|  | 20 Å | −411.585 | −524.056 | −106.146 | −6.325 | 2425.481 |
|  | 25 Å | −411.585 | −524.047 | −106.146 | −6.316 | 2186.369 |

Table S4. Convergence test of the adsorption energies of [Emim]+ cations by supercells with different lateral dimensions, taking Ti2CO2 as example.

| Supercell | Energy of slab (eV) | Total Energy (with [Emim]+) (eV) | [Emim]+ (eV) | Eads (eV) | CPU time (Sec) |
| --- | --- | --- | --- | --- | --- |
| 3×3×1 | −411.590 | −524.172 | −106.146 | −6.437 | 1524.009 |
| 4×4×1 | −7731.666 | −844.202 | −106.146 | −6.260 | 6896.892 |
| 5×5×1 | −1143.346 | −1255.835 | −106.146 | −5.520 | 36892.563 |

Table S5. Comparison of adsorption energy and diffusion barrier of adsorbate on MXenes.

| Adsorbate | Slab | Method | Adsorption energies (eV) | Diffusion barrier (eV) | Intercalation free energy (eV) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| [Emim][Cl] | Ti2CO2 | DFT | −1.732 |  |  | This work |
| [Emim][BF4] | Ti2CO2 | DFT | −1.670 |  |  | This work |
| [Emim][PF6] | Ti2CO2 | DFT | −1.464 |  |  | This work |
| [Emim][OAc] | Ti2CO2 | DFT | −1.488 |  |  | This work |
| [Emim][Cl] | Ti2CF2 | DFT | −1.529 |  |  | This work |
| [Emim][BF4] | Ti2CF2 | DFT | −1.581 |  |  | This work |
| [Emim][PF6] | Ti2CF2 | DFT | −1.752 |  |  | This work |
| [Emim][OAc] | Ti2CF2 | DFT | −1.387 |  |  | This work |
| Emim+ | Ti2CO2 | DFT | −6.460 | 0.029 | −3.778 | This work |
| Emim+ | Ti2CF2 | DFT | −6.179 | 0.025 |  | This work |
| [AICl4]− | Graphene | DFT |  | 0.021 |  | Reference 4 |
| [Emim]+ | Bilayer Ti3C2(OH)2 | DFT |  |  | −14.5 (with solvent) | Reference 5 |
| [Emim] + | Bilayer Ti3C2(OH)2 | DFT |  |  | −16.0 (without solvent) | Reference 5 |
| [TFSI]− | Bilayer Ti3C2(OH)2 | DFT |  |  | 6.9 (with solvent) | Reference 5 |
| [TFSI]− | Bilayer Ti3C2(OH)2 | DFT |  |  | 5.8.(without solvent) | Reference 5 |
| [Emim]+ | Ti3C2F2 | DFT | −2.51 |  |  | Reference 6 |
| [Emim] + | Ti3C2O2 | DFT | −4.11 |  |  | Reference 6 |
| [Emim]+ | Ti3C2(OH)2 | DFT | −1.44 |  |  | Reference 6 |
| [BF4]− | Ti3C2(OH)2 | DFT | −7.36 |  |  | Reference 6 |
| [EMIM][BF₄] | Ti3C2F2 | DFT | –1.00 | — |  | Reference 6 |
| [EMIM][NTf₂] | Ti3C2F2 | DFT | –1.50 | — |  | Reference 6 |
| [EMIM][BF₄] | Ti3C2O2 | DFT | –1.18 | — |  | Reference 6 |
| [EMIM][NTf₂] | Ti3C2O2 | DFT | –1.60 | — |  | Reference 6 |
| Li+ | Ti₂CS₂ | DFT | −2.11 | 0.22 |  | Reference 7 |
| Na+ | Ti₂CS₂ | DFT | −2.05 | 0.11 |  | Reference 7 |
| K+ | Ti₂CS₂ | DFT | −2.60 | 0.06 |  | Reference 7 |
| Mg2+ | Ti₂CS₂ | DFT | −1.18 | 0.46 |  | Reference 7 |
| Ca2+ | Ti₂CS₂ | DFT | −2.03 | 0.33 |  | Reference 7 |
| Al3+ | Ti₂CS₂ | DFT | −2.08 | 0.47 |  | Reference 7 |
| Na+ | Ti3C2 | DFT | −4.40 | 0.096 |  | Reference 8 |
| NH3 | Ti3C2O2 | DFT | −0.420 |  |  | Reference 9 |
| NO | Ti3C2O2 | DFT | −0.348 |  |  | Reference 9 |
| SO3 | Ti3C2O2 | DFT | −0.340 |  |  | Reference 9 |
| SO2 | Ti3C2O2 | DFT | −0.285 |  |  | Reference 9 |
| H2S | Ti3C2O2 | DFT | −0.254 |  |  | Reference 9 |
| HOCO | Ti3C2O2 | DFT | −0.233 |  |  | Reference 9 |
| CH4 | Ti3C2O2 | DFT | −0.207 |  |  | Reference 9 |
| CO | Ti3C2O2 | DFT | −0.162 |  |  | Reference 9 |
| CO2 | Ti3C2O2 | DFT | −0.201 |  |  | Reference 9 |
| NO2 | Ti3C2O2 | DFT | −0.185 |  |  | Reference 9 |
| CO2 | V2CO2 | DFT | −0.18 |  |  | Reference 10 |
| CO2 | V2C(OH)2 | DFT | −3.01 |  |  | Reference 10 |

Table S6. Sensitivity test of the adsorption energies of Ti2CO2-[Emim]+ with or without background.

| Supercell | Energy of Ti2CO2 slab (eV) | [Emim]+ Adsorbate (eV) | Total Energy (with [Emim]+) (eV) | Eads (eV) |
| --- | --- | --- | --- | --- |
| Add background charge | −411.590 | −106.146 | −524.172 | −6.436 |
| Remove background charge | −411.590 | −109.078 | −524.437 | −3.769 |

Table S7. The variations in the height of the NEB process snapshot. Since the center of the imidazolium ring was taken as the center during the NEB process, the center height (Å) of the imidazolium ring center trace as the quantitative descriptor for the representative NEB path.

| System | NEB images | N1 | C2 | N3 | C4 | C5 | Ring-Center (d) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C-C' path of Ti2CO2-[Emim]+ | 0 | 2.972 | 2.984 | 2.966 | 2.938 | 2.939 | 2.960 |
|  | 1 | 2.970 | 2.984 | 2.968 | 2.940 | 2.940 | 2.960 |
|  | 2 | 2.968 | 2.985 | 2.972 | 2.941 | 2.940 | 2.961 |
|  | 3 | 2.968 | 2.985 | 2.974 | 2.942 | 2.940 | 2.962 |
|  | 4 | 2.971 | 2.986 | 2.973 | 2.942 | 2.941 | 2.963 |
|  | 5 | 2.975 | 2.987 | 2.972 | 2.942 | 2.943 | 2.964 |
|  | 6 | 2.977 | 2.988 | 2.971 | 2.943 | 2.945 | 2.965 |
|  | 7 | 2.945 | 2.990 | 2.972 | 2.944 | 2.945 | 2.959 |
| C-Ti1-C' path of Ti2CO2-[Emim]+ | 0 | 2.972 | 2.984 | 2.966 | 2.938 | 2.939 | 2.960 |
|  | 1 | 2.967 | 2.978 | 2.962 | 2.933 | 2.934 | 2.955 |
|  | 2 | 2.927 | 2.987 | 2.973 | 2.896 | 2.866 | 2.930 |
|  | 3 | 3.014 | 2.976 | 2.949 | 2.964 | 3.003 | 2.981 |
|  | 4 | 2.968 | 2.980 | 2.963 | 2.934 | 2.936 | 2.956 |
|  | 5 | 2.859 | 3.010 | 3.005 | 2.841 | 2.747 | 2.892 |
|  | 6 | 2.859 | 3.010 | 3.005 | 2.845 | 2.747 | 2.893 |
|  | 7 | 2.978 | 3.084 | 2.972 | 2.944 | 2.945 | 2.985 |
| C-Ti2-C' path of Ti2CO2-[Emim]+ | 0 | 2.972 | 2.984 | 2.966 | 2.938 | 2.939 | 2.960 |
|  | 1 | 2.980 | 2.993 | 2.962 | 2.923 | 2.932 | 2.958 |
|  | 2 | 3.007 | 3.026 | 2.948 | 2.868 | 2.904 | 2.951 |
|  | 3 | 3.017 | 3.035 | 2.941 | 2.849 | 2.896 | 2.948 |
|  | 4 | 3.040 | 3.053 | 2.925 | 2.816 | 2.886 | 2.944 |
|  | 5 | 2.861 | 3.012 | 3.007 | 2.844 | 2.750 | 2.895 |
|  | 6 | 2.904 | 2.994 | 2.995 | 2.897 | 2.837 | 2.925 |
|  | 7 | 2.978 | 3.084 | 2.972 | 2.944 | 2.945 | 2.985 |
| C-C' path of Ti2CO2-[Emim]+ | 0 | 2.837 | 2.851 | 2.885 | 2.890 | 2.858 | 2.864 |
|  | 1 | 2.829 | 2.845 | 2.882 | 2.886 | 2.853 | 2.859 |
|  | 2 | 2.821 | 2.840 | 2.879 | 2.881 | 2.846 | 2.853 |
|  | 3 | 2.815 | 2.834 | 2.874 | 2.875 | 2.839 | 2.847 |
|  | 4 | 2.812 | 2.828 | 2.866 | 2.868 | 2.833 | 2.841 |
|  | 5 | 2.808 | 2.822 | 2.857 | 2.862 | 2.829 | 2.836 |
|  | 6 | 2.803 | 2.816 | 2.850 | 2.856 | 2.824 | 2.830 |
|  | 7 | 2.794 | 2.883 | 2.842 | 2.847 | 2.816 | 2.836 |
| C-Ti1-C' path of Ti2CO2-[Emim]+ | 0 | 2.837 | 2.851 | 2.885 | 2.890 | 2.858 | 2.864 |
|  | 1 | 2.826 | 2.826 | 2.838 | 2.838 | 2.838 | 2.833 |
|  | 2 | 2.825 | 2.881 | 2.808 | 2.827 | 2.839 | 2.836 |
|  | 3 | 2.828 | 2.806 | 2.811 | 2.830 | 2.842 | 2.842 |
|  | 4 | 2.830 | 2.808 | 2.813 | 2.832 | 2.844 | 2.825 |
|  | 5 | 2.832 | 2.810 | 2.815 | 2.834 | 2.846 | 2.827 |
|  | 6 | 2.839 | 2.817 | 2.822 | 2.841 | 2.853 | 2.834 |
|  | 7 | 2.844 | 2.822 | 2.827 | 2.846 | 2.858 | 2.839 |
| C-Ti2-C' path of Ti2CO2-[Emim]+ | 0 | 2.837 | 2.851 | 2.885 | 2.890 | 2.858 | 2.864 |
|  | 1 | 2.835 | 2.848 | 2.881 | 2.884 | 2.856 | 2.861 |
|  | 2 | 2.836 | 2.844 | 2.871 | 2.874 | 2.852 | 2.855 |
|  | 3 | 2.839 | 2.834 | 2.855 | 2.865 | 2.854 | 2.849 |
|  | 4 | 2.841 | 2.824 | 2.841 | 2.863 | 2.861 | 2.846 |
|  | 5 | 2.840 | 2.818 | 2.823 | 2.842 | 2.854 | 2.835 |
|  | 6 | 2.842 | 2.819 | 2.824 | 2.844 | 2.856 | 2.837 |
|  | 7 | 2.843 | 2.821 | 2.826 | 2.845 | 2.857 | 2.838 |

Table S8. The convergence standard test of [Emim]+ on the Ti2CO2 via C-C′ path.

| System | Convergence criterion of energy (eV) | Convergence criterion of force (eV/A˚) | Ediff (eV) |
| --- | --- | --- | --- |
| [Emim]+ on Ti2CO2 via C-C′ path | 10−4 | −0.02 | −0.027 |
|  | 10−5 | −0.02 | −0.029 |
|  | 10−4 | −0.01 | -0.019 |
|  | 10−5 | −0.01 | −0.032 |

Table S9. The diffusion coefficient of [Emim]+ on Ti2CT2.

| System | D/nm2 ns−1 |
| --- | --- |
| Ti2CO2-[Emim]+ | 4.639 ± 0.031 |
| Ti2CF2-[Emim]+ | 1.736 ± 0.005 |

Table S10. Charge transfer between [Emim]+ cation and Ti2CT2 monolayer

| Systems | △Q-Cation | △Q-MXene |
| --- | --- | --- |
| Ti2C-[Emim]+ | 0.371 | -0.371 |
| Ti2CF2-[Emim]+ | 0.013 | -0.013 |
| Ti2CO2-[Emim]+ | 0.035 | -0.035 |
| Ti2C(OH)2-[Emim]+ | 1.037 | -1.037 |

△Q = Qafter -Qbefore; negative charge means [Emim]+ transfer charge to Ti2CT2; positive number means [Emim]+ get charge from Ti2CT2

Reference

(1).	Hutter, J.; Iannuzzi, M.; Schiffmann, F.; VandeVondele, J., Cp2k: Atomistic Simulations of Condensed Matter Systems. WIREs Computational Molecular Science 2014, 4, 15-25.

(2).	Albavera-Mata, A.; Botello-Mancilla, K.; Trickey, S. B.; Gázquez, J. L.; Vela, A., Generalized Gradient Approximations with Local Parameters. Physical Review B 2020, 102, 035129.

(3).	Becke, A. D., Density-Functional Exchange-Energy Approximation with Correct Asymptotic Behavior. Physical Review A 1988, 38, 3098-3100.

(4).	Agiorgousis, M. L.; Sun, Y.-Y.; Zhang, S., The Role of Ionic Liquid Electrolyte in an Aluminum–Graphite Electrochemical Cell. ACS Energy Letters 2017, 2, 689-693.

(5).	Valurouthu, G.; Panigrahi, R.; Saraf, M.; Shuck, C. E.; Mallik, B. S.; Kurra, N.; Gogotsi, Y., Ambipolar Electrochemistry of Pre-Intercalated Ti3c2tx MXene in Ionic Liquid Electrolyte. Batteries & Supercaps 2023, 6, e202300009.

(6).	Sampaio, A. M.; Silveira, J. F. R. V.; Dias, L. G.; Da Silva, J. L. F.; Siqueira, L. J. A., Adsorption of Ionic Liquids Forming Species on Ti3c2tx Mxenes Surfaces by First-Principle Calculations. FlatChem 2022, 35, 100413.

(7).	Wang, Y.; Zhou, M.; Xu, L.-C.; Zhao, W.; Li, R.; Yang, Z.; Liu, R.; Li, X., Achieving Superior High-Capacity Batteries with the Lightest Ti2c MXene Anode by First-Principles Calculations: Overarching Role of S-Functionate (Ti 2cs2) and Multivalent Cations Carrier. Journal of Power Sources 2020, 451, 227791.

(8).	Su, D.; Zhang, H.; Zhang, J.; Zhao, Y., Design and Synthesis Strategy of Mxenes-Based Anode Materials for Sodium-Ion Batteries and Progress of First-Principles Research. Molecules 2023, 28, 6292.

(9).	Weng, K.; Peng, J.; Shi, Z.; Arramel, A.; Li, N., Highly Nh3 Sensitive and Selective Ti3c2o2-Based Gas Sensors: A Density Functional Theory-Negf Study. ACS Omega 2023, 8, 4261-4269.

(10).	Kajal, A.; Kumar, K.; Kharb, A. S.; Mishra, A. K., Surface Chemistry–Driven Co2 Activation and Conversion on V2c Mxenes. Scientific Reports 2025, 15, 38384.