Supporting information for

Insights into phonons and spin-lattice relaxation in copper(II) and vanadyl(II) porphyrin metal-organic frameworks from density functional theory

Yukina Suzuki1*, Nina Strasser2, Ryota Sakamoto1, Masahiro Yamashita3,1,4*

1Department of Chemistry, Graduate School of Science, Tohoku University, 6-3 Aramaki-Aza-Aoba, Aoba-Ku, Sendai 980-8578, Japan

2 Institute of Solid State Physics, NAWI Graz, Graz University of Technology, Petersgasse 16, 8010 Graz, Austria

3School of Chemical Science and Engineering, Tongji University, Siping Road 1239, Shanghai 200092, P. R. China

4Institute of Materials Research, Tohoku University, 2-1-1 Katahira, Aoba-Ku, Sendai 980-8577, Japan

E-mail: suzuki.yukina.s2@dc.tohoku.ac.jp , masahiro.yamashita.c5@tohoku.ac.jp

Table of Contents

Spin-lattice relaxation of (1)-(4) diluted in a diamagnetic matrix	3

CW-EPR spectra and EPR parameters	4

Material and synthesis	5

Synthesis of 1	5

Synthesis of 2	5

Synthesis of 3	5

Synthesis of 4	5

Powder X-ray diffraction of the samples used for Raman spectroscopy	6

Computational methods	8

Structure optimization	8

Convergence test	9

Two limiting cases of the disordered VO(TPP) crystal	10

Spin-phonon coupling calculations	11

Raman spectroscopy	13

Lattice constants of optimized structures	15

DFT basis set dependence of vibrational calculations (eigenvectors)	16

First-order SPC dependence on the DFT basis set for phonon calculations	18

SPC calculations functional, basis set dependence	20

Spin-phonon coupling calculations	23

Distributions of Spin-phonon coupling coefficients	31

SPC coefficients scaled by the Bose–Einstein distribution for (1)	32

SPC coefficients scaled by the Bose–Einstein distribution for (2)	34

SPC coefficients scaled by the Bose–Einstein distribution for (3)	35

SPC coefficients scaled by the Bose–Einstein distribution for (4)	37

Frequency shifts between the molecular crystals and MOFs	39

Correlation with the symmetry of vibrational modes and spin-phonon coupling	40

Correlation with normal-coordinate structural decomposition (NSD) analysis	43

Correlation of SPC coefficients and out-of-plane and in-plane distortion	44

Correlation of SPC coefficients and each out-of-plane distortion mode for (1)	46

Correlation of SPC coefficients and each out-of-plane distortion mode for (2)	47

Correlation of first-order SPC coefficients and each out-of-plane distortion mode for (3)	48

Correlation of first-order SPC coefficients and each out-of-plane distortion mode for (4)	49

Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (1)	50

Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (2)	51

Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (3)	52

Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (4)	53

## Spin-lattice relaxation of (1)-(4) diluted in a diamagnetic matrix

Spin-lattice relaxation times (T1) for [{Cu(TCPP)}Zn2(H2O)2] (1) diluted in [{Zn(TCPP)}Zn2(H2O)2] (1%), [{VO(TCPP)}Zn2(H2O)2] (2) diluted in [(TCPP)}Zn2(H2O)2] (1%)1, CuTPP (TPP = tetraphenylporphyrin) (3) diluted in NiTPP (1%), and VOTPP (4) diluted in TiOTPP (2%)2 were measured at X-band in the previous studies. For (1), previous studies diluted the Cu(II) MOF into a non-isostructural Zn(TCPP) MOF matrix, generating a mixture of two different Cu(II) and Zn(II) phases3. This creates a discrepancy between the structure used in our simulations (the crystal structure of pristine [{Cu(TCPP)}Zn2(H2O)2] and the actual lattice structure. Therefore, we diluted the copper(II) MOF in an isostructural diamagnetic Ni(TCPP) MOF matrix [{Ni(TCPP)}Zn2(H2O)2]. T1 of (1) diluted in the isostructural Ni matrix (7% and 1%) was measured at Q-band. Similar to the previous study, the MOF showed slower T1 compared to CuTPP.

Figure S1. Spin-lattice relaxation times of copper(II) and vanadyl(IV) porphyrins. Color coding for the left panel: light blue: 1% (1) diluted in [{Zn(TCPP)}Zn2(H2O)2] (X-band; 335 mT)3; pink: 7% (1) diluted in [{Ni(TCPP)}Zn2(H2O)2] (measured in this study at Q-band; 1173 mT; 33.74 GHz); orange: 4% (1) diluted in [{Ni(TCPP)}Zn2(H2O)2] (this study at Q-band; 1176 mT; 33.74 GHz); blue: 1% (3) in NiTPP4. Color coding for the right panel: red: 1% (2) in [(TCPP)Zn2(H2O)2]1; light pink: 1% (4) in TiOTPP2.

## CW-EPR spectra and EPR parameters

Previous studies have shown that the EPR parameters of metalloporphyrins in MOFs barely change from those of the corresponding molecular crystals1–3. This indicates that their electronic structures remain comparable to those of the corresponding molecular species. Therefore, the change in the electronic structures cannot explain the markedly different spin-lattice relaxation behaviors. CW-EPR spectra of MOF (1) and (2) diluted in the diamagnetic Ni matrix were also measured and fitted in this study, as shown in Table S1-2 and Figure S2. They showed values similar to those reported in the previous studies, where (2) was diluted in a non-metalated TCPP MOF matrix1.

Table S1. EPR parameters of similar Cu(II) porphyrins

|  | g∥ | g⊥ | ACu,∥ /MHz | ACu,⊥ /MHz | AN,∥ /MHz | AN,⊥ /MHz | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (1) | 2.192 | 2.0476 | 621 | 54.3 | 43.4 | 50.2 |  |
| (3) | 2.176 | 2.043 | 625 | 86 | 46 | 51 | 4 |
| CuOEP | 2.195 | 2.047 | 606 | 79 | 44 | 50 | 4 |

Table S2. EPR parameters of similar VO(IV) porphyrins

|  | g∥ | g⊥ | AV,∥ /MHz | AV,⊥ /MHz | Ref |
| --- | --- | --- | --- | --- | --- |
| (2) diluted in NiTCPP | 1.983 | 1.962 | 167.7 | 473.7 |  |
| (2) diluted in TCPP | 1.99 | 1.969 | 172 | 475 | 1 |
| (4) | 1.9865 | 1.963 | 168 | 477 | 2 |
| [VO(TCPP-Zn2-bpy)] MOF | 1.9865 | 1.963 | 169 | 480 | 2 |

Figure S2. Left: Experimental (red) and simulated (blue) CW-EPR spectra of 7% [{Cu(TCPP)}Zn2(H2O)2] (1) diluted in the Ni matrix. Right: Experimental (red) and simulated (blue) cw-EPR spectra of 4% [{VO(TCPP)}Zn2(H2O)2] (2) diluted in the Ni matrix.

## Material and synthesis

All chemicals were used as received without further purification, unless otherwise noted. Vanadyl acetylacetonate (VO(acac)2) was purchased from Sigma-Aldrich. Methanol (MeOH), phenol, zinc nitrate hexahydrate (Zn(NO3)2·6H2O), and N, N-dimethylformamide (DMF) were obtained from Wako Pure Chemical Industries, Ltd. 5,10,15,20-Tetraphenylporphyrin (H2TPP), Copper(II) 5,10,15,20-tetra(4-carboxyphenyl)porphyrin (CuTCPP) and vanadyl 5,10,15,20-tetra(4-carboxyphenyl)porphyrin (VOTCPP) were synthesized according to previously reported procedures5. The crystallinity and phase purity of the synthesized materials were confirmed by powder X-ray diffraction (PXRD) (Figure S3-Figure S4).

### Synthesis of 1

The synthesis was conducted following the previous procedure3. A glass vial was charged with CuTCPP (95 mg), Zn(NO3)2·6H2O (119 mg), and 50 mL DMF. The sealed vial was heated at 120 °C for 48 h. After cooling the solution, the crystalline solids were filtered and washed with dimethylformamide (DMF) and acetone. The solids were then dried under vacuum.

### Synthesis of 2

The synthesis was conducted following the previous procedure1. A glass vial was charged with VOTCPP (18.1 mg, 21 µmol), Zn(NO3)2•6H2O (24.3 mg, 82 µmol), and 10 mL DMF. The sealed vial was heated at 120 °C for 48 h. After cooling the solution, the crystalline solids were filtered and washed with dimethylformamide (DMF) and acetone. The solids were then dried under vacuum.

### Synthesis of 3

CuTPP powder was purchased from either Sigma Aldrich or Tokyo Chemical Industry (TCI). The as-received power contained a mixture of different phases of CuTPP. To prepare the pure CuTPP phase for pulse EPR measurements, the CuTPP powder was dissolved in DCM, and the solvent was slowly evaporated by rotary evaporation.

### Synthesis of 4

The synthesis was conducted following a previously described procedure2,5. 440 mg H2TPP and 190 mg VO(acac)2 were refluxed in 10 mL phenol overnight. While hot, 30 mL of MeOH was slowly added to the phenol solution. The solution was left still for a while until the crystals precipitated. The crystals were collected by filtration and washed with MeOH. The crystallinity and phase purity were confirmed using powder X-ray diffraction.

## Powder X-ray diffraction of the samples used for Raman spectroscopy

Powder X-ray diffraction (PXRD) measurements were performed to confirm the structural integrity and phase purity of the synthesized MOFs. As previously reported for (1) and (2)1,3, the experimental diffraction patterns have different diffraction peak intensities from those calculated from the single-crystal structure. This was attributed to the preferred orientation effects of the crystallites in the previous study3. The agreement between the experimental patterns and simulated data, particularly when accounting for preferential orientation along the (010) direction, confirms the successful synthesis of the target MOF structures. Slight deviations in the peak positions between the as-synthesized and dried samples reflect slight changes in the lattice constants due to the evacuation of the solvent, consistent with the previous study1,3.

Figure S3. PXRD patterns of (1) and (2) used for Raman spectroscopy. Comparison of simulated and experimental PXRD patterns: (a) simulated pattern with no preferred orientation, (b) simulated pattern with preferred orientation along the (010) direction, (c) experimental pattern of the dried (2), (d) experimental pattern of dried (1), (e) experimental pattern of as-synthesized (2), and (f) experimental pattern of as-synthesized (1).

Figure S4. The experimental (blue) and simulated (light blue) PXRD patterns of (3) were used for Raman spectroscopy.

Figure S5. The experimental (blue) and simulated (light blue) PXRD patterns of (4) samples used for Raman spectroscopy.

## Computational methods

### Structure optimization

Geometry optimizations in CRYSTAL23 employed the default convergence thresholds applied when subsequent frequency calculations are intended; the RMS of the gradient was set to (TOLDEG) 0.00003 a.u., the RMS of the displacement (TOLDEX) was set to 0.00012 a.u., and the energy difference between two steps (TOLDEE) was set to the default value of 10-7 a.u. TOLINTEG, which defines the thresholds for screening Coulomb and exchange integrals, was set to 8 8 8 8 16 for all systems in the PBE-D3/VTZP calculations. For the VASP calculations, the convergence criterion for the self-consistent field (SCF) calculation (EDIFF) was set to 1E-08 eV, and the convergence criterion for geometry optimization (EDIFFG) was set to -0.001 eV.

Other parameters for calculations (the shrinking factor for CRYSTAL23, and ENCUT and KPOINTS for VASP) are tabulated in Table S3 and Table S4, which were determined based on the convergence test performed prior to the geometry optimization, as exemplified for 4 in Figure S6-Figure S7. Convergence is assumed to be achieved when the change in total energy is less than 1 meV/atom from one setting to the next. These settings were also used in the subsequent phonon calculations.

Table S3. Parameters used for each system with PBE-D3/VTZP in CRYSTAL23 calculations

|  | shrink |
| --- | --- |
| 1 | 2 2 |
| 2 | 2 2 |
| 3 | 2 2 |
| 4 | 3 3 |

Table S4. Parameters used for each system with PBE-D3 or PBEsol-D3 functionals in VASP calculations

|  | KPOINTS | ENCUT /eV |
| --- | --- | --- |
| 1 | 2 1 1 | 850 |
| 2 | 2 1 1 | 850 |
| 3 | 2 2 2 | 850 |
| 4 | 2 2 2 | 850 |

### Convergence test

Figure S6. Energy difference relative to the largest setting used (shrinking factor [5 5]) as a function of the shrinking factor for (4). Calculations were performed using the PBEsol03c/def2-mSVP in CRYSTAL23.

Figure S7. Energy difference relative to the largest setting used (ENCUT = 900 eV or K grid = 5×5×5) as a function of the plane wave energy cutoff and the k-grid for (4). Calculations were performed using the PBEsol functional with the DFT-D3 method with Becke-Johnson damping in VASP.

### Two limiting cases of the disordered VO(TPP) crystal

When all the VO groups point in the same direction, the mirror plane between the two up and down VO groups is lost. With the loss of the mirror plane, the inversion center is also lost. This results in the I4 space group. When the V=O groups are placed alternately up and down, the mirror plane between the two up and down VO groups is lost, similar to the I4 case. Additionally, the (0, 0, 0) and (1/2, 1/2, 1/2) VO(TPP) units are no longer related by a simple body-centered translation, reducing the symmetry from I to P. However, these VO(TPP) units remain related by a glide plane, and the inversion center is preserved, resulting in the P4/n space group.

Figure S8. Unit cell of the two limiting cases of disordered V=O orientations (left – I4, right – P4/n).

### Spin-phonon coupling calculations

The contribution of each Γ-point optical phonon mode to the spin-lattice relaxation can be quantified using the following equation6:

1T1∝i=13N-3∂g∂Q2expEikBTexpEikBT-12 #1

where N is the number of atoms in the primitive unit cell, g is the g-factor, Q is the normal coordinate which describes the vibrational mode, Ei is the energy of the i-th optical phonon mode, kB is the Boltzmann constant, and T is the temperature.

The term ∂g∂Q is typically called the first-order spin-phonon coupling coefficient6, and it quantifies how much a specific vibrational mode perturbs the electronic structure and contributes to spin-lattice relaxation. This term is crucial because it indicates the magnitude of the spin-phonon interaction for each vibrational/phonon mode. The exponential factor accounts for the thermal distribution of phonons, following the Bose-Einstein distribution. It governs the population of phonons at a given temperature. Higher temperatures result in the excitation of higher-energy phonon modes. The summation runs over all optical phonon modes of the system. Since our focus is to study the contribution of optical phonons at higher temperatures, the translational modes (acoustic phonons at the Γ-point) were excluded from this study.

Spin-phonon coupling calculations (the calculation of the ∂g∂Q term) were carried out based on the reported methods4,6–12. This method involves numerical calculations of the spin-phonon coupling coefficient ∂g∂Q. First, g-factors are calculated as a function of the normal coordinate Q. Then, by fitting the g-factors using a combination of linear and quadratic functions (f(Q) = aQ2+ bQ+c), the first-order spin-phonon coupling coefficients ∂g∂Q are obtained from the coefficient b. In the same manner, the second-order non-cross terms ∂2g∂Q2 were evaluated from the coefficient a. The contribution of the second-order non-cross terms were also evaluated from eq. 1 by replacing ∂g∂Q with ∂2g∂Q2.

A schematic procedure of spin-phonon coupling calculation is depicted in Figure S9. The displaced geometries in the optimized crystal structure required for this calculation were prepared using the SCANMODE module in CRYSTAL23. For the spin-phonon coupling calculations based on the VASP-computed phonon modes, the displaced geometries were prepared using the eigenvectors computed in the phonon calculations using Phonopy. The magnitude of displacement Q was scanned from -0.15 to 0.15 with a step size of 0.05 (Q = ±0.15, ±0.10, and ±0.05). Although the summation over all vibrational/phonon modes contributes to T1, a previous study showed that modes above 400 cm-1 barely contribute to T1 due to the small thermal population of these modes6. Therefore, only the spin-phonon coupling coefficients of phonon modes up to 400 cm-1 were evaluated in this study.

The g-factor calculations were performed on the molecular unit in the gas phase using ORCA 6.0.0. Because the g-factor calculations in ORCA are performed without periodic conditions, the molecular unit was cut out from the distorted crystal structures along each vibrational normal coordinate for further g-factor calculations.

Figure S9. Schematic procedure for spin-phonon coupling calculations.

## Raman spectroscopy

For (2), the absence of symmetry (P1) made the simulation of the Raman spectra prohibitively expensive with a large basis set. Therefore, the Raman spectrum was simulated using a basis set of double zeta quality(sol-def2-mSVP), as shown in Figure S10. Based on the simulations of the Raman spectra for other species, the Raman spectral shape obtained with sol-def2-mSVP is expected to be in good agreement with the simulations using larger basis sets.

Since relaxing the crystal cell reduces the original monoclinic cell determined by the previous report1 to a triclinic cell, optimization with the fixed cell was also carried out with the same method. The spectral shapes do not differ significantly between the cases in which both the atomic positions and cells were relaxed and only the atomic positions were relaxed.

Although the simulated Raman spectra were not simulated with a larger basis set, the Γ-point phonon modes and their frequencies, which are required for the spin-phonon coupling calculations, were computed with the VTZP basis set or ENCUT = 850 eV. Because an accurate simulation of phonon modes requires a large basis set, the spin-phonon coupling calculations were conducted based on these higher-level phonon calculations; therefore, the lack of Raman simulations with a large basis set does not affect the quality of our spin-phonon coupling calculations.

Figure S10. Comparison of the simulated and experimental Raman spectra for (2). The Raman spectra were simulated using PBEsol0-3c/sol-def2-mSVP.

Figure S11. Comparisons of the simulated Raman spectra with the experimental Raman spectra for (3) with different functionals and basis sets (PBEsol-D3 in VASP, PBE-D3/VTZP, PBE-D3/6-31G**, and PBEsol0-3c/sol-def2-mSVP from the top).

Figure S12. Comparisons of the simulated Raman spectra with the experimental Raman spectra for (4) with different functionals and basis sets (PBEsol-D3 in VASP, PBE-D3/VTZP, and PBEsol0-3c/sol-def2-mSVP from the top).

## Lattice constants of optimized structures

Table S5. Lattice constants of the optimized geometries for (1)

|  | a /Å | b /Å | c /Å | β /° |
| --- | --- | --- | --- | --- |
| Exp (HICXOJ)3 | 6.655 | 16.689 | 12.629 | 100.66 |
| PBEsol-D3 (VASP) | 6.493 | 16.735 | 12.352 | 98.557 |
| PBE-D3 (VASP) | 6.583 | 16.845 | 12.571 | 99.521 |
| PBEsol0-3c/sol-def2-mSVP | 6.676 | 16.735 | 12.619 | 101.216 |
| PBE-D3/6-31G** | 6.481 | 16.839 | 12.375 | 98.523 |
| PBE-D3/VTZP | 6.551 | 16.936 | 12.405 | 99.315 |

Table S6. Lattice constants of the optimized geometries for (3)

|  | a /Å | b /Å |
| --- | --- | --- |
| Exp (CUTPOR)13 | 15.03 | 13.99 |
| PBEsol-D3 (VASP) | 14.894 | 13.026 |
| PBE-D3 (VASP) | 15.0269 | 13.455 |
| PBEsol0-3c/sol-def2-mSVP | 14.867 | 13.823 |
| PBE-D3/6-31G** | 15.007 | 12.953 |
| PBE-D3/VTZP | 15.058 | 13.283 |
| PBE-D3/POV-TZVP | 14.781 | 12.149 |

Table S7. Lattice constants of the optimized geometries for (4)

|  | a /Å | c /Å |
| --- | --- | --- |
| Exp (CIPLIW)14 | 13.345 | 9.745 |
| PBEsol-D3 (VASP) | 13.405 | 9.361 |
| PBE-D3 (VASP) | 13.277 | 9.686 |
| PBEsol0-3c/sol-def2-mSVP | 13.318 | 9.621 |
| PBE-D3/6-31G** | 13.154 | 9.489 |
| PBE-D3/VTZP | 13.247 | 9.649 |
| PBE-D3/POV-TZVP | 13.338 | 8.321 |

## DFT basis set dependence of vibrational calculations (eigenvectors)

As shown, the simulated Raman spectral shapes with different functionals or basis sets reproduce the experimentally obtained Raman spectra features relatively well, regardless of the simulation method. However, a closer examination of the computed phonon modes revealed that a basis set of double-ζ-quality was insufficient to obtain consistent phonon modes across different functionals/basis sets. This is manifested in the poor overlap of the eigenvectors of the computed phonons, particularly the low-frequency modes.

Figure S13 shows the eigenvector overlaps (dot product) from the two simulations with different functionals/basis sets. In the color map, the modes with high similarity (dot product close to 1) are shown in red, and those with poor similarity are shown in blue. When the two calculations are consistent, a clear red diagonal line appears, as shown in (Figure S13a), indicating good convergence. When basis sets of double zeta quality are used, light blue dots are scattered around the low-frequency modes (Figure S13b, c, and d), indicating that they are not sufficient for an accurate phonon mode description. Using a triple zeta basis set, particularly the VTZP basis set, resulted in better agreement with the well-converged VASP simulation results (Figure S13f).

Discrepancies in phonon mode descriptions lead to inconsistencies in the spin–phonon coupling (SPC) coefficients and the relative contributions of individual modes to spin–lattice relaxation. For simulations performed with smaller basis sets (sol-def2-mSVP, 6-31G**, and POB-TZVP), several modes contributed to spin-lattice relaxation, with a very low-frequency mode being the primary but not the exclusive contributor (Figure S14). By contrast, calculations with larger basis sets (VTZP or ENCUT = 850 eV) yielded relaxation dominated almost entirely by a single low-frequency mode (Figure S15).

Figure S13. Comparisons of the eigenvectors for (4) calculated with a) PBEsol-D3 (VASP) and PBE-D3 (VASP), b) PBEsol-3c/sol-def2-mSVP (CRYSTAL) and PBE-D3 (VASP), c) PBEsol-3c/sol-def2-mSVP (CRYSTAL) and PBE-D3/6-31G** (CRYSTAL) d) PBE-D3/6-31G** (CRYSTAL) and PBE-D3 (VASP), e) PBE-D3/POB-TZVP (CRYSTAL) and PBE-D3 (VASP) f) PBE-D3/VTZP and PBEsol-D3 (VASP)

## First-order SPC dependence on the DFT basis set for phonon calculations

Figure S14. The dependence of temperature-scaled spin-phonon coupling on DFT methods to compute the phonon modes (PBE-D3/6-31G** (CRYSTAL), PBE-D3/POB-TZVP (CRYSTAL), PBEsol0-3c/sol-def2-mSVP (CRYSTAL) from the top)

Figure S15. The dependence of temperature-scaled spin-phonon coupling on DFT methods to compute the phonon modes (PBE-D3/VTZP (CRYSTAL), PBE-D3 (VAPS), PBEsol-D3 (VASP) from the top)

## SPC calculations functional, basis set dependence

The dependence of the g-factor variation on the computational settings was examined by changing the functional (PBE0, B3LYP), basis set, and relativistic correction scheme (DKH, ZORA). The resulting trends of the g-factor change as a function of Q were found to be largely independent of these choices (Figure S16-Figure S18).

Figure S16. Dependence of g-factor (gx) changes on DFT methods for (3) calculated by a) PBE0/DKH-def2-TZVP (Cu), def2-SVP(others), b) PBE0/ZORA-def2-TZVP (Cu), ZORA-def2-SVP(others), c) B3LYP/ZORA-def2-TZVP (Cu), def2-SVP(others) d) PBE0/ZORA-def2-TZVP (Cu, N), ZORA-def2-SVP(others)

Figure S17. Dependence of g-factor (gy) changes on DFT methods for (3) calculated by a) PBE0/DKH-def2-TZVP (Cu), def2-SVP(others), b) PBE0/ZORA-def2-TZVP (Cu), ZORA-def2-SVP(others), c) B3LYP/ZORA-def2-TZVP (Cu), ZORA-def2-SVP(others) d) PBE0/ZORA-def2-TZVP (Cu, N), ZORA-def2-SVP(others)

Figure S18. Dependence of g-factor (gz) changes on DFT methods for (3) calculated by a) PBE0/DKH-def2-TZVP (Cu), def2-SVP(others), b) PBE0/ZORA-def2-TZVP (Cu), def2-SVP(others), c) B3LYP/ZORA-def2-TZVP (Cu), def2-SVP(others) d) PBE0/ZORA-def2-TZVP (Cu, N), def2-SVP(others)

## Spin-phonon coupling calculations

Figure S19. Calculated g tensor orientations in the molecular unit of a) CuMOF (1), b) VOMOF (2), c) CuTPP (3), and d) VOTPP (4)

Table S8. Calculated g-factors by ORCA at PBE0/def2-TZVP (M, N), def2-SVP(others) and experimental values

|  | Optimized by | Theory |  |  | Exp |  |  | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | gx | gy | gz | gx | gy | gz |  |
| (1) (CuTCPP4-) | PBE-D3/VTZP | 2.049 | 2.049 | 2.152 | 2.048 | 2.048 | 2.192 |  |
|  | VASP | 2.047 | 2.047 | 2.145 |  |  |  |  |
| (2) (VOTCPP4-) | VASP PBE-D3 | 1.985 | 1.985 | 1.972 | 1.987 | 1.987 | 1.965 |  |
| (3) | PBE-D3/VTZP | 2.047 | 2.047 | 2.146 | 2.043 | 2.043 | 2.176 | 4 |
|  | VASP PBE-D3 | 2.046 | 2.046 | 2.145 |  |  |  |  |
| (4) | PBE-D3/VTZP | 1.986 | 1.986 | 1.971 | 1.981 | 1.987 | 1.961 | 15 |
|  | VASP | 1.985 | 1.985 | 1.971 |  |  |  |  |

Figure S20. g-factor changes as a function of the normal coordinate for each vibrational mode of (1) at PBE0/def2-VTZP (Cu, N) and def2-SVP (others). The vibrational modes were calculated at the PBE-D3/VTZP level using CRYSTAL23.

Figure S21. g-factors change as a function of the normal coordinate for each vibrational mode of (1) at PBE0/def2-VTZP (Cu,N) and def2-SVP (others). The vibrational modes were calculated using the PBE-D3 functional in VASP.

Figure S22. g-factor changes as a function of the normal coordinate for each vibrational mode for (2) at PBE0/def2-VTZP (V,N) and def2-SVP (others). The vibrational modes were calculated using the PBE-D3 functional in VASP.

Figure S23. g-factor changes as a function of the normal coordinate for each vibrational mode for (3) at PBE0/def2-VTZP (Cu,N), def2-SVP (others). The vibrational modes were calculated at the PBE-D3/VTZP level using CRYSTAL23.

Figure S24. g-factor changes as a function of the normal coordinate for each vibrational mode for (3) at PBE0/def2-VTZP (Cu,N), def2-SVP (others). The vibrational modes were calculated using the PBE-D3 functional in VASP.

Figure S25. g-factor changes as a function of the dimensionless normal coordinate for each vibrational mode of (4) at PBE0/def2-VTZP (V,N), def2-SVP (others). The vibrational modes were calculated at the PBE-D3/VTZP level using CRYSTAL23.

Figure S26. g-factor changes as a function of the dimensionless normal coordinate for each vibrational mode of (4) at PBE0/def2-VTZP (V,N), def2-SVP (others). The vibrational modes were calculated using the PBE-D3 functional in VASP.

### Distributions of Spin-phonon coupling coefficients

Figure S27. First-order SPC coefficients for a) (2) and b) (4). Vibrational modes were computed using VASP with the PBE-D3 functional.

Figure S28. Second-order SPC coefficients for a) (2) and b) (4). Vibrational modes were computed using VASP with the PBE-D3 functional.

### SPC coefficients scaled by the Bose–Einstein distribution for (1)

Figure S29. Temperature-scaled first- and second-order spin–phonon coupling coefficients for (1). The black line represents the total contribution from all vibrational modes, while the colored lines show the individual contributions of each mode. Vibrational modes were computed using a) CRYSTAL at the PBE-D3/VTZP level, and b) VASP with the PBE-D3 functional.

The table below summarizes the correspondence between phonon modes denoted in Figure S29 across the two computational methods (PBE-D3/VTZP in CRYSTAL and PBE-D3 in VASP). For each mode, the dot product between the eigenvectors obtained using the two methods is also listed, providing a quantitative measure of their similarity. Minor discrepancies in the contributions of each phonon mode depending on the method arise from variations in the phonon eigenvectors, as reflected in the dot products and differences in the phonon frequencies. Modes with lower computed frequencies contribute more strongly to overall relaxation owing to the temperature factor. The agreement may improve if the basis set quality size is improved further from VTZP. However, increasing the size of atom-centered Gaussian basis sets in periodic systems causes linear dependence. Although some variations exist between the results obtained using phonon modes simulated with PBE-D3/VTZP and those obtained using PBE-D3 with plane-wave basis sets, the same modes consistently emerge as dominant at the qualitative level.

Table 9. Corresponding modes appearing in Figure S29 in each calculation (PBE-D3/VTZP in CRYSTAL  and PBE-D3 in VASP) and their dop products.

| CRYSTAL PBE-D3/VTZP | VASP PBE-D3 | Eigenvector dot product |
| --- | --- | --- |
| 4 | 4 | 0.90 |
| 6 | 6 | 0.86 |
| 7 | 7 | 0.90 |
| 8 | 8 | 0.77 |
| 39 | 39 | 0.61 |
| 43 | 42 | 0.62 |
| 49 | 50 | 0.72 |
| 50 | 48 | 0.62 |
| 67 | 67 | 0.90 |

### SPC coefficients scaled by the Bose–Einstein distribution for (2)

Figure S30. Temperature-scaled first- and second-order spin–phonon coupling coefficients for (2). The black line represents the total contribution from all vibrational modes, while the colored lines show the individual contributions of each mode. Vibrational modes were computed using VASP with the PBE-D3 functional. PBE-D3/VTZP resulted in imaginary frequencies, and further spin-phonon coupling calculations were not conducted.

### SPC coefficients scaled by the Bose–Einstein distribution for (3)

Figure S31. Temperature-scaled first- and second-order spin-phonon coupling coefficients for (3). The black line represents the total contribution from all vibrational modes, while the colored lines show the individual contributions of each mode. Vibrational modes were computed using a) CRYSTAL at the PBE-D3/VTZP level, and b) VASP with the PBE-D3 functional.

Table 10. Corresponding modes appearing in Figure S31in each calculation (PBE-D3/VTZP in CRYSTAL  and PBE-D3 in VASP) and their dot products.

| CRYSTAL PBE-D3/VTZP | VASP PBE-D3 | Eigenvector dot product |
| --- | --- | --- |
| 4 | 4 | 0.66 |
| 6 | 7 | 0.83 |
| 7 | 8 | 0.66 |
| 20 | 22 | 0.59 |
| 22 | 20 | 0.83 |
| 35 | 35 | 0.76 |
| 37 | 38 | 0.85 |
| 40 | 40 | 0.75 |
| 58 | 55 | 0.90 |
| 59 | 56 | 0.92 |
| 87 | 87 | 0.87 |
| 88 | 88 | 0.84 |

### SPC coefficients scaled by the Bose–Einstein distribution for (4)

Figure S32. Temperature-scaled first- and second-order spin-phonon coupling coefficients for (4). The black line represents the total contribution from all vibrational modes, while the colored lines show the individual contributions of each mode. Vibrational modes were computed using a) CRYSTAL at the PBE-D3/VTZP level, and b) VASP at the PBE-D3 functional.

Table 11. Corresponding modes appearing in Figure S32 in each calculation (PBE-D3/VTZP in CRYSTAL  and PBE-D3 in VASP) and their dop products.

| CRYSTAL PBE-D3/VTZP | VASP PBE-D3 | Eigenvector dot product |
| --- | --- | --- |
| 4 | 4 | 0.84 |
| 5 | 5 | 0.83 |
| 7 | 7 | 0.85 |
| 22 | 22 | 0.90 |

### Frequency shifts between the molecular crystals and MOFs

Figure S33. Shift of the low-frequency mode in Raman spectroscopy (>~10cm-1) for (1)-(4)

Figure S34. Γ-point phonon modes computed with PBE-D3/VTZP in CRYSTAL23 for a) (1) and b) (3), the PBEsol-D3 functional in VASP for c) (1) and d) (3), and the PBE-D3 functional in VASP for e) (1) and f) (3)

Figure S35. Γ-point phonon modes computed with the PBE-D3 functional in VASP for a) 2 and b) 4

### Correlation with the symmetry of vibrational modes and spin-phonon coupling

Figure S36. Distributions of first- and second-order spin–phonon coupling coefficients for (1), categorized by the irreducible representation of the vibrational modes. Vibrational modes were computed using VASP at the PBE-D3 functional.

Figure S37. Distributions of the first- and second-order spin–phonon coupling coefficients for (3), categorized by the irreducible representation of the vibrational modes. Vibrational modes were computed using VASP at the PBE-D3 functional.

Figure S38. Distributions of the first- and second-order spin–phonon coupling coefficients for (4), categorized by the irreducible representation of the vibrational modes. Vibrational modes were computed using VASP at the PBE-D3 functional.

### Correlation with normal-coordinate structural decomposition (NSD) analysis

Figure S39. Distortion modes used for out-of-plane structural decomposition of the porphyrin unit

Figure S40. Distribution of average V–N distance changes of phonon modes in a) VOMOF (2) b) VOTPP (4) and out-of-plane distortion (ΔDoop) of phonon modes in c) (2) d) (4)

Table S12. Average and median of ΔM-N (M = Cu/V) and |ΔDoop| for (1)-(4)

|  | Average of average ΔCu/V-N (Å) | Median of average ΔCu/V-N (Å) | Average of ¦ ¦ΔDoop ¦ (Å) | Median of ¦ ¦ΔDoop ¦ (Å) |
| --- | --- | --- | --- | --- |
| (1) | 0.0030 | 0.0010 | 0.010 | 0.0056 |
| (3) | 0.0031 | 0.0012 | 0.0047 | 0.0006 |
| (2) | 0.0034 | 0.002 | 0.011 | 0.0040 |
| (4) | 0.0042 | 0.002 | 0.018 | 0.011 |

### Correlation of SPC coefficients and out-of-plane and in-plane distortion

Figure S41. First- and second-order spin-phonon coupling coefficients as a function of out-of-plane distortions (ΔDoop) for a) Cu MOF (1), b) VO MOF (2), c) CuTPP (3), and d) VOTPP (4). The circles are color-coded: light green – gx, green – gy, and dark purple – gz.

Figure S42. First- and second-order spin-phonon coupling coefficients as a function of Cu/V-N distance changes (ΔCu/V-N) for a) Cu MOF (1), b) VO MOF (2), c) CuTPP (3), and d) VOTPP (4). The circles are color-coded: light green – gx, green – gy, and dark purple – gz.

### Correlation of SPC coefficients and each out-of-plane distortion mode for (1)

Figure S43. First-order spin-phonon coupling coefficients as a function of the magnitude of each distortion mode for Cu MOF (1) optimized by VASP using the PBE-D3 functional.

### Correlation of SPC coefficients and each out-of-plane distortion mode for (2)

Figure S44. First-order spin-phonon coupling coefficients as a function of the magnitude of each distortion mode for VO MOF (2) optimized by VASP using the PBE-D3 functional.

### Correlation of first-order SPC coefficients and each out-of-plane distortion mode for (3)

Figure S45. First-order spin-phonon coupling coefficients as a function of the magnitude of each distortion mode for CuTPP (3) optimized by VASP with the PBE-D3 functional.

### Correlation of first-order SPC coefficients and each out-of-plane distortion mode for (4)

Figure S46. First-order spin-phonon coupling coefficients as a function of the magnitude of each distortion mode for VOTPP (4) optimized by VASP with the PBE-D3 functional.

### Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (1)

Figure S47. Second-order spin-phonon coupling coefficients as a function of the magnitude of each distortion mode for Cu MOF (1) optimized by VASP with the PBE-D3 functional.

### Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (2)

Figure S48. Second-order spin-phonon coupling coefficients as a function of out-of-plane distortions for VO MOF (2) optimized by VASP with the PBE-D3 functional.

### Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (3)

Figure S49. Second-order spin-phonon coupling coefficients as a function of out-of-plane distortions for CuTPP (3) optimized by VASP with the PBE-D3 functional.

### Correlation of second-order SPC coefficients and each out-of-plane distortion mode for (4)

Figure S50. Second-order spin-phonon coupling coefficients as a function of out-of-plane distortions for VOTPP (4) optimized by VASP using the PBE-D3 functional.

Figure S51. Average Cu–N distance changes of the phonon modes in a) VO MOF (2) b) VOTPP (4) and out-of-plane distortion (ΔDoop) of the phonon modes in c) (2) and d) (4) as a function of the phonon mode frequency.

Figure S52. The lowest optical phonon mode (mode 4) in VOTPP (4). Color code V – silver, N – light blue, O – red, C – black, H – omitted for clarity.

Table S13. The first- and second-order SPC coefficients, Doop and average distance change of Cu-N bonds for each mode with its frequency and irreducible representation for (1). The modes indicated in Figure S29 are marked in bold red for the first-order and blue for the second-order coefficients. Those not indicated in Figure S29 but showing relatively large values are also colored.

|  |  |  | First-order SPC |  |  |  |  | Second-order SPC |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mode | freq | Sym | gx | gy | gz | Doop | avg Cu-N | gx | gy | gz |
| 4 | 18.2 | B | 2.0×10-14 | 8.2×10-14 | 2.5×10-13 | 7×10-4 | 0 | 8.2×10-10 | 4.5×10-10 | 8.1×10-9 |
| 5 | 31.7 | B | 8.2×10-14 | 8.2×10-14 | 5.1×10-15 | 2×10-2 | 2×10-4 | 7.3×10-11 | 1.4×10-10 | 1.4×10-9 |
| 6 | 41.6 | A | 7.8×10-9 | 2.1×10-9 | 2.4×10-9 | 4×10-2 | 1×10-3 | 2.9×10-10 | 2.7×10-9 | 1.2×10-8 |
| 7 | 42.4 | B | 1.2×10-28 | 4.6×10-14 | 3.3×10-13 | 5×10-4 | 0 | 8.2×10-10 | 4.5×10-11 | 3.4×10-9 |
| 8 | 64.0 | B | 4.6×10-14 | 1.8×10-13 | 1.8×10-12 | 4×10-2 | 2×10-4 | 3.6×10-10 | 8.9×10-10 | 6.6×10-9 |
| 9 | 66.9 | B | 1.0×10-23 | 1.3×10-13 | 5.1×10-13 | 7×10-3 | 5×10-4 | 1.7×10-10 | 2.7×10-10 | 1.9×10-9 |
| 10 | 77.6 | A | 4.0×10-9 | 3.3×10-11 | 1.3×10-8 | 1×10-2 | 5×10-4 | 1.4×10-10 | 1.1×10-11 | 1.1×10-10 |
| 11 | 78.3 | B | 5.1×10-15 | 5.1×10-15 | 3.3×10-13 | 1×10-2 | 2×10-4 | 6.3×10-11 | 6.3×10-10 | 2.6×10-9 |
| 12 | 83.2 | A | 4.5×10-9 | 1.2×10-9 | 2.7×10-8 | 3×10-2 | 7×10-4 | 3.7×10-13 | 8.4×10-11 | 4.2×10-10 |
| 13 | 88.4 | A | 2.7×10-10 | 1.8×10-10 | 3.5×10-11 | 2×10-2 | 3×10-4 | 4.2×10-12 | 8.1×10-11 | 5.3×10-10 |
| 14 | 93.4 | B | 1.8×10-13 | 1.3×10-13 | 2.3×10-12 | 3×10-4 | 2×10-4 | 4.8×10-11 | 2.2×10-10 | 1.4×10-9 |
| 15 | 95.5 | A | 8.4×10-9 | 5.6×10-9 | 7.7×10-8 | 2×10-2 | 1×10-3 | 5.4×10-11 | 2.8×10-10 | 2.5×10-10 |
| 16 | 102.2 | B | 5.1×10-15 | 4.6×1014 | 8.6×10-13 | 2×10-3 | 0 | 5.7×10-11 | 3.5×10-11 | 6.5×10-10 |
| 17 | 104.9 | A | 3.5×10-10 | 1.1×10-9 | 3.9×10-10 | 7×10-3 | 1×10-3 | 2.7×10-10 | 2.4×10-23 | 9.1×10-10 |
| 18 | 104.9 | B | 2.0×10-14 | 1.8×10-13 | 1.0×10-12 | 3×10-3 | 2×10-4 | 2.4×10-11 | 1.7×10-11 | 3.4×10-10 |
| 19 | 106.4 | A | 7.2×10-10 | 1.7×10-8 | 2.6×10-8 | 2×10-2 | 1×10-3 | 2.2×10-11 | 1.7×10-11 | 3.7×10-11 |
| 20 | 108.5 | A | 6.7×10-9 | 3.7×10-10 | 9.4×10-9 | 3×10-3 | 1×10-3 | 2.0×10-10 | 2.3×10-10 | 2.1×10-9 |
| 21 | 111.2 | B | 2.5×10-13 | 5.1×10-15 | 1.7×10-12 | 2×10-3 | 1×10-3 | 4.0×10-11 | 7.0×10-11 | 1.1×10-11 |
| 22 | 117.1 | B | 5.1×10-15 | 4.5×10-30 | 1.0×10-12 | 6×10-3 | 2×10-4 | 5.5×10-10 | 1.6×10-10 | 2.9×10-9 |
| 23 | 121.8 | A | 5.0×10-9 | 4.0×10-11 | 1.1×10-8 | 4×10-3 | 7×10-4 | 2.2×10-10 | 3.7×10-13 | 5.7×10-10 |
| 24 | 124.1 | A | 1.4×10-9 | 3.4×10-9 | 1.5×10-9 | 9×10-3 | 1×10-3 | 1.6×10-10 | 1.1×10-11 | 3.3×10-10 |
| 25 | 125.8 | B | 5.7×10-33 | 5.1×10-13 | 1.3×10-12 | 3×10-3 | 5×10-4 | 4.2×10-12 | 1.1×10-10 | 2.0×10-10 |
| 26 | 127.9 | A | 2.0×10-11 | 4.8×10-11 | 8.5×10-10 | 2×10-2 | 7×10-4 | 3.2×10-10 | 1.3×10-10 | 2.0×10-10 |
| 27 | 137.6 | A | 1.2×10-8 | 7.6×10-9 | 1.1×10-7 | 9×10-3 | 5×10-4 | 3.7×10-10 | 1.7×10-11 | 1.6×10-9 |
| 28 | 142.9 | B | 1.3×10-13 | 2.0×10-14 | 1.3×10-13 | 2×10-3 | 2×10-4 | 4.5×10-11 | 1.4×10-10 | 1.3×10-9 |
| 29 | 143.1 | A | 8.5×10-9 | 2.5×10-8 | 1.5×10-7 | 6×10-2 | 1×10-3 | 3.7×10-10 | 1.1×10-9 | 1.8×10-10 |
| 30 | 147.4 | B | 1.8×10-13 | 5.1×10-13 | 1.1×10-12 | 4×10-4 | 2×10-4 | 5.4×10-11 | 1.8×10-10 | 5.3×10-10 |
| 31 | 153.5 | B | 1.3×10-13 | 5.1×10-15 | 8.2×10-14 | 2×10-3 | 2×10-4 | 7.0×10-12 | 1.0×10-12 | 8.1×10-11 |
| 32 | 154.9 | A | 9.9×10-12 | 1.5×10-9 | 3.9×10-9 | 3×10-3 | 8×10-4 | 4.3×10-10 | 1.3×10-10 | 2.8×10-9 |
| 33 | 161.8 | B | 4.6×10-14 | 5.1×10-15 | 1.8×10-13 | 2×10-2 | 2×10-4 | 1.4×10-10 | 2.6×10-11 | 1.1×10-10 |
| 34 | 165.2 | A | 1.3×10-10 | 1.9×10-9 | 2.2×10-9 | 1×10-2 | 0 | 1.7×10-10 | 2.0×10-10 | 1.1×10-24 |
| 35 | 168.9 | B | 3.3×10-13 | 4.1×10-13 | 4.6×10-14 | 9×10-4 | 7×10-4 | 3.7×10-11 | 9.2×10-11 | 7.4×10-10 |
| 36 | 172.5 | B | 2.6×10-23 | 4.6×1014 | 1.5×10-12 | 9×10-5 | 5×10-4 | 3.7×10-11 | 1.4×10-10 | 9.7×10-10 |
| 37 | 190.5 | A | 9.4×10-9 | 1.2×10-8 | 4.6×10-10 | 3×10-3 | 3×10-3 | 2.3×10-10 | 1.0×10-12 | 9.5×10-10 |
| 38 | 193.3 | B | 2.5×10-13 | 1.0×10-12 | 1.0×10-12 | 2×10-3 | 1×10-3 | 4.2×10-14 | 1.7×10-11 | 1.1×10-10 |
| 39 | 196.8 | A | 2.0×10-6 | 2.0×10-6 | 1.5×10-10 | 1×10-2 | 2×10-2 | 1.8×10-10 | 1.2×10-10 | 3.7×10-9 |
| 40 | 197.7 | B | 1.0×10-12 | 3.3×10-13 | 1.8×10-12 | 2×10-3 | 3×10-3 | 1.6×10-10 | 8.2×10-12 | 4.4×10-10 |
| 41 | 202.2 | B | 1.3×10-13 | 8.2×10-14 | 1.5×10-12 | 8×10-3 | 5×10-4 | 1.7×10-10 | 4.6×10-9 | 6.6×10-9 |
| 42 | 207.6 | A | 1.2×10-7 | 2.2×10-7 | 4.7×10-8 | 4×10-2 | 6×10-3 | 1.5×10-10 | 5.3×10-9 | 1.9×10-8 |
| 43 | 210.1 | A | 1.2×10-7 | 1.1×10-7 | 1.6×10-10 | 9×10-3 | 5×10-3 | 3.5×10-11 | 3.1×10-10 | 4.0×10-10 |
| 44 | 213.5 | B | 8.6×10-13 | 1.3×10-13 | 2.0×10-14 | 2×10-2 | 2×10-3 | 7.0×10-9 | 4.8×10-10 | 3.4×10-8 |
| 45 | 214.9 | B | 1.8×10-13 | 1.3×10-13 | 1.7×10-12 | 2×10-2 | 5×10-4 | 3.1×10-9 | 5.1×10-11 | 8.2×10-9 |
| 46 | 241.3 | A | 6.1×10-9 | 1.1×10-8 | 9.7×10-8 | 2×10-3 | 8×10-3 | 4.6×10-10 | 3.0×10-10 | 1.0×10-10 |
| 47 | 245.2 | B | 1.2×10-11 | 1.0×10-12 | 2.4×10-11 | 4×10-4 | 2×10-2 | 5.0×10-9 | 4.9×10-10 | 3.8×10-9 |
| 48 | 250.1 | A | 1.6×10-8 | 8.1×10-9 | 1.3×10-7 | 5×10-3 | 1×10-2 | 2.2×10-9 | 9.4×10-10 | 2.1×10--9 |
| 49 | 251.9 | B | 2.0×10-29 | 4.6×10-14 | 1.1×10-26 | 5×10-3 | 7×10-4 | 8.7×10-9 | 5.1×10-9 | 4.7×10-8 |
| 50 | 252.0 | A | 2.7×10-7 | 3.2×10-7 | 3.3×10-6 | 1×10-2 | 5×10-3 | 8.5×10-10 | 2.8×10-11 | 3.7×10-9 |
| 51 | 262.4 | B | 1.1×10-12 | 1.3×10-13 | 6.7×10-23 | 6×10-3 | 4×10-3 | 4.8×10-9 | 2.6×10-9 | 2.8×10-8 |
| 52 | 268.8 | A | 3.0×10-8 | 2.2×10-8 | 2.9×10-7 | 3×10-2 | 8×10-3 | 2.3×10-10 | 5.4×10-11 | 3.5×10-10 |
| 53 | 272.2 | A | 7.3×10-9 | 7.7×10-9 | 8.4×10-8 | 6×10-3 | 4×10-3 | 4.3×10-11 | 1.1×10-10 | 1.2×10-11 |
| 54 | 274.4 | B | 8.2×10-14 | 8.2×10-14 | 8.6×10-13 | 3×10-4 | 3×10-3 | 4.2×10-12 | 1.7×10-13 | 1.8×10-11 |
| 55 | 277.6 | A | 8.5×10-9 | 8.7×10-9 | 9.6×10-8 | 3×10-2 | 3×10-3 | 4.5×10-11 | 1.1×10-10 | 1.3×10-10 |
| 56 | 282.3 | B | 4.6×10-12 | 5.1×10-15 | 4.6×10-14 | 3×10-3 | 9×10-3 | 6.7×10-11 | 2.3×10-10 | 3.6×10-10 |
| 57 | 285.3 | A | 7.0×10-9 | 6.9×10-9 | 8.0×10-8 | 3×10-2 | 8×10-3 | 3.1×10-9 | 1.0×10-12 | 9.0×10-9 |
| 58 | 306.7 | B | 2.0×10-14 | 1.8×10-13 | 4.6×10-14 | 8×10-4 | 2×10-3 | 6.7×10-11 | 4.8×10-11 | 7.1×10-10 |
| 59 | 316.5 | B | 2.7×10-12 | 3.3×10-13 | 2.5×10-12 | 1×10-3 | 8×10-3 | 2.2×10-11 | 6.4×10-10 | 2.9×10-9 |
| 60 | 318.7 | A | 3.1×10-9 | 1.9×10-9 | 2.9×10-8 | 2×10-2 | 7×10-3 | 9.2×10-10 | 1.2×10-11 | 2.2×10-9 |
| 61 | 324.2 | A | 1.5×10-8 | 1.4×10-8 | 1.7×10-7 | 2×10-2 | 4×10-3 | 1.0×10-10 | 1.4×10-10 | 2.0×10-11 |
| 62 | 333.5 | B | 6.2×10-13 | 8.2×10-14 | 7.3×10-13 | 2×10-3 | 3×10-3 | 8.4×10-11 | 1.3×10-10 | 1.2×10-9 |
| 63 | 337.6 | A | 2.9×10-8 | 2.9×10-8 | 3.4×10-7 | 2×10-2 | 5×10-3 | 1.0×10-9 | 7.0×10-12 | 3.2×10-9 |
| 64 | 341.8 | A | 6.5×10-10 | 4.1×10-10 | 5.3×10-9 | 1×10-2 | 1×10-3 | 1.7×10-10 | 1.3×10-10 | 1.0×10-9 |
| 65 | 342.5 | B | 1.0×10-12 | 4.6×10-14 | 2.5×10-13 | 3×10-4 | 2×10-3 | 6.0×10-12 | 7.0×10-12 | 5.0×10-12 |
| 66 | 355.0 | B | 2.5×10-13 | 1.3×10-13 | 1.3×10-12 | 3×10-4 | 2×10-3 | 1.5×10-10 | 3.7×10-13 | 6.7×10-13 |
| 67 | 380.5 | A | 4.0×10-6 | 4.1×10-6 | 4.7×10-5 | 8×10-3 | 2×10-2 | 2.2×10-11 | 4.1×10-10 | 1.7×10-13 |
| 68 | 396.5 | B | 4.6×10-14 | 4.3×10-29 | 7.3×10-13 | 6×10-4 | 7×10-4 | 2.2×10-11 | 1.7×10-10 | 1.2×10-9 |
| 69 | 398.9 | B | 8.6×10-13 | 1.3×10-13 | 1.5×10-12 | 3×10-4 | 5×10-4 | 2.0×10-10 | 2.2×10-10 | 2.0×10-9 |
| 70 | 401.2 | A | 8.2×10-11 | 2.3×10-10 | 1.5×10-9 | 1×10-3 | 5×10-3 | 1.5×10-10 | 4.8×10-11 | 1.3×10-10 |
| 71 | 402.4 | A | 4.0×10-8 | 4.0×10-8 | 4.6×10-7 | 3×10-3 | 2×10-3 | 5.4×10-10 | 1.0×10-10 | 3.7×10-9 |

Table S14. The first- and second-order SPC coefficients, Doop and average distance change of V-N bonds for each mode with its frequency and irreducible representation for (2). The irreducible representations are omitted as all of them belong to A. The modes that are indicated in Figure S30 are marked in bold red for the first-order and in bold blue for the second-order coefficients. Those not indicated in Figure S30 but showing relatively large values are also highlighted in color.

|  |  | First-order SPC |  |  |  |  | Second-order SPC |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mode | freq | gx | gy | gz | Doop | avg V-N | gx | gy | gz |
| 4 | 16.2 | 5.0×10-11 | 1.0×10-10 | 6.9×10-10 | 6.1×10-3 | 2.5×10-4 | 1.3×10-9 | 3.2×10-10 | 2.6×10-10 |
| 5 | 29.1 | 6.3×10-11 | 1.5×10-9 | 3.0×10-9 | 5.7×10-2 | 2.5×10-4 | 6.6×10-9 | 1.5×10-8 | 4.2×10-10 |
| 6 | 33.1 | 1.8×10-10 | 1.5×10-10 | 9.6×10-10 | 3.3×10-3 | 1.5×10-3 | 8.4×10-9 | 7.0×10-9 | 1.4×10-9 |
| 7 | 37.6 | 7.4×10-10 | 1.4×10-10 | 4.7×10-9 | 4.0×10-2 | 1.0×10-3 | 3.4×10-10 | 3.3×10-9 | 3.1×10-9 |
| 8 | 56.5 | 1.4×10-11 | 2.0×10-10 | 7.1×10-10 | 3.7×10-2 | 7.5×10-4 | 1.0×10-10 | 2.6×10-9 | 3.3×10-11 |
| 9 | 64.0 | 1.8×10-10 | 1.9×10-9 | 1.7×10-9 | 5.5×10-2 | 2.5×10-4 | 4.0×10-11 | 1.8×10-9 | 4.8×10-11 |
| 10 | 72.4 | 1.3×10-10 | 1.6×10-9 | 1.7×10-10 | 1.1×10-2 | 5.0×10-4 | 1.1×10-9 | 3.2×10-10 | 3.5×10-11 |
| 11 | 74.2 | 5.4×10-10 | 3.2×10-9 | 5.7×10-10 | 1.1×10-1 | 1.0×10-3 | 3.8×10-10 | 3.6×10-9 | 2.9×10-10 |
| 12 | 78.7 | 2.1×10-10 | 1.3×10-9 | 2.2×10-9 | 5.6×10-2 | 2.5×10-4 | 1.0×10-9 | 2.9×10-9 | 3.7×10-13 |
| 13 | 79.3 | 1.8×10-10 | 1.1×10-9 | 3.8×10-10 | 3.6×10-2 | 7.5×10-4 | 5.5×10-9 | 9.0×10-9 | 9.5×10-10 |
| 14 | 82.0 | 3.2×10-10 | 4.5×10-10 | 1.3×10-10 | 3.6×10-2 | 1.0×10-3 | 1.1×10-11 | 3.4×10-10 | 2.4×10-10 |
| 15 | 83.7 | 8.9×10-11 | 3.3×10-10 | 2.9×10-10 | 2.2×10-2 | 5.0×10-4 | 3.0×10-8 | 2.1×10-8 | 5.0×10-12 |
| 16 | 87.6 | 6.3×10-10 | 2.3×10-10 | 3.3×10-11 | 1.9×10-2 | 5.0×10-4 | 2.1×10-8 | 7.6×10-9 | 1.2×10-10 |
| 17 | 92.6 | 5.3×10-10 | 9.0×10-12 | 7.0×10-9 | 4.5×10-3 | 1.3×10-3 | 9.3×10-9 | 2.5×10-9 | 5.0×10-9 |
| 18 | 99.7 | 4.4×10-10 | 6.2×10-13 | 2.2×10-11 | 5.1×10-3 | 5.0×10-4 | 1.7×10-9 | 2.6×10-9 | 4.5×10-11 |
| 19 | 102.7 | 1.3×10-9 | 8.5×10-10 | 1.9×10-8 | 4.9×10-3 | 1.7×10-3 | 7.7×10-10 | 2.5×10-10 | 3.2×10-10 |
| 20 | 108.6 | 2.1×10-10 | 2.4×10-9 | 6.1×10-9 | 1.6×10-2 | 2.0×10-3 | 7.1×10-8 | 1.8×10-8 | 4.3×10-9 |
| 21 | 110.5 | 4.4×10-10 | 1.1×10-10 | 3.8×10-10 | 4.7×10-3 | 2.3×10-3 | 4.3×10-10 | 6.2×10-10 | 4.0×10-10 |
| 22 | 112.0 | 4.7×10-11 | 7.4×10-10 | 2.0×10-14 | 3.6×10-3 | 1.5×10-3 | 4.8×10-9 | 4.5×10-9 | 4.2×10-10 |
| 23 | 117.8 | 1.0×10-12 | 1.2×10-10 | 7.4×10-9 | 1.3×10-2 | 1.5×10-3 | 2.5×10-8 | 4.2×10-9 | 3.5×10-11 |
| 24 | 118.8 | 5.3×10-9 | 4.8×10-9 | 8.6×10-8 | 1.9×10-2 | 2.3×10-3 | 2.7×10-10 | 1.6×10-9 | 2.2×10-10 |
| 25 | 122.3 | 3.2×10-10 | 1.3×10-12 | 3.0×10-10 | 1.1×10-3 | 1.5×10-3 | 1.1×10-10 | 2.5×10-9 | 1.7×10-9 |
| 26 | 125.8 | 2.0×10-10 | 2.4×10-10 | 4.9×10-10 | 3.0×10-3 | 1.0×10-3 | 9.2×10-10 | 2.3×10-10 | 1.1×10-10 |
| 27 | 129.7 | 6.2×10-11 | 1.7×10-10 | 3.5×10-9 | 1.8×10-4 | 1.0×10-3 | 2.8×10-11 | 2.7×10-10 | 6.7×10-13 |
| 28 | 134.9 | 2.3×10-10 | 3.8×10-10 | 2.6×10-9 | 8.0×10-3 | 1.0×10-3 | 1.4×10-9 | 6.6×10-9 | 3.6×10-10 |
| 29 | 136.1 | 1.3×10-10 | 2.3×10-10 | 4.8×10-9 | 1.1×10-2 | 3.8×10-3 | 2.0×10-10 | 1.5×10-10 | 1.0×10-9 |
| 30 | 139.9 | 8.0×10-11 | 1.2×10-9 | 1.4×10-9 | 4.0×10-2 | 1.2×10-3 | 3.3×10-8 | 2.2×10-8 | 1.7×10-13 |
| 31 | 142.2 | 3.7×10-9 | 2.1×10-10 | 9.9×10-12 | 1.3×10-2 | 2.8×10-3 | 1.4×10-9 | 1.1×10-9 | 6.0×10-12 |
| 32 | 144.9 | 8.6×10-9 | 7.6×10-10 | 1.4×10-9 | 1.1×10-2 | 1.3×10-3 | 5.0×10-9 | 4.4×10-9 | 6.3×10-11 |
| 33 | 146.8 | 2.1×10-10 | 2.7×10-10 | 9.0×10-10 | 2.8×10-3 | 2.8×10-3 | 2.4×10-8 | 4.4×10-9 | 2.3×10-9 |
| 34 | 148.7 | 7.3×10-13 | 2.5×10-9 | 2.6×10-10 | 1.7×10-3 | 2.5×10-3 | 9.9×10-9 | 2.1×10-8 | 1.7×10-9 |
| 35 | 155.1 | 6.7×10-10 | 9.3×10-11 | 1.3×10-11 | 3.7×10-3 | 1.0×10-3 | 4.0×10-11 | 4.2×10-9 | 1.9×10-9 |
| 36 | 165.5 | 1.4×10-10 | 4.0×10-10 | 9.4×10-11 | 1.2×10-4 | 1.7×10-3 | 1.8×10-8 | 9.8×10-9 | 4.2×10-12 |
| 37 | 167.0 | 3.7×10-10 | 7.8×10-10 | 4.9×10-10 | 1.2×10-3 | 1.3×10-3 | 4.2×10-8 | 2.1×10-8 | 3.4×10-12 |
| 38 | 170.3 | 2.8×10-10 | 8.4×10-11 | 5.8×10-10 | 2.3×10-3 | 7.5×10-4 | 1.7×10-8 | 1.1×10-8 | 9.4×10-12 |
| 39 | 187.5 | 7.9×10-10 | 5.1×10-15 | 1.3×10-8 | 3.2×10-3 | 2.3×10-3 | 1.4×10-10 | 4.4×10-10 | 1.8×10-10 |
| 40 | 188.8 | 9.7×10-10 | 9.4×10-10 | 3.6×10-8 | 8.0×10-3 | 7.5×10-4 | 8.1×10-11 | 2.5×10-9 | 2.1×10-10 |
| 41 | 197.0 | 9.8×10-9 | 8.0×10-10 | 8.8×10-8 | 5.4×10-3 | 2.5×10-3 | 2.7×10-8 | 1.7×10-8 | 6.3×10-10 |
| 42 | 200.0 | 8.6×10-11 | 2.6×10-11 | 7.1×10-9 | 4.4×10-3 | 1.2×10-3 | 1.8×10-19 | 1.6×10-9 | 5.9×10-9 |
| 43 | 202.5 | 1.2×10-8 | 1.9×10-8 | 1.1×10-9 | 1.1×10-2 | 1.1×10-2 | 1.1×10-9 | 8.8×10-11 | 1.2×10-9 |
| 44 | 207.0 | 2.2×10-11 | 1.5×10-11 | 1.5×10-8 | 3.7×10-3 | 7.5×10-4 | 1.2×10-8 | 1.2×10-8 | 6.7×10-11 |
| 45 | 234.1 | 3.5×10-11 | 1.5×10-11 | 6.5×10-9 | 6.2×10-3 | 6.0×10-3 | 2.0×10-9 | 1.2×10-9 | 9.7×10-10 |
| 46 | 237.7 | 1.0×10-10 | 1.5×10-10 | 3.9×10-10 | 4.3×10-4 | 5.0×10-3 | 1.9×10-8 | 4.0×10-9 | 1.2×10-11 |
| 47 | 243.4 | 8.0×10-10 | 3.6×10-9 | 6.6×10-9 | 7.3×10-4 | 4.5×10-3 | 1.7×10-8 | 3.6×10-9 | 2.4×10-11 |
| 48 | 244.8 | 1.7×10-8 | 1.1×10-8 | 3.3×10-8 | 9.0×10-4 | 1.5×10-3 | 4.4×10-8 | 2.6×10-8 | 9.6×10-10 |
| 49 | 246.7 | 6.3×10-11 | 6.2×10-11 | 5.4×10-8 | 3.8×10-3 | 5.2×10-3 | 5.0×10-9 | 1.6×10-9 | 5.0×10-9 |
| 50 | 248.5 | 1.5×10-8 | 2.0×10-8 | 5.8×10-8 | 5.9×10-3 | 4.0×10-3 | 5.9×10-10 | 1.8×10-11 | 6.2×10-10 |
| 51 | 265.5 | 2.0×10-8 | 2.3×10-8 | 9.4×10-7 | 4.0×10-3 | 3.7×10-3 | 4.3×10-11 | 1.8×10-9 | 2.7×10-9 |
| 52 | 269.3 | 2.8×10-11 | 3.8×10-11 | 6.9×10-9 | 9.8×10-3 | 2.0×10-3 | 3.1×10-8 | 6.0×10-9 | 2.2×10-9 |
| 53 | 269.8 | 2.2×10-9 | 2.9×10-9 | 4.2×10-8 | 4.7×10-3 | 2.2×10-3 | 3.1×10-10 | 2.7×10-10 | 2.1×10-10 |
| 54 | 273.2 | 2.6×10-9 | 5.4×10-10 | 5.3×10-8 | 1.3×10-2 | 1.5×10-2 | 1.2×10-9 | 5.5×10-10 | 4.1×10-10 |
| 55 | 275.1 | 2.7×10-9 | 2.0×10-9 | 2.0×10-8 | 7.7×10-3 | 6.5×10-3 | 1.2×10-9 | 2.1×10-9 | 1.1×10-9 |
| 56 | 278.9 | 5.3×10-10 | 2.5×10-10 | 8.7×10-8 | 1.5×10-3 | 4.5×10-3 | 3.1×10-8 | 1.2×10-8 | 9.4×10-12 |
| 57 | 281.8 | 2.6×10-10 | 1.6×10-9 | 6.8×10-8 | 6.3×10-3 | 4.2×10-3 | 8.0×10-10 | 3.6×10-9 | 1.5×10-10 |
| 58 | 299.1 | 3.9×10-10 | 8.5×10-11 | 3.2×10-10 | 3.0×10-3 | 3.2×10-3 | 2.8×10-9 | 2.5×10-9 | 6.0×10-9 |
| 59 | 302.8 | 5.1×10-10 | 1.8×10-10 | 1.6×10-8 | 2.5×10-3 | 2.8×10-3 | 3.2×10-8 | 6.5×10-9 | 1.2×10-8 |
| 60 | 307.3 | 7.4×10-9 | 8.2×10-9 | 1.0×10-7 | 4.2×10-3 | 1.5×10-3 | 2.1×10-8 | 1.5×10-8 | 7.0×10-12 |
| 61 | 316.1 | 3.1×10-11 | 7.1×10-11 | 3.7×10-9 | 6.6×10-4 | 1.2×10-3 | 5.4×10-9 | 1.2×10-8 | 2.6×10-11 |
| 62 | 328.9 | 9.8×10-10 | 6.0×10-11 | 2.6×10-11 | 3.8×10-4 | 5.0×10-3 | 9.7×10-10 | 9.9×10-10 | 3.7×10-10 |
| 63 | 331.0 | 3.1×10-10 | 1.3×10-11 | 1.7×10-10 | 1.1×10-3 | 6.0×10-3 | 7.3×10-10 | 9.5×10-10 | 7.7×10-10 |
| 64 | 334.8 | 8.7×10-10 | 1.6×10-9 | 1.7×10-9 | 4.8×10-4 | 1.3×10-3 | 3.2×10-10 | 2.1×10-9 | 2.6×10-11 |
| 65 | 340.8 | 6.7×10-10 | 2.6×10-10 | 7.0×10-10 | 4.4×10-3 | 9.7×10-3 | 1.9×10-10 | 3.5×10-11 | 1.8×10-9 |
| 66 | 342.4 | 5.1×10-11 | 6.6×10-10 | 1.8×10-10 | 9.8×10-4 | 1.5×10-2 | 1.1×10-10 | 1.6×10-9 | 4.5×10-9 |
| 67 | 342.8 | 6.6×10-12 | 1.4×10-9 | 1.5×10-9 | 7.4×10-4 | 1.5×10-2 | 7.7×10-10 | 6.2×10-9 | 5.4×10-9 |
| 68 | 351.0 | 1.0×10-8 | 2.9×10-9 | 4.8×10-10 | 8.5×10-4 | 3.5×10-3 | 5.2×10-9 | 3.7×10-8 | 3.8×10-10 |
| 69 | 380.0 | 2.1×10-9 | 7.4×10-12 | 9.7×10-8 | 7.5×10-5 | 3.2×10-3 | 7.6×10-10 | 2.3×10-9 | 1.6×10-10 |
| 70 | 388.3 | 2.4×10-9 | 1.1×10-9 | 7.7×10-8 | 1.8×10-4 | 2.5×10-3 | 1.2×10-8 | 1.3×10-8 | 1.7×10-10 |
| 71 | 391.0 | 3.0×10-8 | 3.7×10-8 | 2.9×10-6 | 2.2×10-3 | 1.7×10-2 | 9.3×10-9 | 9.4×10-9 | 6.3×10-10 |
| 72 | 395.0 | 2.2×10-10 | 5.8×10-11 | 9.9×10-10 | 7.8×10-5 | 1.7×10-3 | 2.0×10-8 | 2.2×10-8 | 9.6×10-11 |
| 73 | 396.8 | 1.3×10-9 | 6.2×10-10 | 9.1×10-8 | 1.3×10-3 | 3.3×10-3 | 4.5×10-11 | 1.9×10-10 | 2.4×10-10 |
| 74 | 399.9 | 1.3×10-11 | 4.3×10-12 | 1.9×10-10 | 3.7×10-4 | 5.0×10-3 | 6.7×10-11 | 1.3×10-9 | 4.0×10-11 |
| 75 | 401.5 | 4.2×10-10 | 5.1×10-10 | 6.0×10-8 | 1.8×10-3 | 4.0×10-3 | 7.9×10-10 | 2.8×10-9 | 9.4×10-12 |
| 76 | 402.5 | 1.1×10-9 | 1.2×10-9 | 1.1×10-7 | 7.4×10-4 | 3.8×10-3 | 1.7×10-13 | 8.0×10-10 | 8.1×10-11 |
| 77 | 406.7 | 2.9×10-10 | 2.8×10-10 | 4.4×10-8 | 1.2×10-3 | 1.0×10-2 | 8.3×10-10 | 1.5×10-9 | 1.4×10-9 |
| 78 | 407.4 | 1.1×10-10 | 1.0×10-10 | 1.9×10-9 | 8.8×10-4 | 1.3×10-2 | 6.4×10-9 | 2.0×10-9 | 1.8×10-9 |

Table S15. The first- and second-order SPC coefficients, Doop and average distance change of Cu-N bonds for each mode with its frequency and irreducible representation for (3). The modes indicated in Figure S31 are marked in bold red for the first-order and blue for the second-order coefficients. Those not indicated in Figure S31 but showing relatively large values are also highlighted in color.

|  |  |  | First-order SPC |  |  |  |  | Second-order SPC |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mode | freq | Sym | gx | gy | gz | Doop | avg Cu-N | gx | gy | gz |
| 4 | 30.5 | E | 8.2×10-14 | 4.0×10-12 | 5.9×10-12 | 7.9×10-4 | 5.0×10-4 | 4.1×10-9 | 3.2×10-8 | 1.5×10-7 |
| 5 | 30.5 | E | 2.7×10-12 | 2.3×10-11 | 1.1×10-10 | 2.3×10-4 | 5.0×10-4 | 2.0×10-9 | 2.7×10-9 | 2.7×10-8 |
| 6 | 39.0 | B2 | 2.1×10-11 | 1.5×10-10 | 1.0×10-10 | 5.3×10-4 | 5.0×10-4 | 7.3×10-10 | 1.7×10-8 | 6.3×10-8 |
| 7 | 41.4 | A2 | 4.8×10-10 | 7.3×10-10 | 4.9×10-9 | 2.9×10-3 | 1.0×10-3 | 5.3×10-9 | 1.2×10-8 | 9.6×10-8 |
| 8 | 46.4 | E | 3.2×10-12 | 1.5×10-11 | 3.3×10-13 | 8.2×10-4 | 2.5×10-4 | 5.4×10-9 | 2.7×10-8 | 1.4×10-7 |
| 9 | 46.4 | E | 4.1×10-13 | 3.8×10-11 | 9.0×10-11 | 3.5×10-4 | 1.2×10-3 | 2.5×10-9 | 4.8×10-9 | 3.9×10-8 |
| 10 | 50.7 | A2 | 2.6×10-10 | 1.6×10-10 | 1.1×10-8 | 1.8×10-2 | 5.0×10-4 | 4.8×10-9 | 1.0×10-8 | 9.4×10-8 |
| 11 | 51.7 | B1 | 2.2×10-12 | 4.4×10-11 | 1.5×10-10 | 2.6×10-4 | 5.0×10-4 | 2.6×10-9 | 3.9×10-8 | 5.1×10-8 |
| 12 | 55.8 | E | 4.1×10-13 | 2.4×10-11 | 7.1×10-11 | 6.7×10-4 | 1.0×10-3 | 5.1×10-10 | 1.3×10-9 | 9.5×10-9 |
| 13 | 55.8 | E | 2.5×10-13 | 2.7×10-12 | 1.1×10-12 | 1.2×10-4 | 0 | 1.7×10-9 | 3.4×10-8 | 1.2×10-7 |
| 14 | 57.6 | B1 | 1.2×10-10 | 2.5×10-13 | 2.6×10-10 | 5.5×10-4 | 2.0×10-3 | 1.8×10-7 | 3.0×10-7 | 3.9×10-8 |
| 15 | 59.7 | A1 | 6.4×10-10 | 4.7×10-10 | 2.4×10-9 | 6.8×10-3 | 2.5×10-4 | 1.3×10-9 | 2.0×10-9 | 1.9×10-8 |
| 16 | 61.9 | E | 4.3×10-12 | 7.1×10-11 | 2.3×10-10 | 6.1×10-5 | 7.5×10-4 | 1.1×10-9 | 1.3×10-8 | 5.0×10-8 |
| 17 | 61.9 | E | 7.6×10-28 | 4.6×10-14 | 2.2×10-12 | 5.2×10-4 | 7.5×10-4 | 1.8×10-9 | 2.1×10-9 | 2.5×10-8 |
| 18 | 63.2 | E | 1.4×10-11 | 8.2×10-14 | 6.4×10-11 | 1.0×10-4 | 7.5×10-4 | 3.6×10-9 | 3.1×10-8 | 1.4×10-7 |
| 19 | 63.2 | E | 2.5×10-13 | 8.2×10-14 | 1.5×10-12 | 2.2×10-4 | 2.5×10-4 | 1.0×10-9 | 9.1×10-10 | 1.4×10-8 |
| 20 | 65.5 | A1 | 2.8×10-8 | 2.7×10-8 | 1.9×10-7 | 2.8×10-2 | 1.3×10-3 | 3.9×10-10 | 1.2×10-9 | 9.7×10-9 |
| 21 | 66.9 | E | 1.8×10-13 | 1.8×10-13 | 1.3×10-13 | 1.5×10-4 | 5.0×10-4 | 5.2×10-9 | 2.5×10-8 | 1.4×10-7 |
| 22 | 66.9 | E | 4.6×10-14 | 2.8×10-11 | 4.9×10-11 | 2.7×10-4 | 7.5×10-4 | 2.1×10-9 | 6.5×10-9 | 4.6×10-8 |
| 23 | 71.7 | A2 | 5.3×10-9 | 6.5×10-9 | 3.2×10-8 | 2.6×10-2 | 2.5×10-4 | 1.3×10-9 | 9.6×10-9 | 4.6×10-8 |
| 24 | 76.7 | A2 | 1.1×10-8 | 1.1×10-8 | 8.7×10-8 | 1.1×10-2 | 1.0×10-3 | 6.6×10-10 | 4.7×10-10 | 7.5×10-9 |
| 25 | 77.9 | B2 | 3.5×10-11 | 1.1×10-12 | 2.0×10-11 | 3.1×10-4 | 7.5×10-4 | 6.5×10-10 | 1.8×10-8 | 6.2×10-8 |
| 26 | 78.3 | E | 1.3×10-12 | 2.6×10-11 | 8.0×10-11 | 2.5×10-4 | 0 | 1.1×10-9 | 4.7×10-9 | 2.8×10-8 |
| 27 | 78.3 | E | 3.3×10-13 | 2.6×10-11 | 5.6×10-12 | 5.1×10-4 | 5.0×10-4 | 7.1×10-9 | 1.7×10-8 | 1.3×10-7 |
| 28 | 84.5 | A1 | 8.9×10-9 | 9.3×10-9 | 7.5×10-8 | 6.1×10-3 | 7.5×10-4 | 8.4×10-10 | 1.0×10-9 | 1.3×10-8 |
| 29 | 87.4 | E | 3.4×10-12 | 2.0×10-12 | 3.2×10-11 | 3.1×10-4 | 5.0×10-4 | 7.0×10-10 | 4.7×10-10 | 7.9×10-9 |
| 30 | 87.4 | E | 2.1×10-11 | 6.2×10-13 | 8.9×10-11 | 8.6×10-5 | 5.0×10-4 | 3.3×10-9 | 2.8×10-8 | 1.2×10-7 |
| 31 | 89.2 | B1 | 7.0×10-12 | 6.2×10-11 | 1.8×10-11 | 1.4×10-4 | 2.0×10-3 | 1.5×10-6 | 1.9×10-6 | 6.4×10-8 |
| 32 | 95.5 | E | 4.1×10-13 | 9.0×10-12 | 3.1×10-11 | 2.7×10-4 | 2.5×10-4 | 1.3×10-9 | 2.1×10-9 | 2.0×10-8 |
| 33 | 95.5 | E | 9.0×10-12 | 5.1×10-15 | 5.4×10-11 | 2.2×10-4 | 2.5×10-4 | 2.1×10-9 | 2.7×10-8 | 1.1×10-7 |
| 34 | 97.4 | B2 | 4.7×10-10 | 9.6×10-11 | 3.3×10-10 | 1.1×10-3 | 2.5×10-4 | 3.9×10-7 | 6.7×10-7 | 9.5×10-8 |
| 35 | 107.0 | A1 | 1.7×10-8 | 1.7×10-8 | 8.3×10-8 | 3.2×10-2 | 7.5×10-4 | 2.6×10-9 | 3.4×10-9 | 4.2×10-8 |
| 36 | 107.6 | A2 | 7.1×10-9 | 7.0×10-9 | 7.4×10-8 | 5.1×10-3 | 7.5×10-4 | 6.8×10-10 | 9.6×10-10 | 1.1×10-8 |
| 37 | 113.6 | B1 | 4.9×10-12 | 5.4×10-11 | 1.7×10-11 | 4.1×10-4 | 2.5×10-4 | 3.5×10-7 | 5.9×10-7 | 8.1×10-8 |
| 38 | 114.4 | A2 | 1.2×10-7 | 1.2×10-7 | 8.7×10-7 | 6.7×10-2 | 2.2×10-3 | 9.0×10-10 | 2.4×10-9 | 2.0×10-8 |
| 39 | 115.0 | B2 | 7.5×10-11 | 4.3×10-10 | 2.8×10-10 | 8.0×10-4 | 2.0×10-3 | 2.0×10-7 | 3.5×10-7 | 5.4×10-8 |
| 40 | 117.2 | A1 | 1.1×10-7 | 1.1×10-7 | 8.9×10-7 | 4.9×10-2 | 2.5×10-3 | 6.4×10-10 | 5.7×10-9 | 2.8×10-8 |
| 41 | 119.6 | B1 | 2.5×10-11 | 6.4×10-11 | 3.7×10-10 | 6.9×10-4 | 2.5×10-4 | 1.7×10-9 | 3.2×10-8 | 5.4×10-8 |
| 42 | 129.3 | A1 | 2.1×10-8 | 2.1×10-8 | 1.5×10-7 | 2.5×10-2 | 7.5×10-4 | 1.1×10-9 | 1.9×10-9 | 2.2×10-8 |
| 43 | 133.9 | B2 | 2.9×10-10 | 4.3×10-12 | 5.4×10-10 | 3.6×10-4 | 2.5×10-4 | 1.8×10-7 | 3.2×10-7 | 5.7×10-8 |
| 44 | 135.2 | E | 4.6×10-14 | 2.5×10-13 | 1.3×10-12 | 1.8×10-3 | 1.0×10-3 | 9.7×10-10 | 1.2×10-8 | 4.9×10-8 |
| 45 | 135.2 | E | 8.6×10-12 | 1.0×10-12 | 3.8×10-11 | 2.1×10--3 | 7.5×10-4 | 5.5×10-9 | 2.9×10-8 | 1.6×10-7 |
| 46 | 137.2 | B1 | 4.1×10-13 | 1.1×10-10 | 2.3×10-10 | 5.5×10-4 | 7.5×10-4 | 2.6×10-7 | 4.0×10-7 | 4.0×10-8 |
| 47 | 149.5 | E | 1.0×10-11 | 8.6×10-13 | 4.5×10-11 | 2.4×10-3 | 2.5×10-4 | 5.1×10-9 | 2.9×10-8 | 1.6×10-7 |
| 48 | 149.5 | E | 8.2×10-12 | 1.3×10-11 | 1.5×10-10 | 1.5×10-3 | 7.5×10-4 | 2.3×10-9 | 2.2×10-9 | 3.0×10-8 |
| 49 | 193.2 | B2 | 3.5×10-10 | 3.6×10-11 | 3.0×10-10 | 1.0×10-3 | 3.0×10-3 | 5.4×10-6 | 6.3×10-6 | 8.9×10-8 |
| 50 | 200.1 | A2 | 4.4×10-8 | 4.6×10-8 | 5.9×10-7 | 3.8×10-3 | 2.2×10-3 | 2.9×10-9 | 4.4×10-9 | 4.2×10-8 |
| 51 | 200.9 | A1 | 6.9×10-8 | 7.0×10-8 | 8.3×10-7 | 1.9×10-3 | 2.2×10-3 | 7.7×10-9 | 1.6×10-8 | 1.3×10-7 |
| 52 | 201.0 | B1 | 1.0×10-11 | 1.0×10-10 | 4.9×10-10 | 9.8×10-4 | 5.0×10-4 | 7.8×10-7 | 1.2×10-6 | 1.1×10-7 |
| 53 | 205.1 | E | 4.1×10-13 | 4.0×10-11 | 8.2×10-11 | 1.4×10-3 | 3.7×10-3 | 4.5×10-9 | 9.2×10-9 | 7.5×10-8 |
| 54 | 205.1 | E | 1.5×10-12 | 1.2×10-11 | 6.6×10-11 | 8.0×10-4 | 2.8×10-3 | 1.6×10-9 | 3.4×10-9 | 3.2×10-8 |
| 55 | 208.2 | B1 | 9.0×10-11 | 4.6×10-12 | 2.4×10-10 | 1.1×10-4 | 1.6×10-2 | 5.6×10-5 | 5.8×10-5 | 3.2×10-8 |
| 56 | 209.4 | B2 | 1.1×10-10 | 4.4×10-10 | 2.0×10-10 | 1.7×10-4 | 1.7×10-2 | 5.6×10-5 | 5.8×10-5 | 3.7×10-8 |
| 57 | 212.1 | A2 | 1.1×10-7 | 1.1×10-7 | 9.2×10-7 | 7.8×10-3 | 2.5×10-3 | 3.2×10-9 | 2.8×10--9 | 3.1×10-8 |
| 58 | 213.8 | E | 2.7×10-12 | 1.1×10-10 | 2.7×10-10 | 2.9×10-4 | 4.0×10-3 | 2.7×10-9 | 8.5×10-9 | 5.9×10-8 |
| 59 | 213.8 | E | 8.2×10-14 | 1.2×10-11 | 6.6×10-12 | 9.4×10-4 | 4.7×10-3 | 1.5×10-9 | 8.2×10-9 | 4.6×10-8 |
| 60 | 217.3 | A1 | 5.4×10-8 | 5.3×10-8 | 4.5×10-7 | 1.4×10-2 | 2.0×10-3 | 3.2×10-9 | 2.2×10-9 | 2.7×10-8 |
| 61 | 222.1 | E | 8.6×1013 | 1.3×10-11 | 5.3×10-11 | 2.2×10-4 | 1.7×10-3 | 1.2×10-9 | 3.4×10-9 | 2.7×10-8 |
| 62 | 222.1 | E | 8.6×1013 | 3.3×10-13 | 1.8×10-12 | 1.2×10-4 | 1.0×10-3 | 4.1×10-9 | 2.6×10-8 | 1.2×10-7 |
| 63 | 224.4 | E | 1.3×1013 | 1.3×10-13 | 2.0×10-14 | 3.7×10-4 | 6.5×10-3 | 2.5×10-9 | 1.7×10-9 | 2.7×10-8 |
| 64 | 224.4 | E | 4.3×10-12 | 3.7×10-12 | 5.1×10-15 | 9.7×10-5 | 7.5×10-3 | 3.9×10-9 | 3.1×10-8 | 1.5×10-7 |
| 65 | 228.3 | E | 1.1×10-12 | 1.3×10-13 | 8.6×10-12 | 1.6×10-3 | 5.3×10-3 | 3.0×10-9 | 1.6×10-9 | 2.7×10-8 |
| 66 | 228.3 | E | 6.2×10-13 | 1.8×10-13 | 1.3×10-12 | 1.3×10-3 | 5.5×10-3 | 4.0×10-9 | 3.8×10-8 | 1.6×10-7 |
| 67 | 230.4 | E | 5.1×10-13 | 2.0×10-11 | 6.6×10-12 | 2.1×10-4 | 7.2×10-3 | 1.6×10-9 | 1.1×10-8 | 5.5×10-8 |
| 68 | 230.4 | E | 1.3×10-13 | 2.0×10-12 | 3.2×10-12 | 5.5×10-4 | 7.3×10-3 | 3.3×10-9 | 3.4×10-8 | 1.5×10-7 |
| 69 | 237.5 | B1 | 1.4×10-11 | 3.2×10-11 | 3.0×10-10 | 6.7×10-4 | 2.2×10-3 | 4.0×10-6 | 4.9×10-6 | 1.3×10-7 |
| 70 | 238.7 | B2 | 3.4×10-10 | 8.0×10-11 | 1.8×10-10 | 7.2×10-5 | 1.2×10-3 | 1.2×10-8 | 6.3×10-8 | 5.2×10-8 |
| 71 | 264.9 | B1 | 1.0×10-12 | 1.4×10-10 | 2.2×10-10 | 3.2×10-4 | 7.5×10-4 | 2.5×10-6 | 3.3×10-6 | 1.1×10-7 |
| 72 | 267.1 | B2 | 3.0×10-10 | 2.3×10-11 | 3.4×10-10 | 1.2×10-3 | 2.0×10-3 | 3.3×10-6 | 4.1×10-6 | 1.0×10-7 |
| 73 | 273.9 | A1 | 9.1×10-9 | 8.8×10-9 | 8.6×10-8 | 4.8×10-3 | 7.5×10-4 | 1.3×10-9 | 6.9×10-10 | 1.3×10-8 |
| 74 | 276.1 | A2 | 4.5×10-10 | 4.1×10-10 | 2.6×10-9 | 7.1×10-3 | 2.5×10-4 | 9.5×10-10 | 1.2×10-9 | 1.4×10-8 |
| 75 | 279.6 | B2 | 3.4×10-10 | 6.7×10-11 | 2.0×10-10 | 1.9×10-3 | 1.8×10-3 | 5.0×10-7 | 6.8×10-7 | 3.2×10-8 |
| 76 | 280.8 | E | 4.0×10-12 | 1.7×10-12 | 1.2×10-11 | 1.3×10-4 | 1.2×10-2 | 2.7×10-9 | 1.4×10-8 | 6.3×10-8 |
| 77 | 280.8 | E | 2.9×10-29 | 1.3×10-12 | 2.0×10-14 | 6.0×10-4 | 1.2×10-2 | 4.3×10-10 | 9.1×10-10 | 2.2×10-10 |
| 78 | 281.9 | B1 | 2.0×10-11 | 9.2×10-11 | 6.2×10-10 | 1.1×10-3 | 1.0×10-3 | 1.9×10-7 | 3.6×10-7 | 8.7×10-8 |
| 79 | 284.0 | E | 3.4×10-12 | 8.6×10-13 | 9.4×10-12 | 1.9×10-4 | 1.2×10-2 | 3.4×10-9 | 1.8×10-8 | 8.6×10-8 |
| 80 | 284.0 | E | 1.3×10-13 | 4.6×10-14 | 5.1×10-13 | 2.5×10-4 | 1.1×10-2 | 4.6×10-1 | 9.5×10-10 | 8.8×10-11 |
| 81 | 313.0 | E | 7.3×10-13 | 7.3×10-13 | 4.1×10-13 | 1.2×10-3 | 4.2×10-3 | 1.6×10-9 | 1.5×10-9 | 1.9×10-8 |
| 82 | 313.0 | E | 2.0×10-12 | 6.2×10-13 | 1.4×10-11 | 6.8×10-4 | 4.5×10-3 | 1.3×10-9 | 2.7×10-8 | 8.7×10-8 |
| 83 | 316.5 | E | 3.3×10-13 | 4.6×10-12 | 6.2×10-13 | 1.7×10-3 | 4.0×10-3 | 4.3×10-10 | 1.8×10-9 | 1.1×10-8 |
| 84 | 316.5 | E | 1.8×10-12 | 5.0×10-27 | 5.6×10-12 | 7.7×10-4 | 3.2×10-3 | 2.5×10-9 | 3.2×10-8 | 1.2×10-7 |
| 85 | 329.2 | A1 | 2.8×10-7 | 2.8×10-7 | 2.5×10-6 | 3.3×10-2 | 3.8×10-3 | 1.1×10-9 | 1.3×10-8 | 5.2×10-8 |
| 86 | 329.8 | A2 | 3.1×10-7 | 3.1×10-7 | 2.8×10-6 | 3.3×10-2 | 4.2×10-3 | 2.1×10-9 | 1.6×10-9 | 2.7×10-8 |
| 87 | 394.5 | A2 | 1.3×10-6 | 1.3×10-6 | 1.6×10-5 | 1.2×10-2 | 1.0×10-2 | 1.4×10-9 | 2.9×10-9 | 2.1×10-8 |
| 88 | 396.8 | A1 | 1.2×10-6 | 1.2×10-6 | 1.4×10-5 | 1.1×10-2 | 9.7×10-3 | 3.1×10-9 | 8.5×10-9 | 4.9×10-8 |
| 89 | 398.8 | B2 | 9.9×10-12 | 1.6×10-10 | 1.8×10-10 | 8.0×10-5 | 2.5×10-4 | 2.8×10-11 | 2.5×10-8 | 6.1×10-8 |
| 90 | 399.8 | E | 3.7×10-12 | 5.1×10-15 | 3.4×10-11 | 3.1×10-4 | 4.0×10-3 | 8.9×10-9 | 2.5×10-8 | 2.0×10-7 |
| 91 | 399.8 | E | 6.2×10-13 | 2.0×10-14 | 1.7×10-12 | 6.4×10-4 | 3.7×10-3 | 3.3×10-10 | 4.5×10-10 | 5.9×10-9 |
| 92 | 400.8 | B1 | 2.5×10-13 | 1.2×10-10 | 2.7×10-10 | 2.4×10-4 | 2.5×10-4 | 6.2×10-9 | 3.8×10-8 | 3.4×10-8 |
| 93 | 401.8 | A1 | 6.3×10-7 | 6.3×10-7 | 7.8×10-6 | 1.1×10-2 | 7.2×10-3 | 6.9×10-10 | 9.9×10-10 | 1.0×10-8 |
| 94 | 402.2 | E | 6.2×10-13 | 2.0×10-14 | 8.6×10-13 | 5.9×10-5 | 1.8×10-3 | 3.9×10-10 | 6.4×10-10 | 8.0×10-9 |
| 95 | 402.2 | E | 2.3×10-11 | 1.3×10-12 | 1.3×10-10 | 1.2×10-4 | 3.2×10-3 | 4.3×10-9 | 2.5×10-8 | 1.4×10-7 |
| 96 | 405.5 | A2 | 4.9×10-7 | 4.9×10-7 | 6.0×10-6 | 9.1×10-3 | 6.2×10-3 | 3.2×10-9 | 5.8×10-9 | 5.6×10-8 |
| 97 | 407.2 | E | 2.4×10-11 | 6.7×10-11 | 3.9×10-10 | 3.5×10-4 | 1.1×10-2 | 1.8×10-9 | 4.5×10-9 | 3.3×10-8 |
| 98 | 407.2 | E | 2.0×10-14 | 4.6×10-14 | 1.3×10-12 | 1.8×10-4 | 1.1×10-2 | 2.4×10-10 | 2.2×10-11 | 6.0×10-12 |
| 99 | 407.5 | B1 | 3.4×10-12 | 1.9×10-11 | 9.3×10-11 | 7.0×10-5 | 0 | 4.8×10-8 | 1.4×10-7 | 5.6×10-8 |
| 100 | 407.8 | B2 | 3.2×10-12 | 2.0×10-11 | 7.7×10-11 | 4.8×10-4 | 5.0×10-4 | 4.8×10-8 | 1.4×10-7 | 6.3×10-8 |
| 101 | 413.0 | E | 5.6×10-12 | 5.2×10-11 | 1.7×10-10 | 1.1×10-4 | 1.0×10-2 | 2.4×10-9 | 4.3×10-9 | 3.8×10-8 |
| 102 | 413.0 | E | 8.6×10-13 | 1.8×10-13 | 4.9×10-12 | 1.9×10-4 | 1.0×10-2 | 2.6×10-11 | 1.2×10-10 | 4.6×10-10 |

Table 16. The first- and second-order SPC coefficients, Doop, and Average distance change of V-N bonds for each mode with its frequency and irreducible representation for (4). The modes indicated in Figure S32 are marked in bold red for the first-order and in bold blue for the second-order coefficients. Those not indicated in Figure S32 but showing relatively large values are also colored.

|  |  |  | First-order SPC |  |  |  |  | Second-order SPC |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| mode | freq | Sym | gx | gy | gz | Doop | avg V-N | gx | gy | gz |
| 4 | 3.6 | B | 8.2×10-14 | 2.0×10-14 | 1.8×10-13 | 8.5×10-2 | 2.3×10-3 | 4.8×10-7 | 4.7×10-7 | 2.8×10-9 |
| 5 | 22.5 | A | 5.5×10-9 | 5.5×10-9 | 4.8×10-8 | 1.6×10-2 | 2.0×10-3 | 7.0×10-11 | 2.7×10-12 | 1.5×10-11 |
| 6 | 36.0 | E | 1.3×10-11 | 1.5×10-11 | 4.9×10-12 | 5.1×10--3 | 5.0×10-4 | 4.6×10-10 | 2.9×10-10 | 2.5×10-10 |
| 7 | 36.0 | E | 4.0×10-11 | 2.3×10-11 | 2.4×10-11 | 5.5×10-3 | 7.5×10-4 | 2.3×10-10 | 1.4×10-10 | 6.6×10-10 |
| 8 | 47.4 | B | 8.5×10-11 | 3.4×10-11 | 1.1×10-11 | 7.1×10-2 | 5.0×10-4 | 2.0×10-7 | 5.5×10-8 | 6.3×10-9 |
| 9 | 51.8 | A | 3.1×10-11 | 3.0×10-11 | 4.9×10-9 | 9.9×10-3 | 5.0×10-4 | 6.9×10-9 | 5.1×10-9 | 2.0×10-12 |
| 10 | 69.2 | A | 1.7×10-10 | 1.7×10-10 | 1.7×10-9 | 1.9×10-2 | 5.0×10-4 | 1.7×10-10 | 1.3×10-11 | 2.0×10-9 |
| 11 | 69.8 | E | 3.2×10-11 | 3.7×10-12 | 5.2×10-12 | 7.4×10-4 | 5.0×10-4 | 1.6×10-9 | 2.0×10-12 | 1.7×10-10 |
| 12 | 69.8 | E | 1.3×10-12 | 8.8×10-11 | 9.4×10-11 | 9.8×10-4 | 1.0×10-3 | 7.3×10-10 | 7.5×10-9 | 7.2×10-9 |
| 13 | 81.3 | B | 1.8×10-13 | 6.6×10-12 | 2.2×10-12 | 1.5×10-2 | 2.5×10-3 | 1.6×10-8 | 2.6×10-8 | 9.2×10-11 |
| 14 | 87.1 | E | 3.4×10-12 | 1.7×10-12 | 1.3×10-13 | 2.3×10-3 | 1.0×10-3 | 3.5×10-10 | 5.4×10-11 | 7.4×10-10 |
| 15 | 87.1 | E | 1.3×10-10 | 8.0×10-11 | 7.4×10-12 | 2.7×10-3 | 1.2×10-3 | 3.9×10-9 | 5.0×10-9 | 2.9×10-10 |
| 16 | 88.4 | B | 1.3×10-13 | 1.5×10-12 | 1.8×10-12 | 4.7×10-2 | 2.5×10-4 | 2.6×10-7 | 2.1×10-7 | 1.8×10-9 |
| 17 | 100.0 | B | 4.6×10-11 | 9.0×10-11 | 3.0×10-11 | 6.9×10-2 | 2.5×10-4 | 1.3×10-7 | 1.1×10-7 | 1.1×10-9 |
| 18 | 105.1 | E | 4.1×10-13 | 1.2×10-11 | 1.0×10-12 | 4.4×10-4 | 1.5×10-3 | 1.6×10-9 | 2.4×10-10 | 4.9×10-10 |
| 19 | 105.1 | E | 8.2×10-12 | 1.2×10-11 | 1.8×10-11 | 3.9×10-4 | 1.2×10-3 | 1.1×10-11 | 3.5×10-10 | 6.4×10-10 |
| 20 | 111.3 | A | 4.0×10-9 | 4.0×10-9 | 5.7×10-8 | 4.5×10-2 | 1.7×10-3 | 1.3×10-9 | 6.1×10-10 | 5.1×10-11 |
| 21 | 120.5 | A | 6.4×10-9 | 6.4×10-9 | 1.2×10-7 | 8.1×10-2 | 2.0×10-3 | 7.0×10-12 | 2.4×10-11 | 2.7×10-9 |
| 22 | 126.8 | B | 4.6×10-14 | 1.7×10-12 | 1.8×10-13 | 7.6×10-4 | 2.5×10-4 | 2.4×10-6 | 2.5×10-6 | 2.0×10-10 |
| 23 | 132.9 | E | 1.8×10-11 | 1.3×10-13 | 1.4×10-11 | 4.9×10-2 | 1.5×10-3 | 5.6×10-10 | 1.0×10-12 | 4.9×10-9 |
| 24 | 132.9 | E | 5.4×10-10 | 3.1×10-10 | 8.5×10-11 | 4.9×10-2 | 1.7×10-3 | 8.0×10-9 | 1.5×10-8 | 4.0×10-9 |
| 25 | 161.7 | E | 3.7×10-12 | 8.6×10-12 | 2.5×10-13 | 1.1×10-2 | 5.5×10-3 | 1.1×10-8 | 8.0×10-9 | 2.3×10-9 |
| 26 | 161.7 | E | 1.8×10-13 | 2.0×10-14 | 7.4×10-12 | 1.2×10-2 | 5.7×10-3 | 8.1×10-9 | 7.8×10-9 | 2.6×10-9 |
| 27 | 198.5 | A | 1.3×10-8 | 1.3×10-8 | 4.5×10-9 | 3.2×10-2 | 1.7×10-3 | 1.3×10-10 | 6.0×10-12 | 2.1×10-10 |
| 28 | 207.0 | A | 1.9×10-10 | 1.9×10-10 | 2.7×10-7 | 2.4×10-2 | 3.3×10-3 | 1.2×10-11 | 1.4×10-10 | 3.4×10-12 |
| 29 | 209.3 | B | 8.2×10-14 | 7.0×10-12 | 3.3×10-13 | 2.3×10-2 | 1.2×10-2 | 7.3×10-7 | 7.8×10-7 | 3.1×10-9 |
| 30 | 217.6 | E | 5.1×10-13 | 2.3×10-11 | 4.6×10-12 | 1.0×10-4 | 1.0×10-3 | 2.4×10-9 | 1.6×10-9 | 1.8×10-9 |
| 31 | 217.6 | E | 3.9×10-11 | 1.0×10-12 | 3.4×10-11 | 3.7×10-4 | 2.0×10-3 | 1.7×10-10 | 2.9×10-10 | 4.9×10-10 |
| 32 | 234.8 | E | 2.0×10-14 | 8.2×10-14 | 2.3×10-12 | 1.1×10-2 | 2.8×10-3 | 5.4×10-11 | 2.8×10-11 | 1.6×10-9 |
| 33 | 234.8 | E | 6.6×10-12 | 9.4×10-11 | 1.7×10-11 | 1.1×10-2 | 3.8×10-3 | 3.3×10-11 | 1.5×10-9 | 4.4×1010 |
| 34 | 239.6 | B | 2.2×10-12 | 6.6×10-12 | 5.1×10-13 | 3.0×10-4 | 2.5×10-4 | 2.3×10-9 | 2.9×10-9 | 2.4×10-9 |
| 35 | 264.9 | E | 8.6×10-13 | 1.1×10-12 | 8.2×10-14 | 2.0×10-2 | 9.8×10-3 | 7.4×1010 | 1.9×10-9 | 3.7×10-9 |
| 36 | 264.9 | E | 8.2×10-12 | 7.8×10-12 | 4.6×10-12 | 2.0×10-2 | 9.0×10-3 | 3.3×10-9 | 5.1×10-11 | 5.0×10-10 |
| 37 | 276.4 | A | 2.0×10-8 | 2.0×10-8 | 4.8×10-7 | 1.1×10-2 | 3.0×10-3 | 5.4×10-11 | 3.4×1010 | 1.0×10-9 |
| 38 | 276.5 | B | 3.5×10-11 | 5.0×10-11 | 1.5×10-11 | 2.6×10-2 | 1.7×10-2 | 2.0×10-8 | 5.9×10-9 | 3.6×10-9 |
| 39 | 277.1 | A | 1.3×10-8 | 1.3×10-8 | 4.2×10-7 | 5.6×10-3 | 2.8×10-3 | 4.2×10-12 | 7.0×10-11 | 3.8×1010 |
| 40 | 281.3 | A | 1.1×10-8 | 1.1×10-8 | 4.6×10-7 | 1.5×10-2 | 3.0×10-3 | 1.7×1010 | 3.3×10-11 | 1.8×10-9 |
| 41 | 308.6 | E | 2.7×10-11 | 4.3×10-12 | 1.8×1013 | 2.7×10-2 | 2.8×10-3 | 1.9×1010 | 4.2×1010 | 2.7×10-12 |
| 42 | 308.6 | E | 1.3×10-11 | 5.1×10-13 | 1.1×10-12 | 2.6×10-2 | 2.5×10-3 | 8.1×10-11 | 2.4×10-11 | 3.7×10-13 |
| 43 | 332.6 | E | 2.1×10-11 | 1.2×10-11 | 4.1×1011 | 4.9×10-4 | 1.7×10-2 | 5.6×10-9 | 4.2×10-12 | 4.0×10-8 |
| 44 | 332.6 | E | 2.6×10-11 | 2.8×10-11 | 2.0×10-12 | 1.8×10-4 | 1.7×10-2 | 8.4×10-9 | 2.8×10-11 | 3.4×10-8 |
| 45 | 336.5 | B | 3.7×10-12 | 1.0×10-20 | 2.9×10-12 | 2.3×10-2 | 7.5×10-4 | 1.3×10-7 | 2.6×10-7 | 4.7×10-10 |
| 46 | 389.7 | B | 7.8×10-12 | 1.7×10-12 | 1.7×10-12 | 6.2×10-5 | 5.0×10-4 | 1.4×10-9 | 3.2×10-9 | 5.0×10-10 |
| 47 | 390.3 | A | 4.9×10-9 | 5.0×10-9 | 5.2×10-7 | 1.8×10-3 | 7.0×10-3 | 3.4×10-12 | 6.7×10-11 | 2.3×10-10 |
| 48 | 396.3 | E | 1.6×10-11 | 1.8×10-11 | 7.8×10-12 | 7.7×10-4 | 1.0×10-3 | 4.8×10-11 | 1.0×10-12 | 7.6×10-10 |
| 49 | 396.3 | E | 1.7×10-12 | 1.7×10-12 | 2.0×10-12 | 7.9×10-4 | 5.0×10-4 | 8.1×10-11 | 1.7×10-11 | 1.6×10-10 |
| 50 | 396.6 | A | 4.7×10-8 | 4.7×10-8 | 3.0×10-6 | 9.1×10-3 | 1.7×10-2 | 1.1×10-10 | 5.0×10-12 | 2.2×10-9 |
| 51 | 404.1 | E | 1.9×10-11 | 5.9×10-12 | 1.3×1013 | 3.1×10-4 | 1.8×10-2 | 5.0×10-12 | 1.1×10-9 | 4.5×10-9 |
| 52 | 404.1 | E | 1.3×10-11 | 2.5×10-12 | 1.7×10-12 | 4.5×10-4 | 1.8×10-2 | 2.1×10-10 | 5.6×10-10 | 6.5×10-9 |
| 53 | 404.7 | B | 3.4×10-12 | 1.8×10-13 | 2.5×10-13 | 8.3×10-4 | 5.0×10-4 | 2.7×10-6 | 2.7×10-6 | 1.2×10-9 |

References

1. A. Urtizberea, E. Natividad, P. J. Alonso, L. Pérez-Martínez, M. A. Andrés, I. Gascón, I. Gimeno, F. Luis and O. Roubeau, Mater. Horizons, 2019, 7, 885–897.

2. T. Yamabayashi, M. Atzori, L. Tesi, G. Cosquer, F. Santanni, M.-E. Boulon, E. Morra, S. Benci, R. Torre, M. Chiesa, L. Sorace, R. Sessoli and M. Yamashita, J. Am. Chem. Soc., 2018, 140, 12090–12101.

3. A. Urtizberea, E. Natividad, P. J. Alonso, M. A. Andrés, I. Gascón, M. Goldmann and O. Roubeau, Adv. Funct. Mater., 2018, 28, 1801695.

4. N. P. Kazmierczak, N. E. Lopez, K. M. Luedecke and R. G. Hadt, Chem. Sci., 2024, 15, 2380–2390.

5. Y. Horii, M. Makino, T. Yamamoto, S. Tatsumi, H. Suzuki, M. Noguchi, T. Yoshida, T. Kajiwara, Z.-Y. Li and M. Yamashita, Inorg. Chem. Front., 2022, 9, 6271–6278.

6. N. P. Kazmierczak, R. Mirzoyan and R. G. Hadt, J. Am. Chem. Soc., 2021, 143, 17305–17315.

7. A. Albino, S. Benci, L. Tesi, M. Atzori, R. Torre, S. Sanvito, R. Sessoli and A. Lunghi, Inorg. Chem., 2019, 58, 10260–10268.

8. P. C. Bruzzese, Y.-K. Liao, L. Donà, B. Civalleri, E. Salvadori and M. Chiesa, J. Phys. Chem. Lett., 2024, 15, 7161–7167.

9. R. Mirzoyan, N. P. Kazmierczak and R. G. Hadt, Chem. Euro. J., 2021, 27, 9482–9494.

10. M. J. Amdur, K. R. Mullin, M. J. Waters, D. Puggioni, M. K. Wojnar, M. Gu, L. Sun, P. H. Oyala, J. M. Rondinelli and D. E. Freedman, Chem. Sci., 2022, 13, 7034–7045.

11. A. Lunghi and S. Sanvito, Sci. Adv., 2019, 5, eaax7163.

12. F. Santanni, A. Albino, M. Atzori, D. Ranieri, E. Salvadori, M. Chiesa, A. Lunghi, A. Bencini, L. Sorace, F. Totti and R. Sessoli, Inorg. Chem., 2021, 60, 140–151.

13. E. B. Fleischer, J. Am. Chem. Soc., 1963, 85, 1353–1354.

14. M. G. B. Drew, P. C. H. Mitchell and C. E. Scott, Inorg. Chim. Acta, 1984, 82, 63–68.

15. S. S. Eaton, T. Yamabayashi, Y. Horii, M. Yamashita and G. R. Eaton, J. Am. Chem. Soc., 2025, 147, 13815–13823.