Utilization of Cadmium Sulfide/Nickel-Ferric Layered Double Hydroxide Nanocomposite Decorated with Silver Nanoparticles for Efficient Adsorption and Photocatalytic Degradation of 2,4-Dichlorophenoxyacetic Acid

Walaa A. Shaltout*1, Asaad F. Hassan2, Maha S. Elsayed3, H. Hafez4

1Survey of Natural Resources Department, Environmental Studies and Research Institute, University of Sadat City, Egypt.

2Chemistry Department, Faculty of Science, Damanhour University, Damanhour 22511, Egypt

3Central Laboratory of Date Palm Research and Development, Agricultural Research Center, Giza 12619, Egypt

4Nanotechnology Department, Environmental Studies and Research Institute, University of Sadat City, Sadat City, Minufiya 32897, Egypt

Corresponding authors: Walaa A. Shaltout (walaa.abdelaal@esri.usc.edu.eg)

1. Mechanism of 2,4-D adsorption onto Ag@CNFL:

Based on the described findings, the possible 2,4-D adsorption mechanism onto Ag@CNFL was projected using characterization and adsorption data as shown graphically in Fig. S1. The electrostatic interaction between the positively charged functional groups (Ni2+, Fe3-, and Cd2+) present in Ag@CNFL and –COO- from 2,4-D moieties was enhanced in the adsorption tests by using a lower pH of 2. The pore-filling action was facilitated by the presence of adsorbent pores. Adsorption was facilitated through interactions such as π-π stacking between the benzene rings and –OH of Ag@CNFL, hydrogen bonding between –OH in each other, chlorine bonding (donor-acceptor interaction) between –OH of Ag@CNFL and chlorine atoms in 2,4-D, and van der Waals force with 2,4-D molecules. In conclusion, the physical adsorption mechanism showed the strong capacity of Ag@CNFL for the removal of 2,4-D from aqueous solution. Similar kinds of mechanisms have been stated for the 2,4-D removal by many adsorbents such as biochar prepared from Vateria indica fruit biomass 1,  biomass derived magnetic activated carbon nanocomposite 2,  nitrogen doped modified palm kernel shell 3, and Fe–Zr-based metal-organic frameworks 4.

Fig. S1. Mechanism of 2,4-D adsorption onto Ag@CNFL.

2. Mechanism of 2,4-D photodegradation onto Ag@CNFL:

An accurate explanation for the increased 2,4-D photodegradation mechanism by the ternary heterogeneous Ag@CdS/Ni-Fe LDH nanocomposite (Ag@CNFL) has been proposed and schematically depicted in Fig. S3 upon the photocatalyst performance. Visible light excited Ag@CdS/Ni-Fe LDH heterojunction, causing CdS and Ni-Fe LDH to produce electrons in the conduction bands (CB), where h+ and e- were separated. By simultaneously activating CdS and Ni-Fe LDH, the charge separation was enhanced, and the charge recombination was inhibited 5. The adsorbed O2 onto the catalyst surface can be converted into ●O2- by the CB of NFL and CdS, and H2O/OH- may be converted into ●OH by the photogenerated holes in their valence bands (VBs). In the meantime, the Ag nanoparticles quickly absorbed photogenerated electrons from the CB of CdS by acting as an electron sink because of their strong Schottky barriers at the metal-semiconductor interface. It was also possible for the enhanced electrons on the metallic Ag surface to be transferred to the CB of CdS and supported in the oxidation process. This process is known as the SPR effect for Ag metal nanoparticles. Because Ag nanoparticles are visible-photosensitive, their surface electron transfer increased the effectiveness of the photocatalyst reaction 6. On the other hand, the Ag doping made the bandgap narrow in the band catalyst structure and improved the optical absorption capacity. Finally, the produced superoxide and hydroxyl radicals oxidized 2,4-D into CO2 and H2O 7. This mechanism aligned with those of related studies  6,8–10.

Fig. S2: Photocatalyst reusability for the studied photocatalysts.

Fig. S3. Mechanism of 2,4-D photodegradation onto Ag@CNFL.

| Name | Abbreviation |
| --- | --- |
| Layered double hydroxide | LDH |
| Zn-Fe LDH | ZFL |
| Mg-Fe LDH | MFL |
| Ni-Fe LDH | NFL |
| Cadmium sulfide | C |
| Cadmium sulfide/Ni-Fe LDH | CNFL |
| Ag@CdS/Ni-Fe LDH | Ag@CNFL |
| 2,4-dichlorophenoxyacetic acid | 2,4-D |
| Surface plasmon resonance | SPR |
| Thermogravimetric analysis | TGA |
| X-ray diffraction | XRD |
| Point of zero charge | pHPZC |
| Diffuse reflectance spectroscopy | DRS |
| Scanning electron microscopy | SEM |
| Transmission electron microscopy | TEM |
| Pseudo-first-order | PFO |
| Pseudo-second-order | PSO |
| Dubinin-Radushkevich | DR |
| Langmuir-Hinshelwood | L-H |

Table S1: Some abbreviations.

Table S2: Comparison of the maximum efficiency of 2,4-D removal onto NFL and Ag@CNFL with other materials. (Note: g/L and mg/L units refer to sample dosage and 2,4-D concentration, respectively).

| Materials | Available conditions |  | Technique | Capacity | References |
| --- | --- | --- | --- | --- | --- |
| PT-1 |  | pH 5, 0.5 g/L, 30 oC, 0.5 h | Adsorption | 19.10 mg/g | 2 |
| CPAC@Fe3O4 |  | pH 2, 0.2 g/L, 30 oC, 1.5 h | Adsorption | 160.71 mg/g | 3 |
| UiO-66-NH2 |  | pH 3, 0.2 g/L, 25 oC, 12 h | Adsorption | 72.99 mg/g | 5 |
| Fe3O4/algal |  | pH 2, 1.0 g/L, 30 oC, 1.5 h | Adsorption | 21.34 mg/g | 6 |
| MIPs |  | 25 oC, ≈ 5 h | Adsorption | 123.44 mg/g | 7 |
| VI-BC |  | pH 2, 0.3 g/L, 30 oC, 2 h | Adsorption | 131.39 mg/g | 54 |
| Biomixture |  | pH ≈ 6 | Adsorption | 155.7 mg/g | 55 |
| GO-Fe3O4 |  | pH 3 | Adsorption | 67.26 mg/g | 58 |
| UPAC-Fe2O3 |  | pH 2, 2.2 g/L, 30 oC, 0.5 h | Adsorption | 60.61 mg/g | 59 |
| TiO2/BiOBr/ Bi2S3/AC |  | pH 3, 0.6 g/L, 25 oC, ≈ 6 h | Adsorption | 87.61 mg/g | 64 |
| GA3 |  | pH 7, 2.0 g/L, 25 oC, 6 h | Adsorption | 150.4 mg/g | 65 |
| NFL |  | pH 2, 2.4 g/L, 23 oC, 14 h | Adsorption | 203.75 mg/g | [This work] |
| PT-1 |  | pH 5, 10 mg/L, 0.5 g/L | Photodegradation | 99.9% | 2 |
| Magnetite/UV |  | pH= 6, 50 mg/L, 25 oC, 135 min | Photodegradation | ~65.7% | 12 |
| TiO2/BiOBr/ Bi2S3/AC |  | pH =3, 90 mg/L, 0.6 g/L, 90 min | Photodegradation | 98.0% | 64 |
| Calcined LDH |  | pH ≈ 3, 320.5 mg/L, 1.0 g/L, 9 h | Photodegradation | 97.0% | 66 |
| Ag@CNFL |  | pH 3.2, 15 mg/L, 1.0 g/L, 20 oC, 110 min | Photodegradation | 100.0% | [This work] |

References

1	R. Vinayagam, V. Nagendran, L. C. Goveas, M. K. Narasimhan, T. Varadavenkatesan, A. Samanth and R. Selvaraj, Chemosphere, 2024, 350, 141130.

2	A. Samanth, R. Selvaraj, G. Murugesan, T. Varadavenkatesan and R. Vinayagam, Chemosphere, 2024, 361, 142513.

3	H. Mohamed Flafel, M. Rafatullah, J. Lalung, R. Thapar Kapoor, M. Raza Siddiqui and M. Qutob, J. Mol. Liq., 2024, 401, 124754.

4	B. Liu, N. Guo, Z. Wang, Y. Wang, X. Hao, Z. Yang and Q. Yang, J. Environ. Chem. Eng., 2022, 10, 107472.

5	P. R. Lestari, T. Takei and N. Kumada, J. Solid State Chem., 2021, 294, 121858.

6	L. Tabana, D. R. Booysens and S. Tichapondwa, J. Photochem. Photobiol. A Chem., 2023, 444, 114997.

7	L. Bi, G. Fu, D. Cai, J. Shen, J. Zhang, J. Kang, Y. Cheng, P. Yan, Y. Zhou and Z. Chen, Sep. Purif. Technol., 2023, 306, 122562.

8	T. O. Ajiboye, E. E. Imade, O. A. Oyewo and D. C. Onwudiwe, J. Photochem. Photobiol. A Chem., 2022, 432, 114107.

9	R. Fazaeli, H. Aliyan, D. Richeson and Y. Li, J. Environ. Sci. (China), 2025, 148, 437–450.

10	H. huan Chen, S. hua Luo, X. fei Lei, H. Liu, Y. ying Liu, X. yu Xu, Z. hua Jiang and X. dong Li, Ionics (Kiel)., 2020, 26, 5829–5839.