Electronic Supporting Information

Periodic mesoporous organosilica functionalized with p-aminobenzenesulfonic acid: efficient solid acid catalyst for one-pot synthesis of 5-substituted 1H-tetrazoles under eco-friendly conditions

Hamidreza Fanimoghadama, Mohammad G. Dekamina,* M. Reza Naimi-Jamala

aPharmaceutical and Heterocyclic Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran, 16846-13114, Iran.E-mail: mdekamin@iust.ac.ir

| Contents | page |
| --- | --- |
| General procedure for the preparation of PABSA-(3-chloropropyl)trimethoxysilane precursor | 3 |
| FT-IR spectrum of the commercial PABSA-silyl precursor (I). | 3 |
| 1H NMR spectrum of PABSA-silyl precursor (I). | 4 |
| 13C NMR spectrum of PABSA-silyl precursor (I). | 4 |
| Schematic description for the synthesis of PABSA-Pr-PMO nanocatalyst (1) | 5 |
| FT-IR spectra of the commercial (a) CPTMS-PABSA and (b) PABSA-Pr-PMO nanocatalyst (1) | 6 |
| FESEM images of the PABSA-Pr-PMO nanocatalyst (1) | 7 |
| TGA and DTA analysis of the PABSA-Pr-PMO nanocatalyst (1) | 8 |
| The EDX of the PABSA-Pr-PMO nanocatalyst (1) | 9 |
| Elemental mapping of the PABSA-Pr-PMO nanocatalyst (1) | 9 |
| X-ray powder diffraction (XRD) pattern of the periodic mesoporous organosilica (a) low angle PABSA-Pr-PMO nanomaterial (1). (b) Wide angle PABSA-Pr-PMO nanomaterial (1) | 10 |
| Nitrogen adsorption–desorption (A) and BJH (pore size distribution, B) isotherms of the PABSA-Pr-PMO nanocatalyst (1) | 11 |
| Reusability data for the PABSA-Pr-PMO nanocatalyst (1) in the synthesis of 5a | 12 |
| FT-IR spectra of fresh and recovered PABSA-Pr-PMO nanocatalyst (1) after fifth run | 13 |
| FT-IR spectrum of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a) | 14 |
| 1H-NMR of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a) | 14 |
| 13C NMR of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a) | 15 |
| FT-IR spectrum of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile(5k) | 16 |
| 1H-NMR of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5k) | 16 |
| 13C NMR of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5k) | 17 |
| FT-IR spectrum of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n) | 18 |
| 1H-NMR of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n) | 18 |
| 13C NMR of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n) | 19 |
| FT-IR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l) | 20 |
| 1H NMR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l) | 20 |
| 13C NMR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l) | 21 |

General procedure for the preparation of PABSA-(3-chloropropyl)trimethoxysilane precursor

In this step (3-chloropropyl)trimethoxysilane (CPTMS, 1.04 ml, 1.09 g/ml) was reacted dropwise with p-aminobenzenesulfonic acid (PABSA, 1 g, 5.7 mmol)  in a molar ratio of 1:1 in refluxing dry toluene (30 ml). Then, dry triethylamine was added to the reaction mixture with a molar ratio of 1.2 (0.95 ml, 0.7255 g/ml). The reaction was carried out under a nitrogen atmosphere for 24 h to obtain a white gel. The solvent was then removed by rotary evaporation and the residue dried. The product was washed sequentially with hexane, diethyl ether, and dry EtOH, then dried for 24 h. A white powder, the PABSA-silyl precursor (I), was obtained in 95 % yield.52 The PABSA-silyl precursor (I) was characterized through 1H and 13C NMR spectroscopy.

FT-IR (KBr, ν, cm−1) ν: 3420 (O-H), 3335 (N-H), 1400-1600 (C=C), 1389, 1154, 1111, 697 cm-1;  1H NMR (500 MHz, DMSO-d6): δ (ppm) 9.19 (s, 1H, OH), 7.20 (d, J = 8.2 Hz, 2H), 6.46 (d, J = 8.2 Hz, 2H), 5.30 (s, 1H, NH), 3.61 (s, 9H, -OMe), 3.03 (q, J = 7.2 Hz, 2H, -NH-CH2-), 1.13 (m, 2H, -CH2-), 0.84 (t, J = 7.2 Hz, 2H, Si-CH2-). 13C NMR (125 MHz, DMSO-d6) δ (ppm) 149.18, 135.32, 126.65, 112.32, 46.68, 42.66, 34.87, 8.55.

Fig. 1 FT-IR spectrum of the PABSA-silyl precursor (I).

Fig. 2 1H NMR spectrum of PABSA-silyl precursor (I).

Fig. 3 13C NMR spectrum of PABSA-silyl precursor (I).

Scheme 1 Schematic description for the synthesis of PABSA-Pr-PMO nanocatalyst (1).

Fig. 4 FT-IR spectra of the (a) CPTMS-PABSA and (b) PABSA-Pr-PMO nanocatalyst (1).

| A A | B |
| --- | --- |
| C | Length: 52.525 nm Length: 49.192 nm Length: 35.321 nm Length: 63.259 nm D |

Fig. 5 FESEM images of the PABSA-Pr-PMO nanocatalyst (1)

a b

Fig. 6 a) TGA and b) DTA analysis of the PABSA-Pr-PMO nanocatalyst (1).

Elt; W%; A%. C; 20.01; 25.69. N; 5.68; 6.62. O; 49.07; 50.15. Si; 20.23; 12.74. S; 5.01; 4.80. Total; 100%; 100%. Counts

Fig. 7 The EDX of the PABSA-Pr-PMO nanocatalyst (1).

Si

SOI

O

C

N

Fig. 8 Elemental mapping of the PABSA-Pr-PMO nanocatalyst (1).

a

b

Fig. 9 X-Ray powder diffraction (XRD) pattern of the periodic mesoporous organosilica (a) low angle PABSA-Pr-PMO nanomaterial (1) and (b) Wide angle PABSA-Pr-PMO nanomaterial (1).

A

B

Fig. 10 (A) Nitrogen adsorption–desorption and BJH (pore size distribution, B) isotherms of the PABSA-Pr-PMO nanocatalyst (1(.

Fig. 11 Reusability data for the PABSA-Pr-PMO nanocatalyst (1) in the synthesis of 5a.

Fig. 12 FT-IR spectra of (a) fresh and (b) recovered PABSA-Pr-PMO nanocatalyst (1) after fifth run.

Fig. 13 FT-IR spectrum of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a).

Fig. 14 1H NMR of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a).

Fig. 15 13C NMR of (E)-3-(4-chlorophenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5a).

Fig. 16 FT-IR spectrum of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5k).

Fig. 17 1H NMR of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5k).

Fig. 18 13C NMR of (E)-3-(4-hydroxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5k).

Fig. 19 FT-IR spectrum of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n).

Fig. 20 1H NMR of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n).

Fig. 21 13C NMR of (E)-3-(3,4-methoxyphenyl)-2-(1H-tetrazole-5-yl) acrylonitrile (5n).

CO2

CO2

CO2

Fig. 22 FTIR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l).

Fig. 23 1H NMR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l).

Fig. 24 13C NMR spectra of (E)-3‑(4‑methoxyphenyl)‑2‑(1H‑tetrazole‑5‑yl)acrylonitrile (5l).

References

1.	M. Sudharsan, S. Subramanian, A. J. Amali and D. Suresh, ChemistrySelect, 2020, 5, 6131-6140.