Supporting Information

# High-Temperature Solid-State Synthesis of Nb2SiTe4 Nanosheets and Their Photoelectric Performance in Broadband Self-Powered Photodetectors

Chengzheng Ye1,†, Jiaming Song1,†, *, Xin Zhao2, Zijuan Ma1, Jialong Ma1, Yawen Liu1, Shanbo Cui1, Zhuo Wang1, Guoshuai Ban1, Feng Teng1, Peng Hu1, Haibo Fan1

1. School of Physics, Northwest University, Xi’an 710127, China

2. School of Optoelectronic Engineering, Xi'an Technological University, Xi’an 710021, China

†: Chengzheng Ye and Jiaming Song contributed equally

*: Corresponding author: jiaming.song@nwu.edu.cn

| P (mW cm-2) Wavelength (nm) | Ⅰ | Ⅱ | Ⅲ |
| --- | --- | --- | --- |
| 400 nm | 58.10 | 85.50 | 114.00 |
| 520 nm | 69.30 | 101.00 | 126.00 |
| 600 nm | 59.10 | 87.50 | 109.00 |
| 700 nm | 49.30 | 72.40 | 90.40 |
| 800 nm | 31.50 | 46.50 | 57.80 |
| 900 nm | 32.20 | 46.30 | 57.50 |

Table S1 Light intensity values for different wavelengths and power density levels

Figure S1 XRD patterns of Nb2SiTe4 bulk and nanosheets exfoliated using different dispersants.

Figure S2 EDS analysis of Nb2SiTe4.

Table S2 Quantitative EDS analysis for element proportions in bulk Nb2SiTe4.

| Element Line | Weight % | Weight % Error | Atom % | Atom % Error |
| --- | --- | --- | --- | --- |
| C K | 30.62 | ± 0.21 | 61.82 | ± 0.42 |
| O K | 17.33 | ± 0.24 | 26.28 | ± 0.36 |
| Si K | 1.74 | ± 0.11 | 1.50 | ± 0.09 |
| Nb L | 11.81 | ± 0.44 | 3.08 | ± 0.12 |
| Te L | 38.50 | ± 1.74 | 7.32 | ± 0.33 |
| Total | 100.00 |  | 100.00 |  |

Figure S3 Transient photocurrent of NS-NMP, NS-AE, NS-IPA and NS-SC PDs in electrolyte of 0.10 M HCl at 0 V (400 nm light source, level-I light intensity).

Figure S4 (a) Thickness distribution histograms of NST nanosheets exfoliated by different dispersants and (b-e) the corresponding surface morphologies characterized by white light interferometry.

Figure S5 (a-d) AFM morphology images and the corresponding (e-h) line profiles for NS-NMP, NS-SC, NS-IPA and NS-AE, respectively.

Figure S6 Mott-Schottky test of NS-NMP.