Supporting Information for

Non-covalent Interaction of Hydroxyl Capped Layered Double Hydroxide Oligomers for Highly Performing Phosphorus Recovery

Yuchi Chen a, b.*, Guangyu Zhu a, Bo Zuo a, Junxia Yu a, Qingbai Chen b.**

a Key Laboratory for Green Chemical Process of Ministry of Education, School of Chemistry and Environmental Engineering, Wuhan Institute of Technology, Wuhan 430074, PR China

b Center for Water and Ecology, State Key Joint Laboratory of Environment Simulation and Pollution Control, School of Environment, Tsinghua University, Beijing 100084, China

Correspondence and requests for materials should be addressed to Yuchi Chen. (E-mail: cycglacier@163.com)

Contents

S1. Supplemental Materials and Experiments

S2. Supplemental Results and Discussions

19 pages, 18 figures, 3 tables, and 11 equations

S1. Supplemental Materials and Experiments

- CALOx and ordinary Ca/Al-LDH synthesis

For CALOx. 2.22 g of anhydrous CaCl2, 1.21 g of AlCl3·6H2O and 2.4 g of NaOH were dissolved in 100 mL absolute ethanol (< 99.5% ωt) respectively. With continuously stirring, of AlCl3/ethanol (solution B) was stabilized by adding 1.03 mL of acetylacetone. After ultrasonic dispersed, both A (CaCl2/ethanol) and B were stirred for another 1 hour with hermetic condition (by sealing rubber). Solution A was slowly drop into solution B with a rate of 1 drop/s (continuously stirring). Then, different portion of TEA (0 mL, 4.17 mL, 20.85 mL, 41.70 mL, 83.40 mL) was injected into mixed solution by using barrel syringes (avoiding precipitation). The obtained colloidal sols (A, B and TEA) were ultrasonic dispersed for 30 min and stirred for another 1 hours to completely hydrolyze (crystal water come from AlCl3·6H2O). The NaOH/ethanol (solution C) was slowly added into the colloidal sols to intrigue the crystal growth of LDH oligomers and stirred for 6 hours. The suspension liquids then were heated in water-bath with the temperature of 60 °C to evaporate the excessive solvent (ethanol) until the liquid began to congeal. The maturely synthesized LDH oligomers would be collected after 1 days’ ageing from colloidal gel (Figure S5 right).

For ordinary Ca/Al-LDH. 2.22 g of anhydrous CaCl2 and 1.21 g of AlCl3·6H2O were co-dissolved in 200 mL deionized water thoroughly. Prepared a NaOH with the concentration of 0.1 mol L-1 to adjust the pH of mixed aqueous solution at pH≈10. The whole process should be continuously stirred (~6 hours) and the precipitation (ordinary LDH) would be collected after centrifuge and dried.

- Method of Selectivity Determination

The selectivity test was conducted with a solution (P: 5 mg L-1, sulfate: 250 mg L-1, carbonate: 250 mg L-1 and Humus acid: 5 mg L-1) of diverse anions. The concentration was measured after P uptake. The selectivity towards P of CALOx and ordinary Ca/Al-LDH was determined through the calculation of the distribution coefficient Kd (L g-1), which refers to the ratio of an element’s concentration in the sorbent to that in the solution phase after reaction equilibrium, and it can be calculated as:

Kd=(C0-Ce)×VCe×m                                              (S1)

Where,

C0 and Ce, initial and equilibrium phosphate concentration (mg/L);

V, total solution volume (L);

m, dosage of the of adsorbent (g/L).

- Analyses of the P uptake data

The uptake efficiency and adsorption capacity (Qt) of P were calculated as (Eq. S2):

Qt=(C0-Ct)×Vm                                               (S2)

Where,

C0 and Ct, initial and momentary phosphate concentration (mg/L);

V, total solution volume (L);

m, dosage of the of adsorbent (g/L).

Nonlinear Langmuir (Eq. S3) and Freundlich models (Eq. S4) were fitted to depict the isotherms of Phosphate adsorption. The fitted equations are as follows:

Ceqe=CeQm+1QmKL                                     (S3)

where,

Ce, equilibrium concentration of P (mg/L);

qe, P uptake amount at equilibrium (mg/g);

Qm, maximum P uptake capacity (mg/g);

KL, Langmuir affinity coefficient (L/mg).

qe=KfCen                                         (S4)

where,

Kf, Freundlich affinity coefficient (mg/g);

N, Freundlich exponential coefficient.

- Digestion process and P desorption calculation.

The digestion process was improved referring to ASTM D1971-16(2021) and EPA method 3050B. Specifically:

Digestion for liquid. After filtration, the obtained aqueous solution (~50 mL) was mixed with washing liquor (~5 ml) and ethanol (~50 mL) were digested by adding 20 mL of concentrated nitric acid (~65 wt%). Then, boiled for 5 min, the two clear aqueous solution was constant volumed to 200 mL by DI water for desorbed P test.

Digestion for LDHs. After separated, 1g of sorbents loaded with P were digested by adding 2.5 mL of concentrated nitric acid (~65 wt%) and 10 mL concentrated hydrochloric acid. After sealed and boiled for 15 min, the solution was collected and the residues was washed by 20 mL DI water. Then the solutions were mixed and stored for total P test.

Desorption ratio of P. The desorption ratio of P is calculated as (Eq. S5).

η=(Ca+Ce)×VQLm×100%                                (S5)

where,

Ca, concentration of P in aqueous solution of digested liquid (mg/L);

Ce, concentration of P in ethanol of digested liquid (mg/L)

V, volume of total solution consumption (0.2 L);

QL, total absorbed P in LDH (mg/g);

m, original dosage of sorbents (g).

- Ionic Equilibriums and Thermodynamic Stability

The equilibrium states of a binary solid solution AB1-xCx and its related aqueous phase composition. The diagrams are based on the law of mass action equilibrium[1] according to equations S7 to S9. The aqueous activity fractions XC,aq:

XC,aq=[C-][C-]+[B-]=KACXACγAC∑Π                                 (S6)

[A+][B-]=KABXABγAB                                      (S7)

[A+][C-]=KACXACγAC                                      (S8)

∑Π=([C-]+[B-])[A+]                                   (S9)

where,

[A+], [B-] and [C-], aqueous activities of the ionic species A+, B- and C-;

KAB and KAC, solubility products of the end members AB and AC of the binary solid solution series;

XAB and XAC, mole fractions of BA and CA in the solid.

γAB and γAC, activity coefficients of the BA and CA members of the solid solution series. In ideal solution (dilute solution), γAB= γAC= 1.

∑Π, total solubility product.

In this study, [B-] and [C-] are the concentrations of Cl- and HPO42-. The Gibbs free energy GM were calculated with the i mole fraction Xi (%, ∑Xi= 1) in solid phase as the eq S10, and the activity coefficients γC in solid phase was calculated according to Debye-Hűckel equation.

GM=RT∑Xilnγi                                                     (S10)

- Molecular dynamics and DFT calculations

Molecular dynamic (MD) simulations were performed with Materials studio 2017. Simulated Annealing method was performed during 500 ps to gently carry the system from 373 to 500 K, simulating the experimental temperature conditions. After this procedure, one of the frames had the lowest energy which was the most stable structure. Then the structure is relaxed again by optimized. All simulations were performed using the Forcite[2-4], within the universal force field. The electrostatic and van der Waals were Ewald and Atom based respectively

The adsorption energy (Ead) was calculated as

Ead= Etot- Egra- Emolecule                                         (S11)

where the Etot is the energy of the optimized system; Egra is the energy of the bare surface; Emolecule is the energy of the optimized PO43-molecules.

Figure S1 Orthophosphates (Na) forms in aqueous with different pH calculated by Visual MINTEQ[5]

S2. Supplemental Results and Discussions

Scheme S1 Combination manners of Ca(OH)2 (or Al(OH)3) octahedron and TEA

Figure S2 XPS of LDHs synthesized with different TEA: M. (a) General view. (b) Ca 2p1/2 and Ca 2p2/3 of Ca(OH)2 octahedron on LDHs. (c) Al 2p of Al(OH)3 octahedron on LDHs. (d) O 2s of Ca/Al-LDHs

It can be seen that the polymerization degree is reduced with the addition of TEM due to the blue shifts of 2p peaks. When TEA:M= 10 (CALOx), the new diffraction pattern of high binding energy peaks of Ca 2p and Al 2p are immerged because the coordination number of Ca and Al decreased especially for those atoms in the edges of layer frames (combine with SEM).

Figure S3 Mass spectra in positive-ion mode of Ca/Al-LDH oligomers synthesized with different TEA:M in dispersion in ethanol (solid/solution= 250 mg L-1).

Figure S4 DLS of Ca/Al-LDH oligomers synthesized with different M:TEA in dispersion in ethanol

The average diameter of particle size was calculated as the definition of median diameter. The difference of particle size was decreased significantly with the increasing of TEA which means that the capping strategy could homogenize the growth of crystals.

Figure S5 Photographs of macro appearance of flexible CALOx in different shapes by molding or painting

Figure S6 XRD pattern of LDH with capping strategy of TEA:M= 20 after watering desalination and dried.

It can be deduced that the basic brucite layer frame (00l) is absence from the sample when TEA:M= 20. Bimetallic hydroxides reveal amorphous like and are not able to crystalize.

Figure S7 (a) Hydroxide radical amount on layer surface of LDH in different TEA:M value. (b) Zeta potential with pH of CALOx and ordinary Ca/Al-LDH. (c) to (f) Automatic potential titration sources of LDH synthesized with TEA:M=0 (c), 5 (d), 10 (e) and 20 (f).

Figure S8 Original CALOx and elements (Ca, Al, O and N) distribution of macro pieces and SAED of layer edge.

Figure S9 XRD qualification in Retiveld refinement method of gel like CALOx after lyophilization with scanning rete of 2° min-1

The pure CALOx containing of as-prepared slurry sample was calculated. While the original dosage of slurry is 0.5 g L-1, the pure CALOx should be about 0.194 g L-1 (0.5× 38.78%).

Figure S10 (a) Isotherms of ordinary Ca/Al-LDH, CALOx and surface dried CALOx in low initial P concentrations. (b) Adsorption kinetics (50 mg P L-1) of ordinary Ca/Al-LDH, CALOx and surface dried CALOx.

Figure S11 TEA remaining ratio with regeneration cycle

After adsorption, the samples were completely digested with 1 M HCl solution, and the total nitrogen content was measured. The results showed that, except for the first cycle, the TEA loss rate of CALOx after 2–6 regeneration cycles remained nearly constant at approximately 5%.

Figure S12 (a) Lattice plane and its selected area electron diffraction (SAED) of P adsorbed CALOx. (b) TEM image.

Figure S13 (a) AFM images of CALOx before and after P adsorbed. (b) Thickness of relative site (green mark) on AFM images.

Figure S14 Stability of N-O-H of P adsorbed CALOx in air dried without water supply.

The capping effect would be disabled after 40 min for P adsorbed CALOx according to the emission of TEA and interlayered PO4 vanished (Wave number= 1086 cm-1)

Figure S15 (a) Lippmann phase diagram of solid solution composed of CALOx and Cl- or HPO42- in interlayer. (b) Gibbs free energy of designed mixture of solid solution.

Lippmann phase diagram (Figure S14a) suggests that the ion activity product of solid phase decreases with the increasing phosphate containing.

Figure S16 Vibration of -OH belongs to crystal H2O in interlayer or inner surface exposed by extend FTIR (in wave numbers of 3200~ 3400 cm-1) in phosphate adsorption course, (a) Ordinary Ca/Al-LDH and (b) CALOx.

Figure S17 Elements distribution of CALOx after P absorbed and element distribution of P in text were green color changed for noticeability.

Other elements on frame works are uniformly distributed in both surface and inner-space by overlap of layers.

Figure S18 Phosphate adsorption isothermals of CALOx in blended solution of 50 mg P L-1 and different concentration (5~ 100 mg P L-1) of CO32- (pH= 9.82) (a) or H2CO3 (pH= 4.36) (b) with absorbent dosage of 0.5 g L-1. (c) Destruction mechanism of hydrogen bond shielding by HCO3- (H2CO3) on inner surface and edge of LDH.

to testify the activity of hydrogen bond on the surface of Ca/Al-LDH. The trendline of isothermals altered obviously with the invasion of H2CO3, while CO32- affected scarcely. Because protonated HCO3- is a powerful proton donor[6] in aqueous, TEA tend to be attracted by H+ offered by HCO3- rather than M-OH and the isolating effect of hydrogen bond is eliminated. The strong force between hydroxide radicals and absorbate was revealed, so that phosphates adsorption is returned to the surface interaction.

Figure S19 Charge density difference of CALOx & TEA hydroxyl capped (red) and without (blue) in Z direction.

Table S1 The dissolution of CALOx and ordinary Ca/Al-LDH in aqueous solution

|  | Ca2+ (ppm) |  | Al3+ (ppm) | Cl- (ppm) | pH |
| --- | --- | --- | --- | --- | --- |
| CALOx | 0.13 | / |  | 26.73 | 7.73 |
| Ordinary Ca/Al-LDH | 0.72 | / |  | 6.75 | 7.12 |

Table S2 References of P sorbent comparisons

| Calcined Mg/Al-LDH | Triantafyllidis, K. S.., et al., J. Colloid. Interf. Sci., 2010, 342, 427. |
| --- | --- |
| Tobermorite@MgO | Dai, Suwan., et al., Chem. Eng. J., 2022, 446, 136809. |
| NiLa-LDOs@Fe3O4 | Vu, Chi Thanh., et al., Water. Res., 2020, 175, 115679. |
| Mg/Al-LDH | Triantafyllidis, K. S.., et al., J. Colloid. Interf. Sci., 2010, 342, 427. |
| La/Zr Oxides | Chao Xiang., et al., Environ. Sci. Technol., 2020, 54, 437. |
| La/Fe Oxides | Jie Yu., et al., Environ. Sci. Technol., 2019, 53, 9073. |
| La(OH)3 | Wang, Minglu., et al., Appl. Surf. Sci., 2021, 538, 147910. |
| Ce2(CO3)3xH2O@Fe3O4 | Sujie Shan., et al., Chem. Eng. J., 2021, 425, 128894. |
| Ce MOF | Jiaojie He., et al., Chem. Eng. J., 2020, 394, 124912. |
| UiO-66(Zr) | Li, Mohua., et al., Environ. Sci. Technol., 2021, 55, 13209. |
| Lignin | Enmin Zong., et al., Int. J. Biol. Macromol., 2021, 182, 434 |
| Fe@Biochar | Kumuduni N. P., et al., J. Hazard. Mater., 2021, 415,125464. |
| TiO2@polyaniline | Wang, Ning., et al., Chem. Eng. J., 2017, 316, 33. |
| La@Coal Fly Ash | Satoshi Asaoka., et al., J. Hazard. Mater., 2021, 406,124780. |
| Gasification Slags | Yang, Baoguo., et al., Mater. Today. Sus., 2023, 100357. |

Table S3 Contaminations of press-filtrated wastewater of domestic sewage

| Contaminations | COD | Total Phosphate (P) | Cl- | Basicity (OH-) | SO42- | CO32- | pH |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Concentration (mg L-1) | 976.2 | 17.1 | 2219.3 | 51.5 | 27.9 | 15.8 | 7.69 |

The press-filtrated wastewater of domestic sewage is come from Xiaohongmen wastewater treatment plant (Beijing. China). The wastewater is successively treated by flocculating settling (polymerization ferric chloride), dehydration (lime) and denitrogenating (magnesium ammonium phosphate), then filtration (plate-and-frame filter press).

References

[1] T. Matschei, Thermodynamics of Cement Hydration, in:  Department of chemistry, the University of Aberdeen, 2007.

[2] L. Song, W. Liu, F. Xin, Y. Li, Study of adhesion properties and mechanism of sodium silicate binder reinforced with silicate fume, International Journal of Adhesion and Adhesives, 106 (2021) 102820.

[3] Y. Han, W. Liu, J. Chen, DFT simulation of the adsorption of sodium silicate species on kaolinite surfaces, Applied Surface Science, 370 (2016) 403-409.

[4] A.E. Genç, A. Akça, B. Kutlu, The catalytic effect of the Au(111) and Pt(111) surfaces to the sodium borohydride hydrolysis reaction mechanism: A DFT study, International Journal of Hydrogen Energy, 43 (2018) 14347-14359.

[5] S. Dong, Y. Wang, Y. Zhao, X. Zhou, H. Zheng, La3+/La(OH)3 loaded magnetic cationic hydrogel composites for phosphate removal: Effect of lanthanum species and mechanistic study, Water Research, 126 (2017) 433-441.

[6] O. Gutiérrez-Sánchez, N. Daems, W. Offermans, Y.Y. Birdja, M. Bulut, D. Pant, T. Breugelmans, The inhibition of the proton donor ability of bicarbonate promotes the electrochemical conversion of CO2 in bicarbonate solutions, Journal of CO2 Utilization, 48 (2021) 101521.