Supplementary Information

Split-type Photoelectrochemical Biosensing for miRNA-144 Assay Based on ZnIn2S4/TiO2 Heterojunction

Ying Zhenga, Fan Moa, Qian Suna, Xinzhou Huanga, Yijie Dua, Xiaomei Ana, Haoning Maa, Guoqiu Wubc, Yuanjian Zhanga, and Yanfei Shenabc,*

aMedical School, School of Chemistry and Chemical Engineering, Southeast University, Nanjing 210009, China.

bCenter of Clinical Laboratory Medicine, Zhongda Hospital, Southeast University, Nanjing 210009, China.

cJiangsu Provincial Key Laboratory of Critical Care Medicine, Southeast University, Nanjing 210009, China.

Email: Yanfei.Shen@seu.edu.cn

Table of contents

Materials and Reagents	S3

Apparatus	S4

Evaluation of LOD for biosensing	S5

Figure S1	S6

Figure S2	S7

Figure S3	S8

Figure S4	S9

Figure S5	S10

Figure S6	S11

Figure S7	S12

Figure S8	S13

Figure S9	S14

Figure S10	S15

Table S1	S16

Table S2	S17

Table S3	S18

Table S4	S19

Table S5	S20

References	S21

Materials and Reagents

Ethanol, hydrochloric acid (HCl 36%), potassium chloride (KCl), di-sodium hydrogen phosphate (Na2HPO4), sodium dihydrogen phosphate (NaH2PO4) and ascorbic acid (AA) were purchased from Sinopharm Chemical Reagent Co., Ltd. (Beijing, China). Titanium butoxide (TBOT), zinc sulfate heptahydrate (ZnSO4·7H2O), indium chloride tetrahydrate (InCl3·4H2O) and ethanolamine were provided by Shanghai Aladdin Biochemical Technology Co., Ltd. (Shanghai, China). Thioacetamide (TAA) and ascorbic acid 2-phosphate (AAP) were supplied by Shanghai Macklin Biochemical Co., Ltd. (Shanghai, China). Potassium ferricyanide (K3[Fe(CN)6]) and potassium ferrocyanide (K4[Fe(CN)6]) were obtained from Shanghai Lingfeng Chemical Reagent Co., Ltd. (Shanghai, China). Carboxyl silicon oxide magnetic beads (MB), streptavidin-ALP (SA-ALP), phosphate buffer saline (PBS), 1-(3-dimethylamino-propyl)-3-ethylcarbodiimide hydrochloride (EDC), N-hydroxysuccinimide (NHS), triethanolamine buffer (TEA), ethidium bromide (EB) and oligonucleotides were purchased from Sangon Biotech (Shanghai) Co., Ltd (Shanghai, China). Fluorine-doped tin-oxide glass (FTO) was acquired from Zhuhai Kaivo Optoelectronic Technology Co., Ltd. (Guangdong, China). All other reagents were of analytical reagent grade and ultrapure water was gained from a Millipore water purification system.

Apparatus

The scanning electron microscope (SEM) were performed on Crossbeam 350, (Zeiss, Germany). The X-ray photoelectron spectroscopy (XPS) was recorded through an ESCALAB 250XI (Thermo, USA). The X-ray diffraction (XRD) patterns were recorded by a Smartlab SE X-ray diffractometer with Cu Kα lines in the range of 2θ = 5° - 90° (Rigaku, Japan). UV-vis absorption spectra and UV-vis diffuse reflectance spectra (DRS) were recorded on Cary 100 UV-vis spectrophotometer (Agilent, USA). Electrophoresis System were performed on DYY-6C (Liuyi Biotechnology, China). Gel-imaging were recorded on JS-1075 (Peiqing, China). I–t curve (i–t) and electrochemical impedance spectroscopy (EIS) were performed on a CHI 660E electrochemical workstation (Shanghai Chenhua Instrument, China).

Evaluation of LOD for biosensing

The International Union of Pure and Applied Chemistry (IUPAC) states that the limit of detection (LOD) is calculated from the smallest measurable signal (XL) obtained by a specific analytical method.1, 2 The value of XL is given by the equation3:

XL =Xb1 + ksb1    							                              (1)

Where Xb1 and sb1 represent the mean and standard deviation of blank measurements, respectively. Typically, k is 3, corresponding to 99.6% confidence. According to the analytical results in Figure 6b, the linear regression equation of the PEC biosensor can be expressed as:

ΔI = 1.68 lgC+ 0.94   							               (2)

where ΔI is the PEC intensity, and C is the concentration of the target. Based on the standard definition and combining Equations 1 and 2, the LOD can be calculated using the following expression:

LOD = 10Xb1+ksb1-0.941.68   							           (3)

Thus, according to the Equation 3, the LOD is calculated as 6.75 fM.

Figure S1. Optimization of ZnIn2S4 growth time.

To optimize the thickness of the photosensitizer layer, the photocurrent generated by ZnIn2S4 films grown on TiO2/FTO for various durations was measured. Based on these measurements, a growth time of 120 minutes was selected as the optimal time for ZnIn2S4 deposition.

Figure S2. SEM top image of ZnIn2S4.

Figure S3. Elemental analysis of Ti, O, Zn, In and S in ZnIn2S4/TiO2.

Figure S4. High resolution XPS survey spectra of Ti 2p in TiO2/FTO.

Figure S5. XPS survey spectra of ZnIn2S4/TiO2/FTO.

Figure S6. The equivalent circuit for the impedance plots in Figure 3b and 3c, where Rs is the solution resistance, CPE represents the constant phase element, and Rct represents the interfacial charge transfer resistance of the electrode/electrolyte.

Figure S7. Feasibility analysis of HCR amplification strategy by PAGE.

Figure S8. UV-vis absorption spectra of MBs, DNA and the products of DNA and MBs coupling.

Figure S9. The equivalent circuit for impedance plots in Figure 5b, where Rs is the solution resistance, CPE represents the constant phase element, W1 is Warburg diffusion impedance, and Rct represents the interfacial charge transfer resistance of the electrode/electrolyte.

Figure S10. Optimization for (a) the incubation time of HCR and (b) the catalytic time of ALP for the biosensor construction.

Table S1. Sequences of oligonucleotides used in this work.

| Oligonucleotides | Sequence (5'-3') |
| --- | --- |
| H1-NH2 | NH2-TTT AGT ACA TCA TCT ATA CTG TAG CGT TTA GTA TAG ATG A |
| H2-Bio | TTA ACC CAC GCC GAA TCC TAG ACT CAA AGT AGT CTA GGA TTC GGC GTG TTT TTT-Bio |
| H3-Bio | Bio-TTT TTT AGT CTA GGA TTC GGC GTG GGT TAA CAC GCC GAA TCC TAG ACT ACT TTG |
| I | AGT CTA GGA TTC GGC GTG GGT TAA TCA TCT ATA CT |
| miRNA-144 | UAC AGU AUA GAU GAU GUA CU |
| miRNA-124 | CGU GUU CAC AGC GGA CCU UGA U |
| miRNA-21 | UAG CUU AUC AGA CUG AUG UUG A |
| miRNA-16 | UAG CAG CAC GUA AAU AUU GGC G |

All oligonucleotides stock solutions (100 μM) in this work were dissolved in PBS (10 mM, pH 7.4) solution.

Table S2. The fitting results for the impedance plots in Figure 3b and 3c.

|  | Rs (ohm) | CPE (F) | Rct (ohm) |
| --- | --- | --- | --- |
| TiO2 (in dark) | 259.8 | 1.03e-6 | 34920 |
| ZnIn2S4/TiO2 (in dark) | 198.2 | 1.55e-6 | 298100 |
| TiO2 (under illumination) | 195.2 | 1.22e-6 | 72230 |
| ZnIn2S4/TiO2 (under illumination) | 218.1 | 9.28e-6 | 68520 |

Table S3. The fitting results for the impedance plots in Figure 5b.

|  | Rs (ohm) | CPE (F) | Rct (ohm) | W1 (ohm) |
| --- | --- | --- | --- | --- |
| MBs | 136.6 | 4.25e-6 | 912 | 1.19e-3 |
| H1/MBs | 144.4 | 2.91e-6 | 1078 | 1.22e-3 |
| miRNA-144/H1/MBs | 129.0 | 4.43e-6 | 1379 | 1.19e-3 |
| Initiator/miRNA-144/H1/MBs | 134.9 | 3.92e-6 | 1592 | 0.83e-3 |
| H2/Initiator/miRNA-144/H1/MBs | 147.0 | 4.70e-6 | 2054 | 0.76e-3 |

Table S4. Comparisons of different biosensors for miRNA detection.

| Analytical methods | Linear range | Detection limit | References |
| --- | --- | --- | --- |
| ECL | 10 fM-1 nM | 8.19 fM | 3 |
| ECL | 1 aM-1 nM | 0.02 aM | 4 |
| FL | 20 pM - 2.5 nM | 8.9 pM | 5 |
| FL | 100 pM-25 nM | 77.4 pM | 6 |
| CL | 4 pM -20 pM | 2.2 pM | 7 |
| PEC | 1 fM - 5 nM | 0.17 fM | 8 |
| PEC | 10 fM- 1 nM | 3 fM | 9 |
| PEC | 10 fM - 1 nM | 6.75 fM | this work |

Table S5. Recovery assay for miRNA-144 in the human serum samples.

| Sample | Added (fM) | Assayed (fM) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| 1 2 3 | 10 1000 100,000 | 10.29 978.38 101933.25 | 5.60 3.50 2.74 | 102.89 97.84 101.93 |

References

1.	G. L. Long and J. D. Winefordner, Anal. Chem., 1983, 55, 712A-724A.

2.	V. A. Fassel, Anal. Chem., 1976, 48, 2294-2296.

3.	Z. Ning, E. Yang, Y. Zheng, M. Chen, G. Wu, Y. Zhang and Y. Shen, Anal. Chem., 2021, 93, 8971-8977.

4.	Y. Yang, J. Li, S. Xiang, F. Wang, H. Yang, R. Cai and W. Tan, Anal. Chem., 2024, 96, 9653-9658.

5.	D. Li, Z. Luo, H. An, E. Yang, M. Wu, Z. Huang and Y. Duan, Talanta, 2020, 217, 121056.

6.	Y. Xu, X. Li, C. Niu, H. Wu, Y. Yong, C. Qi, W. Gong, H. Bai, Y. Chen, S. Ding and P. Liao, Biosens. Bioelectron., 2022, 212, 114405.

7.	X. Shen, W. Xu, J. Guo, J. Ouyang and N. Na, ACS Sens., 2020, 5, 2800-2805.

8.	W. Tu, L. Zhu, T. Cai, Z. Li and Z. Dai, Biosens. Bioelectron., 2024, 243, 115781.

9.	J. Li, C. Chen, F. Luo, C. Lin, Z. Lin, J. Wang and B. Qiu, Anal. Chem., 2023, 95, 17670-17678.