Ultrathin FeCo-PBA Nanosheets as Highly Efficient Electrocatalysts for the Oxygen Evolution Reactions

Xiangyu Menga,b,†, Chen Zhaoc,†, Liang Maa,b,†, Shihao Wua,b, Shaokuan Hud, Lin Zhua,b, Dechang Jiaa,b,e, Yu Zhoua,b,e,f, Xiaoming Duana,b,* and Zengyan Weia,*

a Key Laboratory of Advanced Structural-Functional Integration Materials & Green Manufacturing Technology, Harbin Institute of Technology, Harbin, 150001, China

b Institute for Advanced Ceramics, School of Materials Science and Engineering, Harbin Institute of Technology, Harbin, 150001, China

c Department of Chemistry, City University of Hong Kong, Hong Kong, China.

d College of Home and Art Design, Northeast Forestry University, Harbin, 150040, China

e State Key Laboratory of Precision Welding & Joining of Materials and Structures, Harbin Institute of Technology, Harbin, 150001, China

f School of Materials Science and Engineering, Harbin Institute of Technology (Shenzhen), Shenzhen, 518055, China

*Email: zwei@hit.edu.cn (Zengyan Wei), dxmhit@126.com (Xiaoming Duan)

†: These authors contributed equally.

- Experimental section

Materials

Cobalt (II) nitrate hexahydrate (Co(NO3)2·6H2O) and nickel(II) nitrate hexahydrate (Ni(NO3)2·6H2O) were purchased from Damao Chemical Reagent Factory (Tianjin, China). Iron (II) perchlorate hydrate (Fe(ClO4)2·xH2O) and potassium hydroxide (KOH) were purchased from Aladdin Biochemical Technology Co., Ltd. (Shanghai, China). Potassium tetracyanonickelate (II) hydrate (K2[Ni(CN)4]·xH2O) and pyrazine (C4N2H4) were purchased from Macklin Chemical Reagent Co., Ltd. (Shanghai, China). Pyridine (C5H5N) was purchased from Fuchen Chemical Reagent Co., Ltd. (Tianjin, China). Naphthol (C10H7OH) was purchased from Sigma-Aldrich Trading Co., Ltd. (Shanghai, China). Methanol (CH3OH) and isopropanol (C3H8O) were purchased from Fuyu Fine Chemical Co., Ltd. (Tianjin, China). All reagents were of analytical grade.

Synthesis of Hofmann MOF and FeCo-PBA

Hofmann MOF and FeCo-PBA electrocatalysts were fabricated through a facile solution method.

1. Synthesis of Hofmann MOF

Prepare Solution A: Dissolve 1.5 mmol (0.381 g) Fe(ClO4)2·xH2O, 1.5 mmol (0.435 g) Co(NO3)2·6H2O and 3 mmol (0.24 g) pyrazine in 20 mL methanol mixed with 20 mL deionized water. Prepare Solution B: Dissolve 3 mmol (0.72 g) K2[Ni(CN)4]·xH2O in 10 mL deionized water. Ultrasonically treat both solutions for 30 minutes to achieve full dissolution. Drop Solution B into Solution A, and stir the mixed system vigorously with magnetic stirring for 30 min. Keep the obtained mixture static for 12 h. Collect the precipitate, rinse thoroughly with deionized water, and dry at 60 °C in a circulating oven for 12 h to obtain target Hofmann MOF.

2. Synthesis of FeCo-PBA

Prepare Solution A: Dissolve 0.1 mmol (0.025 g) Fe(ClO4)2·xH2O and 0.1 mmol (0.029 g) Co(NO3)2·6H2O in 5 mL methanol and 5 mL deionized water. Prepare Solution B: Dissolve 0.2 mmol (0.048 g) K2[Ni(CN)4]·xH2O in 10 mL deionized water. Subject the two prepared solutions to ultrasonic treatment for 30 min until completely dissolved. Add Solution B into Solution A under continuous intense magnetic stirring for 30 min.

Allow the reaction mixture to stand quietly for 12 h. Purify the product by repeated washing with deionized water, then dry at 60 °C for 12 h in a circulating oven to gain FeCo-PBA samples.

For the synthesis of other monometallic and bimetallic Hofmann MOFs and PBA, only the species and proportions of the metal salts in solution A need to be changed, while ensuring the total molar amount of the metal salts is 0.2 mmol. Once the total molar amount of feed metal salts (Fe(ClO4)2·xH2O and Co(NO3)2·6H2O) was increased to 75 mmol L−1 in solution A, while the molar amount of K2[Ni(CN)4]·xH2O was increased to 300 mmol L−1 in solution B, the resulting products were denoted as h-Fe-PBA, h-Co-PBA, h-Ni-PBA, h-FeNi-PBA, h-CoNi-PBA and h-FeCo-PBA.

Materials Characterizations

Scanning electron microscopy (SEM) and energy-dispersive X-ray spectroscopy (EDS) were performed on a HITACHI SU5000 field-emission scanning electron microscope operated at 20 kV accelerating voltage, equipped with an Oxford ULTIMAX 40 EDS detector. Transmission electron microscopy (TEM) and high angular annular dark field scanning TEM (HAADF-STEM) measurements were performed on a JEOL JEM-2100 transmission electron microscope at an operating voltage of 200 kV. X-ray diffraction (XRD) patterns were collected on a PANalytical X’Pert diffractometer with Cu Kα radiation (λ = 0.1542 nm) at an operating voltage of 40 kV. Raman spectra were recorded on an inVia-Reflex confocal Raman microscope with a 532 nm excitation wavelength under ambient conditions with a scanning range of 0–2400 cm⁻1. X-ray photoelectron spectroscopy (XPS) characterization was carried out using a Thermo Fisher ESCALAB 250Xi system with monochromatized Al Kα radiation as the excitation source. Atomic force microscopy (AFM) was performed at room temperature on a Bruker Dimension Fastscan microscope. was conducted on a STA449F3 Jupiter thermal analysis system at a heating rate of 5 ℃/min under Ar atmosphere. Differential Scanning Calorimetry (DSC)/ Thermogravimetric analysis (TGA) measurements were performed on a METTLER TOLEDO TGA/DSC 3+ simultaneous thermal analyzer.

Electrochemical measurements

All electrochemical performance measurements, including linear sweep voltammetry (LSV), cyclic voltammetry (CV), electrochemical impedance spectroscopy (EIS) and electrochemical active surface area (ECSA), were conducted on a CHI760e electrochemical workstation combined with a rotating disk electrode system (model AFMSRCE, PINE Research Instrumentation, USA). All tests were performed in 1 M KOH electrolyte using a three‑electrode configuration at room temperature, in which a glassy carbon electrode encased in polytetrafluoroethylene was used as the working electrode, a graphite rod as the counter electrode, and an Ag/AgCl electrode as the reference electrode. In 1 M KOH (pH = 13.6), the potential conversion of the Ag/AgCl reference electrode relative to the reversible hydrogen electrode (RHE) was determined to be + 0.9984 V. According to the LSV curves, the corresponding Tafel slopes were calculated using the equation: η = b log J + a, where η, J, b, and a represent the overpotential, current density, Tafel slope, and intercept constant, respectively. For preparing the working electrode, samples (5 mg of Hofmann MOF) were dispersed in a mixture containing 0.35 mL water, 0.65 mL isopropanol, and 30 μL of 5% Nafion solution. The mixture was sonicated for 20 min to achieve sufficient dispersion and form a homogeneous catalyst ink. Subsequently, 15 μL of the dispersion was drop-cast onto the glassy carbon region of the electrode in three aliquots, affording a catalyst loading of 0.382 mg cm⁻2. The LSV data in this work did not undergo iR compensation.

Computational Details

Density functional theory (DFT) calculations were executed in the Materials Studio (MS). All the calculations were based on the CASTEP module. The exchange-correlation was approximated with the Perdew-Burke-Ernzerhof generalized gradient approximation (PBE-GGA). The projected augmented wave (PAW) method was utilized for the interaction between valence electrons and ion cores. Ultrasoft pseudopotentials and Koelling-Harmon relativistic treatments were used for calculation process. At the very beginning of the calculations, the spin polarization was set to 2 as the initial value, and the system was assumed to be nonmetallic. A plane-wave energy cutoff of 280 eV was employed. The energy convergence threshold was set to 2×10⁻5 eV. For the single-point energy calculation, the force criterion for convergence was set at less than 0.05 eV/Å. The maximum displacement was set to 0.002 Å.

- Supplementary Figures

Fig. S1. Schematic illustration for the synthesis of Hofmann MOF and PBA nanosheets.

Fig. S2. (a) SEM image of Hofmann MOF. Scale bar: a 500 nm.

Fig. S3. DSC and TGA curves of Hofmann MOF.

Fig. S4. SEM images and corresponding elemental mappings of FeCo-PBA. Scale bars: a-f 5 μm.

Fig. S5. (a) HRTEM image, (b) FFT pattern and (c) simulated pattern using ReciPro software of PBA nanosheets. Scale bar: a 20 nm.

Fig. S6. (a-f) SEM image and corresponding elemental mappings of Fe-PBA. Scale bars: a-f 2μm.

Fig. S7. (a) TEM image and (b) HRTEM image of Fe-PBA. Scale bars: a 500 nm, b 20 nm.

Fig. S8. (a-f) SEM image and corresponding elemental mappings of Co-PBA. Scale bars: a-f 2μm.

Fig. S9. (a-b) TEM images of Co-PBA. (c-g) HAADF-STEM image and the corresponding EDX elemental maps of Co-PBA. Scale bars: a 0.5 μm, b 200 nm, c-g 1 μm.

Fig. S10. SEM images of (a) h-Fe-PBA, (b) h-Co-PBA, (c) h-Ni-PBA, (d) h-FeNi-PBA, (e) h-CoNi-PBA, (f) h-FeCo-PBA. Scale bars: a-f 500 nm.

Fig. S11. (a-f) SEM image and corresponding elemental mappings of h-Fe-PBA. Scale bars: a-f 2μm.

Fig. S12. (a-f) SEM image and corresponding elemental mappings of h-Co-PBA. Scale bars: a-f 2μm.

Fig. S13. (a-h) SEM images and corresponding elemental mappings of h-FeCo-PBA. Scale bars: a 1 µm, b 500 nm, c-h 2μm.

Fig. S14. (a) AFM image of h-FeCo-PBA, (b) height profiles for the orange line. Scale bar: a 1 µm.

### Table S1 Surface area, pore volume and pore size of FeCo-PBA.

| Sample | surface area (m2 g−1) | pore volume (cm3·g−1) | BJH desorption average pore width (nm) |
| --- | --- | --- | --- |
| FeCo-PBA | 20.06 | 0.2583 | 26.69 |

Fig. S15. Raman spectra of Fe-PBA, Co-PBA and FeCo-PBA.

Table S2 Detailed fitting parameters for obtained electrocatalysts.

| Samples | Rs (Ω) | Rct (Ω) | CPE-T | CPE-P |
| --- | --- | --- | --- | --- |
| RuO2 | 3.569 | 4.410 | 0.004931 | 0.7851 |
| Hofmann MOF | 3.488 | 3.368 | 0.03332 | 0.6406 |
| Fe-PBA | 4.186 | 3.404 | 0.0005210 | 0.7226 |
| Co-PBA | 3.897 | 2.591 | 0.02993 | 0.6928 |
| FeCo-PBA | 3.5 | 2.136 | 0.03484 | 0.7319 |

Fig.S16 Cyclic voltammograms of (a) Hofmann MOF, (b) Fe-PBA, (c) Co-PBA and (d) FeCo-PBA in the potential window of 0.85-0.95 V (vs. RHE) at the scan rate of 40, 50, 60, 70, 80, 90 and 100 mV s–1, respectively. (e) Double-layer capacitance (Cdl) calculated from the plots of the double layer charging current against scan rates.

The Cdl values were determined by linearly fitting the double-layer charging current as a function of scan rate. FeCo-PBA exhibits the highest Cdl of 0.899 mF cm−2, corresponding to an ECSA of 14.98 cm2, which demonstrates that its ultrathin nanosheet structure endows the material with abundant exposed active surfaces.

Fig. S17 LSV curves of three FeCo-PBA samples before and after 200 h durability test at the current density of 10 mA cm−2 in 1 M KOH.

Fig. S18 XRD patterns of FeCo-PBA after 200 h OER CP test under 10 mA cm−2 in 1 M KOH solution.

Diffraction peaks of carbon paper can be observed in XRD patterns (Fig. S18), while the characteristic peaks of pristine FeCo-PBA become weakened, confirming the structural transformation. SEM images (Fig. S19) revealed that the sheet-like morphology of FeCo-PBA is partially damaged at the macroscopic scale. TEM images (Fig. S20) further verified the distinct morphological evolution of the as-obtained MOFs, while the nanosheet structure can still be observed at the microscopic level. Elemental distribution analysis demonstrated that Fe and Co are predominantly distributed on the surface of MOF nanosheets, whereas Ni, Fe, Co, C, N and O are homogeneously distributed throughout the interior of the nanosheets. This phenomenon can be attributed to the surface reconstruction of MOFs during long-term electrochemical reactions, which generates metal oxyhydroxide (MOOH) phases. Such in-situ formed MOOH species are widely recognized as the genuine active phases for electrocatalysis.19 XPS characterization (Fig. S21) confirmed the retention of Fe and Co species. Notably, the intense peak located at 531.5 eV in the O 1s spectrum is assigned to the M-OH bond,37 strongly evidencing the formation of metal oxyhydroxides.

Fig. S19 (a-b) SEM images of FeCo-PBA loaded on carbon paper after 200 h OER CP test under 10 mA cm−2. Scale bars: a-b 5 μm.

Fig. S20 (a-b) TEM images and (c-i) corresponding EDX elemental maps of FeCo-PBA after 200 h OER CP test under 10 mA cm−2. Scale bars: a 200 nm, b 10 nm, c-i 200 nm.

Fig. S21 (a) Co 2p, (b) Fe 2p, (c) Ni 2p and (d) O 1s XPS spectra of FeCo-PBA, respectively.

Fig. S22 LSV curve of two-electrode water electrolyzer (FeCo-PBA || Pt/C).

Table S3 Comparison of overpotential at the current density of 10 mA cm−2 with other recently reported advanced OER catalysts in 1 M KOH electrolyte.

| Catalysts | Current Density (mA cm−2) |  | Overpotential (mV) | Tafel Slope (mV dec–1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| FeCo-PBA (This work) | 10 | 266 |  | 43.5 | - |
| P/Ag@AgCo PBA | 10 | 253 |  | 65.3 | [1] |
| NiFe-MOF/G | 10 | 258 |  | 49 | [2] |
| Cex/CoS | 10 | 269 |  | 50 | [3] |
| Co-M-Fe/Ni(150) | 10 | 269 |  | 50 | [4] |
| NiFe-MOF | 10 | 270 |  | 123 | [5] |
| Co-PBA | 10 | 274 |  | 53 | [6] |
| Co10Ce1/C HFs | 10 | 274 |  | 82.6 | [7] |
| FeCoNiMnCu | 10 | 280 |  | 59 | [8] |
| Fe, Ni–N–C/CNF | 10 | 284 |  | 45.4 | [9] |
| Hi-Ni | 10 | 287 |  | 58.7 | [10] |
| sc-PBA/Carbides@NC | 10 | 288 |  | 41.3 | [11] |
| CoFe-PBA/C350 | 10 | 290 |  | 61.4 | [12] |
| Co2.07Ni-LDH | 10 | 290 |  | 65 | [13] |
| NF70@CVL | 10 | 300 |  | 105 | [14] |
| NiCoS/T3C2Tx | 10 | 365 |  | 58.2 | [15] |

- References

1 W. Liao, Q. Yang, H. Jiang and P. Liu, Renew. Energy, 2025, 242, 122383.

2 Y. Wang, B. Liu, X. Shen, H. Arandiyan, T. Zhao, Y. Li, M. Garbrecht, Z. Su, L. Han, A. Tricoli and C. Zhao, Adv. Energy Mater., 2021, 11, 2003759.

3 H. Xu, J. Cao, C. Shan, B. Wang, P. Xi, W. Liu and Y. Tang, Angew. Chem. Int. Ed., 2018, 57, 8654–8658.

4 P. Chen, X. Duan, G. Li, X. Qiu, S. Wang, Y. Huang, A. Stavitskaya and H. Jiang, Int. J. Hydrog. Energy, 2023, 48, 7170–7180.

5 X. Li, D. Ma, C. Cao, R. Zou, Q. Xu, X. Wu and Q. Zhu, Small, 2019, 15, 1902218.

6 Y. Guo, T. Wang, J. Chen, J. Zheng, X. Li and K. Ostrikov, Adv. Energy Mater., 2018, 8, 1800085.

7 L. Ma, M. Zhang, Z. Wei, X. Meng, R. Chen, M. Qin, L. Zhu, Y. Wang, X. Huang, M. Feng, P. He, D. Jia, Y. Zhou and X. Duan, Ceram. Int., 2025, 51, 6244–6252.

8 K. Huang, D. Peng, Z. Yao, J. Xia, B. Zhang, H. Liu, Z. Chen, F. Wu, J. Wu and Y. Huang, Chem. Eng. J., 2021, 425, 131533.

9 Y. Wang, J. Li, W. Gu, Q. Wang, X. Li, G. Shao, P. Zhang and Y. Zhao, Int. J. Hydrog. Energy, 2026, 203, 153193.

10 S. Assavapanumat, M. Ketkaew, P. Garrigue, V. Lapeyre, S. Reculusa, C. Wattanakit and A. Kuhn, ChemCatChem, 2019, 11, 5951−5960.

11 Y. Guo, L. Yan, J. Li, J. Shi, Z. Liu, L. Fan and W. Cai, Chem. Eng. J., 2023, 472, 144818.

12 Y. Li, W. Yu, X. Chen, X. Miao, S. Chen, Q. Lu, C. Si and X. Han, Int. J. Hydrog. Energy, 2025, 101, 627-635.

13 W. Hu, Q. Liu, T. Lv, F. Zhou and Y. Zhong, Electrochim. Acta, 2021, 381, 138276.

14 V. Singh, S. Singh, A. Tiwari, S. Dubey, S. Pandey, A. Yadav, R. Bhatia and V. Gamesan, Electrochim. Acta, 2026, 457, 147828.

15 H. Zou, B. He, P. Kuang, J. Yu and K. Fan, ACS Appl. Mater. Interfaces, 2018, 10, 22311−22319.