Scalable Metal–Organic Frameworks for Efficient Low Concentration CO₂ Capture under Humid Flue Gas Conditions

Supporting information

Thibaud Aumond,a, Mickaele Bonneau,a* Correntin Collomb,a Cécile Daniel,a David Farrussenga

a Université Claude Bernard Lyon 1, IRCELYON, UMR CNRS 5256, 2 avenue A. Einstein, 69626 Villeurbanne CEDEX, France

* Corresponding author: mickaele.bonneau@ircleyon.univ-lyon1.fr

Keywords: Metal Organic Framework, large scale, CO2 capture, realistic flue gas conditions

Characterization of the adsorbents

Figure S1: N2 physisorption isotherms (left) and diffractograms (right) of the different sorbents. For diffractograms, the simulated pattern is presented in dots.

Table S1. List of BET surface area obtained from N2 adsorption isotherms for all materials.

| Material | BET (m2 g-1) |
| --- | --- |
| CALF-20 | 560 |
| NaX | 871 |
| NaY | 930 |
| NaMOR | 63 |
| Al-fum | 1081 |
| MIL-120 | 378 |
| MIL-160 | 1192 |

Polanyi’s adsorption potential theory

Thermodynamic equilibrium is checked using Polanyi’s adsorption potential theory. This function is termed characteristic because it is representative of the fluid/solid system under study. Polanyi’s potential theory enables plotting the adsorbed phase volume (accounting for the molar volume of the adsorbate at the experimental temperature) as a function of the chemical adsorption potential, μ-µ0 (Equation S1):

Equation S1 µ-µ0=RTlnPP0

With R the gas constant (8.314 J K-1 mol-1), T the experimental temperature (K), P the equilibrium pressure, and P0 the saturation pressure at the given temperature. P/P0 can be directly read from the isotherms.

Scheme S1: Scheme of the dynamic custom-built setup used

Figure S2: CO2 adsorption isotherms performed at 0, 10, and 20 °C (top), and the resulting Polanyi’s adsorption potential theory (bottom), on CALF-20 (a), MIL-160 (b), NaMOR (c), NaX (d), NaY (e), MIL-120 (f), Al-Fum (g).

Figure S3: Cycles of adsorption/regeneration with a dry 2.5% CO2 concentration flow at 20 °C on MIL-160 (a) and MIL-120 (b).

Figure S4: Regeneration of CALF-20 (green) and MIL-120 (blue) at 80 °C..

Figure S5: Different steps of an adsorption/regeneration cycle of CO2 2.5% with relative humidity of 50%.