Agentic workflow enables the recovery of critical materials from complex feedstocks via selective precipitation

Andrew Ritchhart,a,# Sarah I. Allec,a,# Pravalika Butreddy,a Krista Kulesa,a Qingpu Wang,b Dan Thien Nguyen,a Maxim Ziatdinov,a,* Elias Nakouzia,c,*

SciLink Agent Descriptions

Planning agent. SciLink’s PlanningAgent is a stateful AI agent for experimental planning and iterative refinement in scientific workflows. The agent combines retrieval-augmented generation (RAG), multimodal reasoning, and human-in-the-loop feedback to generate executable experimental protocols from high-level research objectives. In particular, it uses a dual knowledge base for RAG in order to partition i) scientific knowledge, such as the scientific literature, user manuals, and reports, from ii) code-based knowledge, such as API documentation and code repositories. This partitioning enables efficient chunking for these two types of knowledge. Both knowledge bases use Facebook AI Similarity Search (FAISS)1 indices for efficient similarity search and support incremental updates to avoid redundant reprocessing.

In order to capture, persist, and manage context within and across interactions, all agent actions are tracked in a persistent state dictionary containing:

- Objective and iteration history

- Experimental plans with scientific justification

- Generated implementation code

- Human feedback log

- Experimental results from previous iterations

All planning agent outputs are available in the SI as json files (see *Experiment_Agent.json and *TEA_Agent_Analysis.json in Agent_Outputs/).

Bayesian optimization agent. SciLink’s BOAgent is a stateful AI agent for Gaussian-process-based Bayesian optimization (BO) with LLM-driven strategy configuration. Unlike traditional BO frameworks that require upfront hyperparameter selection and intensive model evaluation, the BOAgent uses vision-language models to inspect diagnostic plots and dynamically adjust acquisition strategies (e.g., switching from exploration to exploitation as data accumulates).

The agent is designed for stop-and-go experimental campaigns with human-in-the-loop: researchers run the agent, receive recommendations, perform experiments, and restart the agent. To allow users to shut down between optimization cycles and seamlessly resume the optimization loop where they left off, the agent maintains persistent state across experimental campaigns through checkpoint files. All context is reconstructed at each invocation by reading:

- The current data file (.xlsx or .csv), which contains all experimental results to date

- A state json file, which records the optimization trajectory, including past configurations, recommendations, budget context, and acquisition function metadata

This design accommodates realistic experimental timelines where data acquisition is the bottleneck and ensures that shutting down the process (intentionally or due to system failure) does not cause state loss. Each time the agent runs, it:

- Loads the complete experimental dataset from disk

- Reads the optimization history to understand past decisions and strategy evolution

- Computes any derived context needed for the current iteration (e.g., budget remaining, data points seen, current best parameters)

- Selects a strategy, fits the Gaussian process model, and recommends the next experiments

- Appends the new iteration to the history log on disk

An example is available in Agent_Outputs/SmCo_Round2_BO_Agent.state.json.

Separation and Characterization Methods

Opentrons System

Experiments were performed on the Opentrons platform using a Flex model Opentrons liquid handling robot equipped with an XYZ lateral-motion gripper as well as P1000 single- and 8-channel pipettes (5-1000 μL). Every liquid-handling experiment was equipped with new Opentrons pipet tips, NEST liquid reservoirs, and microtiter well plates. All disposable labware is ANSI/SLAS-format. All Opentrons manipulations were programmed and edited through python-based protocols. Before running protocols, all disposable deck elements were manually calibrated to labware-specific positional offsets. Protocols retrieved polypropylene non-filtered 1000-, 200- and 50-μL pipet tips from Opentrons tip racks. Experimental solutions originated from 15- to 195-mL single- and 12-well NEST reservoirs. Solutions were transferred into and further processed in Caplugs Evergreen polypropylene flat-bottom 96-well plates (0.37 mL) and Agilent InfinityLab polypropylene round-bottom 96-well plates (0.5 mL, 1.2 mL, 2.0 mL). Microtiter samples were heated and/or agitated by the Opentrons Heater-Shaker Module up 95 °C and 3000 rpm.

ICP-MS Elemental Analysis

High-throughput ICP-MS of samples prepared via Opentrons experiments were measured using an Agilent 8900 QQQ instrument. Samples were centrifuged in an Eppendorf 5810 R 15-amp centrifuge for 10 min at 4500 RPM and room temperature, then subsequently digested in 400 µL of 3 M trace metal grade nitric acid, covered, and incubated at 60 °C overnight. Samples were diluted in 2% acid matrix and data were acquired in He option gas mode.

UV-Vis Spectroscopy

High-throughput UV-Vis were collected using a Thermofisher Varioskan LUX. Digested SmCo samples were measured around the Co2+ transition from 460 to 610 nm using 1 nm slit width and 200 ms dwell time.

Feedstock Preparation Methods

Samarium Cobalt magnet leachate generation

Grade 18 Samarium Cobalt disc magnets (SmCo₅) were purchased from Magnetshop (Product No. 18DRE1304). For de-magnetization, the magnet discs were vacuum-sealed in a quartz ampoule and heated to 700 °C at a ramp rate of 10 °C/min. The temperature was held constant for 2 hours in a tube furnace, followed by natural cooling to room temperature. Afterward, the magnet discs were manually crushed into fine powder using an agate mortar and pestle for approximately 10 minutes to ensure uniform particle size.

The leaching solution was prepared by diluting concentrated sulfuric acid (98%, Sigma-Aldrich) to obtain a 2 M H2SO4 solution. A total of 4 g of SmCo5 magnet powder was added to 200 mL of the prepared 2M H2SO4 solution. The mixture was stirred continuously at a constant rate of 200 rpm for 72 hours at room temperature to facilitate dissolution. After the reaction period, the solution was extracted from the remaining solid residues for further analysis. The composition of the leaching solution was determined using ICP-MS.

Neodymium magnet leachate generation

NdFeB magnets (grade N42, 0.25’’× 0.25’’× 0.25’’ cubes, part number B444; K&J Magnetics) were processed to generate leachate using previously reported hydrometallurgical methods.2,3 The magnets were first demagnetized by heating at 650°C for 2 h in a box furnace (FD1545M, Thermolyne). The demagnetized material was then ground in a tungsten carbide-lined vial using a ball mill (BM-400-115, Cole-Parmer) for 1 h. The resulting magnet powder was leached in 2.0 M H2SO4 at a pulp density of 100 g/L. The slurry was stirred for 3 days at room temperature and subsequently centrifuged to collect the leachate.

For elemental analysis, leachate samples were digested in 70% HNO3 overnight, diluted to final concentrations of 10 – 500 ppb, and analyzed by inductively coupled plasma mass spectrometry (ICP-MS, Thermo Scientific iCAP Q and Elemental Scientific seaFAST autosampler).

Fig. S1. Photographs of NdFeB magnet samples at different steps of the leachate generation process.

Fig S2. Produced water bulk experiments

We aimed to scale up the recovery of magnesium from produced water using bulk precipitation with NaOH as recommended by CICERO. Direct magnesium recovery was achieved at high alkalinity; the addition of 9 mL 0.5 M NaOH into 20 mL of the produced water increased the pH to 12.07, and we were able to recover ~0.11g of pure magnesium-rich precipitates (98.68 mol% Mg, 0.62 mol% Na, and 0.69 mol% Ca).

Fig S3. Reproducibility of the Opentrons Separations Experiments

a.

b.

Typical standard deviation of elements measured by ICP-MS was determined via 12 replicate experiments at each condition of the produced water precipitation. Higher standard deviations were observed prior to complete precipitation of an element and for trace elements.

Figure S4. High-Throughput UV-Vis Spectra

a.

b.

High throughput UV-Vis spectra were obtained using a Thermofisher Varioskan LUX microplate reader. SmCo digests were measured from 460 to 610 nm. The concentrations determined from this method were compared to values from ICP-MS and found to be in highly linear with slope = 0.97. These results support UV-Vis as a robust high throughput metric for automated experiments where UV-Vis signatures are available. Example data are shown for Round 2 of SmCo extraction.

Fig S5. Comparison of Purity vs Yield

For the experimental campaigns described in the text, purity of the desired element (Sm/Nd/Pr) was used and found to be a robust metric for the planning and Bayesian optimization agents. A more detailed technoeconomic metric considering factors such as the nonlinearity of purity and value is beyond the scope of this study, however would be possible with the current agentic capabilities and could lead to different optimizations.

- NdFeB Round 2:

Within the current datasets we consider the product of separation factor and yield as a first order approximation of this. It is clearly seen that while the low-equivalent regime of added oxalate has the best Nd:Pr separation factor, the absolute yield and by extension value of extracted material is much lower.

- SmCo Round 2:

Fig S6. Bayesian Optimization Acquisition Functions

SmCo Round 1 Results:

SmCo Round 2 Results:

Fig S7. SciLink Prompts

The following input prompts were used when generating experimental plans using SciLink’s natural language interface. Full outputs are available in supplemental json files.

Techno-economic Objective (Same for all cases):

“Using the DOE assessment report, the PWS database, and the provided criticality matrix image as context, analyze the ICP-MS results to determine which "measured critical materials show concentrations that might be economically interesting for recovery, considering their market value.”

Experiment Objective (Same for all round 1 cases):

“Based on the ICP-MS results and the prior TEA identifying valuable materials, a simple chemical process (like precipitation) to selectively recover the most promising material from the water sample. Use only reagents that are simple commodity chemicals. In your proposal specifically identify a range of conditions for concentrations, ratios, solubilities, or other variable for testing optimal recovery. Put these conditions in a table for a 96 well plate and using an opentrons. The experiment should cover a wide range of conditions which may span into the non-recovery regime, so as to provide the most data. Rather than measure pH estimate required amounts of acid or base. Prefer additional conditions spread over the columns and rows rather than replicate trials. Target a maximum 360 μL total volume, and prefer to use concentrations at most 1M. Provide corresponding Opentrons code, requirements for this code are in Opentrons_Setup.txt”

Second Round NdFeB Experiment Objective:

Here are the results of an experiment trying to preferentially precipitate and separate Nd from a stock solution made from NdFeB. The experiment used NaOH and NaOxalate in various amounts to see which did a better job of extracting Nd. The experiment done was by Opentrons and is in BFeNd.py. You should also observe the png graphed results. There are two subsquent tasks for the next experiment:

1: Determine which method was superior overall, NaOH or NaOxalate and justify

2: Create a plan for further purifying the Nd containing material, which also contains other trace elements

The requirements for experiment are as before:

Propose a simple chemical process (like precipitation) to selectively recover the most promising material from the water sample. Use only reagents that are simple commodity chemicals. In your proposal specifically identify a range of conditions for concentrations, ratios, solubilities, or other variable for testing optimal recovery of the most valuable component(s). Arrange these conditions as a matrix for a 96 well plate and using an opentrons. The experiment should cover a wide range of conditions which may span into the non-recovery regime, so as to provide the most data. Rather than measure pH estimate required amounts of acid or base. Prefer additional conditions spread over the columns and rows rather than replicate trials. Target a maximum 400 μL total volume, and prefer to use concentrations at most 1M. Provide corresponding Opentrons code, ensure compliance of this code with descriptions in Opentrons_Setup.txt.

Second Round SmCo BO-Informed Experiment Objective:

Our goal is to create a second round of experiments to refine results of a precipitation experiment. We previously Dispensed 1.0M NaOH along the 8 rows of a 96 wellplate and 1.0M Bicarbonate along the 12 columns. Bayesian optimization has found the following values: Compose round 2 as another 96 plate with NaOH and Bicarbonate in rows and columns. Based on these values in batch_step_1.csv compose a range of conditions to span the 96 wellplate that reflect the bayesian values and clustering. Target a maximum 400 uL total volume, using 200 of starting material and use water for any missing volume below that 400. Provide corresponding Opentrons Code, requirements for this code are in Opentrons_Setup.txt and api context in opentrons_api.txt.

Fig S8. Code Feedback Examples

The natural language feedback feature can be used for both small adjustments and corrections or larger semantic changes to experimental design:

Feedback given for SmCo Round 2:

Example A.

tiprack = protocol.load_labware('opentrons_flex_96_tiprack_1000ul', 'C2')

pipette.pick_up_tip()

Feedback:

“make sure to specify using the smaller 200 tips for NaOH and Bicarbonate since those values are small"

tiprack_1000 = protocol.load_labware('opentrons_flex_96_tiprack_1000ul', 'C2')

tiprack_200 = protocol.load_labware('opentrons_flex_96_tiprack_200ul', 'C3')

pipette.pick_up_tip(tiprack_200)

Example B.

# Dispense to each well

for row_idx, row in enumerate(rows):

for col_idx, col in enumerate(columns):

well = plate[f'{row}{col}']

naoh_vol = naoh_volumes[row_idx]

bicarb_vol = bicarbonate_volumes[col_idx]

water_vol = 200 - naoh_vol - bicarb_vol

# Ensure water volume is not negative

if water_vol < 0:

water_vol = 0

# Dispense leachate (200 µL)

pipette.pick_up_tip()

pipette.aspirate(200, leachate)

pipette.dispense(200, well)

pipette.drop_tip()

# Dispense NaOH if volume > 0

if naoh_vol > 0:

pipette.pick_up_tip()

pipette.aspirate(naoh_vol, naoh)

pipette.dispense(naoh_vol, well)

pipette.drop_tip()

# Dispense Bicarbonate if volume > 0

if bicarb_vol > 0:

pipette.pick_up_tip()

pipette.aspirate(bicarb_vol, bicarbonate)

pipette.dispense(bicarb_vol, well)

pipette.drop_tip()

# Dispense water if volume > 0

if water_vol > 0:

pipette.pick_up_tip()

pipette.aspirate(water_vol, water)

pipette.dispense(water_vol, well)

pipette.drop_tip()

Feedback:

"change the looping to go in order: leachate, water, NaOH, bicarbonate. Finish each reagent for the entire plate then move to the next"

Revised Code Snippet:

# Step 1: Dispense leachate (200 \u00b5L) to all wells using 1000 \u00b5L tips

protocol.comment(\"Step 1: Dispensing leachate to all wells\")

for row in rows:

for col in columns:

well = plate[f'{row}{col}']

pipette.pick_up_tip(tiprack_1000)

pipette.aspirate(LEACHATE_VOLUME, leachate)

pipette.dispense(LEACHATE_VOLUME, well)

pipette.drop_tip()

# Step 2: Dispense water to all wells (where volume > 0) using 1000 \u00b5L tips

protocol.comment(\"Step 2: Dispensing water to all wells\")

for row in rows:

for col in columns:

well_name = f'{row}{col}'

well = plate[well_name]

water_vol = water_volumes[well_name]

if water_vol > 0:

pipette.pick_up_tip(tiprack_1000)

pipette.aspirate(water_vol, water)

pipette.dispense(water_vol, well)

pipette.drop_tip()

# Step 3: Dispense NaOH to all wells (where volume > 0) using 200 \u00b5L tips for accuracy

protocol.comment(\"Step 3: Dispensing NaOH to all wells (using 200 \u00b5L tips for small volumes)\")

for row_idx, row in enumerate(rows):

naoh_vol = naoh_volumes[row_idx]

if naoh_vol > 0:

for col in columns:

well = plate[f'{row}{col}']

pipette.pick_up_tip(tiprack_200)

pipette.aspirate(naoh_vol, naoh)

pipette.dispense(naoh_vol, well)

pipette.drop_tip()

# Step 4: Dispense Bicarbonate to all wells (where volume > 0) using 200 \u00b5L tips for accuracy

protocol.comment(\"Step 4: Dispensing bicarbonate to all wells (using 200 \u00b5L tips for small volumes)\")

for col_idx, col in enumerate(columns):

bicarb_vol = bicarbonate_volumes[col_idx]

if bicarb_vol > 0:

for row in rows:

well = plate[f'{row}{col}']

pipette.pick_up_tip(tiprack_200)

pipette.aspirate(bicarb_vol, bicarbonate)

pipette.dispense(bicarb_vol, well)

pipette.drop_tip()

References:

(1) M. Douze et al., "THE FAISS LIBRARY," in IEEE Transactions on Big Data, doi: 10.1109/TBDATA.2025.361847.

(2) Lyman, J.; Palmer, G., Recycling of Rare Earths and Iron from NdFeB Magnet Scrap. High Temperature Materials and Processes 1993, 11 (1-4), 175-188.

(3) Kumari, A.; Jha, M. K.; Pathak, D. D., An Innovative Environmental Process for the Treatment of Scrap Nd-Fe-B Magnets. Journal of Environmental Management 2020, 273, 111063.