Supporting Information

First-Principles Screening of TM@C4N4 Single-Atom Catalysts for Lithium–Sulfur Batteries

Pengwu Wang, Pengbo Lyu*

a Key Laboratory of Low Dimensional Materials and Application Technology of Ministry of Education, School of Materials Science and Engineering, Xiangtan University, Xiangtan 411105, China

b Hunan Provincial Key Laboratory of Thin Film Materials and Devices, School of Materials Science and Engineering, Xiangtan University, Xiangtan 411105, China

⁎Corresponding author.

Email: pengbo.lyu@xtu.edu.cn (P. Lyu)

Fig. S1. Top and side views of C4N4 and all TM@ C4N4 (TM = Ti, V, Cr, Sc, Mn, Fe, Co, Ni, Cu, Zn) fully optimized configurations.

Fig. S2. the total and partial density of states (DOS) of TM@ C4N4 (TM = Ti, Sc, V, Ti, Cr, Mn, Fe, Co, Ni, Zn) configurations.

DME:

DOL:

-0.77eV

-0.81eV

-0.88eV

-0.83eV

-0.84eV

-0.83eV

Fig. S3. The stable adsorption configurations and adsorption energies of 1,3-dioxolane (DOL) and 1,2-dimethoxyethane (DME) solvent molecules for soluble polysulfides (Li2S4, Li2S6, and Li2S8).

Ti@C4N4

Cr@C4N4

Cu@C4N4

Co@C4N4

Fig. S4. The fully relaxed lowest-energy binding configurations of S8/Li2Sx (x = 1, 2, 4, 6, 8) on TM@ C4N4 (TM = Cu, Ti, Co, Cr) surfaces. Herein, the top and side views are given, respectively.

Fig. S5. Projected crystal orbital Hamilton population (pCOHP) analyses of the TM–S bonds in Li2S adsorbed

- The adsorption energies of TM@ C4N4 (TM = V, Cr, Mn, Fe, Co, Sc, Ti, Ni, Zn) to S8/LiPSs, as well as the organic electrolyte solvent molecules of 1, 3-dioxolane (DOL) and 1, 2-dimethoxyethane (DME) to soluble LiPSs.

| Structures | S8 (eV) | Li2S8 (eV) | Li2S6 (eV) | Li2S4 (eV) | Li2S2 (eV) | Li2S (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| V@C4N4 | -2.06 | -3.37 | -2.51 | -2.29 | -3.01 | -4.22 |
| Cr@C4N4 | -1.86 | -2.70 | -2.29 | -2.11 | -2.27 | -3.64 |
| Mn@C4N4 | -1.66 | -2.31 | -1.83 | -1.56 | -1.75 | -2.91 |
| Fe@C4N4 | -1.67 | -0.62 | -1.68 | -1.75 | -2.53 | -3.09 |
| Co@C4N4 | -1.36 | -1.88 | -1.52 | -1.45 | -1.48 | -1.46 |
| Ni@C4N4 | -0.74 | -1.79 | -1.42 | -1.09 | -1.44 | -1.65 |
| Sc@C4N4 | -1.66 | -0.53 | -0.27 | -2.63 | -2.56 | -1.25 |
| Ti@C4N4 | -2.59 | -3.98 | -3.66 | -3.38 | -3.87 | -5.42 |
| Cu@C4N4 DOL DME | -1.32 / / | -1.79 -0.83 -0.84 | -1.43 -0.88 -0.83 | -1.13 -0.81 -0.77 | -1.56 / / | -2.03 / / |

- The Gibbs free-energy change and Li2S dissociation energy-barrier (Ebarrier) of each reaction for the discharging process in LiSBs.

| TM@C4N4 | ∆G1 (eV) | ∆G2 (eV) | ∆G3 (eV) | ∆G4 (eV) | ∆G5 (eV) |
| --- | --- | --- | --- | --- | --- |
| V@C4N4 | -3.61 | -0.52 | -0.77 | -0.91 | 2.53 |
| Cr@C4N4 | -3.13 | -0.97 | -0.81 | -0.34 | 2.37 |
| Mn@C4N4 | -2.95 | -0.90 | -0.71 | -0.38 | 2.58 |
| Fe@C4N4 | -2.67 | -1.02 | -1.06 | -2.38 | 4.60 |
| Co@C4N4 | -2.82 | -1.03 | -0.91 | -0.23 | 3.77 |
| Ni@C4N4 | -3.34 | -1.01 | -0.66 | -0.54 | 3.54 |
| Ti@C4N4 | -3.68 | -1.06 | -0.71 | -0.68 | 2.20 |
| Sc@C4N4 | -1.16 | -1.12 | -0.68 | -0.12 | 2.39 |
| Cu@C4N4 | -2.76 | -1.02 | -0.68 | -0.62 | 3.28 |

- Relative energies of reaction images along the NEB pathway.

| TM@C4N4 | 01 (eV) | 02 (eV) | 03 (eV) | 04 (eV) | 05 (eV) | 06 (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| V@C4N4 | 0.00 | 0.24 | 0.37 | 0.13 | -1.07 | -2.20 |
| Cr@C4N4 | 0.00 | 0.22 | 0.38 | 0.07 | -1.08 | -2.36 |
| Mn@C4N4 | 0.00 | 0.15 | 0.44 | 0.27 | -0.83 | -2.08 |
| Fe@C4N4 | 0.00 | 0.22 | 0.49 | 0.32 | -0.77 | -1.98 |
| Cu@C4N4 | 0.00 | 0.19 | 0.89 | 0.61 | -0.62 | -1.42 |
| Sc@C4N4 | 0.00 | 0.51 | 0.60 | 0.24 | -0.91 | -2.02 |

- Calculated TM–S bonding strength (ICOHP), Li–S bond lengths in adsorbed *Li2S, and adsorption energies (Eₐ) for *Li2S on TM@C₄N₄ single-atom catalysts.

| TM@C4N4 | ICOHPTM-S | B(Li1-S) (Å) | B(Li2-S) (Å) | Ea(*Li2S) (eV) |
| --- | --- | --- | --- | --- |
| Ti@C4N4 | -3.88 | 2.35 | 2.35 | -5.42 |
| Mn@C4N4 | -3.30 | 2.25 | 2.25 | -2.91 |
| Ni@C4N4 | -0.58 | 2.27 | 2.26 | -1.65 |
| Co@C4N4 Cu@C4N4 Cr@C4N4 Fe@C4N4 Sc@C4N4 | -2.92 -2.68 -3.31 -3.26 -2.76 | 2.18 2.20 2.31 2.21 2.27 | 2.18 2.21 2.29 2.21 2.27 | -1.46 -2.03 -3.64 -3.09 -1.25 |