Supplementary Information for

Balancing Stability and Reactivity: A Robust Pd(II) Biaryl Precatalyst for Rapid Generation of Catalytically Active Pd(0) Species

Weiqi Li a Tomoki Iida,a Manaka Kaneko,a Ziwei Hu,a Takaki Kanbara,a and Junpei Kuwabara* a,b

a Institute of Pure and Applied Sciences, University of Tsukuba 1-1-1 Tennodai, Tsukuba, Ibaraki 305-8573, Japan.

b Tsukuba Research Center for Energy Materials Science (TREMS), Institute of Pure and Applied Sciences, University of Tsukuba 1-1-1 Tennodai, Tsukuba, Ibaraki 305-8573, Japan. E-mail: kuwabara@ims.tsukuba.ac.jp

Table of Contents (Supporting Information)

General Information	3

Synthesis
Synthesis of PdBr(4-nitrophenyl)(tmeda)	4
Synthesis of Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda) (Pd precat. 1)	4
Synthesis of PdBr(phenyl)(tmeda)	4
Synthesis of Pd(phenyl)(pentafluorophenyl)(tmeda) (Pd precat. 2)	5
Synthesis of Pd(2,3,5,6-tetrafluoroanisole)₂(pyridine)₂	5

Reactivity Studies
Reductive elimination reaction in the presence of tri-tert-butylphosphine	5

Reductive elimination reaction in the presence of P{3,5-(CF3)2C6H3}3	6

Catalytic Reactions
Suzuki–Miyaura cross-coupling reactions	6
C–N coupling reactions	6

Application to Functional Materials
Synthesis of Spiro-OMeTAD 	7
Polycondensation	7

Schemes
Scheme S1. Reported side reactions involved in Pd(0) generation	8
Scheme S2. Generation of Pd(0) from Buchwald precatalyst	9
Scheme S3. Reactivity of Pd(naphthyl)(C₆F₅)(tmeda)	9

Tables
Table S1. Conversion of active Pd(0) species	10
Table S2. TON and TOF for C–N coupling reactions	11

Figures
Figure S1–S11. Stability and reductive elimination studies 	12-18
Figure S12–S16. Catalytic reaction analyses and polymers	19-21
Figure S17–S29. NMR spectra of Pd complexes 	20-28

References 	29

General

1H, 13C{1H}, 19F, and 31P NMR spectra were recorded using Bruker AVANCE-400 and AVANCE-600 NMR spectrometers. Tetramethylsilane was used as an internal standard (0 ppm) for 1H and 13C{1H} NMR spectra. Hexafluorobenzene was used as an internal standard (-163.0 ppm) for 19F NMR spectra. Trimethyl phosphate was used as an internal standard (3.0 ppm) for 31P NMR spectra. Elemental analyses were carried out using a Yanaco CHN Corder MT-5 or MT-6. Single-crystal X-ray diffraction data were collected on a Rigaku XtaLAB Synergy-R diffractometer with Cu Kα radiation. Crystallographic data for Pd precat. 1 have been deposited with the Cambridge Crystallographic Data Centre under deposition number CCDC 2338611. MALDI-TOF-MS spectra were recorded on an AB SCIEX TOF/TOFTM 5800 system. Pd2(dba)3 and PdCl2 (Kojima Chemicals Co., Ltd.) were used as precursors for the Pd complexes. Dry solvents were purchased from Kanto Chemical. All other reagents were purchased from Tokyo Chemical Industry Co., Ltd. (TCI), Sigma-Aldrich, and FUJIFILM Wako Pure Chemical Corporation. Pd(C6F5)2(tmeda),1 PdCl2(pyridine)2,1 Pd(C6F5)2(pyridine)2,1 and Pd(C6F5)2(acetonitrile)22 were prepared according to literature methods.

Synthesis

Synthesis of PdBr(4-nitrophenyl)(tmeda).3

To a 50 mL Schlenk tube, Pd2(dba)3 (275 mg, 0.30 mmol), 1‑bromo‑4‑nitrobenzene (364 mg, 1.8 mmol), N,N,N′,N′-tetramethylethylenediamine (234 µL, 1.5 mmol), and THF (5.0 mL) were added under N2, and the mixture was stirred for 16 h at 60 °C. After removal of the volatiles, the residue was extracted with chloroform. Following filtration through Celite, the filtrate was concentrated to dryness under reduced pressure. PdBr(4‑nitrophenyl)(tmeda) was isolated by washing with hot hexane (222 mg, 87%). 1H NMR (600 MHz, CDCl3, Figure S17): δ 7.81 (d, J = 8.4 Hz, 2H, 1-H), 7.57 (d, J = 8.4 Hz, 2H, 2-H), 2.78 (t, J = 5.4 Hz, 2H, 5-H or 6-H), 2.68 (s, 6H, 3-H or 4-H), 2.62 (t, J = 5.4 Hz, 2H, 5-H or 6-H), 2.44 (s, 6H, 3-H or 4-H). 13C{1H} NMR (151 MHz, CDCl3, Figure S18): δ 163.58 (7-C), 145.28 (8-C), 135.63 (2-C), 120.25 (1-C), 62.82 (5-C or 6-C), 58.48 (5-C or 6-C), 50.79 (3-C or 4-C), 48.77 (3-C or 4-C).

Synthesis of Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda), Pd precat. 1.

To a 50 mL Schlenk tube containing pentafluorobenzene (49.4 µL, 0.45 mmol) and diethyl ether (6.0 mL), n-BuLi (1.51 M in hexane, 0.30 mL, 0.45 mmol) was added dropwise at –78 °C under N2, and the mixture was stirred for 1 h. PdBr(4-nitrophenyl)(tmeda) (191 mg, 0.45 mmol) was then added. The reaction mixture was allowed to warm to room temperature and stirred for 16 h. After removal of the volatiles, the residue was extracted with chloroform. Following filtration through Celite and concentration, Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda) was isolated by silica gel column chromatography (chloroform/hexane = 8:2) as a yellow solid (211 mg, 91%). 1H NMR (600 MHz, CDCl3, Figure S19): δ 7.73 (dt, J =8.8, 2.1 Hz, 2H, 1-H), 7.66 (d, J = 8.4 Hz, 2H, 2-H), 2.77 (t , J = 5.4 Hz, 2H, 5-H or 6-H), 2.66 (t, J = 5.4 Hz, 2H, 5-H or 6-H), 2.44 (s, 6H, 3-H or 4-H), 2.41 (s, 6H, 3-H or 4-H). 19F NMR (564 MHz, CDCl3, Figure S20): δ –119.25 (dd, J =23.1, 6.5 Hz, 2F, 1-F), –161.61 (t, J = 20.0 Hz, 1F, 3-F), –163.72 to –163.83 (m, 2F, 2-F). 13C{1H} NMR (151 MHz, CDCl3, Figure S21): δ171.18 (7-C), 147.06 (dm, JF = 223.4 Hz, 10-C), 144.46 (8-C), 136.61 (dm, JF = 242.2 Hz, 12-C), 136.44 (2-C), 135.97 (dm, JF = 252.1 Hz, 11-C), 120.92 (t, JF = 55.8 Hz, 9-C), 119.97 (1-C), 60.85 (5-C or 6-C), 59.26 (5-C or 6-C), 49.05 (3-C or 4-C), 48.81 (3-C or 4-C). EA: Found. C 42.19%, H 3.81%, N 8.18%; Calcd. For C18H20F5N3O2Pd: C 42.24%, H 3.94%, N 8.21%.

Synthesis of PdBr(phenyl)(tmeda). 4

To a 50 mL Schlenk tube, Pd2(dba)3 (274.7 mg, 0.30 mmol), bromobenzene (1.26 mL, 12 mmol), N,N,N′,N′-tetramethylethylenediamine (234 µL, 1.5 mmol), and THF (5.0 mL) were added under N2, and the mixture was stirred for 16 h at 60 °C. After removal of the volatiles, the residue was extracted with chloroform. Following filtration through Celite, the filtrate was concentrated to dryness under reduced pressure. PdBr(phenyl)(tmeda) was isolated by washing with hot hexane (194 mg, 85%). 1H NMR (600 MHz, CDCl3, Figure S22): δ7.27-7.26 (m, 2H, 1-H), 6.96-6.93 (m, 2H, 2-H), 6.84 (tt, J = 7.2, 1.2 Hz, 1H, 3-H), 2.75 (t, J = 5.4 Hz, 2H, 6-H or 7-H), 2.65 (s, 6H, 4-H or 5-H), 2.58 (t, J = 5.4 Hz, 2H, 6-H or 7-H), 2.42 (s, 6H, 4-H or 5-H). 13C{1H} NMR (151 MHz, CDCl3, Figure S23): δ 147.47 (8-C), 135.11 (1-C), 126.53 (2-C), 122.69 (3-C), 62.57 (6-C or 7-C), 58.12 (6-C or 7-C), 50.44 (4-C or 5-C), 48.40 (4-C or 5-C).

Synthesis of Pd(phenyl)(pentafluorophenyl)(tmeda), Pd precat. 2.

To a 50 mL Schlenk tube containing pentafluorobenzene (49.4 µL, 0.45 mmol) and diethyl ether (6.0 mL), n-BuLi (1.51 M in hexane, 0.30 mL, 0.45 mmol) was added dropwise at –78 °C under N2, and the mixture was stirred for 1 h. PdBr(phenyl)(tmeda) (170 mg, 0.45 mmol) was then added. The reaction mixture was allowed to warm to room temperature and stirred for 16 h. After removal of the volatiles, the residue was extracted with chloroform. Following filtration through Celite and concentration, Pd(phenyl)(pentafluorophenyl)(tmeda) was isolated by silica gel column chromatography (chloroform/hexane = 6:4) as a yellow solid (151 mg, 72%). 1H NMR (600 MHz, CDCl3, Figure S24): δ7.42 (d, J = 7.8 Hz, 2H, 1-H), 6.89-6.87 (m, 2H, 2-H), 6.80 (tt, J = 7.2, 1.8 Hz, 1H, 3-H), 2.73 (t, J = 5.4 Hz, 2H, 6-H or 7-H), 2.61 (t, J = 5.4 Hz, 2H, 6-H or 7-H), 2.40 (s, 6H, 4-H or 5-H), 2.39 (s, 6H, 4-H or 5-H). 19F NMR (564 MHz, CDCl3, Figure S25): δ –118.59 (dd, J = 25.4, 5.9 Hz, 2F, 1-F), –163.11 (t, J = 20.0 Hz, 1F, 3-F), –164.52 to –164.66 (m, 2F, 2-F). 13C{1H} NMR (151 MHz, CDCl3, Figure S26): δ154.07 (C-8), 147.20 (dm, JF = 222.2 Hz, C-10), 136.34 (C-1), 136.20 (dm, JF = 241.0 Hz, C-12), 135.87 (dm, JF = 251.0 Hz, C-11), 126.30 (C-2), 123.16 (t, JF = 58.0 Hz, C-9), 122.22 (C-3), 60.77 (6-C or 7-C), 58.97 (6-C or 7-C), 48.82 (4-C or 5-C), 48.59 (4-C or 5-C). Elemental analysis: Found. C 46.59%, H 4.55%, N 5.85%; Calcd. For C18H21F5N2Pd: C 46.32%, H 4.53%, N 6.00%.

Synthesis of Pd(2,3,5,6-tetrafluoroanisole)2(pyridine)2.

To a 50 mL Schlenk tube containing 2,3,5,6-tetrafluoroanisole (228 µL, 1.8 mmol) and diethyl ether (8.8 mL), n-BuLi 1.6 M in hexane (1.1 mL, 1.8 mmol) was added dropwise at –78 °C under N2 and stirred for 1 h, PdCl2(pyridine)2 (168 mg, 0.50 mmol) was then added. The tube was allowed to warm to room temperature and stirred for 16 h. After removal of the volatiles, residue was extracted with warm acetone and concentrated. Upon addition of ethanol, Pd(2,3,5,6-tetrafluoroanisole)2(pyridine)2 was isolated by recrystallization (56.2 mg, 18%). 1H NMR (600 MHz, CDCl3, Figure S27): δ 8.77 (d, J = 5.2 Hz, 4H, 1-H), 7.63 (t, J = 7.7 Hz, 2H, 3-H), 7.23-7.20 (m, 4H, 2-H), 3.87 (s, 6H, 4-H). 19F NMR (564 MHz, CDCl3, Figure S28): δ -123.7 (dt, J = 20.9, 9.2 Hz, 4F, 1-F), -157.9 (dt, J = 22.6, 8.2 Hz, 4F, 2-F). 13C{1H} NMR (151 MHz, CDCl3, Figure S29): δ 153.56 (1-C), 148.55 (ddd, JF = 222.0, 26.6, 8.8 Hz, 6-C), 139.88 (ddd, JF = 252.0, 24.7, 4.7 Hz, 7-C), 137.48 (3-C), 134.19 (m, 8-C), 125.87-125.21 (m, 5-C), 125.21 (2-C), 62.01 (t, JF = 3.3Hz, 4-C) Anal. Calcd. for C24H16F8N2O2Pd, %: C, 46.28; H, 2.59; N, 4.50. Found: C, 46.24; H, 2.84; N, 4.16.

Reductive elimination reaction in the presence of tri-tert-butylphosphine

To a Wilmad vacuum NMR sample tube were added, inside a glovebox, Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda) (5.1 mg, 0.010 mmol), tri-tert-butylphosphine (4.2 mg, 0.021 mmol), 4,4′-dimethoxyoctafluorobiphenyl (3.6 mg, 0.010 mmol, used as a fluorine internal standard for quantification), trimethyl phosphate (2.3 μL, 0.020 mmol, used as a phosphorus internal standard for quantification), and toluene-d₈ (600 μL). The tube was sealed and heated at 80 °C to monitor the generation of Pd[P(t-Bu)3]2 and the eliminated biaryl compounds.5 1H NMR (600 MHz, toluene-d₈, Figure S4): δ 7.73 (d, J = 12.0 Hz, 2H), 6.84 (d, J = 12.0 Hz, 2H). 19F NMR (564 MHz, CDCl3, Figure S5): δ -143.8 (m, 2F), -153.9 (m, 1F), -161.9 (m, 2F).

Reductive elimination reaction in the presence of P{3,5-(CF3)2C6H3}3

To a Wilmad vacuum NMR sample tube were added, inside a glovebox, Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda) (2.6 mg, 0.005 mmol), P{3,5-(CF3)2C6H3}3 (10.7 mg, 0.016 mmol), 4,4′-dimethoxyoctafluorobiphenyl (1.8 mg, 0.005 mmol, used as a fluorine internal standard), and toluene-d8 (600 μL). The tube was sealed, and the solution was analysed by NMR spectroscopy prior to heating. The reaction mixture was then heated at 80 °C, and the reaction was monitored by NMR. After 140 min, completion of the reductive elimination reaction was confirmed by 19F NMR spectroscopy (Figure S9). Because the product, Pd[P{3,5-(CF3)2C6H3}3]3, is insoluble in toluene-d8, the signal of P{3,5-(CF3)2C6H3}3 decreased as reductive elimination proceeds (Figure S9b). Indeed, the formation of yellow crystals was clearly observed during the reaction. The solvent was subsequently removed under reduced pressure, and THF-d8 and trimethyl phosphate (4.6 μL, 0.040 mmol, used as a phosphorus internal standard) were added. The resulting solution was analysed by 31P NMR spectroscopy (Figure S10), leading to the identification of Pd[P{3,5-(CF3)2C6H3}3]3. 31P NMR spectrum (243 MHz, THF-d8, 243 MHz): δ 26.3 (s, 3P).6

The Suzuki-Miyaura cross-coupling reactions

To a 25 mL Schlenk tube, a mixture of Pd source (0.0025 mmol of Pd relative to 2-chloropyridine), 2-chloropyridine (47.0 µL, 0.50 mmol), phenylboronic acid (64.0 mg, 0.53 mmol), K2CO3 (138 mg, 1.0 mmol), ferrocene (18.6 mg, 0.10 mmol, used as an internal standard), 1,4-dioxane (1.0 mL) were added under N2. When Pd precat. 1 was used, a phosphine ligand (0.0055 mol%) was added. The mixture was stirred for 4 h at 100 °C. The 1H NMR spectrum was recorded to determine an NMR yield of 2-phenylpyridine.7

C-N coupling reactions

To a 25 mL Schlenk tube, a mixture of Pd source (0.0050 mmol of Pd), rac-BINAP (4.7 mg, 0.0075 mmol, added in a Glove box), NaOt-Bu (135 mg, 1.4 mmol, added in a glove box), 1,3,5-trimethoxybenzene (16.8 mg, 0.10 mmol as an internal standard), 4-bromotoluene (123 μL, 1.0 mmol), and morpholine (105 μL, 1.2 mmol) were added under N2. The mixture was stirred at 80 °C for 24 h. The 1H NMR spectrum was recorded to determine an NMR yield of 4-(4-methylphenyl)morpholine.8 1H NMR (400 MHz, CDCl3, Figure S13): δ 7.09 (d, J = 8.0 Hz, 2H, 2-H), 6.83 (d, J = 8.8 Hz, 2H, 3-H), 3.85 (t, J = 4.8 Hz, 4H, 5-H), 3.10 (t, J = 4.8 Hz, 4H, 4-H), 2.28 (s, 3H, 1-H).

Synthesis of Spiro-OMeTAD

To a 25 mL Schlenk tube, Pd precat. 1 (0.64 mg, 0.0013 mmol) and 2,2',7,7'-tetrabromo-9,9'-spirobifluorene (158 mg, 0.25 mmol) were added. The Schlenk tube was transferred into a glovebox, bis(4-methoxyphenyl)amine (287 mg, 1.3 mmol), NaOt-Bu (144 mg, 1.5 mmol), P(t-Bu)3 (0.01 mol/L in toluene, 0.25 mL, 0.0025 mmol), and toluene (7.75 mL) were added. Then the Schlenk tube was taken out from the glove box, mesitylene (34.8 μL, 0.25 mmol) was added under N2 as an internal standard. The mixture was stirred at 90°C for 2 h. After cooling to room temperature, the quantitative formation of the product was confirmed by 1H NMR spectroscopy. The volatiles were then removed under reduced pressure. The yellow solid product 2,2',7,7'-tetrakis-di(p-methoxyphenylamino)-9,9'-spirobifluorene was isolated by column chromatography on silica gel using a mixture of hexane and ethyl acetate (4:1) as an eluent (281 mg, 92%).9 1H NMR (400 MHz, DMSO-d6, Figure S14): δ 7.48 (d, J = 8.4 Hz, 4H, 4-H), 6.83 (dd, J = 9.2, 2.4 Hz, 32H, 2-H), 6.69 (dd, J = 8.4, 2.4 Hz, 4H, 3-H), 6.18 (d, J = 2.0 Hz, 4H, 5-H), 3.71 (s, 24H, 1-H).

Polycondensation

To a 25 mL Schlenk tube were added 2,7-dibromo-9,9-dioctylfluorene (54.8 mg, 0.10 mmol), TPD (26.5 mg, 0.10 mmol), Pd(II) precat. 1 (1.0 mg, 0.0020 mmol), and Cs2CO3 (81.5 mg, 0.25 mmol). Tricyclohexylphosphine (PCy3) (1.2 mg, 0.0040 mmol) was then added in a glovebox. Pivalic acid (3.5 μL, 0.030 mmol) and dry toluene (1.0 mL) were added under a nitrogen stream. The mixture was stirred at 100°C for 48 h. After cooling to room temperature, volatiles were removed under reduced pressure. The products were dissolved in CHCl3 (100 mL) and an aqueous solution of sodium diethyldithiocarbamate (0.1 M, 150 mL) was added. The mixture was stirred for 16 h at room temperature. After separation, the organic layer was washed with water (3 times) and brine. The organic layer was dried over Na2SO4 and was concentrated. The solution was poured into vigorously stirred MeOH (200 mL) and stirred overnight. The precipitated solid was collected by filtration and washed with hexane (150 mL) for 1 h. Polymer 1 was isolated as a yellow solid after drying under vacuum (63.3 mg, 96%).10 1H NMR (600 MHz, CDCl3, Figure S15): δ 8.25 (br, 4H, 1-H and 2-H), 7.86 (br, 2H, 3-H), 3.67 (br, 2H, NCH2), 2.2-0.8 (m, alkyl chains).

Scheme S1. Reported side reactions involved in the formation of Pd(0) active species from Pd(II) precatalysts. (a) Oxidation of a phosphine ligand;11 (b) consumption of an organometallic reagent accompanied by formation of a homocoupling side product;12 (c) decomposition of a Pd catalyst.13

Scheme S2. Generation of Pd(0) active species from a Buchwald precatalyst through base-promoted reductive elimination of the aminobiphenyl substituent or through transmetalation and subsequent reductive elimination, accompanied by consumption of an organoboronic acid substrate.14

Scheme S3. Reactivity of Pd(1-naphthyl)(pentafluorophenyl)(tmeda) at 120 °C in the absence and presence of PPh₃. (a) In the absence of PPh₃, no reaction is observed. (b) In the presence of PPh₃, quantitative reductive elimination occurs, suggesting the formation of a Pd(0) complex.15

Table S1. Conversion of active Pd(0) species

| Entry | Pd(II) complex | Time | Conversion to Pd[P(t-Bu)3]2 / % a |
| --- | --- | --- | --- |
| 1 |  | 24 h | 3% |
| 2 |  | 24 h | 18% (+ unknown species) |
| 3 |  | 24 h | 57% |
| 4 |  | 24 h | 85% |
| 5 |  | 35 min | 95% |
| 6 |  | 35 min | 97% |

a Conversion was calculated from the 31P NMR integral values of the internal standard and the product.

Reductive elimination from Pd complexes bearing two pentafluorophenyl groups was slow even in the presence of P(t-Bu)₃ (Entries 1–3). Among the supporting ligands examined, the TMEDA ligand retarded reductive elimination more effectively than acetonitrile or pyridine ligands (Entries 1–3). These results indicate that TMEDA contributes to enhanced stability of Pd(II) biaryl complexes. In the case of the acetonitrile complex, multiple palladium species were formed, and selective generation of a Pd(0) complex was not achieved (Entry 2). Introduction of an electron-donating methoxy group at the para position of the fluorobenzene accelerated reductive elimination, demonstrating that the rate of reductive elimination can be modulated by para substituents on the aryl group (Entry 4). When TMEDA was employed as the supporting ligand and fluorine atoms are removed from one of the aryl groups, reductive elimination proceeds rapidly (Entries 5 and 6).

Table S2. TON and TOF for C–N coupling reactions in the synthesis of Spiro‑OMeTAD.

| Entry | Pd source | Amount of Pd / mol% | Time / h | Yield / % | TON | TOF / h-1 | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Pd(II) Precat. 1 | 0.5 | 2 | 92 | 736 | 368 | This work |
| 2 | Pd2(dba)3 | 8 | 12 | 45 | 22.5 | 1.9 | 9 |
| 3 | SPhos-Pd-MAH | 1 | 24 | 81 | 324 | 13.5 | 16 |
| 4 | Pd(OAc)2 | 8 | 24 | 75 | 37.5 | 1.6 | 17 |

Figure S1. 1H NMR spectra of Pd precat. 1 recorded (a) immediately after synthesis; (b) after storage in the solid state under air at room temperature for 5 months; (c) after heating in the solid state under air at 60 °C for 2 h; and (d) after standing in CDCl3 under air for 48 h (CDCl3, 400 MHz).

Figure S2. 19F NMR spectra of Pd precat. 2 recorded (a) immediately after synthesis; (b) after storage in the solid state under air at room temperature for over 5 months; (c) after heating in the solid state under air at 60 °C for 2 h; and (d) after standing in CDCl3 under air for 48 h (CDCl3, 376 MHz).

Figure S3. 1H NMR spectra of Pd precat. 2 recorded (a) immediately after synthesis; (b) after storage in the solid state under air at room temperature for over 5 months; (c) after heating in the solid state under air at 60 °C for 2 h; and (d) after standing in CDCl3 under air for 48 h (CDCl3, 400 MHz).

Figure S4. 1H NMR spectra of Pd precat. 1 with P(t-Bu)3 (a) before heating and (b) after heating at 80 °C for 35 min (toluene-d8, 400 MHz).

Figure S5. 19F NMR spectra of Pd precat. 1 with P(t-Bu)3 (a) before heating and (b) after heating at 80 °C for 35 min (toluene-d8, 376 MHz).

Figure S6. 31P NMR spectra of Pd precat. 2 with P(t-Bu)3 (a) before heating and (b) after heating at 80 °C for 35 min (Toluene-d8, 243 MHz).

Figure S7. 1H NMR spectra of Pd precat. 2 with P(t-Bu)3 (a) before heating and (b) after heating at 80 °C for 35 min (toluene-d8, 400 MHz).

Figure S8. 19F NMR spectra of Pd precat. 2 with P(t-Bu)3 (a) before heating and (b) after heating at 80 °C for 35 min (toluene-d8, 376 MHz).

Figure S9. 19F NMR spectra of Pd precat. 1 with P{3,5-(CF3)2C6H3}3 (a) before heating and (b) after heating at 80 °C for 140 min (toluene-d8, 565 MHz).

Figure S10. 31P NMR spectrum of the product (THF-d8, 243 MHz).

Figure S11. Time–conversion plots for the reductive elimination reactions of (a) Pd precat. 1 at 80 °C, monitored by 1H NMR. Black: with P(t-Bu)3 in TCE-d2, red: with P(t-Bu)3 in toluene-d8, orange: without P(t-Bu)3 in toluene-d8. gray: without P(t-Bu)3 in TCE-d2. (b) Pd precat. 1 with P(t-Bu)3 in toluene-d8. red: at 80 °C, purple: at 60°C.

Internal standard

(Ferrocene)

Figure S12. 1H NMR spectrum of the crude product obtained from the Suzuki–Miyaura cross-coupling reaction (Table 1, Entry 1). Ferrocene (blue triangle) was used as an internal standard (CDCl3, 400 MHz).

4

5

2

3

1

Figure S13. 1H NMR spectrum of the crude product obtained from the C-N coupling reaction with Pd Precat 1 (Scheme 3). 1,3,5-Trimethoxybenzene (blue triangle) was used as an internal standard (CDCl3, 400 MHz).

Figure S14. 1H NMR spectrum of Spiro-OMeTAD (DMSO-d6, 400 MHz).

Figure S15. 1H NMR spectrum of Polymer 1 obtained from the reaction in Scheme 5a (CDCl3, 600 MHz).

Figure S16. 1H NMR spectrum of Polymer 2 obtained from the reaction in Scheme 5b (CDCl3, 400 MHz).

.

Figure S17. 1H NMR spectrum of PdBr(4-nitrophenyl)(tmeda) (600 MHz, CDCl3, r.t.).

Figure S18. 13C{1H} NMR spectrum of PdBr(4-nitrophenyl)(tmeda) (151 MHz, CDCl3, r.t.).

Figure S19. 1H NMR spectrum of Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda), Pd precat. 1 (600 MHz,CDCl3, r.t.).

Figure S20. 19F NMR spectrum of Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda), Pd precat. 1 (564 MHz, CDCl3, r.t.).

Figure S21. 13C{1H} NMR spectrum of Pd(4-nitrophenyl)(pentafluorophenyl)(tmeda), Pd precat. 1 (151 MHz, CDCl3, r.t.).

Figure S22. 1H NMR spectrum of PdBr(phenyl)(tmeda) (600 MHz, CDCl3, r.t.).

Figure S23. 13C{1H} NMR spectrum of PdBr(phenyl)(tmeda) (151 MHz, CDCl3, r.t.).

Figure S24. 1H NMR spectrum of Pd(phenyl)(pentafluorophenyl)(tmeda), Pd precat. 2 (600MHz, CDCl3, r.t.).

Figure S25. 19F NMR spectrum of Pd(phenyl)(pentafluorophenyl)(tmeda), Pd precat. 2 (564 MHz, CDCl3, r.t.).

Figure S26. 13C{1H} NMR spectrum of Pd(phenyl)(pentafluorophenyl)(tmeda), Pd precat. 2 (151 MHz, CDCl3, r.t.).

Figure S27. 1H NMR spectrum of Pd(2,3,5,6-tetrafluoroanisole)2(pyridine)2 (600 MHz, CDCl3, r.t.).

Figure S28. 19F NMR spectrum of Pd(2,3,5,6-tetrafluoroanisole)2(pyridine)2 (564 MHz, CDCl3, r.t.).

Figure S29. 13C{1H} NMR spectrum of Pd(2,3,5,6-tetrafluoroanisole)2(pyridine)2 (151 MHz, CDCl3, r.t.).

References

1	R. Uson, J. Fornies, J. Gimeno, P. Espinet and R. Navarro, J. Organomet. Chem., 1974, 81, 115–122.

2	Y. P. Budiman, A. Jayaraman, A. Friedrich, F. Kerner, U. Radius and T. B. Marder, J. Am. Chem. Soc., 2020, 142, 6036–6050.

3	M. Tschoerner, R. W. Kunz and P. S. Pregosin, Magn. Reson. Chem., 1999, 37, 91–97.

4	B. A. Markies, A. J. Canty, W. de Graaf, J. Boersma, M. D. Janssen, M. P. Hogerheide, W. J. J. Smeets, A. L. Spek and G. van Koten, J. Organomet. Chem., 1994, 482, 191–199.

5	T. Korenaga, T. Kosaki, R. Fukumura, T. Ema and T. Sakai, Org. Lett., 2005, 7, 4915–4917.

6	A. Jakab, Z. Dalicsek, T. Holczbauer, A. Hamza, I. Pápai, Z. Finta, G. Timári and T. Soós, Eur. J. Org. Chem., 2015, 2015, 60–66.

7	R. Sato, T. Kanbara and J. Kuwabara, Dalton Trans., 2020, 49, 12814–12819.

8	A. Winkler, K. Brandhorst, M. Freytag, P. G. Jones and M. Tamm, Organometallics, 2016, 35, 1160–1169.

9	N. J. Jeon, H. G. Lee, Y. C. Kim, J. Seo, J. H. Noh, J. Lee and S. Il Seok, J. Am. Chem. Soc., 2014, 136, 7837–7840.

10	Z. Hu, T. Yasuda, T. Kanbara and J. Kuwabara, Macromol. Chem. Phys., 2025, 2025, 2400506 (1–8).

11	F. Ozawa, A. Kubo and T. Hayashi, Chem. Lett., 1992, 21, 2177–2180.

12	Z. Bao, W. K. Chan and L. Yu, J. Am. Chem. Soc., 1995, 117, 12426–12435.

13	C. S. Wei, G. H. M. Davies, O. Soltani, J. Albrecht, Q. Gao, C. Pathirana, Y. Hsiao, S. Tummala and M. D. Eastgate, Angew. Chem., Int. Ed., 2013, 52, 5822–5826.

14	R. M. Wolesensky, M. T. Morales-Colón and M. S. Sanford, ACS Catal., 2025, 15, 18758–18768.

15	T. Iida, R. Sato, Y. Yoshigoe, T. Kanbara and J. Kuwabara, Dalton Trans., 2024, 53, 13340–13347.

16	J. Huang, M. Isaac, R. Watt, J. Becica, E. Dennis, M. I. Saidaminov, W. A. Sabbers and D. C. Leitch, ACS Catal., 2021, 11, 5636–5646.

17	S. Mattiello, G. Lucarelli, A. Calascibetta, L. Polastri, E. Ghiglietti, S. K. Podapangi, T. M. Brown, M. Sassi and L. Beverina, ACS Sustain. Chem. Eng., 2022, 10, 4750–4757.