Supplementary Information

Effective degradation of carbofuran and organophosphate pesticides via continuous-flow visible light-activated periodate oxidation system using floatable sodium alginate/water lettuce-derived biochar/hollow glass microspheres

Karim Amer , Arafat Toghan 2, Emad M. Masoud 3*, Magdi E.A. Zaki 2, Hassan Shokry 4, Mahmoud Samy 5, Mohamed Mohamed Gaber 4*

1 Technology Management Department, Egypt-Japan University of Science and Technology (E-JUST), P.O. Box 179, New Borg El-Arab City Postal Code 21934, Alexandria, Egypt

2 Chemistry Department, College of Science, Imam Mohammad Ibn Saud Islamic University (IMSIU), Riyadh 11623, Saudi Arabia

3 Department of Chemistry, Faculty of Science, Islamic University of Madinah, Madinah 42351, Saudi Arabia

4 Environmental Engineering Department, Faculty of Engineering, Egypt-Japan University of Science and Technology (E-JUST), P.O. Box 179, New Borg El-Arab City Postal Code 21934, Alexandria, Egypt

5 Public Works Engineering Department, Faculty of Engineering, Mansoura University, Mansoura 35516, Egypt

# Supplementary texts

## Text S1. Chemicals

Carbofuran (CBF, C12H15NO3, 98%), chlorpyrifos (C9H11Cl3NO3PS, 97%), malathion (C10H19O6PS2, 99%), diazinon (C12H12N2O3PS, ≥ 97.5%), potassium periodate (KIO4, 99.8%), iodine (I2, ≥ 99.99%), sodium alginate (SA, pharmaceutical secondary standard, certified reference material), 2-Iodophenole (IC6H4OH, 98%), 4-Iodophenole (IC6H4OH, ACS reagent grade, 99%), potassium iodide (KI, 99%), and sodium iodate (NaIO3, ≥ 99%) were supplied by Sigma-Aldrich Co. (USA). In addition, hollow glass microspheres (HGMs; 3MTM Glass Bubbles K1) were bought from the 3M Company (St. Paul, MN, USA). These engineered soda-lime-borosilicate glass microspheres exhibit a low true density of 0.125 g g/cm3 (range: 0.10–0.14 g/cm3), an isostatic crush strength of 250 psi (corresponding to 90% survival), and a volume-based particle size distribution with a median diameter of approximately 115 µm. Further, hydrochloric acid (HCl, 37%), potassium hydrogen phosphate  (K2HPO4, ≥ 99.5%), sodium chloride (NaCl, ≥ 99.5%), sulfuric acid (H2SO4, 95-97%), sodium chloride (NaCl, ≥ 99.5%), and sodium thiosulfate (Na2O3S2, ≥ 97%) were purchased from Merck Chemical Co., Ltd. (Germany). Moreover, the reagents employed for chemical oxygen demand (COD) analysis were procured from the Hach Company (Loveland, USA). Moreover, calcium chloride (CaCl2, ≥ 93%), potassium nitrate (KNO3, 99%), sodium bicarbonate (NaHCO3, 99.5%), furfuryl alcohol (C5H2O2, 98%), amylopectin (C30H52O26, 99.8%), sodium sulfate (Na2SO4, 99%), ethanol (C2H6O, 99.8%), sodium hydroxide (NaOH, > 97%), humic acid (technical grade, average molecular weight = 3000, 95%), tert-butyl alcohol (C4H10O, 99.5%), 2-propanol (C3H8O, 99.8%), chloroform (CHCl3, 99.5%), phenol (C6H5OH, ≥ 98%), phosphoric acid (H3PO4, HPLC grade, 85%), formic acid (CH2O2, HPLC grade, 98-100%), methanol (CH4O, HPLC grade, 99.9%), and acetonitrile (C2H3N, HPLC grade, 99.9%) were received from Fisher Chemical Co. Ltd. (UK).

## Text S2. Biochar synthesis

Biochar was produced from the collected water lettuce biomass in accordance with the methodology described in our previous studies. 1,2 Water lettuce samples were initially washed thoroughly with tap water to remove adhering dust and impurities, followed by natural air-drying under sunlight. To enhance brittleness and facilitate size reduction, the dried biomass was oven-dried at 105 °C for 24 h (ED 53, Binder, Germany). The dried material was then mechanically ground using an electric blender to obtain a fine powder. The resulting powder was washed with ethanol and centrifuged (EBA 20, Hettich, USA). Subsequently, the material underwent pyrolysis at 500 °C for 2 h under oxygen-limited conditions (AMF 25 N, Asahi-Rika, Japan) to produce biochar. The obtained biochar was acid-washed with HCl (1 M) for 24 h to remove ash and mineral impurities, then thoroughly rinsed with deionized water until a neutral pH was achieved. Finally, the sample was dried at 60 °C overnight, followed by additional washing, centrifugation, and drying at 105 °C for 24 h to obtain purified water lettuce biochar (WLBC). A schematic illustration summarizing the WLBC synthesis procedure is presented in Fig. S1.

## Text S3. Characterization of the composite beads

The crystalline structure of the beads was analyzed by X-ray diffraction (XRD, XRD 6000, Shimadzu Corp., Japan). Functional groups and chemical bonding were examined by Fourier transform infrared spectroscopy (FTIR, FTIR-8400S, Shimadzu Corp, Japan). The surface morphology and cross-sectional architecture of the SA/WLBC/HGMs beads were characterized by scanning electron microscopy (SEM, JSM-6010L, JEOL Ltd., Japan). Transmission electron microscopy (TEM, JEM 2100F, JEOL Ltd., Japan) was employed to elucidate the internal structure, interfacial characteristics, and nanoscale morphology of the composite. This instrument was coupled with energy-dispersive X-ray spectroscopy (EDX, X-Max 80 mm2, Oxford, UK), which enabled qualitative and quantitative determination of the elemental composition and mapping of the spatial distribution of elements within the analyzed regions. Textural properties, such as specific surface area, pore volume, and pore size distribution, were evaluated by Brunauer–Emmett–Teller (BET) analysis and Barrett–Joyner–Halenda (BJH) methods using a BELSORP MAX surface area analyzer (BEL Corp., Japan).

## Text S4. Analytical methods

The concentrations of CBF, diazinon, chlorpyrifos, malathion, periodate ions (IO4−), and iodate ions (IO3−) were determined using high-performance liquid chromatography (HPLC; LC-2040C, Shimadzu, Japan). Chromatographic separation was performed on an Agilent XDB-C18 column (4.6 × 250 mm, 5 μm). The detailed chromatographic parameters and operating conditions are provided in Table S2.

Total organic carbon (TOC) was measured using a TOC analyzer (TOC-L CPH/CPN, Shimadzu, Japan) based on the high-temperature combustion method (SMWW 5310 B) described in the Standard Methods for the Examination of Water and Wastewater (SMWW). 3 Chemical oxygen demand (COD) was determined using the closed reflux colorimetric method (SMWW 5220 D; Hach Method 8000). In this procedure, samples were digested in a thermal digester (RD 125, Lovibond, Germany), and the resulting absorbance was subsequently measured using a portable spectrophotometer (DR1900, Hach, China). The pH of the samples was determined electrometrically according to SMWW 4500-H+ B using a multiparameter analyzer (HQ440d, Hach, USA) equipped with a pH electrode (PHC301, Hach, USA). Total dissolved solids (TDS) were quantified using the gravimetric method (SMWW 2540 C) after drying the samples at 180 °C in a drying oven (ED 53, Binder, Germany). Turbidity was measured following the nephelometric method (SMWW 2130 B) using a turbidity meter (Turb 430T, WTW, USA).

The transformation products generated during the degradation of CBF were identified using ultra-HPLC coupled with mass spectrometry (UHPLC-MS; LCMS-2020, Shimadzu, Japan). The system was equipped with an electrospray ionization (ESI) source operating in positive ionization mode. Chromatographic separation was carried out on a RESTEK Pinnacle II C18 column (150 × 4.6 mm, 5 µm). The mobile phase composition and ratios were identical to those used in the HPLC analysis. The column temperature was maintained at 30 °C, and the flow rate was set at 0.5 mL/min. The total chromatographic run time for each analysis was 30 min.

# Supplementary figures

Fig. S1. Schematic illustration of the WLBC synthesis procedures.

Fig. S2. Fabrication process of SA/WLBC/HGMs composite beads.

Fig. S3. Elemental mapping images of the SA/WLBC/HGMs beads.

Fig. S4. (a) HRTEM image and (b) the corresponding HRTEM intensity profile of the SA/WLBC/HGMs beads.

Fig. S5. Kinetic rate constants of CBF removal in the SA/WLBC/HGMs–PI/light system at different reaction temperatures: (a) pseudo-first-order rate constants and (b) pseudo-second-order rate constants. Conditions: [catalyst]o = 4 g, [PI]o = 0.8 g/L, input flow rate = 2 mL/min, pH = 7, and [CBF]o = 15 mg/L.

Fig. S6. Activation Energy (Ea) for CBF removal in the SA/WLBC/HGMs–PI/light system.

Fig. S7. UHPLC-MS spectrum of the detected intermediates during CBF degradation in the SA/WLBC/HGMs–PI/Light system.

# Supplementary tables

Table S1 Equations of removal efficiency and kinetic models.

| Equation | No. |
| --- | --- |
| CBF removal efficiency (%)=CBFo-CBFtCBFo x 100 | (1) |
| -lnCBFtCBFo= K1t | (2) |
| 1CBFt= 1CBFo+K2t | (3) |
| CBFo = initial CBF concentration (mg/L), CBFt = CBF concentration at reaction time t (mg/L, K1 = apparent first-order rate constant (min−1), and K2 represents the second-order rate constant (L/mg.min). |  |

| Operating conditions | CBF |  | Diazinon |  | Malathion |  | Chlorpyrifos |  | * IO4– and IO3– |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mobile phase (v/v) | Ultrapure water/ methanol (50/50) |  | Ultrapure water/ acetonitrile (30/70) |  | Ultrapure water/ methanol (80/20) |  | Ultrapure water/ methanol/formic acid (88/11.7/0.3) |  | 0.1% phosphoric acid: acetonitrile (70:30) |
| Detection wavelength (nm) | 280 |  | 220 |  | 220 |  | 299 |  | 228 |
| Injection volume (μL) | 10 |  | 20 |  | 10 |  | 10 |  | 10 |
| Flow rate (mL/min) | 1 |  | 0.8 |  | 1 |  | 1 |  | 1 |
| Column temperature (°C) | 40 |  | 25 |  | 30 |  | 30 |  | 30 |
| Reference | 4 |  | 5 |  | 6 |  | 7 |  | 8 |
| * The concentrations of IO4– and IO3– ions were quantitatively determined using the external calibration method. Calibration curves were constructed using standard solutions of KIO4 and NaIO3, respectively, prepared over a concentration range of 0–500 mM. 9,10 |  |  |  |  |  |  |  |  |  |

Table S2 HPLC conditions used for the analysis of the target compounds.

Table S3 XRD peaks (2θ°) of the synthesized SA/WLBC/HGMs beads with corresponding Miller indices (hkl) assigned based on standard reference data.

| SA/WLBC/HGMs beads | Reference cards |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Silicon dioxide (SiO2) |  | Calcium carbonate (CaCO3) |  | Potassium chloride (KCl) |  | Calcium sulfide (CaS) |  | Carbon (C) |  |
| 2θ° | 2θ° | hkl | 2θ° | hkl | 2θ° | hkl | 2θ° | hkl | 2θ° | hkl |
| 21.8 | 21.806 | 101 | – | – | – | – | – | – | – | – |
| 24.48 | – | – | 23.022 | 012 | 24.486 | 111 | – | – | – | – |
| 27.24 | – | – | – | – | – | – | 27.165 | 111 | 26.382 | 002 |
| 28.26 | 28.243 | 111 | – | – | 28.348 | 200 | – | – | – | – |
| 29.34 | – | – | 29.356 | 104 | – | – | – | – | – | – |
| 31.26 | 31.097 | 102 | – | – | – | – | 31.407 | 200 | – | – |
| 35.94 | 35.904 | 200 | – | – | – | – | – | – | – | – |
| 36.1 | 36.022 | 112 | 36.041 | 110 | – | – | – | – | – | – |
| 38.13 | 38.191 | 201 | – | – | – | – | – | – | – | – |
| 40.66 | 40.315 | 210 | 39.492 | 113 | 40.521 | 220 | – | – | – | – |
| 42.33 | 42.4 | 211 | – | – | – | – | – | – | 42.223 | 100 |
| 43.25 | – | – | 43.254 | 202 | – | – | – | – | – | – |
| 44.38 | 44.456 | 202 | – | – | – | – | 44.997 | 220 | 44.393 | 101 |
| 47.66 | 46.486 | 113 | 47.306 | 024 | 47.916 | 311 | – | – | – | – |
| 48.42 | 48.218 | 212 | 48.652 | 116 | – | – | – | – | – | – |
| 50.24 | 51.684 | 220 | – | – | 50.19 | 222 | – | – | 50.453 | 102 |
| 56.78 | 56.739 | 301 | – | – | – | – | 55.884 | 222 | 55.544 | 005 |
| 58.57 | 58.413 | 222 | 57.559 | 122 | 58.646 | 400 | – | – | 59.694 | 103 |
| 64.78 | 64.839 | 204 | 64.678 | 300 | 64.508 | 331 | 65.506 | 400 | – | – |
| 67.55 | 67.511 | 320 | – | – | 66.397 | 420 | – | – | – | – |
| 73.32 | 73.363 | 322 | 72.675 | 128 | 73.711 | 422 | 72.256 | 331 | – | – |
| 74.52 | – | – | – | – | – | – | 74.425 | 420 | – | – |

| Wavenumber (cm–1) of the synthesized beads |  | Literature comparison |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Vibration |  | Wavenumber (cm–1) |  | References |
| 3377.58 |  | O–H |  | 3454 |  | 11 |
|  |  |  |  | 3435 |  | 12 |
|  |  |  |  | 3300 |  | 13 |
|  |  |  |  | 3415.61 |  | 2 |
| 2316.48 |  | Alginate |  | 2358.6 |  | 14,15 |
| 1607.33 |  | O–H |  | 1641 |  | 11 |
|  |  |  |  | 1624.45 |  | 2 |
|  |  | C=C and C=O |  | 1618 |  | 12 |
|  |  |  |  | 1698 |  | 16 |
|  |  | Asymmetric stretching vibrations of COO– in alginate |  | 1600 |  | 17,18 |
|  |  |  |  | 1630 |  | 19 |
| 1423.77 |  | –CH2 |  | 1429.14 |  | 2 |
|  |  |  |  | 1368 |  | 16 |
|  |  |  |  | 1420 |  | 12 |
|  |  | Symmetric stretching vibrations of COO⁻ in alginate |  | 1410 |  | 17 |
|  |  |  |  | 1401 |  | 19 |
|  |  |  |  | 1415.6 |  | 14 |

Table S4 FTIR spectral bands of SA/WLBC/HGMs beads and corresponding functional group assignments based on the literature.

| 1012.81 |  | C–O |  | 1078 |  | 16 |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 1045.04 |  | 2 |
|  |  |  |  | 1056 |  | 12 |
| 789.68 |  | O–C–O or Alginate–O in alginate |  | 795.5 |  | 14,15 |
| 454.2 |  | Si–O–Si and Si–O |  | 479 |  | 20 |

Table S5 Summary of investigated operational parameters and optimal conditions for CBF degradation.

| Parameter |  | Tested values |  | Fixed conditions |  | Optimal value |
| --- | --- | --- | --- | --- | --- | --- |
| Reaction temperature (T, °C) |  | 25, 35, 45, 55, and 65 |  | [CBF]o = 15 mg/L, [catalyst]o = 4 g, [PI]o = 0.8 g/L, flow rate = 2 mL/min, and pH = 7 |  | 25 °C |
| Initial solution pH |  | 4, 5, 6, 7, 8, 9, and 10 |  | [CBF]o = 15 mg/L, [catalyst]o = 4 g, [PI]o = 0.8 g/L, flow rate = 2 mL/min, and T = 25 °C |  | pH 7 |
| Input flow rate (mL/min) |  | 2, 4, 6, 8, and 10 |  | [CBF]o = 15 mg/L, [catalyst]o = 4 g, [PI]o = 0.8 g/L, pH = 7, and T = 25 °C |  | 2 mL/min |
| Catalyst dosage (g) |  | 0, 1, 2.5, 4, 5.5, and 7 |  | [CBF]o = 15 mg/L, [PI]o = 0.8 g/L, pH = 7, flow rate = 2 mL/min, and T = 25 °C |  | 4 g |
| PI concentration (g/L) |  | 0, 0.2, 0.4, 0.6, 0.8, and 1 |  | [CBF]o = 15 mg/L, [catalyst]o = 4 g, pH = 7, flow rate = 2 mL/min, and T = 25 °C |  | 0.8 g/L |
| Initial CBF concentration (mg/L) |  | 15, 20, 25, 30, and 35 |  | [Catalyst]o = 4 g, [PI]o = 0.8 g/L, pH = 7, flow rate = 2 mL/min, and T = 25 °C |  | 15 mg/L |

Table S6 Summary of reactive species quenching reactions at excess periodate dosage.

| Equation | No. |
| --- | --- |
| IO3• + IO3• → I2O6 | (1) |
| IO4• + IO4• → I2O8 | (2) |
| OH• + OH• → H2O2 | (3) |
| IO4- + OH• → OH− + IO4• | (4) |
| IO3• + IO4- → IO4• + IO3- | (5) |
| IO3• + H• → IO3- + H+ | (6) |

Table S7 Mechanism equations for CBF degradation in the SA/WLBC/HGMs–PI/light system.

| Equation | No. |
| --- | --- |
| IO4- + ℎ𝜈 → O•- + IO3• | (1) |
| IO4- + ℎ𝜈 → IO3- + O(3P) | (2) |
| O(3P) + O2 → O3 | (3) |
| IO3• + O3 → O2 + IO4• | (4) |
| O•- + H+ ⇄ •OH | (5) |
| O•- + H2O ⇄ OH− + •OH | (6) |
| SA/WLBC/HGMs beads–OOH + IO4- → SA/WLBC/HGMs beads–OO• + •OH + IO3• | (7) |
| SA/WLBC/HGMs beads–OH + IO4- → SA/WLBC/HGMs beads–O• + •OH + IO3• | (8) |
| IO4- + IO3• → IO3- + IO4• | (9) |
| IO4- + •OH → OH− + IO4• | (10) |
| IO3- + •OH → OH− + IO3• | (11) |
| IO4- + 2OH− + O2 → H2O + IO3- + 2O2•- | (12) |
| 3IO4- + 2OH− → H2O + 3IO3- + 2O2•- | (13) |
| 2IO4• → 2IO3- + 1O2 | (14) |
| 2O2•- + IO4- + H2O → IO3- + 2OH− + 2(1O2) | (15) |
| O2•- + •OH → OH− + 1O2 | (16) |
| IO4- + H2O2 → H2O + O2•- + IO3• | (17) |

Table S8 Basic water quality parameters of different water bodies.

| Parameter |  | Tap water |  | River water |  | Seawater |  | Lake water |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TOC (mg/L) |  | 3.7 |  | 8.5 |  | 10.6 |  | 13.8 |
| COD (mg/L) |  | 8.6 |  | 27.6 |  | 19.1 |  | 23.8 |
| pH |  | 7.8 |  | 8.1 |  | 7.6 |  | 8.4 |
| TDS (mg/L) |  | 62.4 |  | 113.2 |  | 35361.8 |  | 182.3 |
| Turbidity |  | 0.36 |  | 0.58 |  | 5.3 |  | 0.82 |

Table S9 Techno-economic analysis of the SA/WLBC/HGMs–PI/light system.

| Item | Unit | Cost | Justification |
| --- | --- | --- | --- |
| Capital expenditure (CAPEX) |  |  |  |
| Reactor cost (A) | USD | 20000 | 1 m3 of reinforced concrete = 500 USD, cost of construction = 10000 USD, contractor cost = 2000 USD, Design cost = 2000 USD, Electrical works cost = 3000 USD, and plumbing works = 3000 USD |
| Equipment (B) | USD | 9900 | Pump price = 500 USD, hotplate stirrer price = 300 USD, oven price = 2000 USD, muffle furnace price = 3000 USD, centrifuge price = 2000 USD, and electric blender price = 1000 USD |
| Other costs (C) | USD | 5000 | To cover emergencies such as the downtime of equipment |
| Total CAPEX | USD | 34900 | The sum of A, B, and C |
| Yearly CAPEX | USD/year | 4716.2 | To estimate yearly CAPEX, total CAPEX is divided by the annuity factor ([1-(1+r)-t]/r), where r refers to the interest rate (6%), and t is the project’s lifetime |
| Unit CAPEX | USD/m3 | 0.8 | Yearly CAPEX/Treated volume of wastewater per year |
| Operational expenditure (OPEX) |  |  |  |
| Chemical costs (D) | USD/year | 5136 | KIO4 dose and price = 0.8 kg/m3 and 0.1 USD/kg, NaOH (3 kg/m3, 0.01 USD/kg), H2SO4 (3 kg/m3, 0.012 USD/kg), SA (60 kg/m3, 0.001 USD/kg), HGMs (70 kg/m3,0.005 USD/kg), and CaCl2 (30 kg/m3, 0.01 USD/kg) |
| Energy cost (E) | USD/year | 240 | The average power for equipment = 500 W with a unit price of 0.2 USD per KW.h |
| Labor cost (F) | USD/year | 471.6 | 10% of yearly CAPEX |
| Taxes and other charges (e.g., water) (G) | USD/year | 47.2 | 1% of yearly CAPEX |
| Maintenance cost (H) | USD/year | 943.2 | 20% of yearly CAPEX |
| Total OPEX | USD/year | 6838 | Sum of D, E, F, G, and H |
| Unit OPEX | USD/m3 | 1.14 | Total OPEX/treated volume of wastewater per year |
| Revenues |  |  |  |
| TOC abatement | USD/year | 10.6 | Mass of TOC removed per year (81.9 Kg/year) x shadow price (0.13 USD/KgTOC removed) |
| Reclaimed water | USD/year | 4200 | Unit price of reclaimed water per m3 = 0.7 USD, revenues = 0.7 * 6000 = 4200 USD |
| Beads price | USD/year | 9000 | Unit price of the beads = 3 USD/kg, the yearly production of the material = 3000 kg |
| Total profits | USD/year | 13210.6 | Summation of revenues |
| Feasibility analysis |  |  |  |
| Net profit | USD/year | 6372.6 | Total profits – Total OPEX |
| Payback period | Years | 5.5 | CAPEX/Net profit |
| Net present value (NPV) | USD | 12002.9 | NPV = -CAPEX + y=1nNet profit(1+r)t, NPV with a positive sign indicates the potential of the project to attain profits |
| Internal rate of return (IRR) | % | 12.6 | t=1nNet profit(1+IRR)t = CAPEX IRR is higher than the interest rate, indicating the potential for investment by stakeholders. |
| Profitability index | – | 1.3 | Profitability index = NPV+CAPEXCAPEX Profitability index > 1 confirms the feasibility of the project |

# References

1	M. M. Gaber, M. Abdel Rafea, H. Shokry, M. Samy, A. M. Ahmed and M. Elkady, Catalysts, 2025, 15, 1049.

2	M. M. Gaber, A. Toghan, H. Shokry and M. Samy, RSC Adv., 2025, 15, 31522–31538.

3	APHA; AWWA and WEF, American Public Works Association, 2017, 1469.

4	M. Samy, A. G. Kumi, E. Salama, M. ElKady, K. Mensah and H. Shokry, Process Safety and Environmental Protection, 2023, 169, 337–351.

5	N. A. Amiri, F. A. Amiri, L. Faravardeh, A. Eslami, A. Ghasemi and M. Rafiee, J. Environ. Manage., 2022, 316, 115293.

6	Y. Chen, D. Chai, X. Zhang, Z. Jiang, H. Yao, X. Yuan, X. Chen, K. Cui and Y. Wang, Sep. Purif. Technol., 2025, 362, 131880.

7	M. Samy, M. G. Ibrahim, M. Gar Alalm, M. Fujii, K. E. Diab and M. ElKady, Chemical Engineering Journal, 2020, 395, 124974.

8	Y. Xiong, X. Tang, Y. Liu, W. Li, Y. He, Y. Deng, Z. Lin and Y. Zhou, Sep. Purif. Technol., 2024, 333, 125813.

9	K. Zhang, S. Zhang, C. Ye, R. Ou, H. Zeng, X. Yu and M. Feng, Chemical Engineering Journal, 2023, 451, 138642.

10	H. Sun, F. He and W. Choi, Environ. Sci. Technol., 2020, 54, 6427–6437.

11	Q. Chen, T. C. Zhang, L. Ouyang, S. Yuan, Q. Chen, T. C. Zhang, L. Ouyang and S. Yuan, Molecules, 2022, 27, 269.

12	Y. Kassa, A. Amare, T. Nega, T. Alem, M. Gedefaw, B. Chala, B. Freyer, B. Waldmann, T. Fentie, T. Mulu, T. Adgo, G. Ayalew, M. Adugna and D. Tibebe, Scientific Reports, 2025, 15, 1820.

13	D. Losacco, C. Campanale, M. Tumolo, V. Ancona, C. Massarelli and V. F. Uricchio, Sustainability 2022, 14, 11985.

14	J. Raissouni, K. Draoui, A. A. Aghzzaf, R. Cela-Dablanca, A. Barreiro, M. J. Fernández-Sanjurjo, A. Núñez-Delgado and E. Álvarez-Rodríguez, J. Environ. Manage., 2025, 374, 123952.

15	J. Raissouni, K. Draoui, A. A. Aghzzaf, R. Cela-Dablanca, A. Barreiro, M. J. Fernández-Sanjurjo, A. Núñez-Delgado and E. Álvarez-Rodríguez, J. Hazard. Mater., 2025, 496, 139267.

16	A. Ray, A. Banerjee and A. Dubey, International Journal of Agriculture Environment and Biotechnology, 2020, 13,  864.

17	T. K. Das, Q. Scott and A. N. Bezbaruah, J. Environ. Chem. Eng., 2025, 13, 116815.

18	E. J. Lee and J. W. Lee, Environ. Technol. Innov., 2025, 40, 104660.

19	M. N. Abdul-Raheem, I. O. Saheed, N. H. M. Kaus, R. Adnan, S. Thongmee, S. Shehu Imam, O. H. Hassan and S. Sagadevan, Journal of Water Process Engineering, 2025, 74, 107826.

20	S. Mohan, M. Vellakkat and R. U, Journal of the Indian Chemical Society, 2026, 103, 102341.

Corresponding authors:

* emad.youssef@iu.edu.sa (Emad M. Masoud); mohamed.gaber@ejust.edu.eg (Mohamed Mohamed Gaber).