## Slide 1
(a)
(b)
(c)
(d)
500 nm
(e）
(f)
(h)
(g)
Yb
Ta
O
N
(i)
Fig. 1 (a) XRD patterns and its partial enlarged drawing of YbTaO4 and nitrided samples. (b) Rietveld refinement results of YbTaO4-xNy(Mg). (c) Thermogravimetric-temperature curve and (d) thermogravimetric-temperature first derivative curve of the nitrided sample. (e) SEM image and (f-i) energy dispersive spectroscopy mapping for Yb, Ta, O and N element of YbTaO4-xNy(Mg).

## Slide 2
(a)
(b)
(c)
(d)
Fig. 2 (a) UV-Vis DRS and (b) Tauc plots of YbTaO4 and nitrided samples. (c) Mott-Schottky of YbTaO4-xNy(Mg), carried out in 0.5 M Na2SO4 and the measured potential (E vs. Ag/AgCl) was converted into the potential versus reversible hydrogen electrode (RHE) by E(vs. RHE) = E (vs. Ag/AgCl) + 0.197 + 0.0591 × 7. (d) Band diagrams of YbTaO4 and nitrided samples.

## Slide 3
Fig. 3 TRPL spectra and its fitting curve of YbTaO4-xNy(M) (M = Mg, Zr, Al) and YbTaO4-xNy.

## Slide 4
(a)
(b)
(c)
Fig. 4 (a) Time course of H2 evolution for the photocatalytic hydrogen evolution half-reaction. (b) Schematic diagram and (c) time course of gases evolution of Z-scheme overall water splitting. Reaction conditions: 300 W Xenon lamp with a cutoff filter as the light source (λ ≥420 nm), for H2-evolving half reaction, 100 mg of 1 wt.% Pt/YbTaO4-xNy(M), 150 mL of 20 vol.% CH3OH solution; for Z-scheme overall water splitting, 100 mg of 1 wt.% Pt/YbTaO4-xNy(M) as H2-evolving photocatalyst, 50 mg of Ir-FeCoOx/BiVO4 as O2-evolving photocatalyst, 150 mL 25 mM sodium phosphate buffer solution (pH 6.0) containing 5 mM K4[Fe(CN)6]

## Slide 5
(a)
(b)
Fig. 5 (a) Schematic diagram and (b) time course of gases evolution of one step photocatalytic overall water splitting. Reaction conditions: 100 mg of YbTaO4-xNy(M) loading with 1 wt.% Pt@CrOx and 0.5 wt.% IrO2, 150 mL H2O, 300 W Xenon lamp with a cutoff filter (λ ≥420 nm).

## Slide 6
(a)
(b)
(c)
(d)
Fig. S1 UPS of (a) YbTaO4-xNy(Mg), (b) YbTaO4-xNy(Zr), (c) YbTaO4-xNy(Al), and (d) YbTaO4.

## Slide 7
Fig. S2 Rietveld refinement results of (a) YbTaO4-xNy(Zr), (b) YbTaO4-xNy(Al) and (c) YbTaO4-xNy.
(a)
(b)
(c)

## Slide 8
Fig. S3 SEM images of (a) YbTaO4-xNy(Zr), (b) YbTaO4-xNy(Al) and (c) YbTaO4-xNy.
500 nm
500 nm
500 nm
(a)
(b)
(c)

## Slide 9
Fig. S4 Open-circuit potential of nitride samples under dark state and light switching.

## Slide 10
Fig. S5. Mott-Schottky plots of (a) YbTaO4-xNy(Zr), (b) YbTaO4-xNy(Al), (c) YbTaO4-xNy, and (d) YbTaO4 at different frequencies
(a)
(b)
(c)
(d)

## Slide 11
Fig. S6 Optimization curve of Pt cocatalyst content loading on YbTaO4-xNy(Mg) for hydrogen evolution reaction.
Reaction conditions: 100 mg Pt/YbTaO4-xNy(Mg), 150 mL 20 vol.% methanol solution, 300 W Xe lamp with a cutoff filter (λ ≥ 420 nm).

## Slide 12
Fig. S7 Optimization loading content of IrO2 cocatalyst on Pt@CrOx/YbTaO4-xNy(Mg) for overall water splitting.
Reaction conditions: 100 mg photocatalyst, 150 mL H2O, 300 W Xe lamp with a cutoff filter (λ ≥ 420 nm).