Lattice Oxygen Activation Enabled by Fe Doping in Double Perovskite Oxides for Efficient Zinc–Air Batteries

Xiaoyi Fu a, 1, Xia Lei a, 1, Yanyi Wang a, Shuyu Cui a, Junjie Hu c, Tian Lang a, Xiaolong Zhou d, Sarayut Tunmee e, Suttipong Wannapaiboon e, Xingzhu Wang a, f, g, *, Xiongwei Zhong b, *, Baomin Xu a, h, *

a Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China.

E-mails: wangxz@sustech.edu.cn (X. Wang); xubm@sustech.edu.cn (B. Xu)

b College of Chemistry and Environmental Engineering, Shenzhen University, Shenzhen 518071, China

E-mail: zhongxw@szu.edu.cn (X. Zhong)

c Department of Physics and Optoelectronic Engineering, Xiangtan University, Xiangtan, 411100, China.

d Advanced Energy Storage Technology Research Center, Shenzhen Institute of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, China

e Synchrotron Light Research Institute (Public Organization), 111 University Avenue, Muang District, Nakhon Ratchasima 30000, Thailand.

f Engineering and Research Center for Integrated New Energy Photovoltaics & Energy Storage Systems of Hunan Province and Electrical Engineering, University of South China, Hengyang 421001, China.

g Shenzhen Putai Technology Co, Ltd, Shenzhen·518110, China

h SUSTech Energy Institute for Carbon Neutrality, Southern University of Science and

Technology, Shenzhen 518055, China

1 Contributed equally to this work

Section S1. Materials and Methods.

  - Characterization

Morphologies of the catalysts were characterized by field-emission scanning electron microscopy (FESEM, MIRA3 TESCAN), high-resolution transmission electron microscopy (TEM, Talos F200X G2, 200 kV), and high-angle annular dark field scanning transmission electron microscopy. Structural information was obtained from an X-ray diffractometer (Bruker D8, Copper Kα 4 radiation, λ=1.5406 Å). X-ray photoelectron spectroscopy (XPS) was performed using PHI 5000 Versa Probe III (Al-Kα, hv = 1486.6 eV) to investigate the prepared catalysts' chemical composition and surface properties. Electron paramagnetic resonance (EPR) was performed using Bruker-EmxPlus to investigate the oxygen vacancy. The specific surface area was calculated using the Brunauer-Emmett-Teller (BET) method based on N2 adsorption/desorption isotherms (Micromeritics-ASAP2460). The synchrotron X-ray absorption measurements were conducted at the SYT-NANOTEC-SLRI X-ray absorption beamline (BL 5.2), Synchrotron Light Research Institute (public organization), Thailand. The processes of data reduction, data analysis, EXAFS fitting, and wavelet transformation were carried out using the Athena, Artemis, and HAMA fortran software packages, respectively 1.

  - Electrochemical measurements

A CHI 760E electrochemical workstation at room temperature evaluated all catalytic activities. A standard Hg/HgO electrode and a graphite rod electrode were used as the reference (RE) and counter electrodes (CE), respectively. The Hg/HgO reference electrode was calibrated for a reversible hydrogen electrode (RHE) with a Pt wire in a high-purity H2-saturated electrolyte. The overpotential of OER and ORR were referenced to RHE. All polarization curves were given with iR compensation. Electrochemical impedance spectroscopy (EIS) was performed in the frequency range from 100 kHz to 0.1 kHz under an alternating voltage with an amplitude of 5 mV.

  - OER activity measurement

A homogeneous catalyst ink was prepared by dispersing 5mg of the catalyst with 1.5 mg Super P (Canrd) in 350 μL ethanol and 50 μL Nafion solution (D520, Du Pont,5wt% in water), followed by 2h of ultrasonication. For comparison, a homogeneous catalyst ink with 2 mg IrO2, 375 μL water/ethanol (1:1 v:v), and 25 μL Nafion, followed by ultrasonication for 2h to form a homogeneous ink. The catalyst ink was dropped on a rotating disc electrode (RDE, Φ:5mm) and dried in air. The loading mass of the catalyst was 0.65mg⋅cm-2. Linear sweep voltammetry (LSV) was carried out at a scan rate of 5 mV⋅s-1 with iR correction.

The electrochemically active surface area (ESCA) was calculated by using the following equation: ESCA=Cdl/Cs, where Cs is the specific capacitance of a flat surface (60 µF⋅cm-2) 2. ECSA estimation determined from Cdl. The Cdl obtained from the CV method is expected to be linearly proportional to the ECSA. CV measurements in a non-faradic current region (0.2-0.3 V vs. Hg/HgO) at scan rates of 10-80 mV⋅s−1 of a BPC and BPCF-0.2, BPCF-0.8.

Oxygen intercalation and diffusion coefficient measurements.

The electrochemical oxygen intercalation was performed at room temperature in an Arsaturated 6M KOH solution using a catalyst-modified GC working electrode, a Pt wire counter electrode, and a Hg/HgO reference electrode. CV was run at a 20 mV⋅s−1 scan rate with the stationary working electrode. Chroamperometry was performed on the same working electrode to measure the oxygen ion diffusion coefficient by applying a potential 50 mV more anodic than the E1/2 (defined as the potential halfway between the peak currents for oxygen insertion and extraction). The rotation rate was set at 2000 rpm during the chronoamperometry testing to remove any electrolyte-based mass-transfer effect. The chronoamperometry data were plotted as current versus the inverse square root of time (i vs. t−1/2), in which the linear portion was fitted to obtain the intercept with the t−1/2 axis (at i = 0). Using a bounded three-dimensional diffusion model 3, 4, this intercept was used to calculate the oxygen ion diffusion coefficient according to the equation λ = a(DOt)−1/2, where λ is a dimensionless shape factor, a is the radius of the particle, and DO is the diffusion coefficient. Here, λ was assumed to be 2, which is representative of a rounded parallelepiped, halfway between the values for a sphere (λ = 1.77) and a cube (λ = 2.26). 𝑎 is the radius of the perovskite particles identified from the HRTEM image 5.

  - Turnover frequencies (TOFs) for the OER

Equation (1) was used to compute the TOFs for the OER with each catalyst to evaluate the capacity of the catalytic sites:

TOF=JA/4Fn		(1)

Where J, A, F, and n are the current density at 1.55V for OER (mA·cm-2), electrode area(cm2), Faraday constant (96500 A s mol-1), and the amount of catalyst (moles), respectively.

  - Calculation of the specific activity (SA) and mass activity (MA)

The specific activity (mA⋅cm-2BET) was calculated with the equation:

Specific activity=JA/104*m*SBET		(2)

The mass activity(A⋅g-1catalyst​) was calculated from the measured current density(mA·cm-2) and normalized by the catalyst mass loading at a fixed potential of 1.55 V versus RHE. The following equation was used:

Mass activity=JA/m catalyst		(3)

where J is the current density at 1.55 V (mA·cm-2), A is the geometric electrode area (cm2), and m is the mass loading of the catalyst on the electrode (mg).

  - Zn-air batteries

In this work, catalyst Super P = 1:1 (wt.%) was mixed and ground for 15 min. After that, 5wt.% PTFE solution (10% of the total mass) was introduced into the resulting mixture, followed by grinding for 45 min. The resulting mixture was then coated onto carbon film (CF), named air cathode, which was then dried at high temperature overnight to remove the ethanol. To assemble an aqueous RZAB, a Zn plate was used as the anode, 6 M KOH and 0.2 M Zn (Ac)2⋅2H2O as an electrolyte, and a pump to circulate the electrolyte. The effective exposure area of the cathode to air is about 1 cm2.

The LANDT testing system was used to evaluate the performance of the assembled ZABs. The galvanostatic charging-discharging process with 1 h per cycle (charge for 30 min, discharge for 30 min) was used to estimate the cycle life of the RZABs. The discharge plateau of the RZABs at various current densities from 5 to 50 mA⋅cm-2 was obtained by the galvanostatic discharging process. According to the galvanostatic discharge curves at a constant current density of 10 mA⋅cm-2 and the consumed mass of the Zn plate, the specific capacity of the RZABs was calculated.

1.7. Density functional theory (DFT) calculations

All spin-polarized density functional theory (DFT) calculations were performed using the Vienna Ab-initio Simulation Package (VASP) 6-8. The exchange-correlation functional was treated within the generalized gradient approximation (GGA) using the Perdew-Burke-Ernzerhof (PBE) formulation 9. The electron-ion interactions were described by the projector augmented-wave (PAW) pseudopotentials. A plane-wave kinetic energy cutoff of 520 eV was set for the basis set. The Brillouin zone was sampled using a 3×4×1 Monkhorst-Pack k-point mesh for geometric optimization. To account for the strong on-site Coulomb interactions of the 3d electrons, the DFT+U approach was employed for Co and Fe atoms, with an effective U-J parameter of 4.0 eV applied to Co and Fe. Van der Waals interactions were considered using Grimme's DFT-D3 dispersion correction method. A vacuum layer of at least 15 Å was applied in the direction perpendicular to the slab to avoid spurious interactions between periodic images.

Section S2 Figures

Figure S1. Rietveld refinement analysis of XRD patterns. (a) BPC; (b) BPCF-0.2; (c) BPCF-0.8

Figure S2. (a) O 1s XPS of BPCF-x and (b) concentration of various oxygen species present in different perovskite catalysts.

Figure S3. (a) XPS spectra of BPCF-0.8 and BPCF-1.0; (b) concentration of various oxygen species present in different perovskite catalysts; (c) EPR spectra of BPCF-0.8 and BPCF-1.0.

Figure S4. Fe 2p XPS spectra of BPCF-x (x=0.2,0.8) electrocatalysts.

Figure S5. The Fe K-edge XANES spectra of BPCF-0.8, inset in (S5), and the amplification results of the corresponding spectra.

Figure S6. TEM and corresponding EDX mapping of BPCF-0.8.

Figure S7. SEM images of (a) BPC; (b) BPCF-0.2 and (c) BPCF-0.8.

Figure S8. N2 adsorption-desorption isotherms and pore size distributions of (a) BPC; (b) BPCF-0.2; (c) BPCF-0.8.

Figure S9. CV curves for measuring the double-layer capacitance (Cdl) in a non-faradic current region (0.2V-0.3V vs. Hg/HgO) at scan rates of 10,20,30,40,50,60,70, and 80 mV⋅s-1 of BPC; BPCF-0.2 and BPCF-0.8.

Figure S10. XPS analysis of BPCF-0.8 before and after cycling. (a) Co 2p spectra; (b) Fe 2p spectra; (c) O 1s spectra, and (d) relative concentration of oxygen species obtained by peak deconvolution. XPS measurements were performed on the carbon-free catalyst after electrochemical cycling to probe intrinsic structural evolution.

Figure S11. (a) ORR LSV curves in an O2-saturated 0.1 M KOH solution; (b) ORR polarization curves of BPCF-0.8 at various rotation speeds from 400 to 2025 rpm; (c) Corresponding Koutecký-Levich (K-L) plots at different potentials; (d) Chronoamperometry comparison of the ORR between BPCF-0.8 and Pt/C.

Figure S12. (a) pH-dependent LSV curves of BPCF-0.2; (b) OER specific activities of BPCF-0.2 at 1.55 V versus different pHs of KOH.

Figure S13. (a) LSV polarization curves of BPCF-0.2 in 1 M KOH and TMAOH electrolyte; respectively; (b) Tafel slope decay of BPCF-0.2 in TMAOH.

Figure S14. CV curves of BPCF-x in Ar-saturated 6 M KOH, where redox peaks indicate the electrochemical oxygen intercalation/deintercalation. Inset of d shows the chronoamperometry data (i vs. t–1/2) used for the calculation of oxygen ion diffusion coefficients.

Figure S15. The absorption model on (a) BPC; (b) BPCF-0.2, and (c) BPCF-0.8 surface via AEM.

Figure S16. The absorption model on (a) BPC; (b) BPCF-0.2, and (c) BPCF-0.8 surface via LOM.

Figure S17. The multimeter tested the OCV of RZABs.

Section S3 Tables

Table S1. Refined structure parameters of BPCF-x using powder X-ray diffraction data.

| Sample | Space group | a (Å) | b (Å) | C (Å) |
| --- | --- | --- | --- | --- |
| BPC | P4/mmm | 3.903 | 3.903 | 7.654 |
| BPCF-0.2 | P4/mmm | 3.903 | 3.903 | 7.682 |
| BPCF-0.8 | P4/mmm | 3.920 | 3.920 | 7.868 |

Table S2. Fitting result of FT-EXAFS curves shown in Figure 1f.

| Catalysts | Bond type | R (Å) | σ2(*10-3Å) | R-factor | N |
| --- | --- | --- | --- | --- | --- |
| BPC | Co-O | 1.9074 | 3.2933 | 0.012 | 4.211 |
| BPCF-0.8 | Co-O | 1.8722 | 1.8900 | 0.018 | 3.844 |

N: coordination number; R: bonding distance; σ2: Debye-Waller factor; R factor: goodness of fit.

Table S3. BET surface areas, theoretical density, and Do of BPCF-x.

| Sample | BET surface areas (m2 g-1) | density (g/cm3) | Do (cm2 s-1) |
| --- | --- | --- | --- |
| BPC | 1.37 | 6.8938 | 0.51*10-12 |
| BPCF-0.2 | 2.29 | 6.8517 | 0.63*10-12 |
| BPCF-0.8 | 3.15 | 6.5805 | 2*10-12 |

Table S4. OER activity comparison of BPCF-0.8 with other reported electrocatalysts.

| Catalysts | Current density (mA cm-2) | Overpotential (mV) | Tafel (mv dec-1) | Reference |
| --- | --- | --- | --- | --- |
| BPCF-0.8 | 10 | 295 | 45 | This work |
| ES-LSFN-0.5 | 10 | 295 | 73 | 10 |
| La0.9Sn0.1NiO3-δ | 10 | 318 | 74 | 11 |
| 3S-LaCo0.5Ni0.5HoMSs | 10 | 330 | 60 | 12 |
| LaNi0.3Fe0.7O2.759QDs/CNT | 10 | 340 | 74 | 13 |
| LSFNO-0.4 | 10 | 340 | 53.75 | 14 |
| LSC&MoSe2 | 10 | 350 | 77 | 15 |
| SrCo0.8Fe0.5-xO3-δ/FexOy | 10 | 352 | 79 | 16 |
| LaCoO3/NiCo2O4 | 10 | 353 | 59 | 17 |
| Ce- LaCoO3 | 10 | 380 | 80 | 18 |
| F0.2-LCO | 10 | 390 | 65 | 19 |
| LaMn0.4Co0.6O3 | 10 | 400 | 95 | 20 |

Table S5.  OCP comparison of BPCF-0.8 with other reported electrocatalysts.

| Catalyst | OCP（V） | Reference |
| --- | --- | --- |
| Co3O4@LaCoO3 | 1.46 | 21 |
| ZnCoMnO4/N-rGO | 1.45 | 22 |
| 1 nm-CoOx/N-RGO | 1.39 | 23 |
| SFCNM | 1.43 | 24 |
| S5.84%-LCO | 1.47 | 25 |
| LSCF@rGO-0.50 | 1.38 | 26 |
| FeNiCo¦MnGaOx/CNT | 1.43 | 27 |
| Co3O4/CoNGDY | 1.51 | 28 |

Reference

1.	B. Ravel and M. Newville, Journal of Synchrotron Radiation, 2005, 12, 537-541.

2.	F. Qin, Z. Zhao, M. K. Alam, Y. Ni, F. Robles-Hernandez, L. Yu, S. Chen, Z. Ren, Z. Wang and J. Bao, ACS Energy Letters, 2018, 3, 546-554.

3.	F. R. Van Buren, G. H. J. Broers, A. J. Bouman and C. Boesveld, Journal of Electroanalytical Chemistry and Interfacial Electrochemistry, 1978, 88, 353-361.

4.	J. T. Mefford, X. Rong, A. M. Abakumov, W. G. Hardin, S. Dai, A. M. Kolpak, K. P. Johnston and K. J. Stevenson, Nature Communications, 2016, 7, 11053.

5.	J. T. Mefford, W. G. Hardin, S. Dai, K. P. Johnston and K. J. Stevenson, Nature Materials, 2014, 13, 726-732.

6.	J. Hafner, Journal of Computational Chemistry, 2008, 29, 2044-2078.

7.	E. Wimmer, M. Christensen, V. Eyert, W. Wolf, D. Reith, X. Rozanska, C. Freeman and P. Saxe, J. Korean Ceram. Soc, 2016, 53, 263-272.

8.	G. Kresse and J. Furthmüller, Physical review. B, Condensed matter, 1996, 54, 11169-11186.

9.	J. P. Perdew, K. Burke and M. Ernzerhof, Physical Review Letters, 1996, 77, 3865-3868.

10.	L. Li, Z. Zheng, J. Li, Y. Mu, Y. Wang, Z. Huang, Y. Xiao, H. Huang, S. Wang, G. Chen and L. Zeng, Small, 2023, 19, 2301261.

11.	C. Liu, D. Ji, H. Shi, Z. Wu, H. Huang, Z. Kang and Z. Chen, Journal of Materials Chemistry A, 2022, 10, 1336-1342.

12.	H. Wang, J. Qi, N. Yang, W. Cui, J. Wang, Q. Li, Q. Zhang, X. Yu, L. Gu, J. Li, R. Yu, K. Huang, S. Song, S. Feng and D. Wang, Angewandte Chemie International Edition, 2020, 59, 19691-19695.

13.	S. Lu, Y. Wang, Y. Han, M. Zhong, H. Yang, B. Su and Z. Lei, European Journal of Inorganic Chemistry, 2021, 2021, 2225-2230.

14.	S.-F. Li, B.-Q. Zhang, Y.-Q. Wang and D. Yan, Chemical Engineering Journal, 2024, 491, 151912.

15.	M. Kunitski, N. Eicke, P. Huber, J. Köhler, S. Zeller, J. Voigtsberger, N. Schlott, K. Henrichs, H. Sann, F. Trinter, L. P. H. Schmidt, A. Kalinin, M. S. Schöffler, T. Jahnke, M. Lein and R. Dörner, Nature Communications, 2019, 10, 1.

16.	Y. Yi, Q. Wu, J. Li, W. Yao and C. Cui, ACS Applied Materials & Interfaces, 2021, 13, 17439-17449.

17.	D. Kubba, I. Ahmed, P. Kour, R. Biswas, H. Kaur, K. Yadav and K. K. Haldar, ACS Applied Nano Materials, 2022, 5, 16344-16353.

18.	D. Ji, C. Liu, Y. Yao, L. Luo, W. Wang and Z. Chen, Nanoscale, 2021, 13, 9952-9959.

19.	J. Ran, L. Wang, M. Si, X. Liang and D. Gao, Small, 2023, 19, 2206367.

20.	X. Jiang, Y. Dong, Z. Zhang, J. Li, J. Qian and D. Gao, Journal of Alloys and Compounds, 2021, 878, 160433.

21.	J. Ran, J.-F. Wu, Y. Hu, M. Shakouri, B. Xia and D. Gao, Journal of Materials Chemistry A, 2022, 10, 1506-1513.

22.	W. Liu, D. Rao, J. Bao, L. Xu, Y. Lei and H. Li, Journal of Energy Chemistry, 2021, 57, 428-435.

23.	T. Zhou, W. Xu, N. Zhang, Z. Du, C. Zhong, W. Yan, H. Ju, W. Chu, H. Jiang, C. Wu and Y. Xie, Advanced Materials, 2019, 31, 1807468.

24.	K. Li, J. Gao, X. Han, Q. Shao and Z. Lü, Journal of Energy Chemistry, 2024, 96, 669-678.

25.	J. Ran, T. Wang, J. Zhang, Y. Liu, C. Xu, S. Xi and D. Gao, Chemistry of Materials, 2020, 32, 3439-3446.

26.	X. Wang, J. Sui, Z. Hou, M. Zhang, Q. Zhang, J. Yu, Z. Gan, L. Sui and L. Dong, Diamond and Related Materials, 2023, 132, 109668.

27.	L. Luo, Y. Liu, S. Chen, Q. Zhu, D. Zhang, Y. Fu, J. Li, J. Han and S. Gong, Small, 2024, 20, 2308756.

28.	Q. Chang, F. He, Z. Zhang, X. Fu, Y. Wang, C. Huang and Y. Li, Angewandte Chemie International Edition, 2025, 64, e202416664.