Supporting Information

Rational Tuning of naphthalene diimide (NDI)-thienoisoindigo (TIIG) copolymer compositions for high-performance all-polymer photodetectors with broadband response from 300 nm to 1050 nm

Jiawei Liua, 1, Xin Wangb, 1, Huaxin Zhua, Shijia Gaoc, Wenqiang Qiaoa,*

a State Key Laboratory of Fine Chemicals, Department of Polymer Science & Materials, School of Chemical Engineering, Dalian University of Technology, Dalian 116024, P. R. China.

b China Nuclear Power Engineering Co., Ltd., Beijing 100142, P. R. China.

c Sinopec (Beijing) Research Institute of Chemical Industry Co., Ltd., Beijing 100013, P. R. China.

1 These authors contributed equally to this work.

* Corresponding author: E-mail addresses: wqqiao@dlut.edu.cn (W. Qiao)

1. Synthesis

Scheme S1. Synthetic route of monomer (6)

Synthesis of 3. Compound 1 (9.8 g, 60.0 mmol), Compound 2 (26.8 g, 90.0 mmol), copper powder (190.5 mg, 3.0 mmol), CuI (572.0 g, 3.0 mmol), K3PO4 (25.4 g, 120.0 mmol) were dissolved in dimethylethanolamine (100 mL) in a dry round-bottomed flask. Seal the flask, evacuate it, and purge it with nitrogen four times under vacuum. Keep the reaction system in the dark, heat it to 90 °C, and allow the reaction to proceed for 48 hours. Upon completion of the reaction, filter the reaction mixture, reduce the pressure, and perform rotary evaporation to concentrate the solvent. Finally, use a n-hexane/ethyl acetate (10:1, v/v) mixture as the eluent for silica gel column chromatography purification to obtain 12.7 g of a brown oily product, with a yield of 55%. The amino product 3 is unstable; therefore, it is immediately utilized for the synthesis of the next compound. 1H NMR (400 MHz，CDCl3, δ/ppm): 7.14 (d, 1H), 6.62 (d, 1H), 5.91 (d, 1H), 3.59 (br, 1H)，2.97 (d, 2H), 1.59 (br, 1H), 1.29 (m, 32H), 0.88 (m, 6H).

Synthesis of 4. At 0 °C, the oxalyl chloride (3.9 mL, 45.2 mmol) was dissolved in 110 mL of dichloromethane within a round-bottom flask. The resulting mixture was stirred under a nitrogen atmosphere. The compound 3 (12.7 g, 33.4 mmol), which was synthesized in the previous step, was dissolved in 42 mL of dichloromethane and introduced into the round- bottom flask through a dropping funnel. Once the dropwise addition was finished, the mixture was stirred for an additional 1 hour. Subsequently, 12.88 mL of triethylamine was dissolved in 35 mL of dichloromethane and added to the reaction system. The mixture was then allowed to warm to room temperature naturally and was left to react for 24 hours. Upon completion of the reaction, the mixture was directly filtered. The filter residue was washed three times with ethyl acetate, and the solvent was removed via vacuum rotary evaporation. Finally, the product was purified by column chromatography using a silica gel column with a eluent of n-hexane/ethyl acetate (5:1, v/v), affording 6.8 g of a red oily product with a yield of 47%. 1H NMR (400 MHz, CDCl3, δ/ppm): 7.92 (d, 1H), 6.68 (d, 1H), 3.46 (d, 1H)，1.79 (br, 2H), 1.18 (m, 32H), 0.88 (m, 6H).

Synthesis of 5. Compound 4 (6.75 g, 15.6 mmol), Lawesson's reagent (3.15 g, 7.8 mmol), and 140 mL of toluene were introduced into a dry round-bottom flask. The flask was then sealed, evacuated, and purged with nitrogen under vacuum four times. The reaction was conducted in the absence of light at 80 °C for 3 hours. Upon completion of the reaction, the system was cooled to ambient temperature, and 40 mL of deionized water was added to terminate the reaction. The resulting mixture was extracted three times with diethyl ether, dried over anhydrous Na₂SO₄, filtered, and the solvent was removed under reduced pressure via rotary evaporation. Ultimately, the product was purified by column chromatography using a silica gel column with a eluent of n-hexane/dichloromethane (3.5:1, v/v). A deep purple solid product (3.17 g) was obtained, with a yield of 48%. 1H NMR (400 MHz，CDCl3, δ/ppm): 7.54 (d, 2H), 6.78 (d, 2H), 3.70 (d, 4H), 1.90 (br, 2H), 1.28 (m, 64H), 0.88 (m, 12H).

Synthesis of 6. At 0 °C, the compound 5 (3.17 g, 3.8 mmol) and 120 mL of tetrahydrofuran were introduced into a dry Schlenk flask. The flask was then sealed, and the system was evacuated and purged with nitrogen four times. Under light-shielding conditions, N- bromosuccinimide (NBS) (2.29 g, 12.8 mmol) was dissolved in 30 mL of tetrahydrofuran and added dropwise to the reaction mixture. After the dropwise addition was finished, the reaction was allowed to proceed for 1 hour. Upon the completion of the reaction, 40 mL of deionized water was added to quench the reaction, and the resulting mixture was extracted three times with dichloromethane. The organic layer was dried over anhydrous Na2SO4 and then filtered. Finally, purification via silica gel column chromatography was performed using n-hexane/dichloromethane (4:1, v/v) as the elution solvent, and 3.02 g of a deep-blue solid product was obtained, with a yield of 80%. 1H NMR (400 MHz, CDCl3, δ/ppm): 6.81 (s, 2H), 3.63 (d, 4H), 1.83 (m, 2H), 1.26 (bm, 64H), 0.87 (m, 12H).  13C NMR (100 MHz, CDCl3, δ/ppm): 170.45, 150.23, 123.16, 119.77, 114.98, 114.76, 46.21, 37.20, 31.91, 31.87, 31.40, 29.94, 29.61, 29.56, 29.50, 29.34, 29.28, 26.40, 22.66, 14.09. MALDI-TOF-MS (m/z) calc. for C52H84Br2N2O2S2 990.43, found: 990.40.

Scheme S2. Synthsis of acceptor polymers

Synthesis of PNDI. Monomer 7 (295.5 mg, 0.3 mmol), monomer 8 (122.7 mg, 0.3 mmol), Pd2(dba)3 (5.5 mg, 0.006 mmol), P(o-tol)3 (7.3 mg, 0.024 mmol) were dissolved in anhydrous toluene (8 mL) in a dry Schlenk tube. The mixture was degassed and charged with nitrogen for several times, then stirred vigorously at 110 °C for 4 h under nitrogen atmosphere. After the solution was cooled to room tempreture, the solution was poured into anhydrous methanol (150 mL), and stirred for 30 min. After suction filtration, the crude product was purified with acetone, n-hexane, and chloroform on a Soxhlet’s extractor. The final product was obtained by precipitating the concentrated chloroform solution into methanol. The polymer was collected by suction filtration and dried under reduced pressure at 55 °C for 48 h to obtain a black solid (244.5 mg, 89.5%). GPC (tetrahydrofuran): Mn = 113.2 kDa, Mw = 292.1 kDa, PDI = 2.6. 1H NMR (400 MHz, C2D2Cl4, δ/ppm): 8.98 (br, 2H), 7.52 (br, 2H), 4.18 (br, 2H), 2.07 (br, 2H), 1.22 (br, 64H), 0.87 (m, 12H).

Synthesis of PNDITII-10. It was synthesized with the same procedure as PNDI. Monomers and catalyst: 6 (266.0 mg, 0.27 mmol), 7 (29.8 mg, 0.03 mmol), 8 (122.7 mg, 0.3 mmol), Pd2(dba)3 (5.5 mg, 0.006 mmol), P(o-tol)3 (7.3 mg, 0.024 mmol) and anhydrous toluene (8 mL). Black solid, (247.6 mg, 90.5%). GPC (Tetrahydrofuran): Mn = 123.8 kDa, Mw = 358.4 kDa, PDI = 2.9. 1H NMR (400 MHz, C2D2Cl4, δ/ppm): 8.98 (br, 2H), 7.52 (br, 2H), 4.17 (br, 4H), 2.06 (br, 2H), 1.22 (br, 64H), 0.87 (m, 12H).

Synthesis of PNDITII-30. It was synthesized with the same procedure as PNDI. Monomers and catalyst: 6 (206.9 mg, 0.21 mmol), 7 (89.4 mg, 0.09 mmol), 8 (122.7 mg, 0.3 mmol), Pd2(dba)3 (5.5 mg, 0.006 mmol), P(o-tol)3 (7.3 mg, 0.024 mmol) and anhydrous toluene (8 mL). Black solid, (256.9 mg, 93.9%).GPC (Tetrahydrofuran): Mn = 217.0 kDa, Mw = 530.7 kDa, PDI = 2.4. 1H NMR (400 MHz, C2D2Cl4, δ/ppm): 8.98 (br, 2H), 7.52 (br, 2H), 4.18 (br, 2H), 2.07 (br, 2H), 1.22 (br, 64H), 0.87 (m, 12H).

Synthesis of PNDITII-50. It was synthesized with the same procedure as PNDI. Monomers and catalyst: 6 (147.8 mg, 0.15 mmol), 7 (174.3 mg, 0.15 mmol), 8 (122.7 mg, 0.3 mmol), Pd2(dba)3 (5.5 mg, 0.006 mmol), P(o-tol)3 (7.3 mg, 0.024 mmol) and anhydrous toluene (8 mL). Black solid, (243.4 mg, 89.0%). GPC (Tetrahydrofuran): Mn = 110.7 kDa, Mw = 234.9 kDa, PDI = 2.1. 1H NMR (400 MHz, C2D2Cl4, δ/ppm): 8.98 (br, 2H), 7.52 (br, 2H), 4.18 (br, 2H), 2.07 (br, 2H), 1.22 (br, 64H), 0.87 (m, 12H).

Scheme S3. Synthsis of donor polymer PDPP

Synthesis of PDPP. It was synthesized with the same procedure as PNDI. Monomers and catalyst: 9 (305.8 mg, 0.3 mmol), 10 (174.3 mg, 0.3 mmol), Pd2(dba)3 (5.5 mg, 0.006 mmol), P(o-tol)3 (7.3 mg, 0.024 mmol) and anhydrous toluene (8 mL). Black solid, (315.2 mg, 92.1%). GPC (Tetrahydrofuran): Mn = 6.9 kDa, Mw = 11.7 kDa, PDI = 1.7.

2. Instruments and Measurements

The 1H NMR (400 MHz) and 13C NMR (100 MHz) spectra were recorded on Varian DLG400 using deuterated chloroform (CDCl3) and 1,1,2,2-tetrachloroethane (C2D2Cl4) as the solvent and tetramethylsilane (TMS) as internal standard. MALDI-TOF-MS spectra were recorded by Bruker Ultraflextreme mass spectrometer. The molecular weight of the three polymers was determined by gel permeation chromatography (GPC) analysis on a Shimadzu GPC system with an SPD-20A UV-vis detector using polystyrene (PS) as standard and tetrahydrofuran (THF) as eluent at 40 °C. Thermogravimetric analysis (TGA) data were obtained on a TA Q500 instrument from 30 to 800 °C at a heating rate of 10 °C·min−1 under a nitrogen flow. Differential scanning calorimetry (DSC) was performed on a TA Q20 from 40 to 300 °C with a heating rate of 10 ºC·min−1 under nitrogen flow. The UV-vis-NIR absorption spectra were conducted on a Shimadzu UV-3700 spectrophotometer. The temperature-dependent UV-vis absorption spectra were measured on an Agilent Cary 100 spectrophotometer. Cyclic voltammetry (CV) was carried out on a CHI660b electrochemical workstation in dry acetonitrile solution with tetrabutylammonium hexafluorophosphate (n-Bu4NPF6, 0.1 M) as the electrolyte at a scan rate of 50 mV·s-1 under an inert atmosphere. A platinum disk (2 mm diameter), an Ag/AgCl and a platinum wire electrode were used as the working electrode, the reference electrode and the counter electrode, respectively. Ferrocene/ferrocenium (Fc/Fc+) was used as an internal standard for calibration and the energy level of Fe/Fc+ was taken as -4.8 eV below vacuum. Density functional theory (DFT) calculations were performed at B3LYP/6-31G(d) level using the Gaussian 16 Package [1]. The long alkyl chains of the trimer were replaced by methyl groups to simplify the computational complexity. The frontier molecular orbitals (HOMO and LUMO) were deduced on Gaussian view 6. The electrostatic potential surface (EPS) files were generated on Multiwfn 3.8(dev) and the image of ESP distributions was exported by VMD 1.9.4 program [2,3]. Atomic force microscopy (AFM) studies were carried out on a JPK Nanowizard 4XP instrument in tapping mode under ambient condition. Transmission electron microscopy (TEM) images were obtained by using JEOL JEM-1400 transmission electron microscope operated at 100 kV, with samples on top of the copper grids. Grazing incidence wide-angle X-ray scattering (GIWAXS) measurements were performed at 1W1A Diffuse X-ray Scattering Station, Beijing Synchrotron Radiation Facility (BSRF-1W1A). The incident X-ray beam (8.02 keV, 0.154 nm) at a grazing angle of 0.15° was selected to maximize the scattering intensity from the samples. The 2D scattering patterns were recorded using an eiger 1M detector. Contact angle (CA) was tested on POWEREACH JCD2000D2W contact angle analyzer. The film thickness was measured by KLA Tencor D-100 stylus profilometer.

3. Device characterization

Characterizations of all-polymer photodetector devices. Responsivity (R), linear dynamic range (LDR), and transient photocurrent response (τr/τf) measurements were conducted under ambient conditions using a photodetector test system from Beijing Sofn Optical Instruments Co., Ltd. A crystalline silicon photo-diode (Thorlabs’ FDS010) calibrated by Thorlabs GmbH manufacturer was used as the reference to measure the polymer photodetectors. The maximum and minimum light source power for linear dynamic range test is 0.37 W and 9.78 × 10-14 W, respectively. The transient photocurrent response of the photodetector was obtained by measuring the output electrical signal of the device with pulse radiation (640 nm or 790 nm monochromatic light with a period of 150 μs or 75 μs).[4] The current density-voltage (J-V) characteristics of the devices were measured using a Keithley 2400 source meter. The light current density was tested under a white light of 100 mW·cm–2 illumination. The noise power spectra of photodetectors were measured in a shielded metallic box by using a low-noise current amplifier (DLPCA-200, Femto) and a multifunctional I/O device (USB-6361, NI), with a fast-Fourier transformation applied to the resulting measurement.

4. Supplementary figures and Tables

Fig. S1. 1H NMR spectrum of compound 3 (400 MHz, CDCl3).

Fig. S2. 1H NMR spectrum of compound 4 (400 MHz, CDCl3).

Fig. S3. 1H NMR spectrum of compound 4 (400 MHz, CDCl3).

Fig. S4. 1H NMR spectrum of compound 5 (400 MHz, CDCl3).

Fig. S5. 13C NMR spectrum of compound 5 (400 MHz, CDCl3).

Fig. S6. Mass spectrum (MALDI-TOF) of compound 5.

Fig. S7. 1H NMR spectrum of PNDI (400 MHz, C2D2Cl4).

Fig. S8. 1H NMR spectrum of PNDITII-10  (400 MHz, C2D2Cl4).

Fig. S9. 1H NMR spectrum of PNDITII-30  (400 MHz, C2D2Cl4).

Fig. S10. 1H NMR spectrum of PNDITII-50  (400 MHz, C2D2Cl4).

Fig. S11. GPC test curve of (a) PNDI, (b) PNDITII-10, (c) PNDITII-30, and (d) PNDITII-50

Fig. S12.  DSC curves of PNDI, PNDITII-10, PNDITII-30, and PNDITII-50

Fig. S13. TGA curves of PNDI, PNDITII-10, PNDITII-30, and PNDITII-50

Fig. S14. The frontier molecular orbitals (HOMO and LUMO) of the PNDI, PNDITII, and PTII trimer repeating units

Fig. S15. Comparison of R and D* in reported (a) organic photodetectors (OPDs) or (b) all-PPDs and in this work.

Fig. S16. (a) Responsivity, (b) EQE and (c) D* of the polymer photodetectors at -0.5 V. (d) Responsivity, (e) EQE and (f) D* of the polymer photodetectors at -1.0 V.

Fig. S17. I-V curves for the shunt resistance (Rsh) of the four polymer photodetectors.

Fig. S18. Summary of response time at different bias with a period of (a) 150 μs and (b) 75 μs; Transient photocurrent response of the devices with a period of (c) 150 μs and (d) 75 μs

Fig. S19. AFM histogram data of (a) PDPP:PNDI, (b) PDPP:PNDITII-10, (c) PDPP:PNDITII-30, and (d) PDPP:PNDITII-50; Three-dimensional topography images with (e) PDPP:PNDI , (f) PDPP:PNDITII-10, (g) PDPP:PNDITII-30, (h) PDPP:PNDITII-50 as the active layer films (2.0 μm × 2.0 μm).

Fig. S20. AFM histogram data of (a) PDPP, (b) PNDI, (c) PNDITII-10, (d) PNDITII-30, and (e) PNDITII-50 polymer pristine films; Three-dimensional topography images of (f) PDPP, (g) PNDI, (h) PNDITII-10, (i) PNDITII-30, and (j) PNDITII-50 polymer pristine films (2.0 μm × 2.0 μm).

Fig. S21.  Film thickness data of the blend films (Lblend films = LZnO/blend films - LZnO)

Supplementary tables

Table S1. Comparison of device performances of organic photodetectors and this work.

| Active layer | Wavelength (nm) | Rmax (mA·W-1) | Dmax* (Jones) | Jd (A·cm−2) | LDR (dB) | tr(μs)/ f-3 dB (kHz) | bias (V) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Organic photodetectors |  |  |  |  |  |  |  |  |
| NT812:IEICO-4F | 300~1000 | ~420 | 5.0×1013 | 2.2×10-10 | 129 | 4.5/- | -0.1 | [5] |
| PTB7-Th:COB | 300~1100 | ~455 | 3.2×1012 | 5.2×10-8 | 97 | -/52.1 | -0.5 | [6] |
| PffBT4T-2OD: PC71BM:IEICO-4F | 300~950 | ~210 | 7.2×1012 | 2.6×10-9 | 110 | 0.27/440 | -1 | [7] |
| PTB7-Th:COTCN2 | 400~1200 | ~230 | 1.2×1012 | 1.1×10-7 | 82 | -/45.8 | -0.5 | [8] |
| PNTB6-Cl:Y6 | 400~900 | ~470 | 6.8×1012 | 4.5×10-7 | 132 | -/23.7 | 0 | [9] |
| BODIPYF:PCBM | 300~900 | ~125 | 6.0×1011 | ~10-8 | - | 0.5/700 | -0.5 | [10] |
| PTB7-Th: COi8DFIC:PC71BM | 400~1100 | ~435 | 8.8×1010 | 3.5×10-5 | - | -/100 | -1 | [11] |
| DTDCPB:C70 | 300~800 | ~295 | 7.0×1012 | 5.3×10-9 | 124 | 0.68/692 | -3 | [12] |
| PTQ10:EH-TCNBT | 400~800 | ~170 | 2.9×1011 | 1.3×10-5 | 98 | - | -2 | [13] |
| TQ-T:IECO-4F | 400~1600 | ~90 | 2.0×1010 | 8.3×10-3 | 46 | 6.6/100 | -2 | [14] |
| TQ-Por-TQ:PC71BM | 300~1100 | ~110 | 4.0×1011 | ~10-6 | - | 435/- | -2 | [15] |
| PMDPP3T:PC61BM | 300~900 | ~560 | 5.6×1012 | 3.2×10-8 | ~60 | ~16/- | -2 | [16] |
| SQ-H:PC61BM | 450~1100 | ~110 | 4.0×1010 | ~10-7 | ~100 | -/330 | 0 | [17] |
| PBT7-Th:CO1-4Cl | 300~1000 | ~340 | 5.8×1012 | ~10-8 | - | 5/95 | -1 | [18] |
| PNIR:ITIC | 400~1000 | ~100 | 1.0×1012 | 6.1×10-8 | 58 | 52/- | -0.5 | [19] |
| PSNT-IT:PC71BM | 300~1000 | ~70 | 7.1×1010 | 2.8×10-6 | 141 | 66/7.5 | -1.5 | [20] |
| PM6:O4TFIC | 400~1000 | ~500 | 9.0×1011 | 8.3×10-5 | - | 2.9/- | -2 | [21] |
| All-polymer photodetectors |  |  |  |  |  |  |  |  |
| PF3:IT-4F | 300~800 | ~310 | 7.4×1012 | 5.6×10-9 | 95 | 2.3/63 | -2 | [4] |
| TQ1:N2200 | 400~800 | ~30 | 1.9×1011 | 3.4×10-3 | 83 | - | -0.5 | [22] |
| PBDB-T:N2200 | 300~800 | ~420 | 6.3×1012 | 1.4×10-8 | - | -/50 | -2 | [23] |
| PM6:PY-IT | 300~900 | ~470 | 2.1×1012 | 1.5×10-7 | 80 | 4.9/- | -1 | [24] |
| PBDB-T6:PNDI-DTBT | 300~800 | ~310 | 4.8×1012 | 1.3×10-8 | - | - | -0.1 | [25] |
| PTB7-Th:PNDI-T10 | 350~800 | ~180 | 4.0×1011 | 1.5×10-9 | 75 | -/350 | 0 | [26] |
| PSBOTz:PDNBO | 300~650 | ~86 | 1.1×1013 | 2.1×10-10 | - | 110/- | -2 | [27] |
| PtzBI-Ph:N2200 | 300~800 | ~250 | 5.7×1012 | 5.7×10-9 | - | - | -0.1 | [28] |
| PBnDT-FTAZ:N2200 | 350~800 | ~250 | 6.0×1012 | ~10-6 | - | -/~1 | -0.5 | [29] |
| PBDB-T:PNDI-FT10 | 300~800 | ~350 | 5.8×1012 | 1×10-7 | 105 | - | -3 | [30] |
| PTB7-Th:PNDI-DPP10 | 300~1000 | ~49 | 2.4×1012 | 1.3×10-9 | - | - | -0.1 | [31] |
| PolyD:PolyAA’25 | 300~1000 | ~94 | 4.7×1012 | 1.7×10-9 | - | - | -0.1 | [32] |
| PTB7-Th:PIIG-PDI(EH) | 350~800 | ~120 | 6×1011 | 7.5×10-8 | - | - | -0.2 | [33] |
| PDPP:PNDITII-10 | 300~1050 | 50.0 | 1.6×1012 | 3.1×10-9 | 96 | 3.4/- | -0.1 | This work |

Table S2. Summary of responsivity and specific detectivity of the polymer photodetectors at -0.5 V and -1.0 V

| Active layer | aR600 nm (Ma·W-1) | aR900 nm (Ma·W-1) | bR600 nm (Ma·W-1) | bR900 nm (Ma·W-1) | aDmax* (Jones) | bDmax* (Jones) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PDPP: PNDI | 28.1 | 48.4 | 37.3 | 61.5 | 2.8 × 1011 | 1.8 × 1011 |  |  |
| PDPP: PNDITII-10 | 31.5 | 58.3 | 37.0 | 70.3 | 5.9 × 1011 | 3.2 × 1011 |  |  |
| PDPP: PNDITII-30 | 16.8 | 34.2 | 21.4 | 43.6 | 3.4 × 1011 | 2.2 × 1011 |  |  |
| PDPP: PNDITII-50 | 5.8 | 11.3 | 8.1 | 15.4 | 1.8 × 1011 | 1.6 × 1011 |  |  |

aTest under -0.5 V. bTest under -1.0 V.

Table S3. The noise power densities of the four devices at different frequencies and the corresponding Dmax* at -0.1 V.

| Active layer |  | 10 Hz |  | 50 Hz |  | 100 Hz | 500 Hz |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DPP: PNDI | noise power density (A·Hz-1/2) | 2.2 × 10-12 | 6.3 × 10-13 |  | 3.2 × 10-13 |  |  | 1.0 × 10-13 |
|  | Dmax* (Jones) | 2.5 × 1010 | 1.9 ​​× 1011 |  | 5.5 × 1011 |  |  | 3.9 × 1012 |
| PDPP: PNDITII-10 | noise power density (A·Hz-1/2) | 1.0 × 10-12 | 3.2 × 10-13 |  | 3.0 × 10-13 |  |  | 1.0 × 10-13 |
|  | Dmax* (Jones) | 6.3 × 1010 | 4.5 × 1011 |  | 6.7 × 1011 |  |  | 4.5 × 1012 |
| PDPP: PNDITII-30 | noise power density (A·Hz-1/2) | 1.0 × 10-12 | 2.8 × 10-13 |  | 1.4 × 10-13 |  |  | 6.3 × 10-14 |
|  | Dmax* (Jones) | 3.2 × 1010 | 2.5 × 1011 |  | 7.0 × 1011 |  |  | 3.5 × 1012 |
| PDPP: PNDITII-50 | noise power density (A·Hz-1/2) | 6.3 × 10-13 | 2.2 × 10-13 |  | 1.4 × 10-13 |  |  | 2.8 × 10-14 |
|  | Dmax* (Jones) | 1.6 × 1010 | 1.0 × 1011 |  | 2.3 × 1011 |  |  | 2.6 × 1012 |

Table S4. Summary of transient photocurrent response

| Active layer | a) -0.1 V (μs) | a) -0.5 V (μs) | a) -1.0 V (μs) | b) -0.1 V (μs) | b) -0.5 V (μs) | b) -1.0 V (μs) |
| --- | --- | --- | --- | --- | --- | --- |
| PDPP:PNDI | 3.6/11.2 | 3.4/10.7 | 3.0/9.6 | 3.2/10.3 | 2.9/9.6 | 2.4/8.6 |
| PDPP:PNDITII-10 | 3.4/10.1 | 2.9/9.7 | 2.4/9.3 | 2.9/9.8 | 2.6/9.4 | 1.9/8.5 |
| PDPP:PNDITII-30 | 4.5/13.5 | 4.4/12.9 | 3.6/12.5 | 4.1/11.7 | 3.2/12 | 3.0/11.1 |
| PDPP:PNDITII-50 | 10.2/23.1 | 9.2/19.5 | 8.4/16.5 | 10.1/18.6 | 8.6/15.6 | 8.2/14.5 |

a) Test with a period of 150 μs. b) Test with a period of 75 μs.

Table S5. Calculated in-plane GIWAXS data of the pristine films and blend films.

| Active layer | Direction | Location (Å-1) | d-spacing (Å) | FWHM (Å-1) | CCL (Å) |
| --- | --- | --- | --- | --- | --- |
| PNDI | (100) | 0.278 | 22.59 | 0.074 | 76.9 |
| PNDITII-10 | (100) | 0.278 | 22.59 | 0.073 | 77.4 |
| PNDITII-30 | (100) | 0.277 | 22.67 | 0.072 | 78.0 |
| PNDITII-50 | (100) | 0.275 | 22.84 | 0.071 | 80.2 |
| PDPP:PNDI | (100) | 0.261 | 24.06 | 0.054 | 105.6 |
| PDPP:PNDITII-10 | (100) | 0.263 | 23.88 | 0.056 | 100.9 |
| PDPP:PNDITII-30 | (100) | 0.262 | 23.97 | 0.057 | 100.0 |
| PDPP:PNDITII-50 | (100) | 0.263 | 23.88 | 0.058 | 98.3 |

d-spacing = 2π/q; CCL = 1.8π/FWHM

Table S6. Calculated out-of-plane GIWAXS data of the pristine films and blend films.

| Active layer | Direction | Location (Å-1) | d-spacing (Å) | FWHM (Å-1) | CCL (Å) |
| --- | --- | --- | --- | --- | --- |
| PNDI | (010) | 1.479 | 4.25 | 0.41 | 13.6 |
| PNDITII-10 | (010) | 1.500 | 4.19 | 0.39 | 14.5 |
| PNDITII-30 | (010) | 1.544 | 4.07 | 0.38 | 14.9 |
| PNDITII-50 | (010) | 1.604 | 3.91 | 0.38 | 14.9 |
| PDPP:PNDI | (010) | 1.453 | 4.32 | 0.39 | 14.5 |
| PDPP:PNDITII-10 | (010) | 1.445 | 4.35 | 0.37 | 15.5 |
| PDPP:PNDITII-30 | (010) | 1.444 | 4.35 | 0.38 | 15.1 |
| PDPP:PNDITII-50 | (010) | 1.448 | 4.34 | 0.41 | 13.8 |

d-spacing = 2π/q; CCL = 1.8π/FWHM

Table S7. Contact angles and surface energies of PDPP, PNDI, PNDITII-10, PNDITII-30, and PNDITII-50

| Polymer | θwater (°) | θEG (°) | Surface energy (Mj·m-1) |
| --- | --- | --- | --- |
| PDPP | 101.2 | 80.2 | 19.9 |
| PNDI | 103.6 | 78.2 | 21.5 |
| PNDITII-10 | 103.5 | 77.7 | 21.9 |
| PNDITII-30 | 103.8 | 77.4 | 22.3 |
| PNDITII-50 | 104.5 | 76.5 | 23.8 |

The surface energy (γ) of the polymer film can be calculated using the Wu methodology as:

γwater(1 + cosθwater) = 4γdwaterγd /(γdwater + γd) + 4γpwaterγp /(γpwater + γp)                   (1)

γEG(1 + cosθEG) = 4γdEGγd /(γdEG + γd) + 4γpEGγp /(γpEG + γp)                                 (2)

γ = γd + γp                                                                                                              (3)

where θ is the contact angle of water or EG on the pure polymer film, superscript d and p refer to the dispersion component and the polar component of the surface energy [34].

Reference

[1] M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. V. Marenich, J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian, J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, Williams, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery Jr., J. E. Peralta, F. Ogliaro, M. J. Bearpark, J. J. Heyd, E. N. Brothers, K. N. Kudin, V. N. Staroverov, T. A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. P. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, D. J. Fox, Gaussian 16, Revision A.03, Gaussian, Inc., Wallingford, CT 2016.

[2] W. Humphrey, A. Dalke, K. Schulten, VMD: Visual Molecular Dynamics, J. Mol. Graphics   14 (1996) 33.

[3] T. Lu, F. Chen, Multiwfn: A multifunctional wavefunction analyzer, J. Comput. Chem. 33 (2012) 580.

[4] B. Park, J. Jung, D. Lim, H. Lee, S. Park, M. Kyeong, S. Ko, S. H. Eom, S. Lee, C. Lee, S. C. Yoon, Significant dark current suppression in organic photodetectors using side chain fluorination of conjugated polymer, Adv. Funct. Mater. 32 (2022) 2108026.

[5] H. Quan, Z. Zhong, T. Hao, K. An, W. Zhong, C. Wang, F. Liu, L. Ying, F. Huang, High-performance organic photodetectors enabled by a refined fibrillar multiphase morphology, Chem. Eng. J. 452 (2023) 139295.

[6] U. Lee, B. Park, S. Rhee, J. Ha, D.R. Whang, H.J. Eun, J.H. Kim, Y. Shim, J. Heo, C. Lee, B.J. Kim, S.C. Yoon, J. Lee, S. Ko, Achieving highly sensitive near-infrared organic photodetectors using asymmetric non-fullerene acceptor, Adv. Opt. Mater. 11 (2023) 2300312.

[7] B. Jiang, F. Hsiao, Y. Lin, C. Lin, Y. Shen, Y. Hsu, P. Lee, Y. Su, H. Lu, C. Lin, C.K. Chan, C. Chen, Highly efficient ternary near-infrared organic photodetectors for biometric monitoring, ACS Appl. Mater. Interfaces 15 (2023) 10907-10917.

[8] J. Ha, H.J. Eun, B. Park, H. Ahn, D.R. Hwang, Y.S. Shim, J. Heo, C. Lee, S.C. Yoon, J.H. Kim, S. Ko, Effect of cyano substitution on non-fullerene acceptor for near-infrared organic photodetectors above 1000 nm, Adv. Funct. Mater. 33 (2023) 2211486.

[9] Y. Gao, J. Liao, H. Chen, H. Ning, Q. Wu, Z. Li, Z. Wang, X. Zhang, M. Shao, Y. Yu, High performance polarization-resolved photodetectors based on intrinsically stretchable organic semiconductors, Adv Sci 10 (2023) 2204727.

[10] X. Chen, B. Yu, J. Wang, Z. Luo, H. Meng, B. Xie, R. Zhou, S. Liu, Q. Zhao, A near-infrared organic photodetector based on an aza-BODIPY dye for a laser microphone system, J. Mater. Chem. C 11 (2023) 2267-2272.

[11] Z. Lan, Y.S. Lau, L. Cai, J. Han, C. W. Suen, F. Zhu, Dual-band organic photodetectors for dual-channel optical communications, Laser & Photonics Reviews 16 (2022) 2100602.

[12] K. Kuo, R. Estrada, C. Lee, N.R. Al Amin, Y. Li, M.Y. Hadiyanto, S. Liu, K. Wong, A new dioxasilepine-aryldiamine hybrid electron-blocking material for wide linear dynamic range and fast response organic photodetector, ACS Appl. Mater. Interfaces 14 (2022) 18782-18793.

[13] P. Kafourou, Z. Qiao, M. Toth, F. Anies, F. Eisner, N. Gasparini, M. Heeney, Low dark current organic photodetectors utilizing highly cyanated non-fullerene acceptors, ACS Appl. Mater. Interfaces 14 (2022) 39141-39148.

[14] P. Jacoutot, A.D. Scaccabarozzi, T. Zhang, Z. Qiao, F. Anies, M. Neophytou, H. Bristow, R. Kumar, M. Moser, A.D. Nega, A. Schiza, A. Dimitrakopoulou-Strauss, V.G. Gregoriou, T. D. Anthopoulos, M. Heeney, I. McCulloch, A.A. Bakulin, C.L. Chochos, N. Gasparini, Infrared organic photodetectors employing ultralow bandgap polymer and non-fullerene acceptors for biometric monitoring, Small 18 (2022) 2200580.

[15] S. Gielen, V.C. Gomez, S. Brebels, T.J. Quill, J. Vanderspikken, L. Lutsen, P. de la Cruz, K. Vandewal, F. Langa, W. Maes, meso-Ethynyl-extended push-pull type porphyrins for near-infrared organic photodetectors, J. Mater. Chem. C 10 (2022) 10853-10859.

[16] B. Wang, A.D. Scaccabarozzi, H. Wang, M. Koizumi, M.I. Nugraha, Y. Lin, Y. Firdaus, Y. Wang, S. Lee, T. Yokota, T.D. Anthopoulos, T. Someya, Molecular doping of near-infrared organic photodetectors for photoplethysmogram sensors, J. Mater. Chem. C 9 (2021) 3129-3135.

[17] J.H. Kim, A. Liess, M. Stolte, A. Krause, V. Stepanenko, C. Zhong, D. Bialas, F. Spano, F. Wurthner, An efficient narrowband near-infrared at 1040 nm organic photodetector realized by intermolecular charge transfer mediated coupling based on a squaraine dye, Adv. Mater. 33 (2021) 2100582.

[18] J. Huang, J. Lee, H. Nakayama, M. Schrock, D.X. Cao, K. Cho, G. C. Bazan, T. Nguyen, Understanding and countering illumination-sensitive dark current: toward organic photodetectors with reliable high detectivity, ACS Nano 15 (2021) 1753-1763.

[19] H.J. Eun, H. Kye, D. Kim, I.S. Jin, J.W. Jung, S. Ko, J. Heo, B. Kim, J.H. Kim, Effective dark current suppression for high-detectivity organic near-infrared photodetectors using a non-fullerene acceptor, ACS Appl. Mater. Interfaces 13 (2021) 11144-11150.

[20] G. Bhat, Q. Liu, M. Kielar, Y. Hamada, T. Michinobu, P. Sah, A.K.K. Kyaw, A. K. Pandey, P. Sonar, Energy-Level Manipulation in Novel Indacenodithiophene-Based Donor–Acceptor Polymers for Near-Infrared Organic Photodetectors., ACS Appl. Mater. Interfaces 13 (2021) 29866-29871.

[21] M. Babics, H. Bristow, W. Zhang, A. Wadsworth, M. Neophytou, N. Gasparini, I. McCulloch, Non-fullerene-based organic photodetectors for infrared communication, J. Mater. Chem. C 9 (2021) 2375-2385.

[22] X. Luo, Y. Xue, J. Wu, W. Cai, D. Tauber, I. Malovicho, B. Sava, G. Cen, X. Lu, C. Zhao, I.G. Scheblykin, J. Yu, W. Mai, F. Liu, E. Wang, L. Hou, Intrinsic polarization-sensitive organic photodetector with self-assembled all-polymer heterojunction, Appl. Phys. Lett. 121 (2022) 233301.

[23] H. Lin, B. Xu, J. Wang, X. Yu, X. Du, C. Zheng, S. Tao, Novel dark current reduction strategy via deep bulk traps for high-performance solution-processed organic photodetectors, ACS Appl. Mater. Interfaces 14 (2022) 34891-34900.

[24] X. Huang, Z. Zhao, S. Chung, K. Cho, J. Lv, S. Lu, Z. Kan, Balancing the performance and stability of organic photodiodes with all-polymer active layers, J. Mater. Chem. C 10 (2022) 17502-17511.

[25] Y. Zhao, T. Liu, B. Wu, S. Zhang, N. Prine, L. Zhang, S. Pang, B. Yin, L. Ye, X. Gu, G. Yu, C. Duan, F. Huang, Y. Cao, High-performance all-polymer solar cells and photodetectors enabled by a high-mobility n-type polymer and optimized bulk-heterojunction morphology, Chem. Mater. 33 (2021) 3746-3756.

[26] Y. Xia, L.E. Aguirre, X. Xu, O. Inganas, All-polymer high-performance photodetector through lamination, Adv. Electron. Mater. 6 (2020) 1901017.

[27] J. Kang, J. Kim, H. Ham, H. Ahn, S.Y. Lim, H.M. Kim, I. Kang, I.H. Jung, High-detectivity green-selective all-polymer p-n junction photodetectors, Adv. Opt. Mater. 8 (2020) 2001038.

[28] Z. Zhong, L. Bu, P. Zhu, T. Xiao, B. Fan, L. Ying, G. Lu, G. Yu, F. Huang, Y. Cao, Dark current reduction strategy via a layer-by-layer solution process for a high-performance all-plymer photodetector, ACS Appl. Mater. Interfaces 11 (2019) 8350-8356.

[29] P. Sen, R. Yang, J. J. Rech, Y. Feng, C. H. Y. Ho, J. Huang, F. So, R. J. Kline, W. You, M. W. Kudenov, B. T. O'Connor, Panchromatic all-polymer photodetector with tunable polarization sensitivity, Adv. Opt. Mater. 7 (2019) 1801346.

[30] X. Xu, X. Zhou, K. Zhou, Y. Xia, W. Ma, O. Inganas, Large-area, semitransparent, and flexible all-polymer photodetectors, Adv. Funct. Mater. 28 (2018) 1805570.

[31] L. Hu, W. Qiao, J. Han, X. Zhou, C. Wang, D. Ma, Z.Y. Wang, Y. Li, Naphthalene diimide-diketopyrrolopyrrole copolymers as non-fullerene acceptors for use in bulk-heterojunction all-polymer UV-NIR photodetectors, Polym. Chem. 8 (2017) 528-536.

[32] L. Hu, W. Qiao, X. Zhou, X. Zhang, D. Ma, Y. Li, Z.Y. Wang, Effect of compositions of acceptor polymers on dark current and photocurrent of all-polymer bulk-heterojunction photodetectors, Polymer 114 (2017) 173-179.

[33] X. Wang, L. Lv, L. Li, Y. Chen, K. Zhang, H. Chen, H. Dong, J. Huang, G Shen, Z. Yang, H. Huang, High-performance all-polymer photoresponse devices based on acceptor-acceptor conjugated polymer, Adv. Funct. Mater. 26 (2016) 6306-6315.

[34] M.S. Kim, D. Luo, W. Jang, B.G. Kim, C.W. Shan, A.K.K. Kyaw, D.H. Wang, High-sensitivity organic photodetector based on surface-concentrated nonfused ring electron acceptor, Adv. Opt. Mater. 11 (2022) 2202525.