Supplementary material

Mechanistic studies on the epoxidation of alkenes with molecular oxygen and aldehydes catalyzed by transition metal--diketonate complexes.

B.B. Wentzel,†  P.A. Gosling,† M.C. Feiters, R.J.M. Nolte*

Department of Organic Chemistry/Nijmegen SON Research Center

University of Nijmegen,

6525 ED Nijmegen, The Netherlands

Abstract

The scope, mechanism and kinetics were studied of the aerobic epoxidation of alkenes with an aldehyde and substituted -diketonate-transition metal complexes as catalysts. Diketonate complexes of nickel(II) proved to be among the best catalysts for this reaction. The epoxidation is not dependent on substrate concentration and is first order in aldehyde, catalyst and oxygen partial pressure. It was shown by reactivity studies and EPR experiments that the reaction is radical in nature. Additional evidence for this radical nature was obtained from stereochemical investigations. The metal catalyst is not only an efficient initiator of the reaction, but is also believed to enhance the reactivity of intermediate species in the oxidation process by allowing these to coordinate to the metal center. A mechanism is proposed for the catalytic reaction.

Supplementary material

Table I:  Epoxidation of -pinene and S-limonene with a variety of metal catalysts.a

Catalyst	Conversion (%)	Yield epoxide (%)	Selectivity (%)

Substrate: -pinene

Ni(II)OAc2	80	63	79

Co(II)OAc2	100	87	87

Mn(II)OAc2	48	37	77

Fe(III)OAc3	31	0	0

Ni(II)acac2	100	91	91

Mn(II)acac2	99	61	62

Fe(III)acac3	25	22	88

Pd(II)acac2	<1	<1	-

Substrate: S-limonene

Ni(II)acac2	70	65	93

Co(II)acac2	92	74	80

Mn(II)acac2	4	2	-b

Fe(III)acac3	69	60	87

Pd(II)acac2	<1	<1	-

Ni(II)OAc2	48	44	92

Co(II)OAc2	87	77	89c

Ni(II)dmp2d	74	63	86

Co(II)dmp2d	71	63	89

a Reaction conditions: 0.1 mol l-1 alkene, 0.3 mol l-1 isobutyraldehyde, 1.0·10-3 mol l-1 catalyst, 5.0 ml CH2Cl2, 1.0 atm. O2, 25°C, 4 hrs. b After 24 hrs. c After 1 h. d Hdmp = 1,5-di(p-methoxyphenyl)acetylacetone 1b.

Supplementary material

Table II: Reactivity of various aldehydes as co-reactant in the epoxidation of  -pinene.a

Aldehyde 	Yield -pinene (%)

Isobutyraldehyde 	91

Butyraldehyde 	5

Acetaldehydeb  	2

Propionaldehyde 	2

Benzaldehyde 	0

Cinnamaldehyde 	0

Pivaldehyde 	68

Crotonaldehyde 	0

a Reaction conditions: 0.1 mol l-1 alkene, 0.3 mol l-1  isobutyraldehyde, 1.0·10-3 mol l-1, catalyst Ni(II)-1c, 5.0 ml CH2Cl2, 1.0 atm. O2, 25°C, 4 hrs. b Due to its low boiling point, the reaction with this aldehyde was carried out at 15°C.

† These authors contributed equally to this paper

* Corresponding author