SUPPLEMENTARY MATERIAL

Complex Chemistry of 4-{2,2’:6’,2’’-Terpyrid-4’-yloxy}-2,2,6,6-tetramethyl-1-piperidinoxyl, a Spin-Labelled Terpyridine.

Malcolm A. Halcrow*,†,a, Euan K. Brechinb, Eric J.L. McInnesc,

Frank E. Mabbsc and John E. Daviesa.

aDepartment of Chemistry, University of Cambridge,

Lensfield Road, Cambridge CB2 1EW, U.K.

bDepartment of Chemistry, The University of Edinburgh,

West Mains Road, Edinburgh EH9 3JJ, U.K.

cEPSRC CW EPR Service Centre, Department of Chemistry,

University of Manchester, Oxford Road,

Manchester M13 9PL, U.K.

†Present address: School of Chemistry, University of Leeds, Leeds LS2 9JT, U.K.

Table C1. Magnetic data for [Mn(L1)2](BF4)2 (1).

T (K)  	M      	MT	T (K)  	M      	MT

1.79	1.272	2.276             	25.02	0.208	5.193

2.00	1.213	2.426           	30.02	0.174	5.210

2.20	1.180	2.596           	35.02	0.149	5.223

2.40	1.134	2.721           	40.01	0.131	5.226

2.60	1.101	2.862           	45.01	0.116	5.220

2.80	1.072	3.002             	50.00	0.104	5.223

3.00	1.049	3.147           	59.94	0.0873	5.231

3.50	1.027	3.594             	69.90	0.0747	5.219

4.00	1.014	4.057          	79.89	0.0654	5.221

4.49	1.022	4.589             	90.08	0.0581	5.235

5.00	0.973	4.863           	100.10	0.0523	5.231

5.50	0.909	4.998          	125.14	0.0417	5.217

6.01	0.832	5.023             	150.17 	0.0348	5.221

7.00 	0.725	5.076          	175.20	0.0298	5.229

8.01	0.636	5.093          	200.22	0.0261	5.231

9.01	0.567	5.105         	225.21	0.0232	5.233

10.01	0.510	5.109            	250.21	0.0209	5.237

12.00	0.428	5.131            	275.20	0.0191	5.244

14.00	0.367	5.145         	300.18	0.0175	5.261

16.01	0.322	5.158         	325.14	0.0162	5.266

18.01	0.287	5.169         	340.14 	0.0155	5.266

20.01	0.258	5.172

Field strength: 1000 G

Diamagnetic correction from Pascal’s constants: –568.30x10–6 emu.mol–1

Derivation of Van Vleck equation describing intermolecular superexchange in 1.

H = –2J(S1.S2 + S1.S3) –2J’(S2.S3)

Let SA = S2 + S3

SA2 = S22 + S32 + 2S2.S3

Let ST = S1 + SA

ST2 = S12 + SA2 + 2S1.SA

= S12 + S22 + S32 + 2S1.S2 + 2S1.S3 + 2S2.S3

H = –2J(ST2 – SA2 – S12) –2J’(SA2 – S22 – S32)

E(SA, ST) = –J[ST(ST + 1) – SA(SA + 1) – S1(S1 + 1)]

–J’[SA(SA + 1) – S2(S2 + 1) – S3(S3 + 1)]

Van Vleck equation:

Calculate relative energies, pre-exponential terms and g-values for all E(SA, ST) states:

S1 = 5/2, S2 = S3 = 1/2

SA = 0, 1and ST = SA + S1...SA – S1

SA	ST	E       		ST(ST + 1)(2ST + 1)	2ST + 1	c	ca	cb

0	5/2	–35/4J		52.5		  	      6		–1	0	1

1	3/2	–7/4J –2J’		15		  	      4		–9/5	–2/5	7/5

1	5/2	–27/4J –2J’		52.5		 	      6		–27/35	4/35	31/35

1	7/2	–55/4J –2J’		126			      8		–3/7	2/7	5/7

Substitute these values into the Van Vleck equation.

Check: set J = J’ = 0

Compare with the Curie law for 1 S = 5/2 and 2 S = 1/2 non-interacting spins:

Table C2. Magnetic data for [Cu(L1)2](BF4)2 (4).

T (K)  	M      	MT	T (K)  	M      	MT

1.79	0.521	0.932	25.01	0.0448	1.121

2.00	0.478	0.956	30.03	0.0374	1.124

2.20	0.443	0.975	35.02	0.0322	1.127

2.40	0.412	0.988	40.01	0.0283	1.131

2.60	0.385	1.001	45.01	0.0251	1.131

2.80	0.361	1.010	50.00	0.0226	1.132

3.00	0.340	1.019	59.95	0.0189	1.135

3.50	0.297	1.040	69.90	0.0163	1.138

4.00	0.262	1.050	79.84	0.0143	1.140

4.49	0.236	1.061	90.08	0.0127	1.147

5.00	0.214	1.071	100.11	0.0115	1.150

5.50	0.196	1.077	125.13	0.00922	1.155

5.99	0.180	1.081	150.15	0.00775	1.164

7.00	0.156	1.090	175.18	0.00669	1.172

8.01	0.137	1.095	200.19	0.00589	1.180

9.01	0.122	1.099	225.20	0.00528	1.189

10.01	0.110	1.102	250.19	0.00478	1.196

12.01	0.0922	1.107	275.21	0.00437	1.204

14.01	0.0793	1.111	300.19	0.00402	1.208

16.01	0.0695	1.114	325.20	0.00376	1.222

18.01	0.0620	1.116	340.14	0.00361	1.227

20.01	0.0559	1.118

Field strength: 1000 G

Diamagnetic correction from Pascal’s constants: –568.30x10–6 emu.mol–1

Derivation of Van Vleck equation describing intermolecular superexchange in 4.

As for 1:

E(SA, ST) = –J[ST(ST + 1) – SA(SA + 1) – S1(S1 + 1)]

–J’[SA(SA + 1) – S2(S2 + 1) – S3(S3 + 1)]

Also, when S1 = S2 = S3 = 1/2, g can be written as:

g(SA, ST) = ca.g{L1} + cb.g{Cu}

where:

ca = (1+c)/2

cb = (1–c)/2

and:

Van Vleck equation:

Calculate relative energies, pre-exponential terms and g-values for all E(SA, ST) states:

S1 = S2 = S3 = 1/2

SA = 0, 1and ST = SA + S1...SA – S1

SA	ST	E       		ST(ST + 1)(2ST + 1)	2ST + 1	c	ca	cb

0	1/2	–3/4J			3/2		  	      2		–1	0	1

1	1/2	5/4J –2J’		3/2		  	      2		5/3	4/3	–1/3

1	3/2	–7/4J –2J’		15		 	      4		1/3	2/3	1/3

Substitute these values into the Van Vleck equation.

Check: set J = 0

Compare with the Curie law for 3 S = 1/2 non-interacting spins:

and:

g for the entire spin manifold should be the average value [2g{L1} + g{Cu}]/3.