Table *  Crystal and refinement data for three [Cu(bipy)2X]Y complexes - preliminary data.

All three structures showed no disorder on the cation, but 15 and 30 involved  	unresolved disorder on the anions present.

Y			15			27			30

Chemical Formula	C24H16N4ClCuF9O3S		C20H16N4CuI2	 C21H16N4F3CuIO3S

Formula Weight		709.98		629.724		639.97

Crystal System		Triclinic		Triclinic		Triclinic

Space Group			P1			P1			P1

a (Å)				8.701(2)		7.424(2)		7.571(1)

b (Å)				13.225(2)		10.554(2)		12.022(2)

c (Å)				13.256(3)		14.315(3)		14.147(3)

_ (o)				71.92(2)		108.21(1)		109.88(1)

_ (o)				78.16(2)		95.42(2)		97.01(2)

_ (o)				70.60(2)		98.75(2)		101.88(2)

Z				2			2			2

V (Å-3)			1358.82		1040.91		1158.82

R = (__/__Fo_)		0.1197		0.0573		0.1053

Rw = (__w½/__Fo_w½)	0.1221		0.0572		0.1057

Temperature (K)		298			298			298