Supplementary Material

Thermogravimetric Analysis

Selected samples of the lanthanide-L4 complexes were heated in a Stanton Redcroft TGA/DTA STA-1000. The samples were heated from room temperature up to 850oC, at a ramp rate of 15oC/min, under a static air atmosphere. Both the mass percent loss and the energy change versus temperature were recorded. The samples that were examined were: 2-Nd, 2-Sm, 4-Eu, 4-Gd, 4-Dy, 4-Ho, 4-Er and 5-Yb. A noncrystalline sample formed between the addition of cerium and L4 with the same method as for 2-Pr, was also included. Details of mass loss and heat flow are given in Table S1 and the data are described in Figures S1 and S2.

Table S1 - Breakdown of TGA/DTA Data

| Complex | 1st Mass Loss/% | 2nd Mass Loss/% | 3rd Mass Loss | 4th Mass Loss/% | 5th Mass Loss/% |
| --- | --- | --- | --- | --- | --- |
| Ce | 93 | 71 | 47 | 32 | 29 |
| 2-Nd | 95 | 80 | 57 | 35 | 28 |
| 2-Sm | 93 | 75 | 56 | 34 | 31 |
| 4-Eu | 89 | 73 | 53 | 31 | 27 |
| 4-Gd | 89 | 74 | 54 | 31 | 28 |
| 4-Dy | 89 | 73 | 54 | 31 | 29 |
| 4-Ho | 88 | 73 | 53 | 31 | 28 |
| 4- Er | 90 | 77 | 52 | 31 | 30 |
| 5-Yb | 87 | 77 | 61 | 34 | 31 |

Table S2

Heat Flow Data (oC)

| Complex | Endo 1 | Endo 2 | Exo 1 | Exo 2 | Exo 3 |
| --- | --- | --- | --- | --- | --- |
| Ce | 60-85 | 133-180 | 280-340 | 340-480 |  |
| 2-Nd | - | 120-130 | 330-350 | 350 - 360 - 380 - 395 | 395 - 475 |
| 2-Sm | - | 150-200 | 350 - 400 - 410 - 440 - 460 | 460-570 |  |
| 4-Eu | 90-150 | 160-180 | 355 - 400 - 415 - 450 | 450-600 |  |
| 4-Gd | 65-125 | 140-180 | 340 - 385 - 420 - 450 | 450-565 |  |
| 4-Dy | 95-150-195 | - | 355 - 400 - 415 - 441 -461 | 461 -575 |  |
| 4-Ho | 100-151-180 | - | 350-410 | 425 - 470 - 550 |  |
| 4-Er | 95-187 | - | 360-415 | 430 - 470 - 555 |  |
| 5-Yb | 95-155 | - | 200-250 | 340 - 425 - 550 - 620 |  |