Table 1.  Crystal data and structure refinement for [Cu2(CN)2(2,6-dmp)].

Identification code 	[Cu2(CN)2(2,6-dmp)]

Empirical formula 	C8H8Cu2N4

Formula weight 	287.26

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 16.553(4) Å	= 90.

b = 7.773(2) Å	= 116.051(5).

c = 18.025(5) Å	 = 90.

Volume	2083.5(9) Å3

Z	8

Density (calculated)	1.832 Mg/m3

Absorption coefficient	4.045 mm-1

F(000)	1136

Crystal size	0.11 x 0.11 x 0.09 mm3

Theta range for data collection	2.52 to 28.28.

Index ranges	-21<=h<=21, -8<=k<=10, -19<=l<=23

Reflections collected	6527

Independent reflections	2476 [R(int) = 0.0404]

Completeness to theta = 28.28	95.9 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2476 / 0 / 128

Goodness-of-fit on F2	1.063

Final R indices [I>2sigma(I)]	R1 = 0.0455, wR2 = 0.1071

R indices (all data)	R1 = 0.0655, wR2 = 0.1154

Extinction coefficient	0.00014(15)

Largest diff. peak and hole	0.981 and -0.826 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)  for [Cu2(CN)2(2,6-dmp)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	1928(1)	10211(1)	4012(1)	17(1)

Cu(2)	156(1)	6621(1)	5015(1)	16(1)

N(5)	782(2)	7456(5)	6242(2)	18(1)

N(6)	1432(2)	8771(5)	7829(2)	16(1)

N(1)	3170(2)	10793(5)	4443(2)	13(1)

N(2)	1178(3)	8891(6)	4323(3)	26(1)

N(3)	739(2)	8027(5)	4513(2)	15(1)

N(4)	-1067(3)	5979(6)	4662(3)	26(1)

C(1)	3170(2)	10793(5)	4443(2)	13(1)

C(2)	1178(3)	8891(6)	4323(3)	26(1)

C(3)	739(2)	8027(5)	4513(2)	15(1)

C(4)	-1067(3)	5979(6)	4662(3)	26(1)

C(5)	890(3)	6458(6)	6885(3)	17(1)

C(6)	1017(3)	9105(6)	6402(3)	17(1)

C(7)	1338(3)	9787(6)	7193(3)	17(1)

C(8)	1225(3)	7102(6)	7684(3)	18(1)

C(9)	1554(4)	11650(6)	7360(3)	26(1)

C(10)	1381(4)	5986(6)	8420(3)	28(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(2,6-dmp)].

_____________________________________________________

Cu(1)-N(2) 	1.877(5)

Cu(1)-N(1) 	1.905(4)

Cu(1)-N(6)#1 	2.075(4)

Cu(2)-N(4) 	1.903(5)

Cu(2)-N(3) 	1.927(4)

Cu(2)-N(5) 	2.090(4)

Cu(2)-C(4)#2 	2.434(5)

Cu(2)-N(4)#2 	2.434(5)

Cu(2)-Cu(2)#2 	2.5686(13)

N(5)-C(6) 	1.334(6)

N(5)-C(5) 	1.340(6)

N(6)-C(8) 	1.338(6)

N(6)-C(7) 	1.345(6)

N(6)-Cu(1)#3 	2.075(4)

N(1)-C(4)#4 	1.156(6)

N(1)-N(4)#4 	1.156(6)

N(2)-N(3) 	1.147(6)

N(4)-C(1)#5 	1.156(6)

N(4)-N(1)#5 	1.156(6)

N(4)-Cu(2)#2 	2.434(5)

C(5)-C(8) 	1.390(6)

C(6)-C(7) 	1.389(6)

C(7)-C(9) 	1.490(6)

C(8)-C(10) 	1.509(6)

N(2)-Cu(1)-N(1)	138.14(17)

N(2)-Cu(1)-N(6)#1	120.00(16)

N(1)-Cu(1)-N(6)#1	101.44(15)

N(4)-Cu(2)-N(3)	132.09(18)

N(4)-Cu(2)-N(5)	113.33(16)

N(3)-Cu(2)-N(5)	101.72(15)

N(4)-Cu(2)-C(4)#2	108.55(16)

N(3)-Cu(2)-C(4)#2	101.40(16)

N(5)-Cu(2)-C(4)#2	92.14(15)

N(4)-Cu(2)-N(4)#2	108.55(16)

N(3)-Cu(2)-N(4)#2	101.40(16)

N(5)-Cu(2)-N(4)#2	92.14(15)

C(4)#2-Cu(2)-N(4)#2	0.0(3)

N(4)-Cu(2)-Cu(2)#2	63.94(14)

N(3)-Cu(2)-Cu(2)#2	133.14(12)

N(5)-Cu(2)-Cu(2)#2	109.20(11)

C(4)#2-Cu(2)-Cu(2)#2	44.61(12)

N(4)#2-Cu(2)-Cu(2)#2	44.61(12)

C(6)-N(5)-C(5)	116.9(4)

C(6)-N(5)-Cu(2)	119.3(3)

C(5)-N(5)-Cu(2)	123.5(3)

C(8)-N(6)-C(7)	118.6(4)

C(8)-N(6)-Cu(1)#3	121.5(3)

C(7)-N(6)-Cu(1)#3	119.8(3)

C(4)#4-N(1)-N(4)#4	0.0(4)

C(4)#4-N(1)-Cu(1)	172.2(4)

N(4)#4-N(1)-Cu(1)	172.2(4)

N(3)-N(2)-Cu(1)	177.2(4)

N(2)-N(3)-Cu(2)	170.6(4)

C(1)#5-N(4)-N(1)#5	0.0(5)

C(1)#5-N(4)-Cu(2)	172.0(4)

N(1)#5-N(4)-Cu(2)	172.0(4)

C(1)#5-N(4)-Cu(2)#2	116.6(4)

N(1)#5-N(4)-Cu(2)#2	116.6(4)

Cu(2)-N(4)-Cu(2)#2	71.45(16)

N(5)-C(5)-C(8)	122.0(4)

N(5)-C(6)-C(7)	122.2(4)

N(6)-C(7)-C(6)	120.0(4)

N(6)-C(7)-C(9)	118.1(4)

C(6)-C(7)-C(9)	121.9(4)

N(6)-C(8)-C(5)	120.2(4)

N(6)-C(8)-C(10)	117.1(4)

C(5)-C(8)-C(10)	122.7(4)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,-y+2,z-1/2    #2 -x,-y+1,-z+1    #3 x,-y+2,z+1/2

#4 x+1/2,y+1/2,z    #5 x-1/2,y-1/2,z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(2,6-dmp)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	17(1) 	20(1)	14(1) 	3(1)	9(1) 	-3(1)

Cu(2)	17(1) 	20(1)	12(1) 	-1(1)	7(1) 	-6(1)

N(5)	20(2) 	21(2)	11(2) 	-2(2)	7(2) 	-1(2)

N(6)	16(2) 	17(2)	15(2) 	-3(1)	7(2) 	2(1)

N(1)	12(2) 	16(2)	11(2) 	1(2)	4(2) 	-4(1)

N(2)	23(2) 	30(3)	20(2) 	2(2)	6(2) 	2(2)

N(3)	16(2) 	17(2)	13(2) 	0(2)	8(2) 	-5(2)

N(4)	44(3) 	23(2)	14(2) 	-2(2)	13(2) 	-2(2)

C(1)	12(2) 	16(2)	11(2) 	1(2)	4(2) 	-4(1)

C(2)	23(2) 	30(3)	20(2) 	2(2)	6(2) 	2(2)

C(3)	16(2) 	17(2)	13(2) 	0(2)	8(2) 	-5(2)

C(4)	44(3) 	23(2)	14(2) 	-2(2)	13(2) 	-2(2)

C(5)	24(2) 	11(2)	15(2) 	-2(2)	10(2) 	-3(2)

C(6)	22(2) 	14(2)	16(2) 	3(2)	10(2) 	1(2)

C(7)	17(2) 	18(2)	14(2) 	-1(2)	5(2) 	3(2)

C(8)	22(2) 	22(2)	14(2) 	0(2)	11(2) 	2(2)

C(9)	38(3) 	22(3)	17(2) 	-5(2)	11(2) 	-5(2)

C(10)	51(3) 	19(3)	18(2) 	3(2)	20(2) 	-1(2)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(2,6-dmp)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(5)	737	5300	6794	20

H(6)	964	9823	5970	20

H(9A)	1764	11871	7939	39

H(9B)	1024	12321	7052	39

H(9C)	2014	11959	7196	39

H(10A)	1614	6677	8911	42

H(10B)	1806	5099	8472	42

H(10C)	824	5471	8346	42

______________________________________________________________________________