Table 1.  Crystal data and structure refinement for [Cu2(CN)2(4,4'-bpy)].

Identification code 	[Cu2(CN)2(4,4'-bpy)]

Empirical formula 	C12H8Cu2N4

Formula weight 	335.30

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/n

Unit cell dimensions	a = 8.587(2) Å	= 90.

b = 11.444(3) Å	= 101.033(5).

c = 12.591(3) Å	 = 90.

Volume	1214.5(5) Å3

Z	4

Density (calculated)	1.834 Mg/m3

Absorption coefficient	3.485 mm-1

F(000)	664

Crystal size	0.35 x 0.07 x 0.05 mm3

Theta range for data collection	2.43 to 28.28.

Index ranges	-11<=h<=11, -14<=k<=14, -16<=l<=8

Reflections collected	7859

Independent reflections	2896 [R(int) = 0.0221]

Completeness to theta = 28.28	96.0 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2896 / 0 / 164

Goodness-of-fit on F2	1.049

Final R indices [I>2sigma(I)]	R1 = 0.0259, wR2 = 0.0651

R indices (all data)	R1 = 0.0309, wR2 = 0.0672

Extinction coefficient	0.0038(5)

Largest diff. peak and hole	0.688 and -0.529 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(4,4'-bpy)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	305(1)	9025(1)	5422(1)	11(1)

Cu(2)	-3599(1)	6502(1)	6780(1)	12(1)

C(1)	-1125(2)	7930(2)	5927(2)	10(1)

N(1)	-1125(2)	7930(2)	5927(2)	10(1)

C(2)	-2013(2)	7327(2)	6243(2)	17(1)

N(2)	-2013(2)	7327(2)	6243(2)	17(1)

C(3)	-4025(2)	5947(2)	8125(2)	9(1)

N(3)	-4025(2)	5947(2)	8125(2)	9(1)

C(4)	-4340(2)	5783(2)	8959(2)	18(1)

N(4)	-4340(2)	5783(2)	8959(2)	18(1)

C(5)	-5584(3)	6354(2)	4570(2)	16(1)

C(6)	-6901(3)	6238(2)	3752(2)	15(1)

C(7)	-8398(2)	6114(2)	4019(2)	12(1)

C(8)	-8469(3)	6084(2)	5122(2)	13(1)

C(9)	-7085(3)	6171(2)	5887(2)	12(1)

C(10)	-9855(2)	6048(2)	3175(2)	12(1)

C(11)	-9876(3)	5516(2)	2177(2)	18(1)

C(12)	-11270(3)	5499(2)	1414(2)	18(1)

C(13)	-11278(2)	6549(2)	3352(2)	13(1)

C(14)	-12611(2)	6500(2)	2538(2)	12(1)

N(5)	-5649(2)	6316(2)	5628(2)	13(1)

N(6)	-12631(2)	5986(2)	1578(2)	13(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(4,4'-bpy)].

_____________________________________________________

Cu(1)-N(4)#1 	1.936(2)

Cu(1)-C(4)#1 	1.936(2)

Cu(1)-C(1) 	1.9440(19)

Cu(1)-N(6)#2 	2.0669(19)

Cu(1)-C(4)#3 	2.363(2)

Cu(1)-N(4)#3 	2.363(2)

Cu(1)-Cu(1)#4 	2.4841(7)

Cu(2)-C(2) 	1.886(2)

Cu(2)-C(3) 	1.9084(19)

Cu(2)-N(5) 	2.0670(18)

C(1)-C(2) 	1.155(3)

C(3)-C(4) 	1.149(3)

C(4)-Cu(1)#5 	1.936(2)

C(4)-Cu(1)#6 	2.363(2)

C(5)-N(5) 	1.345(3)

C(5)-C(6) 	1.383(3)

C(6)-C(7) 	1.396(3)

C(7)-C(8) 	1.402(3)

C(7)-C(10) 	1.481(3)

C(8)-C(9) 	1.382(3)

C(9)-N(5) 	1.344(3)

C(10)-C(11) 	1.393(3)

C(10)-C(13) 	1.405(3)

C(11)-C(12) 	1.385(3)

C(12)-N(6) 	1.346(3)

C(13)-C(14) 	1.384(3)

C(14)-N(6) 	1.341(3)

N(6)-Cu(1)#7 	2.0669(18)

N(4)#1-Cu(1)-C(4)#1	0.00(17)

N(4)#1-Cu(1)-C(1)	127.47(8)

C(4)#1-Cu(1)-C(1)	127.47(8)

N(4)#1-Cu(1)-N(6)#2	113.62(8)

C(4)#1-Cu(1)-N(6)#2	113.62(8)

C(1)-Cu(1)-N(6)#2	106.03(8)

N(4)#1-Cu(1)-C(4)#3	110.21(7)

C(4)#1-Cu(1)-C(4)#3	110.21(7)

C(1)-Cu(1)-C(4)#3	99.09(8)

N(6)#2-Cu(1)-C(4)#3	94.61(7)

N(4)#1-Cu(1)-N(4)#3	110.21(7)

C(4)#1-Cu(1)-N(4)#3	110.21(7)

C(1)-Cu(1)-N(4)#3	99.09(8)

N(6)#2-Cu(1)-N(4)#3	94.61(7)

C(4)#3-Cu(1)-N(4)#3	0.00(13)

N(4)#1-Cu(1)-Cu(1)#4	63.21(6)

C(4)#1-Cu(1)-Cu(1)#4	63.21(6)

C(1)-Cu(1)-Cu(1)#4	128.64(6)

N(6)#2-Cu(1)-Cu(1)#4	112.87(5)

C(4)#3-Cu(1)-Cu(1)#4	47.01(6)

N(4)#3-Cu(1)-Cu(1)#4	47.01(6)

C(2)-Cu(2)-C(3)	139.40(8)

C(2)-Cu(2)-N(5)	112.11(8)

C(3)-Cu(2)-N(5)	107.83(8)

C(2)-C(1)-Cu(1)	176.61(18)

C(1)-C(2)-Cu(2)	173.24(19)

C(4)-C(3)-Cu(2)	169.76(18)

C(3)-C(4)-Cu(1)#5	163.41(19)

C(3)-C(4)-Cu(1)#6	126.80(17)

Cu(1)#5-C(4)-Cu(1)#6	69.78(7)

N(5)-C(5)-C(6)	123.5(2)

C(5)-C(6)-C(7)	119.3(2)

C(6)-C(7)-C(8)	117.20(19)

C(6)-C(7)-C(10)	121.6(2)

C(8)-C(7)-C(10)	121.22(19)

C(9)-C(8)-C(7)	119.60(19)

N(5)-C(9)-C(8)	123.1(2)

C(11)-C(10)-C(13)	117.36(19)

C(11)-C(10)-C(7)	122.17(19)

C(13)-C(10)-C(7)	120.5(2)

C(12)-C(11)-C(10)	119.5(2)

N(6)-C(12)-C(11)	123.3(2)

C(14)-C(13)-C(10)	119.2(2)

N(6)-C(14)-C(13)	123.5(2)

C(9)-N(5)-C(5)	117.25(18)

C(9)-N(5)-Cu(2)	122.71(15)

C(5)-N(5)-Cu(2)	120.03(14)

C(14)-N(6)-C(12)	117.24(18)

C(14)-N(6)-Cu(1)#7	119.90(14)

C(12)-N(6)-Cu(1)#7	122.85(15)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x+1/2,-y+3/2,z-1/2    #2 x+3/2,-y+3/2,z+1/2

#3 -x-1/2,y+1/2,-z+3/2    #4 -x,-y+2,-z+1    #5 x-1/2,-y+3/2,z+1/2

#6 -x-1/2,y-1/2,-z+3/2    #7 x-3/2,-y+3/2,z-1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(4,4'-bpy)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	11(1) 	14(1)	8(1) 	1(1)	1(1) 	-2(1)

Cu(2)	10(1) 	16(1)	9(1) 	2(1)	2(1) 	-2(1)

C(1)	12(1) 	12(1)	6(1) 	-1(1)	3(1) 	-2(1)

N(1)	12(1) 	12(1)	6(1) 	-1(1)	3(1) 	-2(1)

C(2)	18(1) 	21(1)	11(1) 	-2(1)	0(1) 	0(1)

N(2)	18(1) 	21(1)	11(1) 	-2(1)	0(1) 	0(1)

C(3)	10(1) 	12(1)	7(1) 	1(1)	1(1) 	-2(1)

N(3)	10(1) 	12(1)	7(1) 	1(1)	1(1) 	-2(1)

C(4)	14(1) 	18(1)	21(1) 	-1(1)	-1(1) 	2(1)

N(4)	14(1) 	18(1)	21(1) 	-1(1)	-1(1) 	2(1)

C(5)	10(1) 	24(1)	13(1) 	5(1)	2(1) 	-1(1)

C(6)	15(1) 	20(1)	9(1) 	3(1)	3(1) 	2(1)

C(7)	12(1) 	10(1)	12(1) 	0(1)	-1(1) 	1(1)

C(8)	13(1) 	13(1)	12(1) 	0(1)	3(1) 	-1(1)

C(9)	14(1) 	13(1)	9(1) 	0(1)	2(1) 	-2(1)

C(10)	11(1) 	13(1)	12(1) 	1(1)	0(1) 	0(1)

C(11)	14(1) 	23(1)	14(1) 	-3(1)	0(1) 	6(1)

C(12)	17(1) 	24(1)	12(1) 	-6(1)	0(1) 	6(1)

C(13)	13(1) 	16(1)	10(1) 	-2(1)	1(1) 	0(1)

C(14)	11(1) 	16(1)	11(1) 	-1(1)	3(1) 	1(1)

N(5)	12(1) 	17(1)	10(1) 	2(1)	0(1) 	-2(1)

N(6)	12(1) 	15(1)	10(1) 	-2(1)	0(1) 	0(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(4,4'-bpy)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(5)	-4601	6465	4379	19

H(6)	-6792	6242	3032	17

H(8)	-9440	6007	5337	15

H(9)	-7150	6126	6614	14

H(11)	-8960	5176	2025	21

H(12)	-11266	5133	755	22

H(13)	-11323	6909	4007	16

H(14)	-13542	6842	2662	15

______________________________________________________________________________