Table 1.  Crystal data and structure refinement for [Cu2(CN)2(etpyr)].

Identification code 	[Cu2(CN)2(etpyr)]

Empirical formula 	C8H8Cu2N4

# Formula weight 	287.26

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 7.846(3) Å	= 76.400(12).

b = 9.048(3) Å	= 88.062(10).

c = 14.539(6) Å	 = 88.520(8).

Volume	1002.5(7) Å3

Z	4

Density (calculated)	1.903 Mg/m3

Absorption coefficient	4.204 mm-1

F(000)	568

Crystal size	.22 x .14 x .05 mm3

Theta range for data collection	1.44 to 28.28.

Index ranges	-10<=h<=10, -11<=k<=11, -11<=l<=19

Reflections collected	6901

Independent reflections	4683 [R(int) = 0.0608]

Completeness to theta = 28.28	94.1 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4683 / 0 / 254

Goodness-of-fit on F2	0.898

Final R indices [I>2sigma(I)]	R1 = 0.0630, wR2 = 0.1205

R indices (all data)	R1 = 0.1455, wR2 = 0.1590

Extinction coefficient	0.0070(9)

Largest diff. peak and hole	1.028 and -1.009 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(etpyr)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	2145(1)	3799(1)	6178(1)	17(1)

Cu(2)	4606(1)	-1105(1)	5706(1)	15(1)

Cu(3)	11891(1)	-4039(1)	8076(1)	17(1)

Cu(4)	14383(1)	-9068(1)	7986(1)	17(1)

N(1)	3146(9)	1937(8)	5939(5)	16(2)

N(2)	3433(9)	-2979(8)	5767(5)	18(2)

N(3)	12884(9)	-2185(8)	8253(5)	17(2)

N(4)	13382(9)	-7191(8)	8209(5)	20(2)

N(5)	-3276(9)	1696(7)	7445(5)	14(2)

N(6)	-185(8)	2982(7)	6728(5)	13(2)

N(7)	6759(8)	-1937(7)	6464(5)	13(2)

N(8)	9636(8)	-3183(7)	7482(5)	12(2)

C(1)	3735(11)	844(9)	5780(6)	15(2)

C(2)	2866(10)	-4189(9)	5900(5)	14(2)

C(3)	13492(10)	-1037(9)	8207(6)	13(2)

C(4)	12764(10)	-6027(9)	8204(6)	15(2)

C(5)	-3188(12)	2917(9)	6725(6)	20(2)

C(6)	-1682(11)	3575(9)	6378(6)	18(2)

C(7)	-266(11)	1726(9)	7431(6)	17(2)

C(8)	-1786(10)	1086(9)	7808(6)	14(2)

C(9)	-1851(11)	-242(9)	8639(6)	17(2)

C(10)	-2343(13)	216(10)	9550(6)	30(2)

C(11)	6670(11)	-3165(9)	7189(6)	16(2)

C(12)	8071(10)	-3813(9)	7693(6)	12(2)

C(13)	7901(11)	-5150(9)	8524(6)	19(2)

C(14)	7628(17)	-4661(12)	9438(7)	54(4)

C(15)	8317(11)	-1317(9)	6285(6)	16(2)

C(16)	9708(10)	-1938(9)	6759(6)	14(2)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(etpyr)].

_____________________________________________________

Cu(1)-C(2)#1 	1.868(8)

Cu(1)-N(1) 	1.940(7)

Cu(1)-N(6) 	2.055(7)

Cu(2)-C(1) 	1.900(8)

Cu(2)-N(2) 	1.932(7)

Cu(2)-N(7) 	2.075(7)

Cu(2)-C(1)#2 	2.451(8)

Cu(2)-Cu(2)#2 	2.578(2)

Cu(3)-C(4) 	1.878(8)

Cu(3)-N(3) 	1.941(7)

Cu(3)-N(8) 	2.048(7)

Cu(4)-C(3)#3 	1.883(8)

Cu(4)-N(4) 	1.944(7)

Cu(4)-N(5)#4 	2.045(7)

N(1)-C(1) 	1.149(10)

N(2)-C(2) 	1.164(10)

N(3)-C(3) 	1.141(10)

N(4)-C(4) 	1.147(10)

N(5)-C(5) 	1.332(10)

N(5)-C(8) 	1.350(11)

N(5)-Cu(4)#5 	2.045(7)

N(6)-C(7) 	1.339(10)

N(6)-C(6) 	1.343(11)

N(7)-C(11) 	1.340(10)

N(7)-C(15) 	1.351(10)

N(8)-C(16) 	1.349(10)

N(8)-C(12) 	1.362(10)

C(1)-Cu(2)#2 	2.451(8)

C(2)-Cu(1)#3 	1.868(8)

C(3)-Cu(4)#1 	1.883(8)

C(5)-C(6) 	1.364(11)

C(7)-C(8) 	1.379(11)

C(8)-C(9) 	1.491(11)

C(9)-C(10) 	1.513(11)

C(11)-C(12) 	1.382(12)

C(12)-C(13) 	1.500(10)

C(13)-C(14) 	1.505(12)

C(15)-C(16) 	1.348(12)

C(2)#1-Cu(1)-N(1)	133.1(3)

C(2)#1-Cu(1)-N(6)	127.7(3)

N(1)-Cu(1)-N(6)	98.9(3)

C(1)-Cu(2)-N(2)	130.3(3)

C(1)-Cu(2)-N(7)	118.1(3)

N(2)-Cu(2)-N(7)	100.4(3)

C(1)-Cu(2)-C(1)#2	108.6(3)

N(2)-Cu(2)-C(1)#2	101.1(3)

N(7)-Cu(2)-C(1)#2	90.1(3)

C(1)-Cu(2)-Cu(2)#2	64.3(2)

N(2)-Cu(2)-Cu(2)#2	131.3(2)

N(7)-Cu(2)-Cu(2)#2	110.38(19)

C(1)#2-Cu(2)-Cu(2)#2	44.3(2)

C(4)-Cu(3)-N(3)	132.5(3)

C(4)-Cu(3)-N(8)	126.8(3)

N(3)-Cu(3)-N(8)	100.1(3)

C(3)#3-Cu(4)-N(4)	130.8(3)

C(3)#3-Cu(4)-N(5)#4	129.4(3)

N(4)-Cu(4)-N(5)#4	99.8(3)

C(1)-N(1)-Cu(1)	178.7(7)

C(2)-N(2)-Cu(2)	171.0(7)

C(3)-N(3)-Cu(3)	169.3(7)

C(4)-N(4)-Cu(4)	170.3(7)

C(5)-N(5)-C(8)	117.0(7)

C(5)-N(5)-Cu(4)#5	119.1(6)

C(8)-N(5)-Cu(4)#5	123.8(5)

C(7)-N(6)-C(6)	116.3(7)

C(7)-N(6)-Cu(1)	119.9(6)

C(6)-N(6)-Cu(1)	123.7(6)

C(11)-N(7)-C(15)	115.1(7)

C(11)-N(7)-Cu(2)	120.6(5)

C(15)-N(7)-Cu(2)	124.3(5)

C(16)-N(8)-C(12)	116.0(7)

C(16)-N(8)-Cu(3)	117.4(5)

C(12)-N(8)-Cu(3)	126.4(5)

N(1)-C(1)-Cu(2)	171.4(7)

N(1)-C(1)-Cu(2)#2	117.1(6)

Cu(2)-C(1)-Cu(2)#2	71.4(3)

N(2)-C(2)-Cu(1)#3	174.4(8)

N(3)-C(3)-Cu(4)#1	173.1(8)

N(4)-C(4)-Cu(3)	173.8(7)

N(5)-C(5)-C(6)	122.7(8)

N(6)-C(6)-C(5)	121.2(8)

N(6)-C(7)-C(8)	122.9(8)

N(5)-C(8)-C(7)	120.0(8)

N(5)-C(8)-C(9)	118.1(7)

C(7)-C(8)-C(9)	121.9(8)

C(8)-C(9)-C(10)	112.4(7)

N(7)-C(11)-C(12)	123.3(8)

N(8)-C(12)-C(11)	120.2(7)

N(8)-C(12)-C(13)	118.2(7)

C(11)-C(12)-C(13)	121.5(7)

C(12)-C(13)-C(14)	111.7(7)

C(16)-C(15)-N(7)	122.6(8)

C(15)-C(16)-N(8)	122.6(8)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,y+1,z    #2 -x+1,-y,-z+1    #3 x,y-1,z    #4 x+2,y-1,z

#5 x-2,y+1,z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(etpyr)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	16(1) 	10(1)	24(1) 	-5(1)	3(1) 	0(1)

Cu(2)	16(1) 	8(1)	21(1) 	-3(1)	-1(1) 	2(1)

Cu(3)	18(1) 	10(1)	21(1) 	-4(1)	-1(1) 	2(1)

Cu(4)	14(1) 	11(1)	26(1) 	-6(1)	2(1) 	0(1)

N(1)	17(4) 	15(4)	16(4) 	-3(3)	5(3) 	-6(3)

N(2)	15(4) 	20(4)	18(4) 	-3(3)	2(3) 	0(3)

N(3)	14(4) 	17(4)	24(4) 	-12(3)	-3(3) 	0(3)

N(4)	19(4) 	14(4)	26(5) 	-1(3)	-2(3) 	3(3)

N(5)	16(4) 	7(3)	21(4) 	-6(3)	3(3) 	0(3)

N(6)	14(4) 	14(4)	12(4) 	-8(3)	2(3) 	3(3)

N(7)	9(4) 	13(3)	18(4) 	-7(3)	4(3) 	4(3)

N(8)	13(4) 	4(3)	18(4) 	0(3)	4(3) 	6(3)

C(1)	18(5) 	17(4)	9(5) 	-4(4)	1(3) 	1(4)

C(2)	15(5) 	19(4)	7(4) 	-6(3)	4(3) 	-1(4)

C(3)	13(4) 	12(4)	17(5) 	-9(3)	-2(3) 	10(3)

C(4)	13(5) 	16(4)	11(5) 	8(3)	0(3) 	5(4)

C(5)	20(5) 	16(4)	25(5) 	-5(4)	-6(4) 	1(4)

C(6)	20(5) 	14(4)	20(5) 	-3(4)	-5(4) 	0(4)

C(7)	16(5) 	11(4)	24(5) 	-7(4)	2(4) 	1(3)

C(8)	16(5) 	15(4)	14(5) 	-10(3)	3(3) 	7(3)

C(9)	18(5) 	15(4)	19(5) 	-2(4)	-1(4) 	1(4)

C(10)	38(6) 	27(5)	21(6) 	0(4)	10(5) 	5(5)

C(11)	14(5) 	11(4)	23(5) 	-4(4)	0(4) 	4(3)

C(12)	15(5) 	11(4)	13(5) 	-6(3)	6(3) 	-2(3)

C(13)	20(5) 	10(4)	23(5) 	3(4)	0(4) 	-1(3)

C(14)	112(12) 	30(6)	21(6) 	-6(5)	7(6) 	-5(7)

C(15)	23(5) 	8(4)	17(5) 	-6(3)	4(4) 	3(4)

C(16)	7(4) 	17(4)	19(5) 	-6(4)	4(3) 	-2(3)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(etpyr)].

x 	y 	z 	U(eq)

________________________________________________________________________

H(5)	-4194	3337	6448	24

H(6)	-1691	4449	5891	22

H(7)	748	1265	7675	20

H(9A)	-742	-749	8705	21

H(9B)	-2671	-960	8528	21

H(10A)	-2365	-672	10064	45

H(10B)	-3452	697	9494	45

H(10C)	-1524	913	9670	45

H(11)	5612	-3602	7360	19

H(13A)	8925	-5783	8560	22

H(13B)	6946	-5755	8432	22

H(14A)	7522	-5543	9953	82

H(14B)	6605	-4048	9409	82

H(14C)	8582	-4079	9537	82

H(15)	8436	-425	5817	19

H(16)	10759	-1491	6580	17

________________________________________________________________________