Table 1.  Crystal data and structure refinement for [Cu2(CN)2(phenz)].

Identification code 	[Cu2(CN)2(phenz)]

Empirical formula 	C14H8Cu2N4

Formula weight 	359.32

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Cmca

Unit cell dimensions	a = 16.869(7) Å	= 90.

b = 8.265(3) Å	= 90.

c = 9.489(3) Å	 = 90.

Volume	1323.0(9) Å3

Z	4

Density (calculated)	1.804 Mg/m3

Absorption coefficient	3.206 mm-1

F(000)	712

Crystal size	0.13 x 0.11 x 0.10 mm3

Theta range for data collection	2.41 to 28.28.

Index ranges	-21<=h<=21, -10<=k<=10, -9<=l<=12

Reflections collected	3919

Independent reflections	837 [R(int) = 0.0328]

Completeness to theta = 28.28	98.2 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	837 / 0 / 48

Goodness-of-fit on F2	1.093

Final R indices [I>2sigma(I)]	R1 = 0.0304, wR2 = 0.0627

R indices (all data)	R1 = 0.0429, wR2 = 0.0676

Extinction coefficient	0.0006(3)

Largest diff. peak and hole	0.405 and -0.332 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(phenz)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	2901(1)	0	5000	15(1)

N(2)	4160(1)	0	5000	12(1)

C(1)	2580(1)	-51(3)	6906(2)	17(1)

N(1)	2580(1)	-51(3)	6906(2)	17(1)

C(2)	4573(1)	1290(3)	5471(2)	12(1)

C(3)	4165(1)	2672(3)	5988(2)	15(1)

C(4)	4576(1)	3965(3)	6476(2)	17(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(phenz)].

_____________________________________________________

Cu(1)-N(1)#1 	1.888(2)

Cu(1)-C(1)#1 	1.888(2)

Cu(1)-C(1) 	1.888(2)

Cu(1)-N(2) 	2.124(3)

N(2)-C(2)#1 	1.350(2)

N(2)-C(2) 	1.350(2)

C(1)-N(1)#2 	1.159(4)

C(1)-C(1)#2 	1.159(4)

C(2)-C(3) 	1.421(3)

C(2)-C(2)#3 	1.440(4)

C(3)-C(4) 	1.356(3)

C(4)-C(4)#3 	1.432(5)

N(1)#1-Cu(1)-C(1)#1	0.00(12)

N(1)#1-Cu(1)-C(1)	146.68(13)

C(1)#1-Cu(1)-C(1)	146.68(13)

N(1)#1-Cu(1)-N(2)	106.66(6)

C(1)#1-Cu(1)-N(2)	106.66(6)

C(1)-Cu(1)-N(2)	106.66(6)

C(2)#1-N(2)-C(2)	117.8(3)

C(2)#1-N(2)-Cu(1)	121.10(13)

C(2)-N(2)-Cu(1)	121.10(13)

N(1)#2-C(1)-C(1)#2	0.0(3)

N(1)#2-C(1)-Cu(1)	176.5(2)

C(1)#2-C(1)-Cu(1)	176.5(2)

N(2)-C(2)-C(3)	119.9(2)

N(2)-C(2)-C(2)#3	121.10(13)

C(3)-C(2)-C(2)#3	119.02(12)

C(4)-C(3)-C(2)	120.2(2)

C(3)-C(4)-C(4)#3	120.76(13)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,-y,-z+1    #2 -x+1/2,y+0,-z+3/2    #3 -x+1,y,z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(phenz)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	11(1) 	21(1)	13(1) 	0(1)	0 	0

N(2)	11(1) 	15(1)	11(1) 	1(1)	0 	0

C(1)	10(1) 	23(1)	16(1) 	1(1)	0(1) 	-1(1)

N(1)	10(1) 	23(1)	16(1) 	1(1)	0(1) 	-1(1)

C(2)	11(1) 	15(1)	9(1) 	1(1)	1(1) 	-1(1)

C(3)	13(1) 	19(1)	14(1) 	-1(1)	1(1) 	3(1)

C(4)	19(1) 	17(1)	14(1) 	-3(1)	1(1) 	4(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(phenz)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(3)	3613	2689	5991	18

H(4)	4303	4862	6815	20

______________________________________________________________________________