Supplementary material

Table S1 :   Intermolecular Distances less than 3.30 angstroms Involving the

Nonhydrogen Atoms

atom   atom   distance    ADC(*)    atom   atom   distance    ADC(*)

N4     O17    2.79(2)      65501     	N81    O25    3.24(3)     65603

N71    O67    3.17(2)     54602     	N78    O72    3.14(4)     45404

N72    O32    3.17(3)     65602     	N84    O17    3.04(3)             1

N75    O88    2.77(7)             4    	N84    O22    3.15(4)     55602

N85    O45    2.83(3)     54602     	N86    O62    2.93(4)     55404

N77    O57    2.82(2)             1     	N87    O42    3.23(5)     64602

N77    O25    3.22(2)             1     	O15    O74    2.78(2)     45504

O25    O77    2.94(3)     65603     	O62    O77    2.98(3)     55601

O15    O83    2.82(2)     45504     	O55    O84    2.92(4)     65603

O22    O74    3.10(2)     65603     	O67    O83    2.71(2)     45504

O57    O78    2.77(4)     65603     	O75    O79    2.76(2)     65603

O71    O84    3.06(5)             4     	O84    O78    2.74(5)             1

O71    O75    3.06(4)     45504     	O85    O77    2.76(5)             1

(*)footnote

The ADC (atom designator code) specifies the position of an atom in a crystal.  The 5-digit number shown in the table is a composite ofthree one digit numbers and one two digit number: TA(1st digit) +  TB(2nd digit) + TC(3rd digit) + SN(4th and 5th digit).  TA, TB, & TC are the crystal lattice translation digits along cell edges a, b, and  c.  A translation digit of 5 indicates the origin unit cell.  If TA=4, this indicates a translation of one unit cell length along the a axis in the negative direction.  Each translation digit can range in value from 1 to 9 and thus (+/-)4 lattice translations from the origin (TA=5,TB=5,TC=5) can be represented.

The SN or symmetry operator number refers to the number of the symmetry operator used to generate the coordinates of the target atom. A list of the symmetry operators relevant to this structure are given below.

Symmetry Operators:

(  1)     +X  ,   +Y  ,   +Z         (  2)  1/2-X  ,1/2+Y  ,1/2-Z

(  3)     -X  ,   -Y  ,   -Z            (  4)  1/2+X  ,1/2-Y  ,1/2+Z