##### Supplementary information

Syntheses, structures, magnetic, and spectroscopic properties of cobalt(II), nickel(II) and zinc(II) complexes containing 2-(6-methyl)-pyridyl-substituted nitronyl and imino nitroxides

# Youhei Yamamoto, Takayoshi Suzuki and Sumio Kaizaki*

# Contents

Figure S1	(a) Packing diagram of [CoCl2(NITmepy)] 1 viwed along crystallographic a axis; and (b) closest intermolecular contacts of [CoCl2(NITmepy)] 1 in the crystal (symmetry operation for the primed atoms: x+1, y, z; only Co, imino nitroxide and pyridine moieties are shown for clarity).

Figure S2	Packing diagram of [CoCl2(IMmepy)] 2.

Figure S3	Solvent-dependence of (a) UV-vis absorption and (b) MCD spectra of 1 in a mixture of dichloromethane and acetonitrile at room temperature [(a) CH2Cl2:CH3CN = 10:0, 9:1, 8:2, 6:4, 4:6, 2:8 and 0:10; (b) CH2Cl2:CH3CN = 10:0, 8:2, 5:5 and 0:10].

Figure S4	UV-vis-NIR absorption spectra of [CoCl2(NITmepy)] 1 in dichloromethane (———), CoCl2•6H2O in acetonitrile (- - - - -) and NITmepy in dichloromethame (– • – • –) at room temperature.

Figure S5	UV-vis-NIR absorption spectra of [CoCl2(IMmepy)] 2 in dichloromethane (———), CoCl2•6H2O in acetonitrile (- - - - -) and IMmepy in dichloromethame (– • – • –) at room temperature.

Figure S6	Temperature-dependence of the anisotropic magnetic properties for complex 1Br in the form of (// or ) vs. T and (// or )•T vs. T.  The //  denotes the molar magnetic susceptibility when the crystallographic a axis parallels to the magnetic field, and the  does that when the a axis is directed to the perpendicular magnetic field.

Figure S1	(a) Packing diagram of [CoCl2(NITmepy)] 1 viwed along crystallographic a axis; and (b) closest intermolecular contacts of [CoCl2(NITmepy)] 1 in the crystal (symmetry operation for the primed atoms: x+1, y, z; only Co, imino nitroxide and pyridine moieties are shown for clarity).

Figure S2	Packing diagram of [CoCl2(IMmepy)] 2.

Figure S3	Solvent-dependence of (a) UV-vis absorption and (b) MCD spectra of 1 in a mixture of dichloromethane and acetonitrile at room temperature [(a) CH2Cl2:CH3CN = 10:0, 9:1, 8:2, 6:4, 4:6, 2:8 and 0:10; (b) CH2Cl2:CH3CN = 10:0, 8:2, 5:5 and 0:10].

Figure S4	UV-vis-NIR absorption spectra of [CoCl2(NITmepy)] 1 in dichloromethane (———), CoCl2•6H2O in acetonitrile (- - - - -) and NITmepy in dichloromethame (– • – • –) at room temperature.

Figure S5	UV-vis-NIR absorption spectra of [CoCl2(IMmepy)] 2 in dichloromethane (———), CoCl2•6H2O in acetonitrile (- - - - -) and IMmepy in dichloromethame (– • – • –) at room temperature.

Figure S6	Temperature-dependence of the anisotropic magnetic properties for complex 1Br in the form of (// or ) vs. T and (// or )•T vs. T.  The //  denotes the molar magnetic susceptibility when the crystallographic a axis parallels to the magnetic field, and the  does that when the a axis is directed to the perpendicular magnetic field.