Supplementary Material

Table 1 Some FT-IR bands (cm1) of  the ligand and sandwich-type complexes 1-7

| Sample | asym(OH) | (OH) | asym(W=Ot) | asym(WOeW) | asym(WOcW) | asym(WOa) |
| --- | --- | --- | --- | --- | --- | --- |
| Ligand | 3385s (br) 3249m (sh) 3099w (sh) | 1624w | 943s | 886s | 789vs | 705vs 669vs (sh) |
| 1 | 3592m (sh) 3432s (br) 3183m (sh) | 1628w (br) | 947s | 872s | 796vs (br) 745vs (br) | 641s (br) |
| 2 | 3602 a 3433s (br) 3203m (sh) | 1627w (br) | 939s | 866s | 777vs (br) | 685m (sh) |
| 3 | 3434s (br) 3165m (sh) | 1628w (br) | 932s |  | 810vs 773 a | 671m (br) |
| 4 | 3430s (br) 3195m (sh) | 1627w (br) | 940s | 866s (br) | 820m (sh) 766vs (br) | 691m (sh) |
| 5 | 3594 a 3421s (br) 3181m (sh) | 1636w (br) | 939s | 869s (sh) | 816vs 771m (br) | 721w (sh) 642m (br) |
| 6 | 3394s (br) 3155m (sh) | 1623w (br) | 946s | 864s (sh) | 822vs (br) 797vs (br) 761vs (br) | 667m (sh) 643m (br) |
| 7 | 3427s (br) 3235m (sh) 3050w (sh) | 1617w | 944s | 884s | 759vs (sh) | 725vs |

a masked band,  obtained from the first derivative of the FT-IR spectrum

Fig. I Powder EPR spectra of the complex 2 recorded in the X-band at two different temperatures.

Fig. II Powder EPR spectra of the complex 3 recorded in the X-band and two different temperatures.

Fig. III Temperature dependence of the inverse of the linewidth (B(p-p))1 of the HF-EPR signal of the complex 3. The solid line represents the best fit of the data.

Fig. IV Powder EPR spectra of the complex 5 recorded in the X-band at two different temperatures.

Fig. V (a) Powder EPR spectra of the complex 7 recorded in the X-band at T = 293 K and (b) its simulated spectrum with S = 3/2.