Supplementary Material (ESI) for Dalton Transactions

This journal is © The Royal Society of Chemistry 2002


Submitted to J. Chem. Soc. Dalton Trans.

Synthesis, Characterization and Properties of Mo6S8(4-tert-butylpyridine)6 and Related M6S8L6 Cluster Complexes (M = Mo, W)

Song Jin, Friedrich Popp, Shannon W. Boettcher,† Min Yuan, Catherine M. Oertel and Francis J. DiSalvo*
Baker Laboratory, Department of Chemistry and Chemical Biology

Cornell University, Ithaca NY 14853, USA

Electronic Supplementary Information

* Author to whom correspondence to be addressed.

† CCMR REU student from Dept. of Chemistry, University of Oregon, Eugene OR.

Email: fjd3@cornell.edu

Telephone number: 607 ( 255 ( 7238

Fax:                         607 ( 255 ( 4137

[image: image1.wmf]40

50

60

70

80

90

100

0

100

200

300

400

500

Temperature (

o

C)

Weight %

Figure S1.  The observed X-ray powder diffraction patterns for compound W6S8(morpholine)6.

[image: image2.jpg]CPS -

6250_]
5750_
5250_]
4750_]
4250_]
3750_
3250_
2750_
2250_]
1750_]

1250_|

750;~mj
250_

J

I S N ST A D= P

T

l
6.0

T

12.0

T

T

I T l—[ T T ] T T I T T I
18.0 24.0 30.0 36.0 42

I I |
.0 48.0

T

54.0

| T
60.0

T

l
66.0

T
72.0

T

5
78.0
Deg.




Figure S2.  The observed X-ray powder diffraction pattern for compound Mo6S8(CH3NH2)6.

[image: image3.jpg]CPS |
2333_|

2111_
1888_]
1666._
1444 |
1222 |
1000_
777
555_]

333_|
111_|

I T T I T T l T T [ I T l T T I I T I T I | T T ] T T | T T l T T I I I
6.0 12.0 18.0 24.0 30.0 36.0 42.0 48.0 54.0 60.0 66.0 72.0 78.0
Deg.





Figure S3.  Traces of thermogravimetric analyses of the compounds Mo6S8(4-tert-butylpyridine)6, Mo6S8(PEt3)6, Mo6S8(bipy)6 and Mo6S8(CH3NH2)6.  The samples were heated from room temperature to 550°C at the rate of 20°C/min under a flow of dinitrogen (60 mL/min) in a Seiko TG/DTA 220 thermal analyzer.












































































Mo6S8(PEt3)6





Mo6S8(4-tbp)6























Mo6S8(bipy)6





Mo6S8(CH3NH2)6





� EMBED Excel.Sheet.8  ���








PAGE  
S2

[image: image4.wmf]40

50

60

70

80

90

100

0

100

200

300

400

500

Temperature (

o

C)

Weight %

_1072106440.xls
Chart1

		20.3189		21.9831		20.9024		26.6406		99.962726539

		20.3213		21.9905		20.9123		26.6468		99.9721182772

		20.3498		21.9954		20.8975		26.6456		99.9835644581

		20.351		22.0226		20.9086		26.6691		100.0008804755

		20.3609		22.0301		20.9111		26.6641		100.0152615746

		20.3547		22.0263		20.8876		26.6444		100.0261207719

		20.3634		22.0387		20.8777		26.6431		100.030816641

		20.3572		22.0461		20.9037		26.6308		100.0322841001

		20.3807		22.0523		20.9086		26.6172		100.0202509355

		20.3943		22.0449		20.9296		26.627		100.0152615746

		20.4413		22.0684		20.968		26.6604		100.0085112627

		20.4833		22.0857		20.9865		26.6592		100.0026414264

		20.5253		22.1042		20.9915		26.6753		99.9973585736

		20.5587		22.1314		21.0384		26.7272		99.9961846064

		20.6069		22.1908		21.0558		26.7445		99.9923692127

		20.6749		22.2378		21.099		26.7606		99.9882603272

		20.7108		22.2786		21.1485		26.8125		99.9856189009

		20.7615		22.3033		21.1905		26.8533		99.978868589

		20.8295		22.3342		21.2338		26.8694		99.9759336708

		20.9049		22.3762		21.3105		26.8916		99.9703573263

		20.9655		22.4257		21.371		26.9287		99.9656614572

		21.0286		22.4875		21.4304		26.9683		99.9536282926

		21.1114		22.5803		21.5194		27.0338		99.9489324235

		21.1621		22.673		21.601		27.0783		99.946584489

		21.2153		22.741		21.6851		27.1463		99.9421821117

		21.2684		22.7929		21.763		27.1933		99.9345513244

		21.3377		22.8622		21.8298		27.2366		99.9316164062

		21.3958		22.9017		21.8743		27.2626		99.9248660944

		21.4959		22.9351		21.9299		27.3021		99.9116589625

		21.5874		22.9697		21.9905		27.3874		99.9090175361

		21.674		23.0489		22.0634		27.4653		99.9049086507

		21.7754		23.107		22.1314		27.5358		99.8996257979

		21.8718		23.1873		22.244		27.6199		99.8934624697

		21.9695		23.2776		22.3342		27.7015		99.891408027

		22.0721		23.3703		22.3997		27.7435		99.8861251743

		22.171		23.4457		22.4999		27.8078		99.8811358133

		22.2625		23.5212		22.6161		27.8795		99.8711570915

		22.3824		23.6176		22.6965		27.9463		99.8644067797

		22.4974		23.7227		22.7966		28.0217		99.854134566

		22.5889		23.8031		22.9265		28.0922		99.8447428278

		22.7064		23.923		23.013		28.154		99.8335901387

		22.8176		24.0207		23.1206		28.2356		99.8306552205

		22.9116		24.0689		23.2195		28.3321		99.8247853841

		23.0303		24.1542		23.3073		28.4631		99.8192090395

		23.1478		24.2593		23.4049		28.5769		99.8124587277

		23.2343		24.3372		23.5286		28.7018		99.8080563504

		23.3468		24.4262		23.6374		28.7994		99.7969036613

		23.4853		24.5758		23.7586		28.8996		99.7854574804

		23.5991		24.6834		23.8884		28.9886		99.7757722503

		23.7252		24.8083		24.0182		29.0677		99.7622716267

		23.8624		24.9282		24.1159		29.1852		99.7511189376

		23.9836		25.037		24.2655		29.2804		99.7464230685

		24.0862		25.1458		24.4126		29.3966		99.7411402157

		24.2185		25.2571		24.5598		29.5017		99.7382052975

		24.3558		25.3721		24.7081		29.6377		99.7346833957

		24.5016		25.4994		24.838		29.7527		99.7332159366

		24.6636		25.6688		24.9492		29.8714		99.7264656248

		24.812		25.8308		25.084		29.9988		99.7197153129

		24.9505		25.9816		25.1953		30.1014		99.7079756402

		25.0976		26.1387		25.3189		30.23		99.7006383447

		25.2509		26.2722		25.5019		30.3397		99.6915400983

		25.3894		26.3785		25.6354		30.4879		99.6847897865

		25.5452		26.4947		25.7504		30.6255		99.6771589992

		25.6775		26.6172		25.9124		30.7844		99.670995671

		25.8197		26.7321		26.041		30.9125		99.6627779001

		25.9693		26.8447		26.1708		31.0679		99.6527991782

		26.1139		26.9943		26.3501		31.1711		99.64017903

		26.2759		27.155		26.5244		31.3086		99.6252109472

		26.4601		27.2947		26.6716		31.4616		99.6140582581

		26.6295		27.4381		26.8459		31.5873		99.6034925526

		26.7878		27.6001		26.9757		31.719		99.5926333553

		26.9671		27.7658		27.134		31.8708		99.5847090762

		27.1204		27.8845		27.2638		32.0167		99.578545748

		27.2861		28.0304		27.4418		32.1364		99.5709149607

		27.4542		28.1862		27.5914		32.2811		99.5612297307

		27.6174		28.3642		27.7856		32.4092		99.5509575171

		27.7868		28.5089		27.9216		32.5658		99.5400983198

		27.9426		28.6622		28.0984		32.7199		99.5292391225

		28.0835		28.8551		28.2702		32.8528		99.5183799252

		28.248		29.0294		28.4656		33.0141		99.5060532688

		28.4495		29.1827		28.6226		33.2204		99.494313596

		28.6164		29.3472		28.8118		33.3758		99.481399956

		28.8217		29.5524		29.0109		33.5229		99.473182185

		29.0356		29.7119		29.158		33.6818		99.4611490205

		29.2124		29.9035		29.3472		33.8217		99.4508768068

		29.4016		30.0668		29.545		33.9486		99.4397241177

		29.587		30.2708		29.6995		34.1052		99.4282779368

		29.7675		30.4239		29.8899		34.3198		99.4156577885

		29.9221		30.584		30.1224		34.5096		99.4015701812

		30.1187		30.7572		30.3112		34.6804		99.3877760657

		30.3136		30.9339		30.4998		34.8761		99.3754494093

		30.501		31.1094		30.6812		35.0302		99.3628292611

		30.6884		31.298		30.8283		35.1915		99.348448162

		30.8864		31.5008		30.9872		35.3552		99.3375889647

		31.0726		31.6704		31.1687		35.5165		99.3279037347

		31.2541		31.8672		31.3596		35.711		99.3152835865

		31.4593		32.0463		31.5684		35.9434		99.304717881

		31.6466		32.2266		31.7925		36.1486		99.2920977328

		31.8471		32.4068		32.0048		36.3348		99.2727272727

		32.057		32.6002		32.2064		36.5412		99.2513023699

		32.2479		32.7591		32.395		36.7131		99.2319319099

		32.4341		32.9311		32.5907		36.8875		99.2157898599

		32.6334		33.1362		32.7828		37.101		99.2005282853

		32.8314		33.3106		32.9785		37.2765		99.1964193998

		33.0485		33.4837		33.1576		37.465		99.1911365471

		33.2477		33.6984		33.345		37.6655		99.1843862352

		33.4446		33.9249		33.5608		37.8944		99.1755814807

		33.6557		34.1147		33.7589		38.0746		99.1641352997

		33.8787		34.321		33.9451		38.2857		99.1465257906

		34.0898		34.5475		34.136		38.4731		99.1318511996

		34.2926		34.7551		34.3685		38.6653		99.1189375596

		34.5381		34.9448		34.5772		38.8681		99.1013280505

		34.7314		35.1429		34.8002		39.0578		99.087533935

		34.9472		35.3659		35.0219		39.2381		99.0722723604

		35.1382		35.5556		35.2307		39.4539		99.0558368185

		35.3635		35.7703		35.4192		39.6425		99.037346834

		35.5331		35.9802		35.6256		39.9022		99.0238462103

		35.7738		36.183		35.8403		40.1359		99.0044757502

		35.9897		36.3941		36.0395		40.3316		98.985398782

		36.2103		36.6028		36.2625		40.5439		98.9680827647

		36.4226		36.8246		36.4997		40.7751		98.9492992883

		36.6823		37.0251		36.7333		40.9732		98.9322767628

		36.9029		37.2267		36.9492		41.208		98.9208305818

		37.1045		37.439		37.2065		41.4155		98.9090909091

		37.3287		37.6477		37.4307		41.6148		98.8932423509

		37.5516		37.8612		37.6204		41.8295		98.8806222027

		37.7758		38.0877		37.8457		42.0939		98.8627192017

		37.9964		38.3296		38.0687		42.2849		98.8433487417

		38.2466		38.5395		38.2869		42.5339		98.826619708

		38.4672		38.7779		38.5158		42.7687		98.8128255925

		38.7269		38.9819		38.7874		42.9502		98.7984444934

		38.957		39.1824		39.008		43.1293		98.7831829188

		39.1847		39.3875		39.2286		43.3674		98.7658669015

		39.4041		39.633		39.4611		43.5722		98.7473769169

		39.6662		39.8465		39.7018		43.7917		98.7259520141

		39.8678		40.0742		39.9224		44.0359		98.7074620295

		40.0956		40.3458		40.1442		44.2407		98.687211094

		40.3588		40.5937		40.3932		44.4882		98.6675471421

		40.5984		40.8237		40.6043		44.7234		98.6505246166

		40.8154		41.0586		40.8344		44.9384		98.6361435175

		41.0669		41.291		41.0657		45.1814		98.6214689266

		41.2922		41.5045		41.3385		45.3953		98.6103162374

		41.5175		41.7334		41.6053		45.6046		98.5991635483

		41.7713		41.9231		41.852		45.8173		98.5800865801

		42.0002		42.1615		42.1283		46.066		98.562477071

		42.2623		42.3809		42.3952		46.2741		98.5425196273

		42.5339		42.5968		42.5944		46.5285		98.5240296427

		42.7865		42.834		42.802		46.7614		98.5049526744

		43.0202		43.0985		43.032		47.0191		98.4914520508

		43.2775		43.3528		43.2467		47.2487		98.4779514271

		43.4878		43.6071		43.4653		47.4906		98.4644508034

		43.7253		43.8446		43.7118		47.7112		98.4506566879

		43.9425		44.0854		43.9537		47.9486		98.4371560643

		44.2047		44.3228		44.2024		48.1647		98.4204270306

		44.4455		44.5445		44.4399		48.4055		98.4063394233

		44.6762		44.7617		44.6807		48.6565		98.3893168978

		44.917		45.0081		44.9485		48.9007		98.3717073887

		45.1668		45.2411		45.2073		49.155		98.3552718468

		45.3728		45.4673		45.4628		49.3992		98.3411842395

		45.6361		45.7014		45.7025		49.6377		98.3247486976

		45.9062		45.95		45.9579		49.8651		98.3106610903

		46.1324		46.1942		46.1976		50.071		98.2909971385

		46.3563		46.4306		46.4418		50.3006		98.2701592193

		46.6196		46.6556		46.6973		50.5673		98.2507887593

		46.8244		46.9167		46.9741		50.7912		98.2299508401

		47.0652		47.1688		47.2048		51.05		98.2067649864

		47.2993		47.3927		47.4512		51.3302		98.1938513464

		47.5514		47.6268		47.6966		51.5643		98.1803507227

		47.8035		47.8699		47.9419		51.786		98.1650891481

		48.0679		48.0994		48.1692		52.0066		98.1527624917

		48.3099		48.3211		48.4213		52.2418		98.1401423435

		48.5799		48.5664		48.6688		52.4893		98.1228263262

		48.868		48.8253		48.9243		52.7549		98.1031623743

		49.1223		49.0908		49.1865		53.0261		98.0814439797

		49.3924		49.3215		49.4487		53.3277		98.0588451097

		49.6512		49.5826		49.7255		53.5708		98.0429965515

		49.9089		49.8471		49.9832		53.8273		98.0230391078

		50.1509		50.0755		50.2207		54.0749		98.0089515005

		50.3861		50.3298		50.4626		54.3349		97.9977988114

		50.6483		50.6021		50.7226		54.5903		97.9872331059

		50.9296		50.8824		50.9881		54.8581		97.9734389904

		51.1873		51.113		51.2481		55.1293		97.9622863013

		51.4619		51.3685		51.544		55.3949		97.9484921858

		51.723		51.6262		51.8198		55.6473		97.9361655294

		51.9852		51.885		52.0887		55.9145		97.9197299875

		52.1889		52.1123		52.3171		56.1686		97.9009465111

		52.4533		52.3813		52.5861		56.4162		97.8880328711

		52.6806		52.6559		52.8123		56.6736		97.8783476411

		52.953		52.8967		53.07		56.9321		97.8666079683

		53.1983		53.1521		53.3288		57.158		97.8580967056

		53.4999		53.4076		53.5978		57.3969		97.8454765573

		53.7643		53.6495		53.8532		57.6391		97.8296279991

		54.04		53.8982		54.1481		57.8954		97.8117249982

		54.3304		54.1694		54.4238		58.1386		97.7932350136

		54.6004		54.4474		54.6893		58.4166		97.7744515372

		54.8536		54.7197		54.9898		58.6849		97.7603639299

		55.1136		55.0056		55.2644		58.9651		97.7451023553

		55.3994		55.288		55.5378		59.2105		97.734243158

		55.6343		55.539		55.7961		59.4777		97.722796977

		55.896		55.7538		56.0785		59.7405		97.709883337

		56.1665		56.009		56.3359		60.0272		97.6978501724

		56.4434		56.2664		56.5933		60.3009		97.6843495488

		56.6942		56.5151		56.8517		60.5724		97.6673270233

		56.9734		56.7822		57.1091		60.82		97.651478465

		57.2329		57.0472		57.3708		61.0936		97.6365103823

		57.5022		57.2905		57.6304		61.3369		97.6189008731

		57.7618		57.5533		57.9258		61.5747		97.6039327904

		58.0083		57.828		58.2005		61.8234		97.5901386749

		58.2483		58.0865		58.484		62.1069		97.5772250349

		58.5068		58.3732		58.7457		62.3534		97.5637244112

		58.7631		58.6567		59.0194		62.6119		97.5537456893

		59.002		58.914		59.2909		62.8866		97.5411255411

		59.2876		59.1725		59.5624		63.1788		97.529972852

		59.5787		59.431		59.8219		63.4514		97.5155917529

		59.8437		59.7025		60.1054		63.7381		97.5009171619

		60.1249		59.9414		60.3769		64.0139		97.4885905055

		60.4116		60.2129		60.6397		64.2702		97.4753833737

		60.6712		60.479		60.9058		64.5406		97.4592413236

		60.9394		60.7668		61.186		64.8197		97.4492626018

		61.2294		61.0296		61.4433		65.0836		97.437522929

		61.4933		61.3152		61.742		65.3812		97.4225548463

		61.7528		61.5975		62.0233		65.6625		97.4093477144

		62.0428		61.856		62.3121		65.9296		97.3955535989

		62.311		62.1243		62.5869		66.2		97.3785310734

		62.588		62.3686		62.8682		66.477		97.3632694989

		62.8595		62.626		63.1462		66.7571		97.3524103016

		63.1527		62.8953		63.4101		67.0688		97.3386161861

		63.4307		63.1722		63.6794		67.3729		97.3283439724

		63.7076		63.4329		63.9683		67.6254		97.3210066769

		63.9639		63.7283		64.2528		67.885		97.3174847751

		64.2387		64.0226		64.4972		68.1613		97.306332086

		64.5091		64.2811		64.785		68.4125		97.2951793969

		64.7622		64.5732		65.0771		68.6857		97.281972265

		65.0271		64.8566		65.3736		68.9986		97.2672976741

		65.3377		65.1292		65.6603		69.2687		97.2546775259

		65.6234		65.3996		65.9633		69.5303		97.2444053122

		65.8894		65.6766		66.2402		69.7983		97.235013574

		66.187		65.9263		66.5356		70.0443		97.2282632622

		66.49		66.2152		66.7713		70.2934		97.2182845403

		66.768		66.4965		67.0514		70.5697		97.2050774085

		67.0558		66.7539		67.3534		70.822		97.1933377357

		67.3555		67.033		67.6495		71.0878		97.1857069484

		67.6149		67.3164		67.9153		71.3872		97.1754347348

		67.8797		67.572		68.2367		71.675		97.1651625211

		68.133		67.8483		68.5235		71.9879		97.1545968156

		68.3759		68.1665		68.7945		72.2904		97.1484334874

		68.6386		68.446		69.0792		72.5971		97.1364003228

		68.9369		68.7276		69.3252		72.8619		97.126421601

		69.1933		69.0416		69.5858		73.1299		97.1161493873

		69.4508		69.2875		69.8601		73.4062		97.1096925673

		69.7596		69.5523		70.1395		73.6658		97.0938440091

		70.0568		69.8339		70.4075		73.9421		97.0797564018

		70.3384		70.1165		70.71		74.2153		97.0624403845

		70.6472		70.3677		70.9999		74.4958		97.0474723017

		70.9434		70.6681		71.2877		74.7732		97.0304497762

		71.2029		70.9256		71.564		75.0641		97.0228189889

		71.4636		71.1967		71.8603		75.3582		97.0169491525

		71.7148		71.4678		72.1575		75.6639		97.011372808

		71.966		71.7242		72.4349		75.9706		97.0078509062

		72.2622		71.9995		72.6819		76.2594		97.0022745616

		72.55		72.2967		72.9687		76.5724		96.9911218725

		72.8389		72.5678		73.2555		76.8623		96.9793821997

		73.1435		72.8651		73.537		77.1418		96.9679360188

		73.4271		73.1707		73.8364		77.415		96.956196346

		73.6836		73.4575		74.1556		77.6808		96.9447501651

		73.9651		73.7191		74.4309		77.9718		96.9362389023

		74.232		73.9986		74.7208		78.2397		96.9283146232

		74.5073		74.253		75.0003		78.5339		96.9200968523

		74.8119		74.5303		75.2975		78.8374		96.9101181305

		75.1154		74.8077		75.5875		79.1281		96.8980849659

		75.4127		75.1018		75.8701		79.3944		96.8851713258

		75.7057		75.4022		76.1223		79.672		96.8702032431

		75.9779		75.7005		76.4238		79.9546		96.8587570621

		76.25		75.9873		76.6928		80.2393		96.8467238976

		76.5232		76.295		76.9848		80.5536		96.8393866021

		76.7974		76.5797		77.2904		80.8424		96.831462323

		77.0947		76.8696		77.6023		81.1414		96.8267664539

		77.3919		77.1648		77.8661		81.4455		96.8179616993

		77.6798		77.4453		78.1633		81.7517		96.8120918629

		77.9875		77.707		78.4533		82.0486		96.8018196493

		78.29		78.0158		78.7547		82.3568		96.7871450583

		78.5841		78.2858		79.0505		82.6435		96.7748184019

		78.8709		78.5611		79.3383		82.916		96.7604373028

		79.1597		78.8531		79.6128		83.2017		96.7425343019

		79.427		79.1393		79.9077		83.4548		96.72932717

		79.7066		79.4077		80.1934		83.7385		96.7211093991

		79.9944		79.7066		80.473		84.0385		96.7120111527

		80.2812		79.9863		80.7802		84.3508		96.704967349

		80.573		80.2638		81.0608		84.6324		96.7002714799

		80.8516		80.5679		81.3475		84.962		96.6923472008

		81.121		80.8537		81.6353		85.2437		96.6826619708

		81.3802		81.1261		81.9384		85.5386		96.6685743635

		81.6731		81.4506		82.2241		85.8172		96.6615305598

		81.9455		81.7517		82.5303		86.11		96.6524323134

		82.2415		82.0241		82.8048		86.3764		96.6480299362

		82.5241		82.3303		83.0987		86.6723		96.6445080343

		82.8486		82.618		83.3793		86.9978		96.6412796243

		83.1385		82.8987		83.6834		87.3019		96.6315943943

		83.4221		83.2058		83.9773		87.5938		96.6219091643

		83.7069		83.4885		84.2722		87.905		96.6101694915

		84.0059		83.7538		84.5691		88.2101		96.5937339497

		84.2701		84.0803		84.8559		88.4897		96.5787658669

		84.5416		84.363		85.1406		88.7816		96.5667327023

		84.8426		84.6569		85.4263		89.0837		96.5573409641

		85.1416		84.9518		85.7192		89.3939		96.5458947832

		85.4151		85.2579		85.9968		89.6908		96.5391444713

		85.7049		85.5365		86.309		89.9827		96.5318071759

		86.0274		85.8141		86.5907		90.2957		96.518600044

		86.3284		86.0978		86.906		90.5903		96.5050994204

		86.6141		86.4182		87.2305		90.8722		96.4936532394

		86.9315		86.7152		87.5244		91.156		96.481326583

		87.2336		87.0274		87.8234		91.4398		96.4695869103

		87.504		87.3417		88.1397		91.7316		96.4601951721

		87.7785		87.6254		88.4408		92.0262		96.4490424829

		88.0703		87.9336		88.7316		92.2972		96.4364223347

		88.3652		88.2397		89.0316		92.6244		96.4264436129

		88.6561		88.5336		89.3204		92.9437		96.4170518747

		88.9663		88.8357		89.6276		93.2374		96.4044317265

		89.2867		89.1592		89.9082		93.5469		96.3968009392

		89.6051		89.4541		90.205		93.8701		96.3888766601

		89.898		89.7592		90.5075		94.149		96.3856482501

		90.206		90.0429		90.7914		94.4378		96.3706801673

		90.4819		90.3449		91.0811		94.7394		96.3692127082

		90.7539		90.6337		91.3916		95.0311		96.3589404945

		91.0328		90.9195		91.6803		95.3317		96.3516031991

		91.3354		91.2151		91.9622		95.6332		96.3339936899

		91.6153		91.5266		92.2687		95.9466		96.3272433781

		91.8961		91.8153		92.5436		96.263		96.3113948199

		92.1888		92.109		92.8284		96.5567		96.3008291144

		92.4825		92.4175		93.1054		96.8464		96.2882089662

		92.7683		92.7062		93.4237		97.1559		96.2785237362

		93.063		93.0048		93.7243		97.4604		96.2644361288

		93.3784		93.3064		94.0278		97.7462		96.2521094724

		93.6809		93.5952		94.3254		98.0724		96.2359674224

		93.9776		93.876		94.6388		98.3887		96.2212928315

		94.2703		94.1747		94.9227		98.6627		96.2104336342

		94.5886		94.4634		95.2213		98.9574		96.1969330105

		94.8882		94.7512		95.5307		99.2737		96.186367305

		95.172		95.0675		95.8402		99.5605		96.1731601732

		95.4282		95.3602		96.1339		99.866		96.1646489104

		95.6983		95.6648		96.4384		100.182		96.1420500404

		95.9437		95.9713		96.736		100.494		96.1355932203

		96.1684		96.2709		97.0258		100.803		96.1194511703

		96.4009		96.5734		97.3224		101.104		96.111820383

		96.6207		96.87		97.6112		101.406		96.0968523002

		96.8356		97.1549		97.8802		101.718		96.0945043657

		97.0504		97.4692		98.1867		102.029		96.0792427911

		97.3037		97.7629		98.4981		102.325		96.0695575611

		97.5806		98.0714		98.7987		102.656		96.0589918556

		97.9078		98.3897		99.117		102.954		96.0457847238

		98.232		98.7011		99.4511		103.268		96.030816641

		98.5701		98.9751		99.7576		103.563		96.0173160173

		98.9199		99.3063		100.053		103.855		96.0052828527

		99.2353		99.6127		100.342		104.153		95.9862058845

		99.5615		99.9035		100.651		104.468		95.9738792281

		99.8779		100.241		100.945		104.769		95.9603786044

		100.194		100.528		101.225		105.077		95.9471714726

		100.516		100.86		101.515		105.403		95.9322033898

		100.849		101.12		101.821		105.722		95.9245726025

		101.166		101.462		102.128		106.05		95.9081370607

		101.49		101.73		102.43		106.365		95.8922885025

		101.801		102.037		102.751		106.661		95.8779074033

		102.095		102.325		103.071		106.969		95.8591239269

		102.421		102.627		103.384		107.28		95.8421014014

		102.736		102.929		103.679		107.567		95.8288942696

		103.045		103.265		103.984		107.882		95.8203830068

		103.364		103.538		104.275		108.193		95.8080563504

		103.681		103.848		104.58		108.512		95.8042409568

		103.976		104.158		104.869		108.812		95.7907403331

		104.281		104.474		105.184		109.127		95.7842835131

		104.587		104.795		105.494		109.428		95.7672609876

		104.906		105.111		105.779		109.764		95.7564017903

		105.227		105.419		106.087		110.078		95.7396727566

		105.549		105.744		106.378		110.404		95.7323354611

		105.857		106.064		106.669		110.727		95.7150194438

		106.174		106.366		106.959		111.066		95.7038667547

		106.481		106.64		107.288		111.399		95.692127082

		106.802		106.955		107.582		111.701		95.6762785237

		107.094		107.277		107.912		112.011		95.6604299655

		107.416		107.576		108.236		112.316		95.6454618827

		107.721		107.873		108.571		112.596		95.6322547509

		108.032		108.21		108.857		112.888		95.6131777827

		108.331		108.532		109.163		113.195		95.6005576345

		108.649		108.807		109.465		113.501		95.586763519

		108.947		109.156		109.745		113.812		95.572088928

		109.259		109.442		110.023		114.157		95.5562403698

		109.558		109.74		110.355		114.478		95.5424462543

		109.863		110.084		110.664		114.783		95.5327610243

		110.172		110.363		110.981		115.072		95.5157384988

		110.482		110.672		111.32		115.395		95.512216597

		110.793		111.021		111.658		115.69		95.4998899406

		111.111		111.309		111.948		115.986		95.4940201042

		111.415		111.646		112.25		116.317		95.4790520214

		111.706		111.902		112.543		116.642		95.4755301196

		112.007		112.237		112.854		116.947		95.4523442659

		112.308		112.527		113.145		117.27		95.4373761831

		112.609		112.794		113.457		117.583		95.4232885758

		112.923		113.119		113.769		117.895		95.4039181158

		113.264		113.406		114.069		118.221		95.3775038521

		113.572		113.749		114.356		118.517		95.3610683102

		113.881		114.033		114.657		118.822		95.3481546702

		114.173		114.374		114.952		119.14		95.3287842101

		114.477		114.684		115.266		119.444		95.3261427838

		114.769		114.989		115.568		119.749		95.3149900947

		115.06		115.262		115.863		120.087		95.3023699464

		115.363		115.569		116.181		120.412		95.28358647

		115.681		115.906		116.502		120.736		95.2689118791

		115.992		116.211		116.807		121.058		95.2424976154

		116.305		116.507		117.124		121.379		95.226942549

		116.62		116.778		117.445		121.687		95.2137354171

		116.933		117.102		117.739		121.987		95.2002347935

		117.226		117.411		118.049		122.271		95.1870276616

		117.532		117.708		118.344		122.577		95.1700051361

		117.832		118.008		118.645		122.876		95.1576784797

		118.146		118.316		118.949		123.176		95.1341991342

		118.44		118.6		119.272		123.502		95.1160026414

		118.758		118.942		119.57		123.834		95.0931102796

		119.062		119.233		119.883		124.157		95.0781421968

		119.369		119.546		120.203		124.469		95.0573042776

		119.677		119.884		120.526		124.811		95.0446841294

		119.985		120.179		120.833		125.122		95.0303030303

		120.307		120.489		121.151		125.442		95.016215423

		120.602		120.793		121.445		125.777		95.0006603566

		120.914		121.14		121.733		126.102		94.9798224374

		121.206		121.44		122.015		126.411		94.9616259447

		121.503		121.733		122.308		126.759		94.9413750092

		121.783		122.004		122.605		127.088		94.9214175655

		122.078		122.308		122.915		127.398		94.8973512363

		122.378		122.601		123.245		127.742		94.8815026781

		122.682		122.91		123.583		128.057		94.8624257099

		122.992		123.217		123.904		128.355		94.8500990535

		123.299		123.524		124.207		128.676		94.8380658889

		123.621		123.874		124.526		129.012		94.8304351016

		123.897		124.184		124.841		129.347		94.820162888

		124.208		124.456		125.141		129.681		94.8069557561

		124.524		124.802		125.451		130.021		94.7931616406

		124.839		125.104		125.783		130.361		94.7732041969

		125.16		125.373		126.111		130.695		94.7573556387

		125.494		125.725		126.414		131.004		94.7382786705

		125.804		126.033		126.729		131.34		94.7233105877

		126.097		126.364		127.034		131.682		94.7021791768

		126.408		126.707		127.338		131.995		94.683982684

		126.716		127.03		127.634		132.306		94.6599163548

		127.029		127.342		127.951		132.64		94.6405458948

		127.333		127.674		128.251		132.959		94.6123706802

		127.647		127.977		128.588		133.263		94.5909457774

		127.964		128.258		128.919		133.592		94.5718688092

		128.272		128.569		129.237		133.924		94.5519113655

		128.602		128.89		129.56		134.246		94.5298994791

		128.904		129.189		129.884		134.579		94.5134639372

		129.229		129.461		130.193		134.938		94.5043656908

		129.538		129.826		130.49		135.272		94.4864626899

		129.862		130.148		130.816		135.599		94.4779514271

		130.158		130.436		131.136		135.936		94.4606354098

		130.482		130.763		131.443		136.279		94.4480152616

		130.805		131.098		131.758		136.606		94.4242424242

		131.117		131.416		132.075		136.929		94.4063394233

		131.402		131.73		132.38		137.265		94.3837405532

		131.716		132.059		132.693		137.617		94.3658375523

		132.03		132.378		133.005		137.95		94.351749945

		132.325		132.703		133.299		138.274		94.3367818622

		132.642		133.014		133.63		138.631		94.3244552058

		132.964		133.329		133.954		138.973		94.3100741067

		133.282		133.667		134.259		139.296		94.3006823685

		133.601		133.988		134.602		139.628		94.2780834984

		133.921		134.298		134.917		139.966		94.2660503338

		134.22		134.62		135.222		140.313		94.2513757429

		134.556		134.956		135.531		140.648		94.2302443319

		134.884		135.27		135.858		140.99		94.2102868883

		135.196		135.589		136.159		141.343		94.1970797564

		135.506		135.919		136.503		141.687		94.1762418373

		135.845		136.25		136.834		142.02		94.1489470981

		136.144		136.559		137.16		142.355		94.1369139335

		136.434		136.887		137.486		142.685		94.1143150635

		136.755		137.2		137.801		143.027		94.0964120625

		137.09		137.518		138.127		143.364		94.0738131925

		137.412		137.829		138.454		143.694		94.0594320933

		137.73		138.153		138.768		144.02		94.0385941742

		138.076		138.468		139.07		144.352		94.0180497469

		138.395		138.785		139.404		144.673		93.9957443686

		138.71		139.089		139.717		145.009		93.9699170886

		139.027		139.419		140.035		145.355		93.9511336122

		139.343		139.741		140.35		145.701		93.9288282339

		139.678		140.068		140.692		146.055		93.9176755448

		139.991		140.425		141.012		146.4		93.8953701666

		140.313		140.753		141.334		146.732		93.8850979529

		140.607		141.069		141.66		147.05		93.8660209847

		140.923		141.41		141.995		147.401		93.8448895737

		141.207		141.739		142.317		147.73		93.8240516546

		141.538		142.041		142.637		148.081		93.8090835718

		141.858		142.39		142.955		148.417		93.7914740627

		142.193		142.727		143.259		148.769		93.7750385208

		142.539		143.037		143.564		149.108		93.7653532908

		142.863		143.371		143.887		149.445		93.7477437816

		143.198		143.698		144.192		149.785		93.7351236334

		143.513		144.008		144.518		150.134		93.7192750752

		143.82		144.329		144.842		150.492		93.7025460415

		144.124		144.655		145.191		150.822		93.6861104997

		144.441		144.967		145.505		151.184		93.6667400396

		144.748		145.302		145.871		151.521		93.6517719569

		145.053		145.632		146.19		151.867		93.6271186441

		145.384		145.963		146.519		152.193		93.6127375449

		145.684		146.284		146.832		152.546		93.5901386749

		146.006		146.609		147.143		152.886		93.5789859858

		146.316		146.935		147.448		153.233		93.5534521975

		146.645		147.274		147.755		153.576		93.5425930002

		146.96		147.601		148.07		153.918		93.5211680974

		147.289		147.924		148.395		154.277		93.4997431947

		147.585		148.26		148.732		154.619		93.4771443246

		147.917		148.583		149.052		154.956		93.4612957664

		148.25		148.916		149.397		155.316		93.4430992736

		148.552		149.248		149.729		155.664		93.424609289

		148.877		149.592		150.065		155.994		93.411695649

		149.209		149.936		150.395		156.314		93.3917382053

		149.524		150.266		150.728		156.661		93.3697263189

		149.845		150.564		151.069		157.002		93.3456599897

		150.196		150.899		151.387		157.375		93.3239415951

		150.509		151.224		151.703		157.71		93.3016362169

		150.851		151.554		152.024		158.072		93.2813852814

		151.165		151.894		152.35		158.394		93.2643627559

		151.473		152.236		152.662		158.744		93.244698804

		151.788		152.563		153.002		159.07		93.2311981804

		152.11		152.901		153.331		159.434		93.2100667694

		152.43		153.222		153.647		159.788		93.1933377357

		152.757		153.55		154.005		160.156		93.1742607675

		153.078		153.9		154.272		160.492		93.1528358647

		153.393		154.224		154.64		160.839		93.1226062074

		153.718		154.548		154.943		161.193		93.1049966982

		154.026		154.89		155.283		161.545		93.0806368772

		154.34		155.221		155.587		161.876		93.0630273681

		154.676		155.549		155.952		162.205		93.0460048426

		154.989		155.882		156.262		162.54		93.0354391371

		155.323		156.224		156.604		162.865		93.0207645462

		155.66		156.55		156.965		163.199		93.0037420207

		155.992		156.881		157.268		163.552		92.9843715606

		156.3		157.216		157.583		163.906		92.9608922151

		156.64		157.56		157.963		164.255		92.9341844596

		156.959		157.901		158.247		164.591		92.9142270159

		157.277		158.237		158.571		164.916		92.8928021131

		157.593		158.591		158.94		165.251		92.8754860958

		157.918		158.928		159.24		165.601		92.8613984885

		158.236		159.272		159.576		165.946		92.841147553

		158.548		159.599		159.953		166.307		92.8206031257

		158.87		159.956		160.267		166.669		92.8062220266

		159.204		160.299		160.6		167.031		92.7862645829

		159.536		160.621		160.988		167.37		92.7630787292

		159.856		160.96		161.298		167.698		92.7460562037

		160.18		161.329		161.596		168.035		92.7255117764

		160.492		161.665		161.894		168.379		92.7055543327

		160.822		161.995		162.242		168.715		92.6826619708

		161.137		162.35		162.525		169.068		92.6632915107

		161.472		162.678		162.861		169.422		92.6439210507

		161.807		162.996		163.214		169.757		92.6219091643

		162.138		163.329		163.577		170.096		92.5969623597

		162.451		163.688		163.88		170.439		92.577004916

		162.778		164.02		164.235		170.76		92.5561669968

		163.098		164.366		164.549		171.112		92.5323941595

		163.421		164.7		164.841		171.46		92.5106757649

		163.751		165.044		165.156		171.8		92.489544354

		164.072		165.369		165.483		172.137		92.4648910412

		164.394		165.718		165.798		172.497		92.4417051875

		164.716		166.07		166.171		172.826		92.4199867929

		165.05		166.418		166.438		173.163		92.4009098246

		165.364		166.756		166.766		173.508		92.3768434955

		165.691		167.076		167.082		173.844		92.3577665273

		166.023		167.398		167.431		174.176		92.3345806736

		166.348		167.704		167.708		174.51		92.3184386235

		166.665		168.05		168.061		174.837		92.2958397535

		167		168.394		168.406		175.176		92.2726538998

		167.326		168.753		168.731		175.534		92.2521094724

		167.647		169.108		169.114		175.865		92.223640766

		167.976		169.45		169.417		176.213		92.1954655514

		168.308		169.766		169.736		176.567		92.1640619268

		168.63		170.095		170.033		176.898		92.1402890894

		168.952		170.418		170.376		177.223		92.1038961039

		169.277		170.779		170.685		177.574		92.0824712011

		169.611		171.151		171.006		177.898		92.0507740847

		169.929		171.515		171.374		178.227		92.0217183946

		170.243		171.858		171.708		178.565		92.0017609509

		170.578		172.216		171.99		178.892		91.9832709663

		170.921		172.533		172.339		179.22		91.9571501944

		171.252		172.846		172.67		179.566		91.9342578326

		171.574		173.156		172.987		179.908		91.9163548316

		171.913		173.48		173.353		180.254		91.8905275515

		172.242		173.809		173.636		180.601		91.8626458287

		172.574		174.146		173.946		180.951		91.8286007778

		172.893		174.471		174.273		181.291		91.8033604813

		173.228		174.813		174.654		181.643		91.7619781349

		173.559		175.167		174.968		181.968		91.7299875266

		173.886		175.517		175.309		182.312		91.7097365911

		174.204		175.848		175.603		182.646		91.6877247047

		174.538		176.203		175.941		182.955		91.6630713919

		174.877		176.539		176.286		183.274		91.6398855382

		175.208		176.864		176.595		183.601		91.6152322254

		175.538		177.168		176.958		183.919		91.578545748

		175.845		177.495		177.246		184.244		91.5497835498

		176.169		177.83		177.608		184.6		91.5180864333

		176.474		178.161		177.916		184.934		91.4922591533

		176.809		178.491		178.235		185.292		91.4640839387

		177.132		178.83		178.618		185.629		91.4353217404

		177.477		179.179		178.963		185.965		91.4077335094

		177.803		179.491		179.29		186.302		91.3681121139

		178.16		179.836		179.58		186.608		91.3346540465

		178.481		180.159		179.91		186.931		91.3017829628

		178.818		180.493		180.269		187.27		91.2730207645

		179.164		180.802		180.547		187.602		91.2533568127

		179.502		181.124		180.909		187.938		91.2345733363

		179.82		181.446		181.239		188.312		91.2166703353

		180.161		181.768		181.586		188.642		91.1870276616

		180.483		182.09		181.907		188.97		91.1614938734

		180.804		182.407		182.262		189.293		91.1300902487

		181.127		182.735		182.601		189.637		91.0983931323

		181.448		183.045		182.94		189.951		91.0658155404

		181.767		183.382		183.261		190.294		91.0391077849

		182.107		183.708		183.597		190.609		91.0077041602

		182.44		184.025		183.926		190.941		90.9760070438

		182.787		184.351		184.25		191.265		90.9507667474

		183.128		184.68		184.581		191.604		90.9261134346

		183.475		184.992		184.916		191.921		90.9035145645

		183.808		185.3		185.247		192.251		90.8765133172

		184.141		185.64		185.591		192.586		90.8571428571

		184.46		185.941		185.924		192.904		90.8316090689

		184.788		186.258		186.238		193.236		90.8031403625

		185.114		186.563		186.569		193.568		90.7793675251

		185.45		186.882		186.911		193.92		90.7514858023

		185.777		187.205		187.236		194.273		90.7282999486

		186.117		187.549		187.591		194.596		90.6977767995

		186.454		187.858		187.943		194.936		90.6731234867

		186.779		188.191		188.298		195.275		90.6431873212

		187.113		188.512		188.637		195.615		90.6150121065

		187.456		188.803		188.976		195.926		90.5806735637

		187.796		189.092		189.293		196.265		90.5516178737

		188.142		189.391		189.64		196.59		90.5222686918

		188.481		189.681		189.952		196.911		90.4917455426

		188.814		189.995		190.299		197.224		90.4665052462

		189.148		190.31		190.642		197.559		90.4362755888

		189.476		190.629		190.995		197.899		90.4157311615

		189.81		190.958		191.334		198.217		90.3884364223

		190.157		191.273		191.681		198.561		90.3611416832

		190.501		191.586		192.006		198.894		90.3332599604

		190.838		191.893		192.342		199.226		90.3077261721

		191.196		192.213		192.681		199.527		90.2801379412

		191.539		192.522		193.016		199.849		90.2481473329

		191.873		192.825		193.344		200.159		90.2246679874

		192.206		193.115		193.699		200.482		90.1926773791

		192.555		193.41		194.057		200.795		90.1697850172

		192.883		193.704		194.396		201.141		90.1360334581

		193.224		194.012		194.737		201.453		90.1131410962

		193.562		194.33		195.106		201.769		90.0832049307

		193.907		194.644		195.433		202.093		90.0573776506

		194.256		194.968		195.764		202.398		90.0271479932

		194.579		195.275		196.101		202.718		89.9995597623

		194.918		195.574		196.458		203.054		89.9749064495

		195.274		195.881		196.795		203.361		89.9520140876

		195.62		196.189		197.14		203.688		89.9317631521

		195.943		196.494		197.484		204.011		89.902707462

		196.303		196.812		197.841		204.324		89.8809890674

		196.625		197.134		198.175		204.64		89.8504659183

		196.973		197.424		198.524		204.988		89.81847531

		197.319		197.73		198.894		205.294		89.7914740627

		197.682		198.046		199.241		205.631		89.7624183726

		198.021		198.36		199.581		205.959		89.7357106171

		198.387		198.663		199.93		206.296		89.7054809597

		198.724		198.991		200.251		206.604		89.6799471715

		199.064		199.307		200.575		206.936		89.6476630714

		199.405		199.608		200.916		207.25		89.6253576932

		199.756		199.918		201.243		207.559		89.5995304131

		200.095		200.234		201.577		207.86		89.5783990021

		200.448		200.552		201.947		208.165		89.5552131484

		200.796		200.863		202.274		208.473		89.5343752293

		201.131		201.178		202.605		208.781		89.5091349329

		201.485		201.481		202.951		209.101		89.479785751

		201.838		201.789		203.278		209.423		89.45865434

		202.176		202.102		203.589		209.76		89.4345880109

		202.518		202.408		203.942		210.079		89.4160980263

		202.884		202.715		204.291		210.397		89.3923251889

		203.23		203.028		204.63		210.725		89.3706067943

		203.571		203.341		204.981		211.05		89.337148727

		203.927		203.645		205.327		211.367		89.3089735124

		204.286		203.964		205.667		211.687		89.2758089368

		204.622		204.279		205.997		212.019		89.247927214

		204.976		204.601		206.327		212.334		89.2247413603

		205.329		204.933		206.677		212.652		89.2062513757

		205.69		205.25		207.014		212.994		89.1889353584

		206.041		205.577		207.345		213.319		89.1748477511

		206.392		205.91		207.684		213.639		89.1601731602

		206.746		206.225		208.044		213.971		89.1419766674

		207.121		206.529		208.367		214.298		89.1179103382

		207.483		206.868		208.708		214.595		89.0941375009

		207.851		207.194		209.055		214.914		89.061559909

		208.218		207.506		209.401		215.227		89.0322107271

		208.588		207.831		209.728		215.532		88.9961112334

		208.957		208.146		210.066		215.841		88.970870937

		209.324		208.452		210.43		216.165		88.943282706

		209.698		208.763		210.765		216.498		88.922151295

		210.08		209.074		211.109		216.829		88.9021938513

		210.451		209.396		211.45		217.15		88.8866387849

		210.824		209.714		211.801		217.483		88.8763665713

		211.205		210.023		212.124		217.797		88.8537677012

		211.59		210.331		212.481		218.102		88.8294078803

		211.957		210.662		212.809		218.423		88.8062220266

		212.347		210.999		213.171		218.747		88.781275222

		212.723		211.334		213.497		219.074		88.7501650891

		213.123		211.679		213.836		219.404		88.7255117764

		213.529		211.985		214.166		219.726		88.7055543327

		213.94		212.311		214.525		220.029		88.6744441999

		214.34		212.632		214.843		220.342		88.6533127889

		214.754		212.96		215.198		220.656		88.6295399516

		215.148		213.276		215.549		220.974		88.6092890161

		215.538		213.635		215.885		221.306		88.583461736

		215.953		213.956		216.221		221.637		88.5676131778

		216.363		214.271		216.577		221.98		88.5491231932

		216.779		214.596		216.919		222.304		88.5285787659

		217.213		214.915		217.246		222.642		88.5083278304

		217.646		215.218		217.601		222.963		88.4898378458

		218.067		215.546		217.939		223.299		88.4745762712

		218.512		215.851		218.281		223.602		88.4522708929

		218.949		216.175		218.622		223.91		88.4378897938

		219.359		216.507		218.983		224.227		88.4179323501

		219.792		216.867		219.334		224.549		88.3994423655

		220.218		217.183		219.668		224.865		88.3838872991

		220.643		217.523		220.016		225.221		88.3621689045

		221.082		217.853		220.362		225.579		88.3395700345

		221.517		218.181		220.696		225.901		88.3187321153

		221.953		218.486		221.032		226.221		88.3031770489

		222.426		218.824		221.39		226.536		88.2747083425

		222.874		219.165		221.738		226.848		88.2570988334

		223.3		219.499		222.091		227.167		88.2374348815

		223.756		219.826		222.46		227.48		88.2189448969

		224.205		220.185		222.789		227.826		88.1972265023

		224.626		220.528		223.123		228.156		88.1790300095

		225.091		220.861		223.469		228.49		88.165235894

		225.567		221.202		223.802		228.809		88.1449849585

		226.023		221.552		224.14		229.146		88.1338322694

		226.476		221.866		224.503		229.457		88.1124073666

		226.937		222.218		224.838		229.784		88.095678333

		227.394		222.549		225.194		230.091		88.0707315284

		227.852		222.879		225.547		230.413		88.0560569374

		228.322		223.215		225.882		230.728		88.0314036246

		228.81		223.539		226.215		231.043		88.0111526891

		229.292		223.87		226.575		231.371		87.99031477

		229.743		224.206		226.882		231.697		87.9712378017

		230.213		224.555		227.237		232.02		87.9480519481

		230.679		224.886		227.567		232.356		87.9260400616

		231.122		225.239		227.907		232.679		87.9090175361

		231.57		225.557		228.253		233.008		87.8893535843

		232.029		225.89		228.595		233.345		87.8758529606

		232.478		226.215		228.914		233.68		87.8597109106

		232.914		226.547		229.266		233.998		87.8421014014

		233.349		226.878		229.612		234.35		87.8259593514

		233.791		227.2		229.934		234.658		87.8068823832

		234.198		227.532		230.283		234.99		87.7878054149

		234.62		227.848		230.629		235.313		87.7652065449

		235.039		228.184		230.969		235.653		87.7481840194

		235.457		228.514		231.284		235.977		87.7264656248

		235.85		228.868		231.627		236.326		87.7079756402

		236.249		229.213		231.961		236.657		87.6859637538

		236.63		229.557		232.303		236.992		87.670995671

		237.012		229.883		232.645		237.324		87.6525056864

		237.373		230.227		232.998		237.644		87.6325482427

		237.737		230.546		233.332		237.973		87.6146452418

		238.102		230.882		233.669		238.307		87.5952747817

		238.446		231.194		234.002		238.644		87.5744368626

		238.766		231.533		234.334		238.981		87.5538924352

		239.103		231.849		234.683		239.322		87.534815467

		239.423		232.2		235.048		239.651		87.5139775479

		239.753		232.518		235.415		239.958		87.4934331206

		240.084		232.864		235.757		240.295		87.4767040869

		240.404		233.206		236.102		240.636		87.4529312495

		240.721		233.553		236.447		240.976		87.4388436422

		241.022		233.885		236.779		241.314		87.4235820676

		241.32		234.231		237.107		241.683		87.4077335094

		241.609		234.572		237.456		242.005		87.3907109839

		241.955		234.903		237.797		242.335		87.3739819503

		242.222		235.245		238.131		242.678		87.3551984738

		242.56		235.569		238.472		243.021		87.3381759483

		242.826		235.918		238.808		243.344		87.3196859638

		243.124		236.253		239.165		243.694		87.3067723237

		243.389		236.589		239.506		244.032		87.2929782082

		243.714		236.923		239.864		244.355		87.27712965

		244.008		237.284		240.204		244.691		87.2562917309

		244.305		237.61		240.563		245.021		87.2389757136

		244.559		237.965		240.897		245.351		87.2137354171

		244.902		238.3		241.265		245.698		87.192897498

		245.196		238.639		241.597		246.037		87.1679506934

		245.481		238.959		241.939		246.379		87.1462322988

		245.817		239.298		242.282		246.721		87.1286227896

		246.107		239.636		242.619		247.058		87.1092523296

		246.407		239.983		242.93		247.384		87.0969256732

		246.691		240.329		243.259		247.741		87.0884144104

		246.982		240.678		243.612		248.077		87.0763812459

		247.269		241.025		243.947		248.428		87.0555433267

		247.583		241.358		244.31		248.768		87.0370533421

		247.896		241.702		244.673		249.114		87.0126935212

		248.214		242.047		245.041		249.435		86.9900946511

		248.518		242.39		245.377		249.784		86.9689632401

		248.798		242.731		245.73		250.114		86.9534081737

		249.083		243.065		246.067		250.467		86.9325702546

		249.417		243.399		246.41		250.815		86.9178956637

		249.726		243.751		246.764		251.179		86.8958837772

		250.007		244.102		247.125		251.509		86.8785677599

		250.341		244.447		247.478		251.865		86.8603712672

		250.641		244.784		247.837		252.206		86.8468706435

		250.953		245.136		248.191		252.544		86.8304351016

		251.291		245.47		248.526		252.862		86.8154670189

		251.572		245.807		248.876		253.204		86.7963900506

		251.872		246.165		249.226		253.543		86.7790740333

		252.186		246.521		249.569		253.873		86.7570621469

		252.489		246.869		249.93		254.209		86.7385721623

		252.799		247.211		250.291		254.556		86.7183212268

		253.101		247.552		250.639		254.914		86.7024726686

		253.446		247.891		250.981		255.24		86.6822217331

		253.71		248.254		251.324		255.586		86.6672536503

		254.057		248.602		251.655		255.931		86.649937633

		254.359		248.95		252.004		256.284		86.6343825666

		254.647		249.308		252.354		256.615		86.6147186147

		254.972		249.651		252.689		256.957		86.6006310074

		255.302		250		253.04		257.302		86.5853694328

		255.616		250.345		253.405		257.651		86.5674664319

		255.927		250.707		253.758		257.992		86.54780248

		256.227		251.058		254.106		258.344		86.5301929709

		256.554		251.405		254.467		258.697		86.5075941008

		256.814		251.75		254.784		259.035		86.4858757062

		257.157		252.084		255.116		259.387		86.4632768362

		257.439		252.424		255.461		259.719		86.4444933597

		257.77		252.777		255.793		260.068		86.4254163915

		258.102		253.129		256.141		260.417		86.4089808497

		258.417		253.466		256.515		260.766		86.3910778487

		258.729		253.834		256.862		261.078		86.3758162741

		259.067		254.171		257.19		261.423		86.354978355

		259.367		254.497		257.551		261.745		86.3353144031

		259.683		254.835		257.904		262.08		86.3115415658

		259.99		255.183		258.25		262.421		86.2939320566

		260.293		255.527		258.598		262.778		86.2742681048

		260.601		255.886		258.954		263.131		86.2584195466

		260.91		256.245		259.306		263.477		86.2387555947

		261.215		256.583		259.643		263.818		86.2240810037

		261.538		256.921		259.992		264.157		86.2035365764

		261.896		257.266		260.342		264.491		86.1824051655

		262.169		257.619		260.711		264.837		86.1595128036

		262.526		257.955		261.062		265.179		86.1380879008

		262.836		258.314		261.409		265.542		86.1149020471

		263.156		258.69		261.759		265.901		86.0881942916

		263.465		259.038		262.116		266.262		86.069704307

		263.75		259.388		262.453		266.608		86.0500403551

		264.062		259.742		262.788		266.958		86.0312568787

		264.424		260.114		263.145		267.287		86.0133538778

		264.715		260.444		263.494		267.629		85.9980923032

		265.079		260.796		263.838		267.958		85.9754934331

		265.413		261.141		264.168		268.29		85.954655514

		265.729		261.495		264.529		268.649		85.9361655294

		266.062		261.841		264.878		269		85.9153276102

		266.393		262.203		265.227		269.33		85.8933157238

		266.698		262.549		265.59		269.674		85.8695428865

		267.017		262.907		265.957		270.034		85.8448895737

		267.363		263.271		266.282		270.37		85.81847531

		267.644		263.619		266.624		270.717		85.7935285054

		267.969		263.977		266.973		271.07		85.771516619

		268.348		264.338		267.316		271.415		85.7547875853

		268.672		264.676		267.675		271.739		85.7395260107

		268.978		265.024		268.033		272.08		85.7236774525

		269.346		265.388		268.386		272.425		85.7119377797

		269.655		265.734		268.754		272.767		85.6949152542

		269.954		266.083		269.094		273.121		85.675838286

		270.324		266.446		269.421		273.468		85.656467826

		270.655		266.809		269.776		273.803		85.638564825

		270.975		267.152		270.132		274.141		85.6162594468

		271.297		267.513		270.46		274.471		85.5974759704

		271.637		267.888		270.796		274.811		85.5742901167

		271.944		268.257		271.16		275.159		85.5522782302

		272.28		268.615		271.502		275.51		85.5308533275

		272.602		268.971		271.838		275.854		85.5070804901

		272.94		269.33		272.201		276.2		85.4868295546

		273.259		269.677		272.558		276.548		85.4677525864

		273.603		270.029		272.902		276.901		85.44896911

		273.927		270.383		273.259		277.253		85.431066109

		274.284		270.758		273.619		277.605		85.4069997799

		274.638		271.116		273.954		277.961		85.3782375816

		274.977		271.47		274.309		278.321		85.3541712525

		275.338		271.828		274.66		278.668		85.3312788906

		275.681		272.199		274.998		279.03		85.3054516105

		276.023		272.551		275.346		279.378		85.2898965441

		276.363		272.911		275.704		279.733		85.2734610023

		276.712		273.296		276.047		280.051		85.2567319686

		277.041		273.668		276.396		280.388		85.2358940495

		277.383		274.027		276.764		280.724		85.2176975567

		277.742		274.395		277.117		281.062		85.1968596375

		278.094		274.766		277.466		281.415		85.1771956857

		278.453		275.108		277.831		281.775		85.1560642747

		278.808		275.468		278.184		282.143		85.1343458801

		279.176		275.845		278.54		282.5		85.110279551

		279.516		276.218		278.889		282.866		85.0882676645

		279.864		276.583		279.264		283.224		85.0686037127

		280.203		276.963		279.631		283.583		85.0498202363

		280.559		277.335		279.983		283.944		85.0295693008

		280.908		277.708		280.346		284.285		85.0101988407

		281.277		278.099		280.729		284.622		84.9873064788

		281.638		278.489		281.093		284.976		84.9652945924

		282.007		278.876		281.46		285.313		84.9418152469

		282.357		279.262		281.824		285.641		84.9162814587

		282.711		279.644		282.188		286.001		84.8925086213

		283.055		280.013		282.53		286.356		84.868735784

		283.406		280.376		282.874		286.698		84.8434954876

		283.748		280.759		283.232		287.064		84.818548683

		284.114		281.145		283.6		287.418		84.8012326656

		284.462		281.518		283.952		287.761		84.7803947465

		284.8		281.913		284.314		288.109		84.7648396801

		285.15		282.31		284.691		288.457		84.7445887446

		285.511		282.698		285.049		288.802		84.7246313009

		285.859		283.085		285.431		289.161		84.6990975127

		286.213		283.478		285.803		289.503		84.6753246753

		286.571		283.854		286.161		289.849		84.645095018

		286.917		284.247		286.514		290.205		84.6201482134

		287.262		284.63		286.89		290.551		84.593146966

		287.608		285.011		287.24		290.88		84.5714285714

		287.943		285.414		287.616		291.234		84.5482427177

		288.297		285.817		288.004		291.58		84.5259373395

		288.637		286.199		288.393		291.908		84.5039254531

		288.985		286.589		288.749		292.241		84.4839680094

		289.321		286.984		289.145		292.591		84.4601951721

		289.672		287.343		289.504		292.946		84.4355418593

		290.008		287.715		289.872		293.292		84.4141169565

		290.362		288.094		290.23		293.649		84.3885831682

		290.7		288.47		290.591		294.011		84.3639298555

		291.033		288.847		290.913		294.371		84.3410374936

		291.363		289.242		291.257		294.696		84.3169711644

		291.691		289.63		291.594		295.052		84.2934918189

		292.018		290.006		291.94		295.4		84.2682515225

		292.348		290.391		292.303		295.762		84.2397828161

		292.69		290.746		292.683		296.091		84.2092596669

		293.036		291.088		293.059		296.45		84.1813779441

		293.387		291.446		293.431		296.806		84.1493873358

		293.735		291.805		293.806		297.171		84.1241470394

		294.091		292.149		294.18		297.511		84.1018416612

		294.441		292.525		294.545		297.874		84.0780688238

		294.775		292.911		294.912		298.225		84.0510675765

		295.126		293.254		295.294		298.576		84.0264142637

		295.449		293.634		295.661		298.921		83.9982390491

		295.775		294.013		296.021		299.269		83.9636070145

		296.112		294.366		296.393		299.608		83.9342578326

		296.452		294.71		296.773		299.966		83.9081370607

		296.77		295.093		297.14		300.302		83.8796683542

		297.128		295.432		297.511		300.624		83.8558955169

		297.467		295.768		297.889		300.967		83.8327096632

		297.793		296.118		298.246		301.349		83.8060019077

		298.13		296.473		298.604		301.71		83.7792941522

		298.483		296.817		298.981		302.067		83.7528798885

		298.808		297.172		299.346		302.431		83.7220632475

		299.147		297.533		299.722		302.788		83.6941815247

		299.491		297.898		300.09		303.114		83.6707021792

		299.832		298.252		300.458		303.453		83.6419399809

		300.172		298.607		300.806		303.82		83.6122973072

		300.495		298.958		301.177		304.181		83.583535109

		300.835		299.297		301.529		304.552		83.5530119598

		301.162		299.626		301.892		304.904		83.5177929415

		301.487		299.963		302.257		305.263		83.4852153496

		301.809		300.303		302.626		305.601		83.4543987086

		302.151		300.645		302.987		305.957		83.4224081004

		302.475		301.007		303.352		306.299		83.3918849512

		302.817		301.357		303.713		306.666		83.3625357693

		303.161		301.717		304.074		307.017		83.3296646856

		303.492		302.071		304.444		307.376		83.2970870937

		303.835		302.424		304.81		307.72		83.2615745836

		304.184		302.757		305.174		308.079		83.2257685817

		304.516		303.086		305.568		308.452		83.1890821043

		304.839		303.437		305.95		308.81		83.1562110206

		305.178		303.78		306.304		309.171		83.1227529533

		305.527		304.118		306.662		309.527		83.0892948859

		305.851		304.467		307.039		309.874		83.0584782449

		306.19		304.836		307.39		310.198		83.0247266857

		306.542		305.177		307.738		310.539		82.9900946511

		306.866		305.516		308.106		310.877		82.9551691247

		307.184		305.871		308.486		311.232		82.9214175655

		307.517		306.22		308.849		311.592		82.8841441045

		307.849		306.556		309.213		311.95		82.8515665126

		308.187		306.907		309.566		312.318		82.8198693961

		308.537		307.248		309.931		312.67		82.7872918042

		308.874		307.578		310.268		313.024		82.7550077042

		309.225		307.914		310.616		313.377		82.7230170959

		309.563		308.258		310.969		313.728		82.6877980776

		309.893		308.597		311.322		314.055		82.6546335021

		310.231		308.936		311.671		314.412		82.6167730575

		310.57		309.283		312.024		314.748		82.5792061046

		310.887		309.625		312.358		315.105		82.5439870864

		311.225		309.965		312.691		315.455		82.5090615599

		311.561		310.283		313.035		315.83		82.4717880989

		311.9		310.615		313.376		316.184		82.4383300316

		312.232		310.952		313.695		316.556		82.4048719642

		312.573		311.279		314.035		316.885		82.3702399296

		312.903		311.617		314.377		317.244		82.3344339277

		313.236		311.952		314.722		317.61		82.299801893

		313.577		312.282		315.042		317.962		82.2639958911

		313.911		312.6		315.392		318.309		82.2299508401

		314.242		312.943		315.74		318.685		82.1920903955

		314.565		313.282		316.084		319.042		82.1580453445

		314.883		313.639		316.426		319.375		82.1237068017

		315.181		313.992		316.766		319.731		82.0911292098

		315.507		314.328		317.106		320.096		82.0562036833

		315.84		314.662		317.438		320.437		82.0233325996

		316.165		314.972		317.785		320.786		81.9892875486

		316.507		315.306		318.128		321.147		81.9555359894

		316.863		315.642		318.469		321.502		81.9209039548

		317.205		315.997		318.824		321.846		81.8877393793

		317.529		316.32		319.153		322.206		81.8536943283

		317.866		316.677		319.477		322.565		81.8175948345

		318.202		317.021		319.801		322.918		81.781201849

		318.533		317.348		320.16		323.286		81.747156798

		318.857		317.673		320.493		323.634		81.7122312716

		319.182		318.018		320.84		323.978		81.6778927287

		319.52		318.34		321.175		324.327		81.6423802187

		319.838		318.656		321.514		324.67		81.6080416758

		320.153		319.004		321.833		325.008		81.5728226576

		320.475		319.341		322.154		325.368		81.5373101475

		320.801		319.682		322.48		325.746		81.5026781128

		321.13		320.034		322.808		326.125		81.4727419473

		321.467		320.366		323.12		326.486		81.4404578472

		321.804		320.697		323.44		326.849		81.4075867635

		322.154		321.031		323.778		327.197		81.374422188

		322.498		321.359		324.101		327.551		81.3453664979

		322.83		321.686		324.444		327.895		81.3104409715

		323.159		322.025		324.789		328.246		81.2766894123

		323.49		322.36		325.126		328.61		81.241470394

		323.818		322.711		325.472		328.972		81.207425343

		324.148		323.058		325.835		329.302		81.1707388657

		324.475		323.408		326.15		329.663		81.1372807983

		324.808		323.759		326.478		330.019		81.1096925673

		325.142		324.102		326.826		330.355		81.0838652873

		325.475		324.423		327.154		330.717		81.0565705481

		325.801		324.761		327.476		331.089		81.0269278744

		326.146		325.084		327.815		331.436		81.0002201189

		326.47		325.424		328.141		331.803		80.9661750679

		326.801		325.743		328.459		332.165		80.9327170005

		327.134		326.085		328.79		332.523		80.9004329004

		327.481		326.432		329.118		332.876		80.8684422922

		327.818		326.782		329.472		333.229		80.8387996185

		328.168		327.099		329.814		333.568		80.8082764693

		328.515		327.462		330.167		333.904		80.779514271

		328.853		327.809		330.474		334.255		80.7486976301

		329.194		328.147		330.819		334.606		80.7187614645

		329.51		328.485		331.141		334.962		80.6814880035

		329.835		328.85		331.473		335.306		80.6474429525

		330.153		329.17		331.806		335.69		80.6125174261

		330.492		329.512		332.173		336.057		80.583461736

		330.817		329.829		332.516		336.403		80.5544060459

		331.163		330.183		332.862		336.744		80.5315136841

		331.508		330.52		333.212		337.101		80.5053929122

		331.864		330.878		333.554		337.448		80.4763372221

		332.198		331.214		333.887		337.792		80.4458140729

		332.551		331.562		334.215		338.148		80.4144104483

		332.895		331.901		334.533		338.531		80.3803653973

		333.237		332.23		334.872		338.861		80.3480812972

		333.571		332.585		335.199		339.199		80.3155037053

		333.907		332.917		335.551		339.582		80.2846870643

		334.245		333.278		335.885		339.906		80.2518159806

		334.604		333.606		336.227		340.269		80.2201188642

		334.95		333.949		336.548		340.612		80.189595715

		335.294		334.272		336.896		340.975		80.1605400249

		335.644		334.605		337.23		341.359		80.1317778267

		335.991		334.936		337.579		341.71		80.1059505466

		336.331		335.268		337.932		342.066		80.0774818402

		336.692		335.605		338.272		342.391		80.0490131338

		337.033		335.934		338.615		342.769		80.0214249028

		337.377		336.293		338.948		343.082		79.9914887373

		337.715		336.639		339.281		343.406		79.962726539

		338.062		336.986		339.63		343.781		79.9322033898

		338.405		337.322		339.99		344.086		79.9054956343

		338.749		337.665		340.321		344.454		79.8799618461

		339.096		337.986		340.671		344.753		79.8488517133

		339.447		338.296		340.999		345.101		79.816861105

		339.786		338.621		341.332		345.484		79.7886858904

		340.117		338.962		341.677		345.784		79.7558148067

		340.467		339.301		342.015		346.148		79.7241176902

		340.816		339.656		342.349		346.499		79.6971164429

		341.166		340.014		342.704		346.877		79.6695282119

		341.508		340.348		343.055		347.224		79.6407660136

		341.857		340.691		343.408		347.629		79.61758016

		342.204		341.015		343.75		347.964		79.5850025681

		342.558		341.331		344.099		348.274		79.5574143371

		342.914		341.659		344.437		348.608		79.5257172206

		343.257		342.003		344.786		348.97		79.4934331206

		343.605		342.336		345.117		349.319		79.4596815614

		343.935		342.685		345.466		349.697		79.4320933304

		344.256		343.039		345.803		350.025		79.4012766894

		344.585		343.369		346.161		350.37		79.3754494093

		344.929		343.706		346.51		350.742		79.3519700638

		345.264		344.031		346.86		351.05		79.3211534228

		345.604		344.368		347.2		351.438		79.2906302737

		345.945		344.692		347.547		351.742		79.2612810918

		346.276		345.026		347.889		352.126		79.2325188935

		346.609		345.358		348.221		352.426		79.2014087607

		346.942		345.704		348.556		352.816		79.1755814807

		347.279		346.051		348.909		353.138		79.1518086433

		347.617		346.39		349.256		353.517		79.1236334287

		347.952		346.729		349.606		353.856		79.097219165

		348.286		347.084		349.955		354.219		79.0672829995

		348.62		347.419		350.302		354.589		79.0338249321

		348.962		347.739		350.652		354.896		78.9947905202

		349.312		348.066		351.003		355.213		78.9581040428

		349.646		348.404		351.336		355.614		78.9208305818

		349.991		348.713		351.679		355.966		78.889720449

		350.326		349.037		352.026		356.293		78.8627192017

		350.67		349.389		352.365		356.636		78.8424682662

		350.998		349.741		352.719		357.006		78.8219238389

		351.355		350.088		353.092		357.37		78.8010859197

		351.69		350.434		353.447		357.717		78.774671656

		352.045		350.787		353.804		358.061		78.7447354905

		352.387		351.119		354.17		358.383		78.7130383741

		352.744		351.458		354.515		358.718		78.6801672903

		353.079		351.795		354.855		359.076		78.6452417639

		353.428		352.144		355.208		359.442		78.6167730575

		353.766		352.474		355.551		359.748		78.5935872038

		354.118		352.822		355.887		360.09		78.5683469073

		354.462		353.171		356.245		360.448		78.54134566

		354.815		353.519		356.598		360.781		78.5163988554

		355.16		353.863		356.94		361.174		78.4849952308

		355.508		354.225		357.296		361.53		78.4491892289

		355.856		354.564		357.656		361.867		78.4127962433

		356.195		354.905		357.999		362.16		78.3787511923

		356.544		355.247		358.351		362.51		78.3426516986

		356.904		355.581		358.719		362.839		78.3109545821

		357.248		355.91		359.091		363.208		78.2810184166

		357.593		356.239		359.441		363.533		78.2566585956

		357.961		356.573		359.815		363.924		78.2320052829

		358.316		356.9		360.168		364.212		78.205884511

		358.671		357.262		360.531		364.598		78.1771223127

		359.039		357.609		360.87		364.887		78.1468926554

		359.398		357.982		361.227		365.211		78.1110866535

		359.726		358.333		361.545		365.556		78.0758676352

		360.079		358.696		361.887		365.941		78.038887666

		360.413		359.031		362.218		366.297		78.0063100741

		360.746		359.37		362.582		366.621		77.9728520068

		361.084		359.693		362.93		366.974		77.9426223494

		361.429		360.015		363.297		367.327		77.910925233

		361.752		360.35		363.652		367.703		77.886565412

		362.106		360.682		364.007		368.006		77.8560422628

		362.463		361.016		364.336		368.393		77.8275735564

		362.821		361.347		364.681		368.738		77.7985178663

		363.162		361.707		365.027		369.09		77.7709296353

		363.516		362.052		365.375		369.467		77.7380585516

		363.86		362.404		365.716		369.836		77.7104703206

		364.199		362.765		366.074		370.183		77.6811211387

		364.524		363.122		366.438		370.551		77.6520654487

		364.877		363.474		366.806		370.887		77.6203683322

		365.222		363.818		367.181		371.198		77.5872037567

		365.566		364.156		367.542		371.523		77.5546261648

		365.914		364.496		367.92		371.864		77.5155917529

		366.264		364.847		368.275		372.204		77.4730354391

		366.629		365.183		368.628		372.551		77.4295986499

		366.988		365.527		368.976		372.912		77.3940861398

		367.346		365.869		369.353		373.265		77.353290777

		367.69		366.197		369.701		373.608		77.3201262015

		368.039		366.543		370.053		373.958		77.2896030523

		368.378		366.893		370.423		374.308		77.2611343459

		368.711		367.236		370.798		374.677		77.2267958031

		369.046		367.585		371.157		375.03		77.197740113

		369.403		367.954		371.508		375.388		77.1666299802

		369.752		368.289		371.878		375.714		77.1343458801

		370.1		368.643		372.233		376.051		77.0994203537

		370.477		368.997		372.588		376.388		77.0671362536

		370.83		369.361		372.951		376.727		77.0298627926

		371.183		369.726		373.308		377.059		76.9914153643

		371.523		370.085		373.668		377.427		76.9559028542

		371.871		370.434		374.034		377.795		76.9212708196

		372.212		370.787		374.395		378.127		76.8866387849

		372.566		371.119		374.753		378.485		76.8490718321

		372.899		371.46		375.119		378.826		76.8147332893

		373.255		371.805		375.478		379.156		76.7768728447

		373.602		372.152		375.835		379.494		76.7360774818

		373.958		372.503		376.204		379.856		76.695282119

		374.306		372.879		376.562		380.187		76.6577151662

		374.663		373.221		376.912		380.53		76.6195612297

		375.017		373.586		377.275		380.863		76.577004916

		375.368		373.961		377.639		381.214		76.539731455

		375.691		374.335		378.005		381.541		76.5009905349

		376.028		374.682		378.379		381.884		76.4654780248

		376.374		375.034		378.757		382.255		76.427911072

		376.717		375.376		379.11		382.621		76.3976814146

		377.052		375.719		379.475		382.958		76.3627558882

		377.401		376.055		379.818		383.329		76.3251889354

		377.749		376.405		380.165		383.675		76.2838065889

		378.116		376.762		380.52		384.012		76.2406632915

		378.467		377.102		380.883		384.351		76.1919436496

		378.835		377.447		381.221		384.701		76.1508547949

		379.19		377.797		381.598		385.03		76.111820383

		379.535		378.154		381.949		385.371		76.071318512

		379.847		378.51		382.314		385.725		76.0343385428

		380.178		378.875		382.671		386.079		75.9979455573

		380.518		379.24		383.054		386.43		75.956269719

		380.855		379.61		383.426		386.776		75.9122459461

		381.213		379.965		383.806		387.118		75.8717440751

		381.567		380.32		384.17		387.446		75.8341771223

		381.927		380.686		384.541		387.784		75.8004255631

		382.278		381.032		384.899		388.124		75.7625651185

		382.648		381.384		385.244		388.472		75.727639592

		382.993		381.733		385.6		388.822		75.6874312129

		383.361		382.101		385.952		389.179		75.6457553746

		383.713		382.456		386.331		389.532		75.6011446181

		384.045		382.821		386.694		389.864		75.5638711571

		384.372		383.177		387.049		390.217		75.5207278597

		384.713		383.542		387.399		390.564		75.4793455132

		385.058		383.892		387.765		390.904		75.4350282486

		385.395		384.256		388.104		391.257		75.3910044758

		385.76		384.604		388.457		391.611		75.3434588011

		386.134		384.969		388.821		391.934		75.301489471

		386.487		385.327		389.184		392.287		75.2574656981

		386.851		385.681		389.547		392.632		75.2143224008

		387.214		386.036		389.898		392.97		75.1752879888

		387.554		386.411		390.262		393.326		75.1318511996

		387.892		386.767		390.597		393.685		75.0890013941

		388.234		387.127		390.962		394.019		75.0496734904

		388.572		387.5		391.315		394.367		75.006530193

		388.922		387.872		391.678		394.716		74.9601584856

		389.279		388.232		392.037		395.049		74.9193631228

		389.629		388.607		392.399		395.397		74.8753393499

		389.992		388.989		392.742		395.744		74.8310220853

		390.344		389.349		393.062		396.083		74.7878787879

		390.687		389.718		393.4		396.416		74.7441485069

		391.029		390.08		393.73		396.766		74.6954288649

		391.366		390.43		394.081		397.097		74.6481766821

		391.697		390.779		394.432		397.432		74.599750532

		392.044		391.142		394.818		397.768		74.5545527918

		392.391		391.477		395.175		398.122		74.5096485435

		392.74		391.821		395.53		398.468		74.4679727053

		393.094		392.174		395.895		398.812		74.4257098833

		393.461		392.539		396.239		399.17		74.3843275369

		393.8		392.896		396.581		399.515		74.3397167804

		394.153		393.283		396.915		399.841		74.2942255485

		394.497		393.655		397.263		400.156		74.2499082838

		394.851		394.026		397.595		400.505		74.202656101

		395.198		394.383		397.942		400.827		74.1551104263

		395.549		394.749		398.269		401.179		74.1096191944

		395.897		395.091		398.634		401.523		74.0638344706

		396.248		395.459		398.985		401.892		74.0133538778

		396.619		395.82		399.338		402.247		73.9699170886

		396.968		396.189		399.667		402.62		73.9282412503

		397.31		396.553		400.029		402.961		73.8804020838

		397.658		396.931		400.362		403.31		73.8357913273

		398.02		397.301		400.699		403.662		73.7955829481

		398.353		397.672		401.035		404.004		73.7509721917

		398.707		398.03		401.397		404.337		73.7031330252

		399.086		398.392		401.728		404.694		73.6611636951

		399.445		398.745		402.083		405.068		73.6144984959

		399.791		399.098		402.42		405.425		73.5734096412

		400.145		399.445		402.75		405.769		73.5346687211

		400.504		399.808		403.087		406.127		73.4971017683

		400.848		400.17		403.434		406.459		73.4583608482

		401.212		400.547		403.779		406.801		73.4210873872

		401.557		400.916		404.13		407.139		73.377650598

		401.896		401.285		404.496		407.489		73.330691907

		402.246		401.657		404.837		407.818		73.285200675

		402.58		402.039		405.193		408.167		73.2370680167

		402.907		402.396		405.522		408.494		73.1942182112

		403.26		402.759		405.856		408.844		73.1510749138

		403.625		403.124		406.186		409.199		73.1076381246

		403.961		403.474		406.528		409.559		73.0636143517

		404.327		403.817		406.841		409.899		73.0245799398

		404.684		404.175		407.192		410.247		72.9840780688

		405.029		404.53		407.525		410.581		72.943282706

		405.38		404.882		407.848		410.897		72.9030743268

		405.718		405.237		408.179		411.24		72.8619854722

		406.058		405.608		408.534		411.604		72.8194291584

		406.404		405.973		408.865		411.955		72.7745249101

		406.751		406.344		409.196		412.315		72.73255558

		407.101		406.734		409.548		412.664		72.6926406926

		407.478		407.118		409.88		413.01		72.6562477071

		407.828		407.485		410.215		413.332		72.6201482134

		408.191		407.849		410.537		413.676		72.5843422115

		408.544		408.212		410.889		414.006		72.5447208159

		408.895		408.564		411.211		414.358		72.5042189449

		409.222		408.907		411.546		414.699		72.4625431066

		409.574		409.251		411.871		415.066		72.4226282192

		409.911		409.617		412.215		415.41		72.3821263482

		410.269		409.983		412.552		415.769		72.3401570181

		410.609		410.341		412.902		416.132		72.3005356226

		410.976		410.712		413.246		416.478		72.2617947025

		411.32		411.094		413.597		416.825		72.2201188642

		411.662		411.447		413.933		417.172		72.1843128623

		411.993		411.8		414.246		417.5		72.1537897131

		412.332		412.152		414.571		417.823		72.1232665639

		412.678		412.514		414.895		418.153		72.0912759557

		413.022		412.871		415.205		418.493		72.0610462983

		413.372		413.234		415.524		418.85		72.0296426737

		413.733		413.593		415.872		419.215		71.9964780982

		414.083		413.954		416.204		419.582		71.9639005063

		414.424		414.311		416.545		419.949		71.9313229144

		414.78		414.667		416.892		420.306		71.9019737325

		415.125		415.041		417.233		420.639		71.8688091569

		415.472		415.388		417.565		420.992		71.8374055323

		415.837		415.752		417.89		421.336		71.8030669895

		416.182		416.108		418.207		421.695		71.7704893976

		416.519		416.451		418.519		422.043		71.7376183139

		416.861		416.796		418.845		422.39		71.7056277056

		417.211		417.175		419.168		422.728		71.6712891628

		417.55		417.531		419.507		423.063		71.6416464891

		417.909		417.889		419.842		423.384		71.6128842909

		418.266		418.262		420.193		423.732		71.5882309781

		418.622		418.626		420.531		424.087		71.5644581407

		418.967		418.976		420.854		424.427		71.5415657789

		419.304		419.346		421.191		424.786		71.5192604006

		419.643		419.714		421.513		425.161		71.4966615306

		419.982		420.073		421.821		425.496		71.4687798078

		420.341		420.439		422.143		425.844		71.4394306259

		420.692		420.814		422.49		426.198		71.4121358867

		421.044		421.169		422.82		426.542		71.3830801966

		421.382		421.536		423.17		426.883		71.3528505393

		421.732		421.893		423.541		427.227		71.3217404065

		422.071		422.242		423.879		427.566		71.2941521755

		422.422		422.583		424.223		427.918		71.2724337809

		422.76		422.933		424.546		428.265		71.2454325336

		423.103		423.269		424.866		428.611		71.2216596962

		423.448		423.627		425.179		428.969		71.1975933671

		423.795		423.992		425.504		429.323		71.1761684643

		424.12		424.348		425.83		429.654		71.1471127742

		424.477		424.715		426.173		430.006		71.124807396

		424.825		425.081		426.523		430.354		71.1010345587

		425.152		425.437		426.859		430.702		71.0819575904

		425.473		425.788		427.202		431.035		71.0578912613

		425.815		426.161		427.543		431.385		71.0382273094

		426.15		426.514		427.886		431.734		71.0144544721

		426.5		426.872		428.227		432.068		70.9903881429

		426.861		427.238		428.578		432.403		70.9651478465

		427.219		427.587		428.905		432.761		70.9402010419

		427.565		427.941		429.229		433.11		70.9178956637

		427.915		428.293		429.559		433.436		70.8967642527

		428.241		428.648		429.887		433.787		70.8750458581

		428.569		429.009		430.212		434.132		70.8533274635

		428.899		429.381		430.569		434.471		70.8319025607

		429.244		429.733		430.889		434.815		70.8110646416

		429.577		430.096		431.215		435.175		70.7931616406

		429.916		430.466		431.558		435.529		70.774671656

		430.268		430.813		431.897		435.879		70.7579426223

		430.623		431.164		432.227		436.22		70.7397461296

		430.957		431.529		432.577		436.548		70.7162667841

		431.307		431.871		432.917		436.883		70.6922004549

		431.669		432.188		433.255		437.209		70.6716560276

		432.009		432.537		433.585		437.564		70.6502311248

		432.345		432.872		433.937		437.918		70.6282192384

		432.689		433.226		434.285		438.266		70.6050333847

		433.021		433.599		434.648		438.605		70.5821410228

		433.355		433.975		434.989		438.954		70.5569007264

		433.688		434.33		435.339		439.283		70.5310734463

		434.043		434.692		435.677		439.624		70.5090615599

		434.384		435.041		436.019		439.965		70.4896910999

		434.732		435.385		436.343		440.311		70.470027148

		435.073		435.732		436.671		440.647		70.452124147

		435.419		436.086		437.001		440.963		70.435982097

		435.745		436.446		437.343		441.295		70.4163181451

		436.083		436.803		437.67		441.638		70.3951867342

		436.406		437.145		438.007		441.992		70.3731748478

		436.74		437.496		438.356		442.336		70.3511629613

		437.07		437.852		438.695		442.713		70.3276836158

		437.412		438.198		439.011		443.065		70.3042042703

		437.746		438.562		439.343		443.407		70.2813119084

		438.09		438.909		439.692		443.751		70.2607674811

		438.43		439.22		440.023		444.094		70.238168611

		438.765		439.552		440.366		444.438		70.215569741

		439.089		439.905		440.726		444.769		70.19766674

		439.412		440.222		441.091		445.117		70.1753613618

		439.733		440.565		441.435		445.445		70.1536429672

		440.061		440.908		441.8		445.792		70.1325115562

		440.389		441.255		442.158		446.135		70.110206178

		440.723		441.618		442.509		446.478		70.0861398489

		441.061		442.014		442.857		446.823		70.0644214543

		441.421		442.346		443.196		447.183		70.0385941742

		441.769		442.696		443.537		447.525		70.0098319759

		442.113		443.078		443.885		447.867		69.9834177122

		442.454		443.387		444.209		448.236		69.9584709076

		442.804		443.744		444.549		448.581		69.9382199721

		443.131		444.076		444.901		448.912		69.9194364957

		443.448		444.424		445.239		449.252		69.902707462

		443.783		444.769		445.573		449.592		69.8821630347

		444.113		445.087		445.93		449.916		69.8607381319

		444.451		445.494		446.277		450.258		69.836378311

		444.797		445.855		446.632		450.605		69.8117249982

		445.149		446.178		447.002		450.952		69.7882456527

		445.495		446.54		447.35		451.295		69.7653532908

		445.833		446.891		447.708		451.629		69.7424609289

		446.162		447.275		448.06		451.98		69.7230904689

		446.493		447.57		448.412		452.32		69.6981436642

		446.809		447.927		448.728		452.66		69.6752513024

		447.149		448.265		449.08		453.024		69.651478465

		447.488		448.634		449.429		453.395		69.6253576932

		447.84		448.952		449.783		453.733		69.5965954949

		448.175		449.276		450.134		454.084		69.573703133

		448.531		449.596		450.508		454.417		69.5458214102

		448.851		449.97		450.867		454.746		69.5194071465

		449.199		450.32		451.214		455.085		69.4891774892

		449.516		450.695		451.568		455.445		69.4621762418

		449.832		451.04		451.913		455.792		69.4340010272

		450.179		451.363		452.27		456.156		69.4081737472

		450.531		451.714		452.63		456.491		69.3802920244

		450.854		452.086		453.001		456.835		69.3553452198

		451.206		452.387		453.344		457.168		69.3239415951

		451.563		452.715		453.713		457.511		69.291657495

		451.892		453.045		454.075		457.862		69.2605473622

		452.223		453.389		454.438		458.205		69.2297307213

		452.569		453.762		454.798		458.552		69.1968596375

		452.921		454.097		455.176		458.901		69.163695062

		453.265		454.399		455.536		459.247		69.1287695355

		453.608		454.742		455.877		459.582		69.0938440091

		453.966		455.084		456.227		459.944		69.0595054663

		454.303		455.433		456.567		460.281		69.0327977108

		454.64		455.791		456.912		460.622		69.0075574143

		454.989		456.147		457.277		460.959		68.9823171179

		455.335		456.505		457.644		461.309		68.9541419033

		455.657		456.841		458.005		461.644		68.9230317705

		456.017		457.187		458.377		461.967		68.8857583095

		456.344		457.549		458.742		462.309		68.8502457994

		456.672		457.859		459.077		462.671		68.8159072566

		457.015		458.232		459.421		463.011		68.781275222

		457.377		458.545		459.761		463.361		68.7478171546

		457.719		458.918		460.092		463.726		68.7158265463

		458.066		459.266		460.424		464.067		68.6820749872

		458.427		459.6		460.762		464.391		68.6492039034

		458.758		459.924		461.087		464.731		68.617506787

		459.086		460.235		461.422		465.069		68.5881576051

		459.423		460.578		461.754		465.399		68.5588084232

		459.772		460.912		462.1		465.746		68.5323941595

		460.11		461.282		462.449		466.087		68.5042189449

		460.473		461.605		462.793		466.421		68.4725218285

		460.82		461.937		463.127		466.765		68.4414116956

		461.162		462.27		463.461		467.127		68.4126494974

		461.503		462.603		463.792		467.465		68.37596302

		461.842		462.939		464.108		467.814		68.34690733

		462.178		463.271		464.448		468.155		68.3251889354

		462.519		463.628		464.778		468.471		68.3008291144

		462.852		463.923		465.095		468.795		68.2747083425

		463.163		464.28		465.401		469.13		68.2588597843

		463.499		464.631		465.721		469.467		68.2394893242

		463.824		464.973		466.038		469.822		68.2160099787

		464.168		465.33		466.359		470.193		68.1981069778

		464.506		465.675		466.705		470.538		68.1819649277

		464.876		466.002		467.055		470.89		68.1631814513

		465.224		466.371		467.39		471.238		68.1461589258

		465.573		466.665		467.725		471.572		68.1338322694

		465.911		467.013		468.07		471.905		68.1173967276

		466.256		467.307		468.388		472.244		68.1056570548

		466.589		467.622		468.693		472.589		68.0877540539

		466.92		467.949		469.013		472.92		68.0748404138

		467.244		468.328		469.316		473.275		68.0554699538

		467.588		468.675		469.619		473.624		68.0463717074

		467.911		469.012		469.94		473.977		68.0220118864

		468.261		469.352		470.269		474.322		68.0123266564

		468.605		469.696		470.601		474.681		67.9953041309

		468.974		470.019		470.944		475.01		67.9879668354

		469.313		470.346		471.281		475.34		67.9762271627

		469.675		470.674		471.599		475.701		67.9750531954

		470.008		470.988		471.929		476.033		67.9683028836

		470.331		471.302		472.259		476.358		67.9580306699

		470.635		471.615		472.575		476.719		67.9480519481

		470.964		471.929		472.888		477.073		67.9357252917

		471.29		472.254		473.216		477.412		67.925453078

		471.625		472.599		473.544		477.763		67.9140068971

		471.981		472.916		473.862		478.122		67.9081370607

		472.352		473.249		474.19		478.427		67.8922885025

		472.712		473.572		474.53		478.759		67.8826032724

		473.071		473.883		474.857		479.074		67.870276616

		473.418		474.177		475.181		479.402		67.8585369433

		473.761		474.501		475.492		479.731		67.8459167951

		474.088		474.822		475.82		480.091		67.8391664832

		474.409		475.142		476.131		480.436		67.8283072859

		474.724		475.469		476.452		480.795		67.8183285641

		475.056		475.807		476.796		481.157		67.8077628586

		475.385		476.117		477.134		481.512		67.7954362022

		475.731		476.421		477.482		481.853		67.7869249395

		476.089		476.724		477.817		482.187		67.7766527258

		476.441		477.016		478.152		482.518		67.7687284467

		476.786		477.305		478.463		482.838		67.7590432167

		477.138		477.629		478.805		483.162		67.7555213148

		477.475		477.963		479.113		483.507		67.7431946584

		477.791		478.29		479.441		483.848		67.7349768875

		478.125		478.624		479.771		484.186		67.7226502311

		478.469		478.964		480.109		484.542		67.7120845256

		478.785		479.282		480.427		484.888		67.698583902

		479.116		479.575		480.754		485.238		67.6935945411

		479.48		479.891		481.092		485.593		67.6798004256

		479.818		480.202		481.431		485.929		67.6665932937

		480.152		480.522		481.758		486.259		67.6574950473

		480.51		480.836		482.095		486.592		67.64663585

		480.853		481.173		482.421		486.91		67.6360701445

		481.197		481.499		482.741		487.236		67.6284393573

		481.556		481.816		483.067		487.584		67.6216890454

		481.905		482.13		483.388		487.937		67.6137647663

		482.258		482.463		483.71		488.279		67.6049600117

		482.607		482.761		484.064		488.632		67.5941008144

		482.943		483.083		484.42		488.979		67.5864700271

		483.254		483.414		484.754		489.318		67.580306699

		483.58		483.736		485.103		489.651		67.5668060753

		483.896		484.042		485.443		490.004		67.5588817962

		484.237		484.385		485.771		490.337		67.5453811725

		484.574		484.699		486.089		490.683		67.5318805488

		484.957		485.03		486.422		491.034		67.5142710397

		485.319		485.359		486.753		491.366		67.5069337442

		485.665		485.692		487.081		491.687		67.4934331206

		485.996		486.022		487.394		492.026		67.4849218578

		486.335		486.346		487.727		492.361		67.4761171032

		486.66		486.668		488.073		492.682		67.4649644141

		486.985		486.995		488.404		493.018		67.4532247414

		487.328		487.328		488.737		493.349		67.4429525277

		487.682		487.647		489.095		493.694		67.4306258713

		488.025		487.984		489.425		494.028		67.4203536576

		488.366		488.323		489.729		494.388		67.4144838213

		488.726		488.655		490.036		494.731		67.4059725585

		489.066		488.981		490.355		495.086		67.4001027221

		489.404		489.299		490.664		495.424		67.3948198694

		489.737		489.62		490.983		495.758		67.3842541639

		490.074		489.944		491.306		496.073		67.3780908357

		490.402		490.269		491.657		496.387		67.3698730648

		490.75		490.599		492.004		496.728		67.3610683102

		491.096		490.956		492.343		497.061		67.3493286375

		491.448		491.303		492.673		497.403		67.3487416538

		491.783		491.632		493.002		497.751		67.3378824565

		492.117		491.966		493.306		498.11		67.3281972265

		492.455		492.301		493.607		498.435		67.3158705701

		492.802		492.631		493.907		498.759		67.3058918483

		493.14		492.954		494.217		499.08		67.2923912246

		493.486		493.293		494.552		499.397		67.2806515518

		493.838		493.622		494.888		499.723		67.2750752073

		494.189		493.938		495.221		500.046		67.2639225182

		494.51		494.256		495.565		500.382		67.2539437963

		494.844		494.592		495.905		500.719		67.2407366645

		495.171		494.915		496.274		501.056		67.2263555653

		495.512		495.222		496.583		501.381		67.2146158926

		495.834		495.55		496.92		501.726		67.2087460562

		496.18		495.884		497.285		502.055		67.1987673344

		496.525		496.209		497.609		502.379		67.1887886125

		496.9		496.55		497.901		502.71		67.1796903661

		497.232		496.896		498.211		503.049		67.1729400543

		497.583		497.232		498.531		503.361		67.1635483161

		497.929		497.559		498.876		503.69		67.1594394306

		498.271		497.885		499.183		504.031		67.1550370533

		498.58		498.206		499.481		504.358		67.1497542006

		498.92		498.547		499.779		504.688		67.1383080197

		499.269		498.891		500.106		505.037		67.1253943796

		499.608		499.22		500.398		505.38		67.1124807396

		499.934		499.561		500.753		505.713		67.0989801159

		500.29		499.886		501.146		506.053		67.087533935

		500.641		500.225		501.473		506.379		67.0787291804

		500.98		500.568		501.863		506.705		67.0693374422

		501.329		500.918		502.157		507.01		67.0622936386

		501.689		501.246		502.493		507.331		67.0511409494

		502.039		501.59		502.8		507.649		67.0367598503

		502.388		501.919		503.103		507.963		67.029129063

		502.717		502.224		503.415		508.288		67.0223787512

		503.053		502.558		503.721		508.646		67.0106390784

		503.379		502.893		504.071		508.982		67.0021278157

		503.706		503.222		504.461		509.323		66.9903881429

		504.016		503.539		504.815		509.674		66.9792354538

		504.353		503.886		505.152		510.011		66.9604519774

		504.694		504.206		505.479		510.328		66.9501797637

		505.045		504.542		505.804		510.649		66.9252329591

		505.384		504.87		506.099		510.965		66.9117323355

		505.738		505.229		506.444		511.284		66.8964707609

		506.072		505.577		506.715		511.602		66.8841441045

		506.403		505.908		507.032		511.933		66.8759263336

		506.717		506.244		507.365		512.269		66.8700564972

		507.047		506.575		507.687		512.618		66.8586103162

		507.386		506.868		508.023		512.963		66.8500990535

		507.727		507.155		508.379		513.306		66.836304938

		508.051		507.477		508.715		513.646		66.8263262162

		508.405		507.793		509.036		513.978		66.8095971825

		508.747		508.122		509.36				66.7999119525

		509.088		508.479		509.699				66.7796610169

		509.427		508.822		509.989				66.7667473769

		509.782		509.148		510.336				66.745615966

		510.12		509.486		510.688				66.727712965

		510.454		509.824		511.057				66.7095164722

		510.788		510.157		511.456				66.6960158486

		511.128		510.502		511.767				66.6831022085

		511.47		510.846		512.078				66.6672536503

		511.809		511.164		512.396				66.6631447648

		512.159		511.487		512.753				66.6461222393

		512.511		511.794		513.06				66.6314476484



1

2

3

4

5

6

Temperature (oC)

Weight %

100.0192539291

99.9682068092

99.9813615325

99.9992336554

100.0403954984

99.9783477408

99.9860581667

100.0050578743

100.0596494275

99.9854738008

99.9917818914

100.0160932365

100.0792808846

100.0021926338

100.0004402368

100.0254426406

100.0989123418

100.0063038223

100.0076304962

100.0357116582

100.0940044775

100.0189114669

100.0130595332

100.0406162637

100.0913617813

100.0126076446

100.0154071336

100.0433751042

100.0909842533

100.0087705354

100.0161407474

100.0430685664

100.0868314451

99.9950665738

100.0101249552

100.0419956839

100.0838112209

99.9876664346

100.0076304962

100.0393901123

100.0781483006

99.9802662954

100.0042555408

100.0335658934

100.0773932445

99.9764291861

100.0013207045

100.0335658934

100.0713527962

99.9712216808

99.9986792781

100.0291210947

100.0713527962

99.9703994431

99.998092285

100.0254426406

100.067955044

99.9720439185

99.9961845336

100.0217641866

100.0653123478

99.9594362738

99.9941299913

100.0249828339

100.0554966192

99.9583399569

99.9928091919

100.020997842

100.0536089791

99.9473767877

99.9894337363

100.0214576487

100.051343811

99.9427174408

99.9879661114

100.0202314974

100.0449258346

99.9287394

99.9851775646

100.0179324636

100.0388853863

99.9306579546

99.9828292544

100.0147138163

100.0362426901

99.9191466269

99.9768114578

100.0128745892

100.0369977462

99.9221614984

99.9744629511

100.0105755554

100.0324674099

99.9128428046

99.973288677

100.0102690176

100.03435505

99.9139391215

99.971086876

100.007663446

100.033599994

99.9081834577

99.967270306

100.0055176811

100.0362426901

99.9065389823

99.9658023557

100.0058242189

100.0283146017

99.8985906846

99.9624259881

100.0026055716

100.0283146017

99.8942054169

99.9558197218

100.0006130757

100.0207640412

99.89667213

99.9544984161

100.0013794203

100.0188764011

99.8933831792

99.952443017

99.9995401932

100.0143460648

99.89667213

99.9498002989

99.996168277

100.0135910088

99.8936572584

99.9467170395

99.9941757811

100.0098157286

99.8958498923

99.9456892652

99.9929496297

100.0090606725

99.8848867231

99.9430463685

99.9900375202

100.0052853923

99.8796792177

99.9405502353

99.9877384864

99.999244944

99.8643307807

99.9355577818

99.9862057972

99.9958471918

99.8547380077

99.9321803923

99.9829871499

99.9886741593

99.8462415515

99.9270406677

99.9832936878

99.9852764071

99.8382932538

99.9223412595

99.9825273432

99.9837662951

99.835004303

99.9167604252

99.9829871499

99.983388767

99.83966365

99.9152917328

99.9834469567

99.9856539352

99.8424044423

99.9123542832

99.984826377

99.983011239

99.8382932538

99.9095636261

99.9808413851

99.9796134868

99.8418562838

99.9061853579

99.9840600324

99.9750831505

99.8336339069

99.903982078

99.9825273432

99.9735730385

99.8382932538

99.8984002181

99.9806881161

99.966400006

99.827878243

99.8926711428

99.9802283094

99.9603595577

99.8262337677

99.887823207

99.9799217715

99.9603595577

99.8160928361

99.8810650858

99.9754769729

99.9569618055

99.8149965192

99.875481945

99.9730246702

99.9520539412

99.79334426

99.8731310556

99.9716452499

99.9497887731

99.7960850523

99.8704862388

99.9701125607

99.9520539412

99.7829292492

99.8690168659

99.9664341066

99.9471460769

99.7788180607

99.8672535898

99.9678135269

99.9426157407

99.7716920007

99.8665188823

99.9653612242

99.9380854044

99.7662104161

99.8631391579

99.9636752661

99.9369528203

99.7610029107

99.8597593192

99.9652079553

99.9354427082

99.7634696238

99.8538810664

99.9644416107

99.9350651802

99.7623733069

99.8502069826

99.9627556526

99.9324224841

99.7599065938

99.845650931

99.9621425769

99.9350651802

99.7596325146

99.8422705003

99.959996812

99.930912372

99.7503138207

99.838449006

99.9578510471

99.9278921478

99.7497656623

99.8353623076

99.9547856687

99.9282696758

99.7560694846

99.8312465614

99.9517202904

99.9305348439

99.7546990884

99.8262486414

99.9514137525

99.9297797879

99.7552472469

99.8199273843

99.9492679876

99.9305348439

99.7599065938

99.8124295603

99.9480418363

99.9282696758

99.7470248699

99.8068425801

99.9489614498

99.9263820357

99.7385284138

99.801549363

99.9480418363

99.9233618115

99.7311282746

99.7961088196

99.9475820295

99.9195865313

99.7185206299

99.7921385061

99.9455895336

99.9169438352

99.7092019361

99.7890503753

99.9460493403

99.914301139

99.710298253

99.7852268428

99.9462026093

99.9082606906

99.699609163

99.7803736868

99.9435970376

99.9033528264

99.7034462722

99.7752261421

99.9426774241

99.89693485

99.706735223

99.7697841632

99.9393055079

99.8893842895

99.7026240346

99.7643418875

99.9359335916

99.8844764253

99.7001573215

99.7588993149

99.9331747511

99.8822112571

99.6949498161

99.7527208996

99.9328682133

99.8867415934

99.6850829638

99.7468363388

99.9313355241

99.8833438412

99.6708308438

99.7403629209

99.929496297

99.8837213692

99.6661714969

99.7362432544

99.9301093727

99.8825887852

99.6587713576

99.7302105786

99.9271972632

99.879946089

99.6590454369

99.7250604446

99.9267374565

99.8712629445

99.6500008222

99.7194685694

99.9239786159

99.8712629445

99.6530156938

99.7137292136

99.9241318848

99.8693753044

99.6475341092

99.7074008229

99.9229057335

99.8686202483

99.6431488415

99.7003360983

99.9207599686

99.8640899121

99.635474623

99.6934180705

99.9198403551

99.862957328

99.6288967215

99.6872355968

99.9203001619

99.8595595758

99.6278004045

99.6809055241

99.9170815145

99.8576719357

99.621222503

99.6736916955

99.9155488253

99.8516314873

99.6204002653

99.6682441727

99.914322674

99.8482337351

99.610533413

99.6633853201

99.9114105645

99.844835983

99.6110815715

99.6570537325

99.908498455

99.8395505906

99.5968294515

99.6517525591

99.9054330767

99.8342651983

99.5940886591

99.6454202323

99.9026742361

99.8331326143

99.5833995691

99.6357000641

99.8997621266

99.8331326143

99.5792883807

99.6249478645

99.8977696307

99.8338876703

99.5746290338

99.6152256986

99.8977696307

99.8387955346

99.5691474491

99.6071231689

99.897156555

99.8365303665

99.5718882415

99.5994619891

99.8951640591

99.8403056467

99.5798365391

99.5973992631

99.8936313699

99.8384180066

99.5779179845

99.5947471241

99.8934781009

99.8361528384

99.578466143

99.5913581769

99.8916388739

99.8308674461

99.5809328561

99.5869376378

99.8890333023

99.8308674461

99.5685992907

99.5811906435

99.8879604198

99.8214292456

99.5540730914

99.5723484661

99.8879604198

99.8202966615

99.549961903

99.5649793851

99.8870408063

99.8206741895

99.5398209714

99.5584941427

99.8839754279

99.8202966615

99.5326949114

99.5496499494

99.8829025455

99.8146337412

99.5277614853

99.5427214491

99.8795306293

99.8123685731

99.5181687122

99.5350553124

99.8775381333

99.8078382368

99.5137834445

99.5267988125

99.8787642847

99.7972674522

99.5110426522

99.5175094312

99.878151209

99.793492172

99.5113167314

99.5107261607

99.8753923684

99.7900944198

99.5099463353

99.5009928344

99.8735531414

99.7885843077

99.514331603

99.491406052

99.8718671833

99.7859416115

99.5110426522

99.4827034035

99.8706410319

99.7882067796

99.5061092261

99.4732623815

99.8668093089

99.7855640835

99.5006276414

99.4647056814

99.8646635441

99.7866966676

99.4926793437

99.4589516242

99.8631308549

99.7874517236

99.4806198576

99.4530496813

99.8594524008

99.7844314994

99.4743160353

99.4450815027

99.8576131738

99.7791461071

99.4660936584

99.438736015

99.8570000981

99.777258467

99.4548564099

99.4297335819

99.8513291481

99.7723506027

99.4496489045

99.4199923263

99.8499497278

99.7670652104

99.4444413991

99.4115786556

99.8499497278

99.7648000423

99.4397820522

99.4046405318

99.8473441562

99.7644225143

99.4340263883

99.397406653

99.8439722399

99.7587595939

99.4351227053

99.3897293078

99.8435124332

99.7564944258

99.4315596753

99.3810177556

99.8412133994

99.7481888093

99.4307374376

99.3717147466

99.8415199372

99.7440360011

99.4203224268

99.3609339802

99.8407535926

99.7383730807

99.4195001891

99.3516290906

99.8402937859

99.7376180247

99.4115518914

99.341437021

99.8398339791

99.7338427445

99.4101814953

99.331539373

99.8406003237

99.7342202725

99.4071666237

99.3229704633

99.8364620629

99.7315775763

99.4036035937

99.3157306359

99.8341630291

99.7364854406

99.4005887222

99.3083425129

99.8329368777

99.7364854406

99.3923663453

99.3027271717

99.8269593899

99.7361079126

99.3890773945

99.297111513

99.8234342047

99.7398831928

99.3841439683

99.2875050447

99.8203688263

99.7406382489

99.3792105422

99.2786367105

99.817150179

99.7342202725

99.371810403

99.2685849739

99.8137782628

99.7289348802

99.3676992145

99.2592714272

99.8159240277

99.7289348802

99.3545434114

99.2496612964

99.8130119182

99.7202517357

99.3452247176

99.2428597184

99.8120923047

99.7160989274

99.3408394499

99.2360576742

99.8104063466

99.7108135351

99.3427580045

99.2292551637

99.8082605817

99.7123236472

99.3416616876

99.2223042909

99.8061148168

99.708548367

99.3438543214

99.2155008375

99.8045821276

99.7138337593

99.3454987968

99.207069824

99.8033559763

99.7096809511

99.3485136683

99.1999694674

99.8005971357

99.707793311

99.3397431329

99.1913891917

99.7990644465

99.6983551104

99.3342615483

99.1825122633

99.7953859924

99.6934472461

99.3219279829

99.1742264133

99.7929336897

99.6870292697

99.3079499422

99.1671237051

99.7891019667

99.6900494939

99.2967126937

99.1588365692

99.7877225465

99.6885393818

99.2854754452

99.1517327586

99.7851169748

99.6896719659

99.2819124152

99.1418161718

99.7815917897

99.6870292697

99.2775271475

99.1313064674

99.7815917897

99.6824989335

99.2799938606

99.1215358836

99.7795992937

99.673438261

99.2723196422

99.1110240287

99.7773002599

99.6685303967

99.2758826722

99.0993264288

99.7745414194

99.6651326445

99.2695788499

99.0928107112

99.7743881505

99.6609798362

99.2698529291

99.0859983664

99.769483545

99.6621124203

99.260260156

99.078296891

99.7684106626

99.6640000604

99.2536822545

99.0720760314

99.7661116288

99.6647551164

99.2369634214

99.0657066515

99.7654985531

99.6632450044

99.2257261729

99.0569666032

99.7631995193

99.6655101725

99.2142148452

99.0470405284

99.7607472166

99.6590921961

99.2043479929

99.0360762448

99.7584481828

99.6583371401

99.2040739137

99.0246661745

99.7550762666

99.6488989395

99.1947552198

99.0166635226

99.7512445436

99.6458787153

99.1966737745

99.006585189

99.7475660896

99.6428584912

99.185436526

98.9994704534

99.7460334004

99.6364405148

99.1857106052

98.9938375917

99.7431212909

99.6322877066

99.1763919114

98.9885009008

99.7417418706

99.6387056829

99.1826957337

98.9815331213

99.7417418706

99.6368180428

99.1703621683

98.9758992388

99.7377568787

99.6334202906

99.1706362475

98.9689305721

99.7356111138

99.6356854588

99.160495316

98.9627028377

99.7340784246

99.6307775945

99.1585767614

98.9543985821

99.7316261219

99.6266247862

99.1500803052

98.944907151

99.7274878611

99.6251146741

99.149806226

98.9383812638

99.7285607435

99.6243596181

99.1487099091

98.933486566

99.7262617097

99.6251146741

99.1478876714

98.9275532743

99.7233496003

99.6266247862

99.1495321468

98.9232514152

99.7210505665

99.6247371461

99.146243196

98.9168724522

99.7192113394

99.62209445

99.1421320075

98.9088610788

99.7167590367

99.6171865857

99.1300725214

98.8998104135

99.7129273137

99.6156764736

99.1196575106

98.8904621354

99.7109348178

99.6081259131

99.1018423606

98.8809645671

99.7074096326

99.6077483851

99.096360776

98.8738407921

99.704804061

99.6013304087

99.0815604975

98.86612279

99.7011256069

99.5994427686

99.0799160221

98.8606307677

99.6992863799

99.5907596241

99.0719677244

98.8548415491

99.6966808083

99.589249512

99.064293506

98.8483097159

99.6948415812

99.5820764796

99.0555229706

98.8422228465

99.6936154299

99.5805663675

99.0533303367

98.8353932297

99.6907033204

99.5764135593

99.0462042767

98.8267813011

99.6903967826

99.5733933351

99.0423671675

98.8187626238

99.6888640934

99.5703731109

99.0412708506

98.8111888312

99.6879444799

99.5635776065

99.0316780775

98.8022777436

99.6831931434

99.5601798543

99.021537146

98.7947026871

99.6810473785

99.5567821022

99.0094776598

98.7877212385

99.6776754623

99.5586697423

99.0034479167

98.781184967

99.676296042

99.5560270461

98.9952255398

98.7743511298

99.674303546

99.5605573824

98.9889217175

98.7692997289

99.6732306636

99.5605573824

98.9872772421

98.7629108224

99.6727708568

99.5567821022

98.9806993406

98.757264468

99.670625092

99.5462113175

98.9765881521

98.749983166

99.6663335622

99.5480989576

98.9722028844

98.7425527126

99.6631149149

99.5386607571

98.9694620921

98.7363106995

99.6618887635

99.5284675005

98.9626101113

98.7296223905

99.6586701162

99.5246922203

98.9617878736

98.7214471752

99.6574439649

99.5299776126

98.9530173383

98.7163930671

99.6559112757

99.5269573884

98.9480839121

98.7104467263

99.6500870567

99.5311101967

98.9382170598

98.7028646222

99.6493207121

99.5303551406

98.9362985052

98.6961740466

99.6464086027

99.5326203087

98.9272538906

98.6891856279

99.6436497621

99.5299776126

98.9269798113

98.6805609396

99.6398180391

99.5250697483

98.9187574344

98.6728278194

99.6415039973

99.520161884

98.9195796721

98.667325038

99.6378255432

99.5178967159

98.9110832159

98.6603345758

99.6369059297

99.5095910994

98.9105350575

98.6551285907

99.6347601648

99.5054382912

98.899297809

98.6514098617

99.6346068959

99.5107236835

98.8918976698

98.6496248219

99.6341470891

99.5046832351

98.8825789759

98.6439719831

99.6329209378

99.5095910994

98.8735343613

98.6383188203

99.6318480553

99.5144989637

98.8677786975

98.6316238663

99.6292424837

99.5167641318

98.8612007959

98.6241844955

99.6275565256

99.5061933472

98.860104479

98.6177861878

99.6232649958

99.5126113236

98.852978419

98.6125779565

99.6203528864

99.503173123

98.8532524982

98.6078159042

99.6174407769

99.4986427868

98.8447560421

98.6043930371

99.6162146255

99.4922248104

98.8472227552

98.5993329289

99.6125361715

99.4869394181

98.8411930121

98.5926353276

99.6116165579

99.4759911054

98.8414670913

98.5866815223

99.6087044485

99.4725933532

98.8305039221

98.5828113559

99.603953112

99.468440545

98.8231037828

98.5776012767

99.6007344647

99.4608899846

98.8091257421

98.5723909222

99.5975158174

99.4574922324

98.7970662559

98.5670314129

99.5950635146

99.4529618961

98.7866512451

98.563904898

99.5941439011

99.4522068401

98.7803474228

98.5578004639

99.5947569768

99.4484315598

98.7759621551

98.5527379635

99.5930710187

99.4503191999

98.7644508274

98.5475262943

99.5919981362

99.4522068401

98.7647249067

98.5442502469

99.5893925646

99.4563596483

98.7592433221

98.5362085779

99.586786993

99.4533394241

98.760339639

98.5290598767

99.5852543038

99.4544720082

98.7507468659

98.5202722207

99.5838748835

99.4484315598

98.7592433221

98.5126754797

99.5831085389

99.4442787516

98.7493764697

98.5040353367

99.5800431605

99.4363506631

98.7449912021

98.5001619232

99.5782039335

99.4397484153

98.7348502705

98.4971822706

99.5743722105

99.434085495

98.7359465874

98.4943515172

99.5723797146

99.4363506631

98.724709339

98.492563631

99.5693143362

99.434463023

98.7252574974

98.4897327449

99.5674751091

99.4371057192

98.7208722297

98.4840707285

99.5642564618

99.4329529109

98.7203240713

98.4781103595

99.5648695375

99.4367281911

98.7170351205

98.4722986524

99.5613443523

99.434840551

98.7148424867

98.4663375708

99.5610378145

99.434840551

98.7110053774

98.4605251688

99.5604247388

99.4329529109

98.7041533967

98.4562029038

99.5599649321

99.4280450466

98.6967532574

98.4521785555

99.5570528226

99.4223821263

98.6822270582

98.4480049835

99.5561332091

99.416341678

98.677293632

98.4429368368

99.552454755

99.4121888697

98.6663304628

98.436824901

99.5504622591

99.4091686455

98.6622192743

98.4302653282

99.5475501496

99.4053933653

98.6545450559

98.42266164

99.5435651577

99.4057708933

98.6515301843

98.4168466586

99.5423390063

99.4053933653

98.6449522828

98.4107331024

99.5398867036

99.4061484214

98.6449522828

98.4070051379

99.5359017117

99.4065259494

98.6331668759

98.4029787776

99.5349820982

99.4080360615

98.6315224005

98.4005927085

99.5346755604

99.4038832532

98.6287816082

98.3961186731

99.5306905684

99.399730445

98.6230259443

98.3931358698

99.5297709549

99.3959551648

98.6134331713

98.3879157464

99.5276251901

99.3940675247

98.6098701413

98.3804579469

99.5262457698

99.3940675247

98.6019218436

98.3741929583

99.5247130806

99.3899147164

98.598906972

98.3668833006

99.5247130806

99.3936899966

98.6010996059

98.3577827637

99.5228738535

99.3944450527

98.5958921005

98.3510687131

99.5222607779

99.3906697725

98.6008255266

98.3468908502

99.5196552062

99.3910473005

98.5983588136

98.3422651522

99.5176627103

99.3940675247

98.5986328928

98.3386838172

99.5161300211

99.3895371884

98.5934253874

98.3362961881

99.5132179116

99.3861394362

98.5994551305

98.3322669325

99.5136777184

99.383119212

98.5915068328

98.3273420625

99.5113786846

99.3729259554

98.5884919613

98.3201781749

99.5104590711

99.3695282032

98.5901364366

98.3165960354

99.5077002305

99.3714158433

98.5813659013

98.311968912

99.5069338859

99.3744360675

98.5780769505

98.3097299031

99.5043283143

99.3782113477

98.5799955051

98.3079386593

99.5031021629

99.38349674

98.584654852

98.3062966571

99.5003433224

99.3842517961

98.5772547128

98.301370486

99.5001900535

99.3800989878

98.5841066936

98.2964440681

99.4986573643

99.3706607873

98.5750620789

98.2904723213

99.4965115994

99.366130451

98.5731435243

98.2821112663

99.4943658345

99.3597124747

98.5687582566

98.2744961152

99.4925266075

99.3574473065

98.5649211474

98.268373703

99.4899210359

99.3559371944

98.5591654836

98.2635949699

99.4865491196

99.3589574186

98.5558765328

98.2577705747

99.4847098926

99.3585798906

98.549024552

98.2543355132

99.481951052

99.3600900027

98.5405280959

98.2506016144

99.4804183628

99.3578248345

98.5405280959

98.2438802389

99.4784258669

99.3548046104

98.5292908474

98.2370090243

99.4787324047

99.3540495543

98.5303871643

98.2311830527

99.4759735642

99.3525394422

98.5281945305

98.2249085431

99.4767399088

99.347631578

98.5309353228

98.218932447

99.4736745304

99.348009106

98.516957282

98.2141513083

99.4730614547

99.3506518021

98.5254537382

98.2084734037

99.4712222277

99.3510293302

98.5199721536

98.2020480106

99.4680035804

99.3563147225

98.520520312

98.1969671695

99.4660110844

99.3623551708

98.5125720143

98.1921849613

99.4655512776

99.3642428109

98.5287426889

98.1857585022

99.4621793614

99.3623551708

98.5243574212

98.1818725321

99.4585009074

99.3646203389

98.5355946697

98.1778369389

99.4583476384

99.3582023626

98.5435429674

98.1761927608

99.455435529

99.3548046104

98.5498467897

98.1685693933

99.453443033

99.348764162

98.5509431066

98.1678219725

99.4509907303

99.3438562977

98.5542320574

98.1625898673

99.44961131

99.3400810175

98.5539579782

98.1588524786

99.4485384276

99.3415911296

98.5509431066

98.1498821649

99.4463926627

99.3412136016

98.552587582

98.1464433274

99.44394036

99.3502742741

98.5449133636

98.1383690612

99.4425609397

99.3555596664

98.5484763936

98.132985848

99.4396488303

99.3563147225

98.5410762543

98.1265555118

99.4359703762

99.3566922505

98.5462837597

98.1216203169

99.434437687

99.3589574186

98.545461522

98.1144414084

99.4315255775

99.3510293302

98.5575210082

98.1081594326

99.4281536613

99.3498967461

98.5572469289

98.0999324273

99.4260078964

99.3464989939

98.5640989097

98.0924527328

99.4263144343

99.3427237137

98.5599877213

98.0869173918

99.4234023248

99.3370607933

98.5640989097

98.0800351807

99.4227892491

99.3363057373

98.5550542951

98.0746487656

99.4206434842

99.3393259615

98.5528616612

98.0679153307

99.4200304086

99.3408360736

98.5512171859

98.063575761

99.4149725342

99.3449888818

98.5457356012

98.0520525233

99.4128267693

99.348386634

98.5438170466

98.0487599209

99.4105277355

99.348764162

98.5416244128

98.0405279312

99.4099146599

99.3449888818

98.541898492

98.0366362045

99.4085352396

99.3423461856

98.5369650659

98.0290019842

99.4063894747

99.3363057373

98.5484763936

98.0278044055

99.4048567855

99.3355506812

98.5465578389

98.0200197873

99.4004119869

99.3336630411

98.5569728497

98.0150792282

99.396273726

99.3359282093

98.5542320574

98.0096892433

99.3910625828

99.3351731532

98.5619062759

98.0029513452

99.3901429692

99.3374383214

98.5591654836

97.9953145007

99.3846252881

99.3332855131

98.563276672

97.988425856

99.3855449017

99.331397873

98.5599877213

97.9822855687

99.3832458679

99.3238473126

98.5635507513

97.9725501784

99.3826327922

99.3253574247

98.5621803551

97.9662591039

99.3794141449

99.3276225928

98.5638248305

97.9593684159

99.3786478003

99.330642817

98.5657433851

97.9526270564

99.3735899259

99.3272450648

98.570402732

97.9449862881

99.3717506989

99.3264900087

98.5723212866

97.9410907651

99.3680722448

99.3174293362

98.5778028713

97.9326998814

99.3651601354

99.3072360796

98.5821881389

97.9246079913

99.3608686056

99.2940225988

98.5862993274

97.9172647715

99.3571901516

99.2887372065

98.5983588136

97.9076727979

99.3521322772

99.2826967582

98.6054848736

97.89897926

99.348760361

99.2823192301

98.6161739636

97.8922337418

99.3443155623

99.2770338378

98.6227518651

97.8878863838

99.3406371082

99.2808091181

98.623848182

97.8815898678

99.3378782677

99.2826967582

98.6276852913

97.8796408641

99.3345063515

99.2823192301

98.6293297666

97.8727440778

99.3306746285

99.2815641741

98.6386484605

97.8694454429

99.3266896366

99.2826967582

98.6476930751

97.8607485091

99.3227046447

99.280054062

98.6512561051

97.8552000613

99.3174935014

99.279676534

98.6561895313

97.8466518368

99.3136617784

99.2751461977

98.6520783428

97.8429023799

99.3095235176

99.2751461977

98.6578340067

97.8340530919

99.306764677

99.2713709175

98.6537228182

97.8283531266

99.3047721811

99.2709933895

98.6586562443

97.8223528044

99.3014002648

99.2691057494

98.6638637497

97.8142517856

99.2975685419

99.2691057494

98.6611229574

97.8061500957

99.2926639364

99.2638203571

98.6657823043

97.7984978835

99.2876060621

99.2638203571

98.666604542

97.7917454343

99.2804024229

99.2615551889

98.6805825828

97.7819910733

99.2754978175

99.263065301

98.6838715336

97.7755376536

99.2696735985

99.2608001329

98.6920939105

97.7684834284

99.2633895728

99.2558922686

98.6975754951

97.7609783748

99.2584849674

99.2494742922

98.699768129

97.7528722697

99.253427093

99.24607654

98.7044274759

97.7458164088

99.2480626809

99.2381484516

98.7038793174

97.7408619894

99.2446907646

99.2362608115

98.7134720905

97.7321536132

99.2370273187

99.2358832834

98.7131980113

97.7303517833

99.2310498308

99.2343731713

98.7249834182

97.7240451171

99.2264517632

99.2272001389

98.7337539536

97.7210417997

99.2194013929

99.2245574428

98.7373169836

97.7133829224

99.2112781402

99.2158742983

98.7359465874

97.7115807464

99.2079062239

99.2177619384

98.7397836967

97.6997155911

99.2031548874

99.2139866582

98.7375910628

97.6920550419

99.1962577861

99.2207821626

98.7433467267

97.6848445645

99.1908933739

99.2158742983

98.7458134397

97.6749292888

99.1852224239

99.2200271065

98.7521172621

97.6614068361

99.179244936

99.2215372186

98.7543098959

97.6529919205

99.1686693805

99.2238023867

98.7619841144

97.6463796923

99.163918044

99.2177619384

98.7600655598

97.6364605105

99.1556415224

99.2256900268

98.7647249067

97.6351078167

99.1490509589

99.2238023867

98.763902669

97.6293962363

99.141234244

99.2222922746

98.7649989859

97.6229327292

99.1369427142

99.2222922746

98.7704805705

97.613311833

99.1272867723

99.2241799148

98.7795251851

97.605794848

99.1214625533

99.2230473307

98.7767843928

97.592262816

99.1137991074

99.2207821626

98.7847326905

97.5842930747

99.1078216195

99.2185169944

98.7882957205

97.5775258024

99.0970927951

99.2211596906

98.792406909

97.570607661

99.0898891559

99.2173844104

98.7981625728

97.5638394394

99.0794668694

99.210966434

98.7984366521

97.5551152611

99.0710370788

99.2079462098

98.8047404744

97.5487972656

99.0623007504

99.2000181213

98.810222059

97.5367618563

99.0575494139

99.1973754252

98.8085775836

97.5274333926

99.0501925058

99.1962428411

98.8126887721

97.5156963158

99.0439084801

99.1958653131

98.8187185151

97.5080213094

99.0354786895

99.1985080093

98.8337928728

97.4973354906

99.0276619746

99.1988855373

98.8365336652

97.490863228

99.0172396881

99.1932226169

98.8379040613

97.4834873352

99.0094229732

99.193600145

98.8332447144

97.4762614296

99.0005333758

99.1920900329

98.8376299821

97.4682822033

98.9921035853

99.1920900329

98.8343410313

97.4575920272

98.9824476433

99.1954877851

98.8392744575

97.4482559847

98.9732515082

99.1951102571

98.8466745967

97.4378648212

98.9619096081

99.1909574488

98.8510598644

97.42762317

98.9517938594

99.1864271126

98.8510598644

97.4152715114

98.9404519594

99.1811417202

98.8516080228

97.407136637

98.9295698661

99.1735911598

98.852978419

97.3973437574

98.9191475796

99.1701934076

98.8579118452

97.3910155268

98.9101047133

99.1660405994

98.8625711921

97.3848375718

98.89922262

99.1686832955

98.8669564598

97.3809196412

98.8892601403

99.1686832955

98.8625711921

97.3756452548

98.8792976605

99.1724585757

98.8680527767

97.3688634812

98.8699482564

99.1709484636

98.8595563205

97.361779791

98.8586063564

99.1788765521

98.8633934298

97.3515301353

98.8506363726

99.1732136318

98.8661342221

97.3433899341

98.8403673549

99.1796316082

98.8686009352

97.3335906409

98.8297917995

99.1758563279

98.8622971128

97.3259012739

98.8190629751

99.1822743043

98.8653119844

97.3150446626

98.8083341508

99.177743968

98.8612007959

97.3056949433

98.7919343764

99.1841619444

98.8603785582

97.2933278056

98.7808990142

99.1758563279

98.8559932905

97.2833726259

98.7684842317

99.1800091362

98.8576377659

97.2688905458

98.7559161803

99.1751012719

98.8617489544

97.2578766874

98.7435013978

99.1735911598

98.8598303998

97.2480687773

98.7343052626

99.1671731834

98.8587340828

97.2378071356

98.7214306734

99.1698158796

98.8474968344

97.2264878925

98.7100887734

99.1645304873

98.8513339436

97.2180353315

98.697367453

99.1675507115

98.8453042005

97.2133559192

98.684186326

99.1671731834

98.8442078836

97.2041473857

98.67085193

99.1751012719

98.8379040613

97.1997692524

98.6582838786

99.1784990241

98.8485931513

97.1908614067

98.6437233312

99.1815192483

98.8359855067

97.1843687336

98.6293160528

99.1754787999

98.8400966952

97.1721371712

98.617514346

99.176611384

98.8285853675

97.1629247312

98.6023407229

99.1660405994

98.8274890505

97.1512946662

98.588853058

99.1588675669

98.8178962775

97.1420802496

98.5776644269

99.1520720625

98.8178962775

97.1348289467

98.5638702241

99.1528271186

98.8115924551

97.1271238441

98.5500760214

99.1460316142

98.8069331082

97.1207780065

98.5379677767

99.1437664461

98.8074812667

97.1133740052

98.5227941537

99.141878806

98.8058367913

97.1085384343

98.5079270685

99.1411237499

98.8085775836

97.096901855

98.4944394036

99.1354608296

98.8017256028

97.0907051853

98.4800321252

99.1396136378

98.8014515236

97.0831477358

98.4656248467

99.1392361098

98.7871994036

97.0722639748

98.4525969886

99.1377259977

98.7866512451

97.0619837466

98.4372700966

99.1328181334

98.7715768874

97.0551800557

98.4237824317

99.1335731895

98.7726732044

97.0444443733

98.4106013046

99.1241349889

98.7630804313

97.0303803446

98.3978799843

99.1188495966

98.7614359559

97.0241794263

98.3839325126

99.1135642043

98.7482801528

97.0125327282

98.3705981166

99.1094113961

98.7411540928

97.0033051306

98.3551179558

99.1052585878

98.7312872405

96.9916559259

98.3402508706

99.1052585878

98.7225167051

96.9842420671

98.32615013

99.1060136439

98.7134720905

96.9734985314

98.3100568934

99.1094113961

98.7005903667

96.9629051477

98.293657119

99.1150743164

98.6942865444

96.9514024492

98.2817021433

99.1188495966

98.677293632

96.9380818299

98.2660687135

99.1192271246

98.6649600667

96.9283929569

98.2489025945

99.1267776851

98.6490634713

96.9168861623

98.2325028201

99.1264001571

98.6394706982

96.9111322526

98.2177890039

99.1294203812

98.623848182

96.8996234082

98.1997032714

99.1275327411

98.6150776466

96.8943228228

98.1840698416

99.1347057735

98.6041144774

96.8844781091

98.1698158321

99.1245125169

98.5942476251

96.8735720275

98.1555618226

99.1199821807

98.5780769505

96.8628162168

98.1405414684

99.1124316202

98.5646470682

96.8550894748

98.1238351562

99.1071462279

98.5465578389

96.8459984009

98.1075886507

99.0924226351

98.5298390059

96.8375126285

98.0893496493

99.0943102752

98.5161350443

96.8325117359

98.0718769925

99.0852496027

98.4985939735

96.823418542

98.05379126

99.0841170186

98.4854381705

96.8169012277

98.0383110991

99.0852496027

98.4720082882

96.8087160721

98.0225244004

99.0935552191

98.4583043266

96.8000754346

98.0079638531

99.0901574669

98.438570622

96.7915856362

97.9930967679

99.0965754433

98.4251407397

96.7815788462

97.9793025651

99.0935552191

98.4034884804

96.7738456179

97.962442984

99.0894024109

98.3848510928

96.7611071888

97.9463497474

99.0822293785

98.3618284374

96.753675664

97.9296434352

99.0818518505

98.3429169704

96.7419964002

97.9124773162

99.0724136499

98.3212647112

96.736232088

97.8930121634

99.0761889301

98.298516135

96.7230335533

97.8759993134

99.0724136499

98.2793305889

96.7174198375

97.8611322282

99.0724136499

98.2524708243

96.7063431722

97.8444259159

99.0648630895

98.2291740896

96.6952652381

97.8287924861

99.0724136499

98.2121811773

96.6835789183

97.8136188631

99.0625979213

98.1929956312

96.6753824747

97.7987517779

99.056935001

98.1683285004

96.6659708861

97.7802062387

99.0490069125

98.1496911127

96.656406559

97.7633466575

99.0508945526

98.1217350312

96.6497261501

97.7461805385

99.0361709598

98.0899418404

96.6394009736

97.7296274952

99.0327732076

98.0636302342

96.6280116317

97.7120015695

99.0237125351

98.0356741527

96.6155577481

97.6946821816

99.0206923109

98.006347675

96.6043174993

97.6773627937

99.0146518625

97.9794879104

96.5927720986

97.6608097504

99.0203147829

97.945776165

96.5822888947

97.6464024719

99.0210698389

97.9117903404

96.5734760459

97.6312288489

99.0297529834

97.8789008327

96.5632946849

97.6171281083

99.0271102873

97.844915008

96.5563038752

97.6016479474

99.0240900631

97.8169589265

96.545360722

97.585401442

99.0161619746

97.7887287657

96.5366965126

97.5685418608

99.0108765823

97.7602245257

96.5268153248

97.5515290107

99.0040810779

97.7224015919

96.5157167847

97.533903085

99.0063462461

97.6911565595

96.5000550297

97.5162771593

98.9999282697

97.6505928334

96.4909305055

97.4989577713

99.0071013021

97.620444118

96.4783068245

97.478726274

99.0033260219

97.5809767087

96.4691802433

97.4609470793

99.005968718

97.5453464087

96.4603570606

97.44240154

98.9984181576

97.5061530787

96.4548801965

97.4264615724

98.9984181576

97.4691523826

96.4472729247

97.4134337143

98.9859597329

97.4244774679

96.4384477378

97.4000993183

98.9821844526

97.3839137418

96.4284043011

97.383546275

98.9746338922

97.3491056795

96.416229036

97.3676063073

98.9787867004

97.3088160325

96.4023778024

97.3498271127

98.9772765884

97.2709930987

96.3920261308

97.3292890774

98.9742563642

97.2287848971

96.3809120693

97.3112033449

98.9750114202

97.1830136656

96.3719285351

97.2915849232

98.9742563642

97.1320349287

96.3646192793

97.2744188043

98.9723687241

97.092019361

96.3541112527

97.2564863407

98.9682159158

97.0396702279

96.3434497647

97.2388604149

98.9689709719

97.0034917694

96.3359860211

97.2195485311

98.9678383878

96.9577205379

96.3256272146

97.2036085634

98.9636855796

96.9160604948

96.3135913198

97.1824574525

98.954247379

96.8626150448

96.3047538825

97.1648315268

98.9519822109

96.8146511794

96.2940869298

97.1485850213

98.9500945708

96.7527092732

96.2837236155

97.1306525578

98.936126034

96.7022786947

96.2718349107

97.1140995144

98.9274428894

96.6403367886

96.2617740906

97.0976997401

98.919514801

96.5844246255

96.2517122189

97.0802270832

98.9134743526

96.5276902247

96.2402769968

97.0624478886

98.903281096

96.4687631901

96.2273154357

97.0439023493

98.9059237922

96.4095620762

96.2169449297

97.0268894992

98.9036586241

96.3536499131

96.2061157083

97.0080374221

98.8964855916

96.2966414331

96.1937597558

96.9901049586

98.8866698631

96.2349736062

96.1824702141

96.9684940409

98.8817619988

96.18015776

96.1714845232

96.9502550395

98.8757215504

96.1154750615

96.1586662975

96.928337584

98.8730788543

96.05901474

96.1466095021

96.9113247339

98.8798743587

95.9929616454

96.1353144234

96.8929324636

98.8810069427

95.9318419769

96.1253919756

96.8742336554

98.8794968307

95.8630480899

96.1128729648

96.8567609986

98.8779867186

95.8005580253

96.1029482

96.8385219972

98.8711912142

95.726556633

96.0908844134

96.8196699201

98.8538249252

95.6563923499

96.0824846804

96.7989786159

98.8474069488

95.582939116

96.0707238202

96.7848778753

98.8383462763

95.508115486

96.0586559867

96.7646463779

98.8296631317

95.4371289652

96.0479617027

96.7467139144

98.8300406598

95.358468226

96.033140512

96.7310804846

98.8364586361

95.2891261806

96.0184698646

96.7140676345

98.8372136922

95.2173174221

96.0021155636

96.6932230615

98.8406114444

95.147153139

95.9897333518

96.6752905979

98.8387238043

95.068766479

95.9707747723

96.6561319829

98.8289080757

95.0002466713

95.9596119214

96.6342145274

98.816449651

94.9240526451

95.9430946367

96.6142895679

98.8021035861

94.8459400644

95.927951294

96.5943646084

98.7873799933

94.7628940574

95.917548421

96.5776582961

98.7783193208

94.6869741105

95.9079094581

96.5592660258

98.7677485361

94.6036540243

95.8942908595

96.5410270244

98.7598204477

94.5197857797

95.8823538679

96.5241674432

98.7564226955

94.4381101689

95.8730174927

96.5048555594

98.7571777515

94.3547900827

95.8595470214

96.4876894404

98.7579328076

94.2668106496

95.8450029103

96.4680710187

98.7564226955

94.1782830581

95.8272407918

96.4489124037

98.7530249433

94.0935925757

95.8140701992

96.4305201334

98.748494607

94.0034205088

95.7924726348

96.4115147874

98.7379238224

93.9190041057

95.7757733076

96.3888309873

98.7299957339

93.825543088

95.7652006687

96.3708985237

98.7269755098

93.7455119526

95.7537073458

96.3514333709

98.7250878696

93.6506805387

95.7408331862

96.332274756

98.7239552856

93.5648937395

95.7287237657

96.3135759478

98.7269755098

93.4728031179

95.7158462458

96.2931911815

98.7171597812

93.3848236848

95.6966800616

96.2738792977

98.7201800054

93.2905404294

95.6816510883

96.2545674138

98.7167822532

93.1981757286

95.6650858116

96.2349489921

98.714517085

93.1063591863

95.6515860576

96.2139511501

98.7092316927

93.0142685648

95.6368568799

96.1926467703

98.714139557

92.9221779432

95.6218185042

96.1724152729

98.6997934922

92.8295391632

95.6073917171

96.1531033891

98.6948856279

92.7366263039

95.5866685861

96.1313392025

98.6888451795

92.6379577808

95.5691655538

96.1131002011

98.6846923713

92.5417559708

95.55196647

96.0974667713

98.6703463065

92.4466504777

95.5369147317

96.0755493158

98.6677036103

92.3625081539

95.5266228926

96.0531720536

98.6575103537

92.2704175323

95.5167908466

96.031407867

98.6480721532

92.1816158615

95.5074187356

96.0076511845

98.6382564246

92.0900733984

95.4918989557

95.9843543087

98.6367463125

92.0023680446

95.47852841

95.9639695424

98.6235328317

91.9020550461

95.4620816077

95.9417455491

98.6171148554

91.8072236322

95.4454782231

95.9222803963

98.6125845191

91.7156811691

95.428410623

95.9023554368

98.6054114867

91.6211238345

95.4144159888

95.8835033597

98.5997485663

91.5295813714

95.3979581334

95.8654176272

98.6016362064

91.4278979767

95.3813435866

95.846718819

98.5978609262

91.337999989

95.3681114143

95.8263340527

98.5974833982

91.2343980398

95.3551851944

95.806715631

98.5910654218

91.1453222898

95.34333462

95.7828056795

98.5891777817

91.0461056082

95.3291735605

95.7601218794

98.5827598053

90.9562076205

95.3190132435

95.7398903821

98.577474413

90.8600058105

95.3056184435

95.7170533131

98.5691687966

90.7728486151

95.2906817913

95.6960554711

98.5699238526

90.6774690428

95.2782071227

95.6768968561

98.5619957641

90.5856525004

95.2635742571

95.6548261317

98.560108124

90.4924655619

95.2514041622

95.6329086762

98.5563328438

90.3990045442

95.2353804001

95.6112977586

98.5521800356

90.3049953681

95.2224361622

95.5880008828

98.542741835

90.2101639542

95.2067157931

95.5643974692

98.5382114987

90.1177992534

95.1919177801

95.5397211732

98.5291508262

90.0215974434

95.1738795908

95.515351415

98.5223553218

89.9393736741

95.1586138369

95.492514346

98.5132946493

89.8437200226

95.1431913968

95.4670717053

98.5049890328

89.7628666495

95.1271494068

95.4427019471

98.4970609443

89.6699537902

95.1138818712

95.4207844916

98.4895103839

89.591293051

95.0979892473

95.3965680024

98.4838474636

89.502217301

95.0871869189

95.370512286

98.474409263

89.4254751163

95.0728333555

95.347675217

98.4695013987

89.3369475248

95.0584776247

95.3251446859

98.456665446

89.2643165286

95.0438109297

95.302001079

98.4547778059

89.1801742048

95.0303773391

95.2794705478

98.4442070213

89.1004171486

95.0158607503

95.2578596302

98.4419418531

89.0212082509

94.999024907

95.2351758301

98.439299157

88.9400807986

94.9866664261

95.2072808868

98.4411867971

88.8570347916

94.9698254074

95.1818382461

98.4302384845

88.7783740524

94.9577722028

95.157315219

98.4291059004

88.6988910754

94.9399986613

95.1311062338

98.422687924

88.6221488908

94.9279416696

95.1061233999

98.4147598355

88.5470511816

94.9121725232

95.0817536417

98.4034339949

88.4678422838

94.8985656639

95.0529390848

98.3939957943

88.3957594461

94.882636975

95.0255039482

98.3834250097

88.3173727861

94.8680977791

94.999294963

98.370589057

88.2480307407

94.8551034207

94.9694075237

98.3592632163

88.1756738238

94.8430356366

94.9433518073

98.353600296

88.1052354615

94.832359009

94.9179091667

98.3456722075

88.0358934161

94.8170382695

94.890627299

98.3434070394

87.9723070345

94.8055847867

94.8636519692

98.3407643432

87.8994019591

94.7894856607

94.8377495218

98.336234007

87.8317043891

94.7726096032

94.8110807298

98.3279283905

87.7719551168

94.7583632524

94.7830325175

98.3241531103

87.6982278037

94.7430305472

94.7543712296

98.3147149097

87.6264190452

94.7289346594

94.7278557065

98.3056542372

87.5543362075

94.7129774422

94.6998074942

98.2950834526

87.4819792906

94.6994969213

94.6691537103

98.2830025559

87.4068815813

94.682449837

94.6414120359

98.2709216592

87.3405544075

94.6706700584

94.6113713277

98.2592182905

87.2750494713

94.6570284834

94.5788783167

98.2467598658

87.2125594067

94.6458657323

94.5496039531

98.234301441

87.1539064513

94.6336161987

94.5204828584

98.2271284086

87.0938830997

94.6226057712

94.4905954191

98.2108947037

87.0281040843

94.609267481

94.4628537447

98.2048542553

86.9656140197

94.5937554762

94.43373265

98.1923958306

86.9072351435

94.5825852575

94.4049180931

98.1908857185

86.8455673166

94.5698620126

94.376563343

98.1788048218

86.7877365989

94.5600856737

94.3482085929

98.1776722377

86.732098515

94.5475146098

94.317554809

98.1603059487

86.6737196389

94.5360284729

94.2861346805

98.1538879723

86.6112295742

94.5183308819

94.2544080141

98.131613819

86.5523025396

94.5034250767

94.2202290451

98.1214205624

86.4873457619

94.485876689

94.1834445044

98.1055643855

86.4349966288

94.4711210974

94.1491122664

98.096881241

86.3777140696

94.4588489028

94.1164659866

98.0844228163

86.3256390157

94.449061073

94.0804477905

98.0776273119

86.2730158034

94.4398937729

94.0499472755

98.061771135

86.2217629872

94.432434974

94.0171477267

98.0470475421

86.1661249034

94.4246647652

93.9831220266

98.0327014773

86.1107608988

94.4150288182

93.9506290156

98.0138250762

86.0592340034

94.4022829905

93.9170631223

97.993061035

85.9989365726

94.38969091

93.8804318505

97.9730520498

85.9438466472

94.3724323672

93.8474790328

97.9530430646

85.8843714541

94.3568814274

93.8131467948

97.9213307108

85.8339408756

94.3377502559

93.7769753298

97.9024543097

85.775013841

94.3243716846

93.7408038648

97.8779149882

85.7295166887

94.3097464242

93.7044791309

97.8514880267

85.6703155748

94.298542563

93.6680011281

97.8261936492

85.6228998679

94.2879599161

93.6324427387

97.804674552

85.5667136256

94.2797108528

93.5982637697

97.77069703

85.5143644925

94.2742629625

93.5620923047

97.7393622042

85.456807854

94.2622764955

93.5285264113

97.7061397382

85.4107625432

94.2493543109

93.4940409044

97.668764464

85.3573170932

94.2370532363

93.4587890529

97.6234611014

85.3088050694

94.2238161093

93.4187858649

97.581555491

85.2611152832

94.2073060273

93.3830742067

97.5328543761

85.206299437

94.1942205108

93.3446037079

97.4849083173

85.1597059678

94.1836261421

93.3058266712

97.4324319223

85.106534597

94.1671090136

93.2673561724

97.3890161997

85.0591188901

94.1558881796

93.2290389426

97.3297443003

85.0108809455

94.1432631427

93.1917945951

97.2772679052

84.9727839324

94.1325071461

93.1514848693

97.2168634217

84.9209829578

94.1187875698

93.1113284124

97.153816242

84.8853526577

94.1103677486

93.0710186865

97.0783106376

84.8351961585

94.1005436718

93.0314753053

97.0050702013

84.7872322931

94.0896268278

92.9914721173

96.9250342607

84.7365276354

94.0788646989

92.9528483496

96.8419780958

84.6926749585

94.069037332

92.9119255481

96.7517488986

84.6384072708

94.0609250811

92.8716158223

96.6626522854

84.5929101185

94.0490674557

92.8303864829

96.570535448

84.5471388869

94.0414216151

92.78823753

96.4704905222

84.5013676554

94.0308100306

92.7468549218

96.3704455963

84.4621743254

94.0209776409

92.7060853892

96.2681355024

84.4180475692

94.0127051516

92.662710285

96.1624276562

84.3829654276

94.0011536655

92.6236267105

96.0506793617

84.3322607699

93.9891323688

92.580711413

95.9400636512

84.2870376969

93.9780464339

92.5371830399

95.8181221001

84.231399613

93.9697701652

92.4956471627

95.7003333572

84.1894654907

93.9546211437

92.4536514787

95.575371582

84.1354718822

93.9452493921

92.4108894502

95.4496547506

84.0921673637

93.9347831644

92.3695068419

95.3095918545

84.0488628453

93.9249407223

92.3282775026

95.1770795187

84.0102176737

93.9133784412

92.2861285497

95.0294660621

83.9622538083

93.9036900284

92.2435197901

94.8773222692

83.9200456068

93.8963449204

92.1995316102

94.7214031962

83.877563326

93.8855606356

92.1563097749

94.5662391791

83.8337106491

93.8796209352

92.110329099

94.3997493214

83.7827319121

93.8682094037

92.0683334151

94.2321268796

83.7312050167

93.8592980652

92.0244985041

94.0603516296

83.6810485175

93.8460076553

91.9779047526

93.8851786274

83.6339068898

93.8381888878

91.9320773456

93.7001898966

83.5938913221

93.8250518916

91.885636863

93.5118034136

83.5544239129

93.8142594114

91.8362842709

93.3207742345

83.5196158506

93.8031528095

91.7896905194

93.1210619108

83.4828892336

93.7929836404

91.7453958017

92.9202170031

83.4467107752

93.7806227043

91.6984955123

92.7193720954

83.4003913851

93.7688861305

91.6561932905

92.5219249399

83.3595535797

93.7598088395

91.6111322282

92.3154171118

83.3225528836

93.7493219092

91.5662244347

92.1096643398

83.2800706028

93.7421212479

91.5190176075

91.9001362876

83.2395068766

93.7335110356

91.4736500074

91.6826801469

83.1992172297

93.7241171745

91.4233778018

91.4625813101

83.1616683751

93.715505308

91.375251361

91.2428600013

83.1180897774

93.7053266272

91.3263585757

91.0261589166

83.0865706658

93.6951468407

91.2789984796

90.8064376078

83.0449106228

93.6830862775

91.2279599294

90.5950219155

83.0076358474

93.6740006722

91.1799867576

90.3768107188

82.9662498835

93.6624074134

91.1287949384

90.1601096341

82.927604712

93.6525363459

91.0789825396

89.9426534935

82.8878632235

93.6407837183

91.0302430232

89.7210445445

82.8522329235

93.6327910889

90.9816567757

89.5028333478

82.8176989404

93.6229168988

90.9338368728

89.2887749593

82.7831649573

93.612257874

90.8857104321

89.0818896033

82.7458901819

93.602695069

90.8365111089

88.8780244714

82.7034079012

93.592347327

90.7851660209

88.6730267554

82.6617478581

93.5812143876

90.7358134288

88.4793548801

82.6157025473

93.5702369535

90.6826291137

88.2736021081

82.5723980288

93.5600424685

90.632663446

88.0727572004

82.5258045596

93.5489056846

90.5820847025

87.8670044284

82.4827741203

93.5379244588

90.5318124969

87.671444913

82.4364547303

93.5289816511

90.4830729805

87.4732427014

82.3986317965

93.5162719796

90.4338736574

87.2829685783

82.3528605649

93.5087395072

90.3865135612

87.0945820954

82.3177784234

93.500578644

90.3363946246

86.9137461728

82.2755702218

93.4921031475

90.28596915

86.7370630585

82.2424066349

93.4829989805

90.2366165579

86.5373507349

82.1993761957

93.474050918

90.185118201

86.3920024464

82.1659385295

93.4640029497

90.1308610035

86.2032384354

82.1248266449

93.4548960453

90.0790561087

86.0458092502

82.0861814733

93.4450030573

90.0234194909

85.871391304

82.0497289356

93.4380930476

89.9687024866

85.7060340304

82.0102615264

93.4307113364

89.9172041297

85.5127396831

81.9790164941

93.4222295013

89.8637132768

85.3424745452

81.9411935602

93.411076287

89.8106822306

85.1824026638

81.9044669433

93.4018071097

89.7593371426

85.0404521276

81.8655476925

93.3882944577

89.7047734072

84.8652791253

81.8408805618

93.37713719

89.6512825543

84.7078499402

81.798398281

93.3637781441

89.596718819

84.5730724363

81.7701681202

93.3521463592

89.5412354701

84.4005421302

81.7372786125

93.3427141183

89.4886642307

84.2684073225

81.711789244

93.3323375522

89.4341004954

84.1207938659

81.6723218348

93.3257336822

89.3798432979

83.9656298489

81.6408027233

93.3211735944

89.3255861003

83.8153736961

81.6057205817

93.3147261936

89.2717887096

83.6654950714

81.5676235686

93.3035601286

89.2187576634

83.5005153258

81.5213041786

93.2936510927

89.1671060376

83.3642277098

81.483755324

93.2805947243

89.1122357644

83.2143490851

81.4478509448

93.2684805554

89.059664525

83.0784389971

81.405368664

93.2571515972

89.0040279072

82.9542322779

81.3708346809

93.2488113456

88.9476249448

82.8141693817

81.3346562224

93.2376373867

88.8903023689

82.665423341

81.2954628924

93.2297675979

88.8326732552

82.527625613

81.2565436416

93.217961669

88.7767300996

82.4094593421

81.2280394016

93.2086732874

88.7227794399

82.2561829652

81.2044685878

93.1989116177

88.6676026289

82.1380166943

81.1795273778

93.1916684278

88.6138052381

82.0058818866

81.151297217

93.1828498714

88.5578620825

81.8643088783

81.1277264031

93.17481796

88.5003862377

81.7506729437

81.0882589939

93.1645802066

88.4427571239

81.6211808321

81.0476952677

93.1552865023

88.3851280102

81.4935763607

81.0065833831

93.1434711329

88.3285717789

81.3655943612

80.9715012416

93.1335450642

88.2710959341

81.2444078662

80.9276485646

93.1226724417

88.2177583501

81.1164258667

80.8909219477

93.1141625472

88.1601292364

80.9756079145

80.8574842816

93.1032876611

88.1031131983

80.8714101804

80.8215799023

93.0952488854

88.0422654372

80.7302147002

80.7878681569

93.0859482591

87.9860157438

80.6150686535

80.7519637777

93.0775926669

87.9242483692

80.504830471

80.72620033

93.0670288635

87.8661594487

80.3862866721

80.6938589808

93.0594600282

87.8068443769

80.264722649

80.6659028992

93.0512597619

87.7476825739

80.1522192985

80.6368505007

93.0416392976

87.6899001913

80.0317878595

80.6056054684

93.0310714117

87.6319645397

79.9177743968

80.5661380592

93.0216066142

87.574182157

79.7931901495

80.536263423

93.009458713

87.5165530433

79.6999407281

80.5017294399

92.9977826113

87.4586173917

79.5798868171

80.4669213776

92.9856315977

87.4005284712

79.4783317792

80.4386912169

92.9755308454

87.3427460886

79.372623933

80.4132018484

92.9652711455

87.2812852519

79.2654059748

80.3797641822

92.9564311114

87.2225832557

79.1585655445

80.3413930899

92.9468008318

87.1631149149

79.0536127544

80.3079554238

92.9385906253

87.1010410025

78.9528127725

80.2706806484

92.9273793642

87.0420324685

78.8501251505

80.235872586

92.9167984829

86.9840968169

78.7459274165

80.1953088599

92.9040050621

86.9227892491

78.6436173225

80.1695454122

92.8945273182

86.8642405218

78.5409297005

80.1328187953

92.8839426945

86.8038525676

78.445792639

80.1043145553

92.8754109259

86.7396328903

78.3457477131

80.068410176

92.8648241234

86.6783253225

78.2547634598

80.0423726491

92.856922738

86.6187037128

78.1600039263

80.0089349829

92.8458596688

86.5590821031

78.0573163043

79.979334426

92.8344791365

86.5011464515

77.9704848592

79.9461708391

92.8221486519

86.4418313797

77.8696848774

79.9146517275

92.810607099

86.3834359213

77.7760579279

79.883132616

92.798115308

86.3209022022

77.6880938988

79.8450356029

92.7837239453

86.2595946344

77.6023950378

79.8124201744

92.7737593865

86.1978272598

77.5234916812

79.7756935575

92.7631609828

86.1359066163

77.435150124

79.7444485252

92.7530360035

86.0759784688

77.3385029504

79.7052551952

92.7433846038

86.0169699348

77.2614872339

79.6759287175

92.7351563881

85.9525969886

77.1637074762

79.6411206552

92.7229709582

85.8911361518

77.0776310872

79.6150831282

92.7117336231

85.8301351219

77.006655819

79.5832899375

92.701761326

85.766988327

76.9179367339

79.5547856974

92.6905214195

85.7055274903

76.8379007932

79.5271036951

92.6786467984

85.6437601157

76.7525794602

79.4953105044

92.6658204984

85.5819927412

76.6710334075

79.4621469174

92.6525172749

85.5222178626

76.5898648827

79.4256943797

92.6382617011

85.4584579921

76.5200221986

79.3958197436

92.6247960891

85.3959242729

76.4448941223

79.3588190474

92.6129130408

85.334769974

76.3667458217

79.3303148074

92.6038809043

85.2717764481

76.2908626893

79.2955067451

92.5956402919

85.2066371573

76.2225301173

79.2697432974

92.5870819567

85.1447165138

76.1413615926

79.2357574728

92.580741939

85.081569719

76.0730290206

79.2141052135

92.5715481421

85.0193425376

76.0088492568

79.1787489928

92.5612436639

84.9571153563

75.9303234283

79.1521633074

92.5507794813

84.8959610574

75.8589706321

79.1192737997

92.5411069877

84.830208691

75.7861077238

79.085287975

92.5290545973

84.7659890137

75.7083369513

79.0499317543

92.5189039982

84.7054477905

75.634718987

79.0192348804

92.5063728165

84.6407683064

75.5648763029

78.9871676104

92.494474554

84.578694394

75.4927684507

78.953455865

92.4828921085

84.5161606749

75.429343743

78.9222108327

92.4700386558

84.45301388

75.3617662271

78.8887731665

92.459088009

84.3875680514

75.2926785991

78.8602689265

92.4487709958

84.3242679876

75.2217033309

78.825186785

92.4386115809

84.2579025455

75.154503343

78.7955862281

92.4289273491

84.1975145912

75.085038187

78.768178305

92.4159076025

84.1352874099

75.0189707831

78.7377555104

92.4003450111

84.072293884

74.9532809073

78.6977399427

92.3873212365

84.009453627

74.8872135034

78.6659467519

92.3749310639

83.9472264456

74.8215236276

78.6289460557

92.3609504122

83.8814740792

74.7524359996

78.5911231219

92.3525292259

83.8163347884

74.6871236518

78.553300188

92.3436305341

83.7525749178

74.622188832

78.5242477896

92.3345720565

83.6874356271

74.5610292924

78.4897138065

92.3232874466

83.6216832606

74.4949618885

78.4584687742

92.3134321519

83.559915886

74.4304045968

78.4277719003

92.3021449575

83.4969223601

74.3684900012

78.389400808

92.2914923954

83.430403649

74.3005349572

78.3589780134

92.2800434952

83.3680231988

74.2363551935

78.3230736341

92.2682750896

83.302883908

74.1680226215

78.2893618887

92.2552326705

83.2375913483

74.107618138

78.2526352718

92.243302014

83.1736782088

74.0336226456

78.227968141

92.2326426558

83.1106846829

73.9747282742

78.1865821772

92.2224594317

83.0467715435

73.9014878379

78.156707541

92.2114793834

82.9868433959

73.8373080742

78.1186105279

92.200975505

82.9218573741

73.7670878621

78.0821579902

92.1885602875

82.8564115454

73.7040406824

78.0429646602

92.1766210014

82.7912722546

73.62815755

78.0073343602

92.1638840582

82.727665653

73.5568047538

77.9697855056

92.1500306341

82.6631394379

73.4873395978

77.927577304

92.1371307461

82.5992262985

73.4182519698

77.8916729248

92.1242290519

82.5362327726

73.3521845659

77.846723931

92.1105289788

82.4746186669

73.2842295219

77.8091750763

92.0969862064

82.4079466869

73.2208048142

77.763677924

92.087584758

82.3446466232

73.1494520181

77.7269513071

92.076269878

82.2779746432

73.0773441659

77.6806319171

92.0678226527

82.2152876551

73.0007059774

77.6414385871

92.0568241602

82.1510679778

72.9312408214

77.5981340686

92.0459837803

82.087921183

72.8576228571

77.5548295501

92.0321126089

82.0237015057

72.788912757

77.513169507

92.0191961904

81.9617808622

72.7179374889

77.4687686716

92.0027689898

81.8960284958

72.6548903092

77.4271086286

91.9892103528

81.8301228604

72.581649873

77.3753076539

91.9745328697

81.7659031831

72.5189802213

77.3276178678

91.9627253682

81.7003040855

72.4502701213

77.2747205762

91.9501183891

81.6370040218

72.3842027174

77.2226455224

91.9379885246

81.5755431851

72.3124723933

77.16645928

91.9260166944

81.5140823483

72.2407420691

77.1124656716

91.9151608873

81.4503224778

72.1625937685

77.0592943008

91.9022280318

81.3873289519

72.0897308603

77.0014635831

91.888814259

81.3237223503

72.0180005361

76.9477440539

91.8771554612

81.259502673

71.9383421234

76.8912837323

91.8632587971

81.1963558782

71.8684994394

76.8392086784

91.8498393333

81.1324427387

71.7979016993

76.78165204

91.8373766468

81.0680697925

71.7261713751

76.7188878961

91.8242730243

81.0058426112

71.6514208267

76.6550274353

91.8114872001

80.9403967826

71.5932815113

76.5884261822

91.7977404529

80.8787826769

71.5204186031

76.5201804538

91.7822329299

80.8165554956

71.4524635591

76.4475494576

91.7656033963

80.7518760116

71.3796006509

76.3831408384

91.7504103228

80.6905684438

71.3105130228

76.3096876045

91.7329751702

80.6286478003

71.2319871942

76.2389751629

91.7192166557

80.5630487027

71.1651647344

76.1605885029

91.7070562504

80.5023542106

71.0960771063

76.0865871106

91.6940940431

80.4415064496

71.0262344222

76.0060078167

91.6793693131

80.377746579

70.9582793783

75.9358435336

91.6659229287

80.3136801707

70.8910793904

75.851975289

91.6505532166

80.2511464515

70.8238794024

75.7823591644

91.6316577469

80.1864669675

70.7464861579

75.6962982859

91.6156415862

80.1240865172

70.6807962821

75.6242154482

91.601384848

80.0612462602

70.6075558458

75.533769302

91.5858440777

80.0008583059

70.5403558579

75.4578493551

91.5728647127

79.9377115111

70.4746659821

75.3665809712

91.5602040535

79.8773235568

70.4176592508

75.2909351035

91.5456180861

79.8163225269

70.3557446551

75.197748165

91.5310297944

79.7539420766

70.2926974755

75.1253912481

91.5165995262

79.6930943156

70.2304053518

75.0319302304

91.4997613371

79.6337792437

70.1662255881

74.962588185

91.4845241146

79.5736978273

70.0982705441

74.8674826919

91.4716908006

79.5137696797

70.0337132524

74.7852589226

91.4559675368

79.4521555741

69.9717986568

74.690701588

91.4397601196

79.3917676198

69.907618893

74.598062808

91.4240313643

79.3310731277

69.8426840732

74.4919941457

91.4073366639

79.2696122909

69.7811470056

74.3996294449

91.3880697583

79.2089177988

69.7177222979

74.3004127633

91.3702442536

79.1488363824

69.6569402864

74.2033887156

91.3533790884

79.0898278483

69.5931380507

74.1192463917

91.3358681463

79.0300529697

69.5346212073

74.0348299887

91.3191573281

78.9690519398

69.4723290836

73.9539766156

91.3030863494

78.9080509098

69.4119246001

73.8709306086

91.2850834943

78.8493489136

69.3503875325

73.7876105224

91.2672378752

78.7888076904

69.2926257451

73.7037422778

91.2477805668

78.7320981902

69.2288235094

73.6201481124

91.2281582526

78.6735494629

69.1714392501

73.5340872339

91.2080490441

78.616380156

69.1121673506

73.4600858416

91.1900274266

78.5604370003

69.0540280352

73.3740249631

91.1716803362

78.5015817352

68.9958887198

73.2975568577

91.153329553

78.4399676296

68.9411471566

73.2071107116

91.1364242468

78.3826450537

68.8833853693

73.1268054969

91.1179053127

78.32501594

68.82788875

73.0391001431

91.0988993628

78.2663139438

68.7739022429

72.9642765131

91.0797283289

78.2097577125

68.7214258478

72.8839712984

91.0611978647

78.1550407082

68.6670618127

72.8113403023

91.0407294042

78.1007835107

68.6074123852

72.7417241776

91.0228358779

78.043154397

68.5473854297

72.6663523891

91.0054225836

77.9872112414

68.4873584742

72.5904324422

90.9875221139

77.9309615479

68.4292191588

72.5139643368

90.9697794348

77.8728726274

68.3759877077

72.4451704499

90.9521946387

77.8195350434

68.330306817

72.3684282652

90.9328312974

77.7632853499

68.2770753659

72.3051159629

90.9145937142

77.7070356565

68.2317720033

72.2319368083

90.893769345

77.6513990387

68.175520328

72.1595798914

90.8731016884

77.5968353033

68.1177585406

72.0817413898

90.8537214903

77.5364473491

68.056221473

72.0121252652

90.8344987105

77.4835695718

68.0060102461

71.9301755752

90.8139791546

77.4302319878

67.9444731785

71.8690559067

90.795556076

77.3770476728

67.8919967835

71.8008101782

90.7771292585

77.3266221982

67.8361226362

71.7421572228

90.7580519456

77.2743574967

67.7859114093

71.6788449205

90.7383237269

77.2225526019

67.7277720939

71.6207401236

90.7192382535

77.1695215557

67.679070979

71.553590712

90.6995015924

77.1154176272

67.6239518878

71.4943895981

90.6807316028

77.0596277404

67.5688327966

71.428884662

90.659853516

77.0069032321

67.5163564016

71.3581722204

90.641075316

76.9498871941

67.4665227026

71.2929413635

90.6221312934

76.8962430722

67.4129137235

71.2285327442

90.6041550978

76.8464306734

67.3604373285

71.1649463627

90.5848793582

76.7935528962

67.3132463257

71.1032785358

90.5667337379

76.7379162784

67.2622800427

71.0479145311

90.5479362264

76.689176762

67.2128238719

70.9925505265

90.5292969096

76.6407437834

67.163367701

70.936090205

90.5101673597

76.5889388886

67.1207070345

70.8766150119

90.4918445935

76.5394330276

67.0678531114

70.8228954826

90.4730315223

76.4916131247

67.0199070526

70.7653388442

90.4530789053

76.4401147678

66.9670531295

70.7127156318

90.4329596159

76.3880033351

66.9168419026

70.6565293895

90.4141342922

76.3358919025

66.8617228114

70.6074692072

90.3948180326

76.2839337388

66.8156643927

70.5458013803

90.3758223911

76.2355007602

66.7650756377

70.4929040887

90.3561731254

76.1859948992

66.7205273311

70.4304140241

90.3371693578

76.1366423071

66.6710711603

70.3758722572

90.3176741605

76.0875962529

66.6287880218

70.3150266679

90.2980122414

76.0376305851

66.5831071311

70.2643220102

90.2788336837

75.9878181863

66.5404464646

70.2073135302

90.2622523247

75.9415309726

66.4985408542

70.1563347933

90.2443670526

75.8927914562

66.4555026597

70.1037115809

90.2261529511

75.8442052087

66.4105768251

70.0549254779

90.2077724966

75.7986843396

66.3667835745

69.9998355525

90.1916661881

75.7519373191

66.3180824597

69.952968004

90.1723022726

75.7024314581

66.2712689849

69.8989743955

90.1535852933

75.6559909755

66.2263431503

69.8458030247

90.1340503883

75.6100102997

66.1791521476

69.7934538917

90.1151626215

75.5644894306

66.1323386728

69.7435714716

90.0948049921

75.5177424101

66.0919431745

69.6945112893

90.0762348227

75.4717617343

66.0428645316

69.6432584732

90.0609196973

75.4250147138

66.0024690333

69.5977613208

90.0465797725

75.380873265

65.9650937591

69.5470566631

90.0314225968

75.3335131689

65.9284735409

69.5021076693

90.0149586871

75.28937172

65.8910982668

69.4505807739

90.0001222882

75.2438508509

65.8510802964

69.4080984931

89.9812064088

75.1987897886

65.8159701904

69.35574936

89.9626127903

75.1555679533

65.7740645799

69.3116226039

89.9446679356

75.1114265045

65.7348016657

69.2611920254

89.9268826838

75.0651392908

65.6921409992

69.2187097446

89.9103996312

75.0202314974

65.654765725

69.1712940377

89.8934238247

74.9745573594

65.6109724744

69.1342933415

89.8774244574

74.9270439943

65.5701994481

69.0860553969

89.8602791171

74.8815231252

65.5309365338

69.0515214138

89.8436205106

74.8352359115

65.4943163156

69.0032834692

89.8228745941

74.7907879249

65.4599612656

68.9649123769

89.8039213802

74.7464932071

65.4301365519

68.9111928476

89.7844738393

74.7025050272

65.3969140859

68.8648734576

89.7682915823

74.661122419

65.3644466761

68.8149910376

89.7521064076

74.6198930796

65.329714098

68.7629159838

89.7393523957

74.5771310511

65.295359048

68.7083742168

89.7247975268

74.5351353671

65.2538309656

68.6601362722

89.7086045049

74.4920668007

65.2157006354

68.6165576745

89.6915905049

74.4491515033

65.1771927771

68.5636603829

89.6740823473

74.4050100544

65.1424601991

68.5239188945

89.6550976784

74.358263034

65.1035748128

68.4778735837

89.6370912609

74.3228579136

65.0692197628

68.4362135406

89.6189174814

74.2810154986

65.037129881

68.3882496752

89.6017226756

74.2335021335

65.0050399991

68.3443969983

89.5833779117

74.1965643239

64.969174837

68.2936923406

89.5656847594

74.1515032616

64.9438804595

68.2542249313

89.548643605

74.1108869979

64.9140557458

68.2076314621

89.5324187236

74.0658259356

64.8861186722

68.1722752413

89.5163548335

74.0203050665

64.8574265425

68.1273262475

89.5019276589

73.9799953406

64.8242040765

68.0958071359

89.4860222829

73.9383061945

64.7932467787

68.0497618251

89.4701140794

73.8975366619

64.7611568969

68.0152278421

89.454695183

73.8541615577

64.7271793749

67.9691825313

89.4379610329

73.8179900927

64.6932018529

67.9269743297

89.4218801743

73.7738486439

64.6614894991

67.880929019

89.4048116098

73.7284810437

64.626379393

67.840639372

89.3898739424

73.68786478

64.5931569271

67.7981570913

89.3755905413

73.6417308353

64.5633322133

67.7584156028

89.3581846913

73.6067855216

64.5335074996

67.7236075405

89.3402826865

73.5666290647

64.5078355941

67.687429082

89.3245128116

73.5181960861

64.4810311045

67.6487839105

89.3061111048

73.4867759576

64.4564917831

67.6063016297

89.2883630101

73.4475391142

64.4311974056

67.5635452697

89.2732414797

73.4047770857

64.4066580842

67.5196925927

89.2577885744

73.366153318

64.3757007864

67.480773342

89.2416752497

73.3305949286

64.352671577

67.4418540912

89.2286838186

73.2889057825

64.3247345034

67.4106090589

89.210426839

73.247982981

64.30057271

67.3725120458

89.1949630512

73.2121180539

64.2741457485

67.3494893904

89.1771928357

73.1695092942

64.2537592353

67.3064589512

89.1590899015

73.127973417

64.2269547457

67.2804214242

89.1401601756

73.0882767669

64.2046805924

67.233827955

89.124684196

73.0416830154

64.180141271

67.2036792396

89.1073940195

73.0088834666

64.1597547578

67.159004325

89.0929006203

72.9725587327

64.1367255485

67.1283074511

89.0797227565

72.928110746

64.1155839792

67.0839066157

89.0624238514

72.8936252391

64.0914221858

67.0507430288

89.0452863849

72.8493305214

64.0691480325

67.0060681142

89.0288049408

72.8107067536

64.0400783748

66.9671488634

89.0126501648

72.7670251116

64.0174266935

66.926311058

88.9951733302

72.731926529

63.9943974842

66.8851991734

88.9806616522

72.6877850802

63.974010971

66.8435391303

88.9673022202

72.6503874638

63.9540019858

66.8095533057

88.951466221

72.6122235029

63.940033449

66.7728266887

88.9366174109

72.5746726176

63.9151165995

66.7382927057

88.9197857619

72.5325236647

63.8992604226

66.7097884656

88.9009701478

72.49206067

63.8784963814

66.6749804033

88.8790135635

72.4542032468

63.8577323402

66.6494910349

88.8583727303

72.4157327481

63.837345827

66.6097495464

88.8373967324

72.3743501398

63.8252649303

66.5828897818

88.8198854137

72.3357263721

63.7984604407

66.5365703918

88.8046841117

72.3024670165

63.7780739275

66.5099847064

88.7932814273

72.2667553583

63.752402022

66.4675024256

88.7817119901

72.2287446662

63.7271076446

66.440642661

88.7699757349

72.1846032174

63.7033233792

66.3959677464

88.7550965613

72.1490448281

63.6889773143

66.3655449517

88.7382304818

72.1102677915

63.6697233852

66.3244330671

88.7203687853

72.0740963265

63.6614177687

66.290995401

88.7018417454

72.0370052479

63.6466941759

66.2509798333

88.6821525246

71.9982282113

63.6338582231

66.2164458502

88.6661000932

71.9557727206

63.6180020462

66.1816377879

88.653024316

71.9219002894

63.6032784533

66.1608077663

88.6387877328

71.884502673

63.5817593561

66.1246293078

88.6235553676

71.8446527539

63.5696784594

66.0942065132

88.6094796596

71.8061822551

63.5530672264

66.0662504317

88.5917576475

71.7629604198

63.5368335215

66.0344572409

88.5715469148

71.7247964589

63.5239975687

65.9963602278

88.5510001317

71.6884717249

63.5126717281

65.962100324

88.5317746305

71.6538329491

63.4881324066

65.9338701632

88.5113844082

71.615975526

63.4685009495

65.8938545955

88.4934769247

71.5799573299

63.4515121885

65.8650762762

88.4765609733

71.5364289568

63.4337683715

65.8234162332

88.4627936455

71.5043957526

63.4133818583

65.7888822501

88.4488582645

71.4622467997

63.3997908495

65.7444814147

88.4340910006

71.4296005199

63.3820470324

65.7121400655

88.4178275648

71.3882179116

63.3677009676

65.6710281808

88.4007311369

71.3537324047

63.3495796225

65.6414276239

88.3804767205

71.3167945951

63.3337234456

65.6025083731

88.3605498145

71.2790904409

63.3193773808

65.57866348

88.3396217255

71.2384741773

63.3076740121

65.5433072593

88.321180967

71.1992373339

63.288042555

65.5186401285

88.3022378011

71.1662845162

63.2752066022

65.4734170554

88.2851189892

71.1298065133

63.2627481775

65.4495721623

88.2671656013

71.0951677375

63.2468920006

65.4081861985

88.2533656083

71.0548580117

63.2280155995

65.3689928685

88.2360710043

71.0228248075

63.2125369506

65.3273328254

88.2199374044

70.9769974006

63.1981908857

65.2982804269

88.20346811

70.9394465153

63.1793144846

65.2590870969

88.1878277515

70.9031217814

63.1645908918

65.2275679854

88.1691888086

70.8652643582

63.1559077473

65.1990637453

88.1535423682

70.8303190446

63.1423167385

65.1637075246

88.1368941697

70.7965998823

63.1253279775

65.1308180169

88.1204093549

70.7595088038

63.1094718005

65.096558113

88.1024224027

70.7224177252

63.0932380956

65.0628463676

88.0835987893

70.6871658738

63.0705864143

65.0239271169

88.0651044199

70.6508411398

63.0520875412

64.9943265599

88.0429393835

70.6145164059

63.0362313643

64.9565036261

88.0187681345

70.5786514787

63.0203751873

64.9216955638

87.9940899436

70.5423267448

63.0048965384

64.879213283

87.9739087115

70.5066150866

62.9939482258

64.8455015376

87.9507195974

70.4719763108

62.9905504736

64.799730306

87.9318635089

70.4361113836

62.9754493527

64.7693075114

87.9145056588

70.4022389524

62.9645010401

64.728469706

87.8983130361

70.3700524793

62.9505325033

64.6969505945

87.8787777584

70.3367931237

62.9331662143

64.6626906906

87.8622445155

70.303993575

62.9082493648

64.6311715791

87.8445388059

70.2713472951

62.8927707159

64.5955412791

87.8261611823

70.2345627544

62.8738943148

64.5634740091

87.8062756035

70.1988510962

62.860680834

64.5264733129

87.7878899698

70.1640590514

62.8512426335

64.4878281414

87.7666581297

70.1271212418

62.8410493769

64.449457049

87.7447521874

70.0895703566

62.8297235362

64.4075229267

87.7245135947

70.0553913875

62.8149999434

64.3751815775

87.7047722872

70.0202928049

62.7995212945

64.339003119

87.6850265353

69.9841213399

62.7806448934

64.3055654529

87.6636023856

69.9499423709

62.7610134362

64.2630831721

87.6440147924

69.9139241748

62.7421370351

64.2274528721

87.6224131399

69.8788255922

62.7296786104

64.1770222936

87.5991309785

69.8440335475

62.7134449054

64.1353622505

87.5758426274

69.8080153514

62.6994763686

64.0832871967

87.5543917609

69.7749092648

62.6847527758

64.0479309759

87.5326003439

69.7419564471

62.6670089587

64.0081894874

87.5082881309

69.7091568983

62.6454898615

63.9725591874

87.4869884354

69.6726788955

62.6269909884

63.9292546689

87.464844672

69.6368139683

62.6050943631

63.8966392405

87.4445412961

69.5997228898

62.5873505461

63.8530606428

87.4230582123

69.5661569964

62.5760247054

63.8108524412

87.4057672094

69.5282995733

62.5662089769

63.7727554281

87.3857859656

69.4967261759

62.5541280802

63.7313694643

87.3642884338

69.4662256609

62.5446898796

63.6869686289

87.3406014342

69.4351120702

62.5310988708

63.650242012

87.3158996355

69.4021592525

62.5159977499

63.6020040673

87.2879966831

69.3728848889

62.4990089889

63.5540402019

87.2644571374

69.342231105

62.482397756

63.5099134458

87.242088686

69.3072857914

62.4703168593

63.4652385312

87.2188732511

69.2728002845

62.4548382104

63.4156301904

87.1976711517

69.2386213154

62.4355842812

63.3761627811

87.1768005591

69.2056684977

62.4208606884

63.3312137873

87.1528942256

69.1710297219

62.4057595675

63.2922945365

87.1276339321

69.1391497866

62.3883932785

63.257212395

87.1043879923

69.1060437

62.3744247417

63.2188413026

87.0828209938

69.073703958

62.3581910367

63.1796479726

87.0634398374

69.0379922998

62.3396921637

63.1371656919

87.0416941003

69.0047329442

62.3253460988

63.0930389357

87.0216292608

68.9731595468

62.3064696977

63.0415120403

86.998523673

68.9434253764

62.2883483527

62.9949185711

86.9745683373

68.9144575506

62.2724921757

62.9436657549

86.9489186926

68.8830374221

62.2566359988

62.9028279495

86.9274819359

68.8531499828

62.2419124059

62.8567826387

86.9026627093

68.8238756192

62.2283213972

62.8143003579

86.8788498504

68.7915358772

62.2143528603

62.7657883341

86.8533408964

68.7562840257

62.1992517395

62.7227578949

86.8279934559

68.7263965864

62.1864157867

62.6704087618

86.8006099063

68.6911447349

62.1675393856

62.624363451

86.7764308271

68.656659228

62.1539483768

62.5750291894

86.7510609146

68.6275381333

62.1433775922

62.5309024333

86.7261912001

68.5979572318

62.1297865834

62.4815681717

86.703683883

68.5682230615

62.1139304065

62.4423748417

86.6786312765

68.5423206141

62.0980742296

62.395233214

86.6539101219

68.5131995193

62.0795753565

62.3502842202

86.6312146344

68.4825457354

62.0557910911

62.2995795625

86.606310505

68.4535779097

62.0425776103

62.2496971424

86.5795348137

68.4230773947

62.0240787372

62.1943331378

86.5559721352

68.3895115013

62.0086000883

62.1395172917

86.5305375864

68.3588577174

61.9897236872

62.0879903963

86.5049259206

68.3275908578

61.9716023422

62.0389302139

86.4799854231

68.296783805

61.9493281889

61.995077537

86.4546982569

68.2667430968

61.9315843719

61.9457432755

86.4265172646

68.2388481534

61.9089326905

61.8999720439

86.3991763167

68.2115662857

61.8896787614

61.8484451485

86.3711471106

68.1830582667

61.8692922482

61.7993849662

86.344978309

68.1560829369

61.8507933751

61.7440209616

86.3189715784

68.129107607

61.8262540537

61.6966052546

86.2948276001

68.100599588

61.8066225966

61.6439820423

86.2703366652

68.0713252244

61.7900113636

61.5968404146

86.2463492195

68.0455760459

61.7711349625

61.5442172023

86.2204829379

68.0153820688

61.7522585614

61.4976237331

86.1940981439

67.9858011673

61.7330046323

61.4452746

86.1683864789

67.9557604591

61.7148832872

61.3992292892

86.1409636009

67.9264860954

61.6910990218

61.3493468692

86.1133615801

67.8953725048

61.6737327328

61.3076868261

86.0869439546

67.8697765952

61.6529686916

61.2586266438

86.0603477047

67.8424947275

61.6363574586

61.2131294915

86.0310141041

67.8218034234

61.6167260015

61.1635211507

86.0057655559

67.7983532787

61.6001147685

61.1177499191

85.981533628

67.7755162097

61.5823709515

61.0673193407

85.9537096836

67.7519127961

61.5634945504

61.0196295545

85.9277553107

67.7283093825

61.5453732053

60.9697471345

85.9043555055

67.7011807838

61.5280069163

60.9163016845

85.8783862166

67.6755848742

61.5102630993

60.8688859776

85.8505288424

67.64922262

61.4872338899

60.8214702706

85.8260821051

67.6213276767

61.4676024328

60.7759731183

85.7988918902

67.5954252293

61.4494810877

60.726912936

85.7749436847

67.5681433616

61.4340024388

60.684156576

85.7523578225

67.5431605277

61.4162586218

60.629614809

85.7304506977

67.5189440385

61.4045552531

60.5811027852

85.7078531105

67.4938079357

61.3890766042

60.5249165429

85.6861058674

67.470204522

61.3743530114

60.4747600436

85.6607556574

67.4456814949

61.3524563861

60.4196701182

85.6333415831

67.4223846192

61.3362226811

60.3821212636

85.6067758271

67.3934167934

61.316591224

60.3300462098

85.5786585643

67.3696601108

61.3014901031

60.2892084044

85.5536195676

67.3436043945

61.2792159498

60.240148222

85.5284016651

67.3193879052

61.264869885

60.1965696243

85.5030046984

67.2940985335

61.2459934839

60.1335314013

85.47725683

67.2720278091

61.2278721388

60.0847452982

85.4544205643

67.2476580509

61.2082406817

60.0247219466

85.4307193396

67.224667713

61.1950272009

59.976484002

85.4068397179

67.2024437197

61.1837013602

59.9224903935

85.3832971528

67.1766945412

61.1670901273

59.8728820527

85.359232349

67.1532443965

61.1565193426

59.8177921273

85.3343009337

67.1310204032

61.1440609179

59.7690060243

85.3079860916

67.1081833342

61.1248069888

59.7128197819

85.283383833

67.0853462651

61.1059305877

59.661841045

85.2599792943

67.0629690029

61.0927171069

59.6157957342

85.2386342612

67.0424309677

61.0685553135

59.5648169973

85.2174560835

67.0188275541

61.0451485762

59.5245273504

85.1964448856

66.9953774094

61.024762063

59.4798524357

85.1731887485

66.9685553485

61.0058856619

59.4376442342

85.1494092433

66.9486303889

60.9828564525

59.3896803688

85.1249335428

66.9239540929

60.9692654437

59.3515833557

85.1014854272

66.9034160577

60.9534092668

59.2967675096

85.0776858807

66.8844107117

60.9405733141

59.254559308

85.0530170059

66.86479229

60.921696913

59.1983730657

85.0297216405

66.8433346412

60.9077283761

59.1482165664

85.0069377771

66.8214171857

60.8911171432

59.0909340072

84.9824210435

66.79812031

60.87073063

59.0446146172

84.9613517208

66.7728309383

60.8567620932

58.9854135033

84.9433868604

66.7501471382

60.8416609723

58.943479381

84.9254181997

66.7250110354

60.8242946833

58.8892116933

84.9065815798

66.7040131934

60.8073059223

58.8439886202

84.8887779971

66.6854676541

60.7929598574

58.7897209325

84.8702790579

66.6641632743

60.7691755921

58.7497053648

84.8507384165

66.6446981215

60.7487890789

58.6970821525

84.8315392447

66.6253862377

60.7310452618

58.6510368417

84.8123357268

66.6054612781

60.7148115569

58.6082804817

84.7950315363

66.5835438226

60.699332908

58.5605906956

84.7754735504

66.565764628

60.6883845953

58.514819464

84.7569498816

66.5433873657

60.6740385305

58.464937044

84.7366903941

66.5243820197

60.66460033

58.4191658125

84.7174653762

66.5036907156

60.6464789849

58.3599646986

84.6980627369

66.4843788317

60.6294902239

58.308163724

84.6791755425

66.462921183

60.6102362948

58.2481403724

84.6588974431

66.4448354505

60.5940025898

58.1960653186

84.6413885101

66.4259833734

60.5694632684

58.1453606609

84.6243961815

66.4063649517

60.5577598997

58.0982190332

84.6098286123

66.3846007651

60.5430363069

58.0524478016

84.5957789377

66.365748688

60.5309554102

58.0096914416

84.5822474157

66.3481227623

60.5184969854

57.9573423085

84.5690607732

66.33141645

60.5079262008

57.9129414731

84.555698525

66.3131774486

60.4905599118

57.8575774685

84.5392097241

66.2943253715

60.4822542953

57.8098876823

84.5218496165

66.2777723282

60.4697958706

57.7553459154

84.5057015158

66.2555483349

60.4539396937

57.7131377139

84.4885082107

66.2340906862

60.4448790211

57.6555810754

84.4706165121

66.2146255334

60.4294003722

57.61474327

84.4521997384

66.1973061455

60.4112790272

57.5604755823

84.4358645218

66.1787606062

60.3954228503

57.5086746077

84.4230026598

66.1646598656

60.3795666733

57.4555032369

84.4070095037

66.1451947128

60.3580475761

57.4039763415

84.3929260639

66.1300210898

60.3455891514

57.3483382576

84.3786663601

66.1114755505

60.3278453343

57.3011966299

84.3659697178

66.0947692383

60.3123666854

57.2529586853

84.3487479304

66.0753040855

60.2991532046

57.2085578499

84.3355247781

66.0607435382

60.2870723079

57.1633347768

84.3214293989

66.04204473

60.270083547

57.1120819607

84.3101165878

66.0234991907

60.2553599541

57.0635699368

84.2958428757

66.0051069204

60.2447891695

57.0112208037

84.2841784141

65.9876342636

60.2304431046

56.9564049575

84.2700744464

65.9693952622

60.2160970398

56.899944636

84.2557939509

65.9536085634

60.201750975

56.8560919591

84.2408142449

65.9367489823

60.1889150222

56.7974390037

84.2260061038

65.9191230566

60.1764565975

56.750297376

84.2127636785

65.9022634754

60.1643757008

56.6971260052

84.2002163018

65.884024474

60.1538049162

56.6527251698

84.1873184382

65.8697704645

60.1409689634

56.5965389275

84.1744185982

65.8536772279

60.1319082909

56.5546048052

84.1616911431

65.8371241846

60.11680717

56.4975963251

84.1493105388

65.8198047967

60.1047262733

56.4504546974

84.1386722266

65.8035582912

60.0900026804

56.4016685944

84.1276837052

65.7856258277

60.0771667277

56.3567196005

84.1177404727

65.76968586

60.0556476304

56.3032741505

84.1069236922

65.7520599343

60.0409240376

56.2624363451

84.0929645

65.7370395802

60.0209150524

56.2092649743

84.0786539229

65.7217126882

60.0095892118

56.1604788712

84.0664356492

65.7019409976

59.995998203

56.1147076397

84.0536918433

65.6826291137

59.9933555068

56.0634548235

84.0405968794

65.6677620285

59.9808970821

56.017683592

84.0268013105

65.6551939771

59.9733465216

55.973830915

84.0131781465

65.6386409338

59.9578678727

55.9261411289

83.998155174

65.6257663446

59.944276864

55.8721475204

83.9827800483

65.6130450243

59.9250229348

55.8299393189

83.9696740258

65.5980246702

59.9155847343

55.7792346612

83.9581390336

65.5814716269

59.8989735013

55.7397672519

83.9464276476

65.5662980038

59.8846274365

55.6918033865

83.9357636214

65.5486720781

59.8717914837

55.649595185

83.9261473541

65.533498455

59.8619757552

55.6046461911

83.9144315032

65.5180182942

59.8468746343

55.5618898311

83.9018395115

65.5003923684

59.8370589057

55.5076221434

83.8887208436

65.4847589386

59.8302634013

55.4676065757

83.8756001238

65.4694320467

59.8196926167

55.4221094234

83.8616024267

65.4548714993

59.8057240799

55.3752418749

83.8476023929

65.4407707587

59.7966634073

55.3275520888

83.8339501088

65.42498406

59.7834499266

55.2806845403

83.8216961658

65.4101169748

59.77325667

55.2379281803

83.8082147591

65.3949433518

59.7623083573

55.1910606318

83.7947311834

65.3802295355

59.7543802689

55.1411782118

83.7840478492

65.3649026436

59.739279148

55.1080146249

83.7707355595

65.3517215165

59.7275757793

55.0696435326

83.7577715601

65.3340955908

59.7128521865

55.0230500633

83.7451560129

65.3192285056

59.6966184815

54.9797455448

83.7318375399

65.3028287312

59.6796297205

54.9323298379

83.7174652321

65.2842831919

59.6690589359

54.8810770217

83.7044929823

65.2689563

59.6588656793

54.842157771

83.6890639057

65.2559284418

59.6498050068

54.8015940448

83.6718781766

65.2445865418

59.6335713018

54.7624007148

83.6560922541

65.2294129187

59.6256432134

54.7262222563

83.6411805916

65.2173046741

59.6094095084

54.6851103717

83.6290738751

65.2009048997

59.5958184996

54.6426280909

83.61784289

65.1871106969

59.5754319864

54.602338444

83.6078390236

65.1700978469

59.5705241222

54.5579376086

83.5955519359

65.1563036441

59.5554230013

54.5214850709

83.5827363347

65.1405169454

59.5414544645

54.469410017

83.568162784

65.1253433224

59.5271083996

54.4272018155

83.5534110603

65.1086370102

59.517292671

54.3904751986

83.5393593779

65.0913176222

59.5040791903

54.3452521255

83.5256567114

65.0747645789

59.4938859337

54.2989327355

83.5119517967

65.0588246113

59.4855803172

54.2586430885

83.5003535734

65.0454902153

59.4772747007

54.2216423924

83.4854140939

65.0295502477

59.4625511079

54.1829972208

83.4717025718

65.0151429692

59.4508477392

54.1454483662

83.4574612992

65.0001226151

59.4380117864

54.102417927

83.4418106786

64.9840293786

59.430083698

54.0665135477

83.4245740144

64.9670165285

59.4168702172

54.0303350893

83.4108524912

64.9523027122

59.4112072969

53.9881268877

83.39413733

64.9372823581

59.3953511199

53.9338592

83.3782988232

64.9224152729

59.3874230315

53.8979548208

83.3601688393

64.9072416499

59.3730769666

53.8513613515

83.3439717327

64.8922212958

59.3636387661

53.8149088138

83.3270670474

64.8793467066

59.3462724771

53.7751673254

83.3115680726

64.865092697

59.3398545007

53.7389888669

83.2948329876

64.8503788808

59.3255084359

53.7025363292

83.27985664

64.8373510226

59.3153151793

53.665535633

83.2610002313

64.8226372063

59.3039893386

53.6288090161

83.2416106854

64.8054710874

59.293796082

53.5885193692

83.22292194

64.788918044

59.2820927133

53.5435703753

83.2044053649

64.7751238413

59.2730320408

53.4931397969

83.1846498084

64.758570798

59.2613286721

53.4536723876

83.1647131072

64.7446233263

59.2515129435

53.4227014345

83.143712652

64.7277637452

59.2454724952

53.3761079653

83.1227068911

64.7136630046

59.2401871029

53.3445888537

83.1020489918

64.6964968856

59.2299938463

53.2993657807

83.0859781857

64.6817830693

59.2216882298

53.265379956

83.0707875335

64.6643104125

59.2126275573

53.2174160906

83.0555941029

64.6502096719

59.1990365485

53.1858969791

83.0386307108

64.6359556624

59.1831803716

53.1412220645

83.0198962722

64.6197091569

59.1722320589

53.1069621606

82.9974447254

64.6053018785

59.1590185782

53.0584501368

82.9760482304

64.5898217176

59.1476927375

53.0236420745

82.9553538095

64.5760275148

59.1367444249

52.962522406

82.9344772829

64.5580950513

59.1310815045

52.9279884229

82.9143034431

64.5438410417

59.1190006078

52.8676909921

82.8950098295

64.5266749228

59.1069197111

52.8304162167

82.8746493128

64.5093555348

59.0925736463

52.7840968267

82.8548151307

64.4915763402

59.0793601655

52.7479183682

82.8356848146

64.4750232969

59.0650141007

52.7010508198

82.8179676188

64.4607692874

59.0555759001

52.6602130144

82.800246632

64.4439097062

59.0468927556

52.6215678428

82.7842945005

64.4301155035

59.0431174754

52.573055819

82.7672755048

64.4123363088

59.036321971

52.536329202

82.7481249506

64.3963963412

59.0261287144

52.4932987628

82.7293247257

64.3758583059

59.0159354578

52.4521868782

82.711939584

64.3593052626

59.002721977

52.4097045974

82.6897593539

64.341526068

58.9921511924

52.3661259997

82.6721883888

64.3248197558

58.9800702957

52.3173398966

82.6590520968

64.3073470989

58.967989399

52.2666352389

82.6443156632

64.290027711

58.9536433342

52.2200417697

82.6285110253

64.2733213988

58.9449601897

52.165774082

82.6189202207

64.2549291285

58.9257062605

52.1276770689

82.607196614

64.2408283879

58.9102276116

52.0750538566

82.5929839506

64.2241220756

58.9019219952

52.0372309227

82.5821451512

64.2084886458

58.8958815468

51.9791261258

82.5723712435

64.191015989

58.8856882902

51.9328067358

82.5609965125

64.1744629457

58.8785152578

51.8651091658

82.5506868087

64.1560706754

58.8739849215

51.8229009642

82.5432203572

64.1366055226

58.865679305

51.7587664242

82.5332640379

64.1202057482

58.8558635765

51.7160100642

82.5261516459

64.1010471333

58.8494456001

51.6587275049

82.5153040677

64.084340821

58.8396298715

51.6061042926

82.5074786997

64.0656420129

58.830191671

51.5493698918

82.4957392559

64.0490889695

58.8192433583

51.4978429965

82.4902246981

64.0328424641

58.8090501017

51.4394641203

82.475458099

64.0175155721

58.7981017891

51.3989003941

82.4695863069

64.002495218

58.7826231402

51.3399733595

82.4592651743

63.985329099

58.7709197715

51.2963947618

82.4548160118

63.96816298

58.7588388748

51.2374677272

82.4476968524

63.949157634

58.7433602259

51.1903260995

82.4469849027

63.9335242042

58.7342995534

51.1311249856

82.4428910723

63.9143655893

58.7252388809

51.082887041

82.4366609403

63.8970462014

58.7191984325

51.0264267194

82.4306083612

63.8778875864

58.7082501199

50.978462854

82.4231310323

63.859648585

58.7003220314

50.9269359586

82.4168994066

63.8415628525

58.6886186627

50.8781498556

82.4099550401

63.8217911619

58.6863534946

50.8364898125

82.4063935995

63.8040119672

58.676915294

50.7871555509

82.3967769409

63.7868458483

58.6720074298

50.7501548548

82.3908995414

63.7709058806

58.6674770935

50.7068503363

82.3834186084

63.7503678454

58.6633242852

50.6745089871

82.3762932786

63.7333549953

58.6527535006

50.6336711817

82.3686328617

63.7151159939

58.6455804682

50.5969445647

82.3645351369

63.6968769925

58.6338770995

50.5519955709

82.3579427171

63.6783314532

58.6206636188

50.5160911916

82.3518843525

63.6593261072

58.6063175539

50.4673050886

82.3454691277

63.6383282652

58.5957467693

50.4289339962

82.337984067

63.6179434989

58.5780029523

50.3941259339

82.3328154137

63.5981718083

58.5636568874

50.3595919508

82.3265769517

63.5773272353

58.5545962149

50.3294432355

82.3217641008

63.5572490068

58.5470456545

50.3061465008

82.3158813454

63.5414623081

58.5364748698

50.2729829139

82.3137420574

63.5253690716

58.5372299259

50.2403674854

82.3062541114

63.5072833391

58.5357198138

50.2074779777

82.3012617689

63.4878181863

58.5323220616

50.1693809646

82.2937726873

63.4688128403

58.5202411649

50.1312839516

82.2873529321

63.4479682672

58.5100479083

50.1036019493

82.2791491825

63.4304956104

58.4930591473

50.0750977092

82.276117155

63.4105706508

58.4809782506

50.04988242

82.2677339092

63.3929447251

58.4658771297

50.0304227946

82.2597065967

63.3751655304

58.4583265693

50.0057556638

82.2541762145

63.3564667223

58.4511535369

49.97862182

82.2475749491

63.33408946

58.4447355605

49.9473767877

82.2411515876

63.3172298789

58.4402052242

49.9199688646

82.2365121812

63.2951591544

58.4352973599

49.8865311984

82.2324078727

63.2756940017

58.4228389352

49.8615899884

82.22758951

63.2574550002

58.419818711

49.8311671938

82.2222354426

63.2366104272

58.4122681506

49.8078704592

82.2156316125

63.2159191231

58.4028299501

49.7823810907

82.2109907659

63.1973735838

58.3964119737

49.7610029107

82.2072421986

63.177908431

58.3922591654

49.7377061761

82.1990304537

63.1582900093

58.3790456847

49.717424313

82.1942101344

63.1386715876

58.3745153484

49.6976906084

82.1859970874

63.1192064348

58.3613018676

49.6752161115

82.1777832196

63.0988216685

58.3526187231

49.6598676745

82.1670682449

63.0824218942

58.3443131066

49.6395858115

82.1626032598

63.0628034725

58.3382726583

49.6261559292

82.154387053

63.0460971602

58.3250591775

49.6055999868

82.1492068482

63.0281646967

58.3171310891

49.5907997084

82.1438476718

63.0129910736

58.3001423281

49.5625695476

82.1370588797

62.993219383

58.2929692956

49.5431099222

82.1299121766

62.9745205748

58.2827760391

49.5154279199

82.1236583012

62.9553619599

58.2733378385

49.4970646114

82.116153022

62.9352837314

58.2605018858

49.4792494614

82.1098980986

62.9156653097

58.2586142456

49.468012213

82.1063236427

62.8935945853

58.2450232368

49.4521156176

82.1011404053

62.8742827015

58.2355850363

49.4411524483

82.0975655681

62.8540512041

58.2348299803

49.4263521699

82.0943480816

62.8365785473

58.2386052605

49.4101814953

82.0879127301

62.816193781

58.2363400923

49.3940108206

82.0841585421

62.7965753593

58.2336973962

49.3792105422

82.079152691

62.776037324

58.229922116

49.3622176299

82.0737889403

62.7554992888

58.2174636912

49.3446765591

82.0666367274

62.7337351023

58.2099131308

49.324394696

82.0662791004

62.7122774535

58.1982097621

49.3027424368

82.0596627196

62.6938851832

58.1906592017

49.2841050491

82.0537611731

62.6725808034

58.1815985292

49.2613564729

82.0462495

62.6532689195

58.1732929127

49.2399782929

82.040168118

62.6339570357

58.1646097682

49.2224372222

82.0319396483

62.6158713032

58.1540389835

49.2043479929

82.0247837863

62.5967126882

58.1476210072

49.1843402091

82.0213845331

62.5795465692

58.1400704467

49.1736511191

82.0145856041

62.5626869881

58.1355401105

49.1607693952

82.0085018741

62.5435283731

58.1223266297

49.1451468791

82.0004491844

62.5257491785

58.1211940456

49.1330873929

81.9916798007

62.5055176811

58.1143985412

49.1188352729

81.9845204246

62.4863590662

58.110245733

49.103486836

81.9809405022

62.4653612242

58.1068479808

49.0906051121

81.9748542752

62.4454362647

58.1011850605

49.0766270714

81.9687675963

62.4245916916

58.0891041638

49.0601823175

81.9632175833

62.4040536564

58.0777783231

49.0437375637

81.9590995889

62.385661386

58.0702277627

49.0253742552

81.9533698612

62.3645102751

58.0668300105

49.0138629275

81.9508629794

62.3474974251

58.0619221462

49.0020775206

81.9481769494

62.3280322723

58.0600345061

48.988373559

81.9449535973

62.3119390358

58.058524394

48.9790548652

81.9379692326

62.2920140762

58.0505963055

48.9763140729

81.9300887218

62.2763806464

58.0468210253

48.9582248436

81.9222074529

62.2547697288

58.042290689

48.9450690406

81.9139671338

62.2340784246

58.0358727127

48.9365725844

81.9069801268

62.2153796165

58.0286996802

48.9256094152

81.9016051005

62.193462161

58.025301928

48.9058757106

81.8958713503

62.1721577812

58.0139760874

48.8943643829

81.8915707741

62.1519262838

58.0045378868

48.8798381836

81.8847610667

62.1323078621

57.9977423824

48.8644897467

81.875979292

62.1090109863

57.9913244061

48.8557192113

81.8713191924

62.0935308254

57.9867940698

48.8447560421

81.8671965754

62.0746787483

57.9807536214

48.835163269

81.8600263123

62.0573593604

57.9796210374

48.8277631298

81.8548274787

62.0388138212

57.9701828368

48.8165258813

81.8476561319

62.0248663495

57.9637648604

48.8047404744

81.8408427705

62.0035619697

57.9535716039

48.7951477013

81.829366353

61.9850164304

57.9497963236

48.7808955813

81.8230895064

61.9666241601

57.9407356511

48.7702064913

81.807843731

61.9465459316

57.9380929549

48.7669175405

81.7995918911

61.9235555937

57.9312974506

48.7551321336

81.7902627217

61.9027110206

57.9252570022

48.7381392213

81.7827268465

61.8795674138

57.9177064418

48.7340280328

81.7777025439

61.856270538

57.9131761055

48.7271760521

81.7741135673

61.8377249988

57.9127985775

48.7173091997

81.7671146099

61.8179533082

57.9094008253

48.7085386644

81.7619098685

61.7968021973

57.9097783533

48.7047015551

81.7534738944

61.7788697337

57.9071356571

48.6970273367

81.7473707321

61.7609372701

57.9022277929

48.6857900882

81.7371379377

61.7407057727

57.8935446484

48.6770195528

81.7312131027

57.8939221764

48.671263889

81.7188234233

57.886749144

48.6652341459

81.7109217773

57.8810862236

48.6539968974

81.6979901625

57.8765558874

48.648789392

81.6870326092

57.8754233033

48.6397447774

81.6758939175

57.8663626308

48.6301520043

81.6676287452

57.8576794863

48.6265889743

81.6597221453

57.8557918461

48.6183665974

81.6500175446

57.85314915

48.6164480428

81.6475013487

57.8505064538

48.614255409

81.6370762824

57.8505064538

48.6087738243

81.6280880876



Sheet1

		20.3189		100.0192539291		21.9831		99.9682068092		20.9024		99.9813615325		26.6406		99.9992336554				99.962726539

		20.3213		100.0403954984		21.9905		99.9783477408		20.9123		99.9860581667		26.6468		100.0050578743				99.9721182772

		20.3498		100.0596494275		21.9954		99.9854738008		20.8975		99.9917818914		26.6456		100.0160932365				99.9835644581

		20.351		100.0792808846		22.0226		100.0021926338		20.9086		100.0004402368		26.6691		100.0254426406				100.0008804755

		20.3609		100.0989123418		22.0301		100.0063038223		20.9111		100.0076304962		26.6641		100.0357116582				100.0152615746

		20.3547		100.0940044775		22.0263		100.0189114669		20.8876		100.0130595332		26.6444		100.0406162637				100.0261207719

		20.3634		100.0913617813		22.0387		100.0126076446		20.8777		100.0154071336		26.6431		100.0433751042				100.030816641

		20.3572		100.0909842533		22.0461		100.0087705354		20.9037		100.0161407474		26.6308		100.0430685664				100.0322841001

		20.3807		100.0868314451		22.0523		99.9950665738		20.9086		100.0101249552		26.6172		100.0419956839				100.0202509355

		20.3943		100.0838112209		22.0449		99.9876664346		20.9296		100.0076304962		26.627		100.0393901123				100.0152615746

		20.4413		100.0781483006		22.0684		99.9802662954		20.968		100.0042555408		26.6604		100.0335658934				100.0085112627

		20.4833		100.0773932445		22.0857		99.9764291861		20.9865		100.0013207045		26.6592		100.0335658934				100.0026414264

		20.5253		100.0713527962		22.1042		99.9712216808		20.9915		99.9986792781		26.6753		100.0291210947				99.9973585736

		20.5587		100.0713527962		22.1314		99.9703994431		21.0384		99.998092285		26.7272		100.0254426406				99.9961846064

		20.6069		100.067955044		22.1908		99.9720439185		21.0558		99.9961845336		26.7445		100.0217641866				99.9923692127

		20.6749		100.0653123478		22.2378		99.9594362738		21.099		99.9941299913		26.7606		100.0249828339				99.9882603272

		20.7108		100.0554966192		22.2786		99.9583399569		21.1485		99.9928091919		26.8125		100.020997842				99.9856189009

		20.7615		100.0536089791		22.3033		99.9473767877		21.1905		99.9894337363		26.8533		100.0214576487				99.978868589

		20.8295		100.051343811		22.3342		99.9427174408		21.2338		99.9879661114		26.8694		100.0202314974				99.9759336708

		20.9049		100.0449258346		22.3762		99.9287394		21.3105		99.9851775646		26.8916		100.0179324636				99.9703573263

		20.9655		100.0388853863		22.4257		99.9306579546		21.371		99.9828292544		26.9287		100.0147138163				99.9656614572

		21.0286		100.0362426901		22.4875		99.9191466269		21.4304		99.9768114578		26.9683		100.0128745892				99.9536282926

		21.1114		100.0369977462		22.5803		99.9221614984		21.5194		99.9744629511		27.0338		100.0105755554				99.9489324235

		21.1621		100.0324674099		22.673		99.9128428046		21.601		99.973288677		27.0783		100.0102690176				99.946584489

		21.2153		100.03435505		22.741		99.9139391215		21.6851		99.971086876		27.1463		100.007663446				99.9421821117

		21.2684		100.033599994		22.7929		99.9081834577		21.763		99.967270306		27.1933		100.0055176811				99.9345513244

		21.3377		100.0362426901		22.8622		99.9065389823		21.8298		99.9658023557		27.2366		100.0058242189				99.9316164062

		21.3958		100.0283146017		22.9017		99.8985906846		21.8743		99.9624259881		27.2626		100.0026055716				99.9248660944

		21.4959		100.0283146017		22.9351		99.8942054169		21.9299		99.9558197218		27.3021		100.0006130757				99.9116589625

		21.5874		100.0207640412		22.9697		99.89667213		21.9905		99.9544984161		27.3874		100.0013794203				99.9090175361

		21.674		100.0188764011		23.0489		99.8933831792		22.0634		99.952443017		27.4653		99.9995401932				99.9049086507

		21.7754		100.0143460648		23.107		99.89667213		22.1314		99.9498002989		27.5358		99.996168277				99.8996257979

		21.8718		100.0135910088		23.1873		99.8936572584		22.244		99.9467170395		27.6199		99.9941757811				99.8934624697

		21.9695		100.0098157286		23.2776		99.8958498923		22.3342		99.9456892652		27.7015		99.9929496297				99.891408027

		22.0721		100.0090606725		23.3703		99.8848867231		22.3997		99.9430463685		27.7435		99.9900375202				99.8861251743

		22.171		100.0052853923		23.4457		99.8796792177		22.4999		99.9405502353		27.8078		99.9877384864				99.8811358133

		22.2625		99.999244944		23.5212		99.8643307807		22.6161		99.9355577818		27.8795		99.9862057972				99.8711570915

		22.3824		99.9958471918		23.6176		99.8547380077		22.6965		99.9321803923		27.9463		99.9829871499				99.8644067797

		22.4974		99.9886741593		23.7227		99.8462415515		22.7966		99.9270406677		28.0217		99.9832936878				99.854134566

		22.5889		99.9852764071		23.8031		99.8382932538		22.9265		99.9223412595		28.0922		99.9825273432				99.8447428278

		22.7064		99.9837662951		23.923		99.835004303		23.013		99.9167604252		28.154		99.9829871499				99.8335901387

		22.8176		99.983388767		24.0207		99.83966365		23.1206		99.9152917328		28.2356		99.9834469567				99.8306552205

		22.9116		99.9856539352		24.0689		99.8424044423		23.2195		99.9123542832		28.3321		99.984826377				99.8247853841

		23.0303		99.983011239		24.1542		99.8382932538		23.3073		99.9095636261		28.4631		99.9808413851				99.8192090395

		23.1478		99.9796134868		24.2593		99.8418562838		23.4049		99.9061853579		28.5769		99.9840600324				99.8124587277

		23.2343		99.9750831505		24.3372		99.8336339069		23.5286		99.903982078		28.7018		99.9825273432				99.8080563504

		23.3468		99.9735730385		24.4262		99.8382932538		23.6374		99.8984002181		28.7994		99.9806881161				99.7969036613

		23.4853		99.966400006		24.5758		99.827878243		23.7586		99.8926711428		28.8996		99.9802283094				99.7854574804

		23.5991		99.9603595577		24.6834		99.8262337677		23.8884		99.887823207		28.9886		99.9799217715				99.7757722503

		23.7252		99.9603595577		24.8083		99.8160928361		24.0182		99.8810650858		29.0677		99.9754769729				99.7622716267

		23.8624		99.9569618055		24.9282		99.8149965192		24.1159		99.875481945		29.1852		99.9730246702				99.7511189376

		23.9836		99.9520539412		25.037		99.79334426		24.2655		99.8731310556		29.2804		99.9716452499				99.7464230685

		24.0862		99.9497887731		25.1458		99.7960850523		24.4126		99.8704862388		29.3966		99.9701125607				99.7411402157

		24.2185		99.9520539412		25.2571		99.7829292492		24.5598		99.8690168659		29.5017		99.9664341066				99.7382052975

		24.3558		99.9471460769		25.3721		99.7788180607		24.7081		99.8672535898		29.6377		99.9678135269				99.7346833957

		24.5016		99.9426157407		25.4994		99.7716920007		24.838		99.8665188823		29.7527		99.9653612242				99.7332159366

		24.6636		99.9380854044		25.6688		99.7662104161		24.9492		99.8631391579		29.8714		99.9636752661				99.7264656248

		24.812		99.9369528203		25.8308		99.7610029107		25.084		99.8597593192		29.9988		99.9652079553				99.7197153129

		24.9505		99.9354427082		25.9816		99.7634696238		25.1953		99.8538810664		30.1014		99.9644416107				99.7079756402

		25.0976		99.9350651802		26.1387		99.7623733069		25.3189		99.8502069826		30.23		99.9627556526				99.7006383447

		25.2509		99.9324224841		26.2722		99.7599065938		25.5019		99.845650931		30.3397		99.9621425769				99.6915400983

		25.3894		99.9350651802		26.3785		99.7596325146		25.6354		99.8422705003		30.4879		99.959996812				99.6847897865

		25.5452		99.930912372		26.4947		99.7503138207		25.7504		99.838449006		30.6255		99.9578510471				99.6771589992

		25.6775		99.9278921478		26.6172		99.7497656623		25.9124		99.8353623076		30.7844		99.9547856687				99.670995671

		25.8197		99.9282696758		26.7321		99.7560694846		26.041		99.8312465614		30.9125		99.9517202904				99.6627779001

		25.9693		99.9305348439		26.8447		99.7546990884		26.1708		99.8262486414		31.0679		99.9514137525				99.6527991782

		26.1139		99.9297797879		26.9943		99.7552472469		26.3501		99.8199273843		31.1711		99.9492679876				99.64017903

		26.2759		99.9305348439		27.155		99.7599065938		26.5244		99.8124295603		31.3086		99.9480418363				99.6252109472

		26.4601		99.9282696758		27.2947		99.7470248699		26.6716		99.8068425801		31.4616		99.9489614498				99.6140582581

		26.6295		99.9263820357		27.4381		99.7385284138		26.8459		99.801549363		31.5873		99.9480418363				99.6034925526

		26.7878		99.9233618115		27.6001		99.7311282746		26.9757		99.7961088196		31.719		99.9475820295				99.5926333553

		26.9671		99.9195865313		27.7658		99.7185206299		27.134		99.7921385061		31.8708		99.9455895336				99.5847090762

		27.1204		99.9169438352		27.8845		99.7092019361		27.2638		99.7890503753		32.0167		99.9460493403				99.578545748

		27.2861		99.914301139		28.0304		99.710298253		27.4418		99.7852268428		32.1364		99.9462026093				99.5709149607

		27.4542		99.9082606906		28.1862		99.699609163		27.5914		99.7803736868		32.2811		99.9435970376				99.5612297307

		27.6174		99.9033528264		28.3642		99.7034462722		27.7856		99.7752261421		32.4092		99.9426774241				99.5509575171

		27.7868		99.89693485		28.5089		99.706735223		27.9216		99.7697841632		32.5658		99.9393055079				99.5400983198

		27.9426		99.8893842895		28.6622		99.7026240346		28.0984		99.7643418875		32.7199		99.9359335916				99.5292391225

		28.0835		99.8844764253		28.8551		99.7001573215		28.2702		99.7588993149		32.8528		99.9331747511				99.5183799252

		28.248		99.8822112571		29.0294		99.6949498161		28.4656		99.7527208996		33.0141		99.9328682133				99.5060532688

		28.4495		99.8867415934		29.1827		99.6850829638		28.6226		99.7468363388		33.2204		99.9313355241				99.494313596

		28.6164		99.8833438412		29.3472		99.6708308438		28.8118		99.7403629209		33.3758		99.929496297				99.481399956

		28.8217		99.8837213692		29.5524		99.6661714969		29.0109		99.7362432544		33.5229		99.9301093727				99.473182185

		29.0356		99.8825887852		29.7119		99.6587713576		29.158		99.7302105786		33.6818		99.9271972632				99.4611490205

		29.2124		99.879946089		29.9035		99.6590454369		29.3472		99.7250604446		33.8217		99.9267374565				99.4508768068

		29.4016		99.8712629445		30.0668		99.6500008222		29.545		99.7194685694		33.9486		99.9239786159				99.4397241177

		29.587		99.8712629445		30.2708		99.6530156938		29.6995		99.7137292136		34.1052		99.9241318848				99.4282779368

		29.7675		99.8693753044		30.4239		99.6475341092		29.8899		99.7074008229		34.3198		99.9229057335				99.4156577885

		29.9221		99.8686202483		30.584		99.6431488415		30.1224		99.7003360983		34.5096		99.9207599686				99.4015701812

		30.1187		99.8640899121		30.7572		99.635474623		30.3112		99.6934180705		34.6804		99.9198403551				99.3877760657

		30.3136		99.862957328		30.9339		99.6288967215		30.4998		99.6872355968		34.8761		99.9203001619				99.3754494093

		30.501		99.8595595758		31.1094		99.6278004045		30.6812		99.6809055241		35.0302		99.9170815145				99.3628292611

		30.6884		99.8576719357		31.298		99.621222503		30.8283		99.6736916955		35.1915		99.9155488253				99.348448162

		30.8864		99.8516314873		31.5008		99.6204002653		30.9872		99.6682441727		35.3552		99.914322674				99.3375889647

		31.0726		99.8482337351		31.6704		99.610533413		31.1687		99.6633853201		35.5165		99.9114105645				99.3279037347

		31.2541		99.844835983		31.8672		99.6110815715		31.3596		99.6570537325		35.711		99.908498455				99.3152835865

		31.4593		99.8395505906		32.0463		99.5968294515		31.5684		99.6517525591		35.9434		99.9054330767				99.304717881

		31.6466		99.8342651983		32.2266		99.5940886591		31.7925		99.6454202323		36.1486		99.9026742361				99.2920977328

		31.8471		99.8331326143		32.4068		99.5833995691		32.0048		99.6357000641		36.3348		99.8997621266				99.2727272727

		32.057		99.8331326143		32.6002		99.5792883807		32.2064		99.6249478645		36.5412		99.8977696307				99.2513023699

		32.2479		99.8338876703		32.7591		99.5746290338		32.395		99.6152256986		36.7131		99.8977696307				99.2319319099

		32.4341		99.8387955346		32.9311		99.5691474491		32.5907		99.6071231689		36.8875		99.897156555				99.2157898599

		32.6334		99.8365303665		33.1362		99.5718882415		32.7828		99.5994619891		37.101		99.8951640591				99.2005282853

		32.8314		99.8403056467		33.3106		99.5798365391		32.9785		99.5973992631		37.2765		99.8936313699				99.1964193998

		33.0485		99.8384180066		33.4837		99.5779179845		33.1576		99.5947471241		37.465		99.8934781009				99.1911365471

		33.2477		99.8361528384		33.6984		99.578466143		33.345		99.5913581769		37.6655		99.8916388739				99.1843862352

		33.4446		99.8308674461		33.9249		99.5809328561		33.5608		99.5869376378		37.8944		99.8890333023				99.1755814807

		33.6557		99.8308674461		34.1147		99.5685992907		33.7589		99.5811906435		38.0746		99.8879604198				99.1641352997

		33.8787		99.8214292456		34.321		99.5540730914		33.9451		99.5723484661		38.2857		99.8879604198				99.1465257906

		34.0898		99.8202966615		34.5475		99.549961903		34.136		99.5649793851		38.4731		99.8870408063				99.1318511996

		34.2926		99.8206741895		34.7551		99.5398209714		34.3685		99.5584941427		38.6653		99.8839754279				99.1189375596

		34.5381		99.8202966615		34.9448		99.5326949114		34.5772		99.5496499494		38.8681		99.8829025455				99.1013280505

		34.7314		99.8146337412		35.1429		99.5277614853		34.8002		99.5427214491		39.0578		99.8795306293				99.087533935

		34.9472		99.8123685731		35.3659		99.5181687122		35.0219		99.5350553124		39.2381		99.8775381333				99.0722723604

		35.1382		99.8078382368		35.5556		99.5137834445		35.2307		99.5267988125		39.4539		99.8787642847				99.0558368185

		35.3635		99.7972674522		35.7703		99.5110426522		35.4192		99.5175094312		39.6425		99.878151209				99.037346834

		35.5331		99.793492172		35.9802		99.5113167314		35.6256		99.5107261607		39.9022		99.8753923684				99.0238462103

		35.7738		99.7900944198		36.183		99.5099463353		35.8403		99.5009928344		40.1359		99.8735531414				99.0044757502

		35.9897		99.7885843077		36.3941		99.514331603		36.0395		99.491406052		40.3316		99.8718671833				98.985398782

		36.2103		99.7859416115		36.6028		99.5110426522		36.2625		99.4827034035		40.5439		99.8706410319				98.9680827647

		36.4226		99.7882067796		36.8246		99.5061092261		36.4997		99.4732623815		40.7751		99.8668093089				98.9492992883

		36.6823		99.7855640835		37.0251		99.5006276414		36.7333		99.4647056814		40.9732		99.8646635441				98.9322767628

		36.9029		99.7866966676		37.2267		99.4926793437		36.9492		99.4589516242		41.208		99.8631308549				98.9208305818

		37.1045		99.7874517236		37.439		99.4806198576		37.2065		99.4530496813		41.4155		99.8594524008				98.9090909091

		37.3287		99.7844314994		37.6477		99.4743160353		37.4307		99.4450815027		41.6148		99.8576131738				98.8932423509

		37.5516		99.7791461071		37.8612		99.4660936584		37.6204		99.438736015		41.8295		99.8570000981				98.8806222027

		37.7758		99.777258467		38.0877		99.4548564099		37.8457		99.4297335819		42.0939		99.8513291481				98.8627192017

		37.9964		99.7723506027		38.3296		99.4496489045		38.0687		99.4199923263		42.2849		99.8499497278				98.8433487417

		38.2466		99.7670652104		38.5395		99.4444413991		38.2869		99.4115786556		42.5339		99.8499497278				98.826619708

		38.4672		99.7648000423		38.7779		99.4397820522		38.5158		99.4046405318		42.7687		99.8473441562				98.8128255925

		38.7269		99.7644225143		38.9819		99.4340263883		38.7874		99.397406653		42.9502		99.8439722399				98.7984444934

		38.957		99.7587595939		39.1824		99.4351227053		39.008		99.3897293078		43.1293		99.8435124332				98.7831829188

		39.1847		99.7564944258		39.3875		99.4315596753		39.2286		99.3810177556		43.3674		99.8412133994				98.7658669015

		39.4041		99.7481888093		39.633		99.4307374376		39.4611		99.3717147466		43.5722		99.8415199372				98.7473769169

		39.6662		99.7440360011		39.8465		99.4203224268		39.7018		99.3609339802		43.7917		99.8407535926				98.7259520141

		39.8678		99.7383730807		40.0742		99.4195001891		39.9224		99.3516290906		44.0359		99.8402937859				98.7074620295

		40.0956		99.7376180247		40.3458		99.4115518914		40.1442		99.341437021		44.2407		99.8398339791				98.687211094

		40.3588		99.7338427445		40.5937		99.4101814953		40.3932		99.331539373		44.4882		99.8406003237				98.6675471421

		40.5984		99.7342202725		40.8237		99.4071666237		40.6043		99.3229704633		44.7234		99.8364620629				98.6505246166

		40.8154		99.7315775763		41.0586		99.4036035937		40.8344		99.3157306359		44.9384		99.8341630291				98.6361435175

		41.0669		99.7364854406		41.291		99.4005887222		41.0657		99.3083425129		45.1814		99.8329368777				98.6214689266

		41.2922		99.7364854406		41.5045		99.3923663453		41.3385		99.3027271717		45.3953		99.8269593899				98.6103162374

		41.5175		99.7361079126		41.7334		99.3890773945		41.6053		99.297111513		45.6046		99.8234342047				98.5991635483

		41.7713		99.7398831928		41.9231		99.3841439683		41.852		99.2875050447		45.8173		99.8203688263				98.5800865801

		42.0002		99.7406382489		42.1615		99.3792105422		42.1283		99.2786367105		46.066		99.817150179				98.562477071

		42.2623		99.7342202725		42.3809		99.371810403		42.3952		99.2685849739		46.2741		99.8137782628				98.5425196273

		42.5339		99.7289348802		42.5968		99.3676992145		42.5944		99.2592714272		46.5285		99.8159240277				98.5240296427

		42.7865		99.7289348802		42.834		99.3545434114		42.802		99.2496612964		46.7614		99.8130119182				98.5049526744

		43.0202		99.7202517357		43.0985		99.3452247176		43.032		99.2428597184		47.0191		99.8120923047				98.4914520508

		43.2775		99.7160989274		43.3528		99.3408394499		43.2467		99.2360576742		47.2487		99.8104063466				98.4779514271

		43.4878		99.7108135351		43.6071		99.3427580045		43.4653		99.2292551637		47.4906		99.8082605817				98.4644508034

		43.7253		99.7123236472		43.8446		99.3416616876		43.7118		99.2223042909		47.7112		99.8061148168				98.4506566879

		43.9425		99.708548367		44.0854		99.3438543214		43.9537		99.2155008375		47.9486		99.8045821276				98.4371560643

		44.2047		99.7138337593		44.3228		99.3454987968		44.2024		99.207069824		48.1647		99.8033559763				98.4204270306

		44.4455		99.7096809511		44.5445		99.3485136683		44.4399		99.1999694674		48.4055		99.8005971357				98.4063394233

		44.6762		99.707793311		44.7617		99.3397431329		44.6807		99.1913891917		48.6565		99.7990644465				98.3893168978

		44.917		99.6983551104		45.0081		99.3342615483		44.9485		99.1825122633		48.9007		99.7953859924				98.3717073887

		45.1668		99.6934472461		45.2411		99.3219279829		45.2073		99.1742264133		49.155		99.7929336897				98.3552718468

		45.3728		99.6870292697		45.4673		99.3079499422		45.4628		99.1671237051		49.3992		99.7891019667				98.3411842395

		45.6361		99.6900494939		45.7014		99.2967126937		45.7025		99.1588365692		49.6377		99.7877225465				98.3247486976

		45.9062		99.6885393818		45.95		99.2854754452		45.9579		99.1517327586		49.8651		99.7851169748				98.3106610903

		46.1324		99.6896719659		46.1942		99.2819124152		46.1976		99.1418161718		50.071		99.7815917897				98.2909971385

		46.3563		99.6870292697		46.4306		99.2775271475		46.4418		99.1313064674		50.3006		99.7815917897				98.2701592193

		46.6196		99.6824989335		46.6556		99.2799938606		46.6973		99.1215358836		50.5673		99.7795992937				98.2507887593

		46.8244		99.673438261		46.9167		99.2723196422		46.9741		99.1110240287		50.7912		99.7773002599				98.2299508401

		47.0652		99.6685303967		47.1688		99.2758826722		47.2048		99.0993264288		51.05		99.7745414194				98.2067649864

		47.2993		99.6651326445		47.3927		99.2695788499		47.4512		99.0928107112		51.3302		99.7743881505				98.1938513464

		47.5514		99.6609798362		47.6268		99.2698529291		47.6966		99.0859983664		51.5643		99.769483545				98.1803507227

		47.8035		99.6621124203		47.8699		99.260260156		47.9419		99.078296891		51.786		99.7684106626				98.1650891481

		48.0679		99.6640000604		48.0994		99.2536822545		48.1692		99.0720760314		52.0066		99.7661116288				98.1527624917

		48.3099		99.6647551164		48.3211		99.2369634214		48.4213		99.0657066515		52.2418		99.7654985531				98.1401423435

		48.5799		99.6632450044		48.5664		99.2257261729		48.6688		99.0569666032		52.4893		99.7631995193				98.1228263262

		48.868		99.6655101725		48.8253		99.2142148452		48.9243		99.0470405284		52.7549		99.7607472166				98.1031623743

		49.1223		99.6590921961		49.0908		99.2043479929		49.1865		99.0360762448		53.0261		99.7584481828				98.0814439797

		49.3924		99.6583371401		49.3215		99.2040739137		49.4487		99.0246661745		53.3277		99.7550762666				98.0588451097

		49.6512		99.6488989395		49.5826		99.1947552198		49.7255		99.0166635226		53.5708		99.7512445436				98.0429965515

		49.9089		99.6458787153		49.8471		99.1966737745		49.9832		99.006585189		53.8273		99.7475660896				98.0230391078

		50.1509		99.6428584912		50.0755		99.185436526		50.2207		98.9994704534		54.0749		99.7460334004				98.0089515005

		50.3861		99.6364405148		50.3298		99.1857106052		50.4626		98.9938375917		54.3349		99.7431212909				97.9977988114

		50.6483		99.6322877066		50.6021		99.1763919114		50.7226		98.9885009008		54.5903		99.7417418706				97.9872331059

		50.9296		99.6387056829		50.8824		99.1826957337		50.9881		98.9815331213		54.8581		99.7417418706				97.9734389904

		51.1873		99.6368180428		51.113		99.1703621683		51.2481		98.9758992388		55.1293		99.7377568787				97.9622863013

		51.4619		99.6334202906		51.3685		99.1706362475		51.544		98.9689305721		55.3949		99.7356111138				97.9484921858

		51.723		99.6356854588		51.6262		99.160495316		51.8198		98.9627028377		55.6473		99.7340784246				97.9361655294

		51.9852		99.6307775945		51.885		99.1585767614		52.0887		98.9543985821		55.9145		99.7316261219				97.9197299875

		52.1889		99.6266247862		52.1123		99.1500803052		52.3171		98.944907151		56.1686		99.7274878611				97.9009465111

		52.4533		99.6251146741		52.3813		99.149806226		52.5861		98.9383812638		56.4162		99.7285607435				97.8880328711

		52.6806		99.6243596181		52.6559		99.1487099091		52.8123		98.933486566		56.6736		99.7262617097				97.8783476411

		52.953		99.6251146741		52.8967		99.1478876714		53.07		98.9275532743		56.9321		99.7233496003				97.8666079683

		53.1983		99.6266247862		53.1521		99.1495321468		53.3288		98.9232514152		57.158		99.7210505665				97.8580967056

		53.4999		99.6247371461		53.4076		99.146243196		53.5978		98.9168724522		57.3969		99.7192113394				97.8454765573

		53.7643		99.62209445		53.6495		99.1421320075		53.8532		98.9088610788		57.6391		99.7167590367				97.8296279991

		54.04		99.6171865857		53.8982		99.1300725214		54.1481		98.8998104135		57.8954		99.7129273137				97.8117249982

		54.3304		99.6156764736		54.1694		99.1196575106		54.4238		98.8904621354		58.1386		99.7109348178				97.7932350136

		54.6004		99.6081259131		54.4474		99.1018423606		54.6893		98.8809645671		58.4166		99.7074096326				97.7744515372

		54.8536		99.6077483851		54.7197		99.096360776		54.9898		98.8738407921		58.6849		99.704804061				97.7603639299

		55.1136		99.6013304087		55.0056		99.0815604975		55.2644		98.86612279		58.9651		99.7011256069				97.7451023553

		55.3994		99.5994427686		55.288		99.0799160221		55.5378		98.8606307677		59.2105		99.6992863799				97.734243158

		55.6343		99.5907596241		55.539		99.0719677244		55.7961		98.8548415491		59.4777		99.6966808083				97.722796977

		55.896		99.589249512		55.7538		99.064293506		56.0785		98.8483097159		59.7405		99.6948415812				97.709883337

		56.1665		99.5820764796		56.009		99.0555229706		56.3359		98.8422228465		60.0272		99.6936154299				97.6978501724

		56.4434		99.5805663675		56.2664		99.0533303367		56.5933		98.8353932297		60.3009		99.6907033204				97.6843495488

		56.6942		99.5764135593		56.5151		99.0462042767		56.8517		98.8267813011		60.5724		99.6903967826				97.6673270233

		56.9734		99.5733933351		56.7822		99.0423671675		57.1091		98.8187626238		60.82		99.6888640934				97.651478465

		57.2329		99.5703731109		57.0472		99.0412708506		57.3708		98.8111888312		61.0936		99.6879444799				97.6365103823

		57.5022		99.5635776065		57.2905		99.0316780775		57.6304		98.8022777436		61.3369		99.6831931434				97.6189008731

		57.7618		99.5601798543		57.5533		99.021537146		57.9258		98.7947026871		61.5747		99.6810473785				97.6039327904

		58.0083		99.5567821022		57.828		99.0094776598		58.2005		98.7877212385		61.8234		99.6776754623				97.5901386749

		58.2483		99.5586697423		58.0865		99.0034479167		58.484		98.781184967		62.1069		99.676296042				97.5772250349

		58.5068		99.5560270461		58.3732		98.9952255398		58.7457		98.7743511298		62.3534		99.674303546				97.5637244112

		58.7631		99.5605573824		58.6567		98.9889217175		59.0194		98.7692997289		62.6119		99.6732306636				97.5537456893

		59.002		99.5605573824		58.914		98.9872772421		59.2909		98.7629108224		62.8866		99.6727708568				97.5411255411

		59.2876		99.5567821022		59.1725		98.9806993406		59.5624		98.757264468		63.1788		99.670625092				97.529972852

		59.5787		99.5462113175		59.431		98.9765881521		59.8219		98.749983166		63.4514		99.6663335622				97.5155917529

		59.8437		99.5480989576		59.7025		98.9722028844		60.1054		98.7425527126		63.7381		99.6631149149				97.5009171619

		60.1249		99.5386607571		59.9414		98.9694620921		60.3769		98.7363106995		64.0139		99.6618887635				97.4885905055

		60.4116		99.5284675005		60.2129		98.9626101113		60.6397		98.7296223905		64.2702		99.6586701162				97.4753833737

		60.6712		99.5246922203		60.479		98.9617878736		60.9058		98.7214471752		64.5406		99.6574439649				97.4592413236

		60.9394		99.5299776126		60.7668		98.9530173383		61.186		98.7163930671		64.8197		99.6559112757				97.4492626018

		61.2294		99.5269573884		61.0296		98.9480839121		61.4433		98.7104467263		65.0836		99.6500870567				97.437522929

		61.4933		99.5311101967		61.3152		98.9382170598		61.742		98.7028646222		65.3812		99.6493207121				97.4225548463

		61.7528		99.5303551406		61.5975		98.9362985052		62.0233		98.6961740466		65.6625		99.6464086027				97.4093477144

		62.0428		99.5326203087		61.856		98.9272538906		62.3121		98.6891856279		65.9296		99.6436497621				97.3955535989

		62.311		99.5299776126		62.1243		98.9269798113		62.5869		98.6805609396		66.2		99.6398180391				97.3785310734

		62.588		99.5250697483		62.3686		98.9187574344		62.8682		98.6728278194		66.477		99.6415039973				97.3632694989

		62.8595		99.520161884		62.626		98.9195796721		63.1462		98.667325038		66.7571		99.6378255432				97.3524103016

		63.1527		99.5178967159		62.8953		98.9110832159		63.4101		98.6603345758		67.0688		99.6369059297				97.3386161861

		63.4307		99.5095910994		63.1722		98.9105350575		63.6794		98.6551285907		67.3729		99.6347601648				97.3283439724

		63.7076		99.5054382912		63.4329		98.899297809		63.9683		98.6514098617		67.6254		99.6346068959				97.3210066769

		63.9639		99.5107236835		63.7283		98.8918976698		64.2528		98.6496248219		67.885		99.6341470891				97.3174847751

		64.2387		99.5046832351		64.0226		98.8825789759		64.4972		98.6439719831		68.1613		99.6329209378				97.306332086

		64.5091		99.5095910994		64.2811		98.8735343613		64.785		98.6383188203		68.4125		99.6318480553				97.2951793969

		64.7622		99.5144989637		64.5732		98.8677786975		65.0771		98.6316238663		68.6857		99.6292424837				97.281972265

		65.0271		99.5167641318		64.8566		98.8612007959		65.3736		98.6241844955		68.9986		99.6275565256				97.2672976741

		65.3377		99.5061933472		65.1292		98.860104479		65.6603		98.6177861878		69.2687		99.6232649958				97.2546775259

		65.6234		99.5126113236		65.3996		98.852978419		65.9633		98.6125779565		69.5303		99.6203528864				97.2444053122

		65.8894		99.503173123		65.6766		98.8532524982		66.2402		98.6078159042		69.7983		99.6174407769				97.235013574

		66.187		99.4986427868		65.9263		98.8447560421		66.5356		98.6043930371		70.0443		99.6162146255				97.2282632622

		66.49		99.4922248104		66.2152		98.8472227552		66.7713		98.5993329289		70.2934		99.6125361715				97.2182845403

		66.768		99.4869394181		66.4965		98.8411930121		67.0514		98.5926353276		70.5697		99.6116165579				97.2050774085

		67.0558		99.4759911054		66.7539		98.8414670913		67.3534		98.5866815223		70.822		99.6087044485				97.1933377357

		67.3555		99.4725933532		67.033		98.8305039221		67.6495		98.5828113559		71.0878		99.603953112				97.1857069484

		67.6149		99.468440545		67.3164		98.8231037828		67.9153		98.5776012767		71.3872		99.6007344647				97.1754347348

		67.8797		99.4608899846		67.572		98.8091257421		68.2367		98.5723909222		71.675		99.5975158174				97.1651625211

		68.133		99.4574922324		67.8483		98.7970662559		68.5235		98.5670314129		71.9879		99.5950635146				97.1545968156

		68.3759		99.4529618961		68.1665		98.7866512451		68.7945		98.563904898		72.2904		99.5941439011				97.1484334874

		68.6386		99.4522068401		68.446		98.7803474228		69.0792		98.5578004639		72.5971		99.5947569768				97.1364003228

		68.9369		99.4484315598		68.7276		98.7759621551		69.3252		98.5527379635		72.8619		99.5930710187				97.126421601

		69.1933		99.4503191999		69.0416		98.7644508274		69.5858		98.5475262943		73.1299		99.5919981362				97.1161493873

		69.4508		99.4522068401		69.2875		98.7647249067		69.8601		98.5442502469		73.4062		99.5893925646				97.1096925673

		69.7596		99.4563596483		69.5523		98.7592433221		70.1395		98.5362085779		73.6658		99.586786993				97.0938440091

		70.0568		99.4533394241		69.8339		98.760339639		70.4075		98.5290598767		73.9421		99.5852543038				97.0797564018

		70.3384		99.4544720082		70.1165		98.7507468659		70.71		98.5202722207		74.2153		99.5838748835				97.0624403845

		70.6472		99.4484315598		70.3677		98.7592433221		70.9999		98.5126754797		74.4958		99.5831085389				97.0474723017

		70.9434		99.4442787516		70.6681		98.7493764697		71.2877		98.5040353367		74.7732		99.5800431605				97.0304497762

		71.2029		99.4363506631		70.9256		98.7449912021		71.564		98.5001619232		75.0641		99.5782039335				97.0228189889

		71.4636		99.4397484153		71.1967		98.7348502705		71.8603		98.4971822706		75.3582		99.5743722105				97.0169491525

		71.7148		99.434085495		71.4678		98.7359465874		72.1575		98.4943515172		75.6639		99.5723797146				97.011372808

		71.966		99.4363506631		71.7242		98.724709339		72.4349		98.492563631		75.9706		99.5693143362				97.0078509062

		72.2622		99.434463023		71.9995		98.7252574974		72.6819		98.4897327449		76.2594		99.5674751091				97.0022745616

		72.55		99.4371057192		72.2967		98.7208722297		72.9687		98.4840707285		76.5724		99.5642564618				96.9911218725

		72.8389		99.4329529109		72.5678		98.7203240713		73.2555		98.4781103595		76.8623		99.5648695375				96.9793821997

		73.1435		99.4367281911		72.8651		98.7170351205		73.537		98.4722986524		77.1418		99.5613443523				96.9679360188

		73.4271		99.434840551		73.1707		98.7148424867		73.8364		98.4663375708		77.415		99.5610378145				96.956196346

		73.6836		99.434840551		73.4575		98.7110053774		74.1556		98.4605251688		77.6808		99.5604247388				96.9447501651

		73.9651		99.4329529109		73.7191		98.7041533967		74.4309		98.4562029038		77.9718		99.5599649321				96.9362389023

		74.232		99.4280450466		73.9986		98.6967532574		74.7208		98.4521785555		78.2397		99.5570528226				96.9283146232

		74.5073		99.4223821263		74.253		98.6822270582		75.0003		98.4480049835		78.5339		99.5561332091				96.9200968523

		74.8119		99.416341678		74.5303		98.677293632		75.2975		98.4429368368		78.8374		99.552454755				96.9101181305

		75.1154		99.4121888697		74.8077		98.6663304628		75.5875		98.436824901		79.1281		99.5504622591				96.8980849659

		75.4127		99.4091686455		75.1018		98.6622192743		75.8701		98.4302653282		79.3944		99.5475501496				96.8851713258

		75.7057		99.4053933653		75.4022		98.6545450559		76.1223		98.42266164		79.672		99.5435651577				96.8702032431

		75.9779		99.4057708933		75.7005		98.6515301843		76.4238		98.4168466586		79.9546		99.5423390063				96.8587570621

		76.25		99.4053933653		75.9873		98.6449522828		76.6928		98.4107331024		80.2393		99.5398867036				96.8467238976

		76.5232		99.4061484214		76.295		98.6449522828		76.9848		98.4070051379		80.5536		99.5359017117				96.8393866021

		76.7974		99.4065259494		76.5797		98.6331668759		77.2904		98.4029787776		80.8424		99.5349820982				96.831462323

		77.0947		99.4080360615		76.8696		98.6315224005		77.6023		98.4005927085		81.1414		99.5346755604				96.8267664539

		77.3919		99.4038832532		77.1648		98.6287816082		77.8661		98.3961186731		81.4455		99.5306905684				96.8179616993

		77.6798		99.399730445		77.4453		98.6230259443		78.1633		98.3931358698		81.7517		99.5297709549				96.8120918629

		77.9875		99.3959551648		77.707		98.6134331713		78.4533		98.3879157464		82.0486		99.5276251901				96.8018196493

		78.29		99.3940675247		78.0158		98.6098701413		78.7547		98.3804579469		82.3568		99.5262457698				96.7871450583

		78.5841		99.3940675247		78.2858		98.6019218436		79.0505		98.3741929583		82.6435		99.5247130806				96.7748184019

		78.8709		99.3899147164		78.5611		98.598906972		79.3383		98.3668833006		82.916		99.5247130806				96.7604373028

		79.1597		99.3936899966		78.8531		98.6010996059		79.6128		98.3577827637		83.2017		99.5228738535				96.7425343019

		79.427		99.3944450527		79.1393		98.5958921005		79.9077		98.3510687131		83.4548		99.5222607779				96.72932717

		79.7066		99.3906697725		79.4077		98.6008255266		80.1934		98.3468908502		83.7385		99.5196552062				96.7211093991

		79.9944		99.3910473005		79.7066		98.5983588136		80.473		98.3422651522		84.0385		99.5176627103				96.7120111527

		80.2812		99.3940675247		79.9863		98.5986328928		80.7802		98.3386838172		84.3508		99.5161300211				96.704967349

		80.573		99.3895371884		80.2638		98.5934253874		81.0608		98.3362961881		84.6324		99.5132179116				96.7002714799

		80.8516		99.3861394362		80.5679		98.5994551305		81.3475		98.3322669325		84.962		99.5136777184				96.6923472008

		81.121		99.383119212		80.8537		98.5915068328		81.6353		98.3273420625		85.2437		99.5113786846				96.6826619708

		81.3802		99.3729259554		81.1261		98.5884919613		81.9384		98.3201781749		85.5386		99.5104590711				96.6685743635

		81.6731		99.3695282032		81.4506		98.5901364366		82.2241		98.3165960354		85.8172		99.5077002305				96.6615305598

		81.9455		99.3714158433		81.7517		98.5813659013		82.5303		98.311968912		86.11		99.5069338859				96.6524323134

		82.2415		99.3744360675		82.0241		98.5780769505		82.8048		98.3097299031		86.3764		99.5043283143				96.6480299362

		82.5241		99.3782113477		82.3303		98.5799955051		83.0987		98.3079386593		86.6723		99.5031021629				96.6445080343

		82.8486		99.38349674		82.618		98.584654852		83.3793		98.3062966571		86.9978		99.5003433224				96.6412796243

		83.1385		99.3842517961		82.8987		98.5772547128		83.6834		98.301370486		87.3019		99.5001900535				96.6315943943

		83.4221		99.3800989878		83.2058		98.5841066936		83.9773		98.2964440681		87.5938		99.4986573643				96.6219091643

		83.7069		99.3706607873		83.4885		98.5750620789		84.2722		98.2904723213		87.905		99.4965115994				96.6101694915

		84.0059		99.366130451		83.7538		98.5731435243		84.5691		98.2821112663		88.2101		99.4943658345				96.5937339497

		84.2701		99.3597124747		84.0803		98.5687582566		84.8559		98.2744961152		88.4897		99.4925266075				96.5787658669

		84.5416		99.3574473065		84.363		98.5649211474		85.1406		98.268373703		88.7816		99.4899210359				96.5667327023

		84.8426		99.3559371944		84.6569		98.5591654836		85.4263		98.2635949699		89.0837		99.4865491196				96.5573409641

		85.1416		99.3589574186		84.9518		98.5558765328		85.7192		98.2577705747		89.3939		99.4847098926				96.5458947832

		85.4151		99.3585798906		85.2579		98.549024552		85.9968		98.2543355132		89.6908		99.481951052				96.5391444713

		85.7049		99.3600900027		85.5365		98.5405280959		86.309		98.2506016144		89.9827		99.4804183628				96.5318071759

		86.0274		99.3578248345		85.8141		98.5405280959		86.5907		98.2438802389		90.2957		99.4784258669				96.518600044

		86.3284		99.3548046104		86.0978		98.5292908474		86.906		98.2370090243		90.5903		99.4787324047				96.5050994204

		86.6141		99.3540495543		86.4182		98.5303871643		87.2305		98.2311830527		90.8722		99.4759735642				96.4936532394

		86.9315		99.3525394422		86.7152		98.5281945305		87.5244		98.2249085431		91.156		99.4767399088				96.481326583

		87.2336		99.347631578		87.0274		98.5309353228		87.8234		98.218932447		91.4398		99.4736745304				96.4695869103

		87.504		99.348009106		87.3417		98.516957282		88.1397		98.2141513083		91.7316		99.4730614547				96.4601951721

		87.7785		99.3506518021		87.6254		98.5254537382		88.4408		98.2084734037		92.0262		99.4712222277				96.4490424829

		88.0703		99.3510293302		87.9336		98.5199721536		88.7316		98.2020480106		92.2972		99.4680035804				96.4364223347

		88.3652		99.3563147225		88.2397		98.520520312		89.0316		98.1969671695		92.6244		99.4660110844				96.4264436129

		88.6561		99.3623551708		88.5336		98.5125720143		89.3204		98.1921849613		92.9437		99.4655512776				96.4170518747

		88.9663		99.3642428109		88.8357		98.5287426889		89.6276		98.1857585022		93.2374		99.4621793614				96.4044317265

		89.2867		99.3623551708		89.1592		98.5243574212		89.9082		98.1818725321		93.5469		99.4585009074				96.3968009392

		89.6051		99.3646203389		89.4541		98.5355946697		90.205		98.1778369389		93.8701		99.4583476384				96.3888766601

		89.898		99.3582023626		89.7592		98.5435429674		90.5075		98.1761927608		94.149		99.455435529				96.3856482501

		90.206		99.3548046104		90.0429		98.5498467897		90.7914		98.1685693933		94.4378		99.453443033				96.3706801673

		90.4819		99.348764162		90.3449		98.5509431066		91.0811		98.1678219725		94.7394		99.4509907303				96.3692127082

		90.7539		99.3438562977		90.6337		98.5542320574		91.3916		98.1625898673		95.0311		99.44961131				96.3589404945

		91.0328		99.3400810175		90.9195		98.5539579782		91.6803		98.1588524786		95.3317		99.4485384276				96.3516031991

		91.3354		99.3415911296		91.2151		98.5509431066		91.9622		98.1498821649		95.6332		99.4463926627				96.3339936899

		91.6153		99.3412136016		91.5266		98.552587582		92.2687		98.1464433274		95.9466		99.44394036				96.3272433781

		91.8961		99.3502742741		91.8153		98.5449133636		92.5436		98.1383690612		96.263		99.4425609397				96.3113948199

		92.1888		99.3555596664		92.109		98.5484763936		92.8284		98.132985848		96.5567		99.4396488303				96.3008291144

		92.4825		99.3563147225		92.4175		98.5410762543		93.1054		98.1265555118		96.8464		99.4359703762				96.2882089662

		92.7683		99.3566922505		92.7062		98.5462837597		93.4237		98.1216203169		97.1559		99.434437687				96.2785237362

		93.063		99.3589574186		93.0048		98.545461522		93.7243		98.1144414084		97.4604		99.4315255775				96.2644361288

		93.3784		99.3510293302		93.3064		98.5575210082		94.0278		98.1081594326		97.7462		99.4281536613				96.2521094724

		93.6809		99.3498967461		93.5952		98.5572469289		94.3254		98.0999324273		98.0724		99.4260078964				96.2359674224

		93.9776		99.3464989939		93.876		98.5640989097		94.6388		98.0924527328		98.3887		99.4263144343				96.2212928315

		94.2703		99.3427237137		94.1747		98.5599877213		94.9227		98.0869173918		98.6627		99.4234023248				96.2104336342

		94.5886		99.3370607933		94.4634		98.5640989097		95.2213		98.0800351807		98.9574		99.4227892491				96.1969330105

		94.8882		99.3363057373		94.7512		98.5550542951		95.5307		98.0746487656		99.2737		99.4206434842				96.186367305

		95.172		99.3393259615		95.0675		98.5528616612		95.8402		98.0679153307		99.5605		99.4200304086				96.1731601732

		95.4282		99.3408360736		95.3602		98.5512171859		96.1339		98.063575761		99.866		99.4149725342				96.1646489104

		95.6983		99.3449888818		95.6648		98.5457356012		96.4384		98.0520525233		100.182		99.4128267693				96.1420500404

		95.9437		99.348386634		95.9713		98.5438170466		96.736		98.0487599209		100.494		99.4105277355				96.1355932203

		96.1684		99.348764162		96.2709		98.5416244128		97.0258		98.0405279312		100.803		99.4099146599				96.1194511703

		96.4009		99.3449888818		96.5734		98.541898492		97.3224		98.0366362045		101.104		99.4085352396				96.111820383

		96.6207		99.3423461856		96.87		98.5369650659		97.6112		98.0290019842		101.406		99.4063894747				96.0968523002

		96.8356		99.3363057373		97.1549		98.5484763936		97.8802		98.0278044055		101.718		99.4048567855				96.0945043657

		97.0504		99.3355506812		97.4692		98.5465578389		98.1867		98.0200197873		102.029		99.4004119869				96.0792427911

		97.3037		99.3336630411		97.7629		98.5569728497		98.4981		98.0150792282		102.325		99.396273726				96.0695575611

		97.5806		99.3359282093		98.0714		98.5542320574		98.7987		98.0096892433		102.656		99.3910625828				96.0589918556

		97.9078		99.3351731532		98.3897		98.5619062759		99.117		98.0029513452		102.954		99.3901429692				96.0457847238

		98.232		99.3374383214		98.7011		98.5591654836		99.4511		97.9953145007		103.268		99.3846252881				96.030816641

		98.5701		99.3332855131		98.9751		98.563276672		99.7576		97.988425856		103.563		99.3855449017				96.0173160173

		98.9199		99.331397873		99.3063		98.5599877213		100.053		97.9822855687		103.855		99.3832458679				96.0052828527

		99.2353		99.3238473126		99.6127		98.5635507513		100.342		97.9725501784		104.153		99.3826327922				95.9862058845

		99.5615		99.3253574247		99.9035		98.5621803551		100.651		97.9662591039		104.468		99.3794141449				95.9738792281

		99.8779		99.3276225928		100.241		98.5638248305		100.945		97.9593684159		104.769		99.3786478003				95.9603786044

		100.194		99.330642817		100.528		98.5657433851		101.225		97.9526270564		105.077		99.3735899259				95.9471714726

		100.516		99.3272450648		100.86		98.570402732		101.515		97.9449862881		105.403		99.3717506989				95.9322033898

		100.849		99.3264900087		101.12		98.5723212866		101.821		97.9410907651		105.722		99.3680722448				95.9245726025

		101.166		99.3174293362		101.462		98.5778028713		102.128		97.9326998814		106.05		99.3651601354				95.9081370607

		101.49		99.3072360796		101.73		98.5821881389		102.43		97.9246079913		106.365		99.3608686056				95.8922885025

		101.801		99.2940225988		102.037		98.5862993274		102.751		97.9172647715		106.661		99.3571901516				95.8779074033

		102.095		99.2887372065		102.325		98.5983588136		103.071		97.9076727979		106.969		99.3521322772				95.8591239269

		102.421		99.2826967582		102.627		98.6054848736		103.384		97.89897926		107.28		99.348760361				95.8421014014

		102.736		99.2823192301		102.929		98.6161739636		103.679		97.8922337418		107.567		99.3443155623				95.8288942696

		103.045		99.2770338378		103.265		98.6227518651		103.984		97.8878863838		107.882		99.3406371082				95.8203830068

		103.364		99.2808091181		103.538		98.623848182		104.275		97.8815898678		108.193		99.3378782677				95.8080563504

		103.681		99.2826967582		103.848		98.6276852913		104.58		97.8796408641		108.512		99.3345063515				95.8042409568

		103.976		99.2823192301		104.158		98.6293297666		104.869		97.8727440778		108.812		99.3306746285				95.7907403331

		104.281		99.2815641741		104.474		98.6386484605		105.184		97.8694454429		109.127		99.3266896366				95.7842835131

		104.587		99.2826967582		104.795		98.6476930751		105.494		97.8607485091		109.428		99.3227046447				95.7672609876

		104.906		99.280054062		105.111		98.6512561051		105.779		97.8552000613		109.764		99.3174935014				95.7564017903

		105.227		99.279676534		105.419		98.6561895313		106.087		97.8466518368		110.078		99.3136617784				95.7396727566

		105.549		99.2751461977		105.744		98.6520783428		106.378		97.8429023799		110.404		99.3095235176				95.7323354611

		105.857		99.2751461977		106.064		98.6578340067		106.669		97.8340530919		110.727		99.306764677				95.7150194438

		106.174		99.2713709175		106.366		98.6537228182		106.959		97.8283531266		111.066		99.3047721811				95.7038667547

		106.481		99.2709933895		106.64		98.6586562443		107.288		97.8223528044		111.399		99.3014002648				95.692127082

		106.802		99.2691057494		106.955		98.6638637497		107.582		97.8142517856		111.701		99.2975685419				95.6762785237

		107.094		99.2691057494		107.277		98.6611229574		107.912		97.8061500957		112.011		99.2926639364				95.6604299655

		107.416		99.2638203571		107.576		98.6657823043		108.236		97.7984978835		112.316		99.2876060621				95.6454618827

		107.721		99.2638203571		107.873		98.666604542		108.571		97.7917454343		112.596		99.2804024229				95.6322547509

		108.032		99.2615551889		108.21		98.6805825828		108.857		97.7819910733		112.888		99.2754978175				95.6131777827

		108.331		99.263065301		108.532		98.6838715336		109.163		97.7755376536		113.195		99.2696735985				95.6005576345

		108.649		99.2608001329		108.807		98.6920939105		109.465		97.7684834284		113.501		99.2633895728				95.586763519

		108.947		99.2558922686		109.156		98.6975754951		109.745		97.7609783748		113.812		99.2584849674				95.572088928

		109.259		99.2494742922		109.442		98.699768129		110.023		97.7528722697		114.157		99.253427093				95.5562403698

		109.558		99.24607654		109.74		98.7044274759		110.355		97.7458164088		114.478		99.2480626809				95.5424462543

		109.863		99.2381484516		110.084		98.7038793174		110.664		97.7408619894		114.783		99.2446907646				95.5327610243

		110.172		99.2362608115		110.363		98.7134720905		110.981		97.7321536132		115.072		99.2370273187				95.5157384988

		110.482		99.2358832834		110.672		98.7131980113		111.32		97.7303517833		115.395		99.2310498308				95.512216597

		110.793		99.2343731713		111.021		98.7249834182		111.658		97.7240451171		115.69		99.2264517632				95.4998899406

		111.111		99.2272001389		111.309		98.7337539536		111.948		97.7210417997		115.986		99.2194013929				95.4940201042

		111.415		99.2245574428		111.646		98.7373169836		112.25		97.7133829224		116.317		99.2112781402				95.4790520214

		111.706		99.2158742983		111.902		98.7359465874		112.543		97.7115807464		116.642		99.2079062239				95.4755301196

		112.007		99.2177619384		112.237		98.7397836967		112.854		97.6997155911		116.947		99.2031548874				95.4523442659

		112.308		99.2139866582		112.527		98.7375910628		113.145		97.6920550419		117.27		99.1962577861				95.4373761831

		112.609		99.2207821626		112.794		98.7433467267		113.457		97.6848445645		117.583		99.1908933739				95.4232885758

		112.923		99.2158742983		113.119		98.7458134397		113.769		97.6749292888		117.895		99.1852224239				95.4039181158

		113.264		99.2200271065		113.406		98.7521172621		114.069		97.6614068361		118.221		99.179244936				95.3775038521

		113.572		99.2215372186		113.749		98.7543098959		114.356		97.6529919205		118.517		99.1686693805				95.3610683102

		113.881		99.2238023867		114.033		98.7619841144		114.657		97.6463796923		118.822		99.163918044				95.3481546702

		114.173		99.2177619384		114.374		98.7600655598		114.952		97.6364605105		119.14		99.1556415224				95.3287842101

		114.477		99.2256900268		114.684		98.7647249067		115.266		97.6351078167		119.444		99.1490509589				95.3261427838

		114.769		99.2238023867		114.989		98.763902669		115.568		97.6293962363		119.749		99.141234244				95.3149900947

		115.06		99.2222922746		115.262		98.7649989859		115.863		97.6229327292		120.087		99.1369427142				95.3023699464

		115.363		99.2222922746		115.569		98.7704805705		116.181		97.613311833		120.412		99.1272867723				95.28358647

		115.681		99.2241799148		115.906		98.7795251851		116.502		97.605794848		120.736		99.1214625533				95.2689118791

		115.992		99.2230473307		116.211		98.7767843928		116.807		97.592262816		121.058		99.1137991074				95.2424976154

		116.305		99.2207821626		116.507		98.7847326905		117.124		97.5842930747		121.379		99.1078216195				95.226942549

		116.62		99.2185169944		116.778		98.7882957205		117.445		97.5775258024		121.687		99.0970927951				95.2137354171

		116.933		99.2211596906		117.102		98.792406909		117.739		97.570607661		121.987		99.0898891559				95.2002347935

		117.226		99.2173844104		117.411		98.7981625728		118.049		97.5638394394		122.271		99.0794668694				95.1870276616

		117.532		99.210966434		117.708		98.7984366521		118.344		97.5551152611		122.577		99.0710370788				95.1700051361

		117.832		99.2079462098		118.008		98.8047404744		118.645		97.5487972656		122.876		99.0623007504				95.1576784797

		118.146		99.2000181213		118.316		98.810222059		118.949		97.5367618563		123.176		99.0575494139				95.1341991342

		118.44		99.1973754252		118.6		98.8085775836		119.272		97.5274333926		123.502		99.0501925058				95.1160026414

		118.758		99.1962428411		118.942		98.8126887721		119.57		97.5156963158		123.834		99.0439084801				95.0931102796

		119.062		99.1958653131		119.233		98.8187185151		119.883		97.5080213094		124.157		99.0354786895				95.0781421968

		119.369		99.1985080093		119.546		98.8337928728		120.203		97.4973354906		124.469		99.0276619746				95.0573042776

		119.677		99.1988855373		119.884		98.8365336652		120.526		97.490863228		124.811		99.0172396881				95.0446841294

		119.985		99.1932226169		120.179		98.8379040613		120.833		97.4834873352		125.122		99.0094229732				95.0303030303

		120.307		99.193600145		120.489		98.8332447144		121.151		97.4762614296		125.442		99.0005333758				95.016215423

		120.602		99.1920900329		120.793		98.8376299821		121.445		97.4682822033		125.777		98.9921035853				95.0006603566

		120.914		99.1920900329		121.14		98.8343410313		121.733		97.4575920272		126.102		98.9824476433				94.9798224374

		121.206		99.1954877851		121.44		98.8392744575		122.015		97.4482559847		126.411		98.9732515082				94.9616259447

		121.503		99.1951102571		121.733		98.8466745967		122.308		97.4378648212		126.759		98.9619096081				94.9413750092

		121.783		99.1909574488		122.004		98.8510598644		122.605		97.42762317		127.088		98.9517938594				94.9214175655

		122.078		99.1864271126		122.308		98.8510598644		122.915		97.4152715114		127.398		98.9404519594				94.8973512363

		122.378		99.1811417202		122.601		98.8516080228		123.245		97.407136637		127.742		98.9295698661				94.8815026781

		122.682		99.1735911598		122.91		98.852978419		123.583		97.3973437574		128.057		98.9191475796				94.8624257099

		122.992		99.1701934076		123.217		98.8579118452		123.904		97.3910155268		128.355		98.9101047133				94.8500990535

		123.299		99.1660405994		123.524		98.8625711921		124.207		97.3848375718		128.676		98.89922262				94.8380658889

		123.621		99.1686832955		123.874		98.8669564598		124.526		97.3809196412		129.012		98.8892601403				94.8304351016

		123.897		99.1686832955		124.184		98.8625711921		124.841		97.3756452548		129.347		98.8792976605				94.820162888

		124.208		99.1724585757		124.456		98.8680527767		125.141		97.3688634812		129.681		98.8699482564				94.8069557561

		124.524		99.1709484636		124.802		98.8595563205		125.451		97.361779791		130.021		98.8586063564				94.7931616406

		124.839		99.1788765521		125.104		98.8633934298		125.783		97.3515301353		130.361		98.8506363726				94.7732041969

		125.16		99.1732136318		125.373		98.8661342221		126.111		97.3433899341		130.695		98.8403673549				94.7573556387

		125.494		99.1796316082		125.725		98.8686009352		126.414		97.3335906409		131.004		98.8297917995				94.7382786705

		125.804		99.1758563279		126.033		98.8622971128		126.729		97.3259012739		131.34		98.8190629751				94.7233105877

		126.097		99.1822743043		126.364		98.8653119844		127.034		97.3150446626		131.682		98.8083341508				94.7021791768

		126.408		99.177743968		126.707		98.8612007959		127.338		97.3056949433		131.995		98.7919343764				94.683982684

		126.716		99.1841619444		127.03		98.8603785582		127.634		97.2933278056		132.306		98.7808990142				94.6599163548

		127.029		99.1758563279		127.342		98.8559932905		127.951		97.2833726259		132.64		98.7684842317				94.6405458948

		127.333		99.1800091362		127.674		98.8576377659		128.251		97.2688905458		132.959		98.7559161803				94.6123706802

		127.647		99.1751012719		127.977		98.8617489544		128.588		97.2578766874		133.263		98.7435013978				94.5909457774

		127.964		99.1735911598		128.258		98.8598303998		128.919		97.2480687773		133.592		98.7343052626				94.5718688092

		128.272		99.1671731834		128.569		98.8587340828		129.237		97.2378071356		133.924		98.7214306734				94.5519113655

		128.602		99.1698158796		128.89		98.8474968344		129.56		97.2264878925		134.246		98.7100887734				94.5298994791

		128.904		99.1645304873		129.189		98.8513339436		129.884		97.2180353315		134.579		98.697367453				94.5134639372

		129.229		99.1675507115		129.461		98.8453042005		130.193		97.2133559192		134.938		98.684186326				94.5043656908

		129.538		99.1671731834		129.826		98.8442078836		130.49		97.2041473857		135.272		98.67085193				94.4864626899

		129.862		99.1751012719		130.148		98.8379040613		130.816		97.1997692524		135.599		98.6582838786				94.4779514271

		130.158		99.1784990241		130.436		98.8485931513		131.136		97.1908614067		135.936		98.6437233312				94.4606354098

		130.482		99.1815192483		130.763		98.8359855067		131.443		97.1843687336		136.279		98.6293160528				94.4480152616

		130.805		99.1754787999		131.098		98.8400966952		131.758		97.1721371712		136.606		98.617514346				94.4242424242

		131.117		99.176611384		131.416		98.8285853675		132.075		97.1629247312		136.929		98.6023407229				94.4063394233

		131.402		99.1660405994		131.73		98.8274890505		132.38		97.1512946662		137.265		98.588853058				94.3837405532

		131.716		99.1588675669		132.059		98.8178962775		132.693		97.1420802496		137.617		98.5776644269				94.3658375523

		132.03		99.1520720625		132.378		98.8178962775		133.005		97.1348289467		137.95		98.5638702241				94.351749945

		132.325		99.1528271186		132.703		98.8115924551		133.299		97.1271238441		138.274		98.5500760214				94.3367818622

		132.642		99.1460316142		133.014		98.8069331082		133.63		97.1207780065		138.631		98.5379677767				94.3244552058

		132.964		99.1437664461		133.329		98.8074812667		133.954		97.1133740052		138.973		98.5227941537				94.3100741067

		133.282		99.141878806		133.667		98.8058367913		134.259		97.1085384343		139.296		98.5079270685				94.3006823685

		133.601		99.1411237499		133.988		98.8085775836		134.602		97.096901855		139.628		98.4944394036				94.2780834984

		133.921		99.1354608296		134.298		98.8017256028		134.917		97.0907051853		139.966		98.4800321252				94.2660503338

		134.22		99.1396136378		134.62		98.8014515236		135.222		97.0831477358		140.313		98.4656248467				94.2513757429

		134.556		99.1392361098		134.956		98.7871994036		135.531		97.0722639748		140.648		98.4525969886				94.2302443319

		134.884		99.1377259977		135.27		98.7866512451		135.858		97.0619837466		140.99		98.4372700966				94.2102868883

		135.196		99.1328181334		135.589		98.7715768874		136.159		97.0551800557		141.343		98.4237824317				94.1970797564

		135.506		99.1335731895		135.919		98.7726732044		136.503		97.0444443733		141.687		98.4106013046				94.1762418373

		135.845		99.1241349889		136.25		98.7630804313		136.834		97.0303803446		142.02		98.3978799843				94.1489470981

		136.144		99.1188495966		136.559		98.7614359559		137.16		97.0241794263		142.355		98.3839325126				94.1369139335

		136.434		99.1135642043		136.887		98.7482801528		137.486		97.0125327282		142.685		98.3705981166				94.1143150635

		136.755		99.1094113961		137.2		98.7411540928		137.801		97.0033051306		143.027		98.3551179558				94.0964120625

		137.09		99.1052585878		137.518		98.7312872405		138.127		96.9916559259		143.364		98.3402508706				94.0738131925

		137.412		99.1052585878		137.829		98.7225167051		138.454		96.9842420671		143.694		98.32615013				94.0594320933

		137.73		99.1060136439		138.153		98.7134720905		138.768		96.9734985314		144.02		98.3100568934				94.0385941742

		138.076		99.1094113961		138.468		98.7005903667		139.07		96.9629051477		144.352		98.293657119				94.0180497469

		138.395		99.1150743164		138.785		98.6942865444		139.404		96.9514024492		144.673		98.2817021433				93.9957443686

		138.71		99.1188495966		139.089		98.677293632		139.717		96.9380818299		145.009		98.2660687135				93.9699170886

		139.027		99.1192271246		139.419		98.6649600667		140.035		96.9283929569		145.355		98.2489025945				93.9511336122

		139.343		99.1267776851		139.741		98.6490634713		140.35		96.9168861623		145.701		98.2325028201				93.9288282339

		139.678		99.1264001571		140.068		98.6394706982		140.692		96.9111322526		146.055		98.2177890039				93.9176755448

		139.991		99.1294203812		140.425		98.623848182		141.012		96.8996234082		146.4		98.1997032714				93.8953701666

		140.313		99.1275327411		140.753		98.6150776466		141.334		96.8943228228		146.732		98.1840698416				93.8850979529

		140.607		99.1347057735		141.069		98.6041144774		141.66		96.8844781091		147.05		98.1698158321				93.8660209847

		140.923		99.1245125169		141.41		98.5942476251		141.995		96.8735720275		147.401		98.1555618226				93.8448895737

		141.207		99.1199821807		141.739		98.5780769505		142.317		96.8628162168		147.73		98.1405414684				93.8240516546

		141.538		99.1124316202		142.041		98.5646470682		142.637		96.8550894748		148.081		98.1238351562				93.8090835718

		141.858		99.1071462279		142.39		98.5465578389		142.955		96.8459984009		148.417		98.1075886507				93.7914740627

		142.193		99.0924226351		142.727		98.5298390059		143.259		96.8375126285		148.769		98.0893496493				93.7750385208

		142.539		99.0943102752		143.037		98.5161350443		143.564		96.8325117359		149.108		98.0718769925				93.7653532908

		142.863		99.0852496027		143.371		98.4985939735		143.887		96.823418542		149.445		98.05379126				93.7477437816

		143.198		99.0841170186		143.698		98.4854381705		144.192		96.8169012277		149.785		98.0383110991				93.7351236334

		143.513		99.0852496027		144.008		98.4720082882		144.518		96.8087160721		150.134		98.0225244004				93.7192750752

		143.82		99.0935552191		144.329		98.4583043266		144.842		96.8000754346		150.492		98.0079638531				93.7025460415

		144.124		99.0901574669		144.655		98.438570622		145.191		96.7915856362		150.822		97.9930967679				93.6861104997

		144.441		99.0965754433		144.967		98.4251407397		145.505		96.7815788462		151.184		97.9793025651				93.6667400396

		144.748		99.0935552191		145.302		98.4034884804		145.871		96.7738456179		151.521		97.962442984				93.6517719569

		145.053		99.0894024109		145.632		98.3848510928		146.19		96.7611071888		151.867		97.9463497474				93.6271186441

		145.384		99.0822293785		145.963		98.3618284374		146.519		96.753675664		152.193		97.9296434352				93.6127375449

		145.684		99.0818518505		146.284		98.3429169704		146.832		96.7419964002		152.546		97.9124773162				93.5901386749

		146.006		99.0724136499		146.609		98.3212647112		147.143		96.736232088		152.886		97.8930121634				93.5789859858

		146.316		99.0761889301		146.935		98.298516135		147.448		96.7230335533		153.233		97.8759993134				93.5534521975

		146.645		99.0724136499		147.274		98.2793305889		147.755		96.7174198375		153.576		97.8611322282				93.5425930002

		146.96		99.0724136499		147.601		98.2524708243		148.07		96.7063431722		153.918		97.8444259159				93.5211680974

		147.289		99.0648630895		147.924		98.2291740896		148.395		96.6952652381		154.277		97.8287924861				93.4997431947

		147.585		99.0724136499		148.26		98.2121811773		148.732		96.6835789183		154.619		97.8136188631				93.4771443246

		147.917		99.0625979213		148.583		98.1929956312		149.052		96.6753824747		154.956		97.7987517779				93.4612957664

		148.25		99.056935001		148.916		98.1683285004		149.397		96.6659708861		155.316		97.7802062387				93.4430992736

		148.552		99.0490069125		149.248		98.1496911127		149.729		96.656406559		155.664		97.7633466575				93.424609289

		148.877		99.0508945526		149.592		98.1217350312		150.065		96.6497261501		155.994		97.7461805385				93.411695649

		149.209		99.0361709598		149.936		98.0899418404		150.395		96.6394009736		156.314		97.7296274952				93.3917382053

		149.524		99.0327732076		150.266		98.0636302342		150.728		96.6280116317		156.661		97.7120015695				93.3697263189

		149.845		99.0237125351		150.564		98.0356741527		151.069		96.6155577481		157.002		97.6946821816				93.3456599897

		150.196		99.0206923109		150.899		98.006347675		151.387		96.6043174993		157.375		97.6773627937				93.3239415951

		150.509		99.0146518625		151.224		97.9794879104		151.703		96.5927720986		157.71		97.6608097504				93.3016362169

		150.851		99.0203147829		151.554		97.945776165		152.024		96.5822888947		158.072		97.6464024719				93.2813852814

		151.165		99.0210698389		151.894		97.9117903404		152.35		96.5734760459		158.394		97.6312288489				93.2643627559

		151.473		99.0297529834		152.236		97.8789008327		152.662		96.5632946849		158.744		97.6171281083				93.244698804

		151.788		99.0271102873		152.563		97.844915008		153.002		96.5563038752		159.07		97.6016479474				93.2311981804

		152.11		99.0240900631		152.901		97.8169589265		153.331		96.545360722		159.434		97.585401442				93.2100667694

		152.43		99.0161619746		153.222		97.7887287657		153.647		96.5366965126		159.788		97.5685418608				93.1933377357

		152.757		99.0108765823		153.55		97.7602245257		154.005		96.5268153248		160.156		97.5515290107				93.1742607675

		153.078		99.0040810779		153.9		97.7224015919		154.272		96.5157167847		160.492		97.533903085				93.1528358647

		153.393		99.0063462461		154.224		97.6911565595		154.64		96.5000550297		160.839		97.5162771593				93.1226062074

		153.718		98.9999282697		154.548		97.6505928334		154.943		96.4909305055		161.193		97.4989577713				93.1049966982

		154.026		99.0071013021		154.89		97.620444118		155.283		96.4783068245		161.545		97.478726274				93.0806368772

		154.34		99.0033260219		155.221		97.5809767087		155.587		96.4691802433		161.876		97.4609470793				93.0630273681

		154.676		99.005968718		155.549		97.5453464087		155.952		96.4603570606		162.205		97.44240154				93.0460048426

		154.989		98.9984181576		155.882		97.5061530787		156.262		96.4548801965		162.54		97.4264615724				93.0354391371

		155.323		98.9984181576		156.224		97.4691523826		156.604		96.4472729247		162.865		97.4134337143				93.0207645462

		155.66		98.9859597329		156.55		97.4244774679		156.965		96.4384477378		163.199		97.4000993183				93.0037420207

		155.992		98.9821844526		156.881		97.3839137418		157.268		96.4284043011		163.552		97.383546275				92.9843715606

		156.3		98.9746338922		157.216		97.3491056795		157.583		96.416229036		163.906		97.3676063073				92.9608922151

		156.64		98.9787867004		157.56		97.3088160325		157.963		96.4023778024		164.255		97.3498271127				92.9341844596

		156.959		98.9772765884		157.901		97.2709930987		158.247		96.3920261308		164.591		97.3292890774				92.9142270159

		157.277		98.9742563642		158.237		97.2287848971		158.571		96.3809120693		164.916		97.3112033449				92.8928021131

		157.593		98.9750114202		158.591		97.1830136656		158.94		96.3719285351		165.251		97.2915849232				92.8754860958

		157.918		98.9742563642		158.928		97.1320349287		159.24		96.3646192793		165.601		97.2744188043				92.8613984885

		158.236		98.9723687241		159.272		97.092019361		159.576		96.3541112527		165.946		97.2564863407				92.841147553

		158.548		98.9682159158		159.599		97.0396702279		159.953		96.3434497647		166.307		97.2388604149				92.8206031257

		158.87		98.9689709719		159.956		97.0034917694		160.267		96.3359860211		166.669		97.2195485311				92.8062220266

		159.204		98.9678383878		160.299		96.9577205379		160.6		96.3256272146		167.031		97.2036085634				92.7862645829

		159.536		98.9636855796		160.621		96.9160604948		160.988		96.3135913198		167.37		97.1824574525				92.7630787292

		159.856		98.954247379		160.96		96.8626150448		161.298		96.3047538825		167.698		97.1648315268				92.7460562037

		160.18		98.9519822109		161.329		96.8146511794		161.596		96.2940869298		168.035		97.1485850213				92.7255117764

		160.492		98.9500945708		161.665		96.7527092732		161.894		96.2837236155		168.379		97.1306525578				92.7055543327

		160.822		98.936126034		161.995		96.7022786947		162.242		96.2718349107		168.715		97.1140995144				92.6826619708

		161.137		98.9274428894		162.35		96.6403367886		162.525		96.2617740906		169.068		97.0976997401				92.6632915107

		161.472		98.919514801		162.678		96.5844246255		162.861		96.2517122189		169.422		97.0802270832				92.6439210507

		161.807		98.9134743526		162.996		96.5276902247		163.214		96.2402769968		169.757		97.0624478886				92.6219091643

		162.138		98.903281096		163.329		96.4687631901		163.577		96.2273154357		170.096		97.0439023493				92.5969623597

		162.451		98.9059237922		163.688		96.4095620762		163.88		96.2169449297		170.439		97.0268894992				92.577004916

		162.778		98.9036586241		164.02		96.3536499131		164.235		96.2061157083		170.76		97.0080374221				92.5561669968

		163.098		98.8964855916		164.366		96.2966414331		164.549		96.1937597558		171.112		96.9901049586				92.5323941595

		163.421		98.8866698631		164.7		96.2349736062		164.841		96.1824702141		171.46		96.9684940409				92.5106757649

		163.751		98.8817619988		165.044		96.18015776		165.156		96.1714845232		171.8		96.9502550395				92.489544354

		164.072		98.8757215504		165.369		96.1154750615		165.483		96.1586662975		172.137		96.928337584				92.4648910412

		164.394		98.8730788543		165.718		96.05901474		165.798		96.1466095021		172.497		96.9113247339				92.4417051875

		164.716		98.8798743587		166.07		95.9929616454		166.171		96.1353144234		172.826		96.8929324636				92.4199867929

		165.05		98.8810069427		166.418		95.9318419769		166.438		96.1253919756		173.163		96.8742336554				92.4009098246

		165.364		98.8794968307		166.756		95.8630480899		166.766		96.1128729648		173.508		96.8567609986				92.3768434955

		165.691		98.8779867186		167.076		95.8005580253		167.082		96.1029482		173.844		96.8385219972				92.3577665273

		166.023		98.8711912142		167.398		95.726556633		167.431		96.0908844134		174.176		96.8196699201				92.3345806736

		166.348		98.8538249252		167.704		95.6563923499		167.708		96.0824846804		174.51		96.7989786159				92.3184386235

		166.665		98.8474069488		168.05		95.582939116		168.061		96.0707238202		174.837		96.7848778753				92.2958397535

		167		98.8383462763		168.394		95.508115486		168.406		96.0586559867		175.176		96.7646463779				92.2726538998

		167.326		98.8296631317		168.753		95.4371289652		168.731		96.0479617027		175.534		96.7467139144				92.2521094724

		167.647		98.8300406598		169.108		95.358468226		169.114		96.033140512		175.865		96.7310804846				92.223640766

		167.976		98.8364586361		169.45		95.2891261806		169.417		96.0184698646		176.213		96.7140676345				92.1954655514

		168.308		98.8372136922		169.766		95.2173174221		169.736		96.0021155636		176.567		96.6932230615				92.1640619268

		168.63		98.8406114444		170.095		95.147153139		170.033		95.9897333518		176.898		96.6752905979				92.1402890894

		168.952		98.8387238043		170.418		95.068766479		170.376		95.9707747723		177.223		96.6561319829				92.1038961039

		169.277		98.8289080757		170.779		95.0002466713		170.685		95.9596119214		177.574		96.6342145274				92.0824712011

		169.611		98.816449651		171.151		94.9240526451		171.006		95.9430946367		177.898		96.6142895679				92.0507740847

		169.929		98.8021035861		171.515		94.8459400644		171.374		95.927951294		178.227		96.5943646084				92.0217183946

		170.243		98.7873799933		171.858		94.7628940574		171.708		95.917548421		178.565		96.5776582961				92.0017609509

		170.578		98.7783193208		172.216		94.6869741105		171.99		95.9079094581		178.892		96.5592660258				91.9832709663

		170.921		98.7677485361		172.533		94.6036540243		172.339		95.8942908595		179.22		96.5410270244				91.9571501944

		171.252		98.7598204477		172.846		94.5197857797		172.67		95.8823538679		179.566		96.5241674432				91.9342578326

		171.574		98.7564226955		173.156		94.4381101689		172.987		95.8730174927		179.908		96.5048555594				91.9163548316

		171.913		98.7571777515		173.48		94.3547900827		173.353		95.8595470214		180.254		96.4876894404				91.8905275515

		172.242		98.7579328076		173.809		94.2668106496		173.636		95.8450029103		180.601		96.4680710187				91.8626458287

		172.574		98.7564226955		174.146		94.1782830581		173.946		95.8272407918		180.951		96.4489124037				91.8286007778

		172.893		98.7530249433		174.471		94.0935925757		174.273		95.8140701992		181.291		96.4305201334				91.8033604813

		173.228		98.748494607		174.813		94.0034205088		174.654		95.7924726348		181.643		96.4115147874				91.7619781349

		173.559		98.7379238224		175.167		93.9190041057		174.968		95.7757733076		181.968		96.3888309873				91.7299875266

		173.886		98.7299957339		175.517		93.825543088		175.309		95.7652006687		182.312		96.3708985237				91.7097365911

		174.204		98.7269755098		175.848		93.7455119526		175.603		95.7537073458		182.646		96.3514333709				91.6877247047

		174.538		98.7250878696		176.203		93.6506805387		175.941		95.7408331862		182.955		96.332274756				91.6630713919

		174.877		98.7239552856		176.539		93.5648937395		176.286		95.7287237657		183.274		96.3135759478				91.6398855382

		175.208		98.7269755098		176.864		93.4728031179		176.595		95.7158462458		183.601		96.2931911815				91.6152322254

		175.538		98.7171597812		177.168		93.3848236848		176.958		95.6966800616		183.919		96.2738792977				91.578545748

		175.845		98.7201800054		177.495		93.2905404294		177.246		95.6816510883		184.244		96.2545674138				91.5497835498

		176.169		98.7167822532		177.83		93.1981757286		177.608		95.6650858116		184.6		96.2349489921				91.5180864333

		176.474		98.714517085		178.161		93.1063591863		177.916		95.6515860576		184.934		96.2139511501				91.4922591533

		176.809		98.7092316927		178.491		93.0142685648		178.235		95.6368568799		185.292		96.1926467703				91.4640839387

		177.132		98.714139557		178.83		92.9221779432		178.618		95.6218185042		185.629		96.1724152729				91.4353217404

		177.477		98.6997934922		179.179		92.8295391632		178.963		95.6073917171		185.965		96.1531033891				91.4077335094

		177.803		98.6948856279		179.491		92.7366263039		179.29		95.5866685861		186.302		96.1313392025				91.3681121139

		178.16		98.6888451795		179.836		92.6379577808		179.58		95.5691655538		186.608		96.1131002011				91.3346540465

		178.481		98.6846923713		180.159		92.5417559708		179.91		95.55196647		186.931		96.0974667713				91.3017829628

		178.818		98.6703463065		180.493		92.4466504777		180.269		95.5369147317		187.27		96.0755493158				91.2730207645

		179.164		98.6677036103		180.802		92.3625081539		180.547		95.5266228926		187.602		96.0531720536				91.2533568127

		179.502		98.6575103537		181.124		92.2704175323		180.909		95.5167908466		187.938		96.031407867				91.2345733363

		179.82		98.6480721532		181.446		92.1816158615		181.239		95.5074187356		188.312		96.0076511845				91.2166703353

		180.161		98.6382564246		181.768		92.0900733984		181.586		95.4918989557		188.642		95.9843543087				91.1870276616

		180.483		98.6367463125		182.09		92.0023680446		181.907		95.47852841		188.97		95.9639695424				91.1614938734

		180.804		98.6235328317		182.407		91.9020550461		182.262		95.4620816077		189.293		95.9417455491				91.1300902487

		181.127		98.6171148554		182.735		91.8072236322		182.601		95.4454782231		189.637		95.9222803963				91.0983931323

		181.448		98.6125845191		183.045		91.7156811691		182.94		95.428410623		189.951		95.9023554368				91.0658155404

		181.767		98.6054114867		183.382		91.6211238345		183.261		95.4144159888		190.294		95.8835033597				91.0391077849

		182.107		98.5997485663		183.708		91.5295813714		183.597		95.3979581334		190.609		95.8654176272				91.0077041602

		182.44		98.6016362064		184.025		91.4278979767		183.926		95.3813435866		190.941		95.846718819				90.9760070438

		182.787		98.5978609262		184.351		91.337999989		184.25		95.3681114143		191.265		95.8263340527				90.9507667474

		183.128		98.5974833982		184.68		91.2343980398		184.581		95.3551851944		191.604		95.806715631				90.9261134346

		183.475		98.5910654218		184.992		91.1453222898		184.916		95.34333462		191.921		95.7828056795				90.9035145645

		183.808		98.5891777817		185.3		91.0461056082		185.247		95.3291735605		192.251		95.7601218794				90.8765133172

		184.141		98.5827598053		185.64		90.9562076205		185.591		95.3190132435		192.586		95.7398903821				90.8571428571

		184.46		98.577474413		185.941		90.8600058105		185.924		95.3056184435		192.904		95.7170533131				90.8316090689

		184.788		98.5691687966		186.258		90.7728486151		186.238		95.2906817913		193.236		95.6960554711				90.8031403625

		185.114		98.5699238526		186.563		90.6774690428		186.569		95.2782071227		193.568		95.6768968561				90.7793675251

		185.45		98.5619957641		186.882		90.5856525004		186.911		95.2635742571		193.92		95.6548261317				90.7514858023

		185.777		98.560108124		187.205		90.4924655619		187.236		95.2514041622		194.273		95.6329086762				90.7282999486

		186.117		98.5563328438		187.549		90.3990045442		187.591		95.2353804001		194.596		95.6112977586				90.6977767995

		186.454		98.5521800356		187.858		90.3049953681		187.943		95.2224361622		194.936		95.5880008828				90.6731234867

		186.779		98.542741835		188.191		90.2101639542		188.298		95.2067157931		195.275		95.5643974692				90.6431873212

		187.113		98.5382114987		188.512		90.1177992534		188.637		95.1919177801		195.615		95.5397211732				90.6150121065

		187.456		98.5291508262		188.803		90.0215974434		188.976		95.1738795908		195.926		95.515351415				90.5806735637

		187.796		98.5223553218		189.092		89.9393736741		189.293		95.1586138369		196.265		95.492514346				90.5516178737

		188.142		98.5132946493		189.391		89.8437200226		189.64		95.1431913968		196.59		95.4670717053				90.5222686918

		188.481		98.5049890328		189.681		89.7628666495		189.952		95.1271494068		196.911		95.4427019471				90.4917455426

		188.814		98.4970609443		189.995		89.6699537902		190.299		95.1138818712		197.224		95.4207844916				90.4665052462

		189.148		98.4895103839		190.31		89.591293051		190.642		95.0979892473		197.559		95.3965680024				90.4362755888

		189.476		98.4838474636		190.629		89.502217301		190.995		95.0871869189		197.899		95.370512286				90.4157311615

		189.81		98.474409263		190.958		89.4254751163		191.334		95.0728333555		198.217		95.347675217				90.3884364223

		190.157		98.4695013987		191.273		89.3369475248		191.681		95.0584776247		198.561		95.3251446859				90.3611416832

		190.501		98.456665446		191.586		89.2643165286		192.006		95.0438109297		198.894		95.302001079				90.3332599604

		190.838		98.4547778059		191.893		89.1801742048		192.342		95.0303773391		199.226		95.2794705478				90.3077261721

		191.196		98.4442070213		192.213		89.1004171486		192.681		95.0158607503		199.527		95.2578596302				90.2801379412

		191.539		98.4419418531		192.522		89.0212082509		193.016		94.999024907		199.849		95.2351758301				90.2481473329

		191.873		98.439299157		192.825		88.9400807986		193.344		94.9866664261		200.159		95.2072808868				90.2246679874

		192.206		98.4411867971		193.115		88.8570347916		193.699		94.9698254074		200.482		95.1818382461				90.1926773791

		192.555		98.4302384845		193.41		88.7783740524		194.057		94.9577722028		200.795		95.157315219				90.1697850172

		192.883		98.4291059004		193.704		88.6988910754		194.396		94.9399986613		201.141		95.1311062338				90.1360334581

		193.224		98.422687924		194.012		88.6221488908		194.737		94.9279416696		201.453		95.1061233999				90.1131410962

		193.562		98.4147598355		194.33		88.5470511816		195.106		94.9121725232		201.769		95.0817536417				90.0832049307

		193.907		98.4034339949		194.644		88.4678422838		195.433		94.8985656639		202.093		95.0529390848				90.0573776506

		194.256		98.3939957943		194.968		88.3957594461		195.764		94.882636975		202.398		95.0255039482				90.0271479932

		194.579		98.3834250097		195.275		88.3173727861		196.101		94.8680977791		202.718		94.999294963				89.9995597623

		194.918		98.370589057		195.574		88.2480307407		196.458		94.8551034207		203.054		94.9694075237				89.9749064495

		195.274		98.3592632163		195.881		88.1756738238		196.795		94.8430356366		203.361		94.9433518073				89.9520140876

		195.62		98.353600296		196.189		88.1052354615		197.14		94.832359009		203.688		94.9179091667				89.9317631521

		195.943		98.3456722075		196.494		88.0358934161		197.484		94.8170382695		204.011		94.890627299				89.902707462

		196.303		98.3434070394		196.812		87.9723070345		197.841		94.8055847867		204.324		94.8636519692				89.8809890674

		196.625		98.3407643432		197.134		87.8994019591		198.175		94.7894856607		204.64		94.8377495218				89.8504659183

		196.973		98.336234007		197.424		87.8317043891		198.524		94.7726096032		204.988		94.8110807298				89.81847531

		197.319		98.3279283905		197.73		87.7719551168		198.894		94.7583632524		205.294		94.7830325175				89.7914740627

		197.682		98.3241531103		198.046		87.6982278037		199.241		94.7430305472		205.631		94.7543712296				89.7624183726

		198.021		98.3147149097		198.36		87.6264190452		199.581		94.7289346594		205.959		94.7278557065				89.7357106171

		198.387		98.3056542372		198.663		87.5543362075		199.93		94.7129774422		206.296		94.6998074942				89.7054809597

		198.724		98.2950834526		198.991		87.4819792906		200.251		94.6994969213		206.604		94.6691537103				89.6799471715

		199.064		98.2830025559		199.307		87.4068815813		200.575		94.682449837		206.936		94.6414120359				89.6476630714

		199.405		98.2709216592		199.608		87.3405544075		200.916		94.6706700584		207.25		94.6113713277				89.6253576932

		199.756		98.2592182905		199.918		87.2750494713		201.243		94.6570284834		207.559		94.5788783167				89.5995304131

		200.095		98.2467598658		200.234		87.2125594067		201.577		94.6458657323		207.86		94.5496039531				89.5783990021

		200.448		98.234301441		200.552		87.1539064513		201.947		94.6336161987		208.165		94.5204828584				89.5552131484

		200.796		98.2271284086		200.863		87.0938830997		202.274		94.6226057712		208.473		94.4905954191				89.5343752293

		201.131		98.2108947037		201.178		87.0281040843		202.605		94.609267481		208.781		94.4628537447				89.5091349329

		201.485		98.2048542553		201.481		86.9656140197		202.951		94.5937554762		209.101		94.43373265				89.479785751

		201.838		98.1923958306		201.789		86.9072351435		203.278		94.5825852575		209.423		94.4049180931				89.45865434

		202.176		98.1908857185		202.102		86.8455673166		203.589		94.5698620126		209.76		94.376563343				89.4345880109

		202.518		98.1788048218		202.408		86.7877365989		203.942		94.5600856737		210.079		94.3482085929				89.4160980263

		202.884		98.1776722377		202.715		86.732098515		204.291		94.5475146098		210.397		94.317554809				89.3923251889

		203.23		98.1603059487		203.028		86.6737196389		204.63		94.5360284729		210.725		94.2861346805				89.3706067943

		203.571		98.1538879723		203.341		86.6112295742		204.981		94.5183308819		211.05		94.2544080141				89.337148727

		203.927		98.131613819		203.645		86.5523025396		205.327		94.5034250767		211.367		94.2202290451				89.3089735124

		204.286		98.1214205624		203.964		86.4873457619		205.667		94.485876689		211.687		94.1834445044				89.2758089368

		204.622		98.1055643855		204.279		86.4349966288		205.997		94.4711210974		212.019		94.1491122664				89.247927214

		204.976		98.096881241		204.601		86.3777140696		206.327		94.4588489028		212.334		94.1164659866				89.2247413603

		205.329		98.0844228163		204.933		86.3256390157		206.677		94.449061073		212.652		94.0804477905				89.2062513757

		205.69		98.0776273119		205.25		86.2730158034		207.014		94.4398937729		212.994		94.0499472755				89.1889353584

		206.041		98.061771135		205.577		86.2217629872		207.345		94.432434974		213.319		94.0171477267				89.1748477511

		206.392		98.0470475421		205.91		86.1661249034		207.684		94.4246647652		213.639		93.9831220266				89.1601731602

		206.746		98.0327014773		206.225		86.1107608988		208.044		94.4150288182		213.971		93.9506290156				89.1419766674

		207.121		98.0138250762		206.529		86.0592340034		208.367		94.4022829905		214.298		93.9170631223				89.1179103382

		207.483		97.993061035		206.868		85.9989365726		208.708		94.38969091		214.595		93.8804318505				89.0941375009

		207.851		97.9730520498		207.194		85.9438466472		209.055		94.3724323672		214.914		93.8474790328				89.061559909

		208.218		97.9530430646		207.506		85.8843714541		209.401		94.3568814274		215.227		93.8131467948				89.0322107271

		208.588		97.9213307108		207.831		85.8339408756		209.728		94.3377502559		215.532		93.7769753298				88.9961112334

		208.957		97.9024543097		208.146		85.775013841		210.066		94.3243716846		215.841		93.7408038648				88.970870937

		209.324		97.8779149882		208.452		85.7295166887		210.43		94.3097464242		216.165		93.7044791309				88.943282706

		209.698		97.8514880267		208.763		85.6703155748		210.765		94.298542563		216.498		93.6680011281				88.922151295

		210.08		97.8261936492		209.074		85.6228998679		211.109		94.2879599161		216.829		93.6324427387				88.9021938513

		210.451		97.804674552		209.396		85.5667136256		211.45		94.2797108528		217.15		93.5982637697				88.8866387849

		210.824		97.77069703		209.714		85.5143644925		211.801		94.2742629625		217.483		93.5620923047				88.8763665713

		211.205		97.7393622042		210.023		85.456807854		212.124		94.2622764955		217.797		93.5285264113				88.8537677012

		211.59		97.7061397382		210.331		85.4107625432		212.481		94.2493543109		218.102		93.4940409044				88.8294078803

		211.957		97.668764464		210.662		85.3573170932		212.809		94.2370532363		218.423		93.4587890529				88.8062220266

		212.347		97.6234611014		210.999		85.3088050694		213.171		94.2238161093		218.747		93.4187858649				88.781275222

		212.723		97.581555491		211.334		85.2611152832		213.497		94.2073060273		219.074		93.3830742067				88.7501650891

		213.123		97.5328543761		211.679		85.206299437		213.836		94.1942205108		219.404		93.3446037079				88.7255117764

		213.529		97.4849083173		211.985		85.1597059678		214.166		94.1836261421		219.726		93.3058266712				88.7055543327

		213.94		97.4324319223		212.311		85.106534597		214.525		94.1671090136		220.029		93.2673561724				88.6744441999

		214.34		97.3890161997		212.632		85.0591188901		214.843		94.1558881796		220.342		93.2290389426				88.6533127889

		214.754		97.3297443003		212.96		85.0108809455		215.198		94.1432631427		220.656		93.1917945951				88.6295399516

		215.148		97.2772679052		213.276		84.9727839324		215.549		94.1325071461		220.974		93.1514848693				88.6092890161

		215.538		97.2168634217		213.635		84.9209829578		215.885		94.1187875698		221.306		93.1113284124				88.583461736

		215.953		97.153816242		213.956		84.8853526577		216.221		94.1103677486		221.637		93.0710186865				88.5676131778

		216.363		97.0783106376		214.271		84.8351961585		216.577		94.1005436718		221.98		93.0314753053				88.5491231932

		216.779		97.0050702013		214.596		84.7872322931		216.919		94.0896268278		222.304		92.9914721173				88.5285787659

		217.213		96.9250342607		214.915		84.7365276354		217.246		94.0788646989		222.642		92.9528483496				88.5083278304

		217.646		96.8419780958		215.218		84.6926749585		217.601		94.069037332		222.963		92.9119255481				88.4898378458

		218.067		96.7517488986		215.546		84.6384072708		217.939		94.0609250811		223.299		92.8716158223				88.4745762712

		218.512		96.6626522854		215.851		84.5929101185		218.281		94.0490674557		223.602		92.8303864829				88.4522708929

		218.949		96.570535448		216.175		84.5471388869		218.622		94.0414216151		223.91		92.78823753				88.4378897938

		219.359		96.4704905222		216.507		84.5013676554		218.983		94.0308100306		224.227		92.7468549218				88.4179323501

		219.792		96.3704455963		216.867		84.4621743254		219.334		94.0209776409		224.549		92.7060853892				88.3994423655

		220.218		96.2681355024		217.183		84.4180475692		219.668		94.0127051516		224.865		92.662710285				88.3838872991

		220.643		96.1624276562		217.523		84.3829654276		220.016		94.0011536655		225.221		92.6236267105				88.3621689045

		221.082		96.0506793617		217.853		84.3322607699		220.362		93.9891323688		225.579		92.580711413				88.3395700345

		221.517		95.9400636512		218.181		84.2870376969		220.696		93.9780464339		225.901		92.5371830399				88.3187321153

		221.953		95.8181221001		218.486		84.231399613		221.032		93.9697701652		226.221		92.4956471627				88.3031770489

		222.426		95.7003333572		218.824		84.1894654907		221.39		93.9546211437		226.536		92.4536514787				88.2747083425

		222.874		95.575371582		219.165		84.1354718822		221.738		93.9452493921		226.848		92.4108894502				88.2570988334

		223.3		95.4496547506		219.499		84.0921673637		222.091		93.9347831644		227.167		92.3695068419				88.2374348815

		223.756		95.3095918545		219.826		84.0488628453		222.46		93.9249407223		227.48		92.3282775026				88.2189448969

		224.205		95.1770795187		220.185		84.0102176737		222.789		93.9133784412		227.826		92.2861285497				88.1972265023

		224.626		95.0294660621		220.528		83.9622538083		223.123		93.9036900284		228.156		92.2435197901				88.1790300095

		225.091		94.8773222692		220.861		83.9200456068		223.469		93.8963449204		228.49		92.1995316102				88.165235894

		225.567		94.7214031962		221.202		83.877563326		223.802		93.8855606356		228.809		92.1563097749				88.1449849585

		226.023		94.5662391791		221.552		83.8337106491		224.14		93.8796209352		229.146		92.110329099				88.1338322694

		226.476		94.3997493214		221.866		83.7827319121		224.503		93.8682094037		229.457		92.0683334151				88.1124073666

		226.937		94.2321268796		222.218		83.7312050167		224.838		93.8592980652		229.784		92.0244985041				88.095678333

		227.394		94.0603516296		222.549		83.6810485175		225.194		93.8460076553		230.091		91.9779047526				88.0707315284

		227.852		93.8851786274		222.879		83.6339068898		225.547		93.8381888878		230.413		91.9320773456				88.0560569374

		228.322		93.7001898966		223.215		83.5938913221		225.882		93.8250518916		230.728		91.885636863				88.0314036246

		228.81		93.5118034136		223.539		83.5544239129		226.215		93.8142594114		231.043		91.8362842709				88.0111526891

		229.292		93.3207742345		223.87		83.5196158506		226.575		93.8031528095		231.371		91.7896905194				87.99031477

		229.743		93.1210619108		224.206		83.4828892336		226.882		93.7929836404		231.697		91.7453958017				87.9712378017

		230.213		92.9202170031		224.555		83.4467107752		227.237		93.7806227043		232.02		91.6984955123				87.9480519481

		230.679		92.7193720954		224.886		83.4003913851		227.567		93.7688861305		232.356		91.6561932905				87.9260400616

		231.122		92.5219249399		225.239		83.3595535797		227.907		93.7598088395		232.679		91.6111322282				87.9090175361

		231.57		92.3154171118		225.557		83.3225528836		228.253		93.7493219092		233.008		91.5662244347				87.8893535843

		232.029		92.1096643398		225.89		83.2800706028		228.595		93.7421212479		233.345		91.5190176075				87.8758529606

		232.478		91.9001362876		226.215		83.2395068766		228.914		93.7335110356		233.68		91.4736500074				87.8597109106

		232.914		91.6826801469		226.547		83.1992172297		229.266		93.7241171745		233.998		91.4233778018				87.8421014014

		233.349		91.4625813101		226.878		83.1616683751		229.612		93.715505308		234.35		91.375251361				87.8259593514

		233.791		91.2428600013		227.2		83.1180897774		229.934		93.7053266272		234.658		91.3263585757				87.8068823832

		234.198		91.0261589166		227.532		83.0865706658		230.283		93.6951468407		234.99		91.2789984796				87.7878054149

		234.62		90.8064376078		227.848		83.0449106228		230.629		93.6830862775		235.313		91.2279599294				87.7652065449

		235.039		90.5950219155		228.184		83.0076358474		230.969		93.6740006722		235.653		91.1799867576				87.7481840194

		235.457		90.3768107188		228.514		82.9662498835		231.284		93.6624074134		235.977		91.1287949384				87.7264656248

		235.85		90.1601096341		228.868		82.927604712		231.627		93.6525363459		236.326		91.0789825396				87.7079756402

		236.249		89.9426534935		229.213		82.8878632235		231.961		93.6407837183		236.657		91.0302430232				87.6859637538

		236.63		89.7210445445		229.557		82.8522329235		232.303		93.6327910889		236.992		90.9816567757				87.670995671

		237.012		89.5028333478		229.883		82.8176989404		232.645		93.6229168988		237.324		90.9338368728				87.6525056864

		237.373		89.2887749593		230.227		82.7831649573		232.998		93.612257874		237.644		90.8857104321				87.6325482427

		237.737		89.0818896033		230.546		82.7458901819		233.332		93.602695069		237.973		90.8365111089				87.6146452418

		238.102		88.8780244714		230.882		82.7034079012		233.669		93.592347327		238.307		90.7851660209				87.5952747817

		238.446		88.6730267554		231.194		82.6617478581		234.002		93.5812143876		238.644		90.7358134288				87.5744368626

		238.766		88.4793548801		231.533		82.6157025473		234.334		93.5702369535		238.981		90.6826291137				87.5538924352

		239.103		88.2736021081		231.849		82.5723980288		234.683		93.5600424685		239.322		90.632663446				87.534815467

		239.423		88.0727572004		232.2		82.5258045596		235.048		93.5489056846		239.651		90.5820847025				87.5139775479

		239.753		87.8670044284		232.518		82.4827741203		235.415		93.5379244588		239.958		90.5318124969				87.4934331206

		240.084		87.671444913		232.864		82.4364547303		235.757		93.5289816511		240.295		90.4830729805				87.4767040869

		240.404		87.4732427014		233.206		82.3986317965		236.102		93.5162719796		240.636		90.4338736574				87.4529312495

		240.721		87.2829685783		233.553		82.3528605649		236.447		93.5087395072		240.976		90.3865135612				87.4388436422

		241.022		87.0945820954		233.885		82.3177784234		236.779		93.500578644		241.314		90.3363946246				87.4235820676

		241.32		86.9137461728		234.231		82.2755702218		237.107		93.4921031475		241.683		90.28596915				87.4077335094

		241.609		86.7370630585		234.572		82.2424066349		237.456		93.4829989805		242.005		90.2366165579				87.3907109839

		241.955		86.5373507349		234.903		82.1993761957		237.797		93.474050918		242.335		90.185118201				87.3739819503

		242.222		86.3920024464		235.245		82.1659385295		238.131		93.4640029497		242.678		90.1308610035				87.3551984738

		242.56		86.2032384354		235.569		82.1248266449		238.472		93.4548960453		243.021		90.0790561087				87.3381759483

		242.826		86.0458092502		235.918		82.0861814733		238.808		93.4450030573		243.344		90.0234194909				87.3196859638

		243.124		85.871391304		236.253		82.0497289356		239.165		93.4380930476		243.694		89.9687024866				87.3067723237

		243.389		85.7060340304		236.589		82.0102615264		239.506		93.4307113364		244.032		89.9172041297				87.2929782082

		243.714		85.5127396831		236.923		81.9790164941		239.864		93.4222295013		244.355		89.8637132768				87.27712965

		244.008		85.3424745452		237.284		81.9411935602		240.204		93.411076287		244.691		89.8106822306				87.2562917309

		244.305		85.1824026638		237.61		81.9044669433		240.563		93.4018071097		245.021		89.7593371426				87.2389757136

		244.559		85.0404521276		237.965		81.8655476925		240.897		93.3882944577		245.351		89.7047734072				87.2137354171

		244.902		84.8652791253		238.3		81.8408805618		241.265		93.37713719		245.698		89.6512825543				87.192897498

		245.196		84.7078499402		238.639		81.798398281		241.597		93.3637781441		246.037		89.596718819				87.1679506934

		245.481		84.5730724363		238.959		81.7701681202		241.939		93.3521463592		246.379		89.5412354701				87.1462322988

		245.817		84.4005421302		239.298		81.7372786125		242.282		93.3427141183		246.721		89.4886642307				87.1286227896

		246.107		84.2684073225		239.636		81.711789244		242.619		93.3323375522		247.058		89.4341004954				87.1092523296

		246.407		84.1207938659		239.983		81.6723218348		242.93		93.3257336822		247.384		89.3798432979				87.0969256732

		246.691		83.9656298489		240.329		81.6408027233		243.259		93.3211735944		247.741		89.3255861003				87.0884144104

		246.982		83.8153736961		240.678		81.6057205817		243.612		93.3147261936		248.077		89.2717887096				87.0763812459

		247.269		83.6654950714		241.025		81.5676235686		243.947		93.3035601286		248.428		89.2187576634				87.0555433267

		247.583		83.5005153258		241.358		81.5213041786		244.31		93.2936510927		248.768		89.1671060376				87.0370533421

		247.896		83.3642277098		241.702		81.483755324		244.673		93.2805947243		249.114		89.1122357644				87.0126935212

		248.214		83.2143490851		242.047		81.4478509448		245.041		93.2684805554		249.435		89.059664525				86.9900946511

		248.518		83.0784389971		242.39		81.405368664		245.377		93.2571515972		249.784		89.0040279072				86.9689632401

		248.798		82.9542322779		242.731		81.3708346809		245.73		93.2488113456		250.114		88.9476249448				86.9534081737

		249.083		82.8141693817		243.065		81.3346562224		246.067		93.2376373867		250.467		88.8903023689				86.9325702546

		249.417		82.665423341		243.399		81.2954628924		246.41		93.2297675979		250.815		88.8326732552				86.9178956637

		249.726		82.527625613		243.751		81.2565436416		246.764		93.217961669		251.179		88.7767300996				86.8958837772

		250.007		82.4094593421		244.102		81.2280394016		247.125		93.2086732874		251.509		88.7227794399				86.8785677599

		250.341		82.2561829652		244.447		81.2044685878		247.478		93.1989116177		251.865		88.6676026289				86.8603712672

		250.641		82.1380166943		244.784		81.1795273778		247.837		93.1916684278		252.206		88.6138052381				86.8468706435

		250.953		82.0058818866		245.136		81.151297217		248.191		93.1828498714		252.544		88.5578620825				86.8304351016

		251.291		81.8643088783		245.47		81.1277264031		248.526		93.17481796		252.862		88.5003862377				86.8154670189

		251.572		81.7506729437		245.807		81.0882589939		248.876		93.1645802066		253.204		88.4427571239				86.7963900506

		251.872		81.6211808321		246.165		81.0476952677		249.226		93.1552865023		253.543		88.3851280102				86.7790740333

		252.186		81.4935763607		246.521		81.0065833831		249.569		93.1434711329		253.873		88.3285717789				86.7570621469

		252.489		81.3655943612		246.869		80.9715012416		249.93		93.1335450642		254.209		88.2710959341				86.7385721623

		252.799		81.2444078662		247.211		80.9276485646		250.291		93.1226724417		254.556		88.2177583501				86.7183212268

		253.101		81.1164258667		247.552		80.8909219477		250.639		93.1141625472		254.914		88.1601292364				86.7024726686

		253.446		80.9756079145		247.891		80.8574842816		250.981		93.1032876611		255.24		88.1031131983				86.6822217331

		253.71		80.8714101804		248.254		80.8215799023		251.324		93.0952488854		255.586		88.0422654372				86.6672536503

		254.057		80.7302147002		248.602		80.7878681569		251.655		93.0859482591		255.931		87.9860157438				86.649937633

		254.359		80.6150686535		248.95		80.7519637777		252.004		93.0775926669		256.284		87.9242483692				86.6343825666

		254.647		80.504830471		249.308		80.72620033		252.354		93.0670288635		256.615		87.8661594487				86.6147186147

		254.972		80.3862866721		249.651		80.6938589808		252.689		93.0594600282		256.957		87.8068443769				86.6006310074

		255.302		80.264722649		250		80.6659028992		253.04		93.0512597619		257.302		87.7476825739				86.5853694328

		255.616		80.1522192985		250.345		80.6368505007		253.405		93.0416392976		257.651		87.6899001913				86.5674664319

		255.927		80.0317878595		250.707		80.6056054684		253.758		93.0310714117		257.992		87.6319645397				86.54780248

		256.227		79.9177743968		251.058		80.5661380592		254.106		93.0216066142		258.344		87.574182157				86.5301929709

		256.554		79.7931901495		251.405		80.536263423		254.467		93.009458713		258.697		87.5165530433				86.5075941008

		256.814		79.6999407281		251.75		80.5017294399		254.784		92.9977826113		259.035		87.4586173917				86.4858757062

		257.157		79.5798868171		252.084		80.4669213776		255.116		92.9856315977		259.387		87.4005284712				86.4632768362

		257.439		79.4783317792		252.424		80.4386912169		255.461		92.9755308454		259.719		87.3427460886				86.4444933597

		257.77		79.372623933		252.777		80.4132018484		255.793		92.9652711455		260.068		87.2812852519				86.4254163915

		258.102		79.2654059748		253.129		80.3797641822		256.141		92.9564311114		260.417		87.2225832557				86.4089808497

		258.417		79.1585655445		253.466		80.3413930899		256.515		92.9468008318		260.766		87.1631149149				86.3910778487

		258.729		79.0536127544		253.834		80.3079554238		256.862		92.9385906253		261.078		87.1010410025				86.3758162741

		259.067		78.9528127725		254.171		80.2706806484		257.19		92.9273793642		261.423		87.0420324685				86.354978355

		259.367		78.8501251505		254.497		80.235872586		257.551		92.9167984829		261.745		86.9840968169				86.3353144031

		259.683		78.7459274165		254.835		80.1953088599		257.904		92.9040050621		262.08		86.9227892491				86.3115415658

		259.99		78.6436173225		255.183		80.1695454122		258.25		92.8945273182		262.421		86.8642405218				86.2939320566

		260.293		78.5409297005		255.527		80.1328187953		258.598		92.8839426945		262.778		86.8038525676				86.2742681048

		260.601		78.445792639		255.886		80.1043145553		258.954		92.8754109259		263.131		86.7396328903				86.2584195466

		260.91		78.3457477131		256.245		80.068410176		259.306		92.8648241234		263.477		86.6783253225				86.2387555947

		261.215		78.2547634598		256.583		80.0423726491		259.643		92.856922738		263.818		86.6187037128				86.2240810037

		261.538		78.1600039263		256.921		80.0089349829		259.992		92.8458596688		264.157		86.5590821031				86.2035365764

		261.896		78.0573163043		257.266		79.979334426		260.342		92.8344791365		264.491		86.5011464515				86.1824051655

		262.169		77.9704848592		257.619		79.9461708391		260.711		92.8221486519		264.837		86.4418313797				86.1595128036

		262.526		77.8696848774		257.955		79.9146517275		261.062		92.810607099		265.179		86.3834359213				86.1380879008

		262.836		77.7760579279		258.314		79.883132616		261.409		92.798115308		265.542		86.3209022022				86.1149020471

		263.156		77.6880938988		258.69		79.8450356029		261.759		92.7837239453		265.901		86.2595946344				86.0881942916

		263.465		77.6023950378		259.038		79.8124201744		262.116		92.7737593865		266.262		86.1978272598				86.069704307

		263.75		77.5234916812		259.388		79.7756935575		262.453		92.7631609828		266.608		86.1359066163				86.0500403551

		264.062		77.435150124		259.742		79.7444485252		262.788		92.7530360035		266.958		86.0759784688				86.0312568787

		264.424		77.3385029504		260.114		79.7052551952		263.145		92.7433846038		267.287		86.0169699348				86.0133538778

		264.715		77.2614872339		260.444		79.6759287175		263.494		92.7351563881		267.629		85.9525969886				85.9980923032

		265.079		77.1637074762		260.796		79.6411206552		263.838		92.7229709582		267.958		85.8911361518				85.9754934331

		265.413		77.0776310872		261.141		79.6150831282		264.168		92.7117336231		268.29		85.8301351219				85.954655514

		265.729		77.006655819		261.495		79.5832899375		264.529		92.701761326		268.649		85.766988327				85.9361655294

		266.062		76.9179367339		261.841		79.5547856974		264.878		92.6905214195		269		85.7055274903				85.9153276102

		266.393		76.8379007932		262.203		79.5271036951		265.227		92.6786467984		269.33		85.6437601157				85.8933157238

		266.698		76.7525794602		262.549		79.4953105044		265.59		92.6658204984		269.674		85.5819927412				85.8695428865

		267.017		76.6710334075		262.907		79.4621469174		265.957		92.6525172749		270.034		85.5222178626				85.8448895737

		267.363		76.5898648827		263.271		79.4256943797		266.282		92.6382617011		270.37		85.4584579921				85.81847531

		267.644		76.5200221986		263.619		79.3958197436		266.624		92.6247960891		270.717		85.3959242729				85.7935285054

		267.969		76.4448941223		263.977		79.3588190474		266.973		92.6129130408		271.07		85.334769974				85.771516619

		268.348		76.3667458217		264.338		79.3303148074		267.316		92.6038809043		271.415		85.2717764481				85.7547875853

		268.672		76.2908626893		264.676		79.2955067451		267.675		92.5956402919		271.739		85.2066371573				85.7395260107

		268.978		76.2225301173		265.024		79.2697432974		268.033		92.5870819567		272.08		85.1447165138				85.7236774525

		269.346		76.1413615926		265.388		79.2357574728		268.386		92.580741939		272.425		85.081569719				85.7119377797

		269.655		76.0730290206		265.734		79.2141052135		268.754		92.5715481421		272.767		85.0193425376				85.6949152542

		269.954		76.0088492568		266.083		79.1787489928		269.094		92.5612436639		273.121		84.9571153563				85.675838286

		270.324		75.9303234283		266.446		79.1521633074		269.421		92.5507794813		273.468		84.8959610574				85.656467826

		270.655		75.8589706321		266.809		79.1192737997		269.776		92.5411069877		273.803		84.830208691				85.638564825

		270.975		75.7861077238		267.152		79.085287975		270.132		92.5290545973		274.141		84.7659890137				85.6162594468

		271.297		75.7083369513		267.513		79.0499317543		270.46		92.5189039982		274.471		84.7054477905				85.5974759704

		271.637		75.634718987		267.888		79.0192348804		270.796		92.5063728165		274.811		84.6407683064				85.5742901167

		271.944		75.5648763029		268.257		78.9871676104		271.16		92.494474554		275.159		84.578694394				85.5522782302

		272.28		75.4927684507		268.615		78.953455865		271.502		92.4828921085		275.51		84.5161606749				85.5308533275

		272.602		75.429343743		268.971		78.9222108327		271.838		92.4700386558		275.854		84.45301388				85.5070804901

		272.94		75.3617662271		269.33		78.8887731665		272.201		92.459088009		276.2		84.3875680514				85.4868295546

		273.259		75.2926785991		269.677		78.8602689265		272.558		92.4487709958		276.548		84.3242679876				85.4677525864

		273.603		75.2217033309		270.029		78.825186785		272.902		92.4386115809		276.901		84.2579025455				85.44896911

		273.927		75.154503343		270.383		78.7955862281		273.259		92.4289273491		277.253		84.1975145912				85.431066109

		274.284		75.085038187		270.758		78.768178305		273.619		92.4159076025		277.605		84.1352874099				85.4069997799

		274.638		75.0189707831		271.116		78.7377555104		273.954		92.4003450111		277.961		84.072293884				85.3782375816

		274.977		74.9532809073		271.47		78.6977399427		274.309		92.3873212365		278.321		84.009453627				85.3541712525

		275.338		74.8872135034		271.828		78.6659467519		274.66		92.3749310639		278.668		83.9472264456				85.3312788906

		275.681		74.8215236276		272.199		78.6289460557		274.998		92.3609504122		279.03		83.8814740792				85.3054516105

		276.023		74.7524359996		272.551		78.5911231219		275.346		92.3525292259		279.378		83.8163347884				85.2898965441

		276.363		74.6871236518		272.911		78.553300188		275.704		92.3436305341		279.733		83.7525749178				85.2734610023

		276.712		74.622188832		273.296		78.5242477896		276.047		92.3345720565		280.051		83.6874356271				85.2567319686

		277.041		74.5610292924		273.668		78.4897138065		276.396		92.3232874466		280.388		83.6216832606				85.2358940495

		277.383		74.4949618885		274.027		78.4584687742		276.764		92.3134321519		280.724		83.559915886				85.2176975567

		277.742		74.4304045968		274.395		78.4277719003		277.117		92.3021449575		281.062		83.4969223601				85.1968596375

		278.094		74.3684900012		274.766		78.389400808		277.466		92.2914923954		281.415		83.430403649				85.1771956857

		278.453		74.3005349572		275.108		78.3589780134		277.831		92.2800434952		281.775		83.3680231988				85.1560642747

		278.808		74.2363551935		275.468		78.3230736341		278.184		92.2682750896		282.143		83.302883908				85.1343458801

		279.176		74.1680226215		275.845		78.2893618887		278.54		92.2552326705		282.5		83.2375913483				85.110279551

		279.516		74.107618138		276.218		78.2526352718		278.889		92.243302014		282.866		83.1736782088				85.0882676645

		279.864		74.0336226456		276.583		78.227968141		279.264		92.2326426558		283.224		83.1106846829				85.0686037127

		280.203		73.9747282742		276.963		78.1865821772		279.631		92.2224594317		283.583		83.0467715435				85.0498202363

		280.559		73.9014878379		277.335		78.156707541		279.983		92.2114793834		283.944		82.9868433959				85.0295693008

		280.908		73.8373080742		277.708		78.1186105279		280.346		92.200975505		284.285		82.9218573741				85.0101988407

		281.277		73.7670878621		278.099		78.0821579902		280.729		92.1885602875		284.622		82.8564115454				84.9873064788

		281.638		73.7040406824		278.489		78.0429646602		281.093		92.1766210014		284.976		82.7912722546				84.9652945924

		282.007		73.62815755		278.876		78.0073343602		281.46		92.1638840582		285.313		82.727665653				84.9418152469

		282.357		73.5568047538		279.262		77.9697855056		281.824		92.1500306341		285.641		82.6631394379				84.9162814587

		282.711		73.4873395978		279.644		77.927577304		282.188		92.1371307461		286.001		82.5992262985				84.8925086213

		283.055		73.4182519698		280.013		77.8916729248		282.53		92.1242290519		286.356		82.5362327726				84.868735784

		283.406		73.3521845659		280.376		77.846723931		282.874		92.1105289788		286.698		82.4746186669				84.8434954876

		283.748		73.2842295219		280.759		77.8091750763		283.232		92.0969862064		287.064		82.4079466869				84.818548683

		284.114		73.2208048142		281.145		77.763677924		283.6		92.087584758		287.418		82.3446466232				84.8012326656

		284.462		73.1494520181		281.518		77.7269513071		283.952		92.076269878		287.761		82.2779746432				84.7803947465

		284.8		73.0773441659		281.913		77.6806319171		284.314		92.0678226527		288.109		82.2152876551				84.7648396801

		285.15		73.0007059774		282.31		77.6414385871		284.691		92.0568241602		288.457		82.1510679778				84.7445887446

		285.511		72.9312408214		282.698		77.5981340686		285.049		92.0459837803		288.802		82.087921183				84.7246313009

		285.859		72.8576228571		283.085		77.5548295501		285.431		92.0321126089		289.161		82.0237015057				84.6990975127

		286.213		72.788912757		283.478		77.513169507		285.803		92.0191961904		289.503		81.9617808622				84.6753246753

		286.571		72.7179374889		283.854		77.4687686716		286.161		92.0027689898		289.849		81.8960284958				84.645095018

		286.917		72.6548903092		284.247		77.4271086286		286.514		91.9892103528		290.205		81.8301228604				84.6201482134

		287.262		72.581649873		284.63		77.3753076539		286.89		91.9745328697		290.551		81.7659031831				84.593146966

		287.608		72.5189802213		285.011		77.3276178678		287.24		91.9627253682		290.88		81.7003040855				84.5714285714

		287.943		72.4502701213		285.414		77.2747205762		287.616		91.9501183891		291.234		81.6370040218				84.5482427177

		288.297		72.3842027174		285.817		77.2226455224		288.004		91.9379885246		291.58		81.5755431851				84.5259373395

		288.637		72.3124723933		286.199		77.16645928		288.393		91.9260166944		291.908		81.5140823483				84.5039254531

		288.985		72.2407420691		286.589		77.1124656716		288.749		91.9151608873		292.241		81.4503224778				84.4839680094

		289.321		72.1625937685		286.984		77.0592943008		289.145		91.9022280318		292.591		81.3873289519				84.4601951721

		289.672		72.0897308603		287.343		77.0014635831		289.504		91.888814259		292.946		81.3237223503				84.4355418593

		290.008		72.0180005361		287.715		76.9477440539		289.872		91.8771554612		293.292		81.259502673				84.4141169565

		290.362		71.9383421234		288.094		76.8912837323		290.23		91.8632587971		293.649		81.1963558782				84.3885831682

		290.7		71.8684994394		288.47		76.8392086784		290.591		91.8498393333		294.011		81.1324427387				84.3639298555

		291.033		71.7979016993		288.847		76.78165204		290.913		91.8373766468		294.371		81.0680697925				84.3410374936

		291.363		71.7261713751		289.242		76.7188878961		291.257		91.8242730243		294.696		81.0058426112				84.3169711644

		291.691		71.6514208267		289.63		76.6550274353		291.594		91.8114872001		295.052		80.9403967826				84.2934918189

		292.018		71.5932815113		290.006		76.5884261822		291.94		91.7977404529		295.4		80.8787826769				84.2682515225

		292.348		71.5204186031		290.391		76.5201804538		292.303		91.7822329299		295.762		80.8165554956				84.2397828161

		292.69		71.4524635591		290.746		76.4475494576		292.683		91.7656033963		296.091		80.7518760116				84.2092596669

		293.036		71.3796006509		291.088		76.3831408384		293.059		91.7504103228		296.45		80.6905684438				84.1813779441

		293.387		71.3105130228		291.446		76.3096876045		293.431		91.7329751702		296.806		80.6286478003				84.1493873358

		293.735		71.2319871942		291.805		76.2389751629		293.806		91.7192166557		297.171		80.5630487027				84.1241470394

		294.091		71.1651647344		292.149		76.1605885029		294.18		91.7070562504		297.511		80.5023542106				84.1018416612

		294.441		71.0960771063		292.525		76.0865871106		294.545		91.6940940431		297.874		80.4415064496				84.0780688238

		294.775		71.0262344222		292.911		76.0060078167		294.912		91.6793693131		298.225		80.377746579				84.0510675765

		295.126		70.9582793783		293.254		75.9358435336		295.294		91.6659229287		298.576		80.3136801707				84.0264142637

		295.449		70.8910793904		293.634		75.851975289		295.661		91.6505532166		298.921		80.2511464515				83.9982390491

		295.775		70.8238794024		294.013		75.7823591644		296.021		91.6316577469		299.269		80.1864669675				83.9636070145

		296.112		70.7464861579		294.366		75.6962982859		296.393		91.6156415862		299.608		80.1240865172				83.9342578326

		296.452		70.6807962821		294.71		75.6242154482		296.773		91.601384848		299.966		80.0612462602				83.9081370607

		296.77		70.6075558458		295.093		75.533769302		297.14		91.5858440777		300.302		80.0008583059				83.8796683542

		297.128		70.5403558579		295.432		75.4578493551		297.511		91.5728647127		300.624		79.9377115111				83.8558955169

		297.467		70.4746659821		295.768		75.3665809712		297.889		91.5602040535		300.967		79.8773235568				83.8327096632

		297.793		70.4176592508		296.118		75.2909351035		298.246		91.5456180861		301.349		79.8163225269				83.8060019077

		298.13		70.3557446551		296.473		75.197748165		298.604		91.5310297944		301.71		79.7539420766				83.7792941522

		298.483		70.2926974755		296.817		75.1253912481		298.981		91.5165995262		302.067		79.6930943156				83.7528798885

		298.808		70.2304053518		297.172		75.0319302304		299.346		91.4997613371		302.431		79.6337792437				83.7220632475

		299.147		70.1662255881		297.533		74.962588185		299.722		91.4845241146		302.788		79.5736978273				83.6941815247

		299.491		70.0982705441		297.898		74.8674826919		300.09		91.4716908006		303.114		79.5137696797				83.6707021792

		299.832		70.0337132524		298.252		74.7852589226		300.458		91.4559675368		303.453		79.4521555741				83.6419399809

		300.172		69.9717986568		298.607		74.690701588		300.806		91.4397601196		303.82		79.3917676198				83.6122973072

		300.495		69.907618893		298.958		74.598062808		301.177		91.4240313643		304.181		79.3310731277				83.583535109

		300.835		69.8426840732		299.297		74.4919941457		301.529		91.4073366639		304.552		79.2696122909				83.5530119598

		301.162		69.7811470056		299.626		74.3996294449		301.892		91.3880697583		304.904		79.2089177988				83.5177929415

		301.487		69.7177222979		299.963		74.3004127633		302.257		91.3702442536		305.263		79.1488363824				83.4852153496

		301.809		69.6569402864		300.303		74.2033887156		302.626		91.3533790884		305.601		79.0898278483				83.4543987086

		302.151		69.5931380507		300.645		74.1192463917		302.987		91.3358681463		305.957		79.0300529697				83.4224081004

		302.475		69.5346212073		301.007		74.0348299887		303.352		91.3191573281		306.299		78.9690519398				83.3918849512

		302.817		69.4723290836		301.357		73.9539766156		303.713		91.3030863494		306.666		78.9080509098				83.3625357693

		303.161		69.4119246001		301.717		73.8709306086		304.074		91.2850834943		307.017		78.8493489136				83.3296646856

		303.492		69.3503875325		302.071		73.7876105224		304.444		91.2672378752		307.376		78.7888076904				83.2970870937

		303.835		69.2926257451		302.424		73.7037422778		304.81		91.2477805668		307.72		78.7320981902				83.2615745836

		304.184		69.2288235094		302.757		73.6201481124		305.174		91.2281582526		308.079		78.6735494629				83.2257685817

		304.516		69.1714392501		303.086		73.5340872339		305.568		91.2080490441		308.452		78.616380156				83.1890821043

		304.839		69.1121673506		303.437		73.4600858416		305.95		91.1900274266		308.81		78.5604370003				83.1562110206

		305.178		69.0540280352		303.78		73.3740249631		306.304		91.1716803362		309.171		78.5015817352				83.1227529533

		305.527		68.9958887198		304.118		73.2975568577		306.662		91.153329553		309.527		78.4399676296				83.0892948859

		305.851		68.9411471566		304.467		73.2071107116		307.039		91.1364242468		309.874		78.3826450537				83.0584782449

		306.19		68.8833853693		304.836		73.1268054969		307.39		91.1179053127		310.198		78.32501594				83.0247266857

		306.542		68.82788875		305.177		73.0391001431		307.738		91.0988993628		310.539		78.2663139438				82.9900946511

		306.866		68.7739022429		305.516		72.9642765131		308.106		91.0797283289		310.877		78.2097577125				82.9551691247

		307.184		68.7214258478		305.871		72.8839712984		308.486		91.0611978647		311.232		78.1550407082				82.9214175655

		307.517		68.6670618127		306.22		72.8113403023		308.849		91.0407294042		311.592		78.1007835107				82.8841441045

		307.849		68.6074123852		306.556		72.7417241776		309.213		91.0228358779		311.95		78.043154397				82.8515665126

		308.187		68.5473854297		306.907		72.6663523891		309.566		91.0054225836		312.318		77.9872112414				82.8198693961

		308.537		68.4873584742		307.248		72.5904324422		309.931		90.9875221139		312.67		77.9309615479				82.7872918042

		308.874		68.4292191588		307.578		72.5139643368		310.268		90.9697794348		313.024		77.8728726274				82.7550077042

		309.225		68.3759877077		307.914		72.4451704499		310.616		90.9521946387		313.377		77.8195350434				82.7230170959

		309.563		68.330306817		308.258		72.3684282652		310.969		90.9328312974		313.728		77.7632853499				82.6877980776

		309.893		68.2770753659		308.597		72.3051159629		311.322		90.9145937142		314.055		77.7070356565				82.6546335021

		310.231		68.2317720033		308.936		72.2319368083		311.671		90.893769345		314.412		77.6513990387				82.6167730575

		310.57		68.175520328		309.283		72.1595798914		312.024		90.8731016884		314.748		77.5968353033				82.5792061046

		310.887		68.1177585406		309.625		72.0817413898		312.358		90.8537214903		315.105		77.5364473491				82.5439870864

		311.225		68.056221473		309.965		72.0121252652		312.691		90.8344987105		315.455		77.4835695718				82.5090615599

		311.561		68.0060102461		310.283		71.9301755752		313.035		90.8139791546		315.83		77.4302319878				82.4717880989

		311.9		67.9444731785		310.615		71.8690559067		313.376		90.795556076		316.184		77.3770476728				82.4383300316

		312.232		67.8919967835		310.952		71.8008101782		313.695		90.7771292585		316.556		77.3266221982				82.4048719642

		312.573		67.8361226362		311.279		71.7421572228		314.035		90.7580519456		316.885		77.2743574967				82.3702399296

		312.903		67.7859114093		311.617		71.6788449205		314.377		90.7383237269		317.244		77.2225526019				82.3344339277

		313.236		67.7277720939		311.952		71.6207401236		314.722		90.7192382535		317.61		77.1695215557				82.299801893

		313.577		67.679070979		312.282		71.553590712		315.042		90.6995015924		317.962		77.1154176272				82.2639958911

		313.911		67.6239518878		312.6		71.4943895981		315.392		90.6807316028		318.309		77.0596277404				82.2299508401

		314.242		67.5688327966		312.943		71.428884662		315.74		90.659853516		318.685		77.0069032321				82.1920903955

		314.565		67.5163564016		313.282		71.3581722204		316.084		90.641075316		319.042		76.9498871941				82.1580453445

		314.883		67.4665227026		313.639		71.2929413635		316.426		90.6221312934		319.375		76.8962430722				82.1237068017

		315.181		67.4129137235		313.992		71.2285327442		316.766		90.6041550978		319.731		76.8464306734				82.0911292098

		315.507		67.3604373285		314.328		71.1649463627		317.106		90.5848793582		320.096		76.7935528962				82.0562036833

		315.84		67.3132463257		314.662		71.1032785358		317.438		90.5667337379		320.437		76.7379162784				82.0233325996

		316.165		67.2622800427		314.972		71.0479145311		317.785		90.5479362264		320.786		76.689176762				81.9892875486

		316.507		67.2128238719		315.306		70.9925505265		318.128		90.5292969096		321.147		76.6407437834				81.9555359894

		316.863		67.163367701		315.642		70.936090205		318.469		90.5101673597		321.502		76.5889388886				81.9209039548

		317.205		67.1207070345		315.997		70.8766150119		318.824		90.4918445935		321.846		76.5394330276				81.8877393793

		317.529		67.0678531114		316.32		70.8228954826		319.153		90.4730315223		322.206		76.4916131247				81.8536943283

		317.866		67.0199070526		316.677		70.7653388442		319.477		90.4530789053		322.565		76.4401147678				81.8175948345

		318.202		66.9670531295		317.021		70.7127156318		319.801		90.4329596159		322.918		76.3880033351				81.781201849

		318.533		66.9168419026		317.348		70.6565293895		320.16		90.4141342922		323.286		76.3358919025				81.747156798

		318.857		66.8617228114		317.673		70.6074692072		320.493		90.3948180326		323.634		76.2839337388				81.7122312716

		319.182		66.8156643927		318.018		70.5458013803		320.84		90.3758223911		323.978		76.2355007602				81.6778927287

		319.52		66.7650756377		318.34		70.4929040887		321.175		90.3561731254		324.327		76.1859948992				81.6423802187

		319.838		66.7205273311		318.656		70.4304140241		321.514		90.3371693578		324.67		76.1366423071				81.6080416758

		320.153		66.6710711603		319.004		70.3758722572		321.833		90.3176741605		325.008		76.0875962529				81.5728226576

		320.475		66.6287880218		319.341		70.3150266679		322.154		90.2980122414		325.368		76.0376305851				81.5373101475

		320.801		66.5831071311		319.682		70.2643220102		322.48		90.2788336837		325.746		75.9878181863				81.5026781128

		321.13		66.5404464646		320.034		70.2073135302		322.808		90.2622523247		326.125		75.9415309726				81.4727419473

		321.467		66.4985408542		320.366		70.1563347933		323.12		90.2443670526		326.486		75.8927914562				81.4404578472

		321.804		66.4555026597		320.697		70.1037115809		323.44		90.2261529511		326.849		75.8442052087				81.4075867635

		322.154		66.4105768251		321.031		70.0549254779		323.778		90.2077724966		327.197		75.7986843396				81.374422188

		322.498		66.3667835745		321.359		69.9998355525		324.101		90.1916661881		327.551		75.7519373191				81.3453664979

		322.83		66.3180824597		321.686		69.952968004		324.444		90.1723022726		327.895		75.7024314581				81.3104409715

		323.159		66.2712689849		322.025		69.8989743955		324.789		90.1535852933		328.246		75.6559909755				81.2766894123

		323.49		66.2263431503		322.36		69.8458030247		325.126		90.1340503883		328.61		75.6100102997				81.241470394

		323.818		66.1791521476		322.711		69.7934538917		325.472		90.1151626215		328.972		75.5644894306				81.207425343

		324.148		66.1323386728		323.058		69.7435714716		325.835		90.0948049921		329.302		75.5177424101				81.1707388657

		324.475		66.0919431745		323.408		69.6945112893		326.15		90.0762348227		329.663		75.4717617343				81.1372807983

		324.808		66.0428645316		323.759		69.6432584732		326.478		90.0609196973		330.019		75.4250147138				81.1096925673

		325.142		66.0024690333		324.102		69.5977613208		326.826		90.0465797725		330.355		75.380873265				81.0838652873

		325.475		65.9650937591		324.423		69.5470566631		327.154		90.0314225968		330.717		75.3335131689				81.0565705481

		325.801		65.9284735409		324.761		69.5021076693		327.476		90.0149586871		331.089		75.28937172				81.0269278744

		326.146		65.8910982668		325.084		69.4505807739		327.815		90.0001222882		331.436		75.2438508509				81.0002201189

		326.47		65.8510802964		325.424		69.4080984931		328.141		89.9812064088		331.803		75.1987897886				80.9661750679

		326.801		65.8159701904		325.743		69.35574936		328.459		89.9626127903		332.165		75.1555679533				80.9327170005

		327.134		65.7740645799		326.085		69.3116226039		328.79		89.9446679356		332.523		75.1114265045				80.9004329004

		327.481		65.7348016657		326.432		69.2611920254		329.118		89.9268826838		332.876		75.0651392908				80.8684422922

		327.818		65.6921409992		326.782		69.2187097446		329.472		89.9103996312		333.229		75.0202314974				80.8387996185

		328.168		65.654765725		327.099		69.1712940377		329.814		89.8934238247		333.568		74.9745573594				80.8082764693

		328.515		65.6109724744		327.462		69.1342933415		330.167		89.8774244574		333.904		74.9270439943				80.779514271

		328.853		65.5701994481		327.809		69.0860553969		330.474		89.8602791171		334.255		74.8815231252				80.7486976301

		329.194		65.5309365338		328.147		69.0515214138		330.819		89.8436205106		334.606		74.8352359115				80.7187614645

		329.51		65.4943163156		328.485		69.0032834692		331.141		89.8228745941		334.962		74.7907879249				80.6814880035

		329.835		65.4599612656		328.85		68.9649123769		331.473		89.8039213802		335.306		74.7464932071				80.6474429525

		330.153		65.4301365519		329.17		68.9111928476		331.806		89.7844738393		335.69		74.7025050272				80.6125174261

		330.492		65.3969140859		329.512		68.8648734576		332.173		89.7682915823		336.057		74.661122419				80.583461736

		330.817		65.3644466761		329.829		68.8149910376		332.516		89.7521064076		336.403		74.6198930796				80.5544060459

		331.163		65.329714098		330.183		68.7629159838		332.862		89.7393523957		336.744		74.5771310511				80.5315136841

		331.508		65.295359048		330.52		68.7083742168		333.212		89.7247975268		337.101		74.5351353671				80.5053929122

		331.864		65.2538309656		330.878		68.6601362722		333.554		89.7086045049		337.448		74.4920668007				80.4763372221

		332.198		65.2157006354		331.214		68.6165576745		333.887		89.6915905049		337.792		74.4491515033				80.4458140729

		332.551		65.1771927771		331.562		68.5636603829		334.215		89.6740823473		338.148		74.4050100544				80.4144104483

		332.895		65.1424601991		331.901		68.5239188945		334.533		89.6550976784		338.531		74.358263034				80.3803653973

		333.237		65.1035748128		332.23		68.4778735837		334.872		89.6370912609		338.861		74.3228579136				80.3480812972

		333.571		65.0692197628		332.585		68.4362135406		335.199		89.6189174814		339.199		74.2810154986				80.3155037053

		333.907		65.037129881		332.917		68.3882496752		335.551		89.6017226756		339.582		74.2335021335				80.2846870643

		334.245		65.0050399991		333.278		68.3443969983		335.885		89.5833779117		339.906		74.1965643239				80.2518159806

		334.604		64.969174837		333.606		68.2936923406		336.227		89.5656847594		340.269		74.1515032616				80.2201188642

		334.95		64.9438804595		333.949		68.2542249313		336.548		89.548643605		340.612		74.1108869979				80.189595715

		335.294		64.9140557458		334.272		68.2076314621		336.896		89.5324187236		340.975		74.0658259356				80.1605400249

		335.644		64.8861186722		334.605		68.1722752413		337.23		89.5163548335		341.359		74.0203050665				80.1317778267

		335.991		64.8574265425		334.936		68.1273262475		337.579		89.5019276589		341.71		73.9799953406				80.1059505466

		336.331		64.8242040765		335.268		68.0958071359		337.932		89.4860222829		342.066		73.9383061945				80.0774818402

		336.692		64.7932467787		335.605		68.0497618251		338.272		89.4701140794		342.391		73.8975366619				80.0490131338

		337.033		64.7611568969		335.934		68.0152278421		338.615		89.454695183		342.769		73.8541615577				80.0214249028

		337.377		64.7271793749		336.293		67.9691825313		338.948		89.4379610329		343.082		73.8179900927				79.9914887373

		337.715		64.6932018529		336.639		67.9269743297		339.281		89.4218801743		343.406		73.7738486439				79.962726539

		338.062		64.6614894991		336.986		67.880929019		339.63		89.4048116098		343.781		73.7284810437				79.9322033898

		338.405		64.626379393		337.322		67.840639372		339.99		89.3898739424		344.086		73.68786478				79.9054956343

		338.749		64.5931569271		337.665		67.7981570913		340.321		89.3755905413		344.454		73.6417308353				79.8799618461

		339.096		64.5633322133		337.986		67.7584156028		340.671		89.3581846913		344.753		73.6067855216				79.8488517133

		339.447		64.5335074996		338.296		67.7236075405		340.999		89.3402826865		345.101		73.5666290647				79.816861105

		339.786		64.5078355941		338.621		67.687429082		341.332		89.3245128116		345.484		73.5181960861				79.7886858904

		340.117		64.4810311045		338.962		67.6487839105		341.677		89.3061111048		345.784		73.4867759576				79.7558148067

		340.467		64.4564917831		339.301		67.6063016297		342.015		89.2883630101		346.148		73.4475391142				79.7241176902

		340.816		64.4311974056		339.656		67.5635452697		342.349		89.2732414797		346.499		73.4047770857				79.6971164429

		341.166		64.4066580842		340.014		67.5196925927		342.704		89.2577885744		346.877		73.366153318				79.6695282119

		341.508		64.3757007864		340.348		67.480773342		343.055		89.2416752497		347.224		73.3305949286				79.6407660136

		341.857		64.352671577		340.691		67.4418540912		343.408		89.2286838186		347.629		73.2889057825				79.61758016

		342.204		64.3247345034		341.015		67.4106090589		343.75		89.210426839		347.964		73.247982981				79.5850025681

		342.558		64.30057271		341.331		67.3725120458		344.099		89.1949630512		348.274		73.2121180539				79.5574143371

		342.914		64.2741457485		341.659		67.3494893904		344.437		89.1771928357		348.608		73.1695092942				79.5257172206

		343.257		64.2537592353		342.003		67.3064589512		344.786		89.1590899015		348.97		73.127973417				79.4934331206

		343.605		64.2269547457		342.336		67.2804214242		345.117		89.1401601756		349.319		73.0882767669				79.4596815614

		343.935		64.2046805924		342.685		67.233827955		345.466		89.124684196		349.697		73.0416830154				79.4320933304

		344.256		64.180141271		343.039		67.2036792396		345.803		89.1073940195		350.025		73.0088834666				79.4012766894

		344.585		64.1597547578		343.369		67.159004325		346.161		89.0929006203		350.37		72.9725587327				79.3754494093

		344.929		64.1367255485		343.706		67.1283074511		346.51		89.0797227565		350.742		72.928110746				79.3519700638

		345.264		64.1155839792		344.031		67.0839066157		346.86		89.0624238514		351.05		72.8936252391				79.3211534228

		345.604		64.0914221858		344.368		67.0507430288		347.2		89.0452863849		351.438		72.8493305214				79.2906302737

		345.945		64.0691480325		344.692		67.0060681142		347.547		89.0288049408		351.742		72.8107067536				79.2612810918

		346.276		64.0400783748		345.026		66.9671488634		347.889		89.0126501648		352.126		72.7670251116				79.2325188935

		346.609		64.0174266935		345.358		66.926311058		348.221		88.9951733302		352.426		72.731926529				79.2014087607

		346.942		63.9943974842		345.704		66.8851991734		348.556		88.9806616522		352.816		72.6877850802				79.1755814807

		347.279		63.974010971		346.051		66.8435391303		348.909		88.9673022202		353.138		72.6503874638				79.1518086433

		347.617		63.9540019858		346.39		66.8095533057		349.256		88.951466221		353.517		72.6122235029				79.1236334287

		347.952		63.940033449		346.729		66.7728266887		349.606		88.9366174109		353.856		72.5746726176				79.097219165

		348.286		63.9151165995		347.084		66.7382927057		349.955		88.9197857619		354.219		72.5325236647				79.0672829995

		348.62		63.8992604226		347.419		66.7097884656		350.302		88.9009701478		354.589		72.49206067				79.0338249321

		348.962		63.8784963814		347.739		66.6749804033		350.652		88.8790135635		354.896		72.4542032468				78.9947905202

		349.312		63.8577323402		348.066		66.6494910349		351.003		88.8583727303		355.213		72.4157327481				78.9581040428

		349.646		63.837345827		348.404		66.6097495464		351.336		88.8373967324		355.614		72.3743501398				78.9208305818

		349.991		63.8252649303		348.713		66.5828897818		351.679		88.8198854137		355.966		72.3357263721				78.889720449

		350.326		63.7984604407		349.037		66.5365703918		352.026		88.8046841117		356.293		72.3024670165				78.8627192017

		350.67		63.7780739275		349.389		66.5099847064		352.365		88.7932814273		356.636		72.2667553583				78.8424682662

		350.998		63.752402022		349.741		66.4675024256		352.719		88.7817119901		357.006		72.2287446662				78.8219238389

		351.355		63.7271076446		350.088		66.440642661		353.092		88.7699757349		357.37		72.1846032174				78.8010859197

		351.69		63.7033233792		350.434		66.3959677464		353.447		88.7550965613		357.717		72.1490448281				78.774671656

		352.045		63.6889773143		350.787		66.3655449517		353.804		88.7382304818		358.061		72.1102677915				78.7447354905

		352.387		63.6697233852		351.119		66.3244330671		354.17		88.7203687853		358.383		72.0740963265				78.7130383741

		352.744		63.6614177687		351.458		66.290995401		354.515		88.7018417454		358.718		72.0370052479				78.6801672903

		353.079		63.6466941759		351.795		66.2509798333		354.855		88.6821525246		359.076		71.9982282113				78.6452417639

		353.428		63.6338582231		352.144		66.2164458502		355.208		88.6661000932		359.442		71.9557727206				78.6167730575

		353.766		63.6180020462		352.474		66.1816377879		355.551		88.653024316		359.748		71.9219002894				78.5935872038

		354.118		63.6032784533		352.822		66.1608077663		355.887		88.6387877328		360.09		71.884502673				78.5683469073

		354.462		63.5817593561		353.171		66.1246293078		356.245		88.6235553676		360.448		71.8446527539				78.54134566

		354.815		63.5696784594		353.519		66.0942065132		356.598		88.6094796596		360.781		71.8061822551				78.5163988554

		355.16		63.5530672264		353.863		66.0662504317		356.94		88.5917576475		361.174		71.7629604198				78.4849952308

		355.508		63.5368335215		354.225		66.0344572409		357.296		88.5715469148		361.53		71.7247964589				78.4491892289

		355.856		63.5239975687		354.564		65.9963602278		357.656		88.5510001317		361.867		71.6884717249				78.4127962433

		356.195		63.5126717281		354.905		65.962100324		357.999		88.5317746305		362.16		71.6538329491				78.3787511923

		356.544		63.4881324066		355.247		65.9338701632		358.351		88.5113844082		362.51		71.615975526				78.3426516986

		356.904		63.4685009495		355.581		65.8938545955		358.719		88.4934769247		362.839		71.5799573299				78.3109545821

		357.248		63.4515121885		355.91		65.8650762762		359.091		88.4765609733		363.208		71.5364289568				78.2810184166

		357.593		63.4337683715		356.239		65.8234162332		359.441		88.4627936455		363.533		71.5043957526				78.2566585956

		357.961		63.4133818583		356.573		65.7888822501		359.815		88.4488582645		363.924		71.4622467997				78.2320052829

		358.316		63.3997908495		356.9		65.7444814147		360.168		88.4340910006		364.212		71.4296005199				78.205884511

		358.671		63.3820470324		357.262		65.7121400655		360.531		88.4178275648		364.598		71.3882179116				78.1771223127

		359.039		63.3677009676		357.609		65.6710281808		360.87		88.4007311369		364.887		71.3537324047				78.1468926554

		359.398		63.3495796225		357.982		65.6414276239		361.227		88.3804767205		365.211		71.3167945951				78.1110866535

		359.726		63.3337234456		358.333		65.6025083731		361.545		88.3605498145		365.556		71.2790904409				78.0758676352

		360.079		63.3193773808		358.696		65.57866348		361.887		88.3396217255		365.941		71.2384741773				78.038887666

		360.413		63.3076740121		359.031		65.5433072593		362.218		88.321180967		366.297		71.1992373339				78.0063100741

		360.746		63.288042555		359.37		65.5186401285		362.582		88.3022378011		366.621		71.1662845162				77.9728520068

		361.084		63.2752066022		359.693		65.4734170554		362.93		88.2851189892		366.974		71.1298065133				77.9426223494

		361.429		63.2627481775		360.015		65.4495721623		363.297		88.2671656013		367.327		71.0951677375				77.910925233

		361.752		63.2468920006		360.35		65.4081861985		363.652		88.2533656083		367.703		71.0548580117				77.886565412

		362.106		63.2280155995		360.682		65.3689928685		364.007		88.2360710043		368.006		71.0228248075				77.8560422628

		362.463		63.2125369506		361.016		65.3273328254		364.336		88.2199374044		368.393		70.9769974006				77.8275735564

		362.821		63.1981908857		361.347		65.2982804269		364.681		88.20346811		368.738		70.9394465153				77.7985178663

		363.162		63.1793144846		361.707		65.2590870969		365.027		88.1878277515		369.09		70.9031217814				77.7709296353

		363.516		63.1645908918		362.052		65.2275679854		365.375		88.1691888086		369.467		70.8652643582				77.7380585516

		363.86		63.1559077473		362.404		65.1990637453		365.716		88.1535423682		369.836		70.8303190446				77.7104703206

		364.199		63.1423167385		362.765		65.1637075246		366.074		88.1368941697		370.183		70.7965998823				77.6811211387

		364.524		63.1253279775		363.122		65.1308180169		366.438		88.1204093549		370.551		70.7595088038				77.6520654487

		364.877		63.1094718005		363.474		65.096558113		366.806		88.1024224027		370.887		70.7224177252				77.6203683322

		365.222		63.0932380956		363.818		65.0628463676		367.181		88.0835987893		371.198		70.6871658738				77.5872037567

		365.566		63.0705864143		364.156		65.0239271169		367.542		88.0651044199		371.523		70.6508411398				77.5546261648

		365.914		63.0520875412		364.496		64.9943265599		367.92		88.0429393835		371.864		70.6145164059				77.5155917529

		366.264		63.0362313643		364.847		64.9565036261		368.275		88.0187681345		372.204		70.5786514787				77.4730354391

		366.629		63.0203751873		365.183		64.9216955638		368.628		87.9940899436		372.551		70.5423267448				77.4295986499

		366.988		63.0048965384		365.527		64.879213283		368.976		87.9739087115		372.912		70.5066150866				77.3940861398

		367.346		62.9939482258		365.869		64.8455015376		369.353		87.9507195974		373.265		70.4719763108				77.353290777

		367.69		62.9905504736		366.197		64.799730306		369.701		87.9318635089		373.608		70.4361113836				77.3201262015

		368.039		62.9754493527		366.543		64.7693075114		370.053		87.9145056588		373.958		70.4022389524				77.2896030523

		368.378		62.9645010401		366.893		64.728469706		370.423		87.8983130361		374.308		70.3700524793				77.2611343459

		368.711		62.9505325033		367.236		64.6969505945		370.798		87.8787777584		374.677		70.3367931237				77.2267958031

		369.046		62.9331662143		367.585		64.6626906906		371.157		87.8622445155		375.03		70.303993575				77.197740113

		369.403		62.9082493648		367.954		64.6311715791		371.508		87.8445388059		375.388		70.2713472951				77.1666299802

		369.752		62.8927707159		368.289		64.5955412791		371.878		87.8261611823		375.714		70.2345627544				77.1343458801

		370.1		62.8738943148		368.643		64.5634740091		372.233		87.8062756035		376.051		70.1988510962				77.0994203537

		370.477		62.860680834		368.997		64.5264733129		372.588		87.7878899698		376.388		70.1640590514				77.0671362536

		370.83		62.8512426335		369.361		64.4878281414		372.951		87.7666581297		376.727		70.1271212418				77.0298627926

		371.183		62.8410493769		369.726		64.449457049		373.308		87.7447521874		377.059		70.0895703566				76.9914153643

		371.523		62.8297235362		370.085		64.4075229267		373.668		87.7245135947		377.427		70.0553913875				76.9559028542

		371.871		62.8149999434		370.434		64.3751815775		374.034		87.7047722872		377.795		70.0202928049				76.9212708196

		372.212		62.7995212945		370.787		64.339003119		374.395		87.6850265353		378.127		69.9841213399				76.8866387849

		372.566		62.7806448934		371.119		64.3055654529		374.753		87.6636023856		378.485		69.9499423709				76.8490718321

		372.899		62.7610134362		371.46		64.2630831721		375.119		87.6440147924		378.826		69.9139241748				76.8147332893

		373.255		62.7421370351		371.805		64.2274528721		375.478		87.6224131399		379.156		69.8788255922				76.7768728447

		373.602		62.7296786104		372.152		64.1770222936		375.835		87.5991309785		379.494		69.8440335475				76.7360774818

		373.958		62.7134449054		372.503		64.1353622505		376.204		87.5758426274		379.856		69.8080153514				76.695282119

		374.306		62.6994763686		372.879		64.0832871967		376.562		87.5543917609		380.187		69.7749092648				76.6577151662

		374.663		62.6847527758		373.221		64.0479309759		376.912		87.5326003439		380.53		69.7419564471				76.6195612297

		375.017		62.6670089587		373.586		64.0081894874		377.275		87.5082881309		380.863		69.7091568983				76.577004916

		375.368		62.6454898615		373.961		63.9725591874		377.639		87.4869884354		381.214		69.6726788955				76.539731455

		375.691		62.6269909884		374.335		63.9292546689		378.005		87.464844672		381.541		69.6368139683				76.5009905349

		376.028		62.6050943631		374.682		63.8966392405		378.379		87.4445412961		381.884		69.5997228898				76.4654780248

		376.374		62.5873505461		375.034		63.8530606428		378.757		87.4230582123		382.255		69.5661569964				76.427911072

		376.717		62.5760247054		375.376		63.8108524412		379.11		87.4057672094		382.621		69.5282995733				76.3976814146

		377.052		62.5662089769		375.719		63.7727554281		379.475		87.3857859656		382.958		69.4967261759				76.3627558882

		377.401		62.5541280802		376.055		63.7313694643		379.818		87.3642884338		383.329		69.4662256609				76.3251889354

		377.749		62.5446898796		376.405		63.6869686289		380.165		87.3406014342		383.675		69.4351120702				76.2838065889

		378.116		62.5310988708		376.762		63.650242012		380.52		87.3158996355		384.012		69.4021592525				76.2406632915

		378.467		62.5159977499		377.102		63.6020040673		380.883		87.2879966831		384.351		69.3728848889				76.1919436496

		378.835		62.4990089889		377.447		63.5540402019		381.221		87.2644571374		384.701		69.342231105				76.1508547949

		379.19		62.482397756		377.797		63.5099134458		381.598		87.242088686		385.03		69.3072857914				76.111820383

		379.535		62.4703168593		378.154		63.4652385312		381.949		87.2188732511		385.371		69.2728002845				76.071318512

		379.847		62.4548382104		378.51		63.4156301904		382.314		87.1976711517		385.725		69.2386213154				76.0343385428

		380.178		62.4355842812		378.875		63.3761627811		382.671		87.1768005591		386.079		69.2056684977				75.9979455573

		380.518		62.4208606884		379.24		63.3312137873		383.054		87.1528942256		386.43		69.1710297219				75.956269719

		380.855		62.4057595675		379.61		63.2922945365		383.426		87.1276339321		386.776		69.1391497866				75.9122459461

		381.213		62.3883932785		379.965		63.257212395		383.806		87.1043879923		387.118		69.1060437				75.8717440751

		381.567		62.3744247417		380.32		63.2188413026		384.17		87.0828209938		387.446		69.073703958				75.8341771223

		381.927		62.3581910367		380.686		63.1796479726		384.541		87.0634398374		387.784		69.0379922998				75.8004255631

		382.278		62.3396921637		381.032		63.1371656919		384.899		87.0416941003		388.124		69.0047329442				75.7625651185

		382.648		62.3253460988		381.384		63.0930389357		385.244		87.0216292608		388.472		68.9731595468				75.727639592

		382.993		62.3064696977		381.733		63.0415120403		385.6		86.998523673		388.822		68.9434253764				75.6874312129

		383.361		62.2883483527		382.101		62.9949185711		385.952		86.9745683373		389.179		68.9144575506				75.6457553746

		383.713		62.2724921757		382.456		62.9436657549		386.331		86.9489186926		389.532		68.8830374221				75.6011446181

		384.045		62.2566359988		382.821		62.9028279495		386.694		86.9274819359		389.864		68.8531499828				75.5638711571

		384.372		62.2419124059		383.177		62.8567826387		387.049		86.9026627093		390.217		68.8238756192				75.5207278597

		384.713		62.2283213972		383.542		62.8143003579		387.399		86.8788498504		390.564		68.7915358772				75.4793455132

		385.058		62.2143528603		383.892		62.7657883341		387.765		86.8533408964		390.904		68.7562840257				75.4350282486

		385.395		62.1992517395		384.256		62.7227578949		388.104		86.8279934559		391.257		68.7263965864				75.3910044758

		385.76		62.1864157867		384.604		62.6704087618		388.457		86.8006099063		391.611		68.6911447349				75.3434588011

		386.134		62.1675393856		384.969		62.624363451		388.821		86.7764308271		391.934		68.656659228				75.301489471

		386.487		62.1539483768		385.327		62.5750291894		389.184		86.7510609146		392.287		68.6275381333				75.2574656981

		386.851		62.1433775922		385.681		62.5309024333		389.547		86.7261912001		392.632		68.5979572318				75.2143224008

		387.214		62.1297865834		386.036		62.4815681717		389.898		86.703683883		392.97		68.5682230615				75.1752879888

		387.554		62.1139304065		386.411		62.4423748417		390.262		86.6786312765		393.326		68.5423206141				75.1318511996

		387.892		62.0980742296		386.767		62.395233214		390.597		86.6539101219		393.685		68.5131995193				75.0890013941

		388.234		62.0795753565		387.127		62.3502842202		390.962		86.6312146344		394.019		68.4825457354				75.0496734904

		388.572		62.0557910911		387.5		62.2995795625		391.315		86.606310505		394.367		68.4535779097				75.006530193

		388.922		62.0425776103		387.872		62.2496971424		391.678		86.5795348137		394.716		68.4230773947				74.9601584856

		389.279		62.0240787372		388.232		62.1943331378		392.037		86.5559721352		395.049		68.3895115013				74.9193631228

		389.629		62.0086000883		388.607		62.1395172917		392.399		86.5305375864		395.397		68.3588577174				74.8753393499

		389.992		61.9897236872		388.989		62.0879903963		392.742		86.5049259206		395.744		68.3275908578				74.8310220853

		390.344		61.9716023422		389.349		62.0389302139		393.062		86.4799854231		396.083		68.296783805				74.7878787879

		390.687		61.9493281889		389.718		61.995077537		393.4		86.4546982569		396.416		68.2667430968				74.7441485069

		391.029		61.9315843719		390.08		61.9457432755		393.73		86.4265172646		396.766		68.2388481534				74.6954288649

		391.366		61.9089326905		390.43		61.8999720439		394.081		86.3991763167		397.097		68.2115662857				74.6481766821

		391.697		61.8896787614		390.779		61.8484451485		394.432		86.3711471106		397.432		68.1830582667				74.599750532

		392.044		61.8692922482		391.142		61.7993849662		394.818		86.344978309		397.768		68.1560829369				74.5545527918

		392.391		61.8507933751		391.477		61.7440209616		395.175		86.3189715784		398.122		68.129107607				74.5096485435

		392.74		61.8262540537		391.821		61.6966052546		395.53		86.2948276001		398.468		68.100599588				74.4679727053

		393.094		61.8066225966		392.174		61.6439820423		395.895		86.2703366652		398.812		68.0713252244				74.4257098833

		393.461		61.7900113636		392.539		61.5968404146		396.239		86.2463492195		399.17		68.0455760459				74.3843275369

		393.8		61.7711349625		392.896		61.5442172023		396.581		86.2204829379		399.515		68.0153820688				74.3397167804

		394.153		61.7522585614		393.283		61.4976237331		396.915		86.1940981439		399.841		67.9858011673				74.2942255485

		394.497		61.7330046323		393.655		61.4452746		397.263		86.1683864789		400.156		67.9557604591				74.2499082838

		394.851		61.7148832872		394.026		61.3992292892		397.595		86.1409636009		400.505		67.9264860954				74.202656101

		395.198		61.6910990218		394.383		61.3493468692		397.942		86.1133615801		400.827		67.8953725048				74.1551104263

		395.549		61.6737327328		394.749		61.3076868261		398.269		86.0869439546		401.179		67.8697765952				74.1096191944

		395.897		61.6529686916		395.091		61.2586266438		398.634		86.0603477047		401.523		67.8424947275				74.0638344706

		396.248		61.6363574586		395.459		61.2131294915		398.985		86.0310141041		401.892		67.8218034234				74.0133538778

		396.619		61.6167260015		395.82		61.1635211507		399.338		86.0057655559		402.247		67.7983532787				73.9699170886

		396.968		61.6001147685		396.189		61.1177499191		399.667		85.981533628		402.62		67.7755162097				73.9282412503

		397.31		61.5823709515		396.553		61.0673193407		400.029		85.9537096836		402.961		67.7519127961				73.8804020838

		397.658		61.5634945504		396.931		61.0196295545		400.362		85.9277553107		403.31		67.7283093825				73.8357913273

		398.02		61.5453732053		397.301		60.9697471345		400.699		85.9043555055		403.662		67.7011807838				73.7955829481

		398.353		61.5280069163		397.672		60.9163016845		401.035		85.8783862166		404.004		67.6755848742				73.7509721917

		398.707		61.5102630993		398.03		60.8688859776		401.397		85.8505288424		404.337		67.64922262				73.7031330252

		399.086		61.4872338899		398.392		60.8214702706		401.728		85.8260821051		404.694		67.6213276767				73.6611636951

		399.445		61.4676024328		398.745		60.7759731183		402.083		85.7988918902		405.068		67.5954252293				73.6144984959

		399.791		61.4494810877		399.098		60.726912936		402.42		85.7749436847		405.425		67.5681433616				73.5734096412

		400.145		61.4340024388		399.445		60.684156576		402.75		85.7523578225		405.769		67.5431605277				73.5346687211

		400.504		61.4162586218		399.808		60.629614809		403.087		85.7304506977		406.127		67.5189440385				73.4971017683

		400.848		61.4045552531		400.17		60.5811027852		403.434		85.7078531105		406.459		67.4938079357				73.4583608482

		401.212		61.3890766042		400.547		60.5249165429		403.779		85.6861058674		406.801		67.470204522				73.4210873872

		401.557		61.3743530114		400.916		60.4747600436		404.13		85.6607556574		407.139		67.4456814949				73.377650598

		401.896		61.3524563861		401.285		60.4196701182		404.496		85.6333415831		407.489		67.4223846192				73.330691907

		402.246		61.3362226811		401.657		60.3821212636		404.837		85.6067758271		407.818		67.3934167934				73.285200675

		402.58		61.316591224		402.039		60.3300462098		405.193		85.5786585643		408.167		67.3696601108				73.2370680167

		402.907		61.3014901031		402.396		60.2892084044		405.522		85.5536195676		408.494		67.3436043945				73.1942182112

		403.26		61.2792159498		402.759		60.240148222		405.856		85.5284016651		408.844		67.3193879052				73.1510749138

		403.625		61.264869885		403.124		60.1965696243		406.186		85.5030046984		409.199		67.2940985335				73.1076381246

		403.961		61.2459934839		403.474		60.1335314013		406.528		85.47725683		409.559		67.2720278091				73.0636143517

		404.327		61.2278721388		403.817		60.0847452982		406.841		85.4544205643		409.899		67.2476580509				73.0245799398

		404.684		61.2082406817		404.175		60.0247219466		407.192		85.4307193396		410.247		67.224667713				72.9840780688

		405.029		61.1950272009		404.53		59.976484002		407.525		85.4068397179		410.581		67.2024437197				72.943282706

		405.38		61.1837013602		404.882		59.9224903935		407.848		85.3832971528		410.897		67.1766945412				72.9030743268

		405.718		61.1670901273		405.237		59.8728820527		408.179		85.359232349		411.24		67.1532443965				72.8619854722

		406.058		61.1565193426		405.608		59.8177921273		408.534		85.3343009337		411.604		67.1310204032				72.8194291584

		406.404		61.1440609179		405.973		59.7690060243		408.865		85.3079860916		411.955		67.1081833342				72.7745249101

		406.751		61.1248069888		406.344		59.7128197819		409.196		85.283383833		412.315		67.0853462651				72.73255558

		407.101		61.1059305877		406.734		59.661841045		409.548		85.2599792943		412.664		67.0629690029				72.6926406926

		407.478		61.0927171069		407.118		59.6157957342		409.88		85.2386342612		413.01		67.0424309677				72.6562477071

		407.828		61.0685553135		407.485		59.5648169973		410.215		85.2174560835		413.332		67.0188275541				72.6201482134

		408.191		61.0451485762		407.849		59.5245273504		410.537		85.1964448856		413.676		66.9953774094				72.5843422115

		408.544		61.024762063		408.212		59.4798524357		410.889		85.1731887485		414.006		66.9685553485				72.5447208159

		408.895		61.0058856619		408.564		59.4376442342		411.211		85.1494092433		414.358		66.9486303889				72.5042189449

		409.222		60.9828564525		408.907		59.3896803688		411.546		85.1249335428		414.699		66.9239540929				72.4625431066

		409.574		60.9692654437		409.251		59.3515833557		411.871		85.1014854272		415.066		66.9034160577				72.4226282192

		409.911		60.9534092668		409.617		59.2967675096		412.215		85.0776858807		415.41		66.8844107117				72.3821263482

		410.269		60.9405733141		409.983		59.254559308		412.552		85.0530170059		415.769		66.86479229				72.3401570181

		410.609		60.921696913		410.341		59.1983730657		412.902		85.0297216405		416.132		66.8433346412				72.3005356226

		410.976		60.9077283761		410.712		59.1482165664		413.246		85.0069377771		416.478		66.8214171857				72.2617947025

		411.32		60.8911171432		411.094		59.0909340072		413.597		84.9824210435		416.825		66.79812031				72.2201188642

		411.662		60.87073063		411.447		59.0446146172		413.933		84.9613517208		417.172		66.7728309383				72.1843128623

		411.993		60.8567620932		411.8		58.9854135033		414.246		84.9433868604		417.5		66.7501471382				72.1537897131

		412.332		60.8416609723		412.152		58.943479381		414.571		84.9254181997		417.823		66.7250110354				72.1232665639

		412.678		60.8242946833		412.514		58.8892116933		414.895		84.9065815798		418.153		66.7040131934				72.0912759557

		413.022		60.8073059223		412.871		58.8439886202		415.205		84.8887779971		418.493		66.6854676541				72.0610462983

		413.372		60.7929598574		413.234		58.7897209325		415.524		84.8702790579		418.85		66.6641632743				72.0296426737

		413.733		60.7691755921		413.593		58.7497053648		415.872		84.8507384165		419.215		66.6446981215				71.9964780982

		414.083		60.7487890789		413.954		58.6970821525		416.204		84.8315392447		419.582		66.6253862377				71.9639005063

		414.424		60.7310452618		414.311		58.6510368417		416.545		84.8123357268		419.949		66.6054612781				71.9313229144

		414.78		60.7148115569		414.667		58.6082804817		416.892		84.7950315363		420.306		66.5835438226				71.9019737325

		415.125		60.699332908		415.041		58.5605906956		417.233		84.7754735504		420.639		66.565764628				71.8688091569

		415.472		60.6883845953		415.388		58.514819464		417.565		84.7569498816		420.992		66.5433873657				71.8374055323

		415.837		60.6740385305		415.752		58.464937044		417.89		84.7366903941		421.336		66.5243820197				71.8030669895

		416.182		60.66460033		416.108		58.4191658125		418.207		84.7174653762		421.695		66.5036907156				71.7704893976

		416.519		60.6464789849		416.451		58.3599646986		418.519		84.6980627369		422.043		66.4843788317				71.7376183139

		416.861		60.6294902239		416.796		58.308163724		418.845		84.6791755425		422.39		66.462921183				71.7056277056

		417.211		60.6102362948		417.175		58.2481403724		419.168		84.6588974431		422.728		66.4448354505				71.6712891628

		417.55		60.5940025898		417.531		58.1960653186		419.507		84.6413885101		423.063		66.4259833734				71.6416464891

		417.909		60.5694632684		417.889		58.1453606609		419.842		84.6243961815		423.384		66.4063649517				71.6128842909

		418.266		60.5577598997		418.262		58.0982190332		420.193		84.6098286123		423.732		66.3846007651				71.5882309781

		418.622		60.5430363069		418.626		58.0524478016		420.531		84.5957789377		424.087		66.365748688				71.5644581407

		418.967		60.5309554102		418.976		58.0096914416		420.854		84.5822474157		424.427		66.3481227623				71.5415657789

		419.304		60.5184969854		419.346		57.9573423085		421.191		84.5690607732		424.786		66.33141645				71.5192604006

		419.643		60.5079262008		419.714		57.9129414731		421.513		84.555698525		425.161		66.3131774486				71.4966615306

		419.982		60.4905599118		420.073		57.8575774685		421.821		84.5392097241		425.496		66.2943253715				71.4687798078

		420.341		60.4822542953		420.439		57.8098876823		422.143		84.5218496165		425.844		66.2777723282				71.4394306259

		420.692		60.4697958706		420.814		57.7553459154		422.49		84.5057015158		426.198		66.2555483349				71.4121358867

		421.044		60.4539396937		421.169		57.7131377139		422.82		84.4885082107		426.542		66.2340906862				71.3830801966

		421.382		60.4448790211		421.536		57.6555810754		423.17		84.4706165121		426.883		66.2146255334				71.3528505393

		421.732		60.4294003722		421.893		57.61474327		423.541		84.4521997384		427.227		66.1973061455				71.3217404065

		422.071		60.4112790272		422.242		57.5604755823		423.879		84.4358645218		427.566		66.1787606062				71.2941521755

		422.422		60.3954228503		422.583		57.5086746077		424.223		84.4230026598		427.918		66.1646598656				71.2724337809

		422.76		60.3795666733		422.933		57.4555032369		424.546		84.4070095037		428.265		66.1451947128				71.2454325336

		423.103		60.3580475761		423.269		57.4039763415		424.866		84.3929260639		428.611		66.1300210898				71.2216596962

		423.448		60.3455891514		423.627		57.3483382576		425.179		84.3786663601		428.969		66.1114755505				71.1975933671

		423.795		60.3278453343		423.992		57.3011966299		425.504		84.3659697178		429.323		66.0947692383				71.1761684643

		424.12		60.3123666854		424.348		57.2529586853		425.83		84.3487479304		429.654		66.0753040855				71.1471127742

		424.477		60.2991532046		424.715		57.2085578499		426.173		84.3355247781		430.006		66.0607435382				71.124807396

		424.825		60.2870723079		425.081		57.1633347768		426.523		84.3214293989		430.354		66.04204473				71.1010345587

		425.152		60.270083547		425.437		57.1120819607		426.859		84.3101165878		430.702		66.0234991907				71.0819575904

		425.473		60.2553599541		425.788		57.0635699368		427.202		84.2958428757		431.035		66.0051069204				71.0578912613

		425.815		60.2447891695		426.161		57.0112208037		427.543		84.2841784141		431.385		65.9876342636				71.0382273094

		426.15		60.2304431046		426.514		56.9564049575		427.886		84.2700744464		431.734		65.9693952622				71.0144544721

		426.5		60.2160970398		426.872		56.899944636		428.227		84.2557939509		432.068		65.9536085634				70.9903881429

		426.861		60.201750975		427.238		56.8560919591		428.578		84.2408142449		432.403		65.9367489823				70.9651478465

		427.219		60.1889150222		427.587		56.7974390037		428.905		84.2260061038		432.761		65.9191230566				70.9402010419

		427.565		60.1764565975		427.941		56.750297376		429.229		84.2127636785		433.11		65.9022634754				70.9178956637

		427.915		60.1643757008		428.293		56.6971260052		429.559		84.2002163018		433.436		65.884024474				70.8967642527

		428.241		60.1538049162		428.648		56.6527251698		429.887		84.1873184382		433.787		65.8697704645				70.8750458581

		428.569		60.1409689634		429.009		56.5965389275		430.212		84.1744185982		434.132		65.8536772279				70.8533274635

		428.899		60.1319082909		429.381		56.5546048052		430.569		84.1616911431		434.471		65.8371241846				70.8319025607

		429.244		60.11680717		429.733		56.4975963251		430.889		84.1493105388		434.815		65.8198047967				70.8110646416

		429.577		60.1047262733		430.096		56.4504546974		431.215		84.1386722266		435.175		65.8035582912				70.7931616406

		429.916		60.0900026804		430.466		56.4016685944		431.558		84.1276837052		435.529		65.7856258277				70.774671656

		430.268		60.0771667277		430.813		56.3567196005		431.897		84.1177404727		435.879		65.76968586				70.7579426223

		430.623		60.0556476304		431.164		56.3032741505		432.227		84.1069236922		436.22		65.7520599343				70.7397461296

		430.957		60.0409240376		431.529		56.2624363451		432.577		84.0929645		436.548		65.7370395802				70.7162667841

		431.307		60.0209150524		431.871		56.2092649743		432.917		84.0786539229		436.883		65.7217126882				70.6922004549

		431.669		60.0095892118		432.188		56.1604788712		433.255		84.0664356492		437.209		65.7019409976				70.6716560276

		432.009		59.995998203		432.537		56.1147076397		433.585		84.0536918433		437.564		65.6826291137				70.6502311248

		432.345		59.9933555068		432.872		56.0634548235		433.937		84.0405968794		437.918		65.6677620285				70.6282192384

		432.689		59.9808970821		433.226		56.017683592		434.285		84.0268013105		438.266		65.6551939771				70.6050333847

		433.021		59.9733465216		433.599		55.973830915		434.648		84.0131781465		438.605		65.6386409338				70.5821410228

		433.355		59.9578678727		433.975		55.9261411289		434.989		83.998155174		438.954		65.6257663446				70.5569007264

		433.688		59.944276864		434.33		55.8721475204		435.339		83.9827800483		439.283		65.6130450243				70.5310734463

		434.043		59.9250229348		434.692		55.8299393189		435.677		83.9696740258		439.624		65.5980246702				70.5090615599

		434.384		59.9155847343		435.041		55.7792346612		436.019		83.9581390336		439.965		65.5814716269				70.4896910999

		434.732		59.8989735013		435.385		55.7397672519		436.343		83.9464276476		440.311		65.5662980038				70.470027148

		435.073		59.8846274365		435.732		55.6918033865		436.671		83.9357636214		440.647		65.5486720781				70.452124147

		435.419		59.8717914837		436.086		55.649595185		437.001		83.9261473541		440.963		65.533498455				70.435982097

		435.745		59.8619757552		436.446		55.6046461911		437.343		83.9144315032		441.295		65.5180182942				70.4163181451

		436.083		59.8468746343		436.803		55.5618898311		437.67		83.9018395115		441.638		65.5003923684				70.3951867342

		436.406		59.8370589057		437.145		55.5076221434		438.007		83.8887208436		441.992		65.4847589386				70.3731748478

		436.74		59.8302634013		437.496		55.4676065757		438.356		83.8756001238		442.336		65.4694320467				70.3511629613

		437.07		59.8196926167		437.852		55.4221094234		438.695		83.8616024267		442.713		65.4548714993				70.3276836158

		437.412		59.8057240799		438.198		55.3752418749		439.011		83.8476023929		443.065		65.4407707587				70.3042042703

		437.746		59.7966634073		438.562		55.3275520888		439.343		83.8339501088		443.407		65.42498406				70.2813119084

		438.09		59.7834499266		438.909		55.2806845403		439.692		83.8216961658		443.751		65.4101169748				70.2607674811

		438.43		59.77325667		439.22		55.2379281803		440.023		83.8082147591		444.094		65.3949433518				70.238168611

		438.765		59.7623083573		439.552		55.1910606318		440.366		83.7947311834		444.438		65.3802295355				70.215569741

		439.089		59.7543802689		439.905		55.1411782118		440.726		83.7840478492		444.769		65.3649026436				70.19766674

		439.412		59.739279148		440.222		55.1080146249		441.091		83.7707355595		445.117		65.3517215165				70.1753613618

		439.733		59.7275757793		440.565		55.0696435326		441.435		83.7577715601		445.445		65.3340955908				70.1536429672

		440.061		59.7128521865		440.908		55.0230500633		441.8		83.7451560129		445.792		65.3192285056				70.1325115562

		440.389		59.6966184815		441.255		54.9797455448		442.158		83.7318375399		446.135		65.3028287312				70.110206178

		440.723		59.6796297205		441.618		54.9323298379		442.509		83.7174652321		446.478		65.2842831919				70.0861398489

		441.061		59.6690589359		442.014		54.8810770217		442.857		83.7044929823		446.823		65.2689563				70.0644214543

		441.421		59.6588656793		442.346		54.842157771		443.196		83.6890639057		447.183		65.2559284418				70.0385941742

		441.769		59.6498050068		442.696		54.8015940448		443.537		83.6718781766		447.525		65.2445865418				70.0098319759

		442.113		59.6335713018		443.078		54.7624007148		443.885		83.6560922541		447.867		65.2294129187				69.9834177122

		442.454		59.6256432134		443.387		54.7262222563		444.209		83.6411805916		448.236		65.2173046741				69.9584709076

		442.804		59.6094095084		443.744		54.6851103717		444.549		83.6290738751		448.581		65.2009048997				69.9382199721

		443.131		59.5958184996		444.076		54.6426280909		444.901		83.61784289		448.912		65.1871106969				69.9194364957

		443.448		59.5754319864		444.424		54.602338444		445.239		83.6078390236		449.252		65.1700978469				69.902707462

		443.783		59.5705241222		444.769		54.5579376086		445.573		83.5955519359		449.592		65.1563036441				69.8821630347

		444.113		59.5554230013		445.087		54.5214850709		445.93		83.5827363347		449.916		65.1405169454				69.8607381319

		444.451		59.5414544645		445.494		54.469410017		446.277		83.568162784		450.258		65.1253433224				69.836378311

		444.797		59.5271083996		445.855		54.4272018155		446.632		83.5534110603		450.605		65.1086370102				69.8117249982

		445.149		59.517292671		446.178		54.3904751986		447.002		83.5393593779		450.952		65.0913176222				69.7882456527

		445.495		59.5040791903		446.54		54.3452521255		447.35		83.5256567114		451.295		65.0747645789				69.7653532908

		445.833		59.4938859337		446.891		54.2989327355		447.708		83.5119517967		451.629		65.0588246113				69.7424609289

		446.162		59.4855803172		447.275		54.2586430885		448.06		83.5003535734		451.98		65.0454902153				69.7230904689

		446.493		59.4772747007		447.57		54.2216423924		448.412		83.4854140939		452.32		65.0295502477				69.6981436642

		446.809		59.4625511079		447.927		54.1829972208		448.728		83.4717025718		452.66		65.0151429692				69.6752513024

		447.149		59.4508477392		448.265		54.1454483662		449.08		83.4574612992		453.024		65.0001226151				69.651478465

		447.488		59.4380117864		448.634		54.102417927		449.429		83.4418106786		453.395		64.9840293786				69.6253576932

		447.84		59.430083698		448.952		54.0665135477		449.783		83.4245740144		453.733		64.9670165285				69.5965954949

		448.175		59.4168702172		449.276		54.0303350893		450.134		83.4108524912		454.084		64.9523027122				69.573703133

		448.531		59.4112072969		449.596		53.9881268877		450.508		83.39413733		454.417		64.9372823581				69.5458214102

		448.851		59.3953511199		449.97		53.9338592		450.867		83.3782988232		454.746		64.9224152729				69.5194071465

		449.199		59.3874230315		450.32		53.8979548208		451.214		83.3601688393		455.085		64.9072416499				69.4891774892

		449.516		59.3730769666		450.695		53.8513613515		451.568		83.3439717327		455.445		64.8922212958				69.4621762418

		449.832		59.3636387661		451.04		53.8149088138		451.913		83.3270670474		455.792		64.8793467066				69.4340010272

		450.179		59.3462724771		451.363		53.7751673254		452.27		83.3115680726		456.156		64.865092697				69.4081737472

		450.531		59.3398545007		451.714		53.7389888669		452.63		83.2948329876		456.491		64.8503788808				69.3802920244

		450.854		59.3255084359		452.086		53.7025363292		453.001		83.27985664		456.835		64.8373510226				69.3553452198

		451.206		59.3153151793		452.387		53.665535633		453.344		83.2610002313		457.168		64.8226372063				69.3239415951

		451.563		59.3039893386		452.715		53.6288090161		453.713		83.2416106854		457.511		64.8054710874				69.291657495

		451.892		59.293796082		453.045		53.5885193692		454.075		83.22292194		457.862		64.788918044				69.2605473622

		452.223		59.2820927133		453.389		53.5435703753		454.438		83.2044053649		458.205		64.7751238413				69.2297307213

		452.569		59.2730320408		453.762		53.4931397969		454.798		83.1846498084		458.552		64.758570798				69.1968596375

		452.921		59.2613286721		454.097		53.4536723876		455.176		83.1647131072		458.901		64.7446233263				69.163695062

		453.265		59.2515129435		454.399		53.4227014345		455.536		83.143712652		459.247		64.7277637452				69.1287695355

		453.608		59.2454724952		454.742		53.3761079653		455.877		83.1227068911		459.582		64.7136630046				69.0938440091

		453.966		59.2401871029		455.084		53.3445888537		456.227		83.1020489918		459.944		64.6964968856				69.0595054663

		454.303		59.2299938463		455.433		53.2993657807		456.567		83.0859781857		460.281		64.6817830693				69.0327977108

		454.64		59.2216882298		455.791		53.265379956		456.912		83.0707875335		460.622		64.6643104125				69.0075574143

		454.989		59.2126275573		456.147		53.2174160906		457.277		83.0555941029		460.959		64.6502096719				68.9823171179

		455.335		59.1990365485		456.505		53.1858969791		457.644		83.0386307108		461.309		64.6359556624				68.9541419033

		455.657		59.1831803716		456.841		53.1412220645		458.005		83.0198962722		461.644		64.6197091569				68.9230317705

		456.017		59.1722320589		457.187		53.1069621606		458.377		82.9974447254		461.967		64.6053018785				68.8857583095

		456.344		59.1590185782		457.549		53.0584501368		458.742		82.9760482304		462.309		64.5898217176				68.8502457994

		456.672		59.1476927375		457.859		53.0236420745		459.077		82.9553538095		462.671		64.5760275148				68.8159072566

		457.015		59.1367444249		458.232		52.962522406		459.421		82.9344772829		463.011		64.5580950513				68.781275222

		457.377		59.1310815045		458.545		52.9279884229		459.761		82.9143034431		463.361		64.5438410417				68.7478171546

		457.719		59.1190006078		458.918		52.8676909921		460.092		82.8950098295		463.726		64.5266749228				68.7158265463

		458.066		59.1069197111		459.266		52.8304162167		460.424		82.8746493128		464.067		64.5093555348				68.6820749872

		458.427		59.0925736463		459.6		52.7840968267		460.762		82.8548151307		464.391		64.4915763402				68.6492039034

		458.758		59.0793601655		459.924		52.7479183682		461.087		82.8356848146		464.731		64.4750232969				68.617506787

		459.086		59.0650141007		460.235		52.7010508198		461.422		82.8179676188		465.069		64.4607692874				68.5881576051

		459.423		59.0555759001		460.578		52.6602130144		461.754		82.800246632		465.399		64.4439097062				68.5588084232

		459.772		59.0468927556		460.912		52.6215678428		462.1		82.7842945005		465.746		64.4301155035				68.5323941595

		460.11		59.0431174754		461.282		52.573055819		462.449		82.7672755048		466.087		64.4123363088				68.5042189449

		460.473		59.036321971		461.605		52.536329202		462.793		82.7481249506		466.421		64.3963963412				68.4725218285

		460.82		59.0261287144		461.937		52.4932987628		463.127		82.7293247257		466.765		64.3758583059				68.4414116956

		461.162		59.0159354578		462.27		52.4521868782		463.461		82.711939584		467.127		64.3593052626				68.4126494974

		461.503		59.002721977		462.603		52.4097045974		463.792		82.6897593539		467.465		64.341526068				68.37596302

		461.842		58.9921511924		462.939		52.3661259997		464.108		82.6721883888		467.814		64.3248197558				68.34690733

		462.178		58.9800702957		463.271		52.3173398966		464.448		82.6590520968		468.155		64.3073470989				68.3251889354

		462.519		58.967989399		463.628		52.2666352389		464.778		82.6443156632		468.471		64.290027711				68.3008291144

		462.852		58.9536433342		463.923		52.2200417697		465.095		82.6285110253		468.795		64.2733213988				68.2747083425

		463.163		58.9449601897		464.28		52.165774082		465.401		82.6189202207		469.13		64.2549291285				68.2588597843

		463.499		58.9257062605		464.631		52.1276770689		465.721		82.607196614		469.467		64.2408283879				68.2394893242

		463.824		58.9102276116		464.973		52.0750538566		466.038		82.5929839506		469.822		64.2241220756				68.2160099787

		464.168		58.9019219952		465.33		52.0372309227		466.359		82.5821451512		470.193		64.2084886458				68.1981069778

		464.506		58.8958815468		465.675		51.9791261258		466.705		82.5723712435		470.538		64.191015989				68.1819649277

		464.876		58.8856882902		466.002		51.9328067358		467.055		82.5609965125		470.89		64.1744629457				68.1631814513

		465.224		58.8785152578		466.371		51.8651091658		467.39		82.5506868087		471.238		64.1560706754				68.1461589258

		465.573		58.8739849215		466.665		51.8229009642		467.725		82.5432203572		471.572		64.1366055226				68.1338322694

		465.911		58.865679305		467.013		51.7587664242		468.07		82.5332640379		471.905		64.1202057482				68.1173967276

		466.256		58.8558635765		467.307		51.7160100642		468.388		82.5261516459		472.244		64.1010471333				68.1056570548

		466.589		58.8494456001		467.622		51.6587275049		468.693		82.5153040677		472.589		64.084340821				68.0877540539

		466.92		58.8396298715		467.949		51.6061042926		469.013		82.5074786997		472.92		64.0656420129				68.0748404138

		467.244		58.830191671		468.328		51.5493698918		469.316		82.4957392559		473.275		64.0490889695				68.0554699538

		467.588		58.8192433583		468.675		51.4978429965		469.619		82.4902246981		473.624		64.0328424641				68.0463717074

		467.911		58.8090501017		469.012		51.4394641203		469.94		82.475458099		473.977		64.0175155721				68.0220118864

		468.261		58.7981017891		469.352		51.3989003941		470.269		82.4695863069		474.322		64.002495218				68.0123266564

		468.605		58.7826231402		469.696		51.3399733595		470.601		82.4592651743		474.681		63.985329099				67.9953041309

		468.974		58.7709197715		470.019		51.2963947618		470.944		82.4548160118		475.01		63.96816298				67.9879668354

		469.313		58.7588388748		470.346		51.2374677272		471.281		82.4476968524		475.34		63.949157634				67.9762271627

		469.675		58.7433602259		470.674		51.1903260995		471.599		82.4469849027		475.701		63.9335242042				67.9750531954

		470.008		58.7342995534		470.988		51.1311249856		471.929		82.4428910723		476.033		63.9143655893				67.9683028836

		470.331		58.7252388809		471.302		51.082887041		472.259		82.4366609403		476.358		63.8970462014				67.9580306699

		470.635		58.7191984325		471.615		51.0264267194		472.575		82.4306083612		476.719		63.8778875864				67.9480519481

		470.964		58.7082501199		471.929		50.978462854		472.888		82.4231310323		477.073		63.859648585				67.9357252917

		471.29		58.7003220314		472.254		50.9269359586		473.216		82.4168994066		477.412		63.8415628525				67.925453078

		471.625		58.6886186627		472.599		50.8781498556		473.544		82.4099550401		477.763		63.8217911619				67.9140068971

		471.981		58.6863534946		472.916		50.8364898125		473.862		82.4063935995		478.122		63.8040119672				67.9081370607

		472.352		58.676915294		473.249		50.7871555509		474.19		82.3967769409		478.427		63.7868458483				67.8922885025

		472.712		58.6720074298		473.572		50.7501548548		474.53		82.3908995414		478.759		63.7709058806				67.8826032724

		473.071		58.6674770935		473.883		50.7068503363		474.857		82.3834186084		479.074		63.7503678454				67.870276616

		473.418		58.6633242852		474.177		50.6745089871		475.181		82.3762932786		479.402		63.7333549953				67.8585369433

		473.761		58.6527535006		474.501		50.6336711817		475.492		82.3686328617		479.731		63.7151159939				67.8459167951

		474.088		58.6455804682		474.822		50.5969445647		475.82		82.3645351369		480.091		63.6968769925				67.8391664832

		474.409		58.6338770995		475.142		50.5519955709		476.131		82.3579427171		480.436		63.6783314532				67.8283072859

		474.724		58.6206636188		475.469		50.5160911916		476.452		82.3518843525		480.795		63.6593261072				67.8183285641

		475.056		58.6063175539		475.807		50.4673050886		476.796		82.3454691277		481.157		63.6383282652				67.8077628586

		475.385		58.5957467693		476.117		50.4289339962		477.134		82.337984067		481.512		63.6179434989				67.7954362022

		475.731		58.5780029523		476.421		50.3941259339		477.482		82.3328154137		481.853		63.5981718083				67.7869249395

		476.089		58.5636568874		476.724		50.3595919508		477.817		82.3265769517		482.187		63.5773272353				67.7766527258

		476.441		58.5545962149		477.016		50.3294432355		478.152		82.3217641008		482.518		63.5572490068				67.7687284467

		476.786		58.5470456545		477.305		50.3061465008		478.463		82.3158813454		482.838		63.5414623081				67.7590432167

		477.138		58.5364748698		477.629		50.2729829139		478.805		82.3137420574		483.162		63.5253690716				67.7555213148

		477.475		58.5372299259		477.963		50.2403674854		479.113		82.3062541114		483.507		63.5072833391				67.7431946584

		477.791		58.5357198138		478.29		50.2074779777		479.441		82.3012617689		483.848		63.4878181863				67.7349768875

		478.125		58.5323220616		478.624		50.1693809646		479.771		82.2937726873		484.186		63.4688128403				67.7226502311

		478.469		58.5202411649		478.964		50.1312839516		480.109		82.2873529321		484.542		63.4479682672				67.7120845256

		478.785		58.5100479083		479.282		50.1036019493		480.427		82.2791491825		484.888		63.4304956104				67.698583902

		479.116		58.4930591473		479.575		50.0750977092		480.754		82.276117155		485.238		63.4105706508				67.6935945411

		479.48		58.4809782506		479.891		50.04988242		481.092		82.2677339092		485.593		63.3929447251				67.6798004256

		479.818		58.4658771297		480.202		50.0304227946		481.431		82.2597065967		485.929		63.3751655304				67.6665932937

		480.152		58.4583265693		480.522		50.0057556638		481.758		82.2541762145		486.259		63.3564667223				67.6574950473

		480.51		58.4511535369		480.836		49.97862182		482.095		82.2475749491		486.592		63.33408946				67.64663585

		480.853		58.4447355605		481.173		49.9473767877		482.421		82.2411515876		486.91		63.3172298789				67.6360701445

		481.197		58.4402052242		481.499		49.9199688646		482.741		82.2365121812		487.236		63.2951591544				67.6284393573

		481.556		58.4352973599		481.816		49.8865311984		483.067		82.2324078727		487.584		63.2756940017				67.6216890454

		481.905		58.4228389352		482.13		49.8615899884		483.388		82.22758951		487.937		63.2574550002				67.6137647663

		482.258		58.419818711		482.463		49.8311671938		483.71		82.2222354426		488.279		63.2366104272				67.6049600117

		482.607		58.4122681506		482.761		49.8078704592		484.064		82.2156316125		488.632		63.2159191231				67.5941008144

		482.943		58.4028299501		483.083		49.7823810907		484.42		82.2109907659		488.979		63.1973735838				67.5864700271

		483.254		58.3964119737		483.414		49.7610029107		484.754		82.2072421986		489.318		63.177908431				67.580306699

		483.58		58.3922591654		483.736		49.7377061761		485.103		82.1990304537		489.651		63.1582900093				67.5668060753

		483.896		58.3790456847		484.042		49.717424313		485.443		82.1942101344		490.004		63.1386715876				67.5588817962

		484.237		58.3745153484		484.385		49.6976906084		485.771		82.1859970874		490.337		63.1192064348				67.5453811725

		484.574		58.3613018676		484.699		49.6752161115		486.089		82.1777832196		490.683		63.0988216685				67.5318805488

		484.957		58.3526187231		485.03		49.6598676745		486.422		82.1670682449		491.034		63.0824218942				67.5142710397

		485.319		58.3443131066		485.359		49.6395858115		486.753		82.1626032598		491.366		63.0628034725				67.5069337442

		485.665		58.3382726583		485.692		49.6261559292		487.081		82.154387053		491.687		63.0460971602				67.4934331206

		485.996		58.3250591775		486.022		49.6055999868		487.394		82.1492068482		492.026		63.0281646967				67.4849218578

		486.335		58.3171310891		486.346		49.5907997084		487.727		82.1438476718		492.361		63.0129910736				67.4761171032

		486.66		58.3001423281		486.668		49.5625695476		488.073		82.1370588797		492.682		62.993219383				67.4649644141

		486.985		58.2929692956		486.995		49.5431099222		488.404		82.1299121766		493.018		62.9745205748				67.4532247414

		487.328		58.2827760391		487.328		49.5154279199		488.737		82.1236583012		493.349		62.9553619599				67.4429525277

		487.682		58.2733378385		487.647		49.4970646114		489.095		82.116153022		493.694		62.9352837314				67.4306258713

		488.025		58.2605018858		487.984		49.4792494614		489.425		82.1098980986		494.028		62.9156653097				67.4203536576

		488.366		58.2586142456		488.323		49.468012213		489.729		82.1063236427		494.388		62.8935945853				67.4144838213

		488.726		58.2450232368		488.655		49.4521156176		490.036		82.1011404053		494.731		62.8742827015				67.4059725585

		489.066		58.2355850363		488.981		49.4411524483		490.355		82.0975655681		495.086		62.8540512041				67.4001027221

		489.404		58.2348299803		489.299		49.4263521699		490.664		82.0943480816		495.424		62.8365785473				67.3948198694

		489.737		58.2386052605		489.62		49.4101814953		490.983		82.0879127301		495.758		62.816193781				67.3842541639

		490.074		58.2363400923		489.944		49.3940108206		491.306		82.0841585421		496.073		62.7965753593				67.3780908357

		490.402		58.2336973962		490.269		49.3792105422		491.657		82.079152691		496.387		62.776037324				67.3698730648

		490.75		58.229922116		490.599		49.3622176299		492.004		82.0737889403		496.728		62.7554992888				67.3610683102

		491.096		58.2174636912		490.956		49.3446765591		492.343		82.0666367274		497.061		62.7337351023				67.3493286375

		491.448		58.2099131308		491.303		49.324394696		492.673		82.0662791004		497.403		62.7122774535				67.3487416538

		491.783		58.1982097621		491.632		49.3027424368		493.002		82.0596627196		497.751		62.6938851832				67.3378824565

		492.117		58.1906592017		491.966		49.2841050491		493.306		82.0537611731		498.11		62.6725808034				67.3281972265

		492.455		58.1815985292		492.301		49.2613564729		493.607		82.0462495		498.435		62.6532689195				67.3158705701

		492.802		58.1732929127		492.631		49.2399782929		493.907		82.040168118		498.759		62.6339570357				67.3058918483

		493.14		58.1646097682		492.954		49.2224372222		494.217		82.0319396483		499.08		62.6158713032				67.2923912246

		493.486		58.1540389835		493.293		49.2043479929		494.552		82.0247837863		499.397		62.5967126882				67.2806515518

		493.838		58.1476210072		493.622		49.1843402091		494.888		82.0213845331		499.723		62.5795465692				67.2750752073

		494.189		58.1400704467		493.938		49.1736511191		495.221		82.0145856041		500.046		62.5626869881				67.2639225182

		494.51		58.1355401105		494.256		49.1607693952		495.565		82.0085018741		500.382		62.5435283731				67.2539437963

		494.844		58.1223266297		494.592		49.1451468791		495.905		82.0004491844		500.719		62.5257491785				67.2407366645

		495.171		58.1211940456		494.915		49.1330873929		496.274		81.9916798007		501.056		62.5055176811				67.2263555653

		495.512		58.1143985412		495.222		49.1188352729		496.583		81.9845204246		501.381		62.4863590662				67.2146158926

		495.834		58.110245733		495.55		49.103486836		496.92		81.9809405022		501.726		62.4653612242				67.2087460562

		496.18		58.1068479808		495.884		49.0906051121		497.285		81.9748542752		502.055		62.4454362647				67.1987673344

		496.525		58.1011850605		496.209		49.0766270714		497.609		81.9687675963		502.379		62.4245916916				67.1887886125

		496.9		58.0891041638		496.55		49.0601823175		497.901		81.9632175833		502.71		62.4040536564				67.1796903661

		497.232		58.0777783231		496.896		49.0437375637		498.211		81.9590995889		503.049		62.385661386				67.1729400543

		497.583		58.0702277627		497.232		49.0253742552		498.531		81.9533698612		503.361		62.3645102751				67.1635483161

		497.929		58.0668300105		497.559		49.0138629275		498.876		81.9508629794		503.69		62.3474974251				67.1594394306

		498.271		58.0619221462		497.885		49.0020775206		499.183		81.9481769494		504.031		62.3280322723				67.1550370533

		498.58		58.0600345061		498.206		48.988373559		499.481		81.9449535973		504.358		62.3119390358				67.1497542006

		498.92		58.058524394		498.547		48.9790548652		499.779		81.9379692326		504.688		62.2920140762				67.1383080197

		499.269		58.0505963055		498.891		48.9763140729		500.106		81.9300887218		505.037		62.2763806464				67.1253943796

		499.608		58.0468210253		499.22		48.9582248436		500.398		81.9222074529		505.38		62.2547697288				67.1124807396

		499.934		58.042290689		499.561		48.9450690406		500.753		81.9139671338		505.713		62.2340784246				67.0989801159

		500.29		58.0358727127		499.886		48.9365725844		501.146		81.9069801268		506.053		62.2153796165				67.087533935

		500.641		58.0286996802		500.225		48.9256094152		501.473		81.9016051005		506.379		62.193462161				67.0787291804

		500.98		58.025301928		500.568		48.9058757106		501.863		81.8958713503		506.705		62.1721577812				67.0693374422

		501.329		58.0139760874		500.918		48.8943643829		502.157		81.8915707741		507.01		62.1519262838				67.0622936386

		501.689		58.0045378868		501.246		48.8798381836		502.493		81.8847610667		507.331		62.1323078621				67.0511409494

		502.039		57.9977423824		501.59		48.8644897467		502.8		81.875979292		507.649		62.1090109863				67.0367598503

		502.388		57.9913244061		501.919		48.8557192113		503.103		81.8713191924		507.963		62.0935308254				67.029129063

		502.717		57.9867940698		502.224		48.8447560421		503.415		81.8671965754		508.288		62.0746787483				67.0223787512

		503.053		57.9807536214		502.558		48.835163269		503.721		81.8600263123		508.646		62.0573593604				67.0106390784

		503.379		57.9796210374		502.893		48.8277631298		504.071		81.8548274787		508.982		62.0388138212				67.0021278157

		503.706		57.9701828368		503.222		48.8165258813		504.461		81.8476561319		509.323		62.0248663495				66.9903881429

		504.016		57.9637648604		503.539		48.8047404744		504.815		81.8408427705		509.674		62.0035619697				66.9792354538

		504.353		57.9535716039		503.886		48.7951477013		505.152		81.829366353		510.011		61.9850164304				66.9604519774

		504.694		57.9497963236		504.206		48.7808955813		505.479		81.8230895064		510.328		61.9666241601				66.9501797637

		505.045		57.9407356511		504.542		48.7702064913		505.804		81.807843731		510.649		61.9465459316				66.9252329591

		505.384		57.9380929549		504.87		48.7669175405		506.099		81.7995918911		510.965		61.9235555937				66.9117323355

		505.738		57.9312974506		505.229		48.7551321336		506.444		81.7902627217		511.284		61.9027110206				66.8964707609

		506.072		57.9252570022		505.577		48.7381392213		506.715		81.7827268465		511.602		61.8795674138				66.8841441045

		506.403		57.9177064418		505.908		48.7340280328		507.032		81.7777025439		511.933		61.856270538				66.8759263336

		506.717		57.9131761055		506.244		48.7271760521		507.365		81.7741135673		512.269		61.8377249988				66.8700564972

		507.047		57.9127985775		506.575		48.7173091997		507.687		81.7671146099		512.618		61.8179533082				66.8586103162

		507.386		57.9094008253		506.868		48.7085386644		508.023		81.7619098685		512.963		61.7968021973				66.8500990535

		507.727		57.9097783533		507.155		48.7047015551		508.379		81.7534738944		513.306		61.7788697337				66.836304938

		508.051		57.9071356571		507.477		48.6970273367		508.715		81.7473707321		513.646		61.7609372701				66.8263262162

		508.405		57.9022277929		507.793		48.6857900882		509.036		81.7371379377		513.978		61.7407057727				66.8095971825

		508.747		57.8935446484		508.122		48.6770195528		509.36		81.7312131027								66.7999119525

		509.088		57.8939221764		508.479		48.671263889		509.699		81.7188234233								66.7796610169

		509.427		57.886749144		508.822		48.6652341459		509.989		81.7109217773								66.7667473769

		509.782		57.8810862236		509.148		48.6539968974		510.336		81.6979901625								66.745615966

		510.12		57.8765558874		509.486		48.648789392		510.688		81.6870326092								66.727712965

		510.454		57.8754233033		509.824		48.6397447774		511.057		81.6758939175								66.7095164722

		510.788		57.8663626308		510.157		48.6301520043		511.456		81.6676287452								66.6960158486

		511.128		57.8576794863		510.502		48.6265889743		511.767		81.6597221453								66.6831022085

		511.47		57.8557918461		510.846		48.6183665974		512.078		81.6500175446								66.6672536503

		511.809		57.85314915		511.164		48.6164480428		512.396		81.6475013487								66.6631447648

		512.159		57.8505064538		511.487		48.614255409		512.753		81.6370762824								66.6461222393

		512.511		57.8505064538		511.794		48.6087738243		513.06		81.6280880876								66.6314476484





Sheet1

		



1

2

3

4

5

6

Temperature (oC)

Weight %



Sheet2

		





Sheet3

		






